V Међународни научни скуп Савремени материјали 2012 –  Бања Лука, 5-7 јул 2012.

V International Scientific Conference Contemporary Materials 2012 – Banja Luka, 5-7 July 2012 

ПРИМЕНА ВИТАМИНА Це КАО ИНХИБИТОРА КОРОЗИЈЕ ЗА

ЗАШТИТУ ЧЕЛИКА И БАКРА
М.Г. Павловић1, М.В. Томић1, R. Fuchs Godec2
1Универзитет у Источном Сарајеву, Технолошки факултет Зворник, Република Српска, e-mail: pavlovicmiomir@gmail.com
2Универзитет у Марибору, Факултет за хемију и хемијско инжењерство, Словениjа

Сажетак:
У овом раду извршено је испитивање заштите челика и бакра обрадом корозионе средине у два основна раствора: 3% NaCl и 4% HCl. Као инхибитор коришћен је витамин Цe у концентрацијама 1g/dm3, 2g/dm3 i 3g/dm3.  

Витамин Цe као инхибитор корозије челика показује различита заштитна својства. У раствору HCl витамин Цe показује боље резултате него у раствору NaCl. Степен заштите креће се у интервалу 68–76%. Такође степен заштите се повећава са повећањем концентрације витамина Цe у раствору. Интересантно је да степен заштите драстично опада са временом,  јер се витамин Цe распада и тако слаби његово инхибиторско дејство. У раствору NaCl витамин Цe показује слабије инхибиторске особине према челику него у раствору HCl. Степен заштите креће се у интервалу од 27–41%. Такође, приметан је пораст степена заштите са порастом концентрације инхибитора у раствору. И у овом случају понавља се ситуација да заштитни фактор z опада са временом, али је то мање изражено што се може објаснити мањом агресивношћу раствора NaCl у односу на агресивност раствора HCl.

Витамин Цe као инхибитор корозије бакра  показује нешто боље резултате у односу на челик. Степен заштите креће се у интервалу од 40–67%. Степен заштите и у овом случају расте са порастом концетрације витамина Цe како у раствору HCl тако и у раствору NaCl. С обзиром да је витамин Цe јефтин, еколошки прихватљив  и доступан на тржишту могућност његовог коришћења у заштити важних конструкционих материјала челика и бакара је веома извесна и потребно је наставити истраживања.

Кључне речи: бакар, челик, инхибитор, корозија, показатељи корозије, заштитни фактор z.
APPLICATION OF VITAMIN C AS A CORROSION INHIBITOR FOR PROTECTION OF STEEL AND COPPER
M.G. Pavlović1, M.V. Tomić1, R. Fuchs Godec2
1University of Eastern Sarajevo, Faculty of Technology Zvornik, Republic of Srpska, e-mail: pavlovicmiomir@gmali.com
2University of Maribor ,Faculty of Chemistry and Chemical Engineering, Slovenia
Abstract:
This paper presents the corrosion protection of steel and copper in two basic solutions: 3% NaCl and 4% HCl.  Vitamin C was used as an inhibitor in concentrations of 1g/dm3, 2g/dm3 and 3g/dm3.

Vitamin C, as an inhibitor of steel corrosion, shows different protective properties. In HCl solution vitamin C showed better results than in NaCl solution. The degree of protection varies in the range of 68-76%. Also the degree of protection increases with increasing concentrations of vitamin C in solution. Interestingly, the degree of protection drastically decreases with time, because vitamin C slowly decays and, hence, its inhibition effect. In NaCl solution, vitamin C showed lower inhibition effect on steel than in HCl solution. The degree of protection varies in the range of 27-41%. Also it can be noticed the increase in the degree of protection with increasing concentration of inhibitor in solution. The same situation with decreasing of the value of protective factor z with time can be seen in this case, but it is less pronounced. This phenomenon may be explained by less aggressive NaCl solution compared to the aggressiveness of HCl solution.
Vitamin C, as copper corrosion inhibitor, shows better results compared to steel. The degree of protection varies in the range of 40-67%. The degree of protection in this case increases with increasing concentration of vitamin C both in HCl and NaCl solutions. Since vitamin C is inexpensive, environmentally friendly and it is available on the market, the possibility of its use in the protection of important structural materials of steel and copper is very certain and the need in research continuation is noticeable.
Key words: copper, steel, inhibitor, corrosion, corrosion indicators, protective factor z.
