PAGE  

MODELING OF SELF–HEALING MATERIALS AND FITTING PARAMETERS PROCEDURE
D. Petrovic1,2, M. Obradovic1,2, M. Radovic1,2 , A. Jovanovic3, S. Jovanovic3, D. Balos3 , M. Kojic2,4 and N. Filipovic1,2
1Faculty of Engineering, University of Kragujevac, Serbia
e-mail: fica@kg.ac.rs
2Research and Development Center for Bioengineering, BioIRC, Kragujevac, Serbia

e-mail: racanac@kg.ac.rs
3Risk-technologies, GmbH, Stuttgart, Germany

e-mail: jovanovic@risk-technologies.com
4Methodist Hospital Research Institute, Houston, USA

e-mail: mkojic@hsph.harvard.edu
Abstract. The surface defects of the material are difficult to detect and difficult to repair. A grand challenge in materials science is to design „smart“ synthetic system that can re-establishing the continuity and integrity of the damaged area. Recent research of the nanocontainers with process of self-healing materials promises a good avenue for new smart nanocoating interfaces. We use continuum modeling approach to investigate coating substrates that contain nanoscale defects with healing agents. Here we use Finite Element Method (FEM) with different diffusivity and fluxes.  The fiting procedure from simulations is performed to determine diffusion coefficient and diameter of nanocontainers to match experimental results. We also show the risk map from the calculations of the creepage and coverage.
Keywords: self-healing material process, finite elеment methods (FEM), nanocoating, fitting
МОДЕЛИРАЊЕ САМОВЕЗУЈУЋИХ МАТЕРИЈАЛА И ПОСТУПАК ФИТОВАЊА ПАРАМЕТАРА
Сажетак. Површинске дефекте у материјалу је тешко открити и санирати. Велики изазов у науци о материјалима је дизајн „паметних“ синтетичких система који могу да поново изграде континуитет и интегритет оштећене области. Недавна истраживања наноконтејнера са процесом самовезивања материјала обећавају нови пут за нове паметне нанопокривајуће заштите. Користимо континуално моделирање за истраживање покривања површина са самовезујућим материјалима које садрже оштећења на нивоу наноскале. Користимо метод коначних елемената са различитим дифузионим коефицијентима и флуксевима. Поступак фитoвања користећи симулације је примењена да би се одредили коефицијенти дифузије и пречник наноконтејнера у односу на експерименталне резултате. Од прорачуном добијених резултата урађена је мапа ризика која показује ризик од прогресије корозије и прекривеност слита.
Кључне речи: Самовезивни процеси у материјалу, метод коначних елемената, нанопокривање, фитовање
1. Introduction

Corrosion degradation of materials and structures is one of important issues that lead to depreciation of investment goods. Two main approaches, an active and a passive one, are currently used for corrosion protection. The passive corrosion protection is achieved by deposition of а barrier layer preventing contact of the material with the corrosive environment [1].

Small size defects can appear on a material surface. Such defects have a substantial effect on the mechanical properties of material. To protect this material failure the coating systems are employed on a wide range of engineering structures, from cars to aircrafts, from chemical factories to household equipment. The “self-healing” or “inhibition” are a relatively new terms in material science which means a self-recovery of initial properties of the material after destructive actions of external environment. It is an urgent demand for industrial applications to initiate development of an active healing mechanism for polymer coatings and adhesives [2].

In this study we presented FEM modeling approach. We begin by describing the details of the nanocontainers healing concept by FEM methodology. We then discuss the effects of fitting parameters such as diffusion coefficient and diameter of nanocontainers. These findings provide guidelines for formulating nanocomposite coatings that effectively heal the surfaces through the self-assembly inhibitors into the defects.
2. Methods

2.1 Nanocontainers healing concept

The initial process of nanocontainer breaking starts at а random position where a crack occurred. Inside the nanocontainers are healing agents – inhibitors. We consider that nanocontainers are fixed in the coating layer (pretreatment or primer layer) as can be seen in Fig. 1.
[image: image1.png]Corrosion protection investigated on artificial crack
(DIN EN ISO 11997-1; cycle B) in Mankiewicz Gebr. & Co.
industrial partner in MUST

Pretreatment

Metallic
substrate




[image: image2.jpg]Nano - containers

Primer

Pretreatment





Figure 1. Model with nanocontainers in primer layer

Nanocontainers release the “self – healing” agent particles which are filling the space inside a crack in order to bond it and to protect crack from further propagation. We modeled a process of self – healing using continuum model in which we have convective-diffusion process for inhibitors binding to the substrate surface.
2.2 FEM model
The mass transport process for inhibition system of coating is governed by convection – diffusion equation,



[image: image3.wmf]222

222

wall

xyz

ccccccc

vvvDq

txyz

xyz

æö

¶¶¶¶¶¶¶

+++=+++

ç÷

¶¶¶¶

¶¶¶

èø


(1)

where c denotes the concentration of inhibitors; 
[image: image4.wmf]x

v

,
[image: image5.wmf]y

v

 and 
[image: image6.wmf]z

v

 are the velocity components in the coordinate system x,y,z; and D is the diffusion coefficient, assumed to be constant, of the transported material; and qwall is flux of the binding process for inhibitors which adhere on the substrate surface. Similar concept is using for calculation of the volume of inhibitors which are possible to diffuse on the scratch surface. Diffusivity coefficient and wall binding flux are the fitting parameters in FEM model. The drawback of continuum approach is that particle-particle interaction cannot be modeled but benefit is that a large substrate area is possible to be modeled.
2.3 Fitting parameters
The goal is to determine diffusion coefficient and diameter of nanocontainers so that computer simulations match experiments. We used a simplex optimization method developed by John Nelder and Roger Mead [3] to reach the best fit. This is a nonlinear procedure which involves only function evaluations (no derivatives). The best fit minimizes the sum of squared residuals, a residual being the difference between an experimental value of the creepage distance and the creepage distance provided by a simulation. We have four different experimental creepages defined with 1200 points all together, thus we have 1200 residuals. The sum of squared residuals is calculated as:


[image: image7.wmf](

)

1200

2

1

ii

i

SEpt

=

=-

å


(2)
where 
[image: image8.wmf]i

p

 is the creepage distance for i-th point calculated by simulation and 
[image: image9.wmf]i

t

 is target (experimental) creepage distance for i-th point. We achieved minimum error (SE=3082) with diffusion coefficient value 0.32 [m2/s] and diameter of nanocontainers 0.092 [nm].

3. Results
3.1 FEM results
The continuum model consists of mesh size of 50,000 finite elements where inhibitors are randomly prescribed as the influx boundary conditions. The coverage of the inhibitors on the substrate surface is presented in Fig. 2. The scratch dimension is 0.1x100 mm, the primer layer is 4000 nm, nanocontainer diameter is 400 nm. The percentage of inhibitor inside nanocontainers is 20% and the percentage of nanocontainers in the primer or pre-treatment layers is 10%. The convection velocity is assumed to be zero due to dominant diffusion process. The binding flux was prescribed to be unit which depends on the mechanical property of scratch, with no water inclusion on the surface. 

[image: image11.png]Contour plot. Corrosion Concentration
Deformed (Scale factor=1)

1.72e+01

1518401

1.508+01

1.408+01

1298401

1188401

1.082+01

9676400

8608400

7528400

6458400

5388400

4308400

3228400

2158+00

1.082+00

0.008+00




Figure 2. Coverage of the inhibitiors on the substrate surface. The width of the scratch is 0.1mm and the length is 100mm.
Distribution of inhibitors on the scratch surface for time = 6h is presented in Fig. 2. The inhibitors fluxes are randomly distributed along the plate, which cause higher coverage near these plate sides. 
3.2 Fitting results
We developed online application where user can change input parameters and get different creepage results. The interface of that software application is shown in Fig. 3.
[image: image12.png] FeNtohibition

| Reslts | toadimese |
et tart & end ot |
sitwth (mm): (0,10 __Clsrssecion |

Percent of nano-container

Percent of fi

Time (h): | 2000

Number of time steps: |500

Diffusion coefficient: |0.001

Diameter of nanocontainer (nm): |40

Calculation comment:

| start calculation |

‘Simulation results: EXPORT Curve Data

— - it

Show histogram — - simulation results

You need to load image in order to continue!





Figure 3. Online application interface.
Results from the fitting parameters calculations are shown in Figure 4. It can be observed that the experimental results (blue color) and results obtained by simulations (red color) are very similar. The reason of error deviation is large error occurs at the points where experiment has very large creepage distance (for example, third experiment at height around 15 mm creepage distance is around 10 mm), but from the histogram we can see that most of the points for both, computer simulation and experiment, have creepage distance around 2 mm.
[image: image13.jpg]100

0

60

0

Eil

Siit 1

sit2 Sit3 Sit4
10 10 10
a0 & CY
&0 &0 &0
0 0 0
2 2 2
0 0 0
40 0w a0 0 a0 0 1 @ 0 10
HISTOGRAM
08
T oot
5 Simulation
£ 04
S 02

5 10
Distance [mrm]





Figure 4. Comparison of the experimental and computer simulation results
The results for risk – map calculations are shown in Fig. 5. and Fig. 6.
[image: image14.png]Home. Page Layout

Fomuias  Data R

Developer

Adddns  LoadTest

F :;“‘W GolioriBosy) -[10 - [A° x| [Fl=1=] Siwiap Text al Bad Good eutra = 5 j:‘““’“ or &
R ot |82 0[5 ) P e coner [ o[ ] onatons rorne [T iput e i D Fom | . ELE RS
Ciipboard 5 Font 5 Aiignment Number styes celis Egiting
Chart 3 - £| v
B C D E F G H 1 J K L M N o P Q R S T u v w X Y z AA AB AC AD 4
Total %
400 39 380 325 320 300 28 260 25 240 210 200 _ 195 _ 19 175 _ 160 _ 150 _ 140 _ 130 _ 120 _ 105 _ 100 080 070 060
0.30 0.32 0.32 0.33
045 045 045 047
Average creepage after 300h [mm] 054 054 055 055
052 082 062 08
T 067 067 067 067
= 071 om0 onm
5 07 07 076 07
k] o 0w 07 om
5 082 082 081 082
£ 085 084 08 o084
2 | 087 o8 o087 o087
£
e H
1 2 300350
= E =2503.00
5 3 =200250
2 g is0200
2 £ sio0as0
2 E e
2 E #000050
2 H
> H
z g
27 <
25 &
2 £
30 H
a £
2 -4
3 E
1 £
35 01 02 03 04 05 0§ 07 08 09 1 11
36
a7 Slit width [mm]
38
3
40
ﬁ'n»w Summary - Dataleft DataRight , DataBottom  Pvot | Plot data ~ PivotBottom  Plot data Bottom ~ PivotMAX  Plot data MAX ~ Distribution ~Plot  PlotBottom . Pid [N m




[image: image15.png]slit

0.1
02
03
0.4
05
06
07
08
09

11

Chart Tools

01

02

03

04 0s 08 07 08 0s

Slit width [mm]

11

Average:

Count: 374

Gaivri oty - |10 - (A" u| [Sf=i] @A
BIU A === W 3 2
£
c D £ F s H 1 [3 L M N o P a R s T u v w x Y z AA
Total %
570 480 475 400 390 380 325 320 300 285 260 250 240 210 200 _ 195 190 _ 175 _ 160 _ 150 _ 140 130 120 105 100
015 019 017 020 02 02 022 026 02 025 028 031 030 032 034 040 033 040 040 037 035 041 041 041 049
0.39 [/ 41 0.58 0.57 0.57|
0ss 0 . 4 065 066 065
Yo Maximum creepage after 300h [mm] i on  on om
0’ 0 570 4 07 075 o7
0.84 0, \? 2/ 0.80 0.80 0.79)
088 0 s 4 08 08  om
0ss o 5 7 oss o087 0s7
0ss o & 0 08 08 030
0.96 0 05 3 0.93 0.93 0.93
0% 0 £ 6095 035 03
325 A
K]
£
500 5
£ 5300350
B
E 250300
250 2
2 2200250
£ 150200
2
w0 g 5100150
g 050100
10 2 000050
g
150 3
S
&
&
140 E
g
£
5
120 S
3
3
100 &

AB

080
045
057
065
072
076
077
0.4
087
0.0
092
095

AC

070
043
056
066
070
075
078
0.4
0386
0.8
093
096

AD

056
04
05
05
07|
07|
07|
03
03
09
09
09

31PM

S/2/2012




[image: image16.png]B Home Insert Page Layout Formulas. Data. Developer Add-Ins Load Test Team layout | Format x
f;:mamn - | || gsnan.rm- - A TextFil + & JJ E’T& El % CA |50 veiont [ =
e[ () (i) () (i) (i) (] = smmeomnes | B\ B\ A\ s :
B resetto atcn syie = QD Shape tects - a A Tetettecs~ | Ho G e MO Croup Relste || Bl wiatn: {1076 <
Curent Selection shape styes 5 Wordart Styles 5 Anange. size 5
Charta - £| v
A B C D E F G H 1 J K L M N o P Q R S T u v w X Y z AA AB A
1 Total %
2 a5 400 390 380 325 320 300 28 260 250 240 210 200 195 180 _ 175 _ 160 _ 150 _ 140 _ 130 _ 120 _ 105 _ 100 080 ¢
- S84.64  487.57  479.64 465.60 39733 39177 36359 35223 32351 30721 29514 26043 249.91 24126 23861 21194 199.07 18459 17022 159.32 14838 12851 124.88) 9569 8
4 15049 12233 12604 12279 10101 9944 980 9215 8121 7885 7640 6604 6284 6157 5978 5515 4994 4730 4335 4008 3770 3324 3.7 2504 2
s 6950 5761 5674 5507 4683 4535 4313 4153 3850 3677 3550 3056  29.60 2825 2720 2522 2359 2203 1929 1894 1736 158 1450 1140 1
5 3894 3218 3140 3095 2698 2601 2466 2405 2101 2084 1935 1795 1629 1575 1667 1401 1325 1245 1165 1052 976 877 842 689 |
7 255 213 2062 2050 1708 1671 158 1468 1385 1349 1318 1100 1027 1042 995 895 868 829 730 65 617 562 549 410
s 7GR 1A% rES A0 TIOT—TRE 1191 nsAe Gz aSn—aan TRy 7ss 71 7 s 585 558 477 483 466 393 375 268
B 448 385 368 365 339 2% 274 225
10 Coverage after 300h [%] 335 319 301 264 248 228 220 168
1n 280 257 218 218 1s5 178 169 127
12 570 £ 212 2.10 180 172 166 138 1.37] 104
13 a7s = 182 167 147 137 131 121 1.10] 0.82 [
14 2
- 0 £
1 g
17 H
18 20 5T msoco0000
D w0 5y weomson
S
2 200 $ & cs0006000
2 oo E E 20004000
2 150 £ E 0002000
> S5
;: w %
% w g
e o E
30
5 w ¥
» 01 02 03 o0a 05 05 07 08 09 1 11 =
3 Slit width [mm]
u
35
36
a7
38
3
40

a1

W 4 v W] Summery . Dataleft .~ DataRight  DataBottom . Piot . Plot data .~ PotBottom | Plot data Bottom . PivOtMAX .~ Plot data MAX . Distribution .~ Plot ~ PlotBottom .~ PId I

Average: 3594 Count: 374

Sum: 13,4417





Figure 5. Average creepage, maximum creepage and average coverage after 300 hours
The average and maximum creepages and average coverage after 300h for different slit width (slit width is in the range of 0.1-1.1mm) is shown in Fig. 5. The obtained results are in good agreement with experimental results. Maximum creepage on the side of the scratch is 0.94mm, and the average creepage is 0.88mm. It can be seen that as slit width increases and total percentage of inhibitors decreases creepage increases, and vice versa. The coverage of the bottom of the scratch is increased if the slit width is smaller and if the number of total percentage of inhibitors is increased.
[image: image17.png]\ Home  Inset  Pagelayout  Formulas  Data Developer  Adddns  loadTest  Team Layout | Format @ - = x
Chart Area - Shape Fill - AtexFin- . = NP -
oo 4 Ty % By B L | meee
B Format selection see | [ aee | [ aec ‘ ave ‘ aee | [ nee ‘ sbe | <] 22 shape outine - A I\ o Zretoune- ||l LU CRE T
B resetto Maten st = QD Shape tects - [\ TedErteds~ || Front facke  pane e o oo | w1387 O
Current selection Shape sties 5 Wordart Styes 5 Anange. size 5
Chart2 He £| v
A B C D E F G H 1 J K L M N o P Q R S T u v w X Y z AA AB AC AD
1 Total %
2 570 480 475 400 390 380 325 320 300 _ 28 _ 260 250 _ 240 210 200 195 190 175 160 _ 150 _ 140 _ 130 _ 120 105 _ 100 _ 080 _ 070 _ 0§
3 % o1 014 015 015 017 017 017 013 020 021 021 023 025 025 028 029 030 030 034 035 037 039 040 041 044 045 050 052 0.
4 o2 039 043 044 050 049 050 055 056 057 058 062 062 063 06 068 06 070 070 073 075 076 078 079 08 082 087 08 09
5 0.3 0.67 0.72 0.72 0.77 i T oin 113 11
5 o4 091 035 09 101 Average creepage after 2000h [mm] 131 133 13
7] Jos 10 115 115 119 147 148 14
8 0.6 128 132 132 136 570 [ 161 161 1.6|
s |7 142 147 145 150 s = 13 1l 1]
10 |os 155 159 159 163 5 183 18 1]
n s 16 1m 1m 1m O 1sa 1% 19
2 | 176 180 181 184 5 202 202 20
1B 11 187 190 191 193 325 é 210 210 24
1
&
300
=2 5
1 20 E
7 H
18 240 2
n I smew
B 200 2
T m2s0300
2 z
> 10 2 5200250
5
2 o £ 10
2 £ mooaso
25 402 woso100
2 H
27 120 £ wo00s0
£
28 100 g
29 Py
30 o0 ¥
31 -
2 oo 2
33 g
025 -]
= ]
35 015 &
36
37 01 02 03 04 o0s 05 07 0s 0s 1 11
) -
s Slit width [mm]
0
a1
W 4 » W] Summary  Dataleft ~ DataRight , DataBottom  Piot | Plot data,  PivotBottom Plot data Bottom  PiOtMAX Plot data MAX , Distrbution . Plot .~ PlotBottom i [l m

Average: 140 Count: 374

Sum: 52232

=g D)

907 PM

57172012




[image: image18.png]- Time 2000 XsmgiMi =
= Home Inset Pageloyout Fomuas  Data  Review Vi Developer  Adddns  loadTest  Team  Design  layout | Format @- o x
;;a:mta‘SIn - l | | gshapeﬁllv - A TextFil + & JJ T% El % PN e
e[ () () () (i) (i) (] - smmeomnes B\ A\ A\ s
B resetto Maten st = QD Shape tects - - A Tetettes~ | Ho G paner M Croup Relste |l wiatn: (1355 <
Current selection Shape Styes 5 Wordat tyles 5 Anange. size 5
Chart 2 - £| v
A B C D E F G H 1 J K L M N o P Q R S T u v w X Y AB AC AD
1 Total %
2 400 390 380 325 320 300 28 _ 260 250 240 210 200 195 _ 19 175 _ 160 _ 15 140 _ 130 120 08 07 0§
3| & 025 028 029 029 031 034 033 038 041 041 _ 043 045 054 046 055 055 053 056 059 058 068 068 07
4 107 105 19
2 Maximum creepage after 2000h [mm] 129 132 13
5 149 150 1|
7 162 163 14
s g s s 17
9 ey 191 1.88 1.8
0 g 200 200 29
1n = 210 209 21
2 5 218 218 23
& £ T -
1 &
5 £
16 £
17 H
18
o Eowmen
20 = =250-3.00
2 s
2 5 “150200
5 £ Lmis
22 £ 050100
P S mocoso
2 £
27 g
28 =
2 &
30 £
32 5
33 -]
a« 3
35 =
36
37 01 02 03 04 o5 05 07 0s 0s 1 11
D Slit width [mm]
39
0
a1
W 4 » M| Summary , Dataleft . DataRight  DataBottom . Pivot  Plot data  PivotBottom  Plot data Bottom . PivotMAX | Plot data MAX ,  Distrbution  Plot . PlotBottom i [l m

=g D)

916 PM

57172012





[image: image19.png]Home Inset  Pagelajout  Fomuas  Data Developer  Adddns  loadTest  Team  Design  layout | Format x
Chart Area - Shape Fill - AtexFin- = NP -
oo 4 5, B By [T G [
B Format selection P ‘ aee ‘ ave ‘ ‘ ave ‘ aee ‘ soc | =] 22 shape outine - A I\ o Zretoune- ||l LU CRE T
B resetto Maten st O shape Effects « 5| A\ Teeteds s | From- packe pane o en OO ROE [l wiath: a0 T
Current selection Shape sties 5 Wordart Styles 5 Arange size 5
Chart 3. - £ v
A B C D E F G H 1 J K L M N o P Q R S T u v w X Y z AA AB A
1 Total %
2 a7s 400 390 380 325 320 300 285 260 250 240 210 200 _ 195 _ 1% 175 _ 160 _ 150 _ 140 _ 130 120 _ 105 _ 100 080 |
- 755.61 63196  621.63 600.41 51355 S07.60 475.90 455.44  413.57 399.40 384.68  336.19 32153 31479 304.65 27585 257.50 240.56 22071 204.54 19058 16844 16113 12502 10§
2 e e e e e e e e e e e e —— e ey
s o 3] 1803 1
. Coverage after 2000h [%] i3 Prem
7 570 2 515 |
s s T ) 3.43
s . 5 27
10 s 5 21
1 400 & 5] 164
12 390 g 3L 131
5] s B ) 108
& 325 &
5 s 2
16 £
= 0 8
. 285 %
& 280 W80.00-100.00
2 250 2
£ wsooosomo
2
200 4
2 £ 40005000
210
» E s
22 200 2
7_5 s 5 moovzom
» o
27 s £
2 =
E 10 3
&
= 150
31 10§
32 130§
33 &
120
) g
105
35 £
= 100
= 01 02 03 04 o5 05 07 0s 0s 1 11
38 Slit width [mm]
39
0
a1
W 4 » W] Summary  Dataleft ~ DataRight , DataBottom . Pivot  Plot data  PivotBottom | Plot data Bottom ~ PiotMAX  Plot data MAX  Distrbution . Plot ~ PlotBottom i [l m

Average: 4599 Count: 374

Sum: 17,201.06





Figure 6. Average and maximum creepages and average coverage after 2000 hours.

The corrosion is progressing during the time. So, the results for 2000h show the greater creepage (worse protection) on side and better coverage of the bottom (because inhibitors are spilled on the bottom surface during time) which is expected. The results can be seen in the Figure 6. The maximum creepage on the side of the scratch is 2.29mm, and the average creepage is 2.16mm.
4. Conclusions
In this study we used FE computer modeling methods to provide guidelines for designing self-healing systems. Also we used data mining technology to fit parameters of interest and to find the best diffusion coefficient and diameter of nanocontainer for the given model size. With this technology we can optimize the number of nanocontainers and inhibitors during experiments and real protection procedures in the industry.
Acknowledgement. This research was supported by Ministry of Science in Serbia, ON174028, III41007 and FP7 MUST project NMP3-LA-2008-214261.

References 

[1] Zheludkevich ML, Shchukin DG, Yasakau KA, Mohwald K, and Ferreira MGS, Anticorrosion Coatings with Self-Healing Effect Based on Nanocontainers Impregnated with Corrosion Inhibitor, Chem. Mater. 2007, 19, 402-411.
[2] Jovanovic A and Filipovic N (2006) Innovative modelling methods in damage assessment: application of dissipative particle dynamics to simulation of damage and self-healing of polymer coated surfaces, J. Theoretical and Applied Mechanics, 44, pp. 637-648. 
[3] Nelder J. and Mead R 1965. A simplex method for function minimization, Computer Journal, 7 (4), 308-313.
PAGE  
2

_1256726106.unknown

_1368179140.unknown

_1400996126.unknown

_1400996165.unknown

_1400996096.unknown

_1256726108.unknown

_1256726104.unknown

