
Процена материјалне дисперзије у стакленим оптичким влакнима

An estimation of material dispersion in the glass optical fibers
M. S. Kovačević1, A. Djordjevich2, and A. Janićijević3

1University of Kragujevac, Faculty of Science, Department of Physics, Kragujevac, Serbia, 

e-mail: kovac@kg.ac.rs
 2City University of Hong Kong, Hong Kong, China, 

e-mail: mealex@cityu.edu.hk   

3University of Belgrade, Faculty of Technology and Metallurgy, Belgrade, Serbia 

e-mail: janicaco@tmf.bg.ac.rs 

Сажетак: У раду је дат прорачун материјалне дисперзије у неким типовима стаклених оптичких влакана. Изведен је израз за матеијалну дисперзију који укључује и трећи извод индекса преламања по таласној дужини, 
[image: image1.wmf]33

/

dnd

l

. Нађено је да за топљени силицијум и флуоридна стакла, у околини таласне дужине која одговара нултој дисперзији,
[image: image2.wmf]22

/0

dnd

l

=

, узимајући у обзир трећи извод индекса преламања, материјална дисперзија у оптичком влакну није једнака нули. 

Кључне ријечи: материјална дисперзија, силицијум, флуоридно стакло, оптичко влакно.

Abstract: An estimation of material dispersion is presented in some typos of glass optical fibers. Using broadly applicable principles for group velocity, a simple expression is derived for material dispersion that includes the third derivative of the index of refraction with respect to the wavelength
[image: image3.wmf]33

/

dnd

l

. It is shown that for fused silica and fluoride based fibers, even
[image: image4.wmf]22

/0

dnd

l

=

, the material dispersion still occurs caused the third derivative of refractive index with respect to the wavelength. 

Key words: material dispersion, fused silica, fluoride glass, optical fiber. 

1. Introduction to dispersion in optical fibers
An information signal becomes distorted due to attenuation and dispersion as it travels in an optical fiber. Attenuation is the loss of signal power and is governed by different mechanisms, including absorption, scattering, and radiation. Since optical fibers were introduced for communication applications five decades ago, great progress has been accomplished in producing optical fibers that exhibit very low signal attenuation. On the other hand, dispersion is the spreading in the time domain of a signal pulse as it travels through the fiber. Spectral components of a pulse propagating down an optical fiber reach their destination at slightly different times. This translates into a wider pulse at the receiving end of the fiber. Both attenuation and dispersion affect repeater spacing in a long distance fiber-optic communication system. Dispersion affects the bandwidth of the system, hence maintaining low dispersion is of equal importance for ensuring increased system information capacity, versatility and cost effectiveness.

2. Dispersion in single-mode fibers

Dispersion in single-mode fibers is an intramodal effect and is a result of group velocity dependence on wavelength. Because of that, the amount of signal distortion depends on the spectral width of the optical source used. Three mechanisms contribute to intramodal dispersion: material dispersion, waveguide dispersion, and polarization-mode dispersion.

2.1. Material dispersion

Material dispersion is caused by variations of refractive index of the fiber material with respect to wavelength. Since the group velocity is a function of the refractive index, the spectral components of any given signal will travel at different speeds causing deformation of the pulse. Variations of refractive index with respect to wavelength are described by the Sellmeier equation which is expressed as follows [1] 


[image: image5.wmf]2

3

2

22

1

1

i

i

i

A

n

B

l

l

=

-=

-

å

,
(1)

where 
[image: image6.wmf]l

is the wavelength of light; 
[image: image7.wmf]i

A

 is the oscillator strength, and  
[image: image8.wmf]i

B

is the oscillator wavelength (Sellmeier coefficients) and are tabulated in [1] and [2] for a number of silica-based glass materials commonly used in fabrication of optical fibers. 
2.2. Waveguide dispersion

Waveguide dispersion occurs because different spectral components of a pulse travel with different velocities by the fundamental mode of the fiber. It is as a result of axial propagation constant 
[image: image9.wmf]b

being a function of wavelength due to the existence of one or more boundaries in the structure of the fiber. Without such boundaries, the fiber reduces to a homogeneous medium, the fundamental mode becomes a uniform plane-wave, and the waveguide dispersion effect is eliminated.

2.3. Polarization-mode dispersion

Single-mode fibers, in reality, support two orthogonally-polarized fundamental modes. In perfectly circular fibers, these two modes have identical propagation constants and pulse spreading due to polarization-mode dispersion does not exist. In practical fibers, however, there is a small difference between the propagation constants of these two modes due to the slight ellipticity of the core. In other words, common single-mode fibers actually support two modes and thus are not truly single-mode. The presence of two fundamental modes contributes to pulse spreading. This phenomenon is known as polarization-mode dispersion.


3. Dispersion in multimode fibers

In applications where two or more modes travel simultaneously though the fiber, intermodal as well as intramodal dispersions exist. Intermodal dispersion does not occur in single-mode fibers, but is a significant effect in multimode fibers. It occurs as a result of different modes having different group velocities at the same frequency. Graded-index fibers with nearly parabolic-index profile were developed mainly to reduce the effect of intermodal dispersion. Here, bound rays deviating from the axis of the fiber travel a longer distance but at larger velocities, reaching the receiving end of the fiber at about the same time with the other rays, thus in graded-index fibers pulse spreading is significantly reduced. Although all forms of dispersion present in single-mode fibers exist in multimode fibers too, the material dispersion is the only significant intramodal effect which should be considered. Thus, pulse spreading in multimode fibers is largely due to material dispersion and intermodal delay distortion. Polarization-mode dispersion is a much weaker effect than material dispersions and intermodal delay, and is often neglected in the analysis and design of fiber-optic links. Apart from the three dispersion effects described above, there is yet another kind of dispersion referred to as profile dispersion. This effect is attributed to core and cladding materials having slightly different material dispersions. 

4. Group Velocity, Group Delay, and Dispersion
Let us consider an information signal propagating in a single-mode fiber of length 
[image: image10.wmf]L

. Each spectral component of the signal undergoes a time delay 
[image: image11.wmf]g

t

. The time delay per unit length, denoted as 
[image: image12.wmf]g

t

, is obtained as


[image: image13.wmf]2

0

11

2

g

g

g

t

dd

Lvcdkcd

blb

t

pl

====-

,
(2)

where 
[image: image14.wmf](

)

(

)

11

0

//

g

vddcddk

bwb

--

==

 is the group velocity, 
[image: image15.wmf]0

2/

k

pl

=

 is the free-space wave number, and 
[image: image16.wmf]c

 is the velocity of light in free space. Spectral components travel at different speeds and experience different time delays. We are interested in the pulse spreading arising from group delay variations. Let the root-mean-square spectral width of the optical source be 
[image: image17.wmf]l

s

, then the total delay difference is given by


[image: image18.wmf]g

d

L

d

l

t

dts

l

=

.
(3)
The amount of pulse spread per unit length of fiber and per unit spectral width of light source is defined as dispersion. Thus, the expression of dispersion is written as



[image: image19.wmf]2

2

1

2

2

g

d

dd

D

Ldcdd

l

t

lbb

dtl

slpll

æö

===-+

ç÷

èø

.
(4)
A more suitable formula for calculation of dispersion is that expressed in terms of the normalized propagation constant 
[image: image20.wmf]b

, defined as 
[image: image21.wmf]0

/2/

k

bbpbl

==

. Substituting for 
[image: image22.wmf]b

, in terms of 
[image: image23.wmf]b

, (4) is reduced to


[image: image24.wmf]2

2

d

D

cd

lb

l

=-

.
(5)
The cumulative effect of waveguide and material dispersion is usually referred to as chromatic dispersion.
The broadening of light pulses caused by dispersion is a critical factor that limits the quality of signal transmission over optical links. Fundamentals about this topic, presented simply and illustrated by numerous examples, can be found in [1, 2]. Much research has been focused on theoretical investigations of the pulse broadening and the information-carrying capacity of multimode glass optical fibers [3-5]. The broadening and deformation of the light pulse in optical fibers has also been the subject of experimental measurements [6]. A review of literature reveals that much research effort (for example [8]) has focused on the computational simulation and modeling dispersion in optical fibers. However, there are only a few studies that have reported about material dispersion around the so-called zero material dispersion (ZMD) wavelengths 
[image: image25.wmf]c

l

 when the second derivative of the index of refraction with respect to the wavelength is zero, 
[image: image26.wmf]22

/0

dnd

l

=

. The purpose of this paper is to model the material dispersion in context of the pulse distortion caused by effects of the term 
[image: image27.wmf]33

/

dnd

l

. Such modeling is based on the assumption that the refractive index of glass optical fibers follows a three-term Sellmeir’s function of wavelength. For operation around ZMD wavelengths in the glass optical fibers, results show that even as 
[image: image28.wmf]22

/0

dnd

l

=

, the material dispersion still occurs caused by effects of the third derivative of refractive index with respect to the wavelength. 

5. Zero material dispersion wavelengths

Over the wavelength region of greatest interest, the material dispersion can best be discussed by studying the propagation of plane waves in homogeneous dispersive medium. The group velocity of a wave is defined as


[image: image29.wmf](

)

1

/

g

v

dd

bw

=

,
(6)

where 
[image: image30.wmf](

)

()/()

cn

bwww

=

 represents the propagation constant, and 
[image: image31.wmf]()

n

w

represents the frequency-dependent refractive index. In the case of a medium for which 
[image: image32.wmf]b

 is not a linear function of 
[image: image33.wmf]w

, the medium is said to be dispersive. Thus,



[image: image34.wmf]111

()()

g

ddndn

nn

vdcdcd

b

wwll

wwl

éùéù

==+=-

êúêú

ëûëû

,
(7)

where the free space wavelength 
[image: image35.wmf]l

 is related to the frequency through the relation 
[image: image36.wmf](

)

2/

c

lpw

=

. The quantity 
[image: image37.wmf](

)

()/

g

Nndnd

lll

=-

 is referred to as the group refractive index since 
[image: image38.wmf]/

g

cN

 determines the group velocity. Thus, the time it takes for a pulse to traverse some distance 
[image: image39.wmf]L

 through the fiber is given by



[image: image40.wmf]()

g

Lddd

tLL

vddd

bbl

l

wlw

===

,
(8)

which depends on the wavelength 
[image: image41.wmf]l

. With 
[image: image42.wmf]2/

c

lpw

=

 the following relation is obtained 



[image: image43.wmf]()()

Ldn

tn

cd

lll

l

éù

=-

êú

ëû

.
(9)

If 
[image: image44.wmf]/0

dnd

l

¹

, then the transit time for the pulse depends on the wavelength. Most light sources such as light emitting diodes (LEDs) or semiconductor lasers have a spectral width 
[image: image45.wmf]l

D

 that exceeds by far that of the pulse itself. Spectral widths
[image: image46.wmf]l

D

 of light sources are comparatively large in the case of LEDs, approximately around 20 nm at half height, and small in the case of laser diodes (LDs), approximately between 1 and 2 nm at half height. If a source is characterized by a spectral width 
[image: image47.wmf]l

D

, then each wavelength component will traverse with a different group velocity resulting in temporal broadening of the pulse. A pulse produced by a light source with spectral width
[image: image48.wmf]l

D

 will thus, after traveling distance
[image: image49.wmf]L

, spread out over a time interval determined by:



[image: image50.wmf]dt

t

d

l

l

D=D

.
(10)

The derivative 
[image: image51.wmf]/

dtd

l

 describes pulse broadening (or spreading) and may be of more interest than the time delay 
[image: image52.wmf]t

 itself. From equation (9), the pulse broadening can be derived as  



[image: image53.wmf]22

22

LdndndnLdn

t

cdddcd

lll

llll

æö

D=--=-D

ç÷

èø


 (11)

or



[image: image54.wmf]2

2

2

Ldn

t

cd

l

l

ll

æö

D

æö

D=-

ç÷

ç÷

èø

èø

.
(12)

The quantity 
[image: image55.wmf]222

/

dnd

ll

 is a dimensionless quantity. Since the material dispersion is proportional to the spectral width 
[image: image56.wmf]l

D

 and to the length 
[image: image57.wmf]L

 of the fiber traversed by the beam, dispersion is usually specified in units of picoseconds per kilometer (length of the fiber) per nanometer (spectral width of the source). Thus, the material dispersion coefficient 
[image: image58.wmf]m

D

of the optical fibers is given by



[image: image59.wmf](

)

2

29

2

11

10ps/kmnm

m

tdtdn

D

LLdcd

l

llll

æö

D

===-××

ç÷

D

èø


(13)

where 
[image: image60.wmf]l

 is measured in micrometers and 
[image: image61.wmf]5

310km/s

c

=×

.

The wavelength 
[image: image62.wmf]c

l

 at which 
[image: image63.wmf]22

/0

dnd

l

=

, is referred to as the zero material dispersion wavelength. At this wavelength, pulses will suffer negligible dispersion as they propagate through an optical fiber. Below this wavelength, 
[image: image64.wmf]22

/

dnd

l

 is positive while above this wavelength 
[image: image65.wmf]22

/

dnd

l

 is negative. The former wavelength region is referred to as a normal group velocity dispersion region, while the latter region is known as an anomalous group velocity dispersion region. It should be noted that the pulse disperses in both regions: longer-wavelength components of the pulse travel faster than the shorter-wavelength ones in the normal dispersion region while the opposite is true for the anomalous dispersion region. It appears that, when an optical fiber is operated at ZMD wavelength, the pulses will not suffer any dispersion at all. However, for operation around ZMD wavelength, pulse distortion would be 
[image: image66.wmf]33

/

dnd

l

. This term has a significant impact in determining of the dispersion around ZMD wavelength. If we consider two closely spaced wavelengths 
[image: image67.wmf]l

 and 
[image: image68.wmf]ll

+D

, then 
[image: image69.wmf]()

t

l

 and 
[image: image70.wmf]()

t

ll

+D

 will represent respective time delays. Then, we may write 



[image: image71.wmf]22

2

()

()()

2

dtdt

tt

dd

l

llll

ll

D

+D=+D+

.
(14)

The term 
[image: image72.wmf]/

dtd

l

 vanishes at the ZDM wavelength, so the pulse broadening due to material dispersion is given by



[image: image73.wmf]2223

23

()()()

()()

22

dtLdn

ttt

dcd

lll

lll

ll

DD-

D=+D-==

.
(15)

Thus,



[image: image74.wmf](

)

3

2

3

2

dn

tL

cd

l

l

l

æö

D=-D

ç÷

èø


(16)

or



[image: image75.wmf]2

3

3

3

2

Ldn

t

cd

l

l

ll

æö

D

æö

D=-

ç÷

ç÷

èø

èø

.
(17)

It should be noted that the broadening that occurs when a pulse propagates through an optical fiber at the wavelengths around ZMD wavelength, is proportional to 
[image: image76.wmf]2

()

l

D

and distance 
[image: image77.wmf]L

. Thus, the material dispersion coefficient 
[image: image78.wmf]m

D

¢

 of the optical fibers around zero material dispersion wavelengths is given by



[image: image79.wmf](

)

3

39

23

10ps/kmnm

m

tdn

D

Lcd

l

l

lll

æö

DD

¢

==-××

ç÷

D

èø


(18)

where 
[image: image80.wmf]l

 is measured in micrometers and 
[image: image81.wmf]5

310km/s

c

=×

.

6. Results and discussion
We have carried out a computer simulation for fused silica first. An empirical expression for the refractive index variation is given by [9]



[image: image82.wmf](

)

(

)

(

)

(

)

24

35

4

012

23

2

22

CC

C

nCCC

l

ll

lll

l

ll

=+++++

-

--

, 
(19)
where C0=
[image: image83.wmf]1.4508554

, C1=
[image: image84.wmf]0.0031268

-

, C2=
[image: image85.wmf]0.0000381

-

, C3=
[image: image86.wmf]0.0030270

, C4=
[image: image87.wmf]0.0000779

-

, C5=
[image: image88.wmf]0.0000018

,  and l=
[image: image89.wmf]0.035

. Based on Eq. (19), the second derivative of refractive index for fused silica with respect to the wavelength is shown in Figure 1. To gain numerical appreciation, we see from Eq. (13) that, at 
[image: image90.wmf]1.2753

μm

c

l

=

, the material dispersion for the fused silica is
[image: image91.wmf]0

t

D=

 (the value of 
[image: image92.wmf]c

l

 is ZMD wavelength).
[image: image93.jpg]0.12

0.10
~, 008
o]
3
T
= 0.06
N

0.04

A =1.2753 ym
0.02 \
0.6 08 1.0 12 7 +

A (pm)




Figure 1: Variation of 
[image: image94.wmf]22

/

dnd

l

 with 
[image: image95.wmf]l

 of the fused silica

[image: image96.jpg]0.8

1.0

14

1.6
A (um)




Figure 2:  Variation of 
[image: image97.wmf]33

/

dnd

l

 with 
[image: image98.wmf]l

 of the fused silica
Third derivative of refractive index for fused silica is shown in Figure 2. As mentioned already for operation around ZMD wavelength, the material dispersion would be determined by the next power term, namely by 
[image: image99.wmf]33

/

dnd

l

. It should be noted that the material dispersion still occurs at around 
[image: image100.wmf]1.2753

μm

c

l

=

 despite 
[image: image101.wmf]22

/0

dnd

l

=

. 
Figure 3 shows the material dispersion for fused silica determined by 
[image: image102.wmf]33

/

dnd

l

 around ZMD wavelength. To gain some numerical appreciation, we see from Eq. (17) that for 
[image: image103.wmf]1.2753

μm

c

l

=

, the material dispersion for fused silica  is 
[image: image104.wmf]31ps/km

t

D@

.

[image: image105.jpg]1.24 1.26 pe's 1.30
A (pm)

18

1.20




Figure 3: Material dispersion of the fused silica-based optical fibers around ZMD wavelength
We continued our analysis of the material dispersion with pure and doped silica-based fibers whose refractive indices can be represented by the three-term Sellmeier’s function of wavelength (1). Values of coefficients in Sellmeir’s formula for pure and doped silica are shown in Table 1 [10]. The corresponding variation of refractive index with wavelength is shown in Figure 4. It is apparent that the refractive index changes with doping.

Table 1: The Sellmeir’s coefficients for pure and doped silica [17].

	Sample
	Dopant

(mole %)
	A1
	A2
	A3
	B1
	B2
	B3

	1
	Pure SiO2
	0.00469148
	0.01351206
	97.93400
	0.6961663
	0.4079426
	0.8974794

	2
	GeO2 (6.3)
	0.007290464
	0.01050294
	97.93428
	0.7083952
	0.4203993
	0.8663412

	3
	GeO2 (19.3)
	0.005847345
	0.01552717
	97.93484
	0.7347008
	0.4461191
	0.8081698

	4
	B2O3 (5.2)
	0.004981838
	0.01375664
	97.93353
	0.6910021
	0.4022430
	0.9439644

	5
	P2O5 (10.5)
	0.005202431
	0.01287730
	97.93401
	0.7058489
	0.4176021
	0.8952753


[image: image106.jpg]1.49

1.48

1.47

1.46

145

1.44

1 - Pure Si0,
s 2 Ge0,(6.3)
3 - Ge0,(19.3)
- 4-B05(5.2)

5P, 05(10.5)

0.6 0.8 1.0 12 14 1.6




Figure 4: Refractive index versus 
[image: image107.wmf]l

 of the pure and doped silica
In Figure 5, the variations of  
[image: image108.wmf]22

/

dnd

l

 are shown for pure and doped silica (the labels 1-5 correspond to various samples given in Table 1). 

[image: image109.jpg]0.05/% 1 - PureSi0,

2-Ge0s (6.3)
3 - Ge0,(19.3)
.\ 4-B04(5.2)
0.044) 5-P;05(10.5)
x
)
= 003
N
I
™
0.02

0.01





Figure 5: Variations of  
[image: image110.wmf]22

/

dnd

l

 with 
[image: image111.wmf]l

 of the pure and doped silica

As an illustration, it follows from Eq. (1) that 
[image: image112.wmf]1

1.2728

μm

c

l

=

, 
[image: image113.wmf]2

1.30947

μm

c

l

=

, 
[image: image114.wmf]3

1.38325

μm

c

l

=

, 
[image: image115.wmf]4

1.26453

μm

c

l

=

 and 
[image: image116.wmf]5

1.28266

μm

c

l

=

. It is apparent that the doping changes the ZMD wavelengths slightly. 
In Figure 6, the variation of 
[image: image117.wmf]33

/

dnd

l

 are shown for pure and doped silica. It is apparent that around ZMD wavelengths the third derivative of the refraction index is not zero and that it contributes to the existence of material dispersion in optical fibers (based on both, pure and doped silica). In Figure 7, the calculated material dispersion is shown for pure and doped silica optical fibers. We conclude that despite 
[image: image118.wmf]22

/0

dnd

l

=

 around ZMD wavelengths, material dispersion occurs nevertheless; it is approximately 20-35 ps/km.
[image: image119.jpg]—-0.020

-0.025

&nfd

—-0.030

1 - PureSi0,
2 - Ge0s (6.3)
3 - Ge0,(19.3)
4-B05(5.2)





Figure 6: Variation of 
[image: image120.wmf]33

/

dnd

l

 with 
[image: image121.wmf]l

 of pure and doped silica

[image: image122.jpg]A7 (ps)

45 1 - Pure Si0,
2-Ge0; (6.3)
*3,, 3 - Ge0y(19.3)

: 4-B,05(5.2)
40N 5-P,05(10.5)

122 124 1.26 1.28 1.30 132 1.34




Figure 7: Material dispersion of the pure and doped silica-based optical fibers around ZMD wavelength

In the last few years, fluoride-based fibers have been investigated in detail for operation in mid-infrared (2-5
[image: image123.wmf]μm

) wavelength region because of their predicted ultra low loss of 10-3 dB/km. Such fibers may find applications in long-wave repeaterless telecommunication links and intercontinental submarine links. This has motivated us to continue with analysis of fluoride fibers in order to calculate a material dispersion around ZMD wavelength. Various fluoride glasses for applications in infrared fiber optic communication are shown in Table 2.

Table 2: Various fluoride glasses (adapted from [18]).

	
	
	Concentration (mole %)

	Sample
	Material
	ZrF4
	BaF2
	LaF3
	NaF
	HfF4
	AlF3
	CaF2
	CdF3
	YF3

	1
	ABCY
	
	22
	
	
	
	40
	22
	
	16

	2
	HBL
	
	33
	5
	
	62
	
	
	
	

	3
	ZBG
	63
	33
	
	
	
	
	
	4
	

	4
	ZBLAN
	53
	20
	4
	20
	
	30
	
	
	


For the fluoride glass, the refractive index versus wavelength can be represented by the following Sellmeier’s expression [11]



[image: image124.wmf]4224

()

nABCDE

lllll

--

=++++

 
(20)
where A to E are Sellmeier’s coefficients listed in Table 3.  
Table 3: Sellmeier’s coefficients for the fluoride glasses [18].

	Sample
	Material
	A
[image: image125.wmf]6

10

-

×


	B
[image: image126.wmf]3

10

-

×


	C
	D
[image: image127.wmf]3

10

-

×


	E
[image: image128.wmf]6

10

-

×



	1
	ABCY
	7.67742
	2.16195
	1.42969
	-1.28304
	-5.35487

	2
	HBL
	-28.61020
	3.11470
	1.50294
	-1.17821
	-2.64123

	3
	ZBG
	93.67070
	2.94329
	1.51236
	-1.25045
	-4.01026

	4
	ZBLA
	-300.80370
	4.03214
	1.51272
	-1.21921
	-6.77630

	5
	ZBLAN
	93.67070
	2.94329
	1.49136
	-1.25045
	-4.01026


Average refractive indices of the fluoride glasses are summarized in Figure 8 for different wavelengths (the labels 1 to 5 denote the fluoride materials).
[image: image129.jpg]1.50

1.48
1.46
5 -ZBLAN
1.44
1
142
1.5 20 2.5 3.0 35

A (um)




Figure 8: Average refractive indices versus 
[image: image130.wmf]l

 of the fluoride glasses

The corresponding variations of the 
[image: image131.wmf]22

/

dnd

l

 and 
[image: image132.wmf]33

/

dnd

l

 with wavelength are shown in Figures 9 and 10. The following values of the ZMD wavelengths were obtained: 
[image: image133.wmf]1

1.48152

μm

c

l

=

, 
[image: image134.wmf]2

1.65832

μm

c

l

=

, 
[image: image135.wmf]3

1.62595

μm

c

l

=

, 
[image: image136.wmf]4

1.69593

μm

c

l

=

 and 
[image: image137.wmf]5

1.62595

μm

c

l

=

. It is apparent that around ZMD wavelengths the third derivatives of index refraction are different from zero (Figure 10), which should be taken into account when calculating the material dispersion.

[image: image138.jpg]0.004

1-ABCY
2-HBL
3-ZBG
4-ZBLA
5-ZBLAN

0.002

& nfdV

—0.002





Figure 9: Variation of 
[image: image139.wmf]22

/

dnd

l

 with 
[image: image140.wmf]l

 of the fluoride glasses
[image: image141.jpg]& nfdv

—0.005

-0.010

—-0.015

—-0.020

1-ABCY
2-HBL
3-7ZBG
4-ZBLA
5-ZBLAN





Figure 10: Variation of 
[image: image142.wmf]33

/

dnd

l

 with 
[image: image143.wmf]l

 of the fluoride glasses
In Figure 11, the material delay distortion of pulse in the fluoride-based optical fibers was obtained from Eq. (13). The material dispersion is approximately 10-25 ps/km around the ZMD wavelengths. 
[image: image144.jpg]At (ps)

10

1-ABCY
2-HBL
3-7ZBG
4-ZBLA
5—-ZBLAN

142

1.44 1.46 1.48 1.50

A (um)




Figure 11: Material dispersion of the fluoride glasses-based optical fibers around ZMD wavelength
7. Conclusion

Details of material dispersion are investigated in the context of pulse distortion in multimode glass optical fibers. Significance of the 
[image: image145.wmf]33

/

dnd

l

 term in an earlier reported concept is estimated. This is done for the operating wavelength around the so-called zero material dispersion wavelength when 
[image: image146.wmf]22

/0

dnd

l

=

. The strong material dispersion persisting under this condition (a pulse of light centered on this zero material dispersion wavelength also suffers significant dispersion) attests to strong influence of the next higher-order term 
[image: image147.wmf]33

/

dnd

l

.

Acknowledgements - The work described in this paper was supported with grants by Serbian Ministry of Science and Technology (Projects 171011 and 171021). 

References
[1] M. J. Adams, An Introduction to Optical Waveguides, John Wiley & Sons, Inc., New York, 1981.
[2] D. Davison, Single-mode wave propagation in cylindrical optical fibers, Optical Fiber Transmission, Edited by E. E. Basch, Indianapolis, Howard W. Sams & Co., Chapter 3, 1987.

[3] D. Gloge, Dispersion in weakly guiding fibers, Appl. Opt.  10, 1971,  2442-2445.
[4] A. Snyder and J. D. Love , Optical Waveguide Theory , Chapman and Hall, London, 1983.

[5] D. Marcuse, Calculation of bandwidth from index profiles of optical fibers 1: Theory,  Appl. Opt. 18,1979,  2073-2080.

[6] R. Olshansky and B. D. Keck, Pulse broadening in graded-index optical fibers, Appl. Opt., 15, 1976, 483-491. 

[7] F. K. Barrell and C. Pask, Pulse dispersion in optical fibers of arbitrary refractive-index profile, Appl. Opt. 19, 1980, 1298-1305. 

[8] S. E. Mechels, J. B. Schlager and D. L. Franzen, Accurate Measurements of the Zero-Dispersion Wavelength in Optical Fibers, J. Res. Natl. Inst. Stand. Technol. 102, 1997, 333 -347. 

[9] Wemple S. H., Material dispersion in optical fibers, Appl. Opt. 18, 1972, 31-35. 

[10] K. Thyagarajan, B. P. Pal, Modeling dispersion in optical fibers: applications to dispersion tailoring and dispersion compensation, J. Opt. Fiber Comm. Rep. 4, 2007, 173-213. 

[11] U. C. Peak, G. E. Peterson, and A. Carnevale A, Bell Sys. Techn. J. 60,  583 (1981).

[12] T. Kimura, Optical Fiber Transmission, Ed. K. Noda, North Holland Studies in Telecommunications, 6, North Holland, Amsterdam, 1986.

[13] A. Ghatak and K. Thyagarajan, Introduction to fiber optics, Cambridge University Press, Cambridge, 1998.

10
9

_1360045404.unknown

_1360771940.unknown

_1433413442.unknown

_1433418245.unknown

_1433497513.unknown

_1433497969.unknown

_1433498180.unknown

_1433498192.unknown

_1433498013.unknown

_1433497525.unknown

_1433418319.unknown

_1433418384.unknown

_1433418712.unknown

_1433418347.unknown

_1433418260.unknown

_1433413690.unknown

_1433417955.unknown

_1433418033.unknown

_1433413784.unknown

_1433413581.unknown

_1433413630.unknown

_1433413462.unknown

_1433410541.unknown

_1433413408.unknown

_1433413409.unknown

_1433410739.unknown

_1433408472.unknown

_1433410533.unknown

_1360772154.unknown

_1433408462.unknown

_1360772192.unknown

_1360772095.unknown

_1360515272.unknown

_1360771618.unknown

_1360771803.unknown

_1360771927.unknown

_1360771670.unknown

_1360771617.unknown

_1360515820.unknown

_1360161455.unknown

_1360515165.unknown

_1360515219.unknown

_1360515253.unknown

_1360515194.unknown

_1360515066.unknown

_1360515118.unknown

_1360161576.unknown

_1360514942.unknown

_1360161622.unknown

_1360161529.unknown

_1360158347.unknown

_1360159071.unknown

_1360160946.unknown

_1360161401.unknown

_1360160927.unknown

_1360159023.unknown

_1360159070.unknown

_1360159061.unknown

_1360158673.unknown

_1360137126.unknown

_1360137514.unknown

_1360157539.unknown

_1360137347.unknown

_1360137373.unknown

_1360055984.unknown

_1360136975.unknown

_1360048215.unknown

_1360048522.unknown

_1360046022.unknown

_1322053627.unknown

_1357478195.unknown

_1357478721.unknown

_1357543947.unknown

_1357544845.unknown

_1359806677.unknown

_1359974940.unknown

_1357543978.unknown

_1357482006.unknown

_1357536761.unknown

_1357480292.unknown

_1357481876.unknown

_1357478656.unknown

_1357478684.unknown

_1357478251.unknown

_1357478524.unknown

_1322054056.unknown

_1322054120.unknown

_1357477964.unknown

_1322054149.unknown

_1322054099.unknown

_1322053694.unknown

_1322053747.unknown

_1322053757.unknown

_1322053713.unknown

_1322053682.unknown

_1322053328.unknown

_1322053512.unknown

_1322053605.unknown

_1322053616.unknown

_1322053561.unknown

_1322053583.unknown

_1322053525.unknown

_1322053385.unknown

_1322053394.unknown

_1322053340.unknown

_1282739864.unknown

_1322053155.unknown

_1322053295.unknown

_1322053311.unknown

_1322053277.unknown

_1295178627.unknown

_1322053111.unknown

_1322053140.unknown

_1322035671.unknown

_1295178696.unknown

_1282739869.unknown

_1295178517.unknown

_1282739868.unknown

_1282739859.unknown

_1282739861.unknown

_1282739862.unknown

_1282739860.unknown

_1282739856.unknown

_1282739857.unknown

_1282739855.unknown

