VIМеђународни научни скуп Савремени материјали2013 –  Бања Лука, 4-6 јул 2013.

VI International Scientific Conference Contemporary Materials 2013 – Banja Luka, 4-6 July 2013

ВИТАМИНИ Б1 И Ц, КАО ИНХИБИТОРИ КОРОЗИЈЕ БАКРА, У РАСТВОРИМА ХЛОРОВОДОНИЧНЕ КИСЕЛИНЕ
М.Г. Павловић1, М.В. Томић1, R. Fuchs Godec2
1Универзитет у Источном Сарајеву, Технолошки факултет Зворник, 
Република Српска, e-mail: pavlovicmiomir@gmail.com
2Универзитет у Марибору, Факултет за хемију и хемијско инжењерство, Марибор
У овом раду извршено је испитивање заштите бакра обрадом корозионе средине применом витамина Б1 и Ц, као инхибитора корозије  у 4% -ним растворима  HCl. Витамин Ц (аскорбинска киселина) и витамин Б1 (тиамин) коришћени су у концентрацијама: 0,5g/dm3, 1g/dm3, 1,5g/dm3, 2g/dm3 и 3g/dm3. Инхибиторско дејство витамина Б и Ц на процес корозије бакра испитивано је гравиметријском методом, као и електрохемијским методама: спректроскопијом електрохемијске импедансе (СЕИ), цикличном волтаметријом и снимљене су поларизационе криве. Утврђено је да се степен заштите витамина Ц у 4% раствору HCl мења са променом концентрације инхибитора и са временом. Највећи степен заштите се постиже у 4% раствору HCl при концентрацији витамина Ц од 1,5g/dm3, у временском интервалу од 4h, где степен заштите, z, износи 71,6233%. Испитивања указују да витамин Б1 као инхибитор корозије у раствору 4% HCl показује слабија заштитна својства од витамина Ц. Витамин Б1 показује најбоља заштитна својства при свим концентрацијама за временски период од 6h (z = 30,3905 – 41,4837). Ови резултати не препоручују витамин Б1 као могући инхибитор у растворима HCl.

Кључне речи: бакар, корозија, инхибитор, показатељи корозије, заштитни фактор z

VITAMINES B1 AND C AS COPPER CORROSION INHIBITORS IN HYDROCHLORIC ACID

M.G. Pavlović1, M.V. Tomić1, R. Fuchs Godec2
1University of Eastern Sarajevo, Faculty of Technology Zvornik, Republic of Srpska,

e-mail: pavlovicmiomir@gmail.com
2University of Maribor, Faculty of Chemistry and Chemical Engineering, Maribor

In this work the protection of copper by processing the corrosion environment using vitamins B1 and C in a 4% solution of hydrochloric acid as a corrosion inhibitor was investigated. Vitamin C (ascorbic acid) and vitamin B1 (thiamine) were used in concentrations of 0.5 g/dm3, 1g/dm3, 1.5 g/dm3, 2g/dm3 and 3g/dm3. Inhibitiory effect of vitamins B1 and C in the corrosion process of copper were investigated by gravimetric and electrochemical methods: electrochemical impedance spectroscopy (EIS), cyclic voltammetry and polarization curves.. It was found that the degree of protection of vitamin C in 4% HCl solution varies both with the concentration of inhibitor and time. The highest level of protection in 4% HCl solution was achieved at the concentration of vitamin C of 1.5 g/dm3 in period of about 4h (z = 71,6233%). Studies suggest that vitamin B1 as a corrosion inhibitor in 4% HCl solution shows weaker protective properties than vitamin C. Vitamin B1 shows the best protective properties for all concentrations for a period of 6h (z = 30,3905 to 41,4837). These results do not recommend vitamin B1 as a possible inhibitor in HCl solutions.


Keywords: copper, corrosion, inhibitor, corrosion indicators, protective factor z
