UTICAJ TERMOCIKLIRANJA I MEHANIČKIH CIKLIČNIH OPTEREĆENJA NA RETENCIJU PRIVREMENIH CEMENATA ZA CEMENTIRANJE  PROTETSKIH NADOKNADA NA IMPLANTATIMA

Veselinović Valentina1, Marković Dubravka2 , Nešković Isidora 2, Mirjanić Vladan1

1 Univerzitet u Banjoj Luci, Medicinski fakultet, Studijski program stomatologija;

valentina.veselinovic01@gmail.com

2 Univerzitet u Novom Sadu, Medicinski fakultet, Klinika za stomatologiju Vojvodine dubravkamarkovic@yahoo.com

Ključne riječi: nadoknade na implantima, privremeni cementi, retencija, mehaničko ciklično opterećenje

UVOD: Najčešći način retiniranja fiksnih nadoknada na implantima je cementiranje. Dentalni cementi, ispunjavajući prostor između abatmenta i nadoknade, kompenzuju neslaganja u nalijeganju dvije površine i obezbjeđuju retenciju fiksne nadoknade na suprastrukturi. Cementirana nadoknada je u funkciji, u usnoj duplji izložena brojnim uticajima koji mogu uticati na  njenu retenciju, od kojih su najznačajniji faktori  mastikatorno opterećenje, promjene temperature i visok stepen vlage. Slabljenje retencione sile dovodi do pokretljivosti nadoknade i  rascementiravanja. Simulacija uslova u usnoj duplji se in vitro postiže termocikliranjem i mehaničkim cikličnim opterećenjem u mašini za vještačko starenje.

CILJ: Utvrditi efekat termocikliranja i kompresivnog mehaničkog opterećenja, kao simulacije uslova u usnoj duplji,  na retencijsku snagu privremenog cementa korištenog za cementiranje kruna na implantima.

MATERIJAL I METOD: Deset livenih superstruktura je cementirano na implantne abatmente (Easy abatment, NP Nobel Biocare) sa zink oksid non eugenol privremenim cementom. U toku vezivanja cementa na superstrukture je primjenjen kontrolisani pritisak od 5 kg.  Uzorci su zatim pohranjeni u toku naredna 24 sata u uslovima 100% vlage i temperature od 37 stepeni C, nakon čega su podvrgnuti termocikliranju. Eksperimentalni uzorci su podvrgnuti mehaničkom cikličnom opterećenju u mašini za simulaciju žvačnih ciklusa, pri čemu je odgovarajući broj ciklusa odgovarao određenom vremenskom periodu funkcije u usnoj duplji.  Retenciona sila, neophodna za odvajanje nadoknade od abatmenta, je mjerena u  Univerzalnoj Instrom mašini za testiranje. Zabilježena je retenciona sila 24 sata nakon cementiranja, bez aplikacije opterećenja, a zatim nakon aplikacije 192, 2500, 5000 i 10 000 ciklusa mehaničkog opterećenja, što je odgovaralo periodima od 7 dana, 3 mjeseca , 6 mjesci i 12 mjeseci funkcije u usnoj duplji.

REZULTATI: Vrijednost retencione sile se mijenjala pod uticajem termocikliranja i u zavisnosti od broja ciklusa mehaničkog cikličnog opterećenja. Srednja vrijednost sile odvajanja se kretala od 4,5 kod neopterećenih uzoraka pa do 18 N kod uzoraka nakon 10 000 ciklusa.

ZAKLJUČAK: Mastikatorna opterećenja, uslovi vlage i temperaturnih promjena značajno utiču na jačinu veze nadoknade i implantnog abatmenta a samim tim i na stabilnost i dugotrajnost nadoknade u funkciji.

INFLUENCE OF THERMOCYCLING AND MECHANICAL CYCLIC LOADING ON RETENTION OF TEMPORARY CEMENTS FOR CEMENTATION OF PROSTHETIC RESTORATIONS ON IMPLANTS

Veselinović Valentina1, Marković Dubravka2 , Nešković Isidora 2, Mirjanić Vladan1

1 University of Banja Luka, Faculty of Medicine, Department of Stomatology

2 University of Novi Sad, Faculty of Medicine, Clinic of Stomatology of Vojvodina

INTRODUCTION:

The most common way of retention of fixed  restorations on implants is cementing. Luting agents, filling the space between the abutment and restoration surface , compensate for differences in the overlaps of the two areas and ensure retention of fixed restauration to the suprastructure. Cemented restoration is, in function in the oral cavity, exposed to a number of influences that can affect its retention, the most significant factors are masticatory load, temperature changes and high levels of humidity. The weakening of the retention force leads to the mobility of restorations and debonding. Simulation of the conditions in the oral cavity is achieved in vitro by thermocycling and mechanical cyclic loading in the machine for artificial aging.

OBJECTIVE:
Determine the effect of thermocycling and compressive mechanical loading on retention force of temporary cement used for the cementing of crowns on implants.

MATERIAL AND METHODS:

Ten cast suprastructures were cemented on the implant abatment (Easy abatment, NP Nobel Biocare) with zinc oxide non eugenol temporary cement. During cement seating on the suprastructure is applied controlled pressure of 5 kg. Samples were then stored during the next 24 hours at 100% humidity and a temperature of 37 degrees C, after which they were subjected to thermocycling. Retention force, necessary to separate the cast from the abatment, is measured in the Universal Instrom testing machine. Retention force is recorded 24 hours after cementation, without application of the load, and then after the application 192, 2500, 5000 and 10 000 cycles of mechanical loading. Masticatory mechanical loads were simulated in the machine for artificial aging.

RESULTS:
Value of the retention force was changing depending on the number of cycles of mechanical cyclic loading. The mean value of the separation force ranged from 4.5 N with unloaded samples up to 18 N with the samples after 10 000 cycles.

CONCLUSION:
Masticatory loading, conditions of moisture and temperature changes significantly impact the retention between restoration and implants abatment and consequently the stability and duration of the fixed restauration in function