УТИЦАЈ ПАСИВАЦИЈЕ АЗОТНОМ КИСЕЛИНОМ НА КОРОЗИОНА СВОЈСТВА НЕРЂАЈУЋЕГ ЧЕЛИКА AISI 316L

Душан Петковић,1 Горан Раденковић2

1 Mашински факултет Универзитет у Нишу, А. Медведева 14, 18000 Ниш, Србија, dulep@masfak.ni.ac.rs

2Mашински факултет Универзитет у Нишу, А. Медведева 14, 18000 Ниш, Србија, rgoran@masfak.ni.ac.rs

Сажетак: Нерђајући челици имају отпорност према корозији услед формирања заштитног пасивног слоја оксида на површини. Пасивација биомедицинског челика 316L потапањем у азотну киселину је изведена у циљу побољшања заштитног слоја и повећања отпорности према питинг корозији у физиолошком раствору. Регресиона анализа је примењена у циљу откривања утицаја радних параметара при пасивацији (HNО3 концентрација. температура и период пасивације) на корозиону отпорност нерђајућег челика 316L у Hank – овом раствору. Експеримент је изведен као пун факторни са три параметара на три нивоа. За меру корозионе отпорности узет је питинг потенцијал (Еp) добијен из потенциодинамичких мерења. На основу математичког модела анализирани су утицаји сваког од параметара, као и њихова међусобна интеракција.

Кључне ријечи: нерђајући челик, пасивација азотном киселином, питинг потенцијал, регресиона анализа.

EFFECT OF NITRIC ACID PASSIVATION ON THE AISI 316L STAINLESS STEEL CORROSION PROPERTIES

Душан Петковић,1 Горан Раденковић2

1Faculty of Mechanical Engineering University of Niš, A. Medvedeva 14, 18000 Niš, Serbia, dulep@masfak.ni.ac.rs

2 Faculty of Mechanical Engineering University of Niš, A. Medvedeva 14, 18000 Niš, Serbia, rgoran@masfak.ni.ac.rs

Abstract: Corrosion resistance of these alloys is due to the formation of a protective oxide film. Passivation of a biomedical grade 316L stainless steel by means immersion in nitric acid was used to improve a protective oxide layer on the surface and to increase resistance to pitting corrosion in physiological solution. Regression analysis was employed to reveal the effects of operating parameters of the nitric acid passivation (HNO3 concentration. temperature and passivation period) on the corrosion resistance of 316L stainless steel in Hank’s solution. The experiment designed as full factorial with three factors and three levels. The responses were the pitting potential values (Ep) obtained from potentiodynamic tests. According to the mathematical model, the effects of each variable and interactions between them were analyzed.

Key words: stainless steel, nitric acid passivation, pitting potential, regression analysis.