ИСТРАЖИВАЊЕ ПОБОЉШАНИХ ПОСТУПАКА ПРИПРЕМЕ ПОВРШИНЕ АЛУМИНИЈУМА И ЊЕГОВИХ ЛЕГУРА ПРЕД НАНОШЕЊЕ ЗАШТИТНИХ ПРЕВЛАКА

Борислав Малиновић1, Гордана Латиновић2, Милорад Томић3, Јово Мандић4, Перо Саиловић5

1Универзитет у Бањој Луци, Технолошки факултет, Степе Степановића 73, 78000 Бања Лука, РС, БиХ, borislav.malinovic@unibl.rs

2Универзитет у Бањој Луци, Технолошки факултет, Степе Степановића 73, 78000 Бања Лука, РС, БиХ, latinovic.gordana@gmail.com

3Универзитет у Источном Сарајеву, Технолошки факултет, Каракај бб,

75400 Зворник, mtomicc@yahoo.com

4Универзитет у Бањој Луци, Технолошки факултет, Степе Степановића 73, 78000 Бања Лука, РС, БиХ, jovo.mandic@unibl.rs

5Универзитет у Бањој Луци, Технолошки факултет, Степе Степановића 73, 78000 Бања Лука, РС, БиХ, pero.sailovic@unibl.rs

Сажетак: У раду је вршено електрохемијско таложење превлака никла и бакра на алуминијум и испитивање изгледа превлаке, дебљине превлаке и искоришћења струје при електрохемијском таложењу. Припрема узорака алуминијума вршена је хемијски.

Циљ рада је да се након хемијске припреме, испита који од три коришћена раствора за таложење основне превлаке на алуминијум утиче позитивно на добијање дебље завршне превлаке никла и бакра, као и на веће искоришћење струје при електрохемијском таложењу.

Добијени  резултати показују да је од три испитивана раствора за припрему алуминијума за електрохемијско таложење металних превлака најефикаснији раствор за међуфазну заштиту.

Кључне ријечи: електрохемијско таложење метала, дебљина превлаке, искоришћење струје, хемијска припрема, активација.

RESEARCH IMPROVED METHODS OF SURFACE PREPARATION OF ALUMINUM AND ITS ALLOYS BEFORE APPLICATION OF PROTECTIVE COATINGS

Borislav Malinovic1, Gordana Latinovic2, Milorad Tomic3, Jovo Mandic4, Pero Sailovic5

1 University of Banja Luka, Faculty of Technology, Stepe Stepanovica 73, 78000 Banja Luka, RS, BiH, borislav.malinovic@unibl.rs

2 University of Banja Luka, Faculty of Technology, Stepe Stepanovica 73, 78000 Banja Luka, RS, BiH, latinovic.gordana@gmail.com

3 University of East Sarajevo, Faculty of Technology, Karakaj bb,

75400 Zvornik, mtomicc@yahoo.com

4 University of Banja Luka, Faculty of Technology, Stepe Stepanovica 73, 78000 Banja Luka, RS, BiH, jovo.mandic@unibl.rs

5 University of Banja Luka, Faculty of Technology, Stepe Stepanovica 73, 78000 Banja Luka, RS, BiH, pero.sailovic@unibl.rs

Summary: This paper studies electrochemical deposition of nickel and copper to aluminum and investigated coating appearance, coating thickness and current efficiency in electrochemical deposition. Preparation of the aluminum samples was carried out chemically.

The aim of this study is that after chemical preparation, examination of the three solutions used for deposition of coatings on aluminum core has a positive effect on getting a thick top coating of nickel and copper, as well as higher current efficiency in electrochemical deposition.

The results show that of the three tested solutions for surface preparation of aluminium for electroplating, most effective solution is solution for intermediate protection.

Keywords: electrochemical metal deposition, coating thickness, current efficiency, chemical preparation, activation.