REDUCTION KINTICS OF SILVER TUNGSTATE POWDER SYNTHESIZED BY A HOMOGENEOUS PRECIPITATION ROUTE

Dijana Jelić1, Slavko Mentus2 and Saša Zeljković3

1University of Banja Luka, Faculty of Medicine, Department of Pharmacy, Banja Luka, Bosnia and Herzegovina, dijana_jelic@hotmail.com

2University of Belgrade, Faculty of Physical Chemistry,  11158 Belgrade, Serbian Academy for Science and Art, slavko@ffh.bg.ac.rs

3University of Banja Luka, Faculty of  Natural and Mathematical Science,  Banja Luka, Bosnia and Herzegovina

Abstract: Silver tungstate (Ag2WO4) was synthesized by homogeneous precipitation route. Тhe  obtained silver tungstate powder was characterized by SEM and X-ray diffraction methods. Its reduction was examined thermogravimetrically in Ar + 25% H2 atmosphere at the  following heating rates  2.5; 5; 10 and 20 °C/min. It was found that the reduction occurs through the three steps. By transforming TG data into the conversion degree parameter α, and using the isoconversional  expended Friedman (F) and modified Coast-Redfern (CR) methods, the following results were obtained for activation energies of various steps: Ag2WO4 → Ag + WO3-x [ЕF=92.4 kJ/mol и ЕCR= 85.8 kJ/mol],  Ag + WO3-x→WO2-x [EF=179.5 kJ/mol and ECR=181.2]  and finally Ag + WO2-x→W [ЕF=175.9 kJ/mol и ЕCR= 195.6 kJ/mol]. Also the preexponetial factors were determined. The data were confirmed by using the Discrete activation energy distribution model.

Key words: tungstates, precipitation, nonisothermal kinetics, isoconversional method

КИНЕТИКА РЕДУКЦИJЕ СРЕБРО ВОЛФРАМАТНОГ ПРАХА СИНТЕТИСАНОГ ХОМОГЕНOM ПРЕЦИПИТАЦИЈOM

Дијана Јелић1, Славко Ментус2 и Саша Зељковић3

Универзитет у Бањалуци, Медицински факултет, Фармација, Бањалука, Босна и Херцеговина, dijana_jelic@hotmail.com

Универзитет у Београду, Факултет за физичку хемију, 11158 Београд,  Српска академија наука и умјетности, slavko@ffh.bg.ac.rs

Универзитет у Бањалуци, Природно-математички факултет, Бања Лука, Босна и Херцеговина

Сажетак: Ag2WO4 је синтетисан методом хомогене преципитације. Карактеризација узорка урађена је методом скенирајуће електронске микроскопије  и дифракцијом X зрачења. Његова рeдукција је испитивана термогравиметријски у атмосфери Ar + 25% H2  брзинама загријавања: 2,5; 5; 10 и 20°C/min. Нађено је да се редукција одиграва у три фазе. Претварањем термогравиметријских података у конверзиони параметар α, и коришћењем изоконверзионих метода, Фридмановe (F) и Коаст-Редферновe (CR), добијене су следеће енергије активације за сваки ступањ: Ag2WO4 → Ag + WO3-x [ЕF=92,411 kJ/mol и ЕCR= 85,795kJ/mol], други ступањ Ag + WO3→WO2-x [EF=179,534kJ/mol и ECR=181,203] и завршни ступањ  Ag + WO2-x→W [ЕF=175,898kJ/mol и ЕCR= 195,565kJ/mol]. Одређени су такође и преекспоненцијални фактори. Провјера резултата извршена је кориштењем модела расподеле дискретних вредности Еа.

Кључне ријечи. Волфрамати, преципитација, неизотермална кинетика, изоконверзиони метод