Stevan Maksimović, Mirjana Đurić, Mirko Maksimović, Ivana Vasović

Fatigue life estimation of aircraft structural components with surface cracks under load spectrum


[image: image1.jpg]



FATIGUE LIFE ESTIMATION OF AIRCRAFT STRUCTURAL COMPONENTS WITH SURFACE CRACKS UNDER LOAD SPECTRUM

Stevan Maksimović
,Mirjana Đurić1,Mirko Maksimović
,Ivana Vasović

Abstract: Subject of this work is focused to developing computation procedure for residual fatigue life estimation of cracked structural componentsunder load spectrum. Finite element method is used for determination of the stress intensity factors (SIF`s) of structural element with surface cracks. These discrete values of the stress intensity factors of cracked structural componentsare used for derivation of analytic function for SIF that is  necessary in crack growth analyses. To demonstrate efficient computation procedure in residual fatigue life estimation of damaged structural elements here numerical examples are included. For residual life estimation of cracked structural elements here Forman and Mettumethod is used. In this approach a low cyclic fatigue material properties are used. Computation procedure to strength analyze with respects to fracture mechanic and residual life estimations is applied to aircraft structural elements with surface cracks under load spectrum. Computation results are compared with correspond analytic experimental results.
Keywords: Fatigue,stress intensity factors, surface cracks, singular finite elements, fatigue life prediction
1. INTRODUCTION

Throughout their service life, aircraft are subjected to the combination of environmental attack and varying loads. The structural integrity of the vehicle can be impaired by surface degradation due to corrosive action or when crack damage is developed or aggravated by the environment. The requirement for lightweight aerospace structures leads to high design stresses [1]. High stresses can produce cracks early in the fatigue life of these structural components.Surface and corner cracks are encountered in engineering structures at locations where high stresses.Such cracks are present during a large percentage of the useful life of these components. Accurate stress intensity factors for such cracks are necessary for reliable prediction of fatigue crack growth rates or fracture. Three-dimensional (3-D) stress analysis of crack configurations have received considerable attention in the literature in the last three decades [2-4 ]. Various methods have been used to obtain stress-intensity factors for surface and corner cracks in plates: the alternating method [1,2], the finite-element method (FEM) with singularity elements [6], the finite element method with displacement hybrid elements and finite element alternating method. The slice synthesis method has also proved to be an accurate an inexpensive method to compute 3D stress intensity factor solutions [4-6]. The most accepted stress intensity factor solutions for surface cracks in finite thickness plates are obtained using FEM [3,4]; other methods are usually compared with FEM solutions to confirm their accuracy and convergence.

The methodology used here involves use the slice synthesis method that utilizes weight function technique. 
2. STRESS INTENSITY FACTORS OF SEMI-ELIPTIC SURFACE CRACK 

The slice synthesis approach used herein to computation of surface flaw stress intensities. The three dimensional surface flaw is idealized as a system of slices in the x-y plane, each containing a center crack whose length is determined by locations thru the thickness at which the slice was taken, Fig.2.1. Each slice is considered to react independently to the applied stress, (, but are coupled through the introduction of pressure distribution, p*, acting on the faces of the cracks. The pressure p*, is determined by second system of slices in the z-y plane. Each of the z-y slices contains an edge crack of depth a(x) over which the pressure, p*, acts in opposition to that applied to the center crack slices [5]. Thus there are two slice systems: center cracks, and edge cracks, Fig. 2.1.
	[image: image2.jpg]00

YA




	[image: image3.jpg]L@, | g
b g
! <
Z %Y
A }

1z

W1






Fig.2.1. Surface crack idealization

The weight function in this case was formulated in the same manner as that of Fujimoto [5].  Using the crack face pressure distributions, stress intensity factors at A and B can be determined as



[image: image4.wmf](

)

(

)

sp

==

=

åå

33

2

00

i

i

Aij

ij

ca

KaA

at


(1)


[image: image5.wmf](

)

(

)

sp

==

=

åå

33

2

00

i

i

Bij

ij

ca

KaB

at


(2)
where: KA is the stress intensity at depth; KB is the stress intensity at surface, ( -applied stress, a - crack depth, c - half surface length, 
[image: image6.wmf]t

-plate thicknes;
[image: image7.wmf]ij

A

 and 
[image: image8.wmf]ij

B

 are the coefficients (represent the displacements over the entire crack face, the continuity expression is evaluated at 13 points).

To validate the analytic computation procedure, finite element method is used. Three-dimensional finite elements were used to model a plate containing a semi-elliptic surface crack. The finite element analyses were made using MSC/NASTRAN [8].
3. NUMERICAL EXAMPLES
3.1. Finite element analysis for surface cracks 

To check validity of the above method for SIF evaluation by the semi-analytic slice synthesis approach, comparison between the calculated SIF results of surface cracks in plate and the solution obtained by finite elements are compared. For this purpose plate with semi-elliptic surface crack under tension ( = 83.3 [N/mm2] is analyzed. Geometry properties of this plate are: w=60 mm, t=10 mm, c=10 mm, a=10 mm, Fig.2.1. Three-dimensional singular finite elements were used to model of a plate containing a semi-elliptic surface cracks under tensile load. 
[image: image9.wmf]X

Y

Z

18.07

17.12

16.17

15.22

14.28

13.33

12.38

11.43

10.49

9.54

8.592

7.645

6.697

5.75

4.802

3.855

2.907

V1

L1

C1

G9

Output Set: 3D3

Deformed(0.057): Total Translation

Contour: Solid VonMises Stress


Fig.3.1.1. Detail finite element model of semi-elliptic crack
[image: image10.emf]0

10

20

30

40

0 10 20 30 40 50 60 70 80 90 100

q

 [ 

o 

]

K

I

Analytic solution

FEM


Fig.3.1.2. Comparisons between analytic and FE results for SIF calculations
Results presented in Fig. 3.1.2 give good agreement between presented computation analytic and finite element results for the stress intensity factors. The difference was found to be less than 6%.

3.2. Fatigue crack growth 
The stress-intensity factor equations (1) and (2) for surface cracks are used herein to predict fatigue-crack-growth patterns under load spectra, Fig. 2.1. For this purpose Forman and Mettu equation [7] is used. 



[image: image11.wmf](

)

D

æö

-

ç÷

D

èø

-

éù

=D

êú

-

ëû

æö

-

ç÷

èø

max

1

1

1

1

p

th

n

q

c

K

K

da

f

CK

dNR

K

K


(3)
where N is the number of applied fatigue cycles, a is the crack length, R is the stress ratio, (K is the stress intensity range, C, n, p and q are empirically derived constants, f is the crack opening function, (Kth is the threshold stress intensity factor and Kc is the fracture toughness.

3.2.1. Numerical validation

Crack growth analysis for the next geometric and material properties of structural component with semi-elliptic surface crack, Fig.2.1, are illustrated in Fig.3.2.1. 

depth of surface crack
a = .100E-02 [m],half-length of surface crack c = .100E-02 [m]

plate thickness

t = .200E-01 [m], width of cracked plate w = .200E-01 [m]

crack growth coef.
C = .300E-10, exponent n= .250E+01 

fracture toughness 
KIC = .500E+02 

Table 4.2.1. Load spectra

	Ni
	Smin [MPa]
	Smax [MPa]

	6000
	0
	500

	6000
	100
	400


Figure 3.2.1 shows results of crack growth analysis under load spectra. Curves denoted as Anal-A and Anal-B represent crack growths of points A and B (Fig.2.1) for semi-elliptic surface cracked structural element under tension load using analytic expressions for (1) and (2) stress intensity factor calculations with one side and Forman and Mettu equation (3).
Curve denoted with MKE-B represents crack growth at point B where SIF determined using approximate finite element results. Procedure for approximations of SIF from finite elements are presented in paper [4]. This procedure is based on determination of SIF using special 3-D finite elements for several successive crack length and defining analytic expression for SIF in polynomial form from these values. This method based on using 3-D special singular quarter-point singular finite elements for determination of SIF is very reliable method. If we compare crack growth in point B using analytic approach derived in previous considerations with finite element results (FEM-B) good agreement is evident. Good agreement between analytic computation method based on slice synthesis method with finite element approximations of SIF confirmate quality of presented analytic method in crack growth analyses. 

[image: image12.png]0,007

0008 i

Hn‘nm //
Eoons ot
® //?

0o02 f
0001 ./‘ﬁ T AeA

25617

——MKE-B

——Anal-B
001003 08+031 8041554042050 255104308+ D+
0001

N (ciklusa)





Fig.3.2.1. Surface crack growth under load spectra  

4. CONCLUSION

Stress intensity factor solutions for semi-elliptical surface cracks were determined using analytic model  and validation by comparisons with special singular finite element solutions. The slice synthesis approach is used herein to computation of surface flaw stress intensities. To validate the analytic derived stress intensity factors for semi-elliptic surface cracks, finite element method is used. The analytic results based on slice synthesis method were compared with finite element solutions and the difference was found to be less than 6% for surface points. Analytic model for the stress intensity factors, derived in this work, are used for crack growth analyses and fatigue life predictions. 

Acknowledgments: The authors would like to thank the Ministry of Education and Science of Serbia for financial support under the project number OI 174001 and TR 34028.
REFERENCES

[1] Broek,D.: (1989) The Practical Uses Of Fracture Mechanics, Kluwer Academic Publishers.
[2] Maksimović,S.,Vasović,I., Maksimović,M., Đurić,M. (2011). Residual Life Estimation of Damaged Structural Componentsusing Low-Cycle Fatigue Properties. Third Serbian (28th Yu) Congress on Theoretical and Applied Mechanics, Vlasina lake, Serbia, 5-8 July 2011; Serbian Society of Mechanics, Belgrade; ISBN: 978-86-909973-3-6; COBISS:SR-ID 187662860; 2011; pp.605 – 617.

[3] Blažić,M., Maksimović,K., Assoul,Y. (2011) Determination of Stress Intensity Factors of Structural Elements by Surface Cracks, Third Serbian Congress Theoretical and Applied Mechanics, Vlasina Lake, 5-8 July 2011, pp. 374-383,  Organized: Serbian Society of Mechanics, ISBN 978-86-909973-3-6, COBISS:SR-ID 187662860, 531/534(082). 

[4] Maksimovic,S., Maksimovic,K. (2012) Improved Computation Method  in Residual Life Estimation of Structural Components, Theoretical and Applied Mechanics, Special Issue – Adress to Mechanics, Vol. 40 (S1), 2012, pp. 223-246, doi: 10.2298/TAM12S1247M. (ISSN 1450-5584). 

[5] Fujimoto,W.T. (1976) Determination of Crack Growth and Fracture Toughness Parameters for Surface Flaws Emanating from Fastener Holes, MDC Report A4093, 17 March 1976, Presented at the AIAA; ASME/SAE 17th SDM Meeting, Valley Forge, Pa., 4-7 May 1976.

[6] Barsoum,R.S. (1977) Triangular Quarter-Point Elements as Elastic and Perfectly-Plastic Crack Tip Elements, Int. J. Numer. Meth. Engng., 11, pp. 85-98.
[7] Forman,R.G., Mettu.S.R. (1992) Behavior of Surface and Corner Cracks Subjected to Tensile and Bending Loads in Ti-6al-4v Alloy, Fracture Mechanics: Twenty-second Symposium, Vol.1, ASTM STP 1131, H.A.Ernst, A.Saxena, and D.L.McDowell, eds., American Society for Testing and Materials, Philadelphia,pp.519-546.

[8] Msc/NASTRAN software code - Theoretical Manuals.
� PhD Stevan Maksimović, Military Technical Institute, Belgrade, Serbia, � HYPERLINK "mailto:s.maksimovic@open.telekom.rs" ��s.maksimovic@open.telekom.rs�  


1 M.Sc Mirjana Đurić, Military Technical Institute, Belgrade, Serbia, � HYPERLINK "mailto:minadjuric12@gmail.com" �minadjuric12@gmail.com�


� PhD student Waterworks and Sewerage, Belgrade, Serbia, � HYPERLINK "mailto:maksimovic.mirko@gmail.com" ��maksimovic.mirko@gmail.com� 


� PhD student Institute GOSA, Milana Rakica 35, Belgrade, Serbia, � HYPERLINK "mailto:ivanavvasovic@gmail.com" ��ivanavvasovic@gmail.com� 





6
5

_1492928454.unknown

_1492928519.unknown

_1492928524.unknown

_1492929238.unknown

_1492928510.unknown

_1492928425.unknown

_1492926492.xls
Chart1

		0		0		0

		4950		3910		3910

		6000		6000		6000

		12000		12000		12000

		15100		14200		14200

		17700		16000		16000

		18000		17500		17500

		24000		18000		18000

		25900		22500		22500

		27500		24000		24000

		28900		25100		25100

		30000		26000		26000

		34200		26900		26900

		36000		27700		27700

		37000		28400		28400

		37900		29000		29000

		38800		29600		29600

		39600		30000		30000

		40300		31900		31900

		41000		33700		33700

		41600		35300		35300

		42000		36000		36000

		44100

		46100

		47900

		48000



Anal - A

MKE - B

Anal - B

N (ciklusa)

a (m)

0.001

0.001

0.001

0.0013

0.0013

0.0013

0.0014

0.0015

0.0015

0.0015

0.0017

0.0017

0.0018

0.002

0.0019

0.0021

0.0023

0.0022

0.0021

0.0025

0.0025

0.0023

0.0027

0.0026

0.0026

0.003

0.0029

0.0029

0.0031

0.003

0.0032

0.0034

0.0033

0.0034

0.0037

0.0036

0.0037

0.004

0.0038

0.0038

0.0042

0.0041

0.0041

0.0045

0.0044

0.0044

0.0048

0.0047

0.0047

0.0051

0.005

0.0049

0.0054

0.0051

0.0052

0.0054

0.0055

0.0057

0.0058

0.006

0.0059

0.0061

0.0062

0.0065

0.0068

0.0068



Sheet1

		a [m]		N (F15A)		N (F15B)		N (german

		0.001		0.00E+00		0.001		0.00E+00		0.001

		0.0013		4.95E+03		0.0013		3.91E+03		0.0013

		0.0014		6.00E+03		0.0015		6.00E+03		0.0015

		0.0015		1.20E+04		0.0017		1.20E+04		0.0017

		0.0018		1.51E+04		0.0019		1.42E+04		0.002

		0.0021		1.77E+04		0.0022		1.60E+04		0.0023

		0.0021		1.80E+04		0.0025		1.75E+04		0.0025

		0.0023		2.40E+04		0.0026		1.80E+04		0.0027

		0.0026		2.59E+04		0.0029		2.25E+04		0.003

		0.0029		2.75E+04		0.003		2.40E+04		0.0031

		0.0032		2.89E+04		0.0033		2.51E+04		0.0034

		0.0034		3.00E+04		0.0036		2.60E+04		0.0037

		0.0037		3.42E+04		0.0038		2.69E+04		0.004

		0.0038		3.60E+04		0.0041		2.77E+04		0.0042

		0.0041		3.70E+04		0.0044		2.84E+04		0.0045

		0.0044		3.79E+04		0.0047		2.90E+04		0.0048

		0.0047		3.88E+04		0.005		2.96E+04		0.0051

		0.0049		3.96E+04		0.0051		3.00E+04		0.0054

		0.0052		4.03E+04		0.0054		3.19E+04

		0.0055		4.10E+04		0.0057		3.37E+04

		0.0058		4.16E+04		0.006		3.53E+04

		0.0059		4.20E+04		0.0061		3.60E+04

		0.0062		4.41E+04

		0.0065		4.61E+04

		0.0068		4.79E+04

		0.0068		4.80E+04





Sheet1

		



Anal - A

MKE - B

Anal - B

N (ciklusa)

a (m)



Sheet2

		





Sheet3

		






