S. Boljanović, S. Maksimović, D. Stamenković
Fatigue strength simulation of aircraft lug

[image: image1.jpg]


[image: image20.emf]0

5

10

15

20

25

0 20 40 60 80 100

N [cycles] (x10

3

)

b [m]  

(x10

-3

)

Calculated curve (one crack)

Calculated curve (two cracks)

Experiment 1

Experiment 2


FATIGUE STRENGTH SIMULATION OF AIRCRAFT LUG 
Slobodanka Boljanović
, Stevan Maksimović
, Dragi Stamenković3
Summary: A computational models for the strength estimation of cracked aircraft lug are formulated. The crack growth propagation is investigated through the stress analysis and fatigue life calculation. The stress field around the crack tip and the stress intensity factor are evaluated by applying analytical approach. The fatigue life up to failure is simulated by employing two different crack growth laws. The estimations are compared with avaiable experimental data, and good correlation between different results are obtained.
Key words: fatigue, crack growth, aircraft lug, strength evaluation
1. INTRODUCTION 
The damage tolerance design of aerospace structures can be achieved if bearing loads are transfered through the lug-type joint. Such connection between the pin and lug represents potentional zone where high stress concentration, fretting, corrosion and material defects could cause the crack growth and even sudden failure. To ensure operational safety of a structure under cyclic loading, it is essentialy important to develop the reliable computational models.

Within the context of fracture mechanics, the complex propagation process has to be considered through adequate crack growth laws. Paris and Erdogan [1] found that the crack extension under cyclic loading can be desctibed by crack growth rate as a function of the stress intensity factor. Elber [2] introduced crack closure concept and took into account the effective stress intensity factor instead of the stress intensity factor. Further, Erdogan and Roberts [3] proposed the maximum stress intensity factor and the stress intensity factor range for the crack growth analysis. Walker [4] and later, Huang and Moan [5] recognized that the stress ratio together with the stress intensity factor range can be used to describe the crack propagation. 
From the engineering point of view, the complex stress field of pin-loaded lug configuration has to be considered through the stress intensity factor by applying different methods. Schijve and Hoemakers [6] proposed an empirical solutions for the stress intensity factor. Impellizeri and Rich [7] suggested to employ the weight function for analyzing through-the-thickness lug problems. Hsu [8] studied the same configurations by applying singular finite element method. Pian et al [9] suggested that the crack growth of through-the-thickness crack initiated in the lug can be investigated by using the hybrid finite element method.
In the present paper, the computational procedure for the fatigue life analysis of the pin-loaded lug with through-the-thickness crack emanating from a hole is developed. In the crack growth estimation, the stress analysis and the residual strength evaluation are considered. For the stress analysis analytical approach is employed. The predictive capability of proposed models is discussed through the adequate comparisons between crack growth evaluations and experimental data.
2. CRACK GROWTH SIMULATION UNDER CYCLIC LOADING
During exploatation of structural components, cyclic loadings with different levels can not be avoided. Complex fatigue process can often lead to unexpected failures of components. From the engineering point of view, the main issue is the evaluation of the reliable computational models while including the adequate loading parameters. The crack propagation of structural components can be investigated through the crack growth rate calculation and the fatigue life estimation.
The strength assessment of components can be realized through the adequate crack growth laws. The present authors theoretically investigated the propagation process of the lug with through-the-thicknes crack(s) by employing two different relationships for crack growth rates, the first one proposed by Huang and Moan [5] i.e.

[image: image2.wmf](

)

m

I

K

M

C

dN

da

D

=








(1)

where 
[image: image3.wmf](

)

b

-

-

=

R

M

1

for 
[image: image4.wmf]5

.

0

0

<

£

R


and then, the following relationship introduced by Erdogan and Roberts [3]:

[image: image5.wmf]I

ax

K

K

C

dN

da

D

=

2

Im

,






(2)
where KImax and (KI are the maximum stress intensity factor and stress intensity factor range, respectively, R denotes stress ratio and C, m and ( represent constants experimentally obtained. 
In the fatigue fracture analysis, the relationships for crack growth rates enable that the number of loading cycles up to failure can be computed. After integration Eqs.(1) and (2) the expressions for final number of loading cycles up to failure can be written as follows:

[image: image6.wmf](

)

(

)

ò

D

-

=

-

f

a

a

m

I

K

R

C

da

N

0

1

b

,





(3)


[image: image7.wmf]ò

D

=

f

a

a

I

ax

K

CK

da

N

0

2

Im

.






(4)
where a0 and af denote initial and final crack length, respectivelly.

The number of loading cycles up to failure is here estimated for adequte crack incements by applying two different crack growth laws where service cyclic loading conditions are taken into account through either stress ratio R or the maximum stress intensity factor KI max, respectively. Since the relationships for stress intensity factor are complex, relevant numerical methods related to the integration of complex functions are employed in developed computational model. 

3. STRESS INTENSITY FACTOR EVALUATION
Under cyclic loading the service life of engineering structures often can be reduced by cracks initiated in the zones of stress concentration or manufacturing defects. In order to ensure the safety design and exploatation, the crack propagation process has to be investigated through the stress inensity factor calculation. Such fracture parameter includes external loading, geometry and material of the structural component, and for the lug with through-the-thickness crack(s) emanating from a hole (Fig.1) it can be expressed as follows [10, 11]:

[image: image8.wmf]n

n

wn

G

w

D

f

f

a

S

K

÷

ø

ö

ç

è

æ

D

=

D

2

cos

1

p

p







(5)
where (S is the stress range, a presents the crack length, D denotes diameter of the hole of the lug and w is width of the lug.
The Bowie correction can be expressed by fn (n = 1 for single crack and n = 2 for two-symmetric cracks) on the following way [12]: 

[image: image9.wmf]ï

î

ï

í

ì

=

+

-

+

-

=

+

-

+

-

=

2

;

52

.

3

47

.

4

46

.

3

15

.

0

0

.

1

1

;

85

.

6

54

.

10

55

.

6

18

.

0

707

.

0

4

3

2

4

3

2

n

n

f

n

l

l

l

l

l

l

l

l





(6)

where

[image: image10.wmf]D

a

2

1

1

+

=

l










(7)
The pin-loaded effect is included through the correction factor Gn given by:

[image: image11.wmf](

)

(

)

ï

ï

î

ï

ï

í

ì

=

+

+

=

+

+

+

=

2

;

2

2

1

1

;

2

2

1

n

a

D

w

n

a

D

D

a

D

w

G

n

p

p







(8)
The finite-width correction factor fwn can be calculated by employing the following relationship:
             
[image: image12.wmf]÷

÷

ø

ö

ç

ç

è

æ

+

-

+

=

na

b

w

na

D

f

wn

2

2

cos

1

p








(9) 
[image: image13.jpg]S [M Pa)

o &
f——
——





Fig. 1 Geometry of the lug with through-the-thickness crack.
4. NUMERICAL RESULTS 
The efficiency of the proposed mathematical models for residual strength analysis of the lug with through-the-thickness crack(s) is considered through a few numerical examples. In such examples, the fatigue life up to failure is estimated by employing two different crack laws. 
Example 4.1 The strength estimation of the lug with through-the-thickness crack(s)
The first example examines the residual life simulation of the lug with one crack and two-symmetric cracks emanating from a hole (Fig.1). Geometry sizes of the lug, made of 7075 T6, are as follows: a0=0.635 mm, t=12.7 mm D=38.1 mm [13]. The fatigue evaluations are performed for two different width of lug w (114.3 mm, 85.72 mm). The strength of considered lug configurations is investigated under axial cyclic loading with constant amplitude (a far field maximum gross stress Smax=41.38 MPa, R=0.5), and the following material parameters are assumed: CB=2.55*10-10, mB=3.06 [14].
According to the mentioned geometries, material and loading parameters, the strength of lug is evaluated through the stress intensity factor calculation by applying appropriate relationships (Eqs (5)-(9)) for either single crack or two-symmetric cracks. 
[image: image14.emf]0

5

10

15

20

25

0 5 10 15 20 25

N [cycles] (x10

3

)

b [m]  

(x10

-3

)

Calculated curve (one crack)

Calculated curve (two cracks)

[image: image15.emf]0

5

10

15

20

25

0 5 10 15 20 25

N [cycles] (x10

3

)

b [m]  

(x10

-3

)

Calculated curve (one crack)

Calculated curve (two cracks)


   (a)




      (b)

[image: image16.jpg]T |

>t
’ (tosed)D-0

.
° (19s82)D-0




Fig. 2 Crack length versus number of loading cycles (by using Eqs.(3) and (5)-(9)).[image: image17.emf]0

5

10

15

20

25

0 20 40 60 80 100

N [cycles] (x10

3

)

b [m]  

(x10

-3

)

Calculated curve (one crack)

Calculated curve (two cracks)

Experiment 1

Experiment 2


    (a)




      (b)
Fig. 3 Crack length versus number of loading cycles (by using Eqs.(4) and (5)-(9)).

Experiment for the lug with one crack from Ref.[13]:
 (a) w = 114.3 mm, 1 - ABPLC84, 2 - ABPLC91; 
(b) w = 85.72 mm, 1 – ABPLC47, 2 – ABPLC94.

Since two different crack growth laws are considered, the residual life up to failure is computed using either Eq.(3) or Eq. (4) together with Eqs.(5)-(9). Obtained results for the number of loading cycles versus crack length by employing Huang and Moan, and Broek's crack growth laws are presented in Fig.2 and Fig.3, respectively.
At the same Figures, all computed results for fatigue life up to failure are compared with experimental data. The comparison between different results shows a good agreement. Additionally from Fig.2 and Fig.3 it can be also deducted that the crack growth law expressed by Eq.(3) is slightly conservative than that one presented by Eq.(4) when compared to experimental results.     
Example 4.2 The residual life calculation of the lug under spectrum loading 

 This section considers the evaluation of the number of loading blocks up to failure. The considered lugs with either single crack or two-symmetric cracks (Fig.1) have the following geometry parameters: a0=1.25 mm, w=80 mm, D=35 mm, t=10 mm. External spectrum loading (Fig.4) is axial with three different stress levels. The values of loading levels are shown in Table 1. The considered plate is made of the same material as in the previous one.
Table 1 Maximum gross stress and appropriate number of loading cycles for considered load spectra.
	Load level
	I
	II
	III
	IV
	V
	VI

	Smax [MPa]
	28.75
	47.50
	75.00
	55.00
	43.75
	22.50

	ni [cycles]
	100
	70
	10
	50
	30
	200



The strength of lug with through-the-thickness crack(s) under spectrum loading includes the stress intensity factor calculation and the crack growth rate simulation. Since the propagation process is investigated through two different crack growth laws, the number of loading blocks up to failure is estimated either by applying Eq. (3) or Eq. (4) together with Eqs (5)-(9). For both lug configurations, the computed number of loading blocks against the crack length is shown in Fig.5a and Fig.5b by using as a crack growth law, Eq. (3) or Eq. (4), respectively.

[image: image18.emf]0

5

10

15

20

25

30

35

0 20 40 60 80 100 120 140

N [cycles] (x10

3

)

b [m]  

(x10

-3

)

Calculated curve (one crack)

Calculated curve (two cracks)

Experiment 1

Experiment 2

[image: image19.emf]0

5

10

15

20

25

30

35

0 20 40 60 80 100 120 140

N [cycles] (x10

3

)

b [m]  

(x10

-3

)

Calculated curve (one crack)

Calculated curve (two cracks)

Experiment 1

Experiment 2


    (a)



(b)
Fig. 4 Load Spectra. 

Fig. 5 Crack length versus number of loading blocks.
The comparison presented in Fig.5 implies that developed computational model based on the crack growth law expressed by Eq.(1) gives sligthly lower number of loading blocks up to failure than the one where Eq.(2) is employed.  
5. CONCLUSION 
The residual strength under cyclic loading of the lug with through-the-thickness crack is theoretically simulated. The crack propagation process is investigated through two different crack growth laws, and the stress intensity factor is calculated by employing analytical approach. The proposed models are verified by comparison with fatigue crack growth data. The implementation of Huang and Moan crack growth law gives slightly conservative fatigue evaluations than the one proposed by Erdogan and Roberts. Good agreement between computed results and experimental data shows that mathematical models are applicable in engineering practice for the reliable strength estimation of the lug with through-the-thickness cracks.
ACKNOWLEDGMENT
This research work is financially supported within the project No. OI 174001 (Mathematical Institute – The Serbian Academy of Sciences and Arts, Belgrade) by the Ministry of Science and Technological Development, Serbia.

LITERATURE
[1] Paris, P.C., Erdogan, F.A. (1963). A critical analysis of crack propagation laws. J Dasic Eng Trans SME, Series D, vol.55, p.528-534.

[2] Elber, W. (1971). The significance of fatigue crack closure. In: Damage tolerance in aircraft structure. ASTM STR 486, p.230-242.

[3] Erdogan, F., Roberts, R. (1965). A comparative study of crack propagation in plates under extension and bending. In: Proc int conf on fracture, Sendai, Japan.
[4] Walker, E.K. (1970). The effect of stress ratio during crack propagation and fatigue for 2024-T3 and 7076-T6 aluminum. In: Effect of environment and complex load history on fatigue life. ASTM STR 462, p.1-4.

[5] Huang, X., Moan T. (2007). Improved modeling of the effect of R-ratio on crack growth rate. Int J Fatigue, p.591-602.
[6] Schijve, J., Hoeymakers, A.H.W. (1979). Fatigue crack growth in lugs. Fatigue of Engineering Materials and Structures, vol.1, p.185-201.

[7] Impellizeri, L.F., Rich, D.L. (1976). Spectrum fatigue crack growth in lugs. In: Fatigue crack growth under spectrum loads. ASTM STP 595, p.320-336.
[8] Hsu, T.M. (1980). Analysis of cracks at attachment lugs. 21st AIAA/ASME/ASCE/AHS Structures, Struct. Dynamics Materials Conf. Seattle Washington.
[9] Pian, T.H.H., Mar, J.W., Orringer, O., Stalk, G. (1976). Numerical computation of stress intensity factors for aircraft structural details by the finite element method. AFFDL-TR-76-12.
[10]  Newman, Jr J.C. (1973). Fracture analysis of surface and through-cracked sheets and plates. Eng Fract Mech, vol.5, p.667-689.
[11] Boljanović, S., Maksimović, S. (2014). Fatigue crack growth modeling of attachment lugs. Int J of Fatigue, vol.58, p.66-74.
[12] Bowie, O.L. (1956). Analysis of an infinite plate containing radial cracks originating at the boundary of an internal circular hole. J Math. & Phys, vol. 35, p.60-71
[13] Kathiresan, K., Brussat, T.R. (1984). Advanced life analysis methods. AFWL-TR-84-3080, OH.
[14]  Flech, W.G., Anderson, R.B. (1969). A mechanical model of fatigue crack propagation. In: Pratt, P.L. ed. Proc of the second international conference on fracture, Brigthon, London, Chapman & Hall.
HERE WILL BE LOGO








� Ph.D, Slobodanka Boljanović, Belgrade, Mathematical Institute – The Serbian Academy of Sciences and Arts, Kneza Mihaila 36, (slobodanka.boljanovic@gmail.com)


� Ph.D, Stevan Maksimović, Belgrade, VTI, Ratka Resanovića 1, (s.maksimovic@open.telekom.rs)


3 Ph.D, Dragi Stamenković, Belgrade, Termoelektro, (dragi33@gmail.com)








2
5

_1491233226.unknown

_1491233695.unknown

_1491394092.unknown

_1491394104.unknown

_1491394122.unknown

_1491394079.unknown

_1491233623.unknown

_1491233095.unknown

_1491233154.unknown

_1491233017.unknown

_1491044069.unknown

