УТИЦАЈ УСЛОВА ПРОИЗВОДЊЕ НА ТОПЛОТНА СВОЈСТВА ПЕНАСТИХ ВИНИЛНИХ ПОДОВА
Рајко Радовановић1, Мирјана Јовичић2, Оскар Бера2, Јелена Павличевић2, Тања Радусин3, Невена Вукић2, Бранка Пилић2
1OOO JUTEKS RU, Kameškovo, Rusija, Rajko.Radovanovic@bintg.com
2Технолошки факултет Нови Сад, Универзитет у Новом Саду, Србија
3Институт за Прехрамбене Технологије, Универзитет у Новом Саду, Србија
Пенасти полимерни производи се састоје од великог броја релативно малих гасом испуњених ћелија. Поливинилхлорид (ПВЦ) је један од најчешће коришћених материјала за добијање пенастих производа. Ћелијска структура ПВЦ пене одређује својства, а самим тим и могућност примене готових производа. У овом раду изучаван је утицај услова производње (температуре пластификације (у опсегу 188-192 °C) и времена пењења (у опсегу 90-150 секунди)) на топлотна својства винилних подова. Термичка стабилност добијених узораka је испитивана помоћу термогравиметријске анализе. Мерења су рађена у температурном опсегу од собне температуре до 700 °C, при брзини загревања од 10 °C/min, у атмосфери азота. Са порастом температуре и времена пењења, топлотна деградација испитиваних ПВЦ композита започиње на нижим температурама и средња температура максималне брзине секундарног степена деградације је смањена, што значи да је потребно више енергије да се раскину угљоводоничне везе у основном ланцу у полимерној матрици. С друге стране, средња температура максималне брзине првог степена деградације ПВЦ је смањена, што је последица почетка издвајања хлора из основног ланца. За све испитиване узорке маса остатка на 700 °C је мања од 38 мас.%.

Кључне речи: пенасти винилни подови, термогравиметријска анализа, термичка својства 
EFFECTS OF PROCESSING CONDITIONS ON THE THERMAL PROPERTIES OF VINYL FOAM FLOORING
Rajko Radovanović1, Mirjana Jovičić2, Oskar Bera2, Jelena Pavličević2, Tanja Radusin3, Nevena Vukić2, Branka Pilić2

1OOO JUTEKS RU, Kameshkovo, Russia, Rajko.Radovanovic@bintg.com
2Faculty of Technology Novi Sad, University of Novi Sad, Serbia, jovicic.mirjana@gmail.com
3Institute of Food Technology, University of Novi Sad, Serbia

Foamed polymeric products consist of a large number of relatively small gas-filled cells. Polyvinyl chloride (PVC) is one of the most commonly used materials for the preparation of foam products. The cellular structure of the PVC foam determines its properties, performances and applications. In this study, the effect of processing condition (temperature of blowing (in the stabile range of 188-192 °C) and blowing time (in the range of 90-150 s)) on thermal properties of PVC foam were investigated. Thermal properties of the foam composites were measured using thermogravimetric analysis, in the temperature range from room temperature to 700 °C, at a heating rate of 10 °C/min, under nitrogen atmosphere. Increasing temperature and time of the blowing, thermal degradation starts at lower temperatures and the temperature of composites secondary decomposition is decreased, causing more energy to break the hydrocarbon backbone of the polymer matrix. On the other hand, the primary degradation temperature of the composites, which indicates the start of the chlorine separation process from the polymer chains, decreases slightly by increasing temperature and time of the blowing. For all samples, residual weight at 700 °C is less than 38 wt. %.
Key words: vinyl foam flooring, thermogravimetric analysis, thermal properties 
