УТИЦАЈ ДОДАТКА ОРГАНСКИ МОДИФИКОВАНОГ МОНТМОРИЛОНИТА НА КИНЕТИКУ УМРЕЖАВАЊА СМЕШЕ ЕПОКСИ/JEFFAMINE D-400
Мирјана Јовичић, Јелена Павличевић, Оскар Бера, Весна Теофиловић, Милан Асурџић, Радмила Радичевић 
Технолошки факултет Нови Сад, Универзитет у Новом Саду, Србија, jovicic.mirjana@gmail.com
Побољшање термичке стабилности и механичких својстава смеша епоксид /амин може се постићи додавањем органски модификованог монтморилонита (ММТ). У зависности од природе органских јона уметнутих у слојеве глине, модификовани ММТ може да катализује реакцију умрежавања, реагује са предполимером или умреживачем. Хибриди са епоксидном матрицом и са различитим уделом монтморилонита су припремљени in situ поступком тако што је прво монтморилонит умешаван у епоксид  на температури од 45 °C у ултразвучном купатилу. Потом је додат умреживач Jeffamine D-400 у смешу. Припремљени су узорци са 0, 3, 5 и 10 мас.% монтморилонита у односу на укупну масу смеше епоксид/Jeffamin D-400. Умрежавање је вођено у диференцијалном сканирајућем калориметру (ДСЦ) у динамичком режиму, при три различите брзине загревања: 5, 10 и 20 °C/min. На основу добијених резултата, може се закључити да поред тога што се са порастом удела монтморилонита (од 0 до 10 мас.%) у реакционој смеши реакција помера на ниже температуре, мења се и облик ДСЦ криви, на основу чега се може претпоставити да се мењају и кинетички параметри, тј. сам механизам умрежавања.
Кључне речи: епоксидни нанокомпозити, органски модификован монтморилонит, кинетика умрежавања
THE EFFECT OF ORGANICALLY MODIFIED MONTMORILLONITE ADDITION ON THE CURING KINETICS OF EPOXY/JEFFAMINE D-400 SYSTEMS
Mirjana Jovičić, Jelena Pavličević, Oskar Bera, Vesna Teofilović, Milan Asurdžić, Radmila Radičević
Faculty of Technology Novi Sad, University of Novi Sad, Serbia, jovicic.mirjana@gmail.com
Improvement of thermal stability and mechanical properties of an epoxy/amine system can be achieved by addition of organically modified montmorillonite (MMT). Depending on the nature of the organic ions intercalated in the interface, the modified MMT can catalyze curing reaction, or react with prepolymer or crosslinking agent. Epoxy hybrids with different montmorillonite were prepared using in-situ procedure. In the first step, montmorillonite was added to epoxy, and the mixing was performed in ultrasound bath at 45 °C. Then, crosslinking agent Jeffamine D-400 was added to the mixture. A series of epoxy/Jeffamine D-400 samples with different montmorillonite content (0, 3, 5 and 10 wt. %) were prepared. The curing of obtained modified systems was carried out by differential scanning calorimetry (DSC), using dynamic regime at three different heating rates: 5, 10 and 20 °C/min. According to the obtained DSC data, it can be noticed that the temperature of maximum curing rate was decreased by increasing montmorillonite content, followed by the change of DSC curves shape. Based on obtained values for kinetic parameters, it is determined that MMT presence affects the mechanism and curing kinetics of epoxy/amine systems.
Key world: epoxy nanocomposites, organically modified montmorillonite, curing kinetics
