STUDY OF PHOTODIELECTRICAL PROPERTIES AND TEMPERATURE CONDUCTIVE COEFFICIENTS OF POLYESTER FABRICS

B. Škipina1*, D. Grujić1, A.S. Luyt2 and D. Dudić3,4

1Faculty of Technology, University of Banja Luka, Vojvode Stepe Stepanovića 73, 78 000 Banja Luka, Bosnia and Herzegovina, blanka.skipina@unibl.rs, dragana.grujic@unibl.rs

2Center for Advanced Materials, Qatar University, PO Box 2713, Doha, Qatar, aluyt@qu.edu.qa

3Vinča Institute of Nuclear Sciences, University of Belgrade, P.O. Box 522, 11001 Belgrade, Serbia, ddudic@outlook.com

4Department of Chemistry, University of the Free State, Private Bag X13, 9866 Phuthaditjhaba, South Africa

In this paper, we report surface dielectric and photodielectric properties of polyester sheet for photo cell application under standard conditions (t=22 ⁰C and RH=60%). At 750 Hz surface dielectric conductanse and susceptanse of polyester have been found 2,34∙10-10 S and 1,70∙10-9 S respectively. We were found increase of conductance and susceptance with increasing of frequency. The results showed that there were pronounced contact relaxation effects at interface between alumina electrode and sample, which falls by about 60% from its initial value about 10 min after beginning of the experiment carried out in the dark. Furthermore, the surface dielectric conductance and susceptance of polyester sample increased during UV-Vis radiation. The temperature coefficients of conductance (TCCG) and susceptance (TCCB) of the polyester sample at various frequencies were also studied.

Key words: Dielectric Properties, Photodielectric Properties; Temperature Conductive Coefficient; Polyester Fabrics

FOTODIELEKTRIČNE OSOBINE I PROVODNI TEMPERATURSKI KOEFICIJENTI POLESTERSKOG VLAKNA

B. Škipina1*, D. Grujić1, A.S. Luyt2 and D. Dudić3,4

1Tehnološki fakultet, Univerzitet u Banjoj Luci, blanka.skipina@unibl.rs, dragana.grujic@unibl.rs

2Center for Advanced Materials, Qatar University, PO Box 2713, Doha, Qatar, aluyt@qu.edu.qa

3Institut za nuklearne nauke Vinča, Univerzitet u Beogradu, ddudic@outlook.com

4Department of Chemistry, University of the Free State, South Africa

U ovom radu, predstavili smo specifična površinska dielektrična i fotodielektrična svojstva poliesterske tkanine namijenjene za primjenu u oblasti foto ćelija. Mjerenja su vršena u standardnim uslovima (t = 22 ⁰C i RH = 60%). Vrijednosti površinske konduktanse i susceptanse na frekvenciji od 750 Hz su 2,34∙10-10 S i 1,70∙10-9 S, respektivno. Uočili smo porast konduktanse i susceptanse sa porastom frekvencije. Rezultati su pokazali izražene kontaktne relaksacije na granici između aluminijumske elektrode i uzorka, tj. dielektrične veličine opadaju i do 60% od početne vrijednosti oko 10 minuta nakon početka eksperimenta u mraku. Vrijednosti specifične površinske konduktanse i susceptanse rastu u toku UV-VIS zračenja. Analizirali smo i provodne temperaturske koeficijente (TCCG i TCCB) na različitim frekvencijama.

Ključne riječi: Dielektrična svojstva, Fotodielektrična svojstva; Provodni temperaturski koeficijenti; Poliester tkanina