Међународни научни скуп Савремени материјали –  Бања Лука.

International Scientific Conference Contemporary Materials – Banja Luka 

УПОТРЕБА КРАТКИХ ВЛАКАНА ЛАНА ЗА СОРПЦИЈУ ХРОМА (Cr)
Свјетлана Јањић1, Биљана Лазић2, Мирјана Костић3
[image: image1.emf]1Универзитет у Бањој Луци, Технолошки факултет, Војводe Степе Степановића 73, 78000 Бања Лука, Република Српска, БиХ, e-mail: svjetlana.janjic@unibl.rs
2 Институт за јавно здравство Републике Српске, Јована Дучића 1, 78000 Бања Лука, Република Српска, БиХ, e-mail: biljanalazic@yahoo.com
3Универзитет у Београду, Технолошко-металуршки факултет, Карнегијева 4, 11000 Београд, Србија, e-mail: kostic@tmf.bg.ac.rs 

Сажетак: Загађење животне средине тешким металима је резултат повећане употребе метала и хемикалија за индустријске процесе и неконтролисаних испуштања токсичних супстанци у непосредно окружењe, посебно водене изворе. Уклањање тешких метала из различитих отпадних вода је стални предмет интересовања бројних истраживача у свијету. Биосорпција се процјењује као безбједна, ефикасна и економична метода за елиминацију тешких метала из контаминираних вода. Циљ овог истраживања је био да се испитају сорпциона својства нетретираних ланених влакана и ланених влакана третираних водоник пероксидом (H2O2) према јонима хрома из водених раствора. Почетне концентрације Cr у раствору су биле 10 mg/L и 20 mg/L. Резултати су показали да третирање ланених влакана са H2O2 значајно повећава сорпциони капацитет влакана према Cr јонима када је почетна концентрација Cr јона у раствору 20 mg/L.
Кључне ријечи: ланена влакна, биосорпција, хром, екологија
USING SHORT flax fibres FOR SORPTION OF CHROMIUM (Cr)
Svjetlana Janjić1, Biljana Lazić2, Mirjana Kostić3
1University of Banja Luka, Faculty of Technology, Vojvode Stepe Stepanovica 73, 78 000 Banja Luka, Republic of Srpska, Bosnia and Herzegovina, e-mail: svjetlana.janjic@unibl.rs
2Public Health Institute, Jovana Ducica 1, 78 000 Banja Luka, Republic of Srpska, Bosnia and Herzegovina, e-mail: biljanalazic@yahoo.com
3University of Belgrade, Faculty of Technology and Metallurgy, Karnegijeva 4, 11 000 Belgrade, Serbia, e-mail: kostic@tmf.bg.ac.rs

Abstract: The pollution of the environment with heavy metals is a result of increased use of metals and chemicals for the industrial processes and uncontrolled discharges of toxic substances in the immediate environment, especially water sources. The removal of heavy metals from various effluents is a constant subject of interest of many researchers in the world. Biosorption is estimated as safe, effective and economical method for the elimination of heavy metals from contaminated waters. The aim of this research was to examine the sorption properties of untreated flax fibres and flax fibres treated with hydrogen peroxide (H2O2) towards Cr ion from aqueous solution. Initial concentrations of Cr in the solution were 10 mg/L and 20 mg/L. The results showed that treating flax fibres with H2O2 significantly increases the sorption capacity of fibres towards Cr ion when initial concentrations of Cr ion in the solution is 20 mg/L.
Keywords: flax fibres, biosorption, chromium, ecology

