XI SAVJETOVANJE HEMIČARA, TEHNOLOGA I EKOLOGA REPUBLIKE SRPSKE

XI Conference of  Chemists, Technologists and Environmentalists of Republic of Srpska


EFFECT OF AUSTENITIZATION AT 920 OC ON THE MECHANICAL PROPERTIES AND MICROSTRUCTURE 
OF MICROALLOYED STEEL 

*Mirko Gojić1, Gorazd Kosec2,  Franc Vodopivec3, Stjepan Kožuh1, Jelena Vojvodič Tuma3, Aleš Nagode4, Borut Kosec4

1University of Zagreb, Faculty of Metallugy, Aleja narodnih heroja 3, 44103 Sisak, Croatia, *gojic@simet.hr, kozuh@simet.hr 
2ACRONI d.o.o.,c. Borisa Kidriča 44, 4270  Jesenice, Slovenia, gorazd.kosec@acroni.si 
3Institute of  Metals and Technology, Lepi pot 11, 1000 Ljubljana, Slovenia, franc.vodopivec@imt.si, jelena.tuma@imt.si 
4University of Ljubljana, Faculty of  Natural Sciences and Engineering, Aškerčeva cesta 12, 1000 Ljubljana, Slovenia, borut.kosec@omm.ntf.uni-lj.si, ales.nagode@omm.ntf.uni-lj.si 
Abstract
In this paper the effect of heat treatment on mechanical properties and microstructure for microalloyed high-strength low-alloy (HSLA) steel is investigated. Austenitization of the steel samples was performed at 920 oC for 15 minutes. After austenitization the quenching procedure was carried out in both, hot water (at 70 °C) and lead bath at 400 oC, following by cooling on air. Tensile strength, hardness and Charpy impact energy are tested. Microstructural analysis was carried out using optical and scanning electron microscopy. Values of tensile strength were in the range from 1160 to 1824 MPa, while values of hardness were in the range from 205 to 282 HV. The microstructure of base material consisted of acicular ferrite and degenerated pearlite. The quenching in water from 920 oC produced a coarse microstructure with platelets of ferrite and lath primary martensite. The cooling in lead bath from 920 oC to 400 oC produced microstructure consisted from ferrite and bainite. 
Keywords: microalloed steel, heat treatment, mechanical properties, microstructure

