Gordana Bogdanović, Vladimir Geroski, Aleksandar Radaković, Dragan Čukanović, Dragan Milosavljević
failure stress analysis of fiber reinforced composite laminates


FAILURE STRESS ANALYSIS OF FIBER REINFORCED COMPOSITE LAMINATES
Gordana Bogdanović
, Vladimir Geroski
, Aleksandar Radaković
, Dragan Čukanović
, Dragan Milosavljević

Summary: The target materials of this paper are failure analysis of fiber reinforced composite laminates. Laminates are constituted of successive layers of lamina, whose layers can differ in constituents and the orientation of the fiber. In order to study the mechanical behavior of materials, it is necessary to determine the stiffness matrix. Constitutive relations are determined by classical lamination theory of first order. Then, the composite material is applied to the failure criteria, to determine whether failure occurs in a lamina. Due to the lack of maximum stress criterion, there is no interaction between the stress components, and therefore Tsai - Hill failure criterion was applied for composite laminates. In this paper the results are presented for several materials, different sequence numbers and loads.
Key words: composite materials, classical laminate theory, failure criterion
1. INTRODUCTION

2. CLASSICAL LAMINATION THEORY 

The most applied method for composite laminate analysis is classical lamination theory, first of all because of its simplicity. This theory made some kinematic assumptions about stress and strain, so three dimensional problem can be analyzed as a plane problem. Limitations of this theory are assumptions that layers are connected perfectly (there is no sliding between two layers), material of every lamina  must be orthotropic and linearly-elastic, layers have the same thickness, stress and strain are very small, laminates have plane stress, there is no deformation in veritical axis of laminate, displacements in laminate plane are linear function of coordinates (Kirchhoff assumption). Displacements (Fig. 1) in the plane of laminate are given as [1], [2], [3]:



[image: image2.wmf]000

,,

ww

uuzvvzww

xy

¶¶

=-=-=

¶¶

 
 MACROBUTTON MTPlaceRef \* MERGEFORMAT (2.1)

[image: image3.jpg]



Fig. 1 Plate deformation in the classical laminate theory
The deformation of the normal to the middle plane (Oxy) is a straight segment normal to the deformed middle plane. Strain field can be written as:



[image: image4.wmf]2

0

2

2

0

2

222

0

00

2

xx

yy

xyxy

u

uw

z

xxx

v

vw

z

yyy

uv

www

zzz

yxyxxyxy

e

e

gg

¶

¶¶

==-

¶¶¶

¶

¶¶

==-

¶¶¶

¶¶

¶¶¶

=+--=-

¶¶¶¶¶¶¶¶

 
 MACROBUTTON MTPlaceRef \* MERGEFORMAT (2.2)

Components of strain 
[image: image5.wmf]yzxz

,,

zz

egg

 are all equal to zero. The strain field is superposition of in-plane strains:



[image: image6.wmf](

)

(

)

(

)

0

0

0

0

0

00

xx

yy

xy

u

x

v

y

uu

yy

e

e

g

ìü

¶

ïï

¶

ìü

ïï

ïï

ïï

¶

ïï

=

íýíý

¶

ïïïï

ïï

ïï

îþ

¶¶

+

ïï

¶¶

îþ

 
 MACROBUTTON MTPlaceRef \* MERGEFORMAT (2.3)

and flexural strains (bending and twisting strains):



[image: image7.wmf](

)

(

)

(

)

2

2

2

2

2

2

f

xx

f

yy

f

xy

w

z

x

w

z

y

w

z

xy

e

e

g

ìü

¶

-

ïï

¶

ìü

ïï

ïï

ïï

¶

ïï

=-

íýíý

¶

ïïïï

ïï

ïï

îþ

¶

-

ïï

¶¶

îþ

 
 MACROBUTTON MTPlaceRef \* MERGEFORMAT (2.4)
 
Stress for layer 
[image: image8.wmf]1

:   

kk

khzh

-

££

 can be written as:


[image: image9.wmf](

)

(

)

(

)

(

)

(

)

0

111216111216

0

22262226

0

6666

QQQQQQ

QQQQ

.Q.Q

22

kk

kk

k

f

xxxx

xx

f

yyyyyy

f

xy

xyxy

symsym

ee

s

see

s

ee

ìüìü

éùéù

ìü

ïïïï

êúêú

ïï

ïïïï

=+

êúêú

íýíýíý

êúêú

ïïïïïï

êúêú

ïïïï

îþ

ëûëû

îþîþ

 
 MACROBUTTON MTPlaceRef \* MERGEFORMAT (2.5)

The reduced stiffness matrix 
[image: image10.wmf](

)

k

Q

 changes from one layer to another. Because of this, there is a discontinuity in the in-plane stress field between successive layers.

2.1 Resultants and Moments
The field of in-plane resultants (Fig. 2 left), denoted by 
[image: image11.wmf](

)

,

xy

N

, is defined as:


[image: image12.wmf](

)

2

2

,

xxxx

h

yyyy

h

xyxy

N

xyNdz

N

s

s

s

-

ìüìü

ïïïï

==

íýíý

ïïïï

îþîþ

ò

N

 
 MACROBUTTON MTPlaceRef \* MERGEFORMAT (2.6)

The components 
[image: image13.wmf],,

xxyyxy

NNN

 are the in-plane resultants, per unit length of the plate, of the normal stresses and of the shear stress in the plane, respectively. The discontinuity of the stresses from one layer to another leads to rewriting (2.6) in the form:


[image: image14.wmf](

)

(

)

1

1

,

k

k

k

xxxx

n

h

yyyy

h

k

xyxy

N

xyNdz

N

s

s

s

-

=

ìüìü

ïïïï

==

íýíý

ïïïï

îþîþ

å

ò

N

 
 MACROBUTTON MTPlaceRef \* MERGEFORMAT (2.7)

[image: image15.png]>V




                     [image: image16.png]



Fig. 2 (left) Resultants loads applied to a laminate element; (right)Resultant moments applied to a laminate element
Moments are given as:


[image: image17.wmf](

)

1

2

1

2

(x,y)zd

k

k

k

xxxxxx

h

h

n

yyyyyy

k

hh

xyxyxy

M

Mzdzz

M

ss

ss

ss

-

=

-

ìüìüìü

ïïïïïï

===

íýíýíý

ïïïïïï

îþîþîþ

å

òò

M

 
 MACROBUTTON MTPlaceRef \* MERGEFORMAT (2.8)

The constitutive equation of a laminated plate expresses the resultants and the moments as functions of the in-plane strains and of the curvatures. 
It has form:



[image: image18.wmf]0

111216111216

0

2226122226

0

66162666

111216

2226

66

AAABBB

AABBB

ABBB

DDD

.DD

D

xx

xx

yy

yy

xy

xy

xx

xx

yy

yy

xy

xy

N

N

N

M

k

sym

M

k

M

k

e

e

e

ìü

ìü

éù

ïï

ïï

êú

ïï

ïï

êú

ïï

ïï

êú

ïïïï

=

íýíý

êú

ïïïï

êú

ïïïï

êú

ïïïï

êú

ëû

ïïïï

îþ

îþ

 
 MACROBUTTON MTPlaceRef \* MERGEFORMAT (2.9)

or in compact form:



[image: image19.wmf]0

ìü

ìü

éù

=

íýíý

êú

îþ

ëû

îþ

NAB

ε

MBD

k

 
 MACROBUTTON MTPlaceRef \* MERGEFORMAT (2.10)

where 
[image: image20.wmf](

)

(

)

1

1

Q

n

k

kk

k

hh

-

=

=-

å

A

 ; 
[image: image21.wmf](

)

(

)

22

1

1

1

Q

2

n

k

kk

k

hh

-

=

=-

å

B

; and 
[image: image22.wmf](

)

(

)

33

1

1

1

Q

3

n

k

kk

k

hh

-

=

=-

å

D

. Integration and discusion of previous constitutive equation in detail is given in [1]. 
3.  FAILURE CRITERIA
The objective of the failure criteria is to allow the designer to have an evaluation of the mechanical strength of laminates. The definition of failure may change from one application to another. In the case of composite materials, the end of the elastic domain is generally associated with the development of microcracking: matrix microcracking, fibre-matrix debonding, etc. In the initial stage of fracture process, the initiated microcracks do not propagate, and their development changes the stiffness of the material very gradually. Failure criteria has been established in the case of a single layer of a laminate. Detailed discussion is given in [1] and [2].
3.1 Maximum Stress Failure Theory
Maximum stress criterion (Fig. 3 (left)) can be written in the form:


[image: image23.wmf]111

222

1212

CT

CT

F

sss

sss

tt

-<<

-<<

<

 
 MACROBUTTON MTPlaceRef \* MERGEFORMAT (3.1)

If these six inequalities are satisfied, then the failure of the layer does not occur. If any of these inequalities are not satisfied, then the layer failure occurs by the fracture mechanism corresponding to the stress of the inequality that is not satisfied. The advantage of this theory is that it is simple to use but the major disadvantage is that there is no interaction between the stress components. 
3.2 Tsai-Hill Failure Theory
According to this theory, failure is assumed to occur whenever the distortional yield energy is equal or greater than a certain value related to the strength of the lamina. There is no distinction between the tensile and compressive strengths. The Tsai-Hill failure theory is given as:



[image: image24.wmf](

)

(

)

(

)

(

)

222

112212

2222

11212

1

FFFF

sssst

ssst

-++£

 
 MACROBUTTON MTPlaceRef \* MERGEFORMAT (3.2)

The advantage of this theory is that there is interaction between the stress components. However, this theory does not distinguish between the tensile and compressive strengths and is not as simple to use as the maximum stress theory or the maximum strain theory.

[image: image25.jpg]102




                        [image: image26.jpg]VCI





Fig. 3 Failure envelope for the (left)-maximum stress failure theory; (right)-Tsai-Hill failure theory
3.1 Comparison of Failure Criterion

Table 1 [0/90/0/90] Carbon-epoxy laminate,
[image: image27.wmf]1000  [N/m]

xy

NN

==

 
	Layer orientation
	Tsai-Hill
	Maximum Stress

	0
	Didn’t fail
	Didn’t fail

	90
	Didn’t fail
	Didn’t fail

	0
	Didn’t fail
	Didn’t fail

	90
	Didn’t fail
	Didn’t fail


Table 2 [30/-602/0/45] Carbon-epoxy laminate,
[image: image28.wmf]1000[Nm/m];500[Nm/m]

xxy

NMM

===

 
	Layer orientation
	Tsai-Hill
	Maximum Stress

	30
	Failure
	Didn't fail

	-60
	Failure
	Failure in Tension

	-60
	Failure
	Failure in Tension

	0
	Failure
	Failure in Compression

	45
	Failure
	Failure in Compression


Table 3 [(0/60/90)2]S Carbon-epoxy laminate,
[image: image29.wmf]xy

1000;MM500

xy

NN

====


	Layer orientation
	Tsai-Hill
	Maximum Stress

	0
	Failure
	Failure in Tension

	60
	Failure
	Failure in Tension

	90
	Didn’t fail
	Failure in Tension

	0
	Didn’t fail
	Failure in Tension

	60
	Didn’t fail
	Didn’t fail

	90
	Didn’t fail
	Didn’t fail

	90
	Didn’t fail
	Didn’t fail

	60
	Didn’t fail
	Didn’t fail

	0
	Didn’t fail
	Didn’t fail

	90
	Didn’t fail
	Didn’t fail

	60
	Didn’t fail
	Didn’t fail

	0
	Failure
	Didn’t fail


4. CONCLUSION
In this paper, fiber-reinforced composite materials were discussed. Constitutive relations of laminate are obtained and analyzed with classical lamination theory. The theory does not consider the effect of shear deformation, and therefore segment that was normal before deformation on the middle plane remains perpendicular to the middle plane after deformation. Such simplifications make it easier for calculation, but it gives accurate results only for thin laminates. For medium thick and thick laminates, this theory is not suitable and it is necessary then to consider some of the high order theories.
For failure criteria, in this paper, maximum stress criterion and Tsai-Hill criterion were selected. Maximum stress criterion is easily applied, but gives good results only under uniaxial strain. This is because there is no connection between stress components. Tsai-Hill criterion gives the relationship between the components of the stress, but does not distinguish between the tensile and compressive strength. Still, this failure theory is better then the previous criteria and gives good results in biaxial and triaxial strain. Even if sometimes maximum stress criterion is more rigorous, it does not correspond to the reality as that is not how material behaves.
REFERENCES
[1] Barthelot, J.M. (2015). Mechanics of Composite Materials and Structures. Vallouise.
[2] Voyiadjis, G.Z., Kattan, P.I. (2015). Mechanics of Composite Materials with MATLAB, Springer, The Netherlands.
[3] Kaw, A.K, (2006). Mechanics of composite materials. CRC Press Taylor & Francis Group, Boca Raton

LOGO WILL BE HERE








� Ph.D., Associate professor, Gordana Bogdanović, Faculty of Engineering, University of Kragujevac, Sestre Janjić 6, 34000 Kragujevac, (� HYPERLINK "mailto:gocab@kg.ac.rs" �gocab@kg.ac.rs�)


� Ph.D. student, Vladimir Geroski, Faculty of Engineering, University of Kragujevac, Sestre Janjić 6, 34000 Kragujevac, (vlada.geroski@gmail.com)


� Ph.D., Assistant, Aleksandar Radaković, State University of Novi Pazar, Vuka Karadžića bb, 36300 Novi Pazar, (aradakovic@np.ac.rs)


� Ph.D., Assistant, Dragan Čukanović, Faculty of Technical Sciences, University of Priština, Knjaza Miloša 7, 38220 Kosovska Mitrovica, (dragan.cukanovic@pr.ac.rs)


� Ph.D. Full professor, Dragan Milosavljević, Faculty of Engineering, University of Kragujevac, Sestre Janjić 6, 34000 Kragujevac, (dmilos@kg.ac.rs)





6
5

_1553006680.unknown

_1553008570.unknown

_1553009459.unknown

_1553011918.unknown

_1553018410.unknown

_1553021195.unknown

_1553021726.unknown

_1553020216.unknown

_1553012709.unknown

_1553009556.unknown

_1553009364.unknown

_1553009424.unknown

_1553009278.unknown

_1553007898.unknown

_1553008145.unknown

_1553007813.unknown

_1553005840.unknown

_1553006468.unknown

_1553006525.unknown

_1553006250.unknown

_1553005375.unknown

_1553005600.unknown

_1553004803.unknown

