Stojana Vesković Bukudur, Aleš Nagode, Blaž Karpe,……………   
Pack aluminization process of heat resistant FeCrAl and NiCr alloys

[image: image1.jpg]


[image: image16.wmf]0

200

400

600

800

1000

1200

1400

0,00

0,10

0,20

0,30

0,40

0,50

0,60

0,70

0,80

-

100

400

900

1.400

T

e

m

p

e

r

a

t

u

r

e

 

[

°

C

]

M

a

s

s

 

g

a

i

n

 

[

m

g

/

c

m

2

]

Time [min]

As

received 

FeCrAl

Aluminized FeCrAl


PACK ALUMINIZATION PROCESS OF HEAT RESISTANT FeCrAl AND NiCr ALLOYS

Stojana Vesković Bukudur1, Aleš Nagode2, Blaž Karpe3, Janez Kovač4,       Stjepan Kožuh5, Milan Bizjak6
Abstract: Pack aluminization process is one of the possible production methods to improve oxidation resistance at high temperatures of various types of metallic materials. It is a chemo-thermal process where products are embedded in the powder mixture, consisting of Al powder, halide activator NH4Cl, and inert diluent Al2O3 powder, and annealed at high temperature. This exposure to high temperature causes the Al diffusion into the base material and formation of the aluminide surface layer. During the component service at elevated temperatures, the oxidation resistance is obtained due to the constant formation of an aluminium oxide film that forms on the aluminide surface layer and acts as an oxygen impermeable barrier. In the present study, FeCrAl and the NiCr heat resistant alloys in the form of 1mm thick sheet were aluminized at various process parameters. The effect of time, temperature, concentration of aluminium and halide activator in the powder mixture as well as the influence of furnace atmosphere on coating formation mechanism, mass gain and the thickness of the aluminide diffusion layer was evaluated by scanning electron microscopy, X-ray photoelectron spectroscopy and micro hardness analytic techniques. Isothermal exposure tests at 1200 °C for 24h in air were conducted and compared with untreated samples for high temperature oxidation resistance estimation. 

Keywords: Aluminizing, heat resistant alloys, FeCrAl, NiCr, high temperature oxidation

------------------------------------------------------
1    Stojana Vesković Bukudur, Hidria AET d.o.o., Poljubinj 89a, 5220 Tolmin, Slovenia (stojana.veskovic@hidria.com)

2 Assoc. Prof. Dr. Aleš Nagode, University of Ljubljana, Faculty of Natural Sciences and Engineering, Ljubljana, Aškerčeva 12, 1000 Ljubljana, Slovenia ales.nagode@omm.ntf.uni-lj.si)
3  Ass. Prof. Dr. Blaž  Karpe, University of Ljubljana, Faculty of Natural Sciences and Engineering, Ljubljana, Aškerčeva 12, 1000 Ljubljana, Slovenia (blaz.karpe@omm.ntf.uni-lj.si)
4 Ass. Prof. Dr. Janez Kovač, Institute Josef Stefan, Jamova c. 39, 1000, Ljubljana, Slovenia (janez.kovac@ijs.si)
5  Assoc. Prof. Dr. Stjepan  Kožuh, University of Zagreb, Faculty of Metallurgy, Sisak, Aleja n. h. 3, 44103 Sisak, Croatia (kozuh@simet.hr)
6  Prof. Dr. Milan Bizjak, University of Ljubljana, Faculty of Natural Sciences and Engineering, Ljubljana, Aškerčeva 12, 1000 Ljubljana, Slovenia (milan.bizjak@omm.ntf.uni-lj.si)
1. INTRODUCTION
Aluminizing is a widely used process to protect materials, particularly metals and alloys against high temperature oxidation and hot corrosion attack. In this process the metal to be coated is placed in a powder pack consisting essentially of the coating element source such as pure aluminium or aluminium alloy (Cr-Al), an activator such as halide salts AlF3, NaCl, NH4Cl and NH4F and an inert filler material, usually alumina [1]. The process is carried out at atmospheric pressure in flowing hydrogen or in an inert atmosphere at a temperature between 700 °C and 1150 °C. The aluminizing process can be divided into three steps: (a) gaseous diffusion, (b) surface reaction and (c) solid diffusion. At the coating temperature halide activator reacts with the metal elements in the powder pack and form a series of metal halide vapour species with characteristic partial pressure distribution that is determined by their thermodynamic stability in a particular powder pack. The coating is formed via reduction reaction of metal halide vapours at the substrate surface and subsequent solid state diffusion between metal elements and substrate [2,3]. The thermodynamics and kinetics of the aluminizing process are defined by the pack components and operating conditions like temperature, time and atmosphere [4]. Two critical issues for the application of aluminide coating have been identified: (i) loss of Al from the coating into the substrate which limits coating lifetime, (ii) the difference in thermal expansion coefficient (CTE) between aluminide coating and the substrate, which can cause mechanical damage (cracks) to the coating [5]..

2.
EXPERIMENTAL PROCEDURE
The substrate alloys used in this study were a commercial ferritic alloy Fe-Cr-Al (Kanthal AF) and a commercial austenitic alloy Ni-Cr (Nicrothal 80); the composition is listed in Table 1. 
Table 1. Chemical composition of the coated alloys in wt.%.
	Alloy
	Ni
	Cr
	Fe
	Mn
	Si
	Al
	Ti

	Kanthal AF
	0.4
	21.0
	Bal.
	0.2
	0.2
	5.5
	1.0

	Nicrothal 80
	Bal.
	20.0
	1.0
	0.5
	1.3
	-
	-


Flat coupons (20 x 10 x 0.7 mm) were ultrasonically cleaned in an alcohol, dried and immediately embedded in a powder pack, which consist of the deposition element (Al), an activator (NH4Cl) and an inert filler (Al2O3), and semi-sealed in alumina crucible. The crucible is heat treated in a tube furnace under an Ar-5%H2 atmosphere. Process parameters of the aluminizing process are process time, process temperature and the powder pack. The coating time was varied from 0.5 to 2.5 hours and the process temperature from 670°C to 750°C. The heating rate was 10°C/min and the cooling rate from the process temperature to 200 °C was 5 °C/min. The Al to NH4Cl mass ratio in the powder mixture was 3 (21 wt.% Al, 7 wt.% NH4Cl, 72 wt.% Al2O3) for all aluminizing experiments. Coated specimens were cleaned with a brush and then put into ultrasonic bath and cleaned in an alcohol. Cross sections of samples for microstructure observations were prepared by standard metallographic preparation by grinding and polishing. Optical microscope AXIO CSM 700 and scanning electron microscope Jeol JSM 5610 with energy dispersive X-ray spectroscopy (EDS) were used for the microstructure observations. The phase constitution of the as deposited coatings was examined by X-ray diffraction (XRD), using Cu Kα radiation. The oxidation resistance of the samples was investigated under isothermal conditions by thermobalance Netzsch STA 429 at 1200 °C, 24 h in a laboratory air atmosphere. Samples were heated at a rate of 20 K/min, followed by cooling at the rate 20 K/min.

3.
RESULTS AND DISCUSSION
3.1 Coating thickness as a function of time and temperature

Aluminium was successfully deposited onto Fe-Cr-Al an Ni-Cr alloy in the form of 0.7 mm sheet through the halide activated aluminizing process at different coating temperature and time.  The coatings show some irregularities and a small pore size but are free of cracks. The number of irregularities in coatings increases with coating temperature. After aluminising, coating thickness measurements were performed at various sites. Figure 1 shows the SEM cross sections of aluminide coatings on Fe-Cr-Al and Ni-Cr alloy deposited at 670 °C for 1.5h and Figure 2 aluminide coatings on both alloys deposited at 730 °C for 1.5 h. The aluminide coating is thicker in the case of Fe-Cr-Al alloy because of a higher diffusion rate of Al in Fe-Cr-Al alloy, especially at higher temperature.  

[image: image3.emf] 

LOGO WILL BE HERE 

[image: image2.emf]A


Fig. 1 SEM image of FeCrAl (A) and NiCr alloy (B) aluminized at 670 °C, 1.5 h

[image: image4.wmf]10,0

30,0

50,0

70,0

90,0

110,0

130,0

670

690

710

730

750

C

o

a

t

i

n

g

 

t

h

i

c

k

n

e

s

 

[

µ

m

]

Temperature [

°

C]

FeCrAl

NiCr

[image: image5.wmf]15,0

25,0

35,0

45,0

55,0

65,0

75,0

0,5

1

1,5

2

2,5

3

C

o

a

t

i

n

g

 

t

h

i

c

k

n

e

s

s

 

[

µ

m

]

Time [h]

FeCrAl

NiCr


Fig. 2 SEM image of FeCrAl (C) and NiCr alloy (D) aluminized at 730 °C, 1.5 h

Figure 3 shows the average coating thickness as a function of coating temperature at constant time. The data points for each coating temperature demonstrate that as the coating temperature is increased, the coating thickness increased. With an increase in aluminizing temperature from 670 °C to 730 °C at constant coating time 1.5 h, the coating thickness is increased threefold for Fe-Cr-Al alloy and thirty percent for Ni-Cr alloy. Figure 4 shows the average coating thickness as a function of coating time at constant temperature 690°C.  The thickness of the coating increase with time from 0.5 to 3 h for both alloys. Increase in thickness was much higher for Fe-Cr-Al alloy.  

[image: image6.wmf]0

200

400

600

800

1000

1200

1400

0,00

0,10

0,20

0,30

0,40

0,50

0,60

0,70

0,80

-

100

400

900

1.400

T

e

m

p

e

r

a

t

u

r

e

 

[

°

C

]

M

a

s

s

 

g

a

i

n

 

[

m

g

/

c

m

2

]

Time [min]

As

received 

FeCrAl

Aluminized FeCrAl


Fig. 3 The average aluminide coating thickness as a function of aluminizing temperature at a constant annealing time 1.5 h
[image: image7.emf]B


Fig. 4 The average aluminide coating thickness as a function of time at a constant temperature 690 °C

3.2 Scanning electron microscopy (SEM/EDS)

Chemical analysis of coating and substrate subsurface were performed by energy dispersive spectroscopy (SEM-EDS). Figure 5 shows the representative sample subjected to the coating temperature of 730 °C for 1.5h for the Fe‑Cr‑Al alloy and Figure 6 for the Ni‑Cr alloy. Coating thickness ranged from 100 to 120 µm for Fe-Cr-Al alloy and 30 to 45 µm for Ni-Cr alloy. 

[image: image8.emf]D


Fig. 5 SEM-EDX analysis of Fe-Cr-Al coated at 730 °C for 1.5 h

[image: image9.emf]C


Fig. 6 SEM-EDX analysis of  NiCr coated at 730 °C for 1.5 h

The coating on Fe-Cr-Al alloy is a dual phase mixture with dark and light areas.  EDS analysis show that the dark phase is rich in aluminium and contain iron and a small amount of chromium. The light phase contains a smaller percentage of aluminium and iron, and a larger percentage of chromium. It is evident that Fe-Cr-Al alloy forms a number of different phases. The formation of these phases depends on the diffusion of aluminium through the coating in direction to the substrate. The aluminium content increased in the direction to coating surface and the content of chromium and iron decreased. 
On the other hand, aluminized layer on Ni-Cr alloy consists of two layers: the darker top layer (Area I), rich on aluminium, chromium and nickel and lighter subsurface layer (Area II), which contains smaller percentage of aluminium and a higher percentage of nickel and chromium. The average coating thickness is 35 µm, thickness of top layer is 15 µm followed by a sub layer of about 20 µm. 
3.3 X-ray diffraction

[image: image10.wmf]10,0

30,0

50,0

70,0

90,0

110,0

130,0

670

690

710

730

750

C

o

a

t

i

n

g

 

t

h

i

c

k

n

e

s

 

[

µ

m

]

Temperature [

°

C]

FeCrAl

NiCr

[image: image11.wmf]15,0

25,0

35,0

45,0

55,0

65,0

75,0

0,5

1

1,5

2

2,5

3

C

o

a

t

i

n

g

 

t

h

i

c

k

n

e

s

s

 

[

µ

m

]

Time [h]

FeCrAl

NiCr

X-ray diffraction (XRD) was used for phase identification of coatings. From these study it was established that for the coating time 1,5h at 730°C, the surface of the coated Fe-Cr-Al alloys consists mainly from α‑ Al8Fe5, β‑ Al5Fe2, γ‑ AlFe3 (see Figure 7a). According to the phase diagram Fe-Cr the iron forms a number of different intermetallic compounds such as: FeAl3, Fe2Al5, FeAl2, FeAl, Fe3Al, as well α-Al and α-Fe. Based on the intensity of the scattered X-rays the largest content has Al5Fe2 phase. 

Fig. 7 XRD patterns of the aluminizing coating on Fe-Cr-Al substrate a) and NiCr substrate b)

Aluminized coating of Ni-Cr alloy comprises the following phases: α‑ Al3Ni2, β‑ Al, γ‑ Ni, δ‑ Cr, ε‑ Al3Ni (see Figure 7 b), with the largest proportion of the Al3Ni2 phase. From the results of XRD and SEM analysis, it can be concluded, that the upper layer (I) is comprised mainly of Al3Ni phase, and the layer (II) of Al3Ni2 phase, with continuously increased proportion of other phases according to the Al-Ni phase diagram. This finding is in a good agreement with [6]. They found out that Al3N2 is the major phase because of a very high diffusivity of Al3Ni2. 

3.4 Oxidation test

[image: image12.emf]SUBSTRATE

COATING

Principal elements in EDS analysis (wt.%)

Phase O Al Cr Fe Co

Dark area 49.68 4.03 45.41 0.89

Light area 0.40 40.34 22.97 35.59 0.69

Substrate 3.82 21.22 73.84

The effectiveness of the aluminizing process was evaluated by the oxidation testing of the commercial Fe-Cr-Al 0.7 mm thick sheet in comparison with aluminized Fe-Cr-Al samples under isothermal conditions (thermo-balance Netzsch STA 429) at constant temperature of 1200 °C/24 h in a laboratory air atmosphere. Samples were heated and cooled at the same rate of 20 K/min. The results are presented by the relative mass gain versus time (Figure 8). According to the measurements, the initial oxidation rate of as received commercial Fe-Cr-Al sheets is higher than for aluminized Fe-Cr-Al samples (first 24 h). Because of short time of isothermal temperature exposure, further longer tests would be needed to determine whether or not the increased Al alloy content prolong the life time of the Kanthal AF sheet at 1200 °C [7]. 

Fig. 8  Relative mass gain as a function of oxidation time in air at 1200 °C (heating rate 20 K/min) 

2. CONCLUSIONS
Within the work it was successfully prepared homogeneous aluminized layer on ferritic Kanthal AF (Fe-Cr-Al) and on austenitic Nicrothal 80 (Ni-Cr) with sufficient aluminium reservoir, which should enable the formation of protective alumina scale in oxidizing conditions. 
The effect of Al activity in powder pack on the coating kinetics and structure was studied at several coating temperatures in the range from 650 to 750 °C for 0.5 to 2.5 hours.  Samples in the form of sheet were uniformly aluminized at various times and temperatures. The dependence of coating thickness from temperature and time at constant powder pack was evaluated. 
The coating is free of cracks with some imperfections like pores or porous area.  According to SEM/EDS analyses of Fe-Cr-Al alloy aluminium content decreased from the coating surface to the substrate material, the content of chromium and iron increases. Aluminized layer on Fe-Cr-Al alloy contains intermetallic phases Al8Fe5, Al5Fe2 and AlFe3. 

Analyses of the aluminized layer on Nicrothal 80 (Ni-Cr) alloy showed that aluminized layer consists of two layers. The upper layer, with higher percent of aluminium and the lower layer, with smaller percentage of aluminium and a higher percentage of nickel and chromium. The upper layer is comprised mainly of Al3Ni phase, and the lower layer of Al3Ni2 phase, with continuously increased proportion of other phases in direction of the substrate alloy. The thickness of the layers increases with aluminizing time and temperature. Coating thickness is increased faster in Fe-Cr-Al alloy because of significantly higher diffusion rate of aluminium in KANTHAL AF alloy than in Nicrothal 80 alloy [8].
REFERENCES 
[1] Mévrel, C., Duret, R., Pichoir, P. (1986). Pack cementation processes. Material Science and Technology, Vol. 2, Issue 3, pp. 201-206.

[2] Gupta, B. K., Sarkhel, A. K., Seigle, L. L. (1976). On the kinetics of pack cementation. Thin solid films, Vol. 39, pp. 313-320.

[3] Xiang, Z. D.J. S. Burnell-Gray, S., Datta, P. K. (2001). Aluminide coating formation on nickel-base super alloys by pack cementation process. Surface & Coatings technology, Vol. 36, Issue 23, pp. 5673–5682.

[4] Zhang, Y. (2008). Formation of aluminide coatings on the Fe-based alloys by chemical vapour deposition. Surface & Coatings technology, Vol. 202, pp. 3830-3849. 
[5] Kung, S. C., Rapp R. A. (1987). Fundamental study of aluminization of iron by pack cementation at 900°C. Surface and coatings technology, Vol. 32, pp. 41-56. 

[6] Seigle,  L. L. (1982) Kinetics of formation and microstructure of aluminide coatings on Ni-Cr alloys, Thin Solid Films, Vol. 95, 1982, pp. 47-56.

[7] Bennett, M.J., Nicholls, J.R., Simms, N.J., Naumenko, D., Quadakkers, W.J., Kochubey, V., Fordham, R., Bachorczyk, R., Goossens, D., Hattendorf, H., Smith, A.B., Britton, D. (2005). Lifetime extension of FeCrAlRE alloys in air: Potential roles of an enhanced Al-reservoir and surface pre-treatment. Materials and Corrosion, Vol. 56, Issue 12, pp. 854–866. 

[8] Goward, G. W., Boone, D. H. (1971).Mechanisms of Formation of diffusion Aluminide Coatings on Nickel-Base Superalloys. Oxidation of Metals, Vol. 3, No. 5, pp. 475-495.

�





� EMBED Excel.Chart.8 \s ���





� EMBED Excel.Chart.8 \s ���





� EMBED Excel.Chart.8 \s ���








8
7

[image: image13.emf]SUBSTRATE

COATING

 

Principal elements in EDS analysis  ( wt.%)  

Phase  Al  Si  Cr  Mn  Fe  Ni  

Area I  48.97  0.26  10.76  0.13  0.34  39.54  

Area II  37.55  0.50  11.50  0.10  0.37  49.98  

Substrate  0.12  1.25  20.43  0.17  0.50  77.54  

[image: image14.emf]a)

[image: image15.emf]b)

_1554485075.xls
Grafikon1

		0.5		0.5

		1		1

		1.5		1.5

		2		2

		2.5		2.5

		3		3



FeCrAl

NiCr

Time [h]

Coating thickness [µm]

22.4

24.9

31.1

24.8

52.5

35.6

60.3

39.4

63.5

39.4

39.5



List1

		

				FeCrAl		NiCr

		670		29.7		40

		690		50.1		44.5

		710		54.5		49.4

		730		108.4		57.7

		750				74.7

				FeCrAl		NiCr

		0.5		22.4		24.9

		1		31.1		24.8

		1.5		52.5		35.6

		2		60.3		39.4

		2.5		63.5		39.4

		3				39.5





List1

		



FeCrAl

NiCr

Temperature [°C]

Coating thicknes [µm]



		



FeCrAl

NiCr

Temperature [°C]

Coating thickness [µm]




_1554495326.xls
Grafikon1

		0		0		0

		0.025		0.025		0.025

		0.05		0.05		0.05

		0.075		0.075		0.075

		0.1		0.1		0.1

		0.125		0.125		0.125

		0.15		0.15		0.15

		0.175		0.175		0.175

		0.2		0.2		0.2

		0.225		0.225		0.225

		0.25		0.25		0.25

		0.275		0.275		0.275

		0.3		0.3		0.3

		0.325		0.325		0.325

		0.35		0.35		0.35

		0.375		0.375		0.375

		0.4		0.4		0.4

		0.425		0.425		0.425

		0.45		0.45		0.45

		0.475		0.475		0.475

		0.5		0.5		0.5

		0.525		0.525		0.525

		0.55		0.55		0.55

		0.575		0.575		0.575

		0.6		0.6		0.6

		0.625		0.625		0.625

		0.65		0.65		0.65

		0.675		0.675		0.675

		0.7		0.7		0.7

		0.725		0.725		0.725

		0.75		0.75		0.75

		0.775		0.775		0.775

		0.8		0.8		0.8

		0.825		0.825		0.825

		0.85		0.85		0.85

		0.875		0.875		0.875

		0.9		0.9		0.9

		0.925		0.925		0.925

		0.95		0.95		0.95

		0.975		0.975		0.975

		1		1		1

		1.025		1.025		1.025

		1.05		1.05		1.05

		1.075		1.075		1.075

		1.1		1.1		1.1

		1.125		1.125		1.125

		1.15		1.15		1.15

		1.175		1.175		1.175

		1.2		1.2		1.2

		1.225		1.225		1.225

		1.25		1.25		1.25

		1.275		1.275		1.275

		1.3		1.3		1.3

		1.325		1.325		1.325

		1.35		1.35		1.35

		1.375		1.375		1.375

		1.4		1.4		1.4

		1.425		1.425		1.425

		1.45		1.45		1.45

		1.475		1.475		1.475

		1.5		1.5		1.5

		1.525		1.525		1.525

		1.55		1.55		1.55

		1.575		1.575		1.575

		1.6		1.6		1.6

		1.625		1.625		1.625

		1.65		1.65		1.65

		1.675		1.675		1.675

		1.7		1.7		1.7

		1.725		1.725		1.725

		1.75		1.75		1.75

		1.775		1.775		1.775

		1.8		1.8		1.8

		1.825		1.825		1.825

		1.85		1.85		1.85

		1.875		1.875		1.875

		1.9		1.9		1.9

		1.925		1.925		1.925

		1.95		1.95		1.95

		1.975		1.975		1.975

		2		2		2

		2.025		2.025		2.025

		2.05		2.05		2.05

		2.075		2.075		2.075

		2.1		2.1		2.1

		2.125		2.125		2.125

		2.15		2.15		2.15

		2.175		2.175		2.175

		2.2		2.2		2.2

		2.225		2.225		2.225

		2.25		2.25		2.25

		2.275		2.275		2.275

		2.3		2.3		2.3

		2.325		2.325		2.325

		2.35		2.35		2.35

		2.375		2.375		2.375

		2.4		2.4		2.4

		2.425		2.425		2.425

		2.45		2.45		2.45

		2.475		2.475		2.475

		2.5		2.5		2.5

		2.525		2.525		2.525

		2.55		2.55		2.55

		2.575		2.575		2.575

		2.6		2.6		2.6

		2.625		2.625		2.625

		2.65		2.65		2.65

		2.675		2.675		2.675

		2.7		2.7		2.7

		2.725		2.725		2.725

		2.75		2.75		2.75

		2.775		2.775		2.775

		2.8		2.8		2.8

		2.825		2.825		2.825

		2.85		2.85		2.85

		2.875		2.875		2.875

		2.9		2.9		2.9

		2.925		2.925		2.925

		2.95		2.95		2.95

		2.975		2.975		2.975

		3		3		3

		3.025		3.025		3.025

		3.05		3.05		3.05

		3.075		3.075		3.075

		3.1		3.1		3.1

		3.125		3.125		3.125

		3.15		3.15		3.15

		3.175		3.175		3.175

		3.2		3.2		3.2

		3.225		3.225		3.225

		3.25		3.25		3.25

		3.275		3.275		3.275

		3.3		3.3		3.3

		3.325		3.325		3.325

		3.35		3.35		3.35

		3.375		3.375		3.375

		3.4		3.4		3.4

		3.425		3.425		3.425

		3.45		3.45		3.45

		3.475		3.475		3.475

		3.5		3.5		3.5

		3.525		3.525		3.525

		3.55		3.55		3.55

		3.575		3.575		3.575

		3.6		3.6		3.6

		3.625		3.625		3.625

		3.65		3.65		3.65

		3.675		3.675		3.675

		3.7		3.7		3.7

		3.725		3.725		3.725

		3.75		3.75		3.75

		3.775		3.775		3.775

		3.8		3.8		3.8

		3.825		3.825		3.825

		3.85		3.85		3.85

		3.875		3.875		3.875

		3.9		3.9		3.9

		3.925		3.925		3.925

		3.95		3.95		3.95

		3.975		3.975		3.975

		4		4		4

		4.025		4.025		4.025

		4.05		4.05		4.05

		4.075		4.075		4.075

		4.1		4.1		4.1

		4.125		4.125		4.125

		4.15		4.15		4.15

		4.175		4.175		4.175

		4.2		4.2		4.2

		4.225		4.225		4.225

		4.25		4.25		4.25

		4.275		4.275		4.275

		4.3		4.3		4.3

		4.325		4.325		4.325

		4.35		4.35		4.35

		4.375		4.375		4.375

		4.4		4.4		4.4

		4.425		4.425		4.425

		4.45		4.45		4.45

		4.475		4.475		4.475

		4.5		4.5		4.5

		4.525		4.525		4.525

		4.55		4.55		4.55

		4.575		4.575		4.575

		4.6		4.6		4.6

		4.625		4.625		4.625

		4.65		4.65		4.65

		4.675		4.675		4.675

		4.7		4.7		4.7

		4.725		4.725		4.725

		4.75		4.75		4.75

		4.775		4.775		4.775

		4.8		4.8		4.8

		4.825		4.825		4.825

		4.85		4.85		4.85

		4.875		4.875		4.875

		4.9		4.9		4.9

		4.925		4.925		4.925

		4.95		4.95		4.95

		4.975		4.975		4.975

		5		5		5

		5.025		5.025		5.025

		5.05		5.05		5.05

		5.075		5.075		5.075

		5.1		5.1		5.1

		5.125		5.125		5.125

		5.15		5.15		5.15

		5.175		5.175		5.175

		5.2		5.2		5.2

		5.225		5.225		5.225

		5.25		5.25		5.25

		5.275		5.275		5.275

		5.3		5.3		5.3

		5.325		5.325		5.325

		5.35		5.35		5.35

		5.375		5.375		5.375

		5.4		5.4		5.4

		5.425		5.425		5.425

		5.45		5.45		5.45

		5.475		5.475		5.475

		5.5		5.5		5.5

		5.525		5.525		5.525

		5.55		5.55		5.55

		5.575		5.575		5.575

		5.6		5.6		5.6

		5.625		5.625		5.625

		5.65		5.65		5.65

		5.675		5.675		5.675

		5.7		5.7		5.7

		5.725		5.725		5.725

		5.75		5.75		5.75

		5.775		5.775		5.775

		5.8		5.8		5.8

		5.825		5.825		5.825

		5.85		5.85		5.85

		5.875		5.875		5.875

		5.9		5.9		5.9

		5.925		5.925		5.925

		5.95		5.95		5.95

		5.975		5.975		5.975

		6		6		6

		6.025		6.025		6.025

		6.05		6.05		6.05

		6.075		6.075		6.075

		6.1		6.1		6.1

		6.125		6.125		6.125

		6.15		6.15		6.15

		6.175		6.175		6.175

		6.2		6.2		6.2

		6.225		6.225		6.225

		6.25		6.25		6.25

		6.275		6.275		6.275

		6.3		6.3		6.3

		6.325		6.325		6.325

		6.35		6.35		6.35

		6.375		6.375		6.375

		6.4		6.4		6.4

		6.425		6.425		6.425

		6.45		6.45		6.45

		6.475		6.475		6.475

		6.5		6.5		6.5

		6.525		6.525		6.525

		6.55		6.55		6.55

		6.575		6.575		6.575

		6.6		6.6		6.6

		6.625		6.625		6.625

		6.65		6.65		6.65

		6.675		6.675		6.675

		6.7		6.7		6.7

		6.725		6.725		6.725

		6.75		6.75		6.75

		6.775		6.775		6.775

		6.8		6.8		6.8

		6.825		6.825		6.825

		6.85		6.85		6.85

		6.875		6.875		6.875

		6.9		6.9		6.9

		6.925		6.925		6.925

		6.95		6.95		6.95

		6.975		6.975		6.975

		7		7		7

		7.025		7.025		7.025

		7.05		7.05		7.05

		7.075		7.075		7.075

		7.1		7.1		7.1

		7.125		7.125		7.125

		7.15		7.15		7.15

		7.175		7.175		7.175

		7.2		7.2		7.2

		7.225		7.225		7.225

		7.25		7.25		7.25

		7.275		7.275		7.275

		7.3		7.3		7.3

		7.325		7.325		7.325

		7.35		7.35		7.35

		7.375		7.375		7.375

		7.4		7.4		7.4

		7.425		7.425		7.425

		7.45		7.45		7.45

		7.475		7.475		7.475

		7.5		7.5		7.5

		7.525		7.525		7.525

		7.55		7.55		7.55

		7.575		7.575		7.575

		7.6		7.6		7.6

		7.625		7.625		7.625

		7.65		7.65		7.65

		7.675		7.675		7.675

		7.7		7.7		7.7

		7.725		7.725		7.725

		7.75		7.75		7.75

		7.775		7.775		7.775

		7.8		7.8		7.8

		7.825		7.825		7.825

		7.85		7.85		7.85

		7.875		7.875		7.875

		7.9		7.9		7.9

		7.925		7.925		7.925

		7.95		7.95		7.95

		7.975		7.975		7.975

		8		8		8

		8.025		8.025		8.025

		8.05		8.05		8.05

		8.075		8.075		8.075

		8.1		8.1		8.1

		8.125		8.125		8.125

		8.15		8.15		8.15

		8.175		8.175		8.175

		8.2		8.2		8.2

		8.225		8.225		8.225

		8.25		8.25		8.25

		8.275		8.275		8.275

		8.3		8.3		8.3

		8.325		8.325		8.325

		8.35		8.35		8.35

		8.375		8.375		8.375

		8.4		8.4		8.4

		8.425		8.425		8.425

		8.45		8.45		8.45

		8.475		8.475		8.475

		8.5		8.5		8.5

		8.525		8.525		8.525

		8.55		8.55		8.55

		8.575		8.575		8.575

		8.6		8.6		8.6

		8.625		8.625		8.625

		8.65		8.65		8.65

		8.675		8.675		8.675

		8.7		8.7		8.7

		8.725		8.725		8.725

		8.75		8.75		8.75

		8.775		8.775		8.775

		8.8		8.8		8.8

		8.825		8.825		8.825

		8.85		8.85		8.85

		8.875		8.875		8.875

		8.9		8.9		8.9

		8.925		8.925		8.925

		8.95		8.95		8.95

		8.975		8.975		8.975

		9		9		9

		9.025		9.025		9.025

		9.05		9.05		9.05

		9.075		9.075		9.075

		9.1		9.1		9.1

		9.125		9.125		9.125

		9.15		9.15		9.15

		9.175		9.175		9.175

		9.2		9.2		9.2

		9.225		9.225		9.225

		9.25		9.25		9.25

		9.275		9.275		9.275

		9.3		9.3		9.3

		9.325		9.325		9.325

		9.35		9.35		9.35

		9.375		9.375		9.375

		9.4		9.4		9.4

		9.425		9.425		9.425

		9.45		9.45		9.45

		9.475		9.475		9.475

		9.5		9.5		9.5

		9.525		9.525		9.525

		9.55		9.55		9.55

		9.575		9.575		9.575

		9.6		9.6		9.6

		9.625		9.625		9.625

		9.65		9.65		9.65

		9.675		9.675		9.675

		9.7		9.7		9.7

		9.725		9.725		9.725

		9.75		9.75		9.75

		9.775		9.775		9.775

		9.8		9.8		9.8

		9.825		9.825		9.825

		9.85		9.85		9.85

		9.875		9.875		9.875

		9.9		9.9		9.9

		9.925		9.925		9.925

		9.95		9.95		9.95

		9.975		9.975		9.975

		10		10		10

		10.025		10.025		10.025

		10.05		10.05		10.05

		10.075		10.075		10.075

		10.1		10.1		10.1

		10.125		10.125		10.125

		10.15		10.15		10.15

		10.175		10.175		10.175

		10.2		10.2		10.2

		10.225		10.225		10.225

		10.25		10.25		10.25

		10.275		10.275		10.275

		10.3		10.3		10.3

		10.325		10.325		10.325

		10.35		10.35		10.35

		10.375		10.375		10.375

		10.4		10.4		10.4

		10.425		10.425		10.425

		10.45		10.45		10.45

		10.475		10.475		10.475

		10.5		10.5		10.5

		10.525		10.525		10.525

		10.55		10.55		10.55

		10.575		10.575		10.575

		10.6		10.6		10.6

		10.625		10.625		10.625

		10.65		10.65		10.65

		10.675		10.675		10.675

		10.7		10.7		10.7

		10.725		10.725		10.725

		10.75		10.75		10.75

		10.775		10.775		10.775

		10.8		10.8		10.8

		10.825		10.825		10.825

		10.85		10.85		10.85

		10.875		10.875		10.875

		10.9		10.9		10.9

		10.925		10.925		10.925

		10.95		10.95		10.95

		10.975		10.975		10.975

		11		11		11

		11.025		11.025		11.025

		11.05		11.05		11.05

		11.075		11.075		11.075

		11.1		11.1		11.1

		11.125		11.125		11.125

		11.15		11.15		11.15

		11.175		11.175		11.175

		11.2		11.2		11.2

		11.225		11.225		11.225

		11.25		11.25		11.25

		11.275		11.275		11.275

		11.3		11.3		11.3

		11.325		11.325		11.325

		11.35		11.35		11.35

		11.375		11.375		11.375

		11.4		11.4		11.4

		11.425		11.425		11.425

		11.45		11.45		11.45

		11.475		11.475		11.475

		11.5		11.5		11.5

		11.525		11.525		11.525

		11.55		11.55		11.55

		11.575		11.575		11.575

		11.6		11.6		11.6

		11.625		11.625		11.625

		11.65		11.65		11.65

		11.675		11.675		11.675

		11.7		11.7		11.7

		11.725		11.725		11.725

		11.75		11.75		11.75

		11.775		11.775		11.775

		11.8		11.8		11.8

		11.825		11.825		11.825

		11.85		11.85		11.85

		11.875		11.875		11.875

		11.9		11.9		11.9

		11.925		11.925		11.925

		11.95		11.95		11.95

		11.975		11.975		11.975

		12		12		12

		12.025		12.025		12.025

		12.05		12.05		12.05

		12.075		12.075		12.075

		12.1		12.1		12.1

		12.125		12.125		12.125

		12.15		12.15		12.15

		12.175		12.175		12.175

		12.2		12.2		12.2

		12.225		12.225		12.225

		12.25		12.25		12.25

		12.275		12.275		12.275

		12.3		12.3		12.3

		12.325		12.325		12.325

		12.35		12.35		12.35

		12.375		12.375		12.375

		12.4		12.4		12.4

		12.425		12.425		12.425

		12.45		12.45		12.45

		12.475		12.475		12.475

		12.5		12.5		12.5

		12.525		12.525		12.525

		12.55		12.55		12.55

		12.575		12.575		12.575

		12.6		12.6		12.6

		12.625		12.625		12.625

		12.65		12.65		12.65

		12.675		12.675		12.675

		12.7		12.7		12.7

		12.725		12.725		12.725

		12.75		12.75		12.75

		12.775		12.775		12.775

		12.8		12.8		12.8

		12.825		12.825		12.825

		12.85		12.85		12.85

		12.875		12.875		12.875

		12.9		12.9		12.9

		12.925		12.925		12.925

		12.95		12.95		12.95

		12.975		12.975		12.975

		13		13		13

		13.025		13.025		13.025

		13.05		13.05		13.05

		13.075		13.075		13.075

		13.1		13.1		13.1

		13.125		13.125		13.125

		13.15		13.15		13.15

		13.175		13.175		13.175

		13.2		13.2		13.2

		13.225		13.225		13.225

		13.25		13.25		13.25

		13.275		13.275		13.275

		13.3		13.3		13.3

		13.325		13.325		13.325

		13.35		13.35		13.35

		13.375		13.375		13.375

		13.4		13.4		13.4

		13.425		13.425		13.425

		13.45		13.45		13.45

		13.475		13.475		13.475

		13.5		13.5		13.5

		13.525		13.525		13.525

		13.55		13.55		13.55

		13.575		13.575		13.575

		13.6		13.6		13.6

		13.625		13.625		13.625

		13.65		13.65		13.65

		13.675		13.675		13.675

		13.7		13.7		13.7

		13.725		13.725		13.725

		13.75		13.75		13.75

		13.775		13.775		13.775

		13.8		13.8		13.8

		13.825		13.825		13.825

		13.85		13.85		13.85

		13.875		13.875		13.875

		13.9		13.9		13.9

		13.925		13.925		13.925

		13.95		13.95		13.95

		13.975		13.975		13.975

		14		14		14

		14.025		14.025		14.025

		14.05		14.05		14.05

		14.075		14.075		14.075

		14.1		14.1		14.1

		14.125		14.125		14.125

		14.15		14.15		14.15

		14.175		14.175		14.175

		14.2		14.2		14.2

		14.225		14.225		14.225

		14.25		14.25		14.25

		14.275		14.275		14.275

		14.3		14.3		14.3

		14.325		14.325		14.325

		14.35		14.35		14.35

		14.375		14.375		14.375

		14.4		14.4		14.4

		14.425		14.425		14.425

		14.45		14.45		14.45

		14.475		14.475		14.475

		14.5		14.5		14.5

		14.525		14.525		14.525

		14.55		14.55		14.55

		14.575		14.575		14.575

		14.6		14.6		14.6

		14.625		14.625		14.625

		14.65		14.65		14.65

		14.675		14.675		14.675

		14.7		14.7		14.7

		14.725		14.725		14.725

		14.75		14.75		14.75

		14.775		14.775		14.775

		14.8		14.8		14.8

		14.825		14.825		14.825

		14.85		14.85		14.85

		14.875		14.875		14.875

		14.9		14.9		14.9

		14.925		14.925		14.925

		14.95		14.95		14.95

		14.975		14.975		14.975

		15		15		15

		15.025		15.025		15.025

		15.05		15.05		15.05

		15.075		15.075		15.075

		15.1		15.1		15.1

		15.125		15.125		15.125

		15.15		15.15		15.15

		15.175		15.175		15.175

		15.2		15.2		15.2

		15.225		15.225		15.225

		15.25		15.25		15.25

		15.275		15.275		15.275

		15.3		15.3		15.3

		15.325		15.325		15.325

		15.35		15.35		15.35

		15.375		15.375		15.375

		15.4		15.4		15.4

		15.425		15.425		15.425

		15.45		15.45		15.45

		15.475		15.475		15.475

		15.5		15.5		15.5

		15.525		15.525		15.525

		15.55		15.55		15.55

		15.575		15.575		15.575

		15.6		15.6		15.6

		15.625		15.625		15.625

		15.65		15.65		15.65

		15.675		15.675		15.675

		15.7		15.7		15.7

		15.725		15.725		15.725

		15.75		15.75		15.75

		15.775		15.775		15.775

		15.8		15.8		15.8

		15.825		15.825		15.825

		15.85		15.85		15.85

		15.875		15.875		15.875

		15.9		15.9		15.9

		15.925		15.925		15.925

		15.95		15.95		15.95

		15.975		15.975		15.975

		16		16		16

		16.025		16.025		16.025

		16.05		16.05		16.05

		16.075		16.075		16.075

		16.1		16.1		16.1

		16.125		16.125		16.125

		16.15		16.15		16.15

		16.175		16.175		16.175

		16.2		16.2		16.2

		16.225		16.225		16.225

		16.25		16.25		16.25

		16.275		16.275		16.275

		16.3		16.3		16.3

		16.325		16.325		16.325

		16.35		16.35		16.35

		16.375		16.375		16.375

		16.4		16.4		16.4

		16.425		16.425		16.425

		16.45		16.45		16.45

		16.475		16.475		16.475

		16.5		16.5		16.5

		16.525		16.525		16.525

		16.55		16.55		16.55

		16.575		16.575		16.575

		16.6		16.6		16.6

		16.625		16.625		16.625

		16.65		16.65		16.65

		16.675		16.675		16.675

		16.7		16.7		16.7

		16.725		16.725		16.725

		16.75		16.75		16.75

		16.775		16.775		16.775

		16.8		16.8		16.8

		16.825		16.825		16.825

		16.85		16.85		16.85

		16.875		16.875		16.875

		16.9		16.9		16.9

		16.925		16.925		16.925

		16.95		16.95		16.95

		16.975		16.975		16.975

		17		17		17

		17.025		17.025		17.025

		17.05		17.05		17.05

		17.075		17.075		17.075

		17.1		17.1		17.1

		17.125		17.125		17.125

		17.15		17.15		17.15

		17.175		17.175		17.175

		17.2		17.2		17.2

		17.225		17.225		17.225

		17.25		17.25		17.25

		17.275		17.275		17.275

		17.3		17.3		17.3

		17.325		17.325		17.325

		17.35		17.35		17.35

		17.375		17.375		17.375

		17.4		17.4		17.4

		17.425		17.425		17.425

		17.45		17.45		17.45

		17.475		17.475		17.475

		17.5		17.5		17.5

		17.525		17.525		17.525

		17.55		17.55		17.55

		17.575		17.575		17.575

		17.6		17.6		17.6

		17.625		17.625		17.625

		17.65		17.65		17.65

		17.675		17.675		17.675

		17.7		17.7		17.7

		17.725		17.725		17.725

		17.75		17.75		17.75

		17.775		17.775		17.775

		17.8		17.8		17.8

		17.825		17.825		17.825

		17.85		17.85		17.85

		17.875		17.875		17.875

		17.9		17.9		17.9

		17.925		17.925		17.925

		17.95		17.95		17.95

		17.975		17.975		17.975

		18		18		18

		18.025		18.025		18.025

		18.05		18.05		18.05

		18.075		18.075		18.075

		18.1		18.1		18.1

		18.125		18.125		18.125

		18.15		18.15		18.15

		18.175		18.175		18.175

		18.2		18.2		18.2

		18.225		18.225		18.225

		18.25		18.25		18.25

		18.275		18.275		18.275

		18.3		18.3		18.3

		18.325		18.325		18.325

		18.35		18.35		18.35

		18.375		18.375		18.375

		18.4		18.4		18.4

		18.425		18.425		18.425

		18.45		18.45		18.45

		18.475		18.475		18.475

		18.5		18.5		18.5

		18.525		18.525		18.525

		18.55		18.55		18.55

		18.575		18.575		18.575

		18.6		18.6		18.6

		18.625		18.625		18.625

		18.65		18.65		18.65

		18.675		18.675		18.675

		18.7		18.7		18.7

		18.725		18.725		18.725

		18.75		18.75		18.75

		18.775		18.775		18.775

		18.8		18.8		18.8

		18.825		18.825		18.825

		18.85		18.85		18.85

		18.875		18.875		18.875

		18.9		18.9		18.9

		18.925		18.925		18.925

		18.95		18.95		18.95

		18.975		18.975		18.975

		19		19		19

		19.025		19.025		19.025

		19.05		19.05		19.05

		19.075		19.075		19.075

		19.1		19.1		19.1

		19.125		19.125		19.125

		19.15		19.15		19.15

		19.175		19.175		19.175

		19.2		19.2		19.2

		19.225		19.225		19.225

		19.25		19.25		19.25

		19.275		19.275		19.275

		19.3		19.3		19.3

		19.325		19.325		19.325

		19.35		19.35		19.35

		19.375		19.375		19.375

		19.4		19.4		19.4

		19.425		19.425		19.425

		19.45		19.45		19.45

		19.475		19.475		19.475

		19.5		19.5		19.5

		19.525		19.525		19.525

		19.55		19.55		19.55

		19.575		19.575		19.575

		19.6		19.6		19.6

		19.625		19.625		19.625

		19.65		19.65		19.65

		19.675		19.675		19.675

		19.7		19.7		19.7

		19.725		19.725		19.725

		19.75		19.75		19.75

		19.775		19.775		19.775

		19.8		19.8		19.8

		19.825		19.825		19.825

		19.85		19.85		19.85

		19.875		19.875		19.875

		19.9		19.9		19.9

		19.925		19.925		19.925

		19.95		19.95		19.95

		19.975		19.975		19.975

		20		20		20

		20.025		20.025		20.025

		20.05		20.05		20.05

		20.075		20.075		20.075

		20.1		20.1		20.1

		20.125		20.125		20.125

		20.15		20.15		20.15

		20.175		20.175		20.175

		20.2		20.2		20.2

		20.225		20.225		20.225

		20.25		20.25		20.25

		20.275		20.275		20.275

		20.3		20.3		20.3

		20.325		20.325		20.325

		20.35		20.35		20.35

		20.375		20.375		20.375

		20.4		20.4		20.4

		20.425		20.425		20.425

		20.45		20.45		20.45

		20.475		20.475		20.475

		20.5		20.5		20.5

		20.525		20.525		20.525

		20.55		20.55		20.55

		20.575		20.575		20.575

		20.6		20.6		20.6

		20.625		20.625		20.625

		20.65		20.65		20.65

		20.675		20.675		20.675

		20.7		20.7		20.7

		20.725		20.725		20.725

		20.75		20.75		20.75

		20.775		20.775		20.775

		20.8		20.8		20.8

		20.825		20.825		20.825

		20.85		20.85		20.85

		20.875		20.875		20.875

		20.9		20.9		20.9

		20.925		20.925		20.925

		20.95		20.95		20.95

		20.975		20.975		20.975

		21		21		21

		21.025		21.025		21.025

		21.05		21.05		21.05

		21.075		21.075		21.075

		21.1		21.1		21.1

		21.125		21.125		21.125

		21.15		21.15		21.15

		21.175		21.175		21.175

		21.2		21.2		21.2

		21.225		21.225		21.225

		21.25		21.25		21.25

		21.275		21.275		21.275

		21.3		21.3		21.3

		21.325		21.325		21.325

		21.35		21.35		21.35

		21.375		21.375		21.375

		21.4		21.4		21.4

		21.425		21.425		21.425

		21.45		21.45		21.45

		21.475		21.475		21.475

		21.5		21.5		21.5

		21.525		21.525		21.525

		21.55		21.55		21.55

		21.575		21.575		21.575

		21.6		21.6		21.6

		21.625		21.625		21.625

		21.65		21.65		21.65

		21.675		21.675		21.675

		21.7		21.7		21.7

		21.725		21.725		21.725

		21.75		21.75		21.75

		21.775		21.775		21.775

		21.8		21.8		21.8

		21.825		21.825		21.825

		21.85		21.85		21.85

		21.875		21.875		21.875

		21.9		21.9		21.9

		21.925		21.925		21.925

		21.95		21.95		21.95

		21.975		21.975		21.975

		22		22		22

		22.025		22.025		22.025

		22.05		22.05		22.05

		22.075		22.075		22.075

		22.1		22.1		22.1

		22.125		22.125		22.125

		22.15		22.15		22.15

		22.175		22.175		22.175

		22.2		22.2		22.2

		22.225		22.225		22.225

		22.25		22.25		22.25

		22.275		22.275		22.275

		22.3		22.3		22.3

		22.325		22.325		22.325

		22.35		22.35		22.35

		22.375		22.375		22.375

		22.4		22.4		22.4

		22.425		22.425		22.425

		22.45		22.45		22.45

		22.475		22.475		22.475

		22.5		22.5		22.5

		22.525		22.525		22.525

		22.55		22.55		22.55

		22.575		22.575		22.575

		22.6		22.6		22.6

		22.625		22.625		22.625

		22.65		22.65		22.65

		22.675		22.675		22.675

		22.7		22.7		22.7

		22.725		22.725		22.725

		22.75		22.75		22.75

		22.775		22.775		22.775

		22.8		22.8		22.8

		22.825		22.825		22.825

		22.85		22.85		22.85

		22.875		22.875		22.875

		22.9		22.9		22.9

		22.925		22.925		22.925

		22.95		22.95		22.95

		22.975		22.975		22.975

		23		23		23

		23.025		23.025		23.025

		23.05		23.05		23.05

		23.075		23.075		23.075

		23.1		23.1		23.1

		23.125		23.125		23.125

		23.15		23.15		23.15

		23.175		23.175		23.175

		23.2		23.2		23.2

		23.225		23.225		23.225

		23.25		23.25		23.25

		23.275		23.275		23.275

		23.3		23.3		23.3

		23.325		23.325		23.325

		23.35		23.35		23.35

		23.375		23.375		23.375

		23.4		23.4		23.4

		23.425		23.425		23.425

		23.45		23.45		23.45

		23.475		23.475		23.475

		23.5		23.5		23.5

		23.525		23.525		23.525

		23.55		23.55		23.55

		23.575		23.575		23.575

		23.6		23.6		23.6

		23.625		23.625		23.625

		23.65		23.65		23.65

		23.675		23.675		23.675

		23.7		23.7		23.7

		23.725		23.725		23.725

		23.75		23.75		23.75

		23.775		23.775		23.775

		23.8		23.8		23.8

		23.825		23.825		23.825

		23.85		23.85		23.85

		23.875		23.875		23.875

		23.9		23.9		23.9

		23.925		23.925		23.925

		23.95		23.95		23.95

		23.975		23.975		23.975

		24		24		24

		24.025		24.025		24.025

		24.05		24.05		24.05

		24.075		24.075		24.075

		24.1		24.1		24.1

		24.125		24.125		24.125

		24.15		24.15		24.15

		24.175		24.175		24.175

		24.2		24.2		24.2

		24.225		24.225		24.225

		24.25		24.25		24.25

		24.275		24.275		24.275

		24.3		24.3		24.3

		24.325		24.325		24.325

		24.35		24.35		24.35

		24.375		24.375		24.375

		24.4		24.4		24.4

		24.425		24.425		24.425

		24.45		24.45		24.45

		24.475		24.475		24.475

		24.5		24.5		24.5

		24.525		24.525		24.525

		24.55		24.55		24.55

		24.575		24.575		24.575

		24.6		24.6		24.6

		24.625		24.625		24.625

		24.65		24.65		24.65

		24.675		24.675		24.675

		24.7		24.7		24.7

		24.725		24.725		24.725

		24.75		24.75		24.75

		24.775		24.775		24.775

		24.8		24.8		24.8

		24.825		24.825		24.825

		24.85		24.85		24.85

		24.875		24.875		24.875

		24.9		24.9		24.9

		24.925		24.925		24.925

		24.95		24.95		24.95

		24.975		24.975		24.975

		25		25		25

		25.025		25.025		25.025

		25.05		25.05		25.05

		25.075		25.075		25.075

		25.1		25.1		25.1

		25.125		25.125		25.125

		25.15		25.15		25.15

		25.175		25.175		25.175

		25.2		25.2		25.2

		25.225		25.225		25.225

		25.25		25.25		25.25

		25.275		25.275		25.275

		25.3		25.3		25.3

		25.325		25.325		25.325

		25.35		25.35		25.35

		25.375		25.375		25.375

		25.4		25.4		25.4

		25.425		25.425		25.425

		25.45		25.45		25.45

		25.475		25.475		25.475

		25.5		25.5		25.5

		25.525		25.525		25.525

		25.55		25.55		25.55

		25.575		25.575		25.575

		25.6		25.6		25.6

		25.625		25.625		25.625

		25.65		25.65		25.65

		25.675		25.675		25.675

		25.7		25.7		25.7

		25.725		25.725		25.725

		25.75		25.75		25.75

		25.775		25.775		25.775

		25.8		25.8		25.8

		25.825		25.825		25.825

		25.85		25.85		25.85

		25.875		25.875		25.875

		25.9		25.9		25.9

		25.925		25.925		25.925

		25.95		25.95		25.95

		25.975		25.975		25.975

		26		26		26

		26.025		26.025		26.025

		26.05		26.05		26.05

		26.075		26.075		26.075

		26.1		26.1		26.1

		26.125		26.125		26.125

		26.15		26.15		26.15

		26.175		26.175		26.175

		26.2		26.2		26.2

		26.225		26.225		26.225

		26.25		26.25		26.25

		26.275		26.275		26.275

		26.3		26.3		26.3

		26.325		26.325		26.325

		26.35		26.35		26.35

		26.375		26.375		26.375

		26.4		26.4		26.4

		26.425		26.425		26.425

		26.45		26.45		26.45

		26.475		26.475		26.475

		26.5		26.5		26.5

		26.525		26.525		26.525

		26.55		26.55		26.55

		26.575		26.575		26.575

		26.6		26.6		26.6

		26.625		26.625		26.625

		26.65		26.65		26.65

		26.675		26.675		26.675

		26.7		26.7		26.7

		26.725		26.725		26.725

		26.75		26.75		26.75

		26.775		26.775		26.775

		26.8		26.8		26.8

		26.825		26.825		26.825

		26.85		26.85		26.85

		26.875		26.875		26.875

		26.9		26.9		26.9

		26.925		26.925		26.925

		26.95		26.95		26.95

		26.975		26.975		26.975

		27		27		27

		27.025		27.025		27.025

		27.05		27.05		27.05

		27.075		27.075		27.075

		27.1		27.1		27.1

		27.125		27.125		27.125

		27.15		27.15		27.15

		27.175		27.175		27.175

		27.2		27.2		27.2

		27.225		27.225		27.225

		27.25		27.25		27.25

		27.275		27.275		27.275

		27.3		27.3		27.3

		27.325		27.325		27.325

		27.35		27.35		27.35

		27.375		27.375		27.375

		27.4		27.4		27.4

		27.425		27.425		27.425

		27.45		27.45		27.45

		27.475		27.475		27.475

		27.5		27.5		27.5

		27.525		27.525		27.525

		27.55		27.55		27.55

		27.575		27.575		27.575

		27.6		27.6		27.6

		27.625		27.625		27.625

		27.65		27.65		27.65

		27.675		27.675		27.675

		27.7		27.7		27.7

		27.725		27.725		27.725

		27.75		27.75		27.75

		27.775		27.775		27.775

		27.8		27.8		27.8

		27.825		27.825		27.825

		27.85		27.85		27.85

		27.875		27.875		27.875

		27.9		27.9		27.9

		27.925		27.925		27.925

		27.95		27.95		27.95

		27.975		27.975		27.975

		28		28		28

		28.025		28.025		28.025

		28.05		28.05		28.05

		28.075		28.075		28.075

		28.1		28.1		28.1

		28.125		28.125		28.125

		28.15		28.15		28.15

		28.175		28.175		28.175

		28.2		28.2		28.2

		28.225		28.225		28.225

		28.25		28.25		28.25

		28.275		28.275		28.275

		28.3		28.3		28.3

		28.325		28.325		28.325

		28.35		28.35		28.35

		28.375		28.375		28.375

		28.4		28.4		28.4

		28.425		28.425		28.425

		28.45		28.45		28.45

		28.475		28.475		28.475

		28.5		28.5		28.5

		28.525		28.525		28.525

		28.55		28.55		28.55

		28.575		28.575		28.575

		28.6		28.6		28.6

		28.625		28.625		28.625

		28.65		28.65		28.65

		28.675		28.675		28.675

		28.7		28.7		28.7

		28.725		28.725		28.725

		28.75		28.75		28.75

		28.775		28.775		28.775

		28.8		28.8		28.8

		28.825		28.825		28.825

		28.85		28.85		28.85

		28.875		28.875		28.875

		28.9		28.9		28.9

		28.925		28.925		28.925

		28.95		28.95		28.95

		28.975		28.975		28.975

		29		29		29

		29.025		29.025		29.025

		29.05		29.05		29.05

		29.075		29.075		29.075

		29.1		29.1		29.1

		29.125		29.125		29.125

		29.15		29.15		29.15

		29.175		29.175		29.175

		29.2		29.2		29.2

		29.225		29.225		29.225

		29.25		29.25		29.25

		29.275		29.275		29.275

		29.3		29.3		29.3

		29.325		29.325		29.325

		29.35		29.35		29.35

		29.375		29.375		29.375

		29.4		29.4		29.4

		29.425		29.425		29.425

		29.45		29.45		29.45

		29.475		29.475		29.475

		29.5		29.5		29.5

		29.525		29.525		29.525

		29.55		29.55		29.55

		29.575		29.575		29.575

		29.6		29.6		29.6

		29.625		29.625		29.625

		29.65		29.65		29.65

		29.675		29.675		29.675

		29.7		29.7		29.7

		29.725		29.725		29.725

		29.75		29.75		29.75

		29.775		29.775		29.775

		29.8		29.8		29.8

		29.825		29.825		29.825

		29.85		29.85		29.85

		29.875		29.875		29.875

		29.9		29.9		29.9

		29.925		29.925		29.925

		29.95		29.95		29.95

		29.975		29.975		29.975

		30		30		30

		30.025		30.025		30.025

		30.05		30.05		30.05

		30.075		30.075		30.075

		30.1		30.1		30.1

		30.125		30.125		30.125

		30.15		30.15		30.15

		30.175		30.175		30.175

		30.2		30.2		30.2

		30.225		30.225		30.225

		30.25		30.25		30.25

		30.275		30.275		30.275

		30.3		30.3		30.3

		30.325		30.325		30.325

		30.35		30.35		30.35

		30.375		30.375		30.375

		30.4		30.4		30.4

		30.425		30.425		30.425

		30.45		30.45		30.45

		30.475		30.475		30.475

		30.5		30.5		30.5

		30.525		30.525		30.525

		30.55		30.55		30.55

		30.575		30.575		30.575

		30.6		30.6		30.6

		30.625		30.625		30.625

		30.65		30.65		30.65

		30.675		30.675		30.675

		30.7		30.7		30.7

		30.725		30.725		30.725

		30.75		30.75		30.75

		30.775		30.775		30.775

		30.8		30.8		30.8

		30.825		30.825		30.825

		30.85		30.85		30.85

		30.875		30.875		30.875

		30.9		30.9		30.9

		30.925		30.925		30.925

		30.95		30.95		30.95

		30.975		30.975		30.975

		31		31		31

		31.025		31.025		31.025

		31.05		31.05		31.05

		31.075		31.075		31.075

		31.1		31.1		31.1

		31.125		31.125		31.125

		31.15		31.15		31.15

		31.175		31.175		31.175

		31.2		31.2		31.2

		31.225		31.225		31.225

		31.25		31.25		31.25

		31.275		31.275		31.275

		31.3		31.3		31.3

		31.325		31.325		31.325

		31.35		31.35		31.35

		31.375		31.375		31.375

		31.4		31.4		31.4

		31.425		31.425		31.425

		31.45		31.45		31.45

		31.475		31.475		31.475

		31.5		31.5		31.5

		31.525		31.525		31.525

		31.55		31.55		31.55

		31.575		31.575		31.575

		31.6		31.6		31.6

		31.625		31.625		31.625

		31.65		31.65		31.65

		31.675		31.675		31.675

		31.7		31.7		31.7

		31.725		31.725		31.725

		31.75		31.75		31.75

		31.775		31.775		31.775

		31.8		31.8		31.8

		31.825		31.825		31.825

		31.85		31.85		31.85

		31.875		31.875		31.875

		31.9		31.9		31.9

		31.925		31.925		31.925

		31.95		31.95		31.95

		31.975		31.975		31.975

		32		32		32

		32.025		32.025		32.025

		32.05		32.05		32.05

		32.075		32.075		32.075

		32.1		32.1		32.1

		32.125		32.125		32.125

		32.15		32.15		32.15

		32.175		32.175		32.175

		32.2		32.2		32.2

		32.225		32.225		32.225

		32.25		32.25		32.25

		32.275		32.275		32.275

		32.3		32.3		32.3

		32.325		32.325		32.325

		32.35		32.35		32.35

		32.375		32.375		32.375

		32.4		32.4		32.4

		32.425		32.425		32.425

		32.45		32.45		32.45

		32.475		32.475		32.475

		32.5		32.5		32.5

		32.525		32.525		32.525

		32.55		32.55		32.55

		32.575		32.575		32.575

		32.6		32.6		32.6

		32.625		32.625		32.625

		32.65		32.65		32.65

		32.675		32.675		32.675

		32.7		32.7		32.7

		32.725		32.725		32.725

		32.75		32.75		32.75

		32.775		32.775		32.775

		32.8		32.8		32.8

		32.825		32.825		32.825

		32.85		32.85		32.85

		32.875		32.875		32.875

		32.9		32.9		32.9

		32.925		32.925		32.925

		32.95		32.95		32.95

		32.975		32.975		32.975

		33		33		33

		33.025		33.025		33.025

		33.05		33.05		33.05

		33.075		33.075		33.075

		33.1		33.1		33.1

		33.125		33.125		33.125

		33.15		33.15		33.15

		33.175		33.175		33.175

		33.2		33.2		33.2

		33.225		33.225		33.225

		33.25		33.25		33.25

		33.275		33.275		33.275

		33.3		33.3		33.3

		33.325		33.325		33.325

		33.35		33.35		33.35

		33.375		33.375		33.375

		33.4		33.4		33.4

		33.425		33.425		33.425

		33.45		33.45		33.45

		33.475		33.475		33.475

		33.5		33.5		33.5

		33.525		33.525		33.525

		33.55		33.55		33.55

		33.575		33.575		33.575

		33.6		33.6		33.6

		33.625		33.625		33.625

		33.65		33.65		33.65

		33.675		33.675		33.675

		33.7		33.7		33.7

		33.725		33.725		33.725

		33.75		33.75		33.75

		33.775		33.775		33.775

		33.8		33.8		33.8

		33.825		33.825		33.825

		33.85		33.85		33.85

		33.875		33.875		33.875

		33.9		33.9		33.9

		33.925		33.925		33.925

		33.95		33.95		33.95

		33.975		33.975		33.975

		34		34		34

		34.025		34.025		34.025

		34.05		34.05		34.05

		34.075		34.075		34.075

		34.1		34.1		34.1

		34.125		34.125		34.125

		34.15		34.15		34.15

		34.175		34.175		34.175

		34.2		34.2		34.2

		34.225		34.225		34.225

		34.25		34.25		34.25

		34.275		34.275		34.275

		34.3		34.3		34.3

		34.325		34.325		34.325

		34.35		34.35		34.35

		34.375		34.375		34.375

		34.4		34.4		34.4

		34.425		34.425		34.425

		34.45		34.45		34.45

		34.475		34.475		34.475

		34.5		34.5		34.5

		34.525		34.525		34.525

		34.55		34.55		34.55

		34.575		34.575		34.575

		34.6		34.6		34.6

		34.625		34.625		34.625

		34.65		34.65		34.65

		34.675		34.675		34.675

		34.7		34.7		34.7

		34.725		34.725		34.725

		34.75		34.75		34.75

		34.775		34.775		34.775

		34.8		34.8		34.8

		34.825		34.825		34.825

		34.85		34.85		34.85

		34.875		34.875		34.875

		34.9		34.9		34.9

		34.925		34.925		34.925

		34.95		34.95		34.95

		34.975		34.975		34.975

		35		35		35

		35.025		35.025		35.025

		35.05		35.05		35.05

		35.075		35.075		35.075

		35.1		35.1		35.1

		35.125		35.125		35.125

		35.15		35.15		35.15

		35.175		35.175		35.175

		35.2		35.2		35.2

		35.225		35.225		35.225

		35.25		35.25		35.25

		35.275		35.275		35.275

		35.3		35.3		35.3

		35.325		35.325		35.325

		35.35		35.35		35.35

		35.375		35.375		35.375

		35.4		35.4		35.4

		35.425		35.425		35.425

		35.45		35.45		35.45

		35.475		35.475		35.475

		35.5		35.5		35.5

		35.525		35.525		35.525

		35.55		35.55		35.55

		35.575		35.575		35.575

		35.6		35.6		35.6

		35.625		35.625		35.625

		35.65		35.65		35.65

		35.675		35.675		35.675

		35.7		35.7		35.7

		35.725		35.725		35.725

		35.75		35.75		35.75

		35.775		35.775		35.775

		35.8		35.8		35.8

		35.825		35.825		35.825

		35.85		35.85		35.85

		35.875		35.875		35.875

		35.9		35.9		35.9

		35.925		35.925		35.925

		35.95		35.95		35.95

		35.975		35.975		35.975

		36		36		36

		36.025		36.025		36.025

		36.05		36.05		36.05

		36.075		36.075		36.075

		36.1		36.1		36.1

		36.125		36.125		36.125

		36.15		36.15		36.15

		36.175		36.175		36.175

		36.2		36.2		36.2

		36.225		36.225		36.225

		36.25		36.25		36.25

		36.275		36.275		36.275

		36.3		36.3		36.3

		36.325		36.325		36.325

		36.35		36.35		36.35

		36.375		36.375		36.375

		36.4		36.4		36.4

		36.425		36.425		36.425

		36.45		36.45		36.45

		36.475		36.475		36.475

		36.5		36.5		36.5

		36.525		36.525		36.525

		36.55		36.55		36.55

		36.575		36.575		36.575

		36.6		36.6		36.6

		36.625		36.625		36.625

		36.65		36.65		36.65

		36.675		36.675		36.675

		36.7		36.7		36.7

		36.725		36.725		36.725

		36.75		36.75		36.75

		36.775		36.775		36.775

		36.8		36.8		36.8

		36.825		36.825		36.825

		36.85		36.85		36.85

		36.875		36.875		36.875

		36.9		36.9		36.9

		36.925		36.925		36.925

		36.95		36.95		36.95

		36.975		36.975		36.975

		37		37		37

		37.025		37.025		37.025

		37.05		37.05		37.05

		37.075		37.075		37.075

		37.1		37.1		37.1

		37.125		37.125		37.125

		37.15		37.15		37.15

		37.175		37.175		37.175

		37.2		37.2		37.2

		37.225		37.225		37.225

		37.25		37.25		37.25

		37.275		37.275		37.275

		37.3		37.3		37.3

		37.325		37.325		37.325

		37.35		37.35		37.35

		37.375		37.375		37.375

		37.4		37.4		37.4

		37.425		37.425		37.425

		37.45		37.45		37.45

		37.475		37.475		37.475

		37.5		37.5		37.5

		37.525		37.525		37.525

		37.55		37.55		37.55

		37.575		37.575		37.575

		37.6		37.6		37.6

		37.625		37.625		37.625

		37.65		37.65		37.65

		37.675		37.675		37.675

		37.7		37.7		37.7

		37.725		37.725		37.725

		37.75		37.75		37.75

		37.775		37.775		37.775

		37.8		37.8		37.8

		37.825		37.825		37.825

		37.85		37.85		37.85

		37.875		37.875		37.875

		37.9		37.9		37.9

		37.925		37.925		37.925

		37.95		37.95		37.95

		37.975		37.975		37.975

		38		38		38

		38.025		38.025		38.025

		38.05		38.05		38.05

		38.075		38.075		38.075

		38.1		38.1		38.1

		38.125		38.125		38.125

		38.15		38.15		38.15

		38.175		38.175		38.175

		38.2		38.2		38.2

		38.225		38.225		38.225

		38.25		38.25		38.25

		38.275		38.275		38.275

		38.3		38.3		38.3

		38.325		38.325		38.325

		38.35		38.35		38.35

		38.375		38.375		38.375

		38.4		38.4		38.4

		38.425		38.425		38.425

		38.45		38.45		38.45

		38.475		38.475		38.475

		38.5		38.5		38.5

		38.525		38.525		38.525

		38.55		38.55		38.55

		38.575		38.575		38.575

		38.6		38.6		38.6

		38.625		38.625		38.625

		38.65		38.65		38.65

		38.675		38.675		38.675

		38.7		38.7		38.7

		38.725		38.725		38.725

		38.75		38.75		38.75

		38.775		38.775		38.775

		38.8		38.8		38.8

		38.825		38.825		38.825

		38.85		38.85		38.85

		38.875		38.875		38.875

		38.9		38.9		38.9

		38.925		38.925		38.925

		38.95		38.95		38.95

		38.975		38.975		38.975

		39		39		39

		39.025		39.025		39.025

		39.05		39.05		39.05

		39.075		39.075		39.075

		39.1		39.1		39.1

		39.125		39.125		39.125

		39.15		39.15		39.15

		39.175		39.175		39.175

		39.2		39.2		39.2

		39.225		39.225		39.225

		39.25		39.25		39.25

		39.275		39.275		39.275

		39.3		39.3		39.3

		39.325		39.325		39.325

		39.35		39.35		39.35

		39.375		39.375		39.375

		39.4		39.4		39.4

		39.425		39.425		39.425

		39.45		39.45		39.45

		39.475		39.475		39.475

		39.5		39.5		39.5

		39.525		39.525		39.525

		39.55		39.55		39.55

		39.575		39.575		39.575

		39.6		39.6		39.6

		39.625		39.625		39.625

		39.65		39.65		39.65

		39.675		39.675		39.675

		39.7		39.7		39.7

		39.725		39.725		39.725

		39.75		39.75		39.75

		39.775		39.775		39.775

		39.8		39.8		39.8

		39.825		39.825		39.825

		39.85		39.85		39.85

		39.875		39.875		39.875

		39.9		39.9		39.9

		39.925		39.925		39.925

		39.95		39.95		39.95

		39.975		39.975		39.975

		40		40		40

		40.025		40.025		40.025

		40.05		40.05		40.05

		40.075		40.075		40.075

		40.1		40.1		40.1

		40.125		40.125		40.125

		40.15		40.15		40.15

		40.175		40.175		40.175

		40.2		40.2		40.2

		40.225		40.225		40.225

		40.25		40.25		40.25

		40.275		40.275		40.275

		40.3		40.3		40.3

		40.325		40.325		40.325

		40.35		40.35		40.35

		40.375		40.375		40.375

		40.4		40.4		40.4

		40.425		40.425		40.425

		40.45		40.45		40.45

		40.475		40.475		40.475

		40.5		40.5		40.5

		40.525		40.525		40.525

		40.55		40.55		40.55

		40.575		40.575		40.575

		40.6		40.6		40.6

		40.625		40.625		40.625

		40.65		40.65		40.65

		40.675		40.675		40.675

		40.7		40.7		40.7

		40.725		40.725		40.725

		40.75		40.75		40.75

		40.775		40.775		40.775

		40.8		40.8		40.8

		40.825		40.825		40.825

		40.85		40.85		40.85

		40.875		40.875		40.875

		40.9		40.9		40.9

		40.925		40.925		40.925

		40.95		40.95		40.95

		40.975		40.975		40.975

		41		41		41

		41.025		41.025		41.025

		41.05		41.05		41.05

		41.075		41.075		41.075

		41.1		41.1		41.1

		41.125		41.125		41.125

		41.15		41.15		41.15

		41.175		41.175		41.175

		41.2		41.2		41.2

		41.225		41.225		41.225

		41.25		41.25		41.25

		41.275		41.275		41.275

		41.3		41.3		41.3

		41.325		41.325		41.325

		41.35		41.35		41.35

		41.375		41.375		41.375

		41.4		41.4		41.4

		41.425		41.425		41.425

		41.45		41.45		41.45

		41.475		41.475		41.475

		41.5		41.5		41.5

		41.525		41.525		41.525

		41.55		41.55		41.55

		41.575		41.575		41.575

		41.6		41.6		41.6

		41.625		41.625		41.625

		41.65		41.65		41.65

		41.675		41.675		41.675

		41.7		41.7		41.7

		41.725		41.725		41.725

		41.75		41.75		41.75

		41.775		41.775		41.775

		41.8		41.8		41.8

		41.825		41.825		41.825

		41.85		41.85		41.85

		41.875		41.875		41.875

		41.9		41.9		41.9

		41.925		41.925		41.925

		41.95		41.95		41.95

		41.975		41.975		41.975

		42		42		42

		42.025		42.025		42.025

		42.05		42.05		42.05

		42.075		42.075		42.075

		42.1		42.1		42.1

		42.125		42.125		42.125

		42.15		42.15		42.15

		42.175		42.175		42.175

		42.2		42.2		42.2

		42.225		42.225		42.225

		42.25		42.25		42.25

		42.275		42.275		42.275

		42.3		42.3		42.3

		42.325		42.325		42.325

		42.35		42.35		42.35

		42.375		42.375		42.375

		42.4		42.4		42.4

		42.425		42.425		42.425

		42.45		42.45		42.45

		42.475		42.475		42.475

		42.5		42.5		42.5

		42.525		42.525		42.525

		42.55		42.55		42.55

		42.575		42.575		42.575

		42.6		42.6		42.6

		42.625		42.625		42.625

		42.65		42.65		42.65

		42.675		42.675		42.675

		42.7		42.7		42.7

		42.725		42.725		42.725

		42.75		42.75		42.75

		42.775		42.775		42.775

		42.8		42.8		42.8

		42.825		42.825		42.825

		42.85		42.85		42.85

		42.875		42.875		42.875

		42.9		42.9		42.9

		42.925		42.925		42.925

		42.95		42.95		42.95

		42.975		42.975		42.975

		43		43		43

		43.025		43.025		43.025

		43.05		43.05		43.05

		43.075		43.075		43.075

		43.1		43.1		43.1

		43.125		43.125		43.125

		43.15		43.15		43.15

		43.175		43.175		43.175

		43.2		43.2		43.2

		43.225		43.225		43.225

		43.25		43.25		43.25

		43.275		43.275		43.275

		43.3		43.3		43.3

		43.325		43.325		43.325

		43.35		43.35		43.35

		43.375		43.375		43.375

		43.4		43.4		43.4

		43.425		43.425		43.425

		43.45		43.45		43.45

		43.475		43.475		43.475

		43.5		43.5		43.5

		43.525		43.525		43.525

		43.55		43.55		43.55

		43.575		43.575		43.575

		43.6		43.6		43.6

		43.625		43.625		43.625

		43.65		43.65		43.65

		43.675		43.675		43.675

		43.7		43.7		43.7

		43.725		43.725		43.725

		43.75		43.75		43.75

		43.775		43.775		43.775

		43.8		43.8		43.8

		43.825		43.825		43.825

		43.85		43.85		43.85

		43.875		43.875		43.875

		43.9		43.9		43.9

		43.925		43.925		43.925

		43.95		43.95		43.95

		43.975		43.975		43.975

		44		44		44

		44.025		44.025		44.025

		44.05		44.05		44.05

		44.075		44.075		44.075

		44.1		44.1		44.1

		44.125		44.125		44.125

		44.15		44.15		44.15

		44.175		44.175		44.175

		44.2		44.2		44.2

		44.225		44.225		44.225

		44.25		44.25		44.25

		44.275		44.275		44.275

		44.3		44.3		44.3

		44.325		44.325		44.325

		44.35		44.35		44.35

		44.375		44.375		44.375

		44.4		44.4		44.4

		44.425		44.425		44.425

		44.45		44.45		44.45

		44.475		44.475		44.475

		44.5		44.5		44.5

		44.525		44.525		44.525

		44.55		44.55		44.55

		44.575		44.575		44.575

		44.6		44.6		44.6

		44.625		44.625		44.625

		44.65		44.65		44.65

		44.675		44.675		44.675

		44.7		44.7		44.7

		44.725		44.725		44.725

		44.75		44.75		44.75

		44.775		44.775		44.775

		44.8		44.8		44.8

		44.825		44.825		44.825

		44.85		44.85		44.85

		44.875		44.875		44.875

		44.9		44.9		44.9

		44.925		44.925		44.925

		44.95		44.95		44.95

		44.975		44.975		44.975

		45		45		45

		45.025		45.025		45.025

		45.05		45.05		45.05

		45.075		45.075		45.075

		45.1		45.1		45.1

		45.125		45.125		45.125

		45.15		45.15		45.15

		45.175		45.175		45.175

		45.2		45.2		45.2

		45.225		45.225		45.225

		45.25		45.25		45.25

		45.275		45.275		45.275

		45.3		45.3		45.3

		45.325		45.325		45.325

		45.35		45.35		45.35

		45.375		45.375		45.375

		45.4		45.4		45.4

		45.425		45.425		45.425

		45.45		45.45		45.45

		45.475		45.475		45.475

		45.5		45.5		45.5

		45.525		45.525		45.525

		45.55		45.55		45.55

		45.575		45.575		45.575

		45.6		45.6		45.6

		45.625		45.625		45.625

		45.65		45.65		45.65

		45.675		45.675		45.675

		45.7		45.7		45.7

		45.725		45.725		45.725

		45.75		45.75		45.75

		45.775		45.775		45.775

		45.8		45.8		45.8

		45.825		45.825		45.825

		45.85		45.85		45.85

		45.875		45.875		45.875

		45.9		45.9		45.9

		45.925		45.925		45.925

		45.95		45.95		45.95

		45.975		45.975		45.975

		46		46		46

		46.025		46.025		46.025

		46.05		46.05		46.05

		46.075		46.075		46.075

		46.1		46.1		46.1

		46.125		46.125		46.125

		46.15		46.15		46.15

		46.175		46.175		46.175

		46.2		46.2		46.2

		46.225		46.225		46.225

		46.25		46.25		46.25

		46.275		46.275		46.275

		46.3		46.3		46.3

		46.325		46.325		46.325

		46.35		46.35		46.35

		46.375		46.375		46.375

		46.4		46.4		46.4

		46.425		46.425		46.425

		46.45		46.45		46.45

		46.475		46.475		46.475

		46.5		46.5		46.5

		46.525		46.525		46.525

		46.55		46.55		46.55

		46.575		46.575		46.575

		46.6		46.6		46.6

		46.625		46.625		46.625

		46.65		46.65		46.65

		46.675		46.675		46.675

		46.7		46.7		46.7

		46.725		46.725		46.725

		46.75		46.75		46.75

		46.775		46.775		46.775

		46.8		46.8		46.8

		46.825		46.825		46.825

		46.85		46.85		46.85

		46.875		46.875		46.875

		46.9		46.9		46.9

		46.925		46.925		46.925

		46.95		46.95		46.95

		46.975		46.975		46.975

		47		47		47

		47.025		47.025		47.025

		47.05		47.05		47.05

		47.075		47.075		47.075

		47.1		47.1		47.1

		47.125		47.125		47.125

		47.15		47.15		47.15

		47.175		47.175		47.175

		47.2		47.2		47.2

		47.225		47.225		47.225

		47.25		47.25		47.25

		47.275		47.275		47.275

		47.3		47.3		47.3

		47.325		47.325		47.325

		47.35		47.35		47.35

		47.375		47.375		47.375

		47.4		47.4		47.4

		47.425		47.425		47.425

		47.45		47.45		47.45

		47.475		47.475		47.475

		47.5		47.5		47.5

		47.525		47.525		47.525

		47.55		47.55		47.55

		47.575		47.575		47.575

		47.6		47.6		47.6

		47.625		47.625		47.625

		47.65		47.65		47.65

		47.675		47.675		47.675

		47.7		47.7		47.7

		47.725		47.725		47.725

		47.75		47.75		47.75

		47.775		47.775		47.775

		47.8		47.8		47.8

		47.825		47.825		47.825

		47.85		47.85		47.85

		47.875		47.875		47.875

		47.9		47.9		47.9

		47.925		47.925		47.925

		47.95		47.95		47.95

		47.975		47.975		47.975

		48		48		48

		48.025		48.025		48.025

		48.05		48.05		48.05

		48.075		48.075		48.075

		48.1		48.1		48.1

		48.125		48.125		48.125

		48.15		48.15		48.15

		48.175		48.175		48.175

		48.2		48.2		48.2

		48.225		48.225		48.225

		48.25		48.25		48.25

		48.275		48.275		48.275

		48.3		48.3		48.3

		48.325		48.325		48.325

		48.35		48.35		48.35

		48.375		48.375		48.375

		48.4		48.4		48.4

		48.425		48.425		48.425

		48.45		48.45		48.45

		48.475		48.475		48.475

		48.5		48.5		48.5

		48.525		48.525		48.525

		48.55		48.55		48.55

		48.575		48.575		48.575

		48.6		48.6		48.6

		48.625		48.625		48.625

		48.65		48.65		48.65

		48.675		48.675		48.675

		48.7		48.7		48.7

		48.725		48.725		48.725

		48.75		48.75		48.75

		48.775		48.775		48.775

		48.8		48.8		48.8

		48.825		48.825		48.825

		48.85		48.85		48.85

		48.875		48.875		48.875

		48.9		48.9		48.9

		48.925		48.925		48.925

		48.95		48.95		48.95

		48.975		48.975		48.975

		49		49		49

		49.025		49.025		49.025

		49.05		49.05		49.05

		49.075		49.075		49.075

		49.1		49.1		49.1

		49.125		49.125		49.125

		49.15		49.15		49.15

		49.175		49.175		49.175

		49.2		49.2		49.2

		49.225		49.225		49.225

		49.25		49.25		49.25

		49.275		49.275		49.275

		49.3		49.3		49.3

		49.325		49.325		49.325

		49.35		49.35		49.35

		49.375		49.375		49.375

		49.4		49.4		49.4

		49.425		49.425		49.425

		49.45		49.45		49.45

		49.475		49.475		49.475

		49.5		49.5		49.5

		49.525		49.525		49.525

		49.55		49.55		49.55

		49.575		49.575		49.575

		49.6		49.6		49.6

		49.625		49.625		49.625

		49.65		49.65		49.65

		49.675		49.675		49.675

		49.7		49.7		49.7

		49.725		49.725		49.725

		49.75		49.75		49.75

		49.775		49.775		49.775

		49.8		49.8		49.8

		49.825		49.825		49.825

		49.85		49.85		49.85

		49.875		49.875		49.875

		49.9		49.9		49.9

		49.925		49.925		49.925

		49.95		49.95		49.95

		49.975		49.975		49.975

		50		50		50

		50.025		50.025		50.025

		50.05		50.05		50.05

		50.075		50.075		50.075

		50.1		50.1		50.1

		50.125		50.125		50.125

		50.15		50.15		50.15

		50.175		50.175		50.175

		50.2		50.2		50.2

		50.225		50.225		50.225

		50.25		50.25		50.25

		50.275		50.275		50.275

		50.3		50.3		50.3

		50.325		50.325		50.325

		50.35		50.35		50.35

		50.375		50.375		50.375

		50.4		50.4		50.4

		50.425		50.425		50.425

		50.45		50.45		50.45

		50.475		50.475		50.475

		50.5		50.5		50.5

		50.525		50.525		50.525

		50.55		50.55		50.55

		50.575		50.575		50.575

		50.6		50.6		50.6

		50.625		50.625		50.625

		50.65		50.65		50.65

		50.675		50.675		50.675

		50.7		50.7		50.7

		50.725		50.725		50.725

		50.75		50.75		50.75

		50.775		50.775		50.775

		50.8		50.8		50.8

		50.825		50.825		50.825

		50.85		50.85		50.85

		50.875		50.875		50.875

		50.9		50.9		50.9

		50.925		50.925		50.925

		50.95		50.95		50.95

		50.975		50.975		50.975

		51		51		51

		51.025		51.025		51.025

		51.05		51.05		51.05

		51.075		51.075		51.075

		51.1		51.1		51.1

		51.125		51.125		51.125

		51.15		51.15		51.15

		51.175		51.175		51.175

		51.2		51.2		51.2

		51.225		51.225		51.225

		51.25		51.25		51.25

		51.275		51.275		51.275

		51.3		51.3		51.3

		51.325		51.325		51.325

		51.35		51.35		51.35

		51.375		51.375		51.375

		51.4		51.4		51.4

		51.425		51.425		51.425

		51.45		51.45		51.45

		51.475		51.475		51.475

		51.5		51.5		51.5

		51.525		51.525		51.525

		51.55		51.55		51.55

		51.575		51.575		51.575

		51.6		51.6		51.6

		51.625		51.625		51.625

		51.65		51.65		51.65

		51.675		51.675		51.675

		51.7		51.7		51.7

		51.725		51.725		51.725

		51.75		51.75		51.75

		51.775		51.775		51.775

		51.8		51.8		51.8

		51.825		51.825		51.825

		51.85		51.85		51.85

		51.875		51.875		51.875

		51.9		51.9		51.9

		51.925		51.925		51.925

		51.95		51.95		51.95

		51.975		51.975		51.975

		52		52		52

		52.025		52.025		52.025

		52.05		52.05		52.05

		52.075		52.075		52.075

		52.1		52.1		52.1

		52.125		52.125		52.125

		52.15		52.15		52.15

		52.175		52.175		52.175

		52.2		52.2		52.2

		52.225		52.225		52.225

		52.25		52.25		52.25

		52.275		52.275		52.275

		52.3		52.3		52.3

		52.325		52.325		52.325

		52.35		52.35		52.35

		52.375		52.375		52.375

		52.4		52.4		52.4

		52.425		52.425		52.425

		52.45		52.45		52.45

		52.475		52.475		52.475

		52.5		52.5		52.5

		52.525		52.525		52.525

		52.55		52.55		52.55

		52.575		52.575		52.575

		52.6		52.6		52.6

		52.625		52.625		52.625

		52.65		52.65		52.65

		52.675		52.675		52.675

		52.7		52.7		52.7

		52.725		52.725		52.725

		52.75		52.75		52.75

		52.775		52.775		52.775

		52.8		52.8		52.8

		52.825		52.825		52.825

		52.85		52.85		52.85

		52.875		52.875		52.875

		52.9		52.9		52.9

		52.925		52.925		52.925

		52.95		52.95		52.95

		52.975		52.975		52.975

		53		53		53

		53.025		53.025		53.025

		53.05		53.05		53.05

		53.075		53.075		53.075

		53.1		53.1		53.1

		53.125		53.125		53.125

		53.15		53.15		53.15

		53.175		53.175		53.175

		53.2		53.2		53.2

		53.225		53.225		53.225

		53.25		53.25		53.25

		53.275		53.275		53.275

		53.3		53.3		53.3

		53.325		53.325		53.325

		53.35		53.35		53.35

		53.375		53.375		53.375

		53.4		53.4		53.4

		53.425		53.425		53.425

		53.45		53.45		53.45

		53.475		53.475		53.475

		53.5		53.5		53.5

		53.525		53.525		53.525

		53.55		53.55		53.55

		53.575		53.575		53.575

		53.6		53.6		53.6

		53.625		53.625		53.625

		53.65		53.65		53.65

		53.675		53.675		53.675

		53.7		53.7		53.7

		53.725		53.725		53.725

		53.75		53.75		53.75

		53.775		53.775		53.775

		53.8		53.8		53.8

		53.825		53.825		53.825

		53.85		53.85		53.85

		53.875		53.875		53.875

		53.9		53.9		53.9

		53.925		53.925		53.925

		53.95		53.95		53.95

		53.975		53.975		53.975

		54		54		54

		54.025		54.025		54.025

		54.05		54.05		54.05

		54.075		54.075		54.075

		54.1		54.1		54.1

		54.125		54.125		54.125

		54.15		54.15		54.15

		54.175		54.175		54.175

		54.2		54.2		54.2

		54.225		54.225		54.225

		54.25		54.25		54.25

		54.275		54.275		54.275

		54.3		54.3		54.3

		54.325		54.325		54.325

		54.35		54.35		54.35

		54.375		54.375		54.375

		54.4		54.4		54.4

		54.425		54.425		54.425

		54.45		54.45		54.45

		54.475		54.475		54.475

		54.5		54.5		54.5

		54.525		54.525		54.525

		54.55		54.55		54.55

		54.575		54.575		54.575

		54.6		54.6		54.6

		54.625		54.625		54.625

		54.65		54.65		54.65

		54.675		54.675		54.675

		54.7		54.7		54.7

		54.725		54.725		54.725

		54.75		54.75		54.75

		54.775		54.775		54.775

		54.8		54.8		54.8

		54.825		54.825		54.825

		54.85		54.85		54.85

		54.875		54.875		54.875

		54.9		54.9		54.9

		54.925		54.925		54.925

		54.95		54.95		54.95

		54.975		54.975		54.975

		55		55		55

		55.025		55.025		55.025

		55.05		55.05		55.05

		55.075		55.075		55.075

		55.1		55.1		55.1

		55.125		55.125		55.125

		55.15		55.15		55.15

		55.175		55.175		55.175

		55.2		55.2		55.2

		55.225		55.225		55.225

		55.25		55.25		55.25

		55.275		55.275		55.275

		55.3		55.3		55.3

		55.325		55.325		55.325

		55.35		55.35		55.35

		55.375		55.375		55.375

		55.4		55.4		55.4

		55.425		55.425		55.425

		55.45		55.45		55.45

		55.475		55.475		55.475

		55.5		55.5		55.5

		55.525		55.525		55.525

		55.55		55.55		55.55

		55.575		55.575		55.575

		55.6		55.6		55.6

		55.625		55.625		55.625

		55.65		55.65		55.65

		55.675		55.675		55.675

		55.7		55.7		55.7

		55.725		55.725		55.725

		55.75		55.75		55.75

		55.775		55.775		55.775

		55.8		55.8		55.8

		55.825		55.825		55.825

		55.85		55.85		55.85

		55.875		55.875		55.875

		55.9		55.9		55.9

		55.925		55.925		55.925

		55.95		55.95		55.95

		55.975		55.975		55.975

		56		56		56

		56.025		56.025		56.025

		56.05		56.05		56.05

		56.075		56.075		56.075

		56.1		56.1		56.1

		56.125		56.125		56.125

		56.15		56.15		56.15

		56.175		56.175		56.175

		56.2		56.2		56.2

		56.225		56.225		56.225

		56.25		56.25		56.25

		56.275		56.275		56.275

		56.3		56.3		56.3

		56.325		56.325		56.325

		56.35		56.35		56.35

		56.375		56.375		56.375

		56.4		56.4		56.4

		56.425		56.425		56.425

		56.45		56.45		56.45

		56.475		56.475		56.475

		56.5		56.5		56.5

		56.525		56.525		56.525

		56.55		56.55		56.55

		56.575		56.575		56.575

		56.6		56.6		56.6

		56.625		56.625		56.625

		56.65		56.65		56.65

		56.675		56.675		56.675

		56.7		56.7		56.7

		56.725		56.725		56.725

		56.75		56.75		56.75

		56.775		56.775		56.775

		56.8		56.8		56.8

		56.825		56.825		56.825

		56.85		56.85		56.85

		56.875		56.875		56.875

		56.9		56.9		56.9

		56.925		56.925		56.925

		56.95		56.95		56.95

		56.975		56.975		56.975

		57		57		57

		57.025		57.025		57.025

		57.05		57.05		57.05

		57.075		57.075		57.075

		57.1		57.1		57.1

		57.125		57.125		57.125

		57.15		57.15		57.15

		57.175		57.175		57.175

		57.2		57.2		57.2

		57.225		57.225		57.225

		57.25		57.25		57.25

		57.275		57.275		57.275

		57.3		57.3		57.3

		57.325		57.325		57.325

		57.35		57.35		57.35

		57.375		57.375		57.375

		57.4		57.4		57.4

		57.425		57.425		57.425

		57.45		57.45		57.45

		57.475		57.475		57.475

		57.5		57.5		57.5

		57.525		57.525		57.525

		57.55		57.55		57.55

		57.575		57.575		57.575

		57.6		57.6		57.6

		57.625		57.625		57.625

		57.65		57.65		57.65

		57.675		57.675		57.675

		57.7		57.7		57.7

		57.725		57.725		57.725

		57.75		57.75		57.75

		57.775		57.775		57.775

		57.8		57.8		57.8

		57.825		57.825		57.825

		57.85		57.85		57.85

		57.875		57.875		57.875

		57.9		57.9		57.9

		57.925		57.925		57.925

		57.95		57.95		57.95

		57.975		57.975		57.975

		58		58		58

		58.025		58.025		58.025

		58.05		58.05		58.05

		58.075		58.075		58.075

		58.1		58.1		58.1

		58.125		58.125		58.125

		58.15		58.15		58.15

		58.175		58.175		58.175

		58.2		58.2		58.2

		58.225		58.225		58.225

		58.25		58.25		58.25

		58.275		58.275		58.275

		58.3		58.3		58.3

		58.325		58.325		58.325

		58.35		58.35		58.35

		58.375		58.375		58.375

		58.4		58.4		58.4

		58.425		58.425		58.425

		58.45		58.45		58.45

		58.475		58.475		58.475

		58.5		58.5		58.5

		58.525		58.525		58.525

		58.55		58.55		58.55

		58.575		58.575		58.575

		58.6		58.6		58.6

		58.625		58.625		58.625

		58.65		58.65		58.65

		58.675		58.675		58.675

		58.7		58.7		58.7

		58.725		58.725		58.725

		58.75		58.75		58.75

		58.775		58.775		58.775

		58.8		58.8		58.8

		58.825		58.825		58.825

		58.85		58.85		58.85

		58.875		58.875		58.875

		58.9		58.9		58.9

		58.925		58.925		58.925

		58.95		58.95		58.95

		58.975		58.975		58.975

		59		59		59

		59.025		59.025		59.025

		59.05		59.05		59.05

		59.075		59.075		59.075

		59.1		59.1		59.1

		59.125		59.125		59.125

		59.15		59.15		59.15

		59.175		59.175		59.175

		59.2		59.2		59.2

		59.225		59.225		59.225

		59.25		59.25		59.25

		59.275		59.275		59.275

		59.3		59.3		59.3

		59.325		59.325		59.325

		59.35		59.35		59.35

		59.375		59.375		59.375

		59.4		59.4		59.4

		59.425		59.425		59.425

		59.45		59.45		59.45

		59.475		59.475		59.475

		59.5		59.5		59.5

		59.525		59.525		59.525

		59.55		59.55		59.55

		59.575		59.575		59.575

		59.6		59.6		59.6

		59.625		59.625		59.625

		59.65		59.65		59.65

		59.675		59.675		59.675

		59.7		59.7		59.7

		59.725		59.725		59.725

		59.75		59.75		59.75

		59.775		59.775		59.775

		59.8		59.8		59.8

		59.825		59.825		59.825

		59.85		59.85		59.85

		59.875		59.875		59.875

		59.9		59.9		59.9

		59.925		59.925		59.925

		59.95		59.95		59.95

		59.975		59.975		59.975

		60		60		60

		60.025		60.025		60.025

		60.05		60.05		60.05

		60.075		60.075		60.075

		60.1		60.1		60.1

		60.125		60.125		60.125

		60.15		60.15		60.15

		60.175		60.175		60.175

		60.2		60.2		60.2

		60.225		60.225		60.225

		60.25		60.25		60.25

		60.275		60.275		60.275

		60.3		60.3		60.3

		60.325		60.325		60.325

		60.35		60.35		60.35

		60.375		60.375		60.375

		60.4		60.4		60.4

		60.425		60.425		60.425

		60.45		60.45		60.45

		60.475		60.475		60.475

		60.5		60.5		60.5

		60.525		60.525		60.525

		60.55		60.55		60.55

		60.575		60.575		60.575

		60.6		60.6		60.6

		60.625		60.625		60.625

		60.65		60.65		60.65

		60.675		60.675		60.675

		60.7		60.7		60.7

		60.725		60.725		60.725

		60.75		60.75		60.75

		60.775		60.775		60.775

		60.8		60.8		60.8

		60.825		60.825		60.825

		60.85		60.85		60.85

		60.875		60.875		60.875

		60.9		60.9		60.9

		60.925		60.925		60.925

		60.95		60.95		60.95

		60.975		60.975		60.975

		61		61		61

		61.025		61.025		61.025

		61.05		61.05		61.05

		61.075		61.075		61.075

		61.1		61.1		61.1

		61.125		61.125		61.125

		61.15		61.15		61.15

		61.175		61.175		61.175

		61.2		61.2		61.2

		61.225		61.225		61.225

		61.25		61.25		61.25

		61.275		61.275		61.275

		61.3		61.3		61.3

		61.325		61.325		61.325

		61.35		61.35		61.35

		61.375		61.375		61.375

		61.4		61.4		61.4

		61.425		61.425		61.425

		61.45		61.45		61.45

		61.475		61.475		61.475

		61.5		61.5		61.5

		61.525		61.525		61.525

		61.55		61.55		61.55

		61.575		61.575		61.575

		61.6		61.6		61.6

		61.625		61.625		61.625

		61.65		61.65		61.65

		61.675		61.675		61.675

		61.7		61.7		61.7

		61.725		61.725		61.725

		61.75		61.75		61.75

		61.775		61.775		61.775

		61.8		61.8		61.8

		61.825		61.825		61.825

		61.85		61.85		61.85

		61.875		61.875		61.875

		61.9		61.9		61.9

		61.925		61.925		61.925

		61.95		61.95		61.95

		61.975		61.975		61.975

		62		62		62

		62.025		62.025		62.025

		62.05		62.05		62.05

		62.075		62.075		62.075

		62.1		62.1		62.1

		62.125		62.125		62.125

		62.15		62.15		62.15

		62.175		62.175		62.175

		62.2		62.2		62.2

		62.225		62.225		62.225

		62.25		62.25		62.25

		62.275		62.275		62.275

		62.3		62.3		62.3

		62.325		62.325		62.325

		62.35		62.35		62.35

		62.375		62.375		62.375

		62.4		62.4		62.4

		62.425		62.425		62.425

		62.45		62.45		62.45

		62.475		62.475		62.475

		62.5		62.5		62.5

		62.525		62.525		62.525

		62.55		62.55		62.55

		62.575		62.575		62.575

		62.6		62.6		62.6

		62.625		62.625		62.625

		62.65		62.65		62.65

		62.675		62.675		62.675

		62.7		62.7		62.7

		62.725		62.725		62.725

		62.75		62.75		62.75

		62.775		62.775		62.775

		62.8		62.8		62.8

		62.825		62.825		62.825

		62.85		62.85		62.85

		62.875		62.875		62.875

		62.9		62.9		62.9

		62.925		62.925		62.925

		62.95		62.95		62.95

		62.975		62.975		62.975

		63		63		63

		63.025		63.025		63.025

		63.05		63.05		63.05

		63.075		63.075		63.075

		63.1		63.1		63.1

		63.125		63.125		63.125

		63.15		63.15		63.15

		63.175		63.175		63.175

		63.2		63.2		63.2

		63.225		63.225		63.225

		63.25		63.25		63.25

		63.275		63.275		63.275

		63.3		63.3		63.3

		63.325		63.325		63.325

		63.35		63.35		63.35

		63.375		63.375		63.375

		63.4		63.4		63.4

		63.425		63.425		63.425

		63.45		63.45		63.45

		63.475		63.475		63.475

		63.5		63.5		63.5

		63.525		63.525		63.525

		63.55		63.55		63.55

		63.575		63.575		63.575

		63.6		63.6		63.6

		63.625		63.625		63.625

		63.65		63.65		63.65

		63.675		63.675		63.675

		63.7		63.7		63.7

		63.725		63.725		63.725

		63.75		63.75		63.75

		63.775		63.775		63.775

		63.8		63.8		63.8

		63.825		63.825		63.825

		63.85		63.85		63.85

		63.875		63.875		63.875

		63.9		63.9		63.9

		63.925		63.925		63.925

		63.95		63.95		63.95

		63.975		63.975		63.975

		64		64		64

		64.025		64.025		64.025

		64.05		64.05		64.05

		64.075		64.075		64.075

		64.1		64.1		64.1

		64.125		64.125		64.125

		64.15		64.15		64.15

		64.175		64.175		64.175

		64.2		64.2		64.2

		64.225		64.225		64.225

		64.25		64.25		64.25

		64.275		64.275		64.275

		64.3		64.3		64.3

		64.325		64.325		64.325

		64.35		64.35		64.35

		64.375		64.375		64.375

		64.4		64.4		64.4

		64.425		64.425		64.425

		64.45		64.45		64.45

		64.475		64.475		64.475

		64.5		64.5		64.5

		64.525		64.525		64.525

		64.55		64.55		64.55

		64.575		64.575		64.575

		64.6		64.6		64.6

		64.625		64.625		64.625

		64.65		64.65		64.65

		64.675		64.675		64.675

		64.7		64.7		64.7

		64.725		64.725		64.725

		64.75		64.75		64.75

		64.775		64.775		64.775

		64.8		64.8		64.8

		64.825		64.825		64.825

		64.85		64.85		64.85

		64.875		64.875		64.875

		64.9		64.9		64.9

		64.925		64.925		64.925

		64.95		64.95		64.95

		64.975		64.975		64.975

		65		65		65

		65.025		65.025		65.025

		65.05		65.05		65.05

		65.075		65.075		65.075

		65.1		65.1		65.1

		65.125		65.125		65.125

		65.15		65.15		65.15

		65.175		65.175		65.175

		65.2		65.2		65.2

		65.225		65.225		65.225

		65.25		65.25		65.25

		65.275		65.275		65.275

		65.3		65.3		65.3

		65.325		65.325		65.325

		65.35		65.35		65.35

		65.375		65.375		65.375

		65.4		65.4		65.4

		65.425		65.425		65.425

		65.45		65.45		65.45

		65.475		65.475		65.475

		65.5		65.5		65.5

		65.525		65.525		65.525

		65.55		65.55		65.55

		65.575		65.575		65.575

		65.6		65.6		65.6

		65.625		65.625		65.625

		65.65		65.65		65.65

		65.675		65.675		65.675

		65.7		65.7		65.7

		65.725		65.725		65.725

		65.75		65.75		65.75

		65.775		65.775		65.775

		65.8		65.8		65.8

		65.825		65.825		65.825

		65.85		65.85		65.85

		65.875		65.875		65.875

		65.9		65.9		65.9

		65.925		65.925		65.925

		65.95		65.95		65.95

		65.975		65.975		65.975

		66		66		66

		66.025		66.025		66.025

		66.05		66.05		66.05

		66.075		66.075		66.075

		66.1		66.1		66.1

		66.125		66.125		66.125

		66.15		66.15		66.15

		66.175		66.175		66.175

		66.2		66.2		66.2

		66.225		66.225		66.225

		66.25		66.25		66.25

		66.275		66.275		66.275

		66.3		66.3		66.3

		66.325		66.325		66.325

		66.35		66.35		66.35

		66.375		66.375		66.375

		66.4		66.4		66.4

		66.425		66.425		66.425

		66.45		66.45		66.45

		66.475		66.475		66.475

		66.5		66.5		66.5

		66.525		66.525		66.525

		66.55		66.55		66.55

		66.575		66.575		66.575

		66.6		66.6		66.6

		66.625		66.625		66.625

		66.65		66.65		66.65

		66.675		66.675		66.675

		66.7		66.7		66.7

		66.725		66.725		66.725

		66.75		66.75		66.75

		66.775		66.775		66.775

		66.8		66.8		66.8

		66.825		66.825		66.825

		66.85		66.85		66.85

		66.875		66.875		66.875

		66.9		66.9		66.9

		66.925		66.925		66.925

		66.95		66.95		66.95

		66.975		66.975		66.975

		67		67		67

		67.025		67.025		67.025

		67.05		67.05		67.05

		67.075		67.075		67.075

		67.1		67.1		67.1

		67.125		67.125		67.125

		67.15		67.15		67.15

		67.175		67.175		67.175

		67.2		67.2		67.2

		67.225		67.225		67.225

		67.25		67.25		67.25

		67.275		67.275		67.275

		67.3		67.3		67.3

		67.325		67.325		67.325

		67.35		67.35		67.35

		67.375		67.375		67.375

		67.4		67.4		67.4

		67.425		67.425		67.425

		67.45		67.45		67.45

		67.475		67.475		67.475

		67.5		67.5		67.5

		67.525		67.525		67.525

		67.55		67.55		67.55

		67.575		67.575		67.575

		67.6		67.6		67.6

		67.625		67.625		67.625

		67.65		67.65		67.65

		67.675		67.675		67.675

		67.7		67.7		67.7

		67.725		67.725		67.725

		67.75		67.75		67.75

		67.775		67.775		67.775

		67.8		67.8		67.8

		67.825		67.825		67.825

		67.85		67.85		67.85

		67.875		67.875		67.875

		67.9		67.9		67.9

		67.925		67.925		67.925

		67.95		67.95		67.95

		67.975		67.975		67.975

		68		68		68

		68.025		68.025		68.025

		68.05		68.05		68.05

		68.075		68.075		68.075

		68.1		68.1		68.1

		68.125		68.125		68.125

		68.15		68.15		68.15

		68.175		68.175		68.175

		68.2		68.2		68.2

		68.225		68.225		68.225

		68.25		68.25		68.25

		68.275		68.275		68.275

		68.3		68.3		68.3

		68.325		68.325		68.325

		68.35		68.35		68.35

		68.375		68.375		68.375

		68.4		68.4		68.4

		68.425		68.425		68.425

		68.45		68.45		68.45

		68.475		68.475		68.475

		68.5		68.5		68.5

		68.525		68.525		68.525

		68.55		68.55		68.55

		68.575		68.575		68.575

		68.6		68.6		68.6

		68.625		68.625		68.625

		68.65		68.65		68.65

		68.675		68.675		68.675

		68.7		68.7		68.7

		68.725		68.725		68.725

		68.75		68.75		68.75

		68.775		68.775		68.775

		68.8		68.8		68.8

		68.825		68.825		68.825

		68.85		68.85		68.85

		68.875		68.875		68.875

		68.9		68.9		68.9

		68.925		68.925		68.925

		68.95		68.95		68.95

		68.975		68.975		68.975

		69		69		69

		69.025		69.025		69.025

		69.05		69.05		69.05

		69.075		69.075		69.075

		69.1		69.1		69.1

		69.125		69.125		69.125

		69.15		69.15		69.15

		69.175		69.175		69.175

		69.2		69.2		69.2

		69.225		69.225		69.225

		69.25		69.25		69.25

		69.275		69.275		69.275

		69.3		69.3		69.3

		69.325		69.325		69.325

		69.35		69.35		69.35

		69.375		69.375		69.375

		69.4		69.4		69.4

		69.425		69.425		69.425

		69.45		69.45		69.45

		69.475		69.475		69.475

		69.5		69.5		69.5

		69.525		69.525		69.525

		69.55		69.55		69.55

		69.575		69.575		69.575

		69.6		69.6		69.6

		69.625		69.625		69.625

		69.65		69.65		69.65

		69.675		69.675		69.675

		69.7		69.7		69.7

		69.725		69.725		69.725

		69.75		69.75		69.75

		69.775		69.775		69.775

		69.8		69.8		69.8

		69.825		69.825		69.825

		69.85		69.85		69.85

		69.875		69.875		69.875

		69.9		69.9		69.9

		69.925		69.925		69.925

		69.95		69.95		69.95

		69.975		69.975		69.975

		70		70		70

		70.025		70.025		70.025

		70.05		70.05		70.05

		70.075		70.075		70.075

		70.1		70.1		70.1

		70.125		70.125		70.125

		70.15		70.15		70.15

		70.175		70.175		70.175

		70.2		70.2		70.2

		70.225		70.225		70.225

		70.25		70.25		70.25

		70.275		70.275		70.275

		70.3		70.3		70.3

		70.325		70.325		70.325

		70.35		70.35		70.35

		70.375		70.375		70.375

		70.4		70.4		70.4

		70.425		70.425		70.425

		70.45		70.45		70.45

		70.475		70.475		70.475

		70.5		70.5		70.5

		70.525		70.525		70.525

		70.55		70.55		70.55

		70.575		70.575		70.575

		70.6		70.6		70.6

		70.625		70.625		70.625

		70.65		70.65		70.65

		70.675		70.675		70.675

		70.7		70.7		70.7

		70.725		70.725		70.725

		70.75		70.75		70.75

		70.775		70.775		70.775

		70.8		70.8		70.8

		70.825		70.825		70.825

		70.85		70.85		70.85

		70.875		70.875		70.875

		70.9		70.9		70.9

		70.925		70.925		70.925

		70.95		70.95		70.95

		70.975		70.975		70.975

		71		71		71

		71.025		71.025		71.025

		71.05		71.05		71.05

		71.075		71.075		71.075

		71.1		71.1		71.1

		71.125		71.125		71.125

		71.15		71.15		71.15

		71.175		71.175		71.175

		71.2		71.2		71.2

		71.225		71.225		71.225

		71.25		71.25		71.25

		71.275		71.275		71.275

		71.3		71.3		71.3

		71.325		71.325		71.325

		71.35		71.35		71.35

		71.375		71.375		71.375

		71.4		71.4		71.4

		71.425		71.425		71.425

		71.45		71.45		71.45

		71.475		71.475		71.475

		71.5		71.5		71.5

		71.525		71.525		71.525

		71.55		71.55		71.55

		71.575		71.575		71.575

		71.6		71.6		71.6

		71.625		71.625		71.625

		71.65		71.65		71.65

		71.675		71.675		71.675

		71.7		71.7		71.7

		71.725		71.725		71.725

		71.75		71.75		71.75

		71.775		71.775		71.775

		71.8		71.8		71.8

		71.825		71.825		71.825

		71.85		71.85		71.85

		71.875		71.875		71.875

		71.9		71.9		71.9

		71.925		71.925		71.925

		71.95		71.95		71.95

		71.975		71.975		71.975

		72		72		72

		72.025		72.025		72.025

		72.05		72.05		72.05

		72.075		72.075		72.075

		72.1		72.1		72.1

		72.125		72.125		72.125

		72.15		72.15		72.15

		72.175		72.175		72.175

		72.2		72.2		72.2

		72.225		72.225		72.225

		72.25		72.25		72.25

		72.275		72.275		72.275

		72.3		72.3		72.3

		72.325		72.325		72.325

		72.35		72.35		72.35

		72.375		72.375		72.375

		72.4		72.4		72.4

		72.425		72.425		72.425

		72.45		72.45		72.45

		72.475		72.475		72.475

		72.5		72.5		72.5

		72.525		72.525		72.525

		72.55		72.55		72.55

		72.575		72.575		72.575

		72.6		72.6		72.6

		72.625		72.625		72.625

		72.65		72.65		72.65

		72.675		72.675		72.675

		72.7		72.7		72.7

		72.725		72.725		72.725

		72.75		72.75		72.75

		72.775		72.775		72.775

		72.8		72.8		72.8

		72.825		72.825		72.825

		72.85		72.85		72.85

		72.875		72.875		72.875

		72.9		72.9		72.9

		72.925		72.925		72.925

		72.95		72.95		72.95

		72.975		72.975		72.975

		73		73		73

		73.025		73.025		73.025

		73.05		73.05		73.05

		73.075		73.075		73.075

		73.1		73.1		73.1

		73.125		73.125		73.125

		73.15		73.15		73.15

		73.175		73.175		73.175

		73.2		73.2		73.2

		73.225		73.225		73.225

		73.25		73.25		73.25

		73.275		73.275		73.275

		73.3		73.3		73.3

		73.325		73.325		73.325

		73.35		73.35		73.35

		73.375		73.375		73.375

		73.4		73.4		73.4

		73.425		73.425		73.425

		73.45		73.45		73.45

		73.475		73.475		73.475

		73.5		73.5		73.5

		73.525		73.525		73.525

		73.55		73.55		73.55

		73.575		73.575		73.575

		73.6		73.6		73.6

		73.625		73.625		73.625

		73.65		73.65		73.65

		73.675		73.675		73.675

		73.7		73.7		73.7

		73.725		73.725		73.725

		73.75		73.75		73.75

		73.775		73.775		73.775

		73.8		73.8		73.8

		73.825		73.825		73.825

		73.85		73.85		73.85

		73.875		73.875		73.875

		73.9		73.9		73.9

		73.925		73.925		73.925

		73.95		73.95		73.95

		73.975		73.975		73.975

		74		74		74

		74.025		74.025		74.025

		74.05		74.05		74.05

		74.075		74.075		74.075

		74.1		74.1		74.1

		74.125		74.125		74.125

		74.15		74.15		74.15

		74.175		74.175		74.175

		74.2		74.2		74.2

		74.225		74.225		74.225

		74.25		74.25		74.25

		74.275		74.275		74.275

		74.3		74.3		74.3

		74.325		74.325		74.325

		74.35		74.35		74.35

		74.375		74.375		74.375

		74.4		74.4		74.4

		74.425		74.425		74.425

		74.45		74.45		74.45

		74.475		74.475		74.475

		74.5		74.5		74.5

		74.525		74.525		74.525

		74.55		74.55		74.55

		74.575		74.575		74.575

		74.6		74.6		74.6

		74.625		74.625		74.625

		74.65		74.65		74.65

		74.675		74.675		74.675

		74.7		74.7		74.7

		74.725		74.725		74.725

		74.75		74.75		74.75

		74.775		74.775		74.775

		74.8		74.8		74.8

		74.825		74.825		74.825

		74.85		74.85		74.85

		74.875		74.875		74.875

		74.9		74.9		74.9

		74.925		74.925		74.925

		74.95		74.95		74.95

		74.975		74.975		74.975

		75		75		75

		75.025		75.025		75.025

		75.05		75.05		75.05

		75.075		75.075		75.075

		75.1		75.1		75.1

		75.125		75.125		75.125

		75.15		75.15		75.15

		75.175		75.175		75.175

		75.2		75.2		75.2

		75.225		75.225		75.225

		75.25		75.25		75.25

		75.275		75.275		75.275

		75.3		75.3		75.3

		75.325		75.325		75.325

		75.35		75.35		75.35

		75.375		75.375		75.375

		75.4		75.4		75.4

		75.425		75.425		75.425

		75.45		75.45		75.45

		75.475		75.475		75.475

		75.5		75.5		75.5

		75.525		75.525		75.525

		75.55		75.55		75.55

		75.575		75.575		75.575

		75.6		75.6		75.6

		75.625		75.625		75.625

		75.65		75.65		75.65

		75.675		75.675		75.675

		75.7		75.7		75.7

		75.725		75.725		75.725

		75.75		75.75		75.75

		75.775		75.775		75.775

		75.8		75.8		75.8

		75.825		75.825		75.825

		75.85		75.85		75.85

		75.875		75.875		75.875

		75.9		75.9		75.9

		75.925		75.925		75.925

		75.95		75.95		75.95

		75.975		75.975		75.975

		76		76		76

		76.025		76.025		76.025

		76.05		76.05		76.05

		76.075		76.075		76.075

		76.1		76.1		76.1

		76.125		76.125		76.125

		76.15		76.15		76.15

		76.175		76.175		76.175

		76.2		76.2		76.2

		76.225		76.225		76.225

		76.25		76.25		76.25

		76.275		76.275		76.275

		76.3		76.3		76.3

		76.325		76.325		76.325

		76.35		76.35		76.35

		76.375		76.375		76.375

		76.4		76.4		76.4

		76.425		76.425		76.425

		76.45		76.45		76.45

		76.475		76.475		76.475

		76.5		76.5		76.5

		76.525		76.525		76.525

		76.55		76.55		76.55

		76.575		76.575		76.575

		76.6		76.6		76.6

		76.625		76.625		76.625

		76.65		76.65		76.65

		76.675		76.675		76.675

		76.7		76.7		76.7

		76.725		76.725		76.725

		76.75		76.75		76.75

		76.775		76.775		76.775

		76.8		76.8		76.8

		76.825		76.825		76.825

		76.85		76.85		76.85

		76.875		76.875		76.875

		76.9		76.9		76.9

		76.925		76.925		76.925

		76.95		76.95		76.95

		76.975		76.975		76.975

		77		77		77

		77.025		77.025		77.025

		77.05		77.05		77.05

		77.075		77.075		77.075

		77.1		77.1		77.1

		77.125		77.125		77.125

		77.15		77.15		77.15

		77.175		77.175		77.175

		77.2		77.2		77.2

		77.225		77.225		77.225

		77.25		77.25		77.25

		77.275		77.275		77.275

		77.3		77.3		77.3

		77.325		77.325		77.325

		77.35		77.35		77.35

		77.375		77.375		77.375

		77.4		77.4		77.4

		77.425		77.425		77.425

		77.45		77.45		77.45

		77.475		77.475		77.475

		77.5		77.5		77.5

		77.525		77.525		77.525

		77.55		77.55		77.55

		77.575		77.575		77.575

		77.6		77.6		77.6

		77.625		77.625		77.625

		77.65		77.65		77.65

		77.675		77.675		77.675

		77.7		77.7		77.7

		77.725		77.725		77.725

		77.75		77.75		77.75

		77.775		77.775		77.775

		77.8		77.8		77.8

		77.825		77.825		77.825

		77.85		77.85		77.85

		77.875		77.875		77.875

		77.9		77.9		77.9

		77.925		77.925		77.925

		77.95		77.95		77.95

		77.975		77.975		77.975

		78		78		78

		78.025		78.025		78.025

		78.05		78.05		78.05

		78.075		78.075		78.075

		78.1		78.1		78.1

		78.125		78.125		78.125

		78.15		78.15		78.15

		78.175		78.175		78.175

		78.2		78.2		78.2

		78.225		78.225		78.225

		78.25		78.25		78.25

		78.275		78.275		78.275

		78.3		78.3		78.3

		78.325		78.325		78.325

		78.35		78.35		78.35

		78.375		78.375		78.375

		78.4		78.4		78.4

		78.425		78.425		78.425

		78.45		78.45		78.45

		78.475		78.475		78.475

		78.5		78.5		78.5

		78.525		78.525		78.525

		78.55		78.55		78.55

		78.575		78.575		78.575

		78.6		78.6		78.6

		78.625		78.625		78.625

		78.65		78.65		78.65

		78.675		78.675		78.675

		78.7		78.7		78.7

		78.725		78.725		78.725

		78.75		78.75		78.75

		78.775		78.775		78.775

		78.8		78.8		78.8

		78.825		78.825		78.825

		78.85		78.85		78.85

		78.875		78.875		78.875

		78.9		78.9		78.9

		78.925		78.925		78.925

		78.95		78.95		78.95

		78.975		78.975		78.975

		79		79		79

		79.025		79.025		79.025

		79.05		79.05		79.05

		79.075		79.075		79.075

		79.1		79.1		79.1

		79.125		79.125		79.125

		79.15		79.15		79.15

		79.175		79.175		79.175

		79.2		79.2		79.2

		79.225		79.225		79.225

		79.25		79.25		79.25

		79.275		79.275		79.275

		79.3		79.3		79.3

		79.325		79.325		79.325

		79.35		79.35		79.35

		79.375		79.375		79.375

		79.4		79.4		79.4

		79.425		79.425		79.425

		79.45		79.45		79.45

		79.475		79.475		79.475

		79.5		79.5		79.5

		79.525		79.525		79.525

		79.55		79.55		79.55

		79.575		79.575		79.575

		79.6		79.6		79.6

		79.625		79.625		79.625

		79.65		79.65		79.65

		79.675		79.675		79.675

		79.7		79.7		79.7

		79.725		79.725		79.725

		79.75		79.75		79.75

		79.775		79.775		79.775

		79.8		79.8		79.8

		79.825		79.825		79.825

		79.85		79.85		79.85

		79.875		79.875		79.875

		79.9		79.9		79.9

		79.925		79.925		79.925

		79.95		79.95		79.95

		79.975		79.975		79.975

		80		80		80

		80.025		80.025		80.025

		80.05		80.05		80.05

		80.075		80.075		80.075

		80.1		80.1		80.1

		80.125		80.125		80.125

		80.15		80.15		80.15

		80.175		80.175		80.175

		80.2		80.2		80.2

		80.225		80.225		80.225

		80.25		80.25		80.25

		80.275		80.275		80.275

		80.3		80.3		80.3

		80.325		80.325		80.325

		80.35		80.35		80.35

		80.375		80.375		80.375

		80.4		80.4		80.4

		80.425		80.425		80.425

		80.45		80.45		80.45

		80.475		80.475		80.475

		80.5		80.5		80.5

		80.525		80.525		80.525

		80.55		80.55		80.55

		80.575		80.575		80.575

		80.6		80.6		80.6

		80.625		80.625		80.625

		80.65		80.65		80.65

		80.675		80.675		80.675

		80.7		80.7		80.7

		80.725		80.725		80.725

		80.75		80.75		80.75

		80.775		80.775		80.775

		80.8		80.8		80.8

		80.825		80.825		80.825

		80.85		80.85		80.85

		80.875		80.875		80.875

		80.9		80.9		80.9

		80.925		80.925		80.925

		80.95		80.95		80.95

		80.975		80.975		80.975

		81		81		81

		81.025		81.025		81.025

		81.05		81.05		81.05

		81.075		81.075		81.075

		81.1		81.1		81.1

		81.125		81.125		81.125

		81.15		81.15		81.15

		81.175		81.175		81.175

		81.2		81.2		81.2

		81.225		81.225		81.225

		81.25		81.25		81.25

		81.275		81.275		81.275

		81.3		81.3		81.3

		81.325		81.325		81.325

		81.35		81.35		81.35

		81.375		81.375		81.375

		81.4		81.4		81.4

		81.425		81.425		81.425

		81.45		81.45		81.45

		81.475		81.475		81.475

		81.5		81.5		81.5

		81.525		81.525		81.525

		81.55		81.55		81.55

		81.575		81.575		81.575

		81.6		81.6		81.6

		81.625		81.625		81.625

		81.65		81.65		81.65

		81.675		81.675		81.675

		81.7		81.7		81.7

		81.725		81.725		81.725

		81.75		81.75		81.75

		81.775		81.775		81.775

		81.8		81.8		81.8

		81.825		81.825		81.825

		81.85		81.85		81.85

		81.875		81.875		81.875

		81.9		81.9		81.9

		81.925		81.925		81.925

		81.95		81.95		81.95

		81.975		81.975		81.975

		82		82		82

		82.025		82.025		82.025

		82.05		82.05		82.05

		82.075		82.075		82.075

		82.1		82.1		82.1

		82.125		82.125		82.125

		82.15		82.15		82.15

		82.175		82.175		82.175

		82.2		82.2		82.2

		82.225		82.225		82.225

		82.25		82.25		82.25

		82.275		82.275		82.275

		82.3		82.3		82.3

		82.325		82.325		82.325

		82.35		82.35		82.35

		82.375		82.375		82.375

		82.4		82.4		82.4

		82.425		82.425		82.425

		82.45		82.45		82.45

		82.475		82.475		82.475

		82.5		82.5		82.5

		82.525		82.525		82.525

		82.55		82.55		82.55

		82.575		82.575		82.575

		82.6		82.6		82.6

		82.625		82.625		82.625

		82.65		82.65		82.65

		82.675		82.675		82.675

		82.7		82.7		82.7

		82.725		82.725		82.725

		82.75		82.75		82.75

		82.775		82.775		82.775

		82.8		82.8		82.8

		82.825		82.825		82.825

		82.85		82.85		82.85

		82.875		82.875		82.875

		82.9		82.9		82.9

		82.925		82.925		82.925

		82.95		82.95		82.95

		82.975		82.975		82.975

		83		83		83

		83.025		83.025		83.025

		83.05		83.05		83.05

		83.075		83.075		83.075

		83.1		83.1		83.1

		83.125		83.125		83.125

		83.15		83.15		83.15

		83.175		83.175		83.175

		83.2		83.2		83.2

		83.225		83.225		83.225

		83.25		83.25		83.25

		83.275		83.275		83.275

		83.3		83.3		83.3

		83.325		83.325		83.325

		83.35		83.35		83.35

		83.375		83.375		83.375

		83.4		83.4		83.4

		83.425		83.425		83.425

		83.45		83.45		83.45

		83.475		83.475		83.475

		83.5		83.5		83.5

		83.525		83.525		83.525

		83.55		83.55		83.55

		83.575		83.575		83.575

		83.6		83.6		83.6

		83.625		83.625		83.625

		83.65		83.65		83.65

		83.675		83.675		83.675

		83.7		83.7		83.7

		83.725		83.725		83.725

		83.75		83.75		83.75

		83.775		83.775		83.775

		83.8		83.8		83.8

		83.825		83.825		83.825

		83.85		83.85		83.85

		83.875		83.875		83.875

		83.9		83.9		83.9

		83.925		83.925		83.925

		83.95		83.95		83.95

		83.975		83.975		83.975

		84		84		84

		84.025		84.025		84.025

		84.05		84.05		84.05

		84.075		84.075		84.075

		84.1		84.1		84.1

		84.125		84.125		84.125

		84.15		84.15		84.15

		84.175		84.175		84.175

		84.2		84.2		84.2

		84.225		84.225		84.225

		84.25		84.25		84.25

		84.275		84.275		84.275

		84.3		84.3		84.3

		84.325		84.325		84.325

		84.35		84.35		84.35

		84.375		84.375		84.375

		84.4		84.4		84.4

		84.425		84.425		84.425

		84.45		84.45		84.45

		84.475		84.475		84.475

		84.5		84.5		84.5

		84.525		84.525		84.525

		84.55		84.55		84.55

		84.575		84.575		84.575

		84.6		84.6		84.6

		84.625		84.625		84.625

		84.65		84.65		84.65

		84.675		84.675		84.675

		84.7		84.7		84.7

		84.725		84.725		84.725

		84.75		84.75		84.75

		84.775		84.775		84.775

		84.8		84.8		84.8

		84.825		84.825		84.825

		84.85		84.85		84.85

		84.875		84.875		84.875

		84.9		84.9		84.9

		84.925		84.925		84.925

		84.95		84.95		84.95

		84.975		84.975		84.975

		85		85		85

		85.025		85.025		85.025

		85.05		85.05		85.05

		85.075		85.075		85.075

		85.1		85.1		85.1

		85.125		85.125		85.125

		85.15		85.15		85.15

		85.175		85.175		85.175

		85.2		85.2		85.2

		85.225		85.225		85.225

		85.25		85.25		85.25

		85.275		85.275		85.275

		85.3		85.3		85.3

		85.325		85.325		85.325

		85.35		85.35		85.35

		85.375		85.375		85.375

		85.4		85.4		85.4

		85.425		85.425		85.425

		85.45		85.45		85.45

		85.475		85.475		85.475

		85.5		85.5		85.5

		85.525		85.525		85.525

		85.55		85.55		85.55

		85.575		85.575		85.575

		85.6		85.6		85.6

		85.625		85.625		85.625

		85.65		85.65		85.65

		85.675		85.675		85.675

		85.7		85.7		85.7

		85.725		85.725		85.725

		85.75		85.75		85.75

		85.775		85.775		85.775

		85.8		85.8		85.8

		85.825		85.825		85.825

		85.85		85.85		85.85

		85.875		85.875		85.875

		85.9		85.9		85.9

		85.925		85.925		85.925

		85.95		85.95		85.95

		85.975		85.975		85.975

		86		86		86

		86.025		86.025		86.025

		86.05		86.05		86.05

		86.075		86.075		86.075

		86.1		86.1		86.1

		86.125		86.125		86.125

		86.15		86.15		86.15

		86.175		86.175		86.175

		86.2		86.2		86.2

		86.225		86.225		86.225

		86.25		86.25		86.25

		86.275		86.275		86.275

		86.3		86.3		86.3

		86.325		86.325		86.325

		86.35		86.35		86.35

		86.375		86.375		86.375

		86.4		86.4		86.4

		86.425		86.425		86.425

		86.45		86.45		86.45

		86.475		86.475		86.475

		86.5		86.5		86.5

		86.525		86.525		86.525

		86.55		86.55		86.55

		86.575		86.575		86.575

		86.6		86.6		86.6

		86.625		86.625		86.625

		86.65		86.65		86.65

		86.675		86.675		86.675

		86.7		86.7		86.7

		86.725		86.725		86.725

		86.75		86.75		86.75

		86.775		86.775		86.775

		86.8		86.8		86.8

		86.825		86.825		86.825

		86.85		86.85		86.85

		86.875		86.875		86.875

		86.9		86.9		86.9

		86.925		86.925		86.925

		86.95		86.95		86.95

		86.975		86.975		86.975

		87		87		87

		87.025		87.025		87.025

		87.05		87.05		87.05

		87.075		87.075		87.075

		87.1		87.1		87.1

		87.125		87.125		87.125

		87.15		87.15		87.15

		87.175		87.175		87.175

		87.2		87.2		87.2

		87.225		87.225		87.225

		87.25		87.25		87.25

		87.275		87.275		87.275

		87.3		87.3		87.3

		87.325		87.325		87.325

		87.35		87.35		87.35

		87.375		87.375		87.375

		87.4		87.4		87.4

		87.425		87.425		87.425

		87.45		87.45		87.45

		87.475		87.475		87.475

		87.5		87.5		87.5

		87.525		87.525		87.525

		87.55		87.55		87.55

		87.575		87.575		87.575

		87.6		87.6		87.6

		87.625		87.625		87.625

		87.65		87.65		87.65

		87.675		87.675		87.675

		87.7		87.7		87.7

		87.725		87.725		87.725

		87.75		87.75		87.75

		87.775		87.775		87.775

		87.8		87.8		87.8

		87.825		87.825		87.825

		87.85		87.85		87.85

		87.875		87.875		87.875

		87.9		87.9		87.9

		87.925		87.925		87.925

		87.95		87.95		87.95

		87.975		87.975		87.975

		88		88		88

		88.025		88.025		88.025

		88.05		88.05		88.05

		88.075		88.075		88.075

		88.1		88.1		88.1

		88.125		88.125		88.125

		88.15		88.15		88.15

		88.175		88.175		88.175

		88.2		88.2		88.2

		88.225		88.225		88.225

		88.25		88.25		88.25

		88.275		88.275		88.275

		88.3		88.3		88.3

		88.325		88.325		88.325

		88.35		88.35		88.35

		88.375		88.375		88.375

		88.4		88.4		88.4

		88.425		88.425		88.425

		88.45		88.45		88.45

		88.475		88.475		88.475

		88.5		88.5		88.5

		88.525		88.525		88.525

		88.55		88.55		88.55

		88.575		88.575		88.575

		88.6		88.6		88.6

		88.625		88.625		88.625

		88.65		88.65		88.65

		88.675		88.675		88.675

		88.7		88.7		88.7

		88.725		88.725		88.725

		88.75		88.75		88.75

		88.775		88.775		88.775

		88.8		88.8		88.8

		88.825		88.825		88.825

		88.85		88.85		88.85

		88.875		88.875		88.875

		88.9		88.9		88.9

		88.925		88.925		88.925

		88.95		88.95		88.95

		88.975		88.975		88.975

		89		89		89

		89.025		89.025		89.025

		89.05		89.05		89.05

		89.075		89.075		89.075

		89.1		89.1		89.1

		89.125		89.125		89.125

		89.15		89.15		89.15

		89.175		89.175		89.175

		89.2		89.2		89.2

		89.225		89.225		89.225

		89.25		89.25		89.25

		89.275		89.275		89.275

		89.3		89.3		89.3

		89.325		89.325		89.325

		89.35		89.35		89.35

		89.375		89.375		89.375

		89.4		89.4		89.4

		89.425		89.425		89.425

		89.45		89.45		89.45

		89.475		89.475		89.475

		89.5		89.5		89.5

		89.525		89.525		89.525

		89.55		89.55		89.55

		89.575		89.575		89.575

		89.6		89.6		89.6

		89.625		89.625		89.625

		89.65		89.65		89.65

		89.675		89.675		89.675

		89.7		89.7		89.7

		89.725		89.725		89.725

		89.75		89.75		89.75

		89.775		89.775		89.775

		89.8		89.8		89.8

		89.825		89.825		89.825

		89.85		89.85		89.85

		89.875		89.875		89.875

		89.9		89.9		89.9

		89.925		89.925		89.925

		89.95		89.95		89.95

		89.975		89.975		89.975

		90		90		90

		90.025		90.025		90.025

		90.05		90.05		90.05

		90.075		90.075		90.075

		90.1		90.1		90.1

		90.125		90.125		90.125

		90.15		90.15		90.15

		90.175		90.175		90.175

		90.2		90.2		90.2

		90.225		90.225		90.225

		90.25		90.25		90.25

		90.275		90.275		90.275

		90.3		90.3		90.3

		90.325		90.325		90.325

		90.35		90.35		90.35

		90.375		90.375		90.375

		90.4		90.4		90.4

		90.425		90.425		90.425

		90.45		90.45		90.45

		90.475		90.475		90.475

		90.5		90.5		90.5

		90.525		90.525		90.525

		90.55		90.55		90.55

		90.575		90.575		90.575

		90.6		90.6		90.6

		90.625		90.625		90.625

		90.65		90.65		90.65

		90.675		90.675		90.675

		90.7		90.7		90.7

		90.725		90.725		90.725

		90.75		90.75		90.75

		90.775		90.775		90.775

		90.8		90.8		90.8

		90.825		90.825		90.825

		90.85		90.85		90.85

		90.875		90.875		90.875

		90.9		90.9		90.9

		90.925		90.925		90.925

		90.95		90.95		90.95

		90.975		90.975		90.975

		91		91		91

		91.025		91.025		91.025

		91.05		91.05		91.05

		91.075		91.075		91.075

		91.1		91.1		91.1

		91.125		91.125		91.125

		91.15		91.15		91.15

		91.175		91.175		91.175

		91.2		91.2		91.2

		91.225		91.225		91.225

		91.25		91.25		91.25

		91.275		91.275		91.275

		91.3		91.3		91.3

		91.325		91.325		91.325

		91.35		91.35		91.35

		91.375		91.375		91.375

		91.4		91.4		91.4

		91.425		91.425		91.425

		91.45		91.45		91.45

		91.475		91.475		91.475

		91.5		91.5		91.5

		91.525		91.525		91.525

		91.55		91.55		91.55

		91.575		91.575		91.575

		91.6		91.6		91.6

		91.625		91.625		91.625

		91.65		91.65		91.65

		91.675		91.675		91.675

		91.7		91.7		91.7

		91.725		91.725		91.725

		91.75		91.75		91.75

		91.775		91.775		91.775

		91.8		91.8		91.8

		91.825		91.825		91.825

		91.85		91.85		91.85

		91.875		91.875		91.875

		91.9		91.9		91.9

		91.925		91.925		91.925

		91.95		91.95		91.95

		91.975		91.975		91.975

		92		92		92

		92.025		92.025		92.025

		92.05		92.05		92.05

		92.075		92.075		92.075

		92.1		92.1		92.1

		92.125		92.125		92.125

		92.15		92.15		92.15

		92.175		92.175		92.175

		92.2		92.2		92.2

		92.225		92.225		92.225

		92.25		92.25		92.25

		92.275		92.275		92.275

		92.3		92.3		92.3

		92.325		92.325		92.325

		92.35		92.35		92.35

		92.375		92.375		92.375

		92.4		92.4		92.4

		92.425		92.425		92.425

		92.45		92.45		92.45

		92.475		92.475		92.475

		92.5		92.5		92.5

		92.525		92.525		92.525

		92.55		92.55		92.55

		92.575		92.575		92.575

		92.6		92.6		92.6

		92.625		92.625		92.625

		92.65		92.65		92.65

		92.675		92.675		92.675

		92.7		92.7		92.7

		92.725		92.725		92.725

		92.75		92.75		92.75

		92.775		92.775		92.775

		92.8		92.8		92.8

		92.825		92.825		92.825

		92.85		92.85		92.85

		92.875		92.875		92.875

		92.9		92.9		92.9

		92.925		92.925		92.925

		92.95		92.95		92.95

		92.975		92.975		92.975

		93		93		93

		93.025		93.025		93.025

		93.05		93.05		93.05

		93.075		93.075		93.075

		93.1		93.1		93.1

		93.125		93.125		93.125

		93.15		93.15		93.15

		93.175		93.175		93.175

		93.2		93.2		93.2

		93.225		93.225		93.225

		93.25		93.25		93.25

		93.275		93.275		93.275

		93.3		93.3		93.3

		93.325		93.325		93.325

		93.35		93.35		93.35

		93.375		93.375		93.375

		93.4		93.4		93.4

		93.425		93.425		93.425

		93.45		93.45		93.45

		93.475		93.475		93.475

		93.5		93.5		93.5

		93.525		93.525		93.525

		93.55		93.55		93.55

		93.575		93.575		93.575

		93.6		93.6		93.6

		93.625		93.625		93.625

		93.65		93.65		93.65

		93.675		93.675		93.675

		93.7		93.7		93.7

		93.725		93.725		93.725

		93.75		93.75		93.75

		93.775		93.775		93.775

		93.8		93.8		93.8

		93.825		93.825		93.825

		93.85		93.85		93.85

		93.875		93.875		93.875

		93.9		93.9		93.9

		93.925		93.925		93.925

		93.95		93.95		93.95

		93.975		93.975		93.975

		94		94		94

		94.025		94.025		94.025

		94.05		94.05		94.05

		94.075		94.075		94.075

		94.1		94.1		94.1

		94.125		94.125		94.125

		94.15		94.15		94.15

		94.175		94.175		94.175

		94.2		94.2		94.2

		94.225		94.225		94.225

		94.25		94.25		94.25

		94.275		94.275		94.275

		94.3		94.3		94.3

		94.325		94.325		94.325

		94.35		94.35		94.35

		94.375		94.375		94.375

		94.4		94.4		94.4

		94.425		94.425		94.425

		94.45		94.45		94.45

		94.475		94.475		94.475

		94.5		94.5		94.5

		94.525		94.525		94.525

		94.55		94.55		94.55

		94.575		94.575		94.575

		94.6		94.6		94.6

		94.625		94.625		94.625

		94.65		94.65		94.65

		94.675		94.675		94.675

		94.7		94.7		94.7

		94.725		94.725		94.725

		94.75		94.75		94.75

		94.775		94.775		94.775

		94.8		94.8		94.8

		94.825		94.825		94.825

		94.85		94.85		94.85

		94.875		94.875		94.875

		94.9		94.9		94.9

		94.925		94.925		94.925

		94.95		94.95		94.95

		94.975		94.975		94.975

		95		95		95

		95.025		95.025		95.025

		95.05		95.05		95.05

		95.075		95.075		95.075

		95.1		95.1		95.1

		95.125		95.125		95.125

		95.15		95.15		95.15

		95.175		95.175		95.175

		95.2		95.2		95.2

		95.225		95.225		95.225

		95.25		95.25		95.25

		95.275		95.275		95.275

		95.3		95.3		95.3

		95.325		95.325		95.325

		95.35		95.35		95.35

		95.375		95.375		95.375

		95.4		95.4		95.4

		95.425		95.425		95.425

		95.45		95.45		95.45

		95.475		95.475		95.475

		95.5		95.5		95.5

		95.525		95.525		95.525

		95.55		95.55		95.55

		95.575		95.575		95.575

		95.6		95.6		95.6

		95.625		95.625		95.625

		95.65		95.65		95.65

		95.675		95.675		95.675

		95.7		95.7		95.7

		95.725		95.725		95.725

		95.75		95.75		95.75

		95.775		95.775		95.775

		95.8		95.8		95.8

		95.825		95.825		95.825

		95.85		95.85		95.85

		95.875		95.875		95.875

		95.9		95.9		95.9

		95.925		95.925		95.925

		95.95		95.95		95.95

		95.975		95.975		95.975

		96		96		96

		96.025		96.025		96.025

		96.05		96.05		96.05

		96.075		96.075		96.075

		96.1		96.1		96.1

		96.125		96.125		96.125

		96.15		96.15		96.15

		96.175		96.175		96.175

		96.2		96.2		96.2

		96.225		96.225		96.225

		96.25		96.25		96.25

		96.275		96.275		96.275

		96.3		96.3		96.3

		96.325		96.325		96.325

		96.35		96.35		96.35

		96.375		96.375		96.375

		96.4		96.4		96.4

		96.425		96.425		96.425

		96.45		96.45		96.45

		96.475		96.475		96.475

		96.5		96.5		96.5

		96.525		96.525		96.525

		96.55		96.55		96.55

		96.575		96.575		96.575

		96.6		96.6		96.6

		96.625		96.625		96.625

		96.65		96.65		96.65

		96.675		96.675		96.675

		96.7		96.7		96.7

		96.725		96.725		96.725

		96.75		96.75		96.75

		96.775		96.775		96.775

		96.8		96.8		96.8

		96.825		96.825		96.825

		96.85		96.85		96.85

		96.875		96.875		96.875

		96.9		96.9		96.9

		96.925		96.925		96.925

		96.95		96.95		96.95

		96.975		96.975		96.975

		97		97		97

		97.025		97.025		97.025

		97.05		97.05		97.05

		97.075		97.075		97.075

		97.1		97.1		97.1

		97.125		97.125		97.125

		97.15		97.15		97.15

		97.175		97.175		97.175

		97.2		97.2		97.2

		97.225		97.225		97.225

		97.25		97.25		97.25

		97.275		97.275		97.275

		97.3		97.3		97.3

		97.325		97.325		97.325

		97.35		97.35		97.35

		97.375		97.375		97.375

		97.4		97.4		97.4

		97.425		97.425		97.425

		97.45		97.45		97.45

		97.475		97.475		97.475

		97.5		97.5		97.5

		97.525		97.525		97.525

		97.55		97.55		97.55

		97.575		97.575		97.575

		97.6		97.6		97.6

		97.625		97.625		97.625

		97.65		97.65		97.65

		97.675		97.675		97.675

		97.7		97.7		97.7

		97.725		97.725		97.725

		97.75		97.75		97.75

		97.775		97.775		97.775

		97.8		97.8		97.8

		97.825		97.825		97.825

		97.85		97.85		97.85

		97.875		97.875		97.875

		97.9		97.9		97.9

		97.925		97.925		97.925

		97.95		97.95		97.95

		97.975		97.975		97.975

		98		98		98

		98.025		98.025		98.025

		98.05		98.05		98.05

		98.075		98.075		98.075

		98.1		98.1		98.1

		98.125		98.125		98.125

		98.15		98.15		98.15

		98.175		98.175		98.175

		98.2		98.2		98.2

		98.225		98.225		98.225

		98.25		98.25		98.25

		98.275		98.275		98.275

		98.3		98.3		98.3

		98.325		98.325		98.325

		98.35		98.35		98.35

		98.375		98.375		98.375

		98.4		98.4		98.4

		98.425		98.425		98.425

		98.45		98.45		98.45

		98.475		98.475		98.475

		98.5		98.5		98.5

		98.525		98.525		98.525

		98.55		98.55		98.55

		98.575		98.575		98.575

		98.6		98.6		98.6

		98.625		98.625		98.625

		98.65		98.65		98.65

		98.675		98.675		98.675

		98.7		98.7		98.7

		98.725		98.725		98.725

		98.75		98.75		98.75

		98.775		98.775		98.775

		98.8		98.8		98.8

		98.825		98.825		98.825

		98.85		98.85		98.85

		98.875		98.875		98.875

		98.9		98.9		98.9

		98.925		98.925		98.925

		98.95		98.95		98.95

		98.975		98.975		98.975

		99		99		99

		99.025		99.025		99.025

		99.05		99.05		99.05

		99.075		99.075		99.075

		99.1		99.1		99.1

		99.125		99.125		99.125

		99.15		99.15		99.15

		99.175		99.175		99.175

		99.2		99.2		99.2

		99.225		99.225		99.225

		99.25		99.25		99.25

		99.275		99.275		99.275

		99.3		99.3		99.3

		99.325		99.325		99.325

		99.35		99.35		99.35

		99.375		99.375		99.375

		99.4		99.4		99.4

		99.425		99.425		99.425

		99.45		99.45		99.45

		99.475		99.475		99.475

		99.5		99.5		99.5

		99.525		99.525		99.525

		99.55		99.55		99.55

		99.575		99.575		99.575

		99.6		99.6		99.6

		99.625		99.625		99.625

		99.65		99.65		99.65

		99.675		99.675		99.675

		99.7		99.7		99.7

		99.725		99.725		99.725

		99.75		99.75		99.75

		99.775		99.775		99.775

		99.8		99.8		99.8

		99.825		99.825		99.825

		99.85		99.85		99.85

		99.875		99.875		99.875

		99.9		99.9		99.9

		99.925		99.925		99.925

		99.95		99.95		99.95

		99.975		99.975		99.975

		100		100		100

		100.025		100.025		100.025

		100.05		100.05		100.05

		100.075		100.075		100.075

		100.1		100.1		100.1

		100.125		100.125		100.125

		100.15		100.15		100.15

		100.175		100.175		100.175

		100.2		100.2		100.2

		100.225		100.225		100.225

		100.25		100.25		100.25

		100.275		100.275		100.275

		100.3		100.3		100.3

		100.325		100.325		100.325

		100.35		100.35		100.35

		100.375		100.375		100.375

		100.4		100.4		100.4

		100.425		100.425		100.425

		100.45		100.45		100.45

		100.475		100.475		100.475

		100.5		100.5		100.5

		100.525		100.525		100.525

		100.55		100.55		100.55

		100.575		100.575		100.575

		100.6		100.6		100.6

		100.625		100.625		100.625

		100.65		100.65		100.65

		100.675		100.675		100.675

		100.7		100.7		100.7

		100.725		100.725		100.725

		100.75		100.75		100.75

		100.775		100.775		100.775

		100.8		100.8		100.8

		100.825		100.825		100.825

		100.85		100.85		100.85

		100.875		100.875		100.875

		100.9		100.9		100.9

		100.925		100.925		100.925

		100.95		100.95		100.95

		100.975		100.975		100.975

		101		101		101

		101.025		101.025		101.025

		101.05		101.05		101.05

		101.075		101.075		101.075

		101.1		101.1		101.1

		101.125		101.125		101.125

		101.15		101.15		101.15

		101.175		101.175		101.175

		101.2		101.2		101.2

		101.225		101.225		101.225

		101.25		101.25		101.25

		101.275		101.275		101.275

		101.3		101.3		101.3

		101.325		101.325		101.325

		101.35		101.35		101.35

		101.375		101.375		101.375

		101.4		101.4		101.4

		101.425		101.425		101.425

		101.45		101.45		101.45

		101.475		101.475		101.475

		101.5		101.5		101.5

		101.525		101.525		101.525

		101.55		101.55		101.55

		101.575		101.575		101.575

		101.6		101.6		101.6

		101.625		101.625		101.625

		101.65		101.65		101.65

		101.675		101.675		101.675

		101.7		101.7		101.7

		101.725		101.725		101.725

		101.75		101.75		101.75

		101.775		101.775		101.775

		101.8		101.8		101.8

		101.825		101.825		101.825

		101.85		101.85		101.85

		101.875		101.875		101.875

		101.9		101.9		101.9

		101.925		101.925		101.925

		101.95		101.95		101.95

		101.975		101.975		101.975

		102		102		102

		102.025		102.025		102.025

		102.05		102.05		102.05

		102.075		102.075		102.075

		102.1		102.1		102.1

		102.125		102.125		102.125

		102.15		102.15		102.15

		102.175		102.175		102.175

		102.2		102.2		102.2

		102.225		102.225		102.225

		102.25		102.25		102.25

		102.275		102.275		102.275

		102.3		102.3		102.3

		102.325		102.325		102.325

		102.35		102.35		102.35

		102.375		102.375		102.375

		102.4		102.4		102.4

		102.425		102.425		102.425

		102.45		102.45		102.45

		102.475		102.475		102.475

		102.5		102.5		102.5

		102.525		102.525		102.525

		102.55		102.55		102.55

		102.575		102.575		102.575

		102.6		102.6		102.6

		102.625		102.625		102.625

		102.65		102.65		102.65

		102.675		102.675		102.675

		102.7		102.7		102.7

		102.725		102.725		102.725

		102.75		102.75		102.75

		102.775		102.775		102.775

		102.8		102.8		102.8

		102.825		102.825		102.825

		102.85		102.85		102.85

		102.875		102.875		102.875

		102.9		102.9		102.9

		102.925		102.925		102.925

		102.95		102.95		102.95

		102.975		102.975		102.975

		103		103		103

		103.025		103.025		103.025

		103.05		103.05		103.05

		103.075		103.075		103.075

		103.1		103.1		103.1

		103.125		103.125		103.125

		103.15		103.15		103.15

		103.175		103.175		103.175

		103.2		103.2		103.2

		103.225		103.225		103.225

		103.25		103.25		103.25

		103.275		103.275		103.275

		103.3		103.3		103.3

		103.325		103.325		103.325

		103.35		103.35		103.35

		103.375		103.375		103.375

		103.4		103.4		103.4

		103.425		103.425		103.425

		103.45		103.45		103.45

		103.475		103.475		103.475

		103.5		103.5		103.5

		103.525		103.525		103.525

		103.55		103.55		103.55

		103.575		103.575		103.575

		103.6		103.6		103.6

		103.625		103.625		103.625

		103.65		103.65		103.65

		103.675		103.675		103.675

		103.7		103.7		103.7

		103.725		103.725		103.725

		103.75		103.75		103.75

		103.775		103.775		103.775

		103.8		103.8		103.8

		103.825		103.825		103.825

		103.85		103.85		103.85

		103.875		103.875		103.875

		103.9		103.9		103.9

		103.925		103.925		103.925

		103.95		103.95		103.95

		103.975		103.975		103.975

		104		104		104

		104.025		104.025		104.025

		104.05		104.05		104.05

		104.075		104.075		104.075

		104.1		104.1		104.1

		104.125		104.125		104.125

		104.15		104.15		104.15

		104.175		104.175		104.175

		104.2		104.2		104.2

		104.225		104.225		104.225

		104.25		104.25		104.25

		104.275		104.275		104.275

		104.3		104.3		104.3

		104.325		104.325		104.325

		104.35		104.35		104.35

		104.375		104.375		104.375

		104.4		104.4		104.4

		104.425		104.425		104.425

		104.45		104.45		104.45

		104.475		104.475		104.475

		104.5		104.5		104.5

		104.525		104.525		104.525

		104.55		104.55		104.55

		104.575		104.575		104.575

		104.6		104.6		104.6

		104.625		104.625		104.625

		104.65		104.65		104.65

		104.675		104.675		104.675

		104.7		104.7		104.7

		104.725		104.725		104.725

		104.75		104.75		104.75

		104.775		104.775		104.775

		104.8		104.8		104.8

		104.825		104.825		104.825

		104.85		104.85		104.85

		104.875		104.875		104.875

		104.9		104.9		104.9

		104.925		104.925		104.925

		104.95		104.95		104.95

		104.975		104.975		104.975

		105		105		105

		105.025		105.025		105.025

		105.05		105.05		105.05

		105.075		105.075		105.075

		105.1		105.1		105.1

		105.125		105.125		105.125

		105.15		105.15		105.15

		105.175		105.175		105.175

		105.2		105.2		105.2

		105.225		105.225		105.225

		105.25		105.25		105.25

		105.275		105.275		105.275

		105.3		105.3		105.3

		105.325		105.325		105.325

		105.35		105.35		105.35

		105.375		105.375		105.375

		105.4		105.4		105.4

		105.425		105.425		105.425

		105.45		105.45		105.45

		105.475		105.475		105.475

		105.5		105.5		105.5

		105.525		105.525		105.525

		105.55		105.55		105.55

		105.575		105.575		105.575

		105.6		105.6		105.6

		105.625		105.625		105.625

		105.65		105.65		105.65

		105.675		105.675		105.675

		105.7		105.7		105.7

		105.725		105.725		105.725

		105.75		105.75		105.75

		105.775		105.775		105.775

		105.8		105.8		105.8

		105.825		105.825		105.825

		105.85		105.85		105.85

		105.875		105.875		105.875

		105.9		105.9		105.9

		105.925		105.925		105.925

		105.95		105.95		105.95

		105.975		105.975		105.975

		106		106		106

		106.025		106.025		106.025

		106.05		106.05		106.05

		106.075		106.075		106.075

		106.1		106.1		106.1

		106.125		106.125		106.125

		106.15		106.15		106.15

		106.175		106.175		106.175

		106.2		106.2		106.2

		106.225		106.225		106.225

		106.25		106.25		106.25

		106.275		106.275		106.275

		106.3		106.3		106.3

		106.325		106.325		106.325

		106.35		106.35		106.35

		106.375		106.375		106.375

		106.4		106.4		106.4

		106.425		106.425		106.425

		106.45		106.45		106.45

		106.475		106.475		106.475

		106.5		106.5		106.5

		106.525		106.525		106.525

		106.55		106.55		106.55

		106.575		106.575		106.575

		106.6		106.6		106.6

		106.625		106.625		106.625

		106.65		106.65		106.65

		106.675		106.675		106.675

		106.7		106.7		106.7

		106.725		106.725		106.725

		106.75		106.75		106.75

		106.775		106.775		106.775

		106.8		106.8		106.8

		106.825		106.825		106.825

		106.85		106.85		106.85

		106.875		106.875		106.875

		106.9		106.9		106.9

		106.925		106.925		106.925

		106.95		106.95		106.95

		106.975		106.975		106.975

		107		107		107

		107.025		107.025		107.025

		107.05		107.05		107.05

		107.075		107.075		107.075

		107.1		107.1		107.1

		107.125		107.125		107.125

		107.15		107.15		107.15

		107.175		107.175		107.175

		107.2		107.2		107.2

		107.225		107.225		107.225

		107.25		107.25		107.25

		107.275		107.275		107.275

		107.3		107.3		107.3

		107.325		107.325		107.325

		107.35		107.35		107.35

		107.375		107.375		107.375

		107.4		107.4		107.4

		107.425		107.425		107.425

		107.45		107.45		107.45

		107.475		107.475		107.475

		107.5		107.5		107.5

		107.525		107.525		107.525

		107.55		107.55		107.55

		107.575		107.575		107.575

		107.6		107.6		107.6

		107.625		107.625		107.625

		107.65		107.65		107.65

		107.675		107.675		107.675

		107.7		107.7		107.7

		107.725		107.725		107.725

		107.75		107.75		107.75

		107.775		107.775		107.775

		107.8		107.8		107.8

		107.825		107.825		107.825

		107.85		107.85		107.85

		107.875		107.875		107.875

		107.9		107.9		107.9

		107.925		107.925		107.925

		107.95		107.95		107.95

		107.975		107.975		107.975

		108		108		108

		108.025		108.025		108.025

		108.05		108.05		108.05

		108.075		108.075		108.075

		108.1		108.1		108.1

		108.125		108.125		108.125

		108.15		108.15		108.15

		108.175		108.175		108.175

		108.2		108.2		108.2

		108.225		108.225		108.225

		108.25		108.25		108.25

		108.275		108.275		108.275

		108.3		108.3		108.3

		108.325		108.325		108.325

		108.35		108.35		108.35

		108.375		108.375		108.375

		108.4		108.4		108.4

		108.425		108.425		108.425

		108.45		108.45		108.45

		108.475		108.475		108.475

		108.5		108.5		108.5

		108.525		108.525		108.525

		108.55		108.55		108.55

		108.575		108.575		108.575

		108.6		108.6		108.6

		108.625		108.625		108.625

		108.65		108.65		108.65

		108.675		108.675		108.675

		108.7		108.7		108.7

		108.725		108.725		108.725

		108.75		108.75		108.75

		108.775		108.775		108.775

		108.8		108.8		108.8

		108.825		108.825		108.825

		108.85		108.85		108.85

		108.875		108.875		108.875

		108.9		108.9		108.9

		108.925		108.925		108.925

		108.95		108.95		108.95

		108.975		108.975		108.975

		109		109		109

		109.025		109.025		109.025

		109.05		109.05		109.05

		109.075		109.075		109.075

		109.1		109.1		109.1

		109.125		109.125		109.125

		109.15		109.15		109.15

		109.175		109.175		109.175

		109.2		109.2		109.2

		109.225		109.225		109.225

		109.25		109.25		109.25

		109.275		109.275		109.275

		109.3		109.3		109.3

		109.325		109.325		109.325

		109.35		109.35		109.35

		109.375		109.375		109.375

		109.4		109.4		109.4

		109.425		109.425		109.425

		109.45		109.45		109.45

		109.475		109.475		109.475

		109.5		109.5		109.5

		109.525		109.525		109.525

		109.55		109.55		109.55

		109.575		109.575		109.575

		109.6		109.6		109.6

		109.625		109.625		109.625

		109.65		109.65		109.65

		109.675		109.675		109.675

		109.7		109.7		109.7

		109.725		109.725		109.725

		109.75		109.75		109.75

		109.775		109.775		109.775

		109.8		109.8		109.8

		109.825		109.825		109.825

		109.85		109.85		109.85

		109.875		109.875		109.875

		109.9		109.9		109.9

		109.925		109.925		109.925

		109.95		109.95		109.95

		109.975		109.975		109.975

		110		110		110

		110.025		110.025		110.025

		110.05		110.05		110.05

		110.075		110.075		110.075

		110.1		110.1		110.1

		110.125		110.125		110.125

		110.15		110.15		110.15

		110.175		110.175		110.175

		110.2		110.2		110.2

		110.225		110.225		110.225

		110.25		110.25		110.25

		110.275		110.275		110.275

		110.3		110.3		110.3

		110.325		110.325		110.325

		110.35		110.35		110.35

		110.375		110.375		110.375

		110.4		110.4		110.4

		110.425		110.425		110.425

		110.45		110.45		110.45

		110.475		110.475		110.475

		110.5		110.5		110.5

		110.525		110.525		110.525

		110.55		110.55		110.55

		110.575		110.575		110.575

		110.6		110.6		110.6

		110.625		110.625		110.625

		110.65		110.65		110.65

		110.675		110.675		110.675

		110.7		110.7		110.7

		110.725		110.725		110.725

		110.75		110.75		110.75

		110.775		110.775		110.775

		110.8		110.8		110.8

		110.825		110.825		110.825

		110.85		110.85		110.85

		110.875		110.875		110.875

		110.9		110.9		110.9

		110.925		110.925		110.925

		110.95		110.95		110.95

		110.975		110.975		110.975

		111		111		111

		111.025		111.025		111.025

		111.05		111.05		111.05

		111.075		111.075		111.075

		111.1		111.1		111.1

		111.125		111.125		111.125

		111.15		111.15		111.15

		111.175		111.175		111.175

		111.2		111.2		111.2

		111.225		111.225		111.225

		111.25		111.25		111.25

		111.275		111.275		111.275

		111.3		111.3		111.3

		111.325		111.325		111.325

		111.35		111.35		111.35

		111.375		111.375		111.375

		111.4		111.4		111.4

		111.425		111.425		111.425

		111.45		111.45		111.45

		111.475		111.475		111.475

		111.5		111.5		111.5

		111.525		111.525		111.525

		111.55		111.55		111.55

		111.575		111.575		111.575

		111.6		111.6		111.6

		111.625		111.625		111.625

		111.65		111.65		111.65

		111.675		111.675		111.675

		111.7		111.7		111.7

		111.725		111.725		111.725

		111.75		111.75		111.75

		111.775		111.775		111.775

		111.8		111.8		111.8

		111.825		111.825		111.825

		111.85		111.85		111.85

		111.875		111.875		111.875

		111.9		111.9		111.9

		111.925		111.925		111.925

		111.95		111.95		111.95

		111.975		111.975		111.975

		112		112		112

		112.025		112.025		112.025

		112.05		112.05		112.05

		112.075		112.075		112.075

		112.1		112.1		112.1

		112.125		112.125		112.125

		112.15		112.15		112.15

		112.175		112.175		112.175

		112.2		112.2		112.2

		112.225		112.225		112.225

		112.25		112.25		112.25

		112.275		112.275		112.275

		112.3		112.3		112.3

		112.325		112.325		112.325

		112.35		112.35		112.35

		112.375		112.375		112.375

		112.4		112.4		112.4

		112.425		112.425		112.425

		112.45		112.45		112.45

		112.475		112.475		112.475

		112.5		112.5		112.5

		112.525		112.525		112.525

		112.55		112.55		112.55

		112.575		112.575		112.575

		112.6		112.6		112.6

		112.625		112.625		112.625

		112.65		112.65		112.65

		112.675		112.675		112.675

		112.7		112.7		112.7

		112.725		112.725		112.725

		112.75		112.75		112.75

		112.775		112.775		112.775

		112.8		112.8		112.8

		112.825		112.825		112.825

		112.85		112.85		112.85

		112.875		112.875		112.875

		112.9		112.9		112.9

		112.925		112.925		112.925

		112.95		112.95		112.95

		112.975		112.975		112.975

		113		113		113

		113.025		113.025		113.025

		113.05		113.05		113.05

		113.075		113.075		113.075

		113.1		113.1		113.1

		113.125		113.125		113.125

		113.15		113.15		113.15

		113.175		113.175		113.175

		113.2		113.2		113.2

		113.225		113.225		113.225

		113.25		113.25		113.25

		113.275		113.275		113.275

		113.3		113.3		113.3

		113.325		113.325		113.325

		113.35		113.35		113.35

		113.375		113.375		113.375

		113.4		113.4		113.4

		113.425		113.425		113.425

		113.45		113.45		113.45

		113.475		113.475		113.475

		113.5		113.5		113.5

		113.525		113.525		113.525

		113.55		113.55		113.55

		113.575		113.575		113.575

		113.6		113.6		113.6

		113.625		113.625		113.625

		113.65		113.65		113.65

		113.675		113.675		113.675

		113.7		113.7		113.7

		113.725		113.725		113.725

		113.75		113.75		113.75

		113.775		113.775		113.775

		113.8		113.8		113.8

		113.825		113.825		113.825

		113.85		113.85		113.85

		113.875		113.875		113.875

		113.9		113.9		113.9

		113.925		113.925		113.925

		113.95		113.95		113.95

		113.975		113.975		113.975

		114		114		114

		114.025		114.025		114.025

		114.05		114.05		114.05

		114.075		114.075		114.075

		114.1		114.1		114.1

		114.125		114.125		114.125

		114.15		114.15		114.15

		114.175		114.175		114.175

		114.2		114.2		114.2

		114.225		114.225		114.225

		114.25		114.25		114.25

		114.275		114.275		114.275

		114.3		114.3		114.3

		114.325		114.325		114.325

		114.35		114.35		114.35

		114.375		114.375		114.375

		114.4		114.4		114.4

		114.425		114.425		114.425

		114.45		114.45		114.45

		114.475		114.475		114.475

		114.5		114.5		114.5

		114.525		114.525		114.525

		114.55		114.55		114.55

		114.575		114.575		114.575

		114.6		114.6		114.6

		114.625		114.625		114.625

		114.65		114.65		114.65

		114.675		114.675		114.675

		114.7		114.7		114.7

		114.725		114.725		114.725

		114.75		114.75		114.75

		114.775		114.775		114.775

		114.8		114.8		114.8

		114.825		114.825		114.825

		114.85		114.85		114.85

		114.875		114.875		114.875

		114.9		114.9		114.9

		114.925		114.925		114.925

		114.95		114.95		114.95

		114.975		114.975		114.975

		115		115		115

		115.025		115.025		115.025

		115.05		115.05		115.05

		115.075		115.075		115.075

		115.1		115.1		115.1

		115.125		115.125		115.125

		115.15		115.15		115.15

		115.175		115.175		115.175

		115.2		115.2		115.2

		115.225		115.225		115.225

		115.25		115.25		115.25

		115.275		115.275		115.275

		115.3		115.3		115.3

		115.325		115.325		115.325

		115.35		115.35		115.35

		115.375		115.375		115.375

		115.4		115.4		115.4

		115.425		115.425		115.425

		115.45		115.45		115.45

		115.475		115.475		115.475

		115.5		115.5		115.5

		115.525		115.525		115.525

		115.55		115.55		115.55

		115.575		115.575		115.575

		115.6		115.6		115.6

		115.625		115.625		115.625

		115.65		115.65		115.65

		115.675		115.675		115.675

		115.7		115.7		115.7

		115.725		115.725		115.725

		115.75		115.75		115.75

		115.775		115.775		115.775

		115.8		115.8		115.8

		115.825		115.825		115.825

		115.85		115.85		115.85

		115.875		115.875		115.875

		115.9		115.9		115.9

		115.925		115.925		115.925

		115.95		115.95		115.95

		115.975		115.975		115.975

		116		116		116

		116.025		116.025		116.025

		116.05		116.05		116.05

		116.075		116.075		116.075

		116.1		116.1		116.1

		116.125		116.125		116.125

		116.15		116.15		116.15

		116.175		116.175		116.175

		116.2		116.2		116.2

		116.225		116.225		116.225

		116.25		116.25		116.25

		116.275		116.275		116.275

		116.3		116.3		116.3

		116.325		116.325		116.325

		116.35		116.35		116.35

		116.375		116.375		116.375

		116.4		116.4		116.4

		116.425		116.425		116.425

		116.45		116.45		116.45

		116.475		116.475		116.475

		116.5		116.5		116.5

		116.525		116.525		116.525

		116.55		116.55		116.55

		116.575		116.575		116.575

		116.6		116.6		116.6

		116.625		116.625		116.625

		116.65		116.65		116.65

		116.675		116.675		116.675

		116.7		116.7		116.7

		116.725		116.725		116.725

		116.75		116.75		116.75

		116.775		116.775		116.775

		116.8		116.8		116.8

		116.825		116.825		116.825

		116.85		116.85		116.85

		116.875		116.875		116.875

		116.9		116.9		116.9

		116.925		116.925		116.925

		116.95		116.95		116.95

		116.975		116.975		116.975

		117		117		117

		117.025		117.025		117.025

		117.05		117.05		117.05

		117.075		117.075		117.075

		117.1		117.1		117.1

		117.125		117.125		117.125

		117.15		117.15		117.15

		117.175		117.175		117.175

		117.2		117.2		117.2

		117.225		117.225		117.225

		117.25		117.25		117.25

		117.275		117.275		117.275

		117.3		117.3		117.3

		117.325		117.325		117.325

		117.35		117.35		117.35

		117.375		117.375		117.375

		117.4		117.4		117.4

		117.425		117.425		117.425

		117.45		117.45		117.45

		117.475		117.475		117.475

		117.5		117.5		117.5

		117.525		117.525		117.525

		117.55		117.55		117.55

		117.575		117.575		117.575

		117.6		117.6		117.6

		117.625		117.625		117.625

		117.65		117.65		117.65

		117.675		117.675		117.675

		117.7		117.7		117.7

		117.725		117.725		117.725

		117.75		117.75		117.75

		117.775		117.775		117.775

		117.8		117.8		117.8

		117.825		117.825		117.825

		117.85		117.85		117.85

		117.875		117.875		117.875

		117.9		117.9		117.9

		117.925		117.925		117.925

		117.95		117.95		117.95

		117.975		117.975		117.975

		118		118		118

		118.025		118.025		118.025

		118.05		118.05		118.05

		118.075		118.075		118.075

		118.1		118.1		118.1

		118.125		118.125		118.125

		118.15		118.15		118.15

		118.175		118.175		118.175

		118.2		118.2		118.2

		118.225		118.225		118.225

		118.25		118.25		118.25

		118.275		118.275		118.275

		118.3		118.3		118.3

		118.325		118.325		118.325

		118.35		118.35		118.35

		118.375		118.375		118.375

		118.4		118.4		118.4

		118.425		118.425		118.425

		118.45		118.45		118.45

		118.475		118.475		118.475

		118.5		118.5		118.5

		118.525		118.525		118.525

		118.55		118.55		118.55

		118.575		118.575		118.575

		118.6		118.6		118.6

		118.625		118.625		118.625

		118.65		118.65		118.65

		118.675		118.675		118.675

		118.7		118.7		118.7

		118.725		118.725		118.725

		118.75		118.75		118.75

		118.775		118.775		118.775

		118.8		118.8		118.8

		118.825		118.825		118.825

		118.85		118.85		118.85

		118.875		118.875		118.875

		118.9		118.9		118.9

		118.925		118.925		118.925

		118.95		118.95		118.95

		118.975		118.975		118.975

		119		119		119

		119.025		119.025		119.025

		119.05		119.05		119.05

		119.075		119.075		119.075

		119.1		119.1		119.1

		119.125		119.125		119.125

		119.15		119.15		119.15

		119.175		119.175		119.175

		119.2		119.2		119.2

		119.225		119.225		119.225

		119.25		119.25		119.25

		119.275		119.275		119.275

		119.3		119.3		119.3

		119.325		119.325		119.325

		119.35		119.35		119.35

		119.375		119.375		119.375

		119.4		119.4		119.4

		119.425		119.425		119.425

		119.45		119.45		119.45

		119.475		119.475		119.475

		119.5		119.5		119.5

		119.525		119.525		119.525

		119.55		119.55		119.55

		119.575		119.575		119.575

		119.6		119.6		119.6

		119.625		119.625		119.625

		119.65		119.65		119.65

		119.675		119.675		119.675

		119.7		119.7		119.7

		119.725		119.725		119.725

		119.75		119.75		119.75

		119.775		119.775		119.775

		119.8		119.8		119.8

		119.825		119.825		119.825

		119.85		119.85		119.85

		119.875		119.875		119.875

		119.9		119.9		119.9

		119.925		119.925		119.925

		119.95		119.95		119.95

		119.975		119.975		119.975

		120		120		120

		120.025		120.025		120.025

		120.05		120.05		120.05

		120.075		120.075		120.075

		120.1		120.1		120.1

		120.125		120.125		120.125

		120.15		120.15		120.15

		120.175		120.175		120.175

		120.2		120.2		120.2

		120.225		120.225		120.225

		120.25		120.25		120.25

		120.275		120.275		120.275

		120.3		120.3		120.3

		120.325		120.325		120.325

		120.35		120.35		120.35

		120.375		120.375		120.375

		120.4		120.4		120.4

		120.425		120.425		120.425

		120.45		120.45		120.45

		120.475		120.475		120.475

		120.5		120.5		120.5

		120.525		120.525		120.525

		120.55		120.55		120.55

		120.575		120.575		120.575

		120.6		120.6		120.6

		120.625		120.625		120.625

		120.65		120.65		120.65

		120.675		120.675		120.675

		120.7		120.7		120.7

		120.725		120.725		120.725

		120.75		120.75		120.75

		120.775		120.775		120.775

		120.8		120.8		120.8

		120.825		120.825		120.825

		120.85		120.85		120.85

		120.875		120.875		120.875

		120.9		120.9		120.9

		120.925		120.925		120.925

		120.95		120.95		120.95

		120.975		120.975		120.975

		121		121		121

		121.025		121.025		121.025

		121.05		121.05		121.05

		121.075		121.075		121.075

		121.1		121.1		121.1

		121.125		121.125		121.125

		121.15		121.15		121.15

		121.175		121.175		121.175

		121.2		121.2		121.2

		121.225		121.225		121.225

		121.25		121.25		121.25

		121.275		121.275		121.275

		121.3		121.3		121.3

		121.325		121.325		121.325

		121.35		121.35		121.35

		121.375		121.375		121.375

		121.4		121.4		121.4

		121.425		121.425		121.425

		121.45		121.45		121.45

		121.475		121.475		121.475

		121.5		121.5		121.5

		121.525		121.525		121.525

		121.55		121.55		121.55

		121.575		121.575		121.575

		121.6		121.6		121.6

		121.625		121.625		121.625

		121.65		121.65		121.65

		121.675		121.675		121.675

		121.7		121.7		121.7

		121.725		121.725		121.725

		121.75		121.75		121.75

		121.775		121.775		121.775

		121.8		121.8		121.8

		121.825		121.825		121.825

		121.85		121.85		121.85

		121.875		121.875		121.875

		121.9		121.9		121.9

		121.925		121.925		121.925

		121.95		121.95		121.95

		121.975		121.975		121.975

		122		122		122

		122.025		122.025		122.025

		122.05		122.05		122.05

		122.075		122.075		122.075

		122.1		122.1		122.1

		122.125		122.125		122.125

		122.15		122.15		122.15

		122.175		122.175		122.175

		122.2		122.2		122.2

		122.225		122.225		122.225

		122.25		122.25		122.25

		122.275		122.275		122.275

		122.3		122.3		122.3

		122.325		122.325		122.325

		122.35		122.35		122.35

		122.375		122.375		122.375

		122.4		122.4		122.4

		122.425		122.425		122.425

		122.45		122.45		122.45

		122.475		122.475		122.475

		122.5		122.5		122.5

		122.525		122.525		122.525

		122.55		122.55		122.55

		122.575		122.575		122.575

		122.6		122.6		122.6

		122.625		122.625		122.625

		122.65		122.65		122.65

		122.675		122.675		122.675

		123.675		123.675		123.675

		124.675		124.675		124.675

		125.675		125.675		125.675

		126.675		126.675		126.675

		127.675		127.675		127.675

		128.675		128.675		128.675

		129.675		129.675		129.675

		130.675		130.675		130.675

		131.675		131.675		131.675

		132.675		132.675		132.675

		133.675		133.675		133.675

		134.675		134.675		134.675

		135.675		135.675		135.675

		136.675		136.675		136.675

		137.675		137.675		137.675

		138.675		138.675		138.675

		139.675		139.675		139.675

		140.675		140.675		140.675

		141.675		141.675		141.675

		142.675		142.675		142.675

		143.675		143.675		143.675

		144.675		144.675		144.675

		145.675		145.675		145.675

		146.675		146.675		146.675

		147.675		147.675		147.675

		148.675		148.675		148.675

		149.675		149.675		149.675

		150.675		150.675		150.675

		151.675		151.675		151.675

		152.675		152.675		152.675

		153.675		153.675		153.675

		154.675		154.675		154.675

		155.675		155.675		155.675

		156.675		156.675		156.675

		157.675		157.675		157.675

		158.675		158.675		158.675

		159.675		159.675		159.675

		160.675		160.675		160.675

		161.675		161.675		161.675

		162.675		162.675		162.675

		163.675		163.675		163.675

		164.675		164.675		164.675

		165.675		165.675		165.675

		166.675		166.675		166.675

		167.675		167.675		167.675

		168.675		168.675		168.675

		169.675		169.675		169.675

		170.675		170.675		170.675

		171.675		171.675		171.675

		172.675		172.675		172.675

		173.675		173.675		173.675

		174.675		174.675		174.675

		175.675		175.675		175.675

		176.675		176.675		176.675

		177.675		177.675		177.675

		178.675		178.675		178.675

		179.675		179.675		179.675

		180.675		180.675		180.675

		181.675		181.675		181.675

		182.675		182.675		182.675

		183.675		183.675		183.675

		184.675		184.675		184.675

		185.675		185.675		185.675

		186.675		186.675		186.675

		187.675		187.675		187.675

		188.675		188.675		188.675

		189.675		189.675		189.675

		190.675		190.675		190.675

		191.675		191.675		191.675

		192.675		192.675		192.675

		193.675		193.675		193.675

		194.675		194.675		194.675

		195.675		195.675		195.675

		196.675		196.675		196.675

		197.675		197.675		197.675

		198.675		198.675		198.675

		199.675		199.675		199.675

		200.675		200.675		200.675

		201.675		201.675		201.675

		202.675		202.675		202.675

		203.675		203.675		203.675

		204.675		204.675		204.675

		205.675		205.675		205.675

		206.675		206.675		206.675

		207.675		207.675		207.675

		208.675		208.675		208.675

		209.675		209.675		209.675

		210.675		210.675		210.675

		211.675		211.675		211.675

		212.675		212.675		212.675

		213.675		213.675		213.675

		214.675		214.675		214.675

		215.675		215.675		215.675

		216.675		216.675		216.675

		217.675		217.675		217.675

		218.675		218.675		218.675

		219.675		219.675		219.675

		220.675		220.675		220.675

		221.675		221.675		221.675

		222.675		222.675		222.675

		223.675		223.675		223.675

		224.675		224.675		224.675

		225.675		225.675		225.675

		226.675		226.675		226.675

		227.675		227.675		227.675

		228.675		228.675		228.675

		229.675		229.675		229.675

		230.675		230.675		230.675

		231.675		231.675		231.675

		232.675		232.675		232.675

		233.675		233.675		233.675

		234.675		234.675		234.675

		235.675		235.675		235.675

		236.675		236.675		236.675

		237.675		237.675		237.675

		238.675		238.675		238.675

		239.675		239.675		239.675

		240.675		240.675		240.675

		241.675		241.675		241.675

		242.675		242.675		242.675

		243.675		243.675		243.675

		244.675		244.675		244.675

		245.675		245.675		245.675

		246.675		246.675		246.675

		247.675		247.675		247.675

		248.675		248.675		248.675

		249.675		249.675		249.675

		250.675		250.675		250.675

		251.675		251.675		251.675

		252.675		252.675		252.675

		253.675		253.675		253.675

		254.675		254.675		254.675

		255.675		255.675		255.675

		256.67499		256.67499		256.67499

		257.67499		257.67499		257.67499

		258.67499		258.67499		258.67499

		259.67499		259.67499		259.67499

		260.67499		260.67499		260.67499

		261.67499		261.67499		261.67499

		262.67499		262.67499		262.67499

		263.67499		263.67499		263.67499

		264.67499		264.67499		264.67499

		265.67499		265.67499		265.67499

		266.67499		266.67499		266.67499

		267.67499		267.67499		267.67499

		268.67499		268.67499		268.67499

		269.67499		269.67499		269.67499

		270.67499		270.67499		270.67499

		271.67499		271.67499		271.67499

		272.67499		272.67499		272.67499

		273.67499		273.67499		273.67499

		274.67499		274.67499		274.67499

		275.67499		275.67499		275.67499

		276.67499		276.67499		276.67499

		277.67499		277.67499		277.67499

		278.67499		278.67499		278.67499

		279.67499		279.67499		279.67499

		280.67499		280.67499		280.67499

		281.67499		281.67499		281.67499

		282.67499		282.67499		282.67499

		283.67499		283.67499		283.67499

		284.67499		284.67499		284.67499

		285.67499		285.67499		285.67499

		286.67499		286.67499		286.67499

		287.67499		287.67499		287.67499

		288.67499		288.67499		288.67499

		289.67499		289.67499		289.67499

		290.67499		290.67499		290.67499

		291.67499		291.67499		291.67499

		292.67499		292.67499		292.67499

		293.67499		293.67499		293.67499

		294.67499		294.67499		294.67499

		295.67499		295.67499		295.67499

		296.67499		296.67499		296.67499

		297.67499		297.67499		297.67499

		298.67499		298.67499		298.67499

		299.67499		299.67499		299.67499

		300.67499		300.67499		300.67499

		301.67499		301.67499		301.67499

		302.67499		302.67499		302.67499

		303.67499		303.67499		303.67499

		304.67499		304.67499		304.67499

		305.67499		305.67499		305.67499

		306.67499		306.67499		306.67499

		307.67499		307.67499		307.67499

		308.67499		308.67499		308.67499

		309.67499		309.67499		309.67499

		310.67499		310.67499		310.67499

		311.67499		311.67499		311.67499

		312.67499		312.67499		312.67499

		313.67499		313.67499		313.67499

		314.67499		314.67499		314.67499

		315.67499		315.67499		315.67499

		316.67499		316.67499		316.67499

		317.67499		317.67499		317.67499

		318.67499		318.67499		318.67499

		319.67499		319.67499		319.67499

		320.67499		320.67499		320.67499

		321.67499		321.67499		321.67499

		322.67499		322.67499		322.67499

		323.67499		323.67499		323.67499

		324.67499		324.67499		324.67499

		325.67499		325.67499		325.67499

		326.67499		326.67499		326.67499

		327.67499		327.67499		327.67499

		328.67499		328.67499		328.67499

		329.67499		329.67499		329.67499

		330.67499		330.67499		330.67499

		331.67499		331.67499		331.67499

		332.67499		332.67499		332.67499

		333.67499		333.67499		333.67499

		334.67499		334.67499		334.67499

		335.67499		335.67499		335.67499

		336.67499		336.67499		336.67499

		337.67499		337.67499		337.67499

		338.67499		338.67499		338.67499

		339.67499		339.67499		339.67499

		340.67499		340.67499		340.67499

		341.67499		341.67499		341.67499

		342.67499		342.67499		342.67499

		343.67499		343.67499		343.67499

		344.67499		344.67499		344.67499

		345.67499		345.67499		345.67499

		346.67499		346.67499		346.67499

		347.67499		347.67499		347.67499

		348.67499		348.67499		348.67499

		349.67499		349.67499		349.67499

		350.67499		350.67499		350.67499

		351.67499		351.67499		351.67499

		352.67499		352.67499		352.67499

		353.67499		353.67499		353.67499

		354.67499		354.67499		354.67499

		355.67499		355.67499		355.67499

		356.67499		356.67499		356.67499

		357.67499		357.67499		357.67499

		358.67499		358.67499		358.67499

		359.67499		359.67499		359.67499

		360.67499		360.67499		360.67499

		361.67499		361.67499		361.67499

		362.67499		362.67499		362.67499

		363.67499		363.67499		363.67499

		364.67499		364.67499		364.67499

		365.67499		365.67499		365.67499

		366.67499		366.67499		366.67499

		367.67499		367.67499		367.67499

		368.67499		368.67499		368.67499

		369.67499		369.67499		369.67499

		370.67499		370.67499		370.67499

		371.67499		371.67499		371.67499

		372.67499		372.67499		372.67499

		373.67499		373.67499		373.67499

		374.67499		374.67499		374.67499

		375.67499		375.67499		375.67499

		376.67499		376.67499		376.67499

		377.67499		377.67499		377.67499

		378.67499		378.67499		378.67499

		379.67499		379.67499		379.67499

		380.67499		380.67499		380.67499

		381.67499		381.67499		381.67499

		382.67499		382.67499		382.67499

		383.67499		383.67499		383.67499

		384.67499		384.67499		384.67499

		385.67499		385.67499		385.67499

		386.67499		386.67499		386.67499

		387.67499		387.67499		387.67499

		388.67499		388.67499		388.67499

		389.67499		389.67499		389.67499

		390.67499		390.67499		390.67499

		391.67499		391.67499		391.67499

		392.67499		392.67499		392.67499

		393.67499		393.67499		393.67499

		394.67499		394.67499		394.67499

		395.67499		395.67499		395.67499

		396.67499		396.67499		396.67499

		397.67499		397.67499		397.67499

		398.67499		398.67499		398.67499

		399.67499		399.67499		399.67499

		400.67499		400.67499		400.67499

		401.67499		401.67499		401.67499

		402.67499		402.67499		402.67499

		403.67499		403.67499		403.67499

		404.67499		404.67499		404.67499

		405.67499		405.67499		405.67499

		406.67499		406.67499		406.67499

		407.67499		407.67499		407.67499

		408.67499		408.67499		408.67499

		409.67499		409.67499		409.67499

		410.67499		410.67499		410.67499

		411.67499		411.67499		411.67499

		412.67499		412.67499		412.67499

		413.67499		413.67499		413.67499

		414.67499		414.67499		414.67499

		415.67499		415.67499		415.67499

		416.67499		416.67499		416.67499

		417.67499		417.67499		417.67499

		418.67499		418.67499		418.67499

		419.67499		419.67499		419.67499

		420.67499		420.67499		420.67499

		421.67499		421.67499		421.67499

		422.67499		422.67499		422.67499

		423.67499		423.67499		423.67499

		424.67499		424.67499		424.67499

		425.67499		425.67499		425.67499

		426.67499		426.67499		426.67499

		427.67499		427.67499		427.67499

		428.67499		428.67499		428.67499

		429.67499		429.67499		429.67499

		430.67499		430.67499		430.67499

		431.67499		431.67499		431.67499

		432.67499		432.67499		432.67499

		433.67499		433.67499		433.67499

		434.67499		434.67499		434.67499

		435.67499		435.67499		435.67499

		436.67499		436.67499		436.67499

		437.67499		437.67499		437.67499

		438.67499		438.67499		438.67499

		439.67499		439.67499		439.67499

		440.67499		440.67499		440.67499

		441.67499		441.67499		441.67499

		442.67499		442.67499		442.67499

		443.67499		443.67499		443.67499

		444.67499		444.67499		444.67499

		445.67499		445.67499		445.67499

		446.67499		446.67499		446.67499

		447.67499		447.67499		447.67499

		448.67499		448.67499		448.67499

		449.67499		449.67499		449.67499

		450.67499		450.67499		450.67499

		451.67499		451.67499		451.67499

		452.67499		452.67499		452.67499

		453.67499		453.67499		453.67499

		454.67499		454.67499		454.67499

		455.67499		455.67499		455.67499

		456.67499		456.67499		456.67499

		457.67499		457.67499		457.67499

		458.67499		458.67499		458.67499

		459.67499		459.67499		459.67499

		460.67499		460.67499		460.67499

		461.67499		461.67499		461.67499

		462.67499		462.67499		462.67499

		463.67499		463.67499		463.67499

		464.67499		464.67499		464.67499

		465.67499		465.67499		465.67499

		466.67499		466.67499		466.67499

		467.67499		467.67499		467.67499

		468.67499		468.67499		468.67499

		469.67499		469.67499		469.67499

		470.67499		470.67499		470.67499

		471.67499		471.67499		471.67499

		472.67499		472.67499		472.67499

		473.67499		473.67499		473.67499

		474.67499		474.67499		474.67499

		475.67499		475.67499		475.67499

		476.67499		476.67499		476.67499

		477.67499		477.67499		477.67499

		478.67499		478.67499		478.67499

		479.67499		479.67499		479.67499

		480.67499		480.67499		480.67499

		481.67499		481.67499		481.67499

		482.67499		482.67499		482.67499

		483.67499		483.67499		483.67499

		484.67499		484.67499		484.67499

		485.67499		485.67499		485.67499

		486.67499		486.67499		486.67499

		487.67499		487.67499		487.67499

		488.67499		488.67499		488.67499

		489.67499		489.67499		489.67499

		490.67499		490.67499		490.67499

		491.67499		491.67499		491.67499

		492.67499		492.67499		492.67499

		493.67499		493.67499		493.67499

		494.67499		494.67499		494.67499

		495.67499		495.67499		495.67499

		496.67499		496.67499		496.67499

		497.67499		497.67499		497.67499

		498.67499		498.67499		498.67499

		499.67499		499.67499		499.67499

		500.67499		500.67499		500.67499

		501.67499		501.67499		501.67499

		502.67499		502.67499		502.67499

		503.67499		503.67499		503.67499

		504.67499		504.67499		504.67499

		505.67499		505.67499		505.67499

		506.67499		506.67499		506.67499

		507.67499		507.67499		507.67499

		508.67499		508.67499		508.67499

		509.67499		509.67499		509.67499

		510.67499		510.67499		510.67499

		511.67499		511.67499		511.67499

		512.67499		512.67499		512.67499

		513.67499		513.67499		513.67499

		514.67499		514.67499		514.67499

		515.67499		515.67499		515.67499

		516.67499		516.67499		516.67499

		517.67499		517.67499		517.67499

		518.67499		518.67499		518.67499

		519.67499		519.67499		519.67499

		520.67499		520.67499		520.67499

		521.67499		521.67499		521.67499

		522.67499		522.67499		522.67499

		523.67499		523.67499		523.67499

		524.67499		524.67499		524.67499

		525.67499		525.67499		525.67499

		526.67499		526.67499		526.67499

		527.67499		527.67499		527.67499

		528.67499		528.67499		528.67499

		529.67499		529.67499		529.67499

		530.67499		530.67499		530.67499

		531.67499		531.67499		531.67499

		532.67499		532.67499		532.67499

		533.67499		533.67499		533.67499

		534.67499		534.67499		534.67499

		535.67499		535.67499		535.67499

		536.67499		536.67499		536.67499

		537.67499		537.67499		537.67499

		538.67499		538.67499		538.67499

		539.67499		539.67499		539.67499

		540.67499		540.67499		540.67499

		541.67499		541.67499		541.67499

		542.67499		542.67499		542.67499

		543.67499		543.67499		543.67499

		544.67499		544.67499		544.67499

		545.67499		545.67499		545.67499

		546.67499		546.67499		546.67499

		547.67499		547.67499		547.67499

		548.67499		548.67499		548.67499

		549.67499		549.67499		549.67499

		550.67499		550.67499		550.67499

		551.67499		551.67499		551.67499

		552.67499		552.67499		552.67499

		553.67499		553.67499		553.67499

		554.67499		554.67499		554.67499

		555.67499		555.67499		555.67499

		556.67499		556.67499		556.67499

		557.67499		557.67499		557.67499

		558.67499		558.67499		558.67499

		559.67499		559.67499		559.67499

		560.67499		560.67499		560.67499

		561.67499		561.67499		561.67499

		562.67499		562.67499		562.67499

		563.67499		563.67499		563.67499

		564.67499		564.67499		564.67499

		565.67499		565.67499		565.67499

		566.67499		566.67499		566.67499

		567.67499		567.67499		567.67499

		568.67499		568.67499		568.67499

		569.67499		569.67499		569.67499

		570.67499		570.67499		570.67499

		571.67499		571.67499		571.67499

		572.67499		572.67499		572.67499

		573.67499		573.67499		573.67499

		574.67499		574.67499		574.67499

		575.67499		575.67499		575.67499

		576.67499		576.67499		576.67499

		577.67499		577.67499		577.67499

		578.67499		578.67499		578.67499

		579.67499		579.67499		579.67499

		580.67499		580.67499		580.67499

		581.67499		581.67499		581.67499

		582.67499		582.67499		582.67499

		583.67499		583.67499		583.67499

		584.67499		584.67499		584.67499

		585.67499		585.67499		585.67499

		586.67499		586.67499		586.67499

		587.67499		587.67499		587.67499

		588.67499		588.67499		588.67499

		589.67499		589.67499		589.67499

		590.67499		590.67499		590.67499

		591.67499		591.67499		591.67499

		592.67499		592.67499		592.67499

		593.67499		593.67499		593.67499

		594.67499		594.67499		594.67499

		595.67499		595.67499		595.67499

		596.67499		596.67499		596.67499

		597.67499		597.67499		597.67499

		598.67499		598.67499		598.67499

		599.67499		599.67499		599.67499

		600.67499		600.67499		600.67499

		601.67499		601.67499		601.67499

		602.67499		602.67499		602.67499

		603.67499		603.67499		603.67499

		604.67499		604.67499		604.67499

		605.67499		605.67499		605.67499

		606.67499		606.67499		606.67499

		607.67499		607.67499		607.67499

		608.67499		608.67499		608.67499

		609.67499		609.67499		609.67499

		610.67499		610.67499		610.67499

		611.67499		611.67499		611.67499

		612.67499		612.67499		612.67499

		613.67499		613.67499		613.67499

		614.67499		614.67499		614.67499

		615.67499		615.67499		615.67499

		616.67499		616.67499		616.67499

		617.67499		617.67499		617.67499

		618.67499		618.67499		618.67499

		619.67499		619.67499		619.67499

		620.67499		620.67499		620.67499

		621.67499		621.67499		621.67499

		622.67499		622.67499		622.67499

		623.67499		623.67499		623.67499

		624.67499		624.67499		624.67499

		625.67499		625.67499		625.67499

		626.67499		626.67499		626.67499

		627.67499		627.67499		627.67499

		628.67499		628.67499		628.67499

		629.67499		629.67499		629.67499

		630.67499		630.67499		630.67499

		631.67499		631.67499		631.67499

		632.67499		632.67499		632.67499

		633.67499		633.67499		633.67499

		634.67499		634.67499		634.67499

		635.67499		635.67499		635.67499

		636.67499		636.67499		636.67499

		637.67499		637.67499		637.67499

		638.67499		638.67499		638.67499

		639.67499		639.67499		639.67499

		640.67499		640.67499		640.67499

		641.67499		641.67499		641.67499

		642.67499		642.67499		642.67499

		643.67499		643.67499		643.67499

		644.67499		644.67499		644.67499

		645.67499		645.67499		645.67499

		646.67499		646.67499		646.67499

		647.67499		647.67499		647.67499

		648.67499		648.67499		648.67499

		649.67499		649.67499		649.67499

		650.67499		650.67499		650.67499

		651.67499		651.67499		651.67499

		652.67499		652.67499		652.67499

		653.67499		653.67499		653.67499

		654.67499		654.67499		654.67499

		655.67499		655.67499		655.67499

		656.67499		656.67499		656.67499

		657.67499		657.67499		657.67499

		658.67499		658.67499		658.67499

		659.67499		659.67499		659.67499

		660.67499		660.67499		660.67499

		661.67499		661.67499		661.67499

		662.67499		662.67499		662.67499

		663.67499		663.67499		663.67499

		664.67499		664.67499		664.67499

		665.67499		665.67499		665.67499

		666.67499		666.67499		666.67499

		667.67499		667.67499		667.67499

		668.67499		668.67499		668.67499

		669.67499		669.67499		669.67499

		670.67499		670.67499		670.67499

		671.67499		671.67499		671.67499

		672.67499		672.67499		672.67499

		673.67499		673.67499		673.67499

		674.67499		674.67499		674.67499

		675.67499		675.67499		675.67499

		676.67499		676.67499		676.67499

		677.67499		677.67499		677.67499

		678.67499		678.67499		678.67499

		679.67499		679.67499		679.67499

		680.67499		680.67499		680.67499

		681.67499		681.67499		681.67499

		682.67499		682.67499		682.67499

		683.67499		683.67499		683.67499

		684.67499		684.67499		684.67499

		685.67499		685.67499		685.67499

		686.67499		686.67499		686.67499

		687.67499		687.67499		687.67499

		688.67499		688.67499		688.67499

		689.67499		689.67499		689.67499

		690.67499		690.67499		690.67499

		691.67499		691.67499		691.67499

		692.67499		692.67499		692.67499

		693.67499		693.67499		693.67499

		694.67499		694.67499		694.67499

		695.67499		695.67499		695.67499

		696.67499		696.67499		696.67499

		697.67499		697.67499		697.67499

		698.67499		698.67499		698.67499

		699.67499		699.67499		699.67499

		700.67499		700.67499		700.67499

		701.67499		701.67499		701.67499

		702.67499		702.67499		702.67499

		703.67499		703.67499		703.67499

		704.67499		704.67499		704.67499

		705.67499		705.67499		705.67499

		706.67499		706.67499		706.67499

		707.67499		707.67499		707.67499

		708.67499		708.67499		708.67499

		709.67499		709.67499		709.67499

		710.67499		710.67499		710.67499

		711.67499		711.67499		711.67499

		712.67499		712.67499		712.67499

		713.67499		713.67499		713.67499

		714.67499		714.67499		714.67499

		715.67499		715.67499		715.67499

		716.67499		716.67499		716.67499

		717.67499		717.67499		717.67499

		718.67499		718.67499		718.67499

		719.67499		719.67499		719.67499

		720.67499		720.67499		720.67499

		721.67499		721.67499		721.67499

		722.67499		722.67499		722.67499

		723.67499		723.67499		723.67499

		724.67499		724.67499		724.67499

		725.67499		725.67499		725.67499

		726.67499		726.67499		726.67499

		727.67499		727.67499		727.67499

		728.67499		728.67499		728.67499

		729.67499		729.67499		729.67499

		730.67499		730.67499		730.67499

		731.67499		731.67499		731.67499

		732.67499		732.67499		732.67499

		733.67499		733.67499		733.67499

		734.67499		734.67499		734.67499

		735.67499		735.67499		735.67499

		736.67499		736.67499		736.67499

		737.67499		737.67499		737.67499

		738.67499		738.67499		738.67499

		739.67499		739.67499		739.67499

		740.67499		740.67499		740.67499

		741.67499		741.67499		741.67499

		742.67499		742.67499		742.67499

		743.67499		743.67499		743.67499

		744.67499		744.67499		744.67499

		745.67499		745.67499		745.67499

		746.67499		746.67499		746.67499

		747.67499		747.67499		747.67499

		748.67499		748.67499		748.67499

		749.67499		749.67499		749.67499

		750.67499		750.67499		750.67499

		751.67499		751.67499		751.67499

		752.67499		752.67499		752.67499

		753.67499		753.67499		753.67499

		754.67499		754.67499		754.67499

		755.67499		755.67499		755.67499

		756.67499		756.67499		756.67499

		757.67499		757.67499		757.67499

		758.67499		758.67499		758.67499

		759.67499		759.67499		759.67499

		760.67499		760.67499		760.67499

		761.67499		761.67499		761.67499

		762.67499		762.67499		762.67499

		763.67499		763.67499		763.67499

		764.67499		764.67499		764.67499

		765.67499		765.67499		765.67499

		766.67499		766.67499		766.67499

		767.67499		767.67499		767.67499

		768.67499		768.67499		768.67499

		769.67499		769.67499		769.67499

		770.67499		770.67499		770.67499

		771.67499		771.67499		771.67499

		772.67499		772.67499		772.67499

		773.67499		773.67499		773.67499

		774.67499		774.67499		774.67499

		775.67499		775.67499		775.67499

		776.67499		776.67499		776.67499

		777.67499		777.67499		777.67499

		778.67499		778.67499		778.67499

		779.67499		779.67499		779.67499

		780.67499		780.67499		780.67499

		781.67499		781.67499		781.67499

		782.67499		782.67499		782.67499

		783.67499		783.67499		783.67499

		784.67499		784.67499		784.67499

		785.67499		785.67499		785.67499

		786.67499		786.67499		786.67499

		787.67499		787.67499		787.67499

		788.67499		788.67499		788.67499

		789.67499		789.67499		789.67499

		790.67499		790.67499		790.67499

		791.67499		791.67499		791.67499

		792.67499		792.67499		792.67499

		793.67499		793.67499		793.67499

		794.67499		794.67499		794.67499

		795.67499		795.67499		795.67499

		796.67499		796.67499		796.67499

		797.67499		797.67499		797.67499

		798.67499		798.67499		798.67499

		799.67499		799.67499		799.67499

		800.67499		800.67499		800.67499

		801.67499		801.67499		801.67499

		802.67499		802.67499		802.67499

		803.67499		803.67499		803.67499

		804.67499		804.67499		804.67499

		805.67499		805.67499		805.67499

		806.67499		806.67499		806.67499

		807.67499		807.67499		807.67499

		808.67499		808.67499		808.67499

		809.67499		809.67499		809.67499

		810.67499		810.67499		810.67499

		811.67499		811.67499		811.67499

		812.67499		812.67499		812.67499

		813.67499		813.67499		813.67499

		814.67499		814.67499		814.67499

		815.67499		815.67499		815.67499

		816.67499		816.67499		816.67499

		817.67499		817.67499		817.67499

		818.67499		818.67499		818.67499

		819.67499		819.67499		819.67499

		820.67499		820.67499		820.67499

		821.67499		821.67499		821.67499

		822.67499		822.67499		822.67499

		823.67499		823.67499		823.67499

		824.67499		824.67499		824.67499

		825.67499		825.67499		825.67499

		826.67499		826.67499		826.67499

		827.67499		827.67499		827.67499

		828.67499		828.67499		828.67499

		829.67499		829.67499		829.67499

		830.67499		830.67499		830.67499

		831.67499		831.67499		831.67499

		832.67499		832.67499		832.67499

		833.67499		833.67499		833.67499

		834.67499		834.67499		834.67499

		835.67499		835.67499		835.67499

		836.67499		836.67499		836.67499

		837.67499		837.67499		837.67499

		838.67499		838.67499		838.67499

		839.67499		839.67499		839.67499

		840.67499		840.67499		840.67499

		841.67499		841.67499		841.67499

		842.67499		842.67499		842.67499

		843.67499		843.67499		843.67499

		844.67499		844.67499		844.67499

		845.67499		845.67499		845.67499

		846.67499		846.67499		846.67499

		847.67499		847.67499		847.67499

		848.67499		848.67499		848.67499

		849.67499		849.67499		849.67499

		850.67499		850.67499		850.67499

		851.67499		851.67499		851.67499

		852.67499		852.67499		852.67499

		853.67499		853.67499		853.67499

		854.67499		854.67499		854.67499

		855.67499		855.67499		855.67499

		856.67499		856.67499		856.67499

		857.67499		857.67499		857.67499

		858.67499		858.67499		858.67499

		859.67499		859.67499		859.67499

		860.67499		860.67499		860.67499

		861.67499		861.67499		861.67499

		862.67499		862.67499		862.67499

		863.67499		863.67499		863.67499

		864.67499		864.67499		864.67499

		865.67499		865.67499		865.67499

		866.67499		866.67499		866.67499

		867.67499		867.67499		867.67499

		868.67499		868.67499		868.67499

		869.67499		869.67499		869.67499

		870.67499		870.67499		870.67499

		871.67499		871.67499		871.67499

		872.67499		872.67499		872.67499

		873.67499		873.67499		873.67499

		874.67499		874.67499		874.67499

		875.67499		875.67499		875.67499

		876.67499		876.67499		876.67499

		877.67499		877.67499		877.67499

		878.67499		878.67499		878.67499

		879.67499		879.67499		879.67499

		880.67499		880.67499		880.67499

		881.67499		881.67499		881.67499

		882.67499		882.67499		882.67499

		883.67499		883.67499		883.67499

		884.67499		884.67499		884.67499

		885.67499		885.67499		885.67499

		886.67499		886.67499		886.67499

		887.67499		887.67499		887.67499

		888.67499		888.67499		888.67499

		889.67499		889.67499		889.67499

		890.67499		890.67499		890.67499

		891.67499		891.67499		891.67499

		892.67499		892.67499		892.67499

		893.67499		893.67499		893.67499

		894.67499		894.67499		894.67499

		895.67499		895.67499		895.67499

		896.67499		896.67499		896.67499

		897.67499		897.67499		897.67499

		898.67499		898.67499		898.67499

		899.67499		899.67499		899.67499

		900.67499		900.67499		900.67499

		901.67499		901.67499		901.67499

		902.67499		902.67499		902.67499

		903.67499		903.67499		903.67499

		904.67499		904.67499		904.67499

		905.67499		905.67499		905.67499

		906.67499		906.67499		906.67499

		907.67499		907.67499		907.67499

		908.67499		908.67499		908.67499

		909.67499		909.67499		909.67499

		910.67499		910.67499		910.67499

		911.67499		911.67499		911.67499

		912.67499		912.67499		912.67499

		913.67499		913.67499		913.67499

		914.67499		914.67499		914.67499

		915.67499		915.67499		915.67499

		916.67499		916.67499		916.67499

		917.67499		917.67499		917.67499

		918.67499		918.67499		918.67499

		919.67499		919.67499		919.67499

		920.67499		920.67499		920.67499

		921.67499		921.67499		921.67499

		922.67499		922.67499		922.67499

		923.67499		923.67499		923.67499

		924.67499		924.67499		924.67499

		925.67499		925.67499		925.67499

		926.67499		926.67499		926.67499

		927.67499		927.67499		927.67499

		928.67499		928.67499		928.67499

		929.67499		929.67499		929.67499

		930.67499		930.67499		930.67499

		931.67499		931.67499		931.67499

		932.67499		932.67499		932.67499

		933.67499		933.67499		933.67499

		934.67499		934.67499		934.67499

		935.67499		935.67499		935.67499

		936.67499		936.67499		936.67499

		937.67499		937.67499		937.67499

		938.67499		938.67499		938.67499

		939.67499		939.67499		939.67499

		940.67499		940.67499		940.67499

		941.67499		941.67499		941.67499

		942.67499		942.67499		942.67499

		943.67499		943.67499		943.67499

		944.67499		944.67499		944.67499

		945.67499		945.67499		945.67499

		946.67499		946.67499		946.67499

		947.67499		947.67499		947.67499

		948.67499		948.67499		948.67499

		949.67499		949.67499		949.67499

		950.67499		950.67499		950.67499

		951.67499		951.67499		951.67499

		952.67499		952.67499		952.67499

		953.67499		953.67499		953.67499

		954.67499		954.67499		954.67499

		955.67499		955.67499		955.67499

		956.67499		956.67499		956.67499

		957.67499		957.67499		957.67499

		958.67499		958.67499		958.67499

		959.67499		959.67499		959.67499

		960.67499		960.67499		960.67499

		961.67499		961.67499		961.67499

		962.67499		962.67499		962.67499

		963.67499		963.67499		963.67499

		964.67499		964.67499		964.67499

		965.67499		965.67499		965.67499

		966.67499		966.67499		966.67499

		967.67499		967.67499		967.67499

		968.67499		968.67499		968.67499

		969.67499		969.67499		969.67499

		970.67499		970.67499		970.67499

		971.67499		971.67499		971.67499

		972.67499		972.67499		972.67499

		973.67499		973.67499		973.67499

		974.67499		974.67499		974.67499

		975.67499		975.67499		975.67499

		976.67499		976.67499		976.67499

		977.67499		977.67499		977.67499

		978.67499		978.67499		978.67499

		979.67499		979.67499		979.67499

		980.67499		980.67499		980.67499

		981.67499		981.67499		981.67499

		982.67499		982.67499		982.67499

		983.67499		983.67499		983.67499

		984.67499		984.67499		984.67499

		985.67499		985.67499		985.67499

		986.67499		986.67499		986.67499

		987.67499		987.67499		987.67499

		988.67499		988.67499		988.67499

		989.67499		989.67499		989.67499

		990.67499		990.67499		990.67499

		991.67499		991.67499		991.67499

		992.67499		992.67499		992.67499

		993.67499		993.67499		993.67499

		994.67499		994.67499		994.67499

		995.67499		995.67499		995.67499

		996.67499		996.67499		996.67499

		997.67499		997.67499		997.67499

		998.67499		998.67499		998.67499

		999.67499		999.67499		999.67499

		1000.67499		1000.67499		1000.67499

		1001.67499		1001.67499		1001.67499

		1002.67499		1002.67499		1002.67499

		1003.67499		1003.67499		1003.67499

		1004.67499		1004.67499		1004.67499

		1005.67499		1005.67499		1005.67499

		1006.67499		1006.67499		1006.67499

		1007.67499		1007.67499		1007.67499

		1008.67499		1008.67499		1008.67499

		1009.67499		1009.67499		1009.67499

		1010.67499		1010.67499		1010.67499

		1011.67499		1011.67499		1011.67499

		1012.67499		1012.67499		1012.67499

		1013.67499		1013.67499		1013.67499

		1014.67499		1014.67499		1014.67499

		1015.67499		1015.67499		1015.67499

		1016.67499		1016.67499		1016.67499

		1017.67499		1017.67499		1017.67499

		1018.67499		1018.67499		1018.67499

		1019.67499		1019.67499		1019.67499

		1020.67499		1020.67499		1020.67499

		1021.67499		1021.67499		1021.67499

		1022.67499		1022.67499		1022.67499

		1023.67499		1023.67499		1023.67499

		1024.67505		1024.67505		1024.67505

		1025.67505		1025.67505		1025.67505

		1026.67505		1026.67505		1026.67505

		1027.67505		1027.67505		1027.67505

		1028.67505		1028.67505		1028.67505

		1029.67505		1029.67505		1029.67505

		1030.67505		1030.67505		1030.67505

		1031.67505		1031.67505		1031.67505

		1032.67505		1032.67505		1032.67505

		1033.67505		1033.67505		1033.67505

		1034.67505		1034.67505		1034.67505

		1035.67505		1035.67505		1035.67505

		1036.67505		1036.67505		1036.67505

		1037.67505		1037.67505		1037.67505

		1038.67505		1038.67505		1038.67505

		1039.67505		1039.67505		1039.67505

		1040.67505		1040.67505		1040.67505

		1041.67505		1041.67505		1041.67505

		1042.67505		1042.67505		1042.67505

		1043.67505		1043.67505		1043.67505

		1044.67505		1044.67505		1044.67505

		1045.67505		1045.67505		1045.67505

		1046.67505		1046.67505		1046.67505

		1047.67505		1047.67505		1047.67505

		1048.67505		1048.67505		1048.67505

		1049.67505		1049.67505		1049.67505

		1050.67505		1050.67505		1050.67505

		1051.67505		1051.67505		1051.67505

		1052.67505		1052.67505		1052.67505

		1053.67505		1053.67505		1053.67505

		1054.67505		1054.67505		1054.67505

		1055.67505		1055.67505		1055.67505

		1056.67505		1056.67505		1056.67505

		1057.67505		1057.67505		1057.67505

		1058.67505		1058.67505		1058.67505

		1059.67505		1059.67505		1059.67505

		1060.67505		1060.67505		1060.67505

		1061.67505		1061.67505		1061.67505

		1062.67505		1062.67505		1062.67505

		1063.67505		1063.67505		1063.67505

		1064.67505		1064.67505		1064.67505

		1065.67505		1065.67505		1065.67505

		1066.67505		1066.67505		1066.67505

		1067.67505		1067.67505		1067.67505

		1068.67505		1068.67505		1068.67505

		1069.67505		1069.67505		1069.67505

		1070.67505		1070.67505		1070.67505

		1071.67505		1071.67505		1071.67505

		1072.67505		1072.67505		1072.67505

		1073.67505		1073.67505		1073.67505

		1074.67505		1074.67505		1074.67505

		1075.67505		1075.67505		1075.67505

		1076.67505		1076.67505		1076.67505

		1077.67505		1077.67505		1077.67505

		1078.67505		1078.67505		1078.67505

		1079.67505		1079.67505		1079.67505

		1080.67505		1080.67505		1080.67505

		1081.67505		1081.67505		1081.67505

		1082.67505		1082.67505		1082.67505

		1083.67505		1083.67505		1083.67505

		1084.67505		1084.67505		1084.67505

		1085.67505		1085.67505		1085.67505

		1086.67505		1086.67505		1086.67505

		1087.67505		1087.67505		1087.67505

		1088.67505		1088.67505		1088.67505

		1089.67505		1089.67505		1089.67505

		1090.67505		1090.67505		1090.67505

		1091.67505		1091.67505		1091.67505

		1092.67505		1092.67505		1092.67505

		1093.67505		1093.67505		1093.67505

		1094.67505		1094.67505		1094.67505

		1095.67505		1095.67505		1095.67505

		1096.67505		1096.67505		1096.67505

		1097.67505		1097.67505		1097.67505

		1098.67505		1098.67505		1098.67505

		1099.67505		1099.67505		1099.67505

		1100.67505		1100.67505		1100.67505

		1101.67505		1101.67505		1101.67505

		1102.67505		1102.67505		1102.67505

		1103.67505		1103.67505		1103.67505

		1104.67505		1104.67505		1104.67505

		1105.67505		1105.67505		1105.67505

		1106.67505		1106.67505		1106.67505

		1107.67505		1107.67505		1107.67505

		1108.67505		1108.67505		1108.67505

		1109.67505		1109.67505		1109.67505

		1110.67505		1110.67505		1110.67505

		1111.67505		1111.67505		1111.67505

		1112.67505		1112.67505		1112.67505

		1113.67505		1113.67505		1113.67505

		1114.67505		1114.67505		1114.67505

		1115.67505		1115.67505		1115.67505

		1116.67505		1116.67505		1116.67505

		1117.67505		1117.67505		1117.67505

		1118.67505		1118.67505		1118.67505

		1119.67505		1119.67505		1119.67505

		1120.67505		1120.67505		1120.67505

		1121.67505		1121.67505		1121.67505

		1122.67505		1122.67505		1122.67505

		1123.67505		1123.67505		1123.67505

		1124.67505		1124.67505		1124.67505

		1125.67505		1125.67505		1125.67505

		1126.67505		1126.67505		1126.67505

		1127.67505		1127.67505		1127.67505

		1128.67505		1128.67505		1128.67505

		1129.67505		1129.67505		1129.67505

		1130.67505		1130.67505		1130.67505

		1131.67505		1131.67505		1131.67505

		1132.67505		1132.67505		1132.67505

		1133.67505		1133.67505		1133.67505

		1134.67505		1134.67505		1134.67505

		1135.67505		1135.67505		1135.67505

		1136.67505		1136.67505		1136.67505

		1137.67505		1137.67505		1137.67505

		1138.67505		1138.67505		1138.67505

		1139.67505		1139.67505		1139.67505

		1140.67505		1140.67505		1140.67505

		1141.67505		1141.67505		1141.67505

		1142.67505		1142.67505		1142.67505

		1143.67505		1143.67505		1143.67505

		1144.67505		1144.67505		1144.67505

		1145.67505		1145.67505		1145.67505

		1146.67505		1146.67505		1146.67505

		1147.67505		1147.67505		1147.67505

		1148.67505		1148.67505		1148.67505

		1149.67505		1149.67505		1149.67505

		1150.67505		1150.67505		1150.67505

		1151.67505		1151.67505		1151.67505

		1152.67505		1152.67505		1152.67505

		1153.67505		1153.67505		1153.67505

		1154.67505		1154.67505		1154.67505

		1155.67505		1155.67505		1155.67505

		1156.67505		1156.67505		1156.67505

		1157.67505		1157.67505		1157.67505

		1158.67505		1158.67505		1158.67505

		1159.67505		1159.67505		1159.67505

		1160.67505		1160.67505		1160.67505

		1161.67505		1161.67505		1161.67505

		1162.67505		1162.67505		1162.67505

		1163.67505		1163.67505		1163.67505

		1164.67505		1164.67505		1164.67505

		1165.67505		1165.67505		1165.67505

		1166.67505		1166.67505		1166.67505

		1167.67505		1167.67505		1167.67505

		1168.67505		1168.67505		1168.67505

		1169.67505		1169.67505		1169.67505

		1170.67505		1170.67505		1170.67505

		1171.67505		1171.67505		1171.67505

		1172.67505		1172.67505		1172.67505

		1173.67505		1173.67505		1173.67505

		1174.67505		1174.67505		1174.67505

		1175.67505		1175.67505		1175.67505

		1176.67505		1176.67505		1176.67505

		1177.67505		1177.67505		1177.67505

		1178.67505		1178.67505		1178.67505

		1179.67505		1179.67505		1179.67505

		1180.67505		1180.67505		1180.67505

		1181.67505		1181.67505		1181.67505

		1182.67505		1182.67505		1182.67505

		1183.67505		1183.67505		1183.67505

		1184.67505		1184.67505		1184.67505

		1185.67505		1185.67505		1185.67505

		1186.67505		1186.67505		1186.67505

		1187.67505		1187.67505		1187.67505

		1188.67505		1188.67505		1188.67505

		1189.67505		1189.67505		1189.67505

		1190.67505		1190.67505		1190.67505

		1191.67505		1191.67505		1191.67505

		1192.67505		1192.67505		1192.67505

		1193.67505		1193.67505		1193.67505

		1194.67505		1194.67505		1194.67505

		1195.67505		1195.67505		1195.67505

		1196.67505		1196.67505		1196.67505

		1197.67505		1197.67505		1197.67505

		1198.67505		1198.67505		1198.67505

		1199.67505		1199.67505		1199.67505

		1200.67505		1200.67505		1200.67505

		1201.67505		1201.67505		1201.67505

		1202.67505		1202.67505		1202.67505

		1203.67505		1203.67505		1203.67505

		1204.67505		1204.67505		1204.67505

		1205.67505		1205.67505		1205.67505

		1206.67505		1206.67505		1206.67505

		1207.67505		1207.67505		1207.67505

		1208.67505		1208.67505		1208.67505

		1209.67505		1209.67505		1209.67505

		1210.67505		1210.67505		1210.67505

		1211.67505		1211.67505		1211.67505

		1212.67505		1212.67505		1212.67505

		1213.67505		1213.67505		1213.67505

		1214.67505		1214.67505		1214.67505

		1215.67505		1215.67505		1215.67505

		1216.67505		1216.67505		1216.67505

		1217.67505		1217.67505		1217.67505

		1218.67505		1218.67505		1218.67505

		1219.67505		1219.67505		1219.67505

		1220.67505		1220.67505		1220.67505

		1221.67505		1221.67505		1221.67505

		1222.67505		1222.67505		1222.67505

		1223.67505		1223.67505		1223.67505

		1224.67505		1224.67505		1224.67505

		1225.67505		1225.67505		1225.67505

		1226.67505		1226.67505		1226.67505

		1227.67505		1227.67505		1227.67505

		1228.67505		1228.67505		1228.67505

		1229.67505		1229.67505		1229.67505

		1230.67505		1230.67505		1230.67505

		1231.67505		1231.67505		1231.67505

		1232.67505		1232.67505		1232.67505

		1233.67505		1233.67505		1233.67505

		1234.67505		1234.67505		1234.67505

		1235.67505		1235.67505		1235.67505

		1236.67505		1236.67505		1236.67505

		1237.67505		1237.67505		1237.67505

		1238.67505		1238.67505		1238.67505

		1239.67505		1239.67505		1239.67505

		1240.67505		1240.67505		1240.67505

		1241.67505		1241.67505		1241.67505

		1242.67505		1242.67505		1242.67505

		1243.67505		1243.67505		1243.67505

		1244.67505		1244.67505		1244.67505

		1245.67505		1245.67505		1245.67505

		1246.67505		1246.67505		1246.67505

		1247.67505		1247.67505		1247.67505

		1248.67505		1248.67505		1248.67505

		1249.67505		1249.67505		1249.67505

		1250.67505		1250.67505		1250.67505

		1251.67505		1251.67505		1251.67505

		1252.67505		1252.67505		1252.67505

		1253.67505		1253.67505		1253.67505

		1254.67505		1254.67505		1254.67505

		1255.67505		1255.67505		1255.67505

		1256.67505		1256.67505		1256.67505

		1257.67505		1257.67505		1257.67505

		1258.67505		1258.67505		1258.67505

		1259.67505		1259.67505		1259.67505

		1260.67505		1260.67505		1260.67505

		1261.67505		1261.67505		1261.67505

		1262.67505		1262.67505		1262.67505

		1263.67505		1263.67505		1263.67505

		1264.67505		1264.67505		1264.67505

		1265.67505		1265.67505		1265.67505

		1266.67505		1266.67505		1266.67505

		1267.67505		1267.67505		1267.67505

		1268.67505		1268.67505		1268.67505

		1269.67505		1269.67505		1269.67505

		1270.67505		1270.67505		1270.67505

		1271.67505		1271.67505		1271.67505

		1272.67505		1272.67505		1272.67505

		1273.67505		1273.67505		1273.67505

		1274.67505		1274.67505		1274.67505

		1275.67505		1275.67505		1275.67505

		1276.67505		1276.67505		1276.67505

		1277.67505		1277.67505		1277.67505

		1278.67505		1278.67505		1278.67505

		1279.67505		1279.67505		1279.67505

		1280.67505		1280.67505		1280.67505

		1281.67505		1281.67505		1281.67505

		1282.67505		1282.67505		1282.67505

		1283.67505		1283.67505		1283.67505

		1284.67505		1284.67505		1284.67505

		1285.67505		1285.67505		1285.67505

		1286.67505		1286.67505		1286.67505

		1287.67505		1287.67505		1287.67505

		1288.67505		1288.67505		1288.67505

		1289.67505		1289.67505		1289.67505

		1290.67505		1290.67505		1290.67505

		1291.67505		1291.67505		1291.67505

		1292.67505		1292.67505		1292.67505

		1293.67505		1293.67505		1293.67505

		1294.67505		1294.67505		1294.67505

		1295.67505		1295.67505		1295.67505

		1296.67505		1296.67505		1296.67505

		1297.67505		1297.67505		1297.67505

		1298.67505		1298.67505		1298.67505

		1299.67505		1299.67505		1299.67505

		1300.67505		1300.67505		1300.67505

		1301.67505		1301.67505		1301.67505

		1302.67505		1302.67505		1302.67505

		1303.67505		1303.67505		1303.67505

		1304.67505		1304.67505		1304.67505

		1305.67505		1305.67505		1305.67505

		1306.67505		1306.67505		1306.67505

		1307.67505		1307.67505		1307.67505

		1308.67505		1308.67505		1308.67505

		1309.67505		1309.67505		1309.67505

		1310.67505		1310.67505		1310.67505

		1311.67505		1311.67505		1311.67505

		1312.67505		1312.67505		1312.67505

		1313.67505		1313.67505		1313.67505

		1314.67505		1314.67505		1314.67505

		1315.67505		1315.67505		1315.67505

		1316.67505		1316.67505		1316.67505

		1317.67505		1317.67505		1317.67505

		1318.67505		1318.67505		1318.67505

		1319.67505		1319.67505		1319.67505

		1320.67505		1320.67505		1320.67505

		1321.67505		1321.67505		1321.67505

		1322.67505		1322.67505		1322.67505

		1323.67505		1323.67505		1323.67505

		1324.67505		1324.67505		1324.67505

		1325.67505		1325.67505		1325.67505

		1326.67505		1326.67505		1326.67505

		1327.67505		1327.67505		1327.67505

		1328.67505		1328.67505		1328.67505

		1329.67505		1329.67505		1329.67505

		1330.67505		1330.67505		1330.67505

		1331.67505		1331.67505		1331.67505

		1332.67505		1332.67505		1332.67505

		1333.67505		1333.67505		1333.67505

		1334.67505		1334.67505		1334.67505

		1335.67505		1335.67505		1335.67505

		1336.67505		1336.67505		1336.67505

		1337.67505		1337.67505		1337.67505

		1338.67505		1338.67505		1338.67505

		1339.67505		1339.67505		1339.67505

		1340.67505		1340.67505		1340.67505

		1341.67505		1341.67505		1341.67505

		1342.67505		1342.67505		1342.67505

		1343.67505		1343.67505		1343.67505

		1344.67505		1344.67505		1344.67505

		1345.67505		1345.67505		1345.67505

		1346.67505		1346.67505		1346.67505

		1347.67505		1347.67505		1347.67505

		1348.67505		1348.67505		1348.67505

		1349.67505		1349.67505		1349.67505

		1350.67505		1350.67505		1350.67505

		1351.67505		1351.67505		1351.67505

		1352.67505		1352.67505		1352.67505

		1353.67505		1353.67505		1353.67505

		1354.67505		1354.67505		1354.67505

		1355.67505		1355.67505		1355.67505

		1356.67505		1356.67505		1356.67505

		1357.67505		1357.67505		1357.67505

		1358.67505		1358.67505		1358.67505

		1359.67505		1359.67505		1359.67505

		1360.67505		1360.67505		1360.67505

		1361.67505		1361.67505		1361.67505

		1362.67505		1362.67505		1362.67505

		1363.67505		1363.67505		1363.67505

		1364.67505		1364.67505		1364.67505

		1365.67505		1365.67505		1365.67505

		1366.67505		1366.67505		1366.67505

		1367.67505		1367.67505		1367.67505

		1368.67505		1368.67505		1368.67505

		1369.67505		1369.67505		1369.67505

		1370.67505		1370.67505		1370.67505

		1371.67505		1371.67505		1371.67505

		1372.67505		1372.67505		1372.67505

		1373.67505		1373.67505		1373.67505

		1374.67505		1374.67505		1374.67505

		1375.67505		1375.67505		1375.67505

		1376.67505		1376.67505		1376.67505

		1377.67505		1377.67505		1377.67505

		1378.67505		1378.67505		1378.67505

		1379.67505		1379.67505		1379.67505

		1380.67505		1380.67505		1380.67505

		1381.67505		1381.67505		1381.67505

		1382.67505		1382.67505		1382.67505

		1383.67505		1383.67505		1383.67505

		1384.67505		1384.67505		1384.67505

		1385.67505		1385.67505		1385.67505

		1386.67505		1386.67505		1386.67505

		1387.67505		1387.67505		1387.67505

		1388.67505		1388.67505		1388.67505

		1389.67505		1389.67505		1389.67505

		1390.67505		1390.67505		1390.67505

		1391.67505		1391.67505		1391.67505

		1392.67505		1392.67505		1392.67505

		1393.67505		1393.67505		1393.67505

		1394.67505		1394.67505		1394.67505

		1395.67505		1395.67505		1395.67505

		1396.67505		1396.67505		1396.67505

		1397.67505		1397.67505		1397.67505

		1398.67505		1398.67505		1398.67505

		1399.67505		1399.67505		1399.67505

		1400.67505		1400.67505		1400.67505

		1401.67505		1401.67505		1401.67505

		1402.67505		1402.67505		1402.67505

		1403.67505		1403.67505		1403.67505

		1404.67505		1404.67505		1404.67505

		1405.67505		1405.67505		1405.67505

		1406.67505		1406.67505		1406.67505

		1407.67505		1407.67505		1407.67505

		1408.67505		1408.67505		1408.67505

		1409.67505		1409.67505		1409.67505

		1410.67505		1410.67505		1410.67505

		1411.67505		1411.67505		1411.67505

		1412.67505		1412.67505		1412.67505

		1413.67505		1413.67505		1413.67505

		1414.67505		1414.67505		1414.67505

		1415.67505		1415.67505		1415.67505

		1416.67505		1416.67505		1416.67505

		1417.67505		1417.67505		1417.67505

		1418.67505		1418.67505		1418.67505

		1419.67505		1419.67505		1419.67505

		1420.67505		1420.67505		1420.67505

		1421.67505		1421.67505		1421.67505

		1422.67505		1422.67505		1422.67505

		1423.67505		1423.67505		1423.67505

		1424.67505		1424.67505		1424.67505

		1425.67505		1425.67505		1425.67505

		1426.67505		1426.67505		1426.67505

		1427.67505		1427.67505		1427.67505

		1428.67505		1428.67505		1428.67505

		1429.67505		1429.67505		1429.67505

		1430.67505		1430.67505		1430.67505

		1431.67505		1431.67505		1431.67505

		1432.67505		1432.67505		1432.67505

		1433.67505		1433.67505		1433.67505

		1434.67505		1434.67505		1434.67505

		1435.67505		1435.67505		1435.67505

		1436.67505		1436.67505		1436.67505

		1437.67505		1437.67505		1437.67505

		1438.67505		1438.67505		1438.67505

		1439.67505		1439.67505		1439.67505

		1440.67505		1440.67505		1440.67505

		1441.67505		1441.67505		1441.67505

		1442.67505		1442.67505		1442.67505

		1443.67505		1443.67505		1443.67505

		1444.67505		1444.67505		1444.67505

		1445.67505		1445.67505		1445.67505

		1446.67505		1446.67505		1446.67505

		1447.67505		1447.67505		1447.67505

		1448.67505		1448.67505		1448.67505

		1449.67505		1449.67505		1449.67505

		1450.67505		1450.67505		1450.67505

		1451.67505		1451.67505		1451.67505

		1452.67505		1452.67505		1452.67505

		1453.67505		1453.67505		1453.67505

		1454.67505		1454.67505		1454.67505

		1455.67505		1455.67505		1455.67505

		1456.67505		1456.67505		1456.67505

		1457.67505		1457.67505		1457.67505

		1458.67505		1458.67505		1458.67505

		1459.67505		1459.67505		1459.67505

		1460.67505		1460.67505		1460.67505

		1461.67505		1461.67505		1461.67505

		1462.67505		1462.67505		1462.67505

		1463.67505		1463.67505		1463.67505

		1464.67505		1464.67505		1464.67505

		1465.67505		1465.67505		1465.67505

		1466.67505		1466.67505		1466.67505

		1467.67505		1467.67505		1467.67505

		1468.67505		1468.67505		1468.67505

		1469.67505		1469.67505		1469.67505

		1470.67505		1470.67505		1470.67505

		1471.67505		1471.67505		1471.67505

		1472.67505		1472.67505		1472.67505

		1473.67505		1473.67505		1473.67505

		1474.67505		1474.67505		1474.67505

		1475.67505		1475.67505		1475.67505

		1476.67505		1476.67505		1476.67505

		1477.67505		1477.67505		1477.67505

		1478.67505		1478.67505		1478.67505

		1479.67505		1479.67505		1479.67505

		1480.67505		1480.67505		1480.67505

		1481.67505		1481.67505		1481.67505

		1482.67505		1482.67505		1482.67505

		1483.67505		1483.67505		1483.67505

		1484.67505		1484.67505		1484.67505

		1485.67505		1485.67505		1485.67505

		1486.67505		1486.67505		1486.67505

		1487.67505		1487.67505		1487.67505

		1488.67505		1488.67505		1488.67505

		1489.67505		1489.67505		1489.67505

		1490.67505		1490.67505		1490.67505

		1491.67505		1491.67505		1491.67505

		1492.67505		1492.67505		1492.67505

		1493.67505		1493.67505		1493.67505

		1494.67505		1494.67505		1494.67505

		1495.67505		1495.67505		1495.67505

		1496.67505		1496.67505		1496.67505

		1497.67505		1497.67505		1497.67505

		1498.67505		1498.67505		1498.67505

		1499.67505		1499.67505		1499.67505

		1500.67505		1500.67505		1500.67505

		1501.67505		1501.67505		1501.67505

		1502.67505		1502.67505		1502.67505

		1503.67505		1503.67505		1503.67505

		1504.67505		1504.67505		1504.67505

		1505.67505		1505.67505		1505.67505

		1506.67505		1506.67505		1506.67505

		1507.67505		1507.67505		1507.67505

		1508.67505		1508.67505		1508.67505

		1509.67505		1509.67505		1509.67505

		1510.67505		1510.67505		1510.67505

		1511.67505		1511.67505		1511.67505

		1512.67505		1512.67505		1512.67505

		1513.67505		1513.67505		1513.67505

		1514.67505		1514.67505		1514.67505

		1515.67505		1515.67505		1515.67505

		1516.67505		1516.67505		1516.67505

		1517.67505		1517.67505		1517.67505

		1518.67505		1518.67505		1518.67505

		1519.67505		1519.67505		1519.67505

		1520.67505		1520.67505		1520.67505

		1521.67505		1521.67505		1521.67505

		1522.67505		1522.67505		1522.67505

		1523.67505		1523.67505		1523.67505

		1524.67505		1524.67505		1524.67505

		1525.67505		1525.67505		1525.67505

		1526.67505		1526.67505		1526.67505

		1527.67505		1527.67505		1527.67505

		1528.67505		1528.67505		1528.67505

		1529.67505		1529.67505		1529.67505

		1530.67505		1530.67505		1530.67505

		1531.67505		1531.67505		1531.67505

		1532.67505		1532.67505		1532.67505

		1533.67505		1533.67505		1533.67505

		1534.67505		1534.67505		1534.67505

		1535.67505		1535.67505		1535.67505

		1536.67505		1536.67505		1536.67505

		1537.67505		1537.67505		1537.67505

		1538.67505		1538.67505		1538.67505

		1539.67505		1539.67505		1539.67505

		1540.67505		1540.67505		1540.67505

		1541.67505		1541.67505		1541.67505

		1542.67505		1542.67505		1542.67505

		1543.67505		1543.67505		1543.67505

		1544.67505		1544.67505		1544.67505

		1545.67505		1545.67505		1545.67505

		1546.67505		1546.67505		1546.67505

		1547.67505		1547.67505		1547.67505

		1548.67505		1548.67505		1548.67505

		1549.67505		1549.67505		1549.67505

		1550.67505		1550.67505		1550.67505

		1551.67505		1551.67505		1551.67505

		1552.67505		1552.67505		1552.67505

		1553.67505		1553.67505		1553.67505

		1554.67505		1554.67505		1554.67505

		1555.67505		1555.67505		1555.67505

		1556.67505		1556.67505		1556.67505

		1557.67505		1557.67505		1557.67505

		1558.67505		1558.67505		1558.67505

		1559.67505		1559.67505		1559.67505

		1560.67505		1560.67505		1560.67505

		1561.67505		1561.67505		1561.67505

		1562.67505		1562.67505		1562.67505

		1563.67505		1563.67505		1563.67505

		1564.67505		1564.67505		1564.67505

		1565.67505		1565.67505		1565.67505



As received FeCrAl

Aluminized FeCrAl

Aluminized FeCrAl

Time [min]

Mass gain [mg/cm2]

Temperature [°C]

0

0

26.096

-0.0007379862

-0.000288197

26.098

-0.0009924642

-0.0001440985

26.108

-0.0055730682

-0.0000617565

26.108

-0.0059038896

0.000041171

26.115

-0.0014759724

0.0001852695

26.113

0.0046823952

0.000288197

26.113

0.013105617

0.0003911245

26.116

0.0055476204

0.0004734665

26.104

0.0092375514

0.0005763939

26.113

0.0084486696

0.0006587359

26.105

0.009670164

0.0007410779

26.108

0.012087705

0.0008234199

26.107

0.0074307576

0.0008851764

26.104

0.0064382934

0.0009263474

26.113

0.008652252

0.0009675184

26.116

0.0053694858

0.0010086894

26.104

0.007761579

0.0010498604

26.099

0.0065909802

0.0010704459

26.12

0.0057512028

0.0010910314

26.115

0.0059547852

0.0011116169

26.125

0.0068963538

0.0011116169

26.122

0.01145151

0.0011322024

26.124

0.0035881398

0.0011322024

26.133

0.0043006782

0.0011116169

26.131

0.0003562692

0.0011116169

26.128

0.0011197032

0.0011116169

26.132

0.0054458292

0.0010910314

26.145

0.0015523158

0.0010704459

26.154

0.0040970958

0.0010704459

26.157

0.0001781346

0.0010498604

26.172

0.0035881398

0.0010498604

26.172

-0.0007379862

0.0010292749

26.173

0.0052422468

0.0010292749

26.182

-0.0000763434

0.0010292749

26.195

-0.005471277

0.0010498604

26.201

0.000127239

0.0010498604

26.206

0

0.0010704459

26.221

0.0036644832

0.0010910314

26.232

0.0080924004

0.0011322024

26.235

0.0042243348

0.0011527879

26.247

0.0063873978

0.0011939589

26.25

0.0022394064

0.0012351299

26.267

0.0018067938

0.0012968864

26.276

0.0045297084

0.0013380574

26.284

0.0017558982

0.0013998139

26.296

0.0025702278

0.0014615703

26.304

0.0025956756

0.0015233268

26.325

0.0067691148

0.0015850833

26.332

0.0023666454

0.0016674253

26.334

0.001399629

0.0017291818

26.358

0.005725755

0.0017909383

26.359

-0.0002035824

0.0018732803

26.373

0.0077361312

0.0019350368

26.383

0.0032064228

0.0019967933

26.392

0.0114006144

0.0020585498

26.411

0.004453365

0.0021203063

26.427

0.0004580604

0.0021820628

26.438

0.0015777636

0.0022438193

26.449

0.0048605298

0.0023055758

26.463

-0.0007125384

0.0023673323

26.474

0.0062856066

0.0024085032

26.488

0.009924642

0.0024702597

26.501

0.0084486696

0.0025114307

26.509

0.0101282244

0.0025731872

26.538

0.0132583038

0.0026143582

26.546

0.004326126

0.0026761147

26.556

0.001399629

0.0027172857

26.576

-0.000636195

0.0027790422

26.601

-0.0040207524

0.0028407987

26.619

-0.0112988232

0.0028819697

26.628

0.0033336618

0.0029437262

26.642

-0.0050386644

0.0029848972

26.661

-0.0006616428

0.0030466537

26.677

0.000127239

0.0030878247

26.69

0.001399629

0.0031495812

26.707

0.0053185902

0.0031907522

26.729

0.0029519448

0.0032525087

26.743

0.0070490406

0.0032936797

26.772

0.0010433598

0.0033348506

26.781

0.007379862

0.0033966071

26.808

-0.0010942554

0.0034377781

26.829

0.0070235928

0.0034789491

26.847

0.0094411338

0.0035407056

26.864

0.007761579

0.0035818766

26.879

0.0070235928

0.0036436331

26.904

-0.0005344038

0.0037053896

26.923

0.0081941916

0.0037671461

26.933

0.0031300794

0.0038289026

26.95

0.0063873978

0.0038906591

26.981

0.0017558982

0.0039524156

27

0.0062092632

0.0040141721

27.023

0.0077106834

0.0040965141

27.041

-0.0047332908

0.0041582706

27.066

0.0046060518

0.0042406126

27.087

-0.0025956756

0.004302369

27.115

-0.0020103762

0.0043641255

27.13

0.0112988232

0.0044464675

27.151

0.0006616428

0.004508224

27.175

0.0037917222

0.0045699805

27.208

0.0005852994

0.0046523225

27.221

-0.0039953046

0.004714079

27.244

0.0059293374

0.0047758355

27.271

0.0092375514

0.004837592

27.297

0

0.004878763

27.331

-0.006107472

0.0049405195

27.343

-0.0003053736

0.005002276

27.373

0.0070999362

0.005043447

27.411

0.0010688076

0.0051052035

27.429

0.0043770216

0.0051463745

27.463

-0.0086268042

0.0051875455

27.489

-0.0041225436

0.0052493019

27.513

0.0029519448

0.0052904729

27.545

-0.0006616428

0.0053316439

27.563

0.011197032

0.0053934004

27.6

0.0039189612

0.0054345714

27.617

0.0005344038

0.0054757424

27.653

0.0041734392

0.0055374989

27.676

0.0055221726

0.0055786699

27.709

0.0021885108

0.0056404264

27.734

0.0064637412

0.0056815974

27.766

0.0068963538

0.0057433539

27.8

-0.0042497826

0.0058051104

27.83

0.0065400846

0.0058462814

27.863

-0.0050641122

0.0059080379

27.886

0.0078124746

0.0059697944

27.917

0.007507101

0.0060109654

27.961

0.0008143296

0.0060727219

27.984

0.0078633702

0.0061138929

28.023

0.0080924004

0.0061550639

28.051

0.0030791838

0.0061962348

28.083

0.0038680656

0.0062374058

28.125

-0.0092375514

0.0062579913

28.155

0.0060820242

0.0062991623

28.183

0.0038426178

0.0063197478

28.224

0.0000254478

0.0063403333

28.256

-0.0044788128

0.0063609188

28.293

0.0083214306

0.0063815043

28.318

0.0009670164

0.0064020898

28.356

0.0162356964

0.0064432608

28.389

0.002926497

0.0064638463

28.431

0.0118841226

0.0065050173

28.461

0.0013741812

0.0065461883

28.494

0.003562692

0.0065873593

28.527

0.001654107

0.0066491158

28.571

0.0032318706

0.0067314578

28.606

0.0070490406

0.0067932143

28.656

0.0095938206

0.0068755563

28.682

0.0040970958

0.0069784838

28.72

0.002926497

0.0070814113

28.754

0.0065909802

0.0071843387

28.8

0.0051150078

0.0073078517

28.836

0.0059038896

0.0074107792

28.876

0.0004835082

0.0075342922

28.912

0.0056748594

0.0076372197

28.947

0.002417541

0.0077607327

28.989

-0.0001526868

0.0078636602

29.044

0.0092375514

0.0079460022

29.08

0.0039189612

0.0080489297

29.122

0.0081941916

0.0081312716

29.154

-0.002035824

0.0082136136

29.197

0.0115278534

0.0082753701

29.244

0.0174062952

0.0083371266

29.279

0.0012978378

0.0083988831

29.326

0.0062856066

0.0084606396

29.374

0.0003308214

0.0085223961

29.412

0.0068963538

0.0085635671

29.457

0.001526868

0.0086253236

29.504

0.0063873978

0.0086870801

29.537

0.004453365

0.0087488366

29.583

0.0001526868

0.0088105931

29.621

0.0101282244

0.0088723496

29.674

0.0040207524

0.0089341061

29.724

0.0034100052

0.0089958626

29.771

0.0122658396

0.009057619

29.822

0.0106626282

0.009139961

29.858

0.0052676946

0.0092017175

29.909

-0.0027483624

0.009263474

29.954

0.013232856

0.009304645

29.994

0.0189840588

0.0093664015

30.038

0.0031046316

0.009428158

30.1

-0.0001017912

0.009469329

30.151

0.0196457016

0.0095105

30.19

0.0134109906

0.009551671

30.229

0.0040207524

0.009592842

30.295

0.0080924004

0.009634013

30.34

0.006489189

0.0096545985

30.392

0.0059293374

0.0096957695

30.435

0.007507101

0.009716355

30.488

0.0099755376

0.009757526

30.541

-0.0012214944

0.0097781115

30.586

0.0077361312

0.0098192825

30.647

-0.0054458292

0.0098604535

30.71

0.0105862848

0.0099016245

30.76

0.003562692

0.0099427955

30.816

0.0014250768

0.0099839665

30.862

-0.004962321

0.0100251374

30.904

0.0022394064

0.0100868939

30.956

-0.0002035824

0.0101280649

31.013

-0.0050386644

0.0101898214

31.075

-0.004580604

0.0102309924

31.12

0.0017304504

0.0102927489

31.175

0.005980233

0.0103545054

31.227

0.0025956756

0.0103956764

31.288

0.0100264332

0.0104574329

31.342

0.004453365

0.0104986039

31.388

-0.0043006782

0.0105603604

31.447

0.0048605298

0.0106015314

31.503

0.0253969044

0.0106427024

31.56

-0.0006870906

0.0107044589

31.616

0.001399629

0.0107456299

31.665

-0.0013487334

0.0107868009

31.73

0.02035824

0.0108279719

31.784

0.0066673236

0.0108691429

31.85

0.0007125384

0.0109103139

31.905

0.0002035824

0.0109514848

31.967

0.0101282244

0.0109926558

32.032

0.005725755

0.0110544123

32.089

0.0112224798

0.0110955833

32.151

0.0036390354

0.0111367543

32.21

0.0159303228

0.0111985108

32.268

0.0166428612

0.0112602673

32.33

0.00508956

0.0113014383

32.397

0.004453365

0.0113631948

32.459

0.0007379862

0.0114249513

32.521

0.0048605298

0.0114867078

32.59

0.0140471856

0.0115484643

32.64

0.008270535

0.0116102208

32.713

0.0021885108

0.0116719773

32.772

0.0135636774

0.0117337338

32.83

0.0013487334

0.0118160758

32.895

0.0139199466

0.0118778323

32.962

0.0042752304

0.0119395887

33.03

0.0008397774

0.0120219307

33.091

0.0100264332

0.0120836872

33.152

0.0028247058

0.0121454437

33.217

0.0077870268

0.0122277857

33.281

0.0150650976

0.0122895422

33.345

0.010433598

0.0123718842

33.404

0.0274581762

0.0124336407

33.469

0.0095683728

0.0125159827

33.535

0.0136909164

0.0125777392

33.605

0.018958611

0.0126394957

33.672

0.014123529

0.0127012522

33.743

0.0025956756

0.0127630087

33.812

0

0.0128041797

33.878

0.0048096342

0.0128659361

33.937

0.0196965972

0.0129071071

34.009

0.01017912

0.0129276926

34.078

0.0018322416

0.0129688636

34.158

0.002417541

0.0129894491

34.217

0.0046823952

0.0130100346

34.289

0.0121894962

0.0130306201

34.364

0.0084741174

0.0130512056

34.423

0.0067182192

0.0130512056

34.494

0.009924642

0.0130717911

34.563

0.003308214

0.0130923766

34.639

0.0066927714

0.0130923766

34.706

0.0205872702

0.0131129621

34.79

0.0029773926

0.0131335476

34.858

0.0258040692

0.0131747186

34.924

0.0076597878

0.0131953041

35.001

0.0050132166

0.0132364751

35.071

0.0101282244

0.0132776461

35.155

0.0031555272

0.0133188171

35.234

0.0013232856

0.0133599881

35.296

0.0077106834

0.0134217446

35.366

0.0151668888

0.0134629156

35.445

-0.0063873978

0.0135246721

35.515

0.004326126

0.0135864286

35.588

0.0149124108

0.0136275996

35.671

0.0176098776

0.0136893561

35.749

0.0026465712

0.0137305271

35.829

-0.0030282882

0.0137922835

35.89

0.0008652252

0.0138334545

35.98

0.0122912874

0.0138746255

36.06

0.0093393426

0.0139157965

36.125

0.0135891252

0.0139569675

36.199

0.0168464436

0.0139981385

36.281

0.0101282244

0.014018724

36.356

0.0009924642

0.014059895

36.44

0.0075325488

0.0140804805

36.506

0.0070999362

0.0141216515

36.579

-0.00381717

0.014142237

36.672

0.0031300794

0.0141628225

36.747

-0.0015523158

0.0142039935

36.819

0.011197032

0.014224579

36.908

0.006616428

0.01426575

36.979

0.0116805402

0.0142863355

37.066

0.0164392788

0.0143275065

37.15

0.0063365022

0.014348092

37.235

0.0271528026

0.014389263

37.317

0.0048096342

0.014430434

37.391

0.0205109268

0.014471605

37.48

0.0228521244

0.014512776

37.554

0.010815315

0.014553947

37.634

0.009924642

0.014595118

37.718

0.0172027128

0.014636289

37.804

0.0050386644

0.01467746

37.888

0.0138944988

0.014718631

37.967

0.010051881

0.0147392165

38.06

0.0118077792

0.0147803874

38.143

0.01145151

0.0148215584

38.219

0.0088303866

0.0148627294

38.312

0.004962321

0.0149039004

38.389

0.0194166714

0.0149244859

38.477

-0.0016032114

0.0149656569

38.568

0.0068454582

0.0150068279

38.66

0.0079906092

0.0150274134

38.737

0.0124948698

0.0150479989

38.816

0.0069726972

0.0150891699

38.908

0.0108662106

0.0151097554

39.005

0.0032573184

0.0151509264

39.075

0.0202564488

0.0151715119

39.175

0.0139199466

0.0152126829

39.255

0.0075325488

0.0152332684

39.34

0.0018322416

0.0152744394

39.427

0.0149124108

0.0152950249

39.521

0.0122403918

0.0153361959

39.605

0.0090085212

0.0153773669

39.692

0.0066418758

0.0154185379

39.8

0.021248913

0.0154597089

39.869

0.0134109906

0.0155008799

39.967

0.0123167352

0.0155420509

40.062

0.0135127818

0.0155832219

40.151

0.0052422468

0.0156243929

40.235

0.0190349544

0.0156655639

40.334

0.0039189612

0.0157067348

40.422

0.0102045678

0.0157479058

40.518

0.0107898672

0.0157684913

40.611

0.0137927076

0.0158096623

40.696

0.0177371166

0.0158302478

40.794

0.0143271114

0.0158508333

40.879

0.0114006144

0.0158714188

40.977

0.0154213668

0.0158920043

41.069

0.0097465074

0.0159125898

41.165

-0.0060820242

0.0159125898

41.26

0.0118841226

0.0159331753

41.358

0.0060056808

0.0159537608

41.443

0.0118077792

0.0159949318

41.539

0.0152432322

0.0160155173

41.633

0.004962321

0.0160361028

41.719

0.0050641122

0.0160772738

41.827

0.0295957914

0.0160978593

41.931

-0.0082959828

0.0161390303

42.032

0.0045297084

0.0161596158

42.118

0.0012978378

0.0162007868

42.212

0.0240227232

0.0162213723

42.324

0.0263639208

0.0162419578

42.404

0.000254478

0.0162625433

42.513

0.00381717

0.0162831288

42.609

0.0062601588

0.0163037143

42.718

-0.0006870906

0.0163242998

42.819

0.0171009216

0.0163242998

42.918

0.003562692

0.0163448853

43.01

0.0195184626

0.0163448853

43.103

0.0011960466

0.0163448853

43.226

0.012087705

0.0163654708

43.304

0.0128256912

0.0163654708

43.406

0.016159353

0.0163860563

43.506

0.007761579

0.0163860563

43.599

0.0079651614

0.0164066418

43.706

0.0215288388

0.0164272273

43.802

0.0235901106

0.0164478128

43.9

0.0079651614

0.0164683983

44.011

0.0117823314

0.0165095693

44.101

0.0065909802

0.0165301548

44.216

0.0103318068

0.0165507403

44.314

0.002290302

0.0165919113

44.413

-0.0027229146

0.0166330823

44.514

0.0058020984

0.0166536677

44.624

0.004835082

0.0166948387

44.724

0.0106371804

0.0167154242

44.833

0.0097465074

0.0167565952

44.935

0.0055476204

0.0167771807

45.033

0.0046823952

0.0168183517

45.142

0.0039698568

0.0168389372

45.253

0.0063365022

0.0168595227

45.362

0.010306359

0.0168801082

45.46

0.0055221726

0.0169006937

45.56

0.0070490406

0.0169212792

45.671

0.0135636774

0.0169418647

45.775

0.0108916584

0.0169624502

45.889

0.0065400846

0.0169624502

45.992

0.0186532374

0.0169830357

46.107

0.0061838154

0.0170036212

46.213

0.0214015998

0.0170242067

46.314

0.0084995652

0.0170653777

46.415

0.0079397136

0.0170859632

46.534

0.0123676308

0.0171065487

46.65

0.0105353892

0.0171271342

46.747

0.0113497188

0.0171683052

46.86

0.0072271752

0.0171888907

46.984

0.0177625644

0.0172300617

47.087

0.0077106834

0.0172506472

47.19

-0.0007125384

0.0172918182

47.292

0.007888818

0.0173124037

47.391

0.0022394064

0.0173535747

47.518

-0.000890673

0.0173741602

47.63

0.006616428

0.0173947457

47.739

0.0039698568

0.0174153312

47.851

0.0126475566

0.0174359167

47.966

-0.0005344038

0.0174565022

48.076

0.0000254478

0.0174770877

48.186

0.0087540432

0.0174976732

48.294

0.0041225436

0.0175182587

48.414

0.0053694858

0.0175388442

48.526

0.0070235928

0.0175594297

48.643

0.0066418758

0.0175800152

48.757

0.0088812822

0.0176211861

48.885

0.0088558344

0.0176417716

48.978

0.007379862

0.0176829426

49.094

0.0138944988

0.0177241136

49.209

0.0068200104

0.0177652846

49.322

0.0096956118

0.0178064556

49.431

0.008143296

0.0178682121

49.564

0.008270535

0.0179093831

49.664

0.0079397136

0.0179711396

49.78

0.0066418758

0.0180123106

49.9

0.0094920294

0.0180740671

50.02

0.0072271752

0.0181152381

50.13

0.0076088922

0.0181769946

50.251

0.0154977102

0.0182181656

50.367

0.0107898672

0.0182593366

50.49

0.011069793

0.0183005076

50.602

0.0088812822

0.0183416786

50.719

0.008652252

0.0183828496

50.834

0.0101027766

0.0184240206

50.962

0.0075579966

0.0184446061

51.073

0.0082959828

0.0184651916

51.191

0.009670164

0.0185063626

51.314

0.0071762796

0.0185269481

51.439

0.01526868

0.0185475335

51.547

0.0144543504

0.0185475335

51.668

0.0121894962

0.018568119

51.791

0.0141744246

0.0185887045

51.914

0.009161208

0.0185887045

52.035

0.0153450234

0.0185887045

52.152

0.0152432322

0.01860929

52.262

0.012342183

0.01860929

52.385

0.0071508318

0.01860929

52.519

0.0104081502

0.01860929

52.641

0.009670164

0.01860929

52.761

0.0081178482

0.01860929

52.881

0.0077361312

0.01860929

53.006

0.0125712132

0.01860929

53.123

0.0076088922

0.01860929

53.254

0.009033969

0.01860929

53.387

0.0100264332

0.0186298755

53.497

0.0078124746

0.0186298755

53.618

0.0132583038

0.018650461

53.754

0.0110443452

0.0186710465

53.866

0.013105617

0.018691632

53.986

0.0109171062

0.0187122175

54.121

0.0140726334

0.018732803

54.242

0.0030028404

0.018773974

54.366

0.0065400846

0.0187945595

54.48

0.0116550924

0.0188357305

54.628

0.0142253202

0.0188769015

54.746

0.0107644194

0.0189180725

54.876

0.0113497188

0.0189592435

55.001

0.0118586748

0.0190004145

55.131

0.0114260622

0.019062171

55.259

0.0087031476

0.019103342

55.389

0.011578749

0.019144513

55.512

0.0077361312

0.019185684

55.645

0.0079142658

0.0192474405

55.764

0.0157012926

0.0192886115

55.907

0.0075834444

0.0193297825

56.035

0.0072780708

0.0193709535

56.157

0.0122403918

0.0194121245

56.287

0.0086776998

0.0194532955

56.415

0.00890673

0.019473881

56.546

0.0088303866

0.0195150519

56.677

0.0130292736

0.0195356374

56.812

0.0073289664

0.0195562229

56.943

0.0119350182

0.0195562229

57.075

0.0121131528

0.0195768084

57.2

0.012851139

0.0195768084

57.315

0.013869051

0.0195768084

57.453

0.0068200104

0.0195768084

57.584

0.0161084574

0.0195768084

57.714

0.0143525592

0.0195768084

57.848

0.012087705

0.0195562229

57.98

0.0103318068

0.0195562229

58.116

0.0123930786

0.0195356374

58.241

0.0111461364

0.0195356374

58.374

0.0111461364

0.0195356374

58.52

0.0084995652

0.0195356374

58.641

0.008397774

0.0195356374

58.775

0.0144289026

0.0195562229

58.914

0.0119095704

0.0195562229

59.044

0.0046314996

0.0195768084

59.175

0.0080669526

0.0196179794

59.319

0.0126475566

0.0196385649

59.443

0.010560837

0.0196797359

59.596

0.0078633702

0.0197209069

59.709

0.0133855428

0.0197620779

59.852

0.0117568836

0.0198032489

60

0.0112733754

0.0198444199

60.13

0.0144289026

0.0199061764

60.266

0.0137927076

0.0199473474

60.402

0.0149633064

0.0199885184

60.55

0.0104844936

0.0200296894

60.678

0.0097719552

0.0200708604

60.817

0.0069472494

0.0201120314

60.947

0.0109680018

0.0201326169

61.094

0.0097210596

0.0201737879

61.232

0.0106371804

0.0201943734

61.365

0.0119095704

0.0201943734

61.511

0.0121386006

0.0202149589

61.651

0.0103572546

0.0202149589

61.78

0.0103827024

0.0202149589

61.921

0.0095174772

0.0202149589

62.054

0.0102045678

0.0202149589

62.198

0.0103572546

0.0202149589

62.339

0.0121640484

0.0202149589

62.48

0.0089830734

0.0201943734

62.61

0.0111206886

0.0201943734

62.757

0.0159812184

0.0201943734

62.913

0.0106626282

0.0201737879

63.043

0.011705988

0.0201737879

63.177

0.0075834444

0.0201532024

63.321

0.0107135238

0.0201532024

63.459

0.0123167352

0.0201532024

63.612

0.0167192046

0.0201326169

63.75

0.0098228508

0.0201326169

63.897

0.0112224798

0.0201326169

64.046

0.0144289026

0.0201532024

64.186

0.015650397

0.0201532024

64.321

0.0139199466

0.0201737879

64.458

0.0114769578

0.0201943734

64.612

0.0117314358

0.0202149589

64.754

0.0103572546

0.0202355444

64.905

0.011705988

0.0202561299

65.042

0.0118077792

0.0202973009

65.182

0.0138181554

0.0203178864

65.329

0.0154977102

0.0203590574

65.488

0.007888818

0.0203796429

65.63

0.0114769578

0.0204208139

65.76

0.0161084574

0.0204413994

65.921

0.0161848008

0.0204619848

66.063

0.0116296446

0.0205031558

66.207

0.0093902382

0.0205237413

66.364

0.0100264332

0.0205443268

66.508

0.0125712132

0.0205649123

66.644

0.0196457016

0.0205649123

66.797

0.0050132166

0.0205854978

66.961

0.012087705

0.0206060833

67.103

0.005980233

0.0206060833

67.249

0.00763434

0.0206266688

67.401

0.0055221726

0.0206266688

67.557

0.0183478638

0.0206472543

67.702

0.0245062314

0.0206472543

67.835

0.022012347

0.0206472543

67.988

0.0150650976

0.0206472543

68.138

0.0113497188

0.0206472543

68.285

0.0101027766

0.0206472543

68.429

0.015395919

0.0206266688

68.585

0.0135127818

0.0206266688

68.737

0.0111461364

0.0206060833

68.882

0.0052931424

0.0205854978

69.032

0.0118077792

0.0205649123

69.184

0.0116041968

0.0205443268

69.337

0.0103318068

0.0205237413

69.485

0.0144289026

0.0204825703

69.646

0.0001781346

0.0204413994

69.792

0.0105353892

0.0204208139

69.95

0.0088049388

0.0203796429

70.098

0.0120113616

0.0203384719

70.247

0.0149124108

0.0202973009

70.404

0.0131819604

0.0202561299

70.558

0.0147088284

0.0202355444

70.711

0.0146833806

0.0201943734

70.853

0.0117823314

0.0201737879

71.001

0.013487334

0.0201326169

71.166

0.0103827024

0.0201120314

71.323

0.01017912

0.0200914459

71.479

0.0038935134

0.0200914459

71.636

0.0186786852

0.0200708604

71.771

0.0160066662

0.0200708604

71.937

0.0068200104

0.0200914459

72.093

0.0116550924

0.0200914459

72.248

0.0188568198

0.0201120314

72.398

0.017431743

0.0201326169

72.553

0.0090848646

0.0201532024

72.705

0.020994435

0.0201943734

72.863

0.0116296446

0.0202149589

73.014

0.0124185264

0.0202561299

73.18

0.0126984522

0.0202767154

73.324

0.0088049388

0.0203178864

73.485

0.017177265

0.0203590574

73.637

0.0023920932

0.0203796429

73.8

0.0201801054

0.0204208139

73.955

0.0104844936

0.0204413994

74.115

0.0094411338

0.0204825703

74.27

0.0069472494

0.0205031558

74.438

0.0125203176

0.0205443268

74.587

0.0194166714

0.0205649123

74.749

0.0074307576

0.0206060833

74.91

0.007252623

0.0206266688

75.069

0.0189077154

0.0206472543

75.22

0.0154213668

0.0206884253

75.388

0.011833227

0.0207090108

75.534

0.0141998724

0.0207295963

75.699

0.0108662106

0.0207501818

75.847

0.017431743

0.0207707673

76.009

0.0142253202

0.0207707673

76.166

0.0177880122

0.0207913528

76.314

0.0106117326

0.0207913528

76.487

0.0144797982

0.0208119383

76.638

0.013741812

0.0208119383

76.81

0.0161339052

0.0208119383

76.966

0.016286592

0.0208119383

77.144

0.0070999362

0.0208119383

77.296

0.00508956

0.0208119383

77.45

0.0036390354

0.0208119383

77.61

-0.0023666454

0.0207913528

77.779

0.0081687438

0.0207913528

77.937

0.0286033272

0.0207707673

78.11

0.0240990666

0.0207707673

78.26

0.0144034548

0.0207707673

78.421

0.0122658396

0.0207501818

78.587

0.020739957

0.0207501818

78.742

0.0269492202

0.0207501818

78.906

-0.000381717

0.0207501818

79.081

0.0252442176

0.0207295963

79.243

0.0208926438

0.0207295963

79.405

0.0186532374

0.0207295963

79.569

0.021503391

0.0207295963

79.727

0.0063110544

0.0207501818

79.892

-0.0114006144

0.0207501818

80.055

-0.0035372442

0.0207501818

80.219

0.0220377948

0.0207707673

80.386

0.002926497

0.0207913528

80.557

0.0082959828

0.0207913528

80.729

0.0098991942

0.0208119383

80.878

0.0124185264

0.0208325238

81.06

-0.0052676946

0.0208531093

81.211

0.007125384

0.0208531093

81.382

0.0224195118

0.0208736948

81.549

-0.0002799258

0.0208942803

81.718

0.0312244506

0.0208942803

81.878

0.0089830734

0.0209148658

82.053

0.0059038896

0.0209148658

82.224

0.0113497188

0.0209148658

82.399

0.0164392788

0.0209148658

82.559

0.0142762158

0.0209148658

82.731

0.0074816532

0.0208942803

82.9

0.0129020346

0.0208942803

83.059

0.0155486058

0.0208942803

83.225

0.0149887542

0.0208736948

83.391

0.0140726334

0.0208736948

83.574

0.0119350182

0.0208736948

83.73

0.0099755376

0.0208531093

83.915

0.0168718914

0.0208531093

84.08

0.014250768

0.0208736948

84.245

0.0225467508

0.0208736948

84.415

0.0279416844

0.0208942803

84.586

0.0014250768

0.0208942803

84.757

0.0238700364

0.0209148658

84.922

0.019594806

0.0209354513

85.087

0.0009670164

0.0209766223

85.262

0.0140980812

0.0209972078

85.428

0.0093393426

0.0210177933

85.608

0.0106117326

0.0210589643

85.783

0.0102554634

0.0210795498

85.958

0.012214944

0.0211207208

86.124

0.0163374876

0.0211618918

86.297

0.0183733116

0.0211824773

86.467

0.0089321778

0.0212236483

86.625

0.0123167352

0.0212442338

86.797

0.017050026

0.0212648193

86.972

0.0170754738

0.0212854048

87.157

0.02417541

0.0213059903

87.312

0.0111206886

0.0213265758

87.497

0.0128002434

0.0213471613

87.659

0.0066673236

0.0213471613

87.844

0.0069218016

0.0213471613

88.017

0.0168973392

0.0213677468

88.206

0.0145815894

0.0213677468

88.364

0.0235137672

0.0213677468

88.546

0.0092629992

0.0213677468

88.729

0.010306359

0.0213677468

88.899

-0.0060311286

0.0213471613

89.078

0.0084995652

0.0213471613

89.244

0.0149378586

0.0213471613

89.428

0.0129274824

0.0213677468

89.593

0.0197729406

0.0213677468

89.775

0.009797403

0.0213677468

89.963

0.0140726334

0.0213677468

90.127

0.0155486058

0.0213883323

90.304

0.0231829458

0.0213883323

90.485

0.0107135238

0.0214089177

90.673

0.0139453944

0.0214089177

90.839

0.0189840588

0.0214295032

91.026

0.0158539794

0.0214295032

91.198

0.020612718

0.0214500887

91.382

0.0200274186

0.0214500887

91.565

0.0141744246

0.0214706742

91.739

0.0140217378

0.0214706742

91.93

0.0152177844

0.0214912597

92.093

0.0106117326

0.0214912597

92.273

0.0139708422

0.0215118452

92.449

0.0229793634

0.0215118452

92.626

0.0104081502

0.0215118452

92.818

0.0049114254

0.0215324307

93

0.020485479

0.0215324307

93.175

-0.0006870906

0.0215324307

93.365

0.0096956118

0.0215324307

93.543

0.0094920294

0.0215324307

93.73

0.0187550286

0.0215324307

93.916

0.0120622572

0.0215324307

94.091

0.0152177844

0.0215324307

94.27

-0.0062601588

0.0215530162

94.463

0.0097465074

0.0215530162

94.645

0.026083995

0.0215530162

94.83

0.0151668888

0.0215530162

95.008

0.011197032

0.0215530162

95.185

-0.0045042606

0.0215736017

95.36

-0.0095938206

0.0215736017

95.547

0.008652252

0.0215736017

95.739

0.0218342124

0.0215941872

95.922

0.004962321

0.0215941872

96.089

0.0148106196

0.0216147727

96.285

0.0120368094

0.0216147727

96.476

0.0148106196

0.0216353582

96.659

0.0140980812

0.0216353582

96.838

0.0148106196

0.0216559437

97.017

0.012978378

0.0216559437

97.21

0.0127239

0.0216559437

97.392

0.0125712132

0.0216559437

97.591

0.0151668888

0.0216559437

97.778

0.0166428612

0.0216559437

97.957

0.0116550924

0.0216559437

98.146

0.0180933858

0.0216559437

98.333

0.012214944

0.0216559437

98.527

0.017177265

0.0216559437

98.692

0.0119350182

0.0216559437

98.892

0.005852994

0.0216559437

99.084

0.0088303866

0.0216559437

99.268

0.012978378

0.0216559437

99.45

0.0123676308

0.0216559437

99.65

0.0076852356

0.0216765292

99.83

0.0175080864

0.0216765292

100.008

0.0153195756

0.0216971147

100.21

0.018958611

0.0216971147

100.398

0.0113751666

0.0217177002

100.585

0.0073544142

0.0217382857

100.79

0.013487334

0.0217588712

100.976

0.0163374876

0.0217794567

101.164

0.0128765868

0.0218000422

101.356

0.0132074082

0.0218206277

101.541

0.0153704712

0.0218412132

101.724

0.029901165

0.0218412132

101.922

0.0150396498

0.0218617987

102.1

0.0130292736

0.0218823842

102.303

0.0121386006

0.0218823842

102.501

0.027865341

0.0218823842

102.683

0.0132583038

0.0219029697

102.876

0.0052422468

0.0218823842

103.075

0.0164901744

0.0218823842

103.267

0.0121640484

0.0218823842

103.451

0.0191367456

0.0218617987

103.657

0.0233610804

0.0218617987

103.844

-0.0036644832

0.0218412132

104.037

0.0129529302

0.0218206277

104.226

0.0060565764

0.0218206277

104.431

0.0116041968

0.0218000422

104.62

0.0141998724

0.0217794567

104.822

0.016922787

0.0217588712

105.009

0.0137672598

0.0217382857

105.225

0.0139453944

0.0217177002

105.407

0.0100773288

0.0217177002

105.605

0.0181697292

0.0216971147

105.79

0.0188822676

0.0216971147

105.979

0.0143271114

0.0216765292

106.181

0.0114260622

0.0216765292

106.372

-0.0002035824

0.0216559437

106.576

0.0130801692

0.0216559437

106.768

0.0131819604

0.0216559437

106.973

0.0104844936

0.0216559437

107.162

0.0345835602

0.0216353582

107.352

-0.0072271752

0.0216353582

107.552

0.0011960466

0.0216353582

107.748

0.023539215

0.0216353582

107.953

0.0322423626

0.0216147727

108.146

0.0205618224

0.0216147727

108.344

0.0250406352

0.0216147727

108.54

-0.008525013

0.0215941872

108.742

0.0117823314

0.0215941872

108.938

-0.0048605298

0.0215736017

109.141

0.0019849284

0.0215530162

109.338

0.008652252

0.0215530162

109.545

0.0284760882

0.0215324307

109.732

0.0277126542

0.0215324307

109.934

-0.0040207524

0.0215118452

110.132

0.0273309372

0.0215118452

110.338

0.0213252564

0.0214912597

110.535

0.019340328

0.0214912597

110.739

-0.0140471856

0.0214912597

110.934

0.0108407628

0.0214912597

111.139

0.006870906

0.0214912597

111.333

0.0026974668

0.0214912597

111.539

-0.0004580604

0.0215118452

111.736

0.0006107472

0.0215118452

111.931

0.0040462002

0.0215324307

112.132

0.0140471856

0.0215324307

112.341

0.015395919

0.0215324307

112.545

0.0127239

0.0215530162

112.752

0.0108407628

0.0215530162

112.946

0.0095938206

0.0215736017

113.16

0.0002290302

0.0215736017

113.361

0.014632485

0.0215941872

113.56

0.013487334

0.0215941872

113.761

0.0175844298

0.0215941872

113.96

0.0117823314

0.0216147727

114.161

0.0135127818

0.0216147727

114.356

0.0068454582

0.0216147727

114.575

0.0109171062

0.0216353582

114.76

0.013232856

0.0216353582

114.98

0.0090848646

0.0216559437

115.175

0.0191876412

0.0216559437

115.384

0.0124185264

0.0216765292

115.585

0.010815315

0.0216765292

115.796

0.0094920294

0.0216971147

116.002

0.0237173496

0.0217177002

116.201

0.0077361312

0.0217382857

116.408

0.00890673

0.0217588712

116.618

0.0156249492

0.0217794567

116.813

0.0158539794

0.0218000422

117.032

0.0100773288

0.0218206277

117.238

0.0118586748

0.0218412132

117.452

0.017940699

0.0218823842

117.652

0.016795548

0.0219029697

117.867

0.0120622572

0.0219441407

118.083

0.012087705

0.0219853117

118.27

0.013360095

0.0220058972

118.479

0.0117823314

0.0220470682

118.693

0.0116805402

0.0220882392

118.899

0.0106626282

0.0221294102

119.106

0.0063873978

0.0221499957

119.308

0.0186023418

0.0221705812

119.52

0.0186786852

0.0222117522

119.724

0.0185259984

0.0222117522

119.935

0.0086268042

0.0222323377

120.142

0.0171518172

0.0222323377

120.349

0.0188568198

0.0222529232

120.559

0.0155995014

0.0222323377

120.755

0.0152432322

0.0222323377

120.971

0.0144034548

0.0222117522

121.184

0.0120368094

0.0221911667

121.393

0.0195693582

0.0221705812

121.603

0.0149378586

0.0221294102

121.813

0.0183733116

0.0221088247

122.03

0.0134618862

0.0220676537

122.246

0.0134618862

0.0220264827

122.45

0.0112733754

0.0219853117

122.649

0.0135636774

0.0219441407

122.861

0.0172027128

0.0219235552

123.064

0.0194421192

0.0218823842

123.283

0.0122658396

0.0218412132

123.506

0.0149887542

0.0218206277

123.71

0.0106371804

0.0217794567

123.93

0.01526868

0.0217588712

124.143

0.0109934496

0.0217382857

124.354

0.0056239638

0.0217177002

124.562

0.0153450234

0.0217177002

124.78

0.0102300156

0.0217177002

124.99

0.0137672598

0.0217177002

125.206

0.0162102486

0.0217177002

125.415

0.0123676308

0.0217382857

125.638

0.017304504

0.0217588712

125.842

0.0177116688

0.0217794567

126.052

0.0144034548

0.0218000422

126.263

0.0197983884

0.0218206277

126.482

0.0161084574

0.0218412132

126.69

0.0199256274

0.0218617987

126.912

0.0153195756

0.0218823842

127.125

0.012342183

0.0219029697

127.341

0.015650397

0.0219235552

127.561

0.0143525592

0.0219441407

127.773

0.018958611

0.0219441407

127.991

0.0073289664

0.0219647262

128.21899

0.0185514462

0.0219647262

128.43201

0.0090594168

0.0219853117

128.658

0.0186532374

0.0219853117

128.868

0.0190604022

0.0219853117

129.08099

0.0153195756

0.0219853117

129.287

0.0161084574

0.0219853117

129.508

0.0118841226

0.0219853117

129.724

0.019467567

0.0219853117

129.94901

0.0098482986

0.0219853117

130.161

0.014759724

0.0220058972

130.38

0.0172281606

0.0220058972

130.601

0.0099755376

0.0220058972

130.814

0.0091357602

0.0220264827

131.033

0.0214270476

0.0220264827

131.257

0.014378007

0.0220264827

131.46201

0.0118841226

0.0220470682

131.686

0.0114260622

0.0220676537

131.899

0.00890673

0.0220676537

132.13499

-0.0082959828

0.0220882392

132.343

-0.0013487334

0.0221088247

132.56599

0.0051404556

0.0221294102

132.78799

0.0192639846

0.0221499957

133.013

0.0112988232

0.0221705812

133.23199

0.0203073444

0.0221911667

133.44099

0.0128256912

0.0221911667

133.67599

0.0056239638

0.0222117522

133.88901

0.0141998724

0.0222323377

134.106

0.0079397136

0.0222529232

134.33

0.0147088284

0.0222529232

134.54201

0.0182460726

0.0222735087

134.77299

0.0132074082

0.0222735087

134.99001

0.0205618224

0.0222735087

135.20799

0.0157012926

0.0222735087

135.438

0.0150905454

0.0222940942

135.658

0.0142762158

0.0222940942

135.888

0.0109934496

0.0222940942

136.097

0.0173808474

0.0222940942

136.32899

0.0110952408

0.0222940942

136.552

0.018704133

0.0222735087

136.76601

0.0125457654

0.0222735087

137.00101

0.0161084574

0.0222735087

137.224

0.0169991304

0.0222735087

137.45

0.013869051

0.0222529232

137.658

0.0138944988

0.0222529232

137.892

0.0071508318

0.0222529232

138.11301

0.0160575618

0.0222529232

138.336

0.015777636

0.0222529232

138.567

0.0222922728

0.0222529232

138.783

0.0230048112

0.0222529232

139.017

0.0114769578

0.0222735087

139.229

0.0218087646

0.0222735087

139.465

0.0228775722

0.0222940942

139.69099

0.019594806

0.0222940942

139.90601

0.0111461364

0.0223146797

140.133

0.0124439742

0.0223352652

140.36301

0.0205109268

0.0223764361

140.578

-0.0025702278

0.0223970216

140.813

0.0224704074

0.0224176071

141.039

0.0067691148

0.0224381926

141.27699

0.01145151

0.0224793636

141.495

0.0112224798

0.0224999491

141.71899

0.0108407628

0.0225411201

141.939

0.0117823314

0.0225617056

142.18201

0.0080669526

0.0226028766

142.40401

0.0125712132

0.0226234621

142.633

0.0126984522

0.0226440476

142.85899

0.0145561416

0.0226852186

143.089

0.0132583038

0.0227058041

143.311

0.01526868

0.0227263896

143.537

0.0177625644

0.0227469751

143.77299

0.0158794272

0.0227675606

144.009

0.0171009216

0.0227881461

144.224

0.0127493478

0.0228087316

144.446

0.0136654686

0.0228293171

144.69299

0.0101027766

0.0228499026

144.91499

0.0134364384

0.0228499026

145.14301

0.012469422

0.0228704881

145.368

0.0120113616

0.0228704881

145.59399

0.0187295808

0.0228910736

145.83501

0.013741812

0.0228910736

146.062

0.0078124746

0.0229116591

146.283

0.0128765868

0.0229116591

146.519

0.0127239

0.0229116591

146.737

0.01017912

0.0229322446

146.963

0.0139199466

0.0229322446

147.189

0.0170245782

0.0229322446

147.438

0.0155995014

0.0229528301

147.66499

0.0146579328

0.0229734156

147.88699

0.0124185264

0.0229734156

148.123

0.0082196394

0.0229940011

148.35201

0.0190349544

0.0230145866

148.58

0.020485479

0.0230351721

148.808

0.0193912236

0.0230557576

149.034

0.0085759086

0.0230969286

149.276

0.0147851718

0.0231175141

149.505

0.003180975

0.0231380996

149.735

0.0222159294

0.0231792706

149.97099

0.0037917222

0.0231998561

150.19299

0.01526868

0.0232204416

150.429

0.0082450872

0.0232410271

150.67101

0.0234374238

0.0232821981

150.89101

0.0010433598

0.0233027835

151.13

0.0055476204

0.0233027835

151.37

0.0114260622

0.023323369

151.597

0.0249897396

0.0233439545

151.83299

0.023157498

0.02336454

152.064

0.0160575618

0.02336454

152.293

0.0207908526

0.0233851255

152.528

0.0148360674

0.0233851255

152.756

0.011705988

0.023405711

152.98199

0.0143016636

0.023405711

153.224

0.016795548

0.023405711

153.461

0.013360095

0.0234262965

153.689

0.0084486696

0.0234262965

153.914

0.0140471856

0.023446882

154.151

0.0047332908

0.023446882

154.394

0.0117314358

0.0234674675

154.62

0.0106371804

0.0234674675

154.85699

0.0137672598

0.023488053

155.086

0.0129274824

0.0235086385

155.32401

0.0121894962

0.0235086385

155.55099

0.0119859138

0.023529224

155.787

0.0146070372

0.023529224

156.02901

0.0150905454

0.0235498095

156.25

0.0125203176

0.0235498095

156.498

0.0158794272

0.023570395

156.722

0.0174826386

0.0235909805

156.957

0.0118841226

0.0235909805

157.187

0.0114006144

0.023611566

157.425

0.0095938206

0.0236321515

157.659

0.0133855428

0.023652737

157.899

0.0110188974

0.0236733225

158.133

0.013614573

0.023693908

158.35899

0.0099755376

0.0237144935

158.601

0.0095938206

0.0237556645

158.83

0.0094665816

0.0237968355

159.07001

0.0158030838

0.023817421

159.31599

0.0154977102

0.023858592

159.55099

0.0144289026

0.023899763

159.77901

0.0126730044

0.023940934

160.008

0.011324271

0.023982105

160.243

0.0114260622

0.024023276

160.479

0.0138181554

0.024064447

160.69901

0.0140217378

0.024105618

160.957

0.011069793

0.0241262035

161.185

0.0102554634

0.0241673745

161.42999

0.0141998724

0.02418796

161.668

0.015141441

0.024229131

161.899

0.0089830734

0.0242497165

162.133

0.0138181554

0.0242703019

162.366

0.0125203176

0.0242908874

162.605

0.0141489768

0.0243114729

162.838

0.0150650976

0.0243320584

163.07401

0.0049114254

0.0243526439

163.312

0.0177625644

0.0243526439

163.54401

0.014505246

0.0243732294

163.787

0.0094411338

0.0243938149

164.017

0.0147342762

0.0244144004

164.252

0.0078124746

0.0244144004

164.48399

0.0138944988

0.0244349859

164.731

0.0133855428

0.0244555714

164.96001

0.0104590458

0.0244761569

165.194

0.013869051

0.0244967424

165.44701

0.0000508956

0.0244967424

165.67799

0.0126221088

0.0245173279

165.91

0.0151923366

0.0245379134

166.14101

0.0144543504

0.0245584989

166.383

0.0077361312

0.0245790844

166.616

0.0083723262

0.0245996699

166.851

0.01781346

0.0246202554

167.09801

0.018195177

0.0246202554

167.34

0.0101027766

0.0246408409

167.576

0.0060820242

0.0246614264

167.817

0.0161339052

0.0246820119

168.039

0.0140217378

0.0247231829

168.28999

0.0122912874

0.0247437684

168.52901

0.0067945626

0.0247643539

168.776

0.0108407628

0.0247849394

168.991

0.015904875

0.0248055249

169.233

0.0030282882

0.0248466959

169.467

0.0188822676

0.0248672814

169.72

0.01017912

0.0248878669

169.952

0.0095683728

0.0249084524

170.19099

0.009542925

0.0249496234

170.42101

0.0137163642

0.0249702089

170.657

0.0123930786

0.0249907944

170.909

0.0103827024

0.0250113799

171.13901

0.0083723262

0.0250319654

171.381

0.0100264332

0.0250525509

171.616

0.0071508318

0.0250731364

171.854

0.0105862848

0.0250937219

172.10001

0.0094920294

0.0251143074

172.33501

0.011197032

0.0251348929

172.573

0.0109171062

0.0251554784

172.80701

0.0078633702

0.0251760639

173.045

0.0109171062

0.0251966494

173.289

0.0088558344

0.0252378203

173.526

0.0122912874

0.0252584058

173.767

0.0045042606

0.0252789913

174.015

0.0116296446

0.0252995768

174.25301

0.0086013564

0.0253407478

174.494

0.0108662106

0.0253613333

174.743

0.014123529

0.0254025043

174.965

0.0135636774

0.0254230898

175.205

0.0104081502

0.0254642608

175.45799

0.013232856

0.0255054318

175.705

0.0116805402

0.0255260173

175.938

0.0031300794

0.0255671883

176.192

0.0121894962

0.0255877738

176.42999

0.0165665178

0.0256289448

176.65601

0.016032114

0.0256495303

176.905

0.0185259984

0.0256907013

177.153

0.0054967248

0.0257112868

177.388

0.0106117326

0.0257318723

177.633

0.02290302

0.0257730433

177.871

0.014505246

0.0257936288

178.11501

0.0138181554

0.0258142143

178.349

0.004580604

0.0258553853

178.59599

0.0148106196

0.0258759708

178.839

0.0110188974

0.0258965563

179.082

0.0130547214

0.0259171418

179.314

0.0081941916

0.0259377273

179.56599

0.0085759086

0.0259788983

179.81

0.0149378586

0.0259994838

180.056

0.0135382296

0.0260200693

180.29201

0.0147851718

0.0260406548

180.545

0.0112733754

0.0260612403

180.78

0.0099500898

0.0260818258

181.02699

0.014632485

0.0261229968

181.263

0.0147088284

0.0261435823

181.51401

0.0073035186

0.0261641677

181.77

0.0064382934

0.0262053387

182.007

0.017686221

0.0262259242

182.255

0.0091357602

0.0262670952

182.49001

0.0101536722

0.0262876807

182.748

0.0135127818

0.0263288517

182.985

0.0134618862

0.0263700227

183.23

0.0150650976

0.0264111937

183.481

0.0136909164

0.0264523647

183.72301

0.011960466

0.0264935357

183.957

0.0130547214

0.0265552922

184.217

0.0084995652

0.0265964632

184.452

0.012978378

0.0266582197

184.703

0.0130038258

0.0266993907

184.94099

0.0055730682

0.0267405617

185.2

0.0075579966

0.0268023182

185.44

0.0033336618

0.0268434892

185.68401

0.0112224798

0.0269052457

185.938

0.0111461364

0.0269464167

186.172

0.0133346472

0.0269875877

186.42599

0.0016795548

0.0270287587

186.66499

0.017431743

0.0270699297

186.92

0.0108407628

0.0270905152

187.157

0.0020867196

0.0271316861

187.41901

0.0083214306

0.0271728571

187.653

0.0217069734

0.0271934426

187.90401

0.0167701002

0.0272140281

188.145

0.0101536722

0.0272551991

188.405

0.0204345834

0.0272757846

188.644

0.0086013564

0.0272963701

188.886

0.0126221088

0.0273375411

189.13901

0.007252623

0.0273581266

189.39

0.0193657758

0.0273787121

189.638

0.013487334

0.0274198831

189.88699

0.0151923366

0.0274404686

190.14

0.0096192684

0.0274816396

190.38901

0.0060820242

0.0275228106

190.633

0.012087705

0.0275639816

190.87601

0.006616428

0.0276051526

191.129

0.0057512028

0.0276463236

191.373

0.0046569474

0.0276874946

191.62601

0.0164392788

0.0277286656

191.87199

0.011578749

0.0277904221

192.127

0.018831372

0.0278521786

192.375

0.0159812184

0.0278933496

192.627

0.0162611442

0.0279551061

192.87601

0.0153195756

0.0280168626

193.116

0.0162356964

0.0280580335

193.377

0.0088558344

0.02811979

193.631

0.0110952408

0.0281815465

193.87199

0.0105099414

0.0282227175

194.117

0.0063365022

0.028284474

194.37601

0.010560837

0.028325645

194.61501

0.0140471856

0.0283874015

194.86301

0.0087540432

0.0284285725

195.116

0.007507101

0.028490329

195.36501

0.0088558344

0.0285315

195.618

0.0088049388

0.0285932565

195.87399

0.0100264332

0.0286344275

196.12601

0.0124948698

0.028696184

196.373

0.0073544142

0.028737355

196.62399

0.0146070372

0.0287991115

196.864

0.013741812

0.0288402825

197.119

0.0094920294

0.0288814535

197.37601

0.0144797982

0.0289226245

197.619

0.0049877688

0.0289637955

197.87

0.007379862

0.028984381

198.127

0.0009161208

0.0290049665

198.37

0.0155740536

0.0290255519

198.62601

0.0148106196

0.0290461374

198.882

0.0098482986

0.0290461374

199.13

0.0106117326

0.0290461374

199.38499

0.0156758448

0.0290461374

199.627

0.0091357602

0.0290255519

199.879

0.0091866558

0.0290255519

200.13901

0.0108407628

0.0290255519

200.386

0.0120622572

0.0290255519

200.63699

0.0106371804

0.0290461374

200.897

0.0116296446

0.0290667229

201.149

0.0096956118

0.0290873084

201.388

0.0112479276

0.0291284794

201.64101

0.0110443452

0.0291696504

201.901

0.0119095704

0.0292108214

202.153

0.0112733754

0.0292725779

202.40601

0.0061329198

0.0293343344

202.655

0.0141744246

0.0293960909

202.905

0.009033969

0.0294784329

203.157

0.0067945626

0.0295401894

203.412

0.013360095

0.0296225314

203.66701

0.0093138948

0.0296842879

203.924

0.0098737464

0.0297666299

204.17101

0.0127493478

0.0298283864

204.42799

0.0138181554

0.0298901429

204.683

0.0097465074

0.0299518994

204.93401

0.0141744246

0.0299930703

205.192

0.0080669526

0.0300548268

205.439

0.0084995652

0.0300959978

205.69299

0.0168209958

0.0301371688

205.936

0.018195177

0.0301783398

206.19901

0.0106626282

0.0302195108

206.45399

0.015523158

0.0302606818

206.70599

0.0100264332

0.0303018528

206.96001

0.0062601588

0.0303224383

207.216

0.012087705

0.0303636093

207.47301

0.0077361312

0.0304047803

207.72301

0.0145561416

0.0304459513

207.97301

0.0088812822

0.0304871223

208.228

0.011069793

0.0305282933

208.48199

0.0140980812

0.0305694643

208.742

0.0077870268

0.0306106353

208.99001

0.004453365

0.0306518063

209.259

0.0186532374

0.0306929773

209.509

0.015777636

0.0307341483

209.76199

0.0130292736

0.0307753193

210.01401

0.0111715842

0.0307959048

210.26801

0.0150650976

0.0308370758

210.515

0.0130801692

0.0308576613

210.769

0.0127747956

0.0308988323

211.024

0.0079906092

0.0309194177

211.278

0.0120368094

0.0309400032

211.539

0.0125712132

0.0309605887

211.793

0.0142253202

0.0309811742

212.045

0.0114006144

0.0309811742

212.30099

0.0103827024

0.0310017597

212.55299

0.0106371804

0.0310223452

212.80901

0.0123676308

0.0310223452

213.065

0.0123167352

0.0310429307

213.326

0.0117568836

0.0310429307

213.584

0.0091103124

0.0310635162

213.834

0.0129020346

0.0310841017

214.097

0.0098737464

0.0311046872

214.354

0.0132074082

0.0311252727

214.61301

0.0118841226

0.0311458582

214.86301

0.011578749

0.0311664437

215.12601

0.0169482348

0.0311870292

215.383

0.0119859138

0.0312076147

215.642

0.0102045678

0.0312487857

215.892

0.0081178482

0.0312693712

216.14301

0.012087705

0.0312899567

216.407

0.0151159932

0.0313311277

216.66499

0.014123529

0.0313517132

216.91499

0.0053949336

0.0313722987

217.17599

0.001781346

0.0314134697

217.42799

0.00763434

0.0314340552

217.686

0.0052422468

0.0314546407

217.948

0.0120368094

0.0314752262

218.207

0.0158539794

0.0314958117

218.453

0.0177371166

0.0315163972

218.72501

0.0155486058

0.0315369827

218.972

0.0108407628

0.0315575682

219.22501

0.0100264332

0.0315781537

219.493

0.0048096342

0.0316193247

219.745

0.0066927714

0.0316399102

220.00301

0.0121640484

0.0316604957

220.261

0.0122403918

0.0316810812

220.51601

0.0116041968

0.0317016667

220.778

0.0107644194

0.0317222522

221.037

0.0149887542

0.0317428377

221.29201

0.0055221726

0.0317634232

221.55499

0.012596661

0.0317840087

221.804

0.0164647266

0.0318045942

222.062

0.0131310648

0.0318251797

222.32201

0.0041479914

0.0318457652

222.577

0.0046060518

0.0318663506

222.838

0.0101282244

0.0318663506

223.09399

0.0082959828

0.0318869361

223.349

0.0069218016

0.0319075216

223.608

0.0195184626

0.0319281071

223.87399

0.0088812822

0.0319486926

224.133

0.005852994

0.0319692781

224.381

0.0122658396

0.0320104491

224.649

0.0091103124

0.0320310346

224.905

0.0020103762

0.0320722056

225.162

0.010306359

0.0321133766

225.41701

0.0120113616

0.0321545476

225.67101

0.0225721986

0.0321957186

225.938

0.013105617

0.0322368896

226.192

0.0108662106

0.0322986461

226.451

0.0126475566

0.0323398171

226.70599

0.006234711

0.0324015736

226.97099

0.023284737

0.0324427446

227.224

0.022139586

0.0325045011

227.487

0.0194930148

0.0325456721

227.748

0.0095174772

0.0326074286

228.005

0.0213507042

0.0326485996

228.26601

0.0073035186

0.0326897706

228.51801

0.0147088284

0.0327309416

228.791

0.006489189

0.0327721126

229.043

0.0103318068

0.0328132835

229.306

0.016159353

0.0328544545

229.561

0.011578749

0.0328956255

229.82201

0.0077106834

0.032916211

230.078

-0.0038426178

0.032957382

230.34

0.0078379224

0.0329779675

230.60699

0.0231320502

0.0330191385

230.85699

-0.0081941916

0.033039724

231.121

-0.0019340328

0.033080895

231.394

0.02035824

0.0331014805

231.63901

-0.003180975

0.033122066

231.90601

0.0144034548

0.033163237

232.172

0.0079906092

0.0331838225

232.42799

0.003435453

0.0332249935

232.68201

0.0127239

0.033245579

232.94299

0.0108407628

0.03328675

233.202

0.0118077792

0.0333073355

233.468

0.0042752304

0.0333485065

233.716

0.012087705

0.033369092

233.974

0.0040207524

0.033410263

234.239

0.0092629992

0.033451434

234.49899

0.006489189

0.0334720195

234.757

0.0068963538

0.0335131905

235.02299

0.0077106834

0.033533776

235.27699

0.006107472

0.0335543615

235.53799

0.0121640484

0.0335955325

235.804

0.011578749

0.033616118

236.063

0.005598516

0.0336367035

236.327

0.013360095

0.033657289

236.58099

0.0052676946

0.0336778745

236.83501

0.0076088922

0.03369846

237.112

-0.0006870906

0.03369846

237.375

-0.0023157498

0.0337190455

237.634

-0.003180975

0.033739631

237.89

0.0036390354

0.0337602165

238.155

0.0052676946

0.0337808019

238.405

0.0050641122

0.0337808019

238.67999

0.011833227

0.0338013874

238.929

0.0137672598

0.0338219729

239.19501

0.0003053736

0.0338425584

239.45599

-0.0032827662

0.0338425584

239.715

-0.0012214944

0.0338631439

239.987

0.0191367456

0.0338837294

240.24899

0.0112733754

0.0339043149

240.509

-0.0060056808

0.0339249004

240.76199

0.0072780708

0.0339249004

241.028

0.0205872702

0.0339454859

241.28799

0.0038426178

0.0339660714

241.55499

0.0070235928

0.0339660714

241.815

0.0046823952

0.0339866569

242.07201

0.009288447

0.0340072424

242.338

0.0098737464

0.0340278279

242.595

0.0093393426

0.0340484134

242.849

-0.0009161208

0.0340484134

243.131

0.002035824

0.0340689989

243.38901

0.020739957

0.0340895844

243.655

-0.0035117964

0.0341101699

243.908

0.02163063

0.0341513409

244.175

-0.0022648542

0.0341719264

244.43201

0.0142762158

0.0341925119

244.696

0.0212234652

0.0342336829

244.968

0.0085504608

0.0342542684

245.222

0.0037408266

0.0342954394

245.487

0.0073035186

0.0343366104

245.745

0.0053185902

0.0343571959

246.013

0.007125384

0.0343983669

246.263

0.0037153788

0.0344395379

246.54201

0.0067182192

0.0344807089

246.797

0.0090085212

0.0345218799

247.061

0.0079397136

0.0345630509

247.327

0.0033336618

0.0346042219

247.59

0.011197032

0.0346453929

247.856

0.0105353892

0.0346865639

248.12601

0.0106117326

0.0347277348

248.37601

0.0078379224

0.0347689058

248.64101

0.0168464436

0.0348100768

248.905

0.010051881

0.0348306623

249.159

0.0163374876

0.0348718333

249.435

0.007888818

0.0349130043

249.687

-0.0008397774

0.0349541753

249.95399

0.002163063

0.0349953463

250.22301

0.0168464436

0.0350365173

250.481

0.002926497

0.0350776883

250.745

0.0041734392

0.0351188593

251.004

0.0094665816

0.0351600303

251.271

0.0055221726

0.0352012013

251.52901

0.0044279172

0.0352217868

251.8

0.0108662106

0.0352629578

252.063

0.0111715842

0.0353041288

252.328

0.0085504608

0.0353452998

252.58299

0.007507101

0.0353864708

252.849

0.0091866558

0.0354070563

253.106

0.005344038

0.0354482273

253.38

0.0100009854

0.0354688128

253.64101

0.0085759086

0.0355099838

253.908

0.0116296446

0.0355511548

254.174

0.0048605298

0.0355717403

254.44

0.0102554634

0.0355923258

254.701

0.0078124746

0.0356334968

254.966

0.0040207524

0.0356540823

255.22701

0.0030791838

0.0356746677

255.49699

0.0083214306

0.0356952532

255.759

0.012342183

0.0357158387

256.01599

0.0060311286

0.0357364242

256.28799

0.0038935134

0.0357570097

256.548

0.010433598

0.0357775952

256.814

0.0056748594

0.0358187662

257.069

0.0129274824

0.0358393517

257.349

0.006870906

0.0358599372

257.61301

0.0061329198

0.0358805227

257.862

0.0087031476

0.0359011082

258.13501

0.0062856066

0.0359011082

258.405

0.0090848646

0.0359216937

258.664

0.0040970958

0.0359422792

258.922

0.011197032

0.0359628647

259.19199

0.0149124108

0.0359834502

259.46701

0.0052422468

0.0360040357

259.715

0.0107898672

0.0360040357

259.98999

0.0063365022

0.0360246212

260.24399

0.0064637412

0.0360246212

260.51999

0.0139708422

0.0360246212

260.78101

0.004580604

0.0360246212

261.05099

0.0103827024

0.0360246212

261.31

0.0083468784

0.0360040357

261.57999

-0.0006870906

0.0360040357

261.82901

0.009797403

0.0360040357

262.10699

0.0075834444

0.0359834502

262.37201

0.0124185264

0.0359834502

262.63501

0.0123676308

0.0359834502

262.897

0.0053694858

0.0360040357

263.16101

0.0095683728

0.0360040357

263.42599

0.0051659034

0.0360246212

263.68701

0.0074053098

0.0360657922

263.95999

0.0067182192

0.0360863777

264.229

0.0034100052

0.0361275487

264.48901

0.0035117964

0.0361893052

264.75

0.0087285954

0.0362304762

265.02802

0.0061329198

0.0362922327

265.28101

0.0122912874

0.0363334037

265.54901

0.007761579

0.0363951602

265.81299

0.0065146368

0.0364363312

266.07501

0.0083214306

0.0364775022

266.34399

0.0035372442

0.0365186732

266.60999

0.0044279172

0.0365598442

266.87399

0.012596661

0.0365804297

267.14499

0.0088812822

0.0366010152

267.40399

0.0107898672

0.0366216006

267.67401

0.0005598516

0.0366216006

267.94101

0.0136654686

0.0366216006

268.20499

0.0062601588

0.0366421861

268.47299

-0.002672019

0.0366421861

268.737

0.0022139586

0.0366421861

268.99399

0.0072017274

0.0366421861

269.26099

0.0066418758

0.0366421861

269.53299

0.0015777636

0.0366421861

269.793

0.0086776998

0.0366627716

270.06601

0.004580604

0.0366627716

270.33301

0.0039189612

0.0366833571

270.582

0.0107389716

0.0367039426

270.854

0.0045042606

0.0367039426

271.12299

0.0069218016

0.0367245281

271.38199

0.0065655324

0.0367451136

271.646

0.0115024056

0.0367656991

271.91299

0.0086013564

0.0368068701

272.173

0.0057512028

0.0368274556

272.43799

0.0038935134

0.0368480411

272.71201

0.0126475566

0.0368686266

272.979

0.0024684366

0.0369097976

273.23801

0.0105353892

0.0369303831

273.513

-0.0055730682

0.0369509686

273.772

0.004835082

0.0369921396

274.03601

0.0054203814

0.0370127251

274.302

0.008270535

0.0370333106

274.57001

0.0020103762

0.0370538961

274.83099

0.0094920294

0.0370950671

275.10199

0.0076852356

0.0371156526

275.358

0.0093902382

0.0371362381

275.62601

0.0087031476

0.0371568236

275.89301

0.0059038896

0.0371774091

276.16501

0.0030028404

0.0371979946

276.43301

0.0186786852

0.0372185801

276.698

0.006107472

0.0372185801

276.96399

0.0085759086

0.0372391656

277.22101

-0.0016286592

0.0372597511

277.487

0.0015777636

0.0372803366

277.76599

0.0049877688

0.0372803366

278.01901

0.0040970958

0.0373009221

278.284

0.0079397136

0.0373215076

278.54901

0.0023411976

0.0373420931

278.81201

0.0015777636

0.0373420931

279.08401

0.0000254478

0.0373626786

279.354

0.0055476204

0.0373626786

279.61301

0.0043006782

0.0373832641

279.87799

0.003435453

0.0374038496

280.14899

0.0036644832

0.0374038496

280.422

0.0056748594

0.0374244351

280.689

0.0037917222

0.0374450206

280.94901

0.0057512028

0.0374450206

281.216

0.0023920932

0.0374656061

281.483

0.0066927714

0.0374656061

281.74301

0.0165665178

0.0374861916

282.01099

0.0030028404

0.0374861916

282.27499

0.003053736

0.0375067771

282.53699

0.0005598516

0.0375067771

282.80801

0.0035372442

0.0375273626

283.07001

0.001781346

0.0375273626

283.332

0.006489189

0.0375479481

283.603

0.0032827662

0.0375479481

283.875

0.0093647904

0.0375479481

284.133

0.0077106834

0.0375685335

284.40399

0.0147851718

0.0375685335

284.66501

0.0025193322

0.037589119

284.92499

0.0120622572

0.037589119

285.19501

0.0072017274

0.037589119

285.46301

0.006743667

0.0376097045

285.728

0.0043770216

0.0376097045

285.98499

0.002799258

0.0376097045

286.26099

0.0099755376

0.0376097045

286.50299

0.0091357602

0.0376097045

286.772

0.0053185902

0.0376097045

287.04599

0.005598516

0.0376097045

287.30899

0.008525013

0.0376097045

287.57901

0.0051404556

0.0376097045

287.84799

0.0024938844

0.0376097045

288.12

0.0039189612

0.0376097045

288.38

0.0088812822

0.0376097045

288.646

0.0103318068

0.0376097045

288.922

0.0111715842

0.0376097045

289.17499

0.0086268042

0.0376097045

289.44601

0.0079397136

0.037589119

289.711

0.0040970958

0.037589119

289.98099

0.0050132166

0.037589119

290.241

0.0030282882

0.037589119

290.50299

0.009033969

0.037589119

290.76401

0.0119350182

0.037589119

291.03799

0.0086268042

0.0375685335

291.298

0.0075834444

0.0375685335

291.55801

0.0094665816

0.037589119

291.836

0.0085504608

0.037589119

292.103

0.0121386006

0.037589119

292.36499

0.0023157498

0.037589119

292.61801

0.005598516

0.037589119

292.901

0.0037917222

0.037589119

293.16101

0.0024429888

0.037589119

293.42801

0.0006107472

0.0376097045

293.702

-0.0012978378

0.0376097045

293.966

0.0024938844

0.0376097045

294.229

0.005216799

0.0376097045

294.48999

0.0029010492

0.0376097045

294.74799

0.0002799258

0.0376097045

295.02301

0.0053694858

0.0376097045

295.28201

0.0016795548

0.03763029

295.55899

0.0033591096

0.03763029

295.82999

0.0121894962

0.03763029

296.086

0.0018067938

0.03763029

296.35101

0.0062092632

0.03763029

296.616

0.0029519448

0.0376508755

296.888

0.0002290302

0.0376508755

297.146

0.0052931424

0.0376508755

297.409

0.0039189612

0.037671461

297.67899

0.0024429888

0.037671461

297.94501

0.0093647904

0.037671461

298.21201

0.0121894962

0.0376920465

298.491

0.008143296

0.0376920465

298.74899

0.0041225436

0.037712632

299.01001

0.0054203814

0.037712632

299.28101

0.0035372442

0.037712632

299.539

0.0053185902

0.0377332175

299.81799

0.0071508318

0.0377332175

300.07501

0.0033336618

0.0377332175

300.34299

0.0002035824

0.0377332175

300.60501

0.0009161208

0.0377332175

300.87399

0.0046314996

0.0377332175

301.14499

-0.0016795548

0.037753803

301.39801

0.005980233

0.037753803

301.672

0.0028247058

0.037753803

301.935

0.005471277

0.037753803

302.19299

0.0106626282

0.037753803

302.46701

0.0009161208

0.037753803

302.733

0.0025956756

0.037753803

302.99899

0.0047332908

0.037753803

303.26599

0.005216799

0.037753803

303.534

0.0081178482

0.037753803

303.789

0.0084741174

0.037753803

304.05801

0.0063873978

0.037753803

304.32401

0.0013741812

0.037753803

304.60101

0.0012978378

0.0377743885

304.85599

0.0069472494

0.0377743885

305.12701

0.0024429888

0.037794974

305.38901

0.0056239638

0.037794974

305.65799

0.0091103124

0.0378155595

305.92999

0.0090085212

0.037836145

306.19501

0.0088303866

0.0378567305

306.45801

-0.00127239

0.037877316

306.72601

0.00254478

0.0378979015

306.97501

0.0041479914

0.0379390725

307.258

0.0031046316

0.037959658

307.52301

0.007761579

0.0379802435

307.797

0.0080415048

0.038000829

308.05399

0.0030282882

0.038000829

308.32901

0.0083468784

0.0380214145

308.59201

0.0058020984

0.038042

308.849

-0.0028247058

0.038042

309.117

0.0009161208

0.038042

309.383

0.0051659034

0.038042

309.64899

0.0059293374

0.038042

309.91901

0.0031300794

0.038042

310.186

0.0006870906

0.038042

310.461

0.0014759724

0.038042

310.716

0.0053949336

0.0380214145

310.98199

0.0019849284

0.0380214145

311.23999

0.0068454582

0.0380214145

311.51401

-0.001399629

0.0380214145

311.78

0.006998145

0.0380214145

312.05301

0.0039953046

0.0380214145

312.323

0.006234711

0.0380214145

312.58301

0.0062601588

0.038042

312.854

0.005344038

0.038042

313.10999

0.0010942554

0.0380625855

313.383

0.0051659034

0.038083171

313.64999

0.0043515738

0.0381037565

313.91501

0.0037153788

0.038124342

314.17999

-0.002035824

0.0381449275

314.44901

0.0081178482

0.038165513

314.711

0.0062856066

0.0381860985

314.97501

0.0024429888

0.038206684

315.23901

0.0042243348

0.038247855

315.517

0.0021376152

0.0382684405

315.78101

-0.0009924642

0.038289026

316.047

0.0050386644

0.0383096115

316.31601

0.00254478

0.038330197

316.577

0.0112479276

0.0383507825

316.84299

0.0044788128

0.038371368

317.112

0.0046823952

0.038371368

317.384

0.00763434

0.0383919535

317.64499

0.0046569474

0.0383919535

317.91

0.0016795548

0.038412539

318.17599

0.001399629

0.0384331245

318.42999

0.0035117964

0.0384331245

318.711

0.002290302

0.03845371

318.979

0.0020612718

0.03845371

319.24799

0.0000254478

0.0384742955

319.517

0.0023411976

0.0384742955

319.77802

0.0044788128

0.038494881

320.05499

0.004707843

0.0385154665

320.31601

0.0092629992

0.0385360519

320.57901

0.0041479914

0.0385566374

320.84399

0.0039953046

0.0385772229

321.116

0.0024429888

0.0385978084

321.37799

0.003944409

0.0385978084

321.642

0.0042497826

0.0386183939

321.91599

0.002672019

0.0386389794

322.185

0.0002035824

0.0386389794

322.44101

0.0041734392

0.0386595649

322.71301

0.0056239638

0.0386595649

322.979

0.0093138948

0.0386595649

323.24399

0.0043515738

0.0386389794

323.509

0.0075579966

0.0386389794

323.78201

0.0038935134

0.0386389794

324.04501

0.0013741812

0.0386183939

324.31299

0.0041225436

0.0386183939

324.578

0.0003308214

0.0385978084

324.84

0.0050132166

0.0385978084

325.10999

0.0041734392

0.0385978084

325.367

0.004071648

0.0385978084

325.642

0.00254478

0.0385978084

325.901

0.0051913512

0.0385978084

326.17599

0.0006870906

0.0386183939

326.45001

0.0033845574

0.0386183939

326.703

0.0044788128

0.0386389794

326.97101

0.0060056808

0.0386595649

327.23199

0.001526868

0.0386595649

327.50699

0.0067691148

0.0386801504

327.77701

0.0015014202

0.0387007359

328.03601

0.0081178482

0.0387213214

328.30899

0.0063873978

0.0387419069

328.57101

-0.0000508956

0.0387624924

328.82901

-0.0006870906

0.0387830779

329.09201

0.0027738102

0.0388036634

329.371

0.0046060518

0.0388242489

329.63501

0.0062092632

0.0388448344

329.90799

0.001654107

0.0388448344

330.17401

0.0006107472

0.0388654199

330.43399

0.0039189612

0.0388860054

330.702

0.0029519448

0.0388860054

330.97

0.0022394064

0.0389065909

331.23599

0.0034100052

0.0389065909

331.49799

0.003944409

0.0389271764

331.76501

0.0039953046

0.0389271764

332.03101

0.0078124746

0.0389271764

332.29199

-0.0008652252

0.0389271764

332.57001

0.0076088922

0.0389477619

332.82999

0.0051913512

0.0389477619

333.095

0.0058020984

0.0389477619

333.367

0.004198887

0.0389683474

333.64099

0.0058275462

0.0389683474

333.90799

0.0078633702

0.0389889329

334.16901

0.0021885108

0.0390095184

334.41599

0.0015523158

0.0390095184

334.70599

0.002417541

0.0390301039

334.96899

0.003308214

0.0390712749

335.23599

0.0027229146

0.0390918604

335.50601

0.002672019

0.0391330314

335.76599

0.0060565764

0.0391742024

336.035

0.0046314996

0.0392153734

336.29501

0.0035117964

0.0392565444

336.56299

-0.000381717

0.0392977154

336.82599

0.003308214

0.0393594719

337.103

-0.000381717

0.0394006429

337.358

0.0018322416

0.0394623994

337.625

0.0044024694

0.0395035703

337.892

0.0043515738

0.0395447413

338.15601

0.0058784418

0.0395859123

338.414

0.0032573184

0.0396270833

338.69299

0.0155740536

0.0396682543

338.948

0.0036644832

0.0396888398

339.22

0.009415686

0.0397094253

339.48199

0.0066418758

0.0397300108

339.74799

0.0046314996

0.0397300108

340.01099

0.000127239

0.0397505963

340.28799

0.0049877688

0.0397505963

340.55701

0.0065146368

0.0397505963

340.81601

0.0111715842

0.0397505963

341.077

0.0064382934

0.0397505963

341.345

0.005216799

0.0397505963

341.61801

0.0041479914

0.0397505963

341.88

0.0047587386

0.0397505963

342.147

-0.0004326126

0.0397505963

342.409

0.0040207524

0.0397505963

342.67999

0.0009924642

0.0397505963

342.94501

0.0004071648

0.0397505963

343.20999

0.0068200104

0.0397505963

343.48499

0.0058784418

0.0397505963

343.742

0.0088049388

0.0397711818

344.00201

0.0071762796

0.0397711818

344.27399

0.0020612718

0.0397917673

344.54501

0.0046569474

0.0397917673

344.811

0.0076597878

0.0398123528

345.07501

0.0021121674

0.0398329383

345.33801

0

0.0398535238

345.599

0.0074816532

0.0398946948

345.866

0.0001526868

0.0399152803

346.13699

-0.0000763434

0.0399564513

346.41199

0.0050386644

0.0399770368

346.659

0.000508956

0.0400182078

346.93799

0.0031046316

0.0400593788

347.20901

0.0040207524

0.0401005498

347.46201

-0.0016795548

0.0401417208

347.73001

0.0023666454

0.0401828918

347.99701

0.004326126

0.0402240628

348.263

-0.0021121674

0.0402652338

348.54099

-0.0002799258

0.0403064048

348.79599

0.00508956

0.0403475758

349.056

0.0058784418

0.0404093323

349.32501

0.0074053098

0.0404505032

349.59299

0.006234711

0.0404916742

349.86401

0.004707843

0.0405328452

350.12299

0.0003053736

0.0405740162

350.38901

0.0019340328

0.0406151872

350.65701

0.004580604

0.0406563582

350.918

0.001654107

0.0406769437

351.19199

-0.001145151

0.0407181147

351.45801

-0.0027738102

0.0407387002

351.733

0.0067182192

0.0407592857

351.987

-0.0002035824

0.0408004567

352.26199

0.008525013

0.0408210422

352.526

0.0028247058

0.0408416277

352.80099

-0.0002035824

0.0408622132

353.05301

0.003562692

0.0408827987

353.32599

0.000508956

0.0409239697

353.58401

0.001017912

0.0409445552

353.86301

0.0000254478

0.0409857262

354.12201

-0.0018576894

0.0410268972

354.384

0.0055476204

0.0410680682

354.647

0.0047332908

0.0411092392

354.923

0.0046823952

0.0411504102

355.18201

0.004326126

0.0412121667

355.45801

0.0034100052

0.0412533377

355.72198

0.0073035186

0.0412945087

355.98599

0.0056494116

0.0413562652

356.254

-0.0022394064

0.0413974361

356.51401

0.0018576894

0.0414386071

356.78299

0.0073035186

0.0415003636

357.04501

0.0062856066

0.0415415346

357.314

0.00508956

0.0415827056

357.57501

-0.003562692

0.0416032911

357.841

0.0038680656

0.0416444621

358.10599

0.0005344038

0.0416650476

358.36801

-0.0015777636

0.0417062186

358.646

-0.0017304504

0.0417268041

358.909

-0.0026974668

0.0417473896

359.177

0.0033845574

0.0417885606

359.44199

0.00254478

0.0418091461

359.70401

0.0064382934

0.0418297316

359.974

0.0056494116

0.0418709026

360.233

0.004835082

0.0418914881

360.50601

0.0051150078

0.0419326591

360.76001

-0.0025956756

0.0419738301

361.03101

0.0030028404

0.0420150011

361.30399

-0.0004835082

0.0420767576

361.552

0.002163063

0.0421179286

361.82401

0.006107472

0.0421796851

362.09

-0.002290302

0.0422208561

362.362

-0.0014505246

0.0422826126

362.617

0.0031046316

0.0423237835

362.88901

0.0054967248

0.04238554

363.16101

0.0024684366

0.0424472965

363.42099

0.0009924642

0.0424884675

363.69601

0.0011705988

0.0425296385

363.95499

0.0058020984

0.042591395

364.216

0.0050386644

0.042632566

364.48901

-0.00127239

0.042673737

364.755

0.001654107

0.042714908

365.01599

0.005216799

0.042756079

365.297

0.0055476204

0.0427766645

365.54599

0.0076088922

0.0428178355

365.815

0.0065909802

0.0428590065

366.082

0.002926497

0.042879592

366.34698

0.002417541

0.042920763

366.612

-0.0029010492

0.0429413485

366.88101

0.0095174772

0.0429825195

367.142

0.0026465712

0.043003105

367.409

-0.004835082

0.0430236905

367.67401

0.0021121674

0.0430648615

367.936

0.0028756014

0.043085447

368.202

0.0006870906

0.0431060325

368.46701

0.0048096342

0.0431472035

368.746

0.0009924642

0.043167789

368.991

-0.0036390354

0.04320896

369.26501

0.00763434

0.0432295455

369.53101

0.003053736

0.0432707165

369.80301

-0.0006870906

0.0433118874

370.05701

0.012087705

0.0433530584

370.323

0.002672019

0.0433942294

370.591

-0.002417541

0.0434354004

370.85599

0.0018067938

0.0434971569

371.117

0.0004326126

0.0435383279

371.38

0.0180424902

0.0436000844

371.65399

-0.0062856066

0.0436412554

371.918

0.0015777636

0.0436824264

372.185

0.0083723262

0.0437441829

372.45001

0.0135382296

0.0437853539

372.71399

-0.000890673

0.0438265249

372.978

0.005980233

0.0438882814

373.245

-0.0022139586

0.0439294524

373.50699

0.004835082

0.0439500379

373.771

0.0034863486

0.0439912089

374.04099

-0.007761579

0.0440117944

374.31

0.0053949336

0.0440529654

374.577

0.003562692

0.0440735509

374.83701

-0.0004580604

0.0440941364

375.10001

0.0044024694

0.0441147219

375.36301

0.005980233

0.0441353074

375.62701

0.0107898672

0.0441353074

375.89301

0.0045042606

0.0441558929

376.14999

0.0074816532

0.0441764784

376.42099

-0.0021376152

0.0441970639

376.68701

-0.0021121674

0.0442176494

376.95401

0.0011197032

0.0442382348

377.22699

0.0040462002

0.0442794058

377.48199

0.0078124746

0.0442999913

377.75201

0.0131310648

0.0443411623

378.01401

0.0116041968

0.0443617478

378.28101

0.0057003072

0.0444029188

378.543

0.001017912

0.0444235043

378.81601

0.0012978378

0.0444646753

379.08099

-0.013487334

0.0444852608

379.33899

0.008652252

0.0445264318

379.608

0.0254223522

0.0445470173

379.867

0.0046569474

0.0445676028

380.134

0.0122912874

0.0446087738

380.39301

-0.01526868

0.0446293593

380.66501

-0.0077106834

0.0446499448

380.92899

-0.008397774

0.0446705303

381.19901

-0.0159303228

0.0447117013

381.461

0.0149633064

0.0447322868

381.72699

0.0018831372

0.0447734578

381.98401

-0.0088812822

0.0447940433

382.25

0.0072017274

0.0448352143

382.52301

-0.0111461364

0.0448763853

382.793

-0.00254478

0.0448969708

383.05099

-0.0104081502

0.0449381418

383.31299

0.0192385368

0.0449793128

383.57599

-0.0103318068

0.0450204838

383.845

-0.0100773288

0.0450616548

384.10999

0.014123529

0.0451028258

384.36401

0.0130292736

0.0451439968

384.64099

-0.0016286592

0.0451645823

384.90701

0.000636195

0.0452057532

385.17499

0.0062601588

0.0452469242

385.43799

0.0089321778

0.0452675097

385.70401

-0.0068454582

0.0453086807

385.96701

-0.007125384

0.0453292662

386.23401

-0.0151923366

0.0453704372

386.5

-0.0002799258

0.0453910227

386.76099

0.0180933858

0.0454116082

387.03699

-0.0144797982

0.0454527792

387.30301

0.0118586748

0.0454733647

387.561

0.007507101

0.0455145357

387.82901

0.0095174772

0.0455351212

388.08801

-0.0016286592

0.0455762922

388.35101

0.0049877688

0.0455968777

388.608

0.0046314996

0.0456174632

388.888

0.012978378

0.0456380487

389.155

-0.000508956

0.0456586342

389.41101

0.0046060518

0.0456792197

389.67499

0.0069218016

0.0456998052

389.94901

-0.0021376152

0.0457203907

390.20801

0.0074053098

0.0457203907

390.474

-0.0185259984

0.0457409762

390.737

0.0049877688

0.0457615617

391.009

0.0030028404

0.0457615617

391.26501

0.008143296

0.0457821472

391.53799

0.0073544142

0.0457821472

391.798

-0.0008143296

0.0458027327

392.06799

-0.0037408266

0.0458027327

392.327

0.0031555272

0.0458233182

392.591

0.0016795548

0.0458439037

392.84799

-0.0063365022

0.0458644892

393.11099

0.0037662744

0.0458850747

393.392

-0.0102300156

0.0459056602

393.64499

0.0046569474

0.0459262457

393.92099

0.0050132166

0.0459674167

394.18301

0.005980233

0.0460085877

394.44699

-0.0000254478

0.0460497587

394.71799

0.0013741812

0.0460909297

394.98001

-0.001781346

0.0461526861

395.23801

0.0021376152

0.0462144426

395.51599

0.0010433598

0.0462761991

395.772

0.002035824

0.0463585411

396.04501

0.005852994

0.0464408831

396.29501

-0.0000254478

0.0465232251

396.565

-0.0024684366

0.0466261526

396.83401

-0.0035881398

0.0467290801

397.09201

0.0045297084

0.0468320076

397.35999

0.0060056808

0.0469555206

397.62201

0.002163063

0.0470584481

397.89899

0.008779491

0.0471613755

398.16

-0.005852994

0.047264303

398.41199

-0.0016795548

0.0473672305

398.685

0.009288447

0.0474495725

398.944

0.0037408266

0.0475525

399.20599

-0.0010433598

0.047634842

399.47198

0.002290302

0.0476965985

399.73599

0.0014250768

0.047758355

400.00699

0.0065909802

0.0478201115

400.271

0.0061583676

0.0478612825

400.53

-0.0038680656

0.0479024535

400.79599

-0.0004580604

0.0479436245

401.065

-0.004453365

0.04796421

401.32501

-0.0044024694

0.0479847955

401.59299

0.0079142658

0.048005381

401.85901

-0.0029773926

0.0480259665

402.11801

-0.0010688076

0.0480259665

402.38901

0.0009415686

0.0480465519

402.651

-0.0068454582

0.0480465519

402.918

-0.0002290302

0.0480465519

403.18399

0.0059293374

0.0480465519

403.44501

0.0007888818

0.0480465519

403.71201

-0.0046314996

0.0480465519

403.987

-0.0036644832

0.0480671374

404.24399

-0.000763434

0.0480671374

404.508

-0.0015014202

0.0480671374

404.78299

0.0009415686

0.0480671374

405.047

0.0062092632

0.0480877229

405.298

0.0060311286

0.0480877229

405.56

-0.0032573184

0.0480877229

405.827

0.0003308214

0.0481083084

406.10001

0.002290302

0.0481083084

406.35901

0.0001526868

0.0481288939

406.62799

0.002672019

0.0481288939

406.901

0.0016795548

0.0481494794

407.14899

-0.0014250768

0.0481494794

407.41599

0.0014505246

0.0481700649

407.67599

0.0012469422

0.0481700649

407.94699

0.001908585

0.0481906504

408.21301

0.0043770216

0.0482112359

408.47501

0.0031046316

0.0482318214

408.74701

0.0052422468

0.0482524069

409.01001

0.0039953046

0.0482729924

409.26599

0.001399629

0.0483141634

409.53699

0.0016795548

0.0483553344

409.79901

0.0017558982

0.0484170909

410.06699

0.005216799

0.0484788474

410.32999

0.0033336618

0.0485611894

410.60001

-0.0012469422

0.0486229459

410.871

0.0061329198

0.0487052879

411.12399

0.0005344038

0.0487876299

411.392

0.0072271752

0.0488699719

411.65399

0.0021885108

0.0489523139

411.91699

0.0068454582

0.0490140703

412.177

0.008016057

0.0490964123

412.44299

0.0072017274

0.0491375833

412.711

0.0013741812

0.0491993398

412.98599

0.0054203814

0.0492199253

413.237

0.0042243348

0.0492405108

413.49799

0.0006616428

0.0492610963

413.763

0.0028501536

0.0492610963

414.03201

0.0106117326

0.0492610963

414.29599

0.004198887

0.0492405108

414.564

0.0023157498

0.0492199253

414.82101

0.0052422468

0.0491993398

415.08499

-0.0004580604

0.0491787543

415.36099

0.003562692

0.0491581688

415.62201

0.003180975

0.0491581688

415.89001

0.0057512028

0.0491581688

416.14899

0.0070490406

0.0491581688

416.41299

0.0068963538

0.0491581688

416.67401

0.0075325488

0.0491787543

416.94299

0.0054203814

0.0491993398

417.20801

0.0041479914

0.0492405108

417.47101

0.000127239

0.0492816818

417.73401

0.0013232856

0.0493228528

417.99701

0.0025702278

0.0493640238

418.26901

0.0023411976

0.0494051948

418.51901

0.0030028404

0.0494463658

418.802

0.0022394064

0.0494875368

419.05399

0.004453365

0.0495287078

419.32199

0.0009924642

0.0495698788

419.57999

0.0051659034

0.0496110498

419.85101

-0.0019594806

0.0496522208

420.11401

-0.0067182192

0.0496933918

420.38599

0.0004580604

0.0497345628

420.64001

0.0070235928

0.0497757338

420.90799

0.0178643556

0.0498169048

421.17099

0.0073544142

0.0498580758

421.439

-0.0060056808

0.0498992468

421.70499

0.0122912874

0.0499610032

421.96799

0.0084232218

0.0500227597

422.22

0.0096192684

0.0500845162

422.492

0.0030282882

0.0501462727

422.755

-0.0031046316

0.0502286147

423.01901

-0.0005598516

0.0502903712

423.28201

0.0089830734

0.0503521277

423.55301

0.0011197032

0.0504138842

423.815

-0.0015014202

0.0504756407

424.07999

-0.0050386644

0.0505373972

424.34

0.003435453

0.0505785682

424.60599

-0.0062856066

0.0506197392

424.87701

0.0137672598

0.0506609102

425.14001

0.0104081502

0.0507020812

425.41

-0.0055476204

0.0507226667

425.66599

-0.0074307576

0.0507432522

425.93799

0.0141489768

0.0507432522

426.19299

0.0002799258

0.0507638377

426.45099

0.0128256912

0.0507844232

426.72101

0.0062856066

0.0507844232

426.991

0.0043770216

0.0507844232

427.25601

-0.0119859138

0.0508050087

427.517

-0.0016032114

0.0508050087

427.77301

-0.0051659034

0.0508050087

428.043

-0.0031046316

0.0508050087

428.30301

0.0082450872

0.0508050087

428.57101

0.0147342762

0.0508050087

428.83801

-0.0106117326

0.0508050087

429.09698

-0.002290302

0.0507844232

429.358

-0.0017558982

0.0507638377

429.62201

0.0099755376

0.0507432522

429.884

0.0055476204

0.0507020812

430.15201

0.0008143296

0.0506814957

430.41299

-0.0053949336

0.0506403247

430.68301

-0.0062092632

0.0505991537

430.952

-0.0058275462

0.0505785682

431.21701

-0.0092375514

0.0505579827

431.479

0.0027483624

0.0505373972

431.74799

0.003435453

0.0505168117

432.009

-0.009033969

0.0505168117

432.26401

-0.0074562054

0.0505373972

432.52899

-0.003944409

0.0505579827

432.79501

0.0037153788

0.0505991537

433.06601

0.0029010492

0.0506403247

433.32901

0.0042243348

0.0506814957

433.59698

0.0073544142

0.0507432522

433.858

0.0037408266

0.0508050087

434.12601

-0.004580604

0.0508667652

434.383

0.0025193322

0.0509079361

434.647

0.0015014202

0.0509696926

434.90701

0.0036390354

0.0510108636

435.17001

-0.0000763434

0.0510520346

435.43799

0.0068200104

0.0510932056

435.698

-0.001781346

0.0511343766

435.97198

0.0009415686

0.0511549621

436.23199

0.0017050026

0.0511755476

436.495

0.0030791838

0.0511755476

436.75601

0.002799258

0.0511755476

437.03201

0.0029773926

0.0511961331

437.29001

0.0049368732

0.0511961331

437.547

-0.0026465712

0.0511961331

437.82199

0.0041479914

0.0511961331

438.082

-0.008143296

0.0511961331

438.34201

-0.0017050026

0.0511755476

438.60101

0.006234711

0.0511755476

438.86899

0.008397774

0.0511755476

439.13

0.0001781346

0.0511549621

439.397

0.0038680656

0.0511549621

439.668

0.006870906

0.0511549621

439.92499

0.0031300794

0.0511343766

440.19901

0.0046060518

0.0511343766

440.45499

0.004580604

0.0511137911

440.71899

-0.0011197032

0.0511137911

440.98599

-0.0051150078

0.0511137911

441.23901

0.0069472494

0.0510932056

441.517

0.0072017274

0.0510932056

441.76901

0.0100264332

0.0511137911

442.039

-0.0025956756

0.0511137911

442.29999

0.006998145

0.0511343766

442.56601

0.007507101

0.0511549621

442.832

0.0013741812

0.0511961331

443.08499

0.0027483624

0.0512167186

443.35699

0.0019594806

0.0512578896

443.62201

0.0032064228

0.0512990606

443.87799

0.0032064228

0.0513402316

444.14999

0.0038426178

0.0513814026

444.41699

0.0049368732

0.0514225736

444.67999

0.0025193322

0.0514843301

444.94199

0.0039698568

0.0515255011

445.20801

0.0019594806

0.0515666721

445.47601

-0.0036135876

0.0516078431

445.737

-0.0021885108

0.0516490141

446.01001

0.0006107472

0.0516695996

446.263

-0.0004835082

0.0516901851

446.52499

0.007761579

0.0517313561

446.798

0.0002799258

0.0517313561

447.05801

0.004962321

0.0517519416

447.31601

-0.0029519448

0.0517519416

447.57501

0.0039698568

0.0517725271

447.84299

0.0032827662

0.0517725271

448.10699

-0.0024429888

0.0517519416

448.375

0.0048096342

0.0517519416

448.63599

0.004071648

0.0517519416

448.91299

0.0071508318

0.0517313561

449.172

-0.0009161208

0.0517107706

449.436

0.0031046316

0.0516901851

449.70099

-0.0015523158

0.0516695996

449.96899

-0.0010688076

0.0516490141

450.23401

0.0023666454

0.0516284286

450.48901

-0.0031046316

0.0516078431

450.754

0.0007379862

0.0515872576

451.01599

-0.0040970958

0.0515460866

451.27301

0.0054203814

0.0515255011

451.54199

0.0057512028

0.0514843301

451.798

0.0000508956

0.0514637446

452.06799

0.0015014202

0.0514225736

452.33401

0.006870906

0.0513814026

452.59601

0.0031046316

0.0513608171

452.866

0.0069218016

0.0513196461

453.13101

-0.003944409

0.0512990606

453.38599

0.009542925

0.0512784751

453.64499

-0.0034863486

0.0512578896

453.91599

-0.0069472494

0.0512373041

454.18399

0.0026211234

0.0512167186

454.44299

0.000127239

0.0512167186

454.69699

-0.0005344038

0.0512167186

454.97

0.0017050026

0.0512167186

455.23801

0.001399629

0.0512167186

455.495

-0.0032318706

0.0512167186

455.76501

0.0003308214

0.0512373041

456.021

0.0028756014

0.0512373041

456.289

0.0027483624

0.0512578896

456.55801

0.0071762796

0.0512784751

456.81201

-0.0011197032

0.0512990606

457.082

0.005852994

0.0513402316

457.34601

-0.0014759724

0.0513608171

457.60699

-0.000127239

0.0514019881

457.87299

0.0001526868

0.0514225736

458.13699

0.0074053098

0.0514431591

458.397

0.010051881

0.0514843301

458.66699

0.0011197032

0.0515049156

458.93399

-0.0006616428

0.0515255011

459.19

0

0.0515460866

459.452

0.001017912

0.0515666721

459.72501

-0.0017050026

0.0515666721

459.98801

0.003562692

0.0515666721

460.241

-0.000636195

0.0515666721

460.509

-0.0000254478

0.0515460866

460.78

0.0037662744

0.0515255011

461.03799

0.0005344038

0.0515049156

461.31

-0.0013487334

0.0514843301

461.56299

0.0033591096

0.0514637446

461.83099

0.0006870906

0.0514431591

462.095

0.0050641122

0.0514019881

462.36499

-0.006234711

0.0513814026

462.62799

0.004326126

0.0513814026

462.888

0.0014250768

0.0513608171

463.15201

0.007252623

0.0513608171

463.41

-0.0003053736

0.0513402316

463.67099

-0.0075579966

0.0513608171

463.944

-0.004962321

0.0513608171

464.19699

0.0026211234

0.0513814026

464.452

0.0011960466

0.0514019881

464.72601

-0.0008652252

0.0514225736

464.99301

0.0001017912

0.0514431591

465.25201

-0.0028247058

0.0514843301

465.526

0.004326126

0.0515255011

465.78101

0.002926497

0.0515666721

466.04599

0.006616428

0.0516078431

466.30899

-0.001526868

0.0516490141

466.573

-0.0012214944

0.0517107706

466.832

-0.00127239

0.0517725271

467.09299

0.0033336618

0.0518342835

467.35901

-0.002417541

0.05189604

467.62701

-0.0022394064

0.0519577965

467.89001

0.000381717

0.0519989675

468.15201

-0.0007125384

0.052060724

468.42099

-0.0028247058

0.0521224805

468.677

0.0026974668

0.0521636515

468.93399

0.0033591096

0.0522048225

469.198

0.0026974668

0.052225408

469.45401

-0.0011960466

0.0522459935

469.729

0.0014759724

0.052266579

469.987

0.0095683728

0.052266579

470.25299

0.0030282882

0.052266579

470.513

0.0043006782

0.0522459935

470.772

-0.0025956756

0.052225408

471.03601

0.0010942554

0.0522048225

471.30801

0.0058784418

0.052184237

471.57501

0.002035824

0.0521636515

471.82901

-0.0095938206

0.0521224805

472.09799

0.0092375514

0.052101895

472.36401

0.0044788128

0.052060724

472.625

0.000636195

0.0520401385

472.888

0.0007125384

0.0519989675

473.14401

-0.0007125384

0.051978382

473.41699

-0.0001526868

0.0519577965

473.67999

0.0035117964

0.0519577965

473.94101

0.007507101

0.051937211

474.211

-0.0086013564

0.0519166255

474.47101

-0.004453365

0.05189604

474.742

-0.0046060518

0.0518754545

475.00201

0.0031555272

0.0518754545

475.26599

0.00127239

0.051854869

475.522

-0.0011197032

0.051854869

475.776

0.0056239638

0.0518342835

476.047

0.0054203814

0.0518342835

476.311

-0.0040970958

0.0518136981

476.57501

-0.0008397774

0.0518136981

476.84299

0.002035824

0.0518136981

477.09299

0.003435453

0.0517931126

477.354

-0.0033336618

0.0517931126

477.61301

-0.0000254478

0.0517931126

477.884

-0.0055476204

0.0517931126

478.15399

0.004071648

0.0517931126

478.41699

-0.0016286592

0.0517931126

478.68201

0.0069218016

0.0517725271

478.93701

-0.0042752304

0.0517725271

479.20801

-0.0090085212

0.0517725271

479.47699

-0.0002799258

0.0517519416

479.728

-0.01781346

0.0517313561

479.995

-0.0180933858

0.0517313561

480.26199

-0.0042497826

0.0517107706

480.52301

0.004835082

0.0516695996

480.784

0.0062856066

0.0516490141

481.04999

0.0022648542

0.0516284286

481.31201

-0.000508956

0.0516078431

481.56799

-0.0074307576

0.0515872576

481.823

0.0036644832

0.0515666721

482.09399

-0.002290302

0.0515460866

482.36401

0.0022394064

0.0515460866

482.62201

0.00890673

0.0515255011

482.88599

-0.0036390354

0.0515255011

483.15799

-0.0096447162

0.0515255011

483.41101

0.0117314358

0.0515255011

483.672

0.0109680018

0.0515255011

483.939

0.0026974668

0.0515460866

484.20499

-0.0040462002

0.0515460866

484.47

0.0007125384

0.0515666721

484.73001

-0.0075579966

0.0515872576

485

-0.0038680656

0.0516078431

485.255

0.0032064228

0.0516284286

485.51801

0.0027738102

0.0516490141

485.785

0.0076088922

0.0516695996

486.04501

-0.0007888818

0.0517107706

486.31201

-0.0072271752

0.0517313561

486.57101

0.0063873978

0.0517519416

486.84399

0.002290302

0.0517931126

487.091

0.0031555272

0.0518136981

487.36801

0.0029010492

0.0518342835

487.629

0.0060056808

0.051854869

487.897

0.000127239

0.0518754545

488.16

0.002799258

0.05189604

488.40701

0.0030028404

0.0519166255

488.681

0.0077106834

0.051937211

488.936

0.0087285954

0.051937211

489.19901

-0.0023157498

0.0519577965

489.46701

0.0028247058

0.051978382

489.72501

0.0031300794

0.051978382

490.00101

0.0022139586

0.0519989675

490.259

0.0035881398

0.0519989675

490.51599

0.0051659034

0.052019553

490.77701

-0.0001017912

0.0520401385

491.04401

-0.0017304504

0.052060724

491.31

0.0015523158

0.0520813095

491.57401

0.0031300794

0.052101895

491.82001

0.0045297084

0.0521224805

492.09201

0

0.052143066

492.36801

0.0102554634

0.0521636515

492.62601

0.0044279172

0.052184237

492.89099

-0.0011705988

0.0522048225

493.14999

0.0000508956

0.052225408

493.42099

0.001017912

0.052266579

493.67401

0.0035117964

0.0522871645

493.94101

0.001017912

0.0522871645

494.19901

0.0025702278

0.05230775

494.466

0.0021376152

0.05230775

494.72699

0.0101027766

0.05230775

494.98499

-0.0021376152

0.05230775

495.254

-0.0072780708

0.05230775

495.513

-0.0060056808

0.0522871645

495.78101

-0.0052676946

0.052266579

496.04099

0.0036390354

0.0522459935

496.30399

-0.008652252

0.0522048225

496.56201

0.0063110544

0.052184237

496.83401

0.0083214306

0.0521636515

497.09399

-0.0004326126

0.0521224805

497.34601

0.0006107472

0.0521224805

497.61099

0.0034863486

0.052101895

497.88199

-0.0002799258

0.052101895

498.14999

0.0004071648

0.052101895

498.40201

-0.0017050026

0.0521224805

498.664

0.0076852356

0.052143066

498.92401

-0.00127239

0.0521636515

499.194

0.003180975

0.0522048225

499.452

0.0157267404

0.052266579

499.72

0.0005852994

0.05230775

499.987

0.0002035824

0.0523695065

500.242

0.0013232856

0.052431263

500.50299

0.0017558982

0.0524930195

500.771

0.003689931

0.052554776

501.03299

0.0061583676

0.0526165325

501.293

0.0043006782

0.052678289

501.55899

0.0048605298

0.05271946

501.823

0.0007379862

0.052760631

502.08099

0.0019594806

0.0528018019

502.34201

0.0080669526

0.0528429729

502.608

0.0004326126

0.0528635584

502.87

-0.0013741812

0.0529047294

503.129

-0.0051150078

0.0529253149

503.39401

0.000254478

0.0529459004

503.664

0.0001526868

0.0529664859

503.927

-0.0020867196

0.0529664859

504.19501

0.0058020984

0.0529870714

504.461

-0.0017304504

0.0529870714

504.72299

-0.0009924642

0.0529870714

504.98199

-0.0006870906

0.0530076569

505.237

0.0003308214

0.0530076569

505.51001

0.0034100052

0.0530076569

505.76199

-0.0037662744

0.0530076569

506.02301

-0.0029773926

0.0530076569

506.28201

-0.0023411976

0.0530076569

506.54199

0.001908585

0.0530076569

506.81699

0.0022648542

0.0530076569

507.08401

0.000381717

0.0530076569

507.33899

-0.0026465712

0.0530076569

507.60199

0.0030282882

0.0530282424

507.86801

0.0017304504

0.0530282424

508.12601

0.0008143296

0.0530488279

508.383

0.0039698568

0.0530488279

508.647

0.0044788128

0.0530694134

508.90701

0.003562692

0.0530899989

509.17999

0.004453365

0.0531105844

509.44

-0.0002035824

0.0531311699

509.702

0.0030791838

0.0531517554

509.96701

0.0022648542

0.0531929264

510.23001

0.004326126

0.0532135119

510.48599

0.0043515738

0.0532340974

510.754

0.0032318706

0.0532546829

511.017

0.0030028404

0.0532752684

511.27899

-0.00127239

0.0532958539

511.54501

0.0012214944

0.0533164394

511.80301

0.0033845574

0.0533370249

512.065

0.0026974668

0.0533576104

512.32898

0.001654107

0.0533576104

512.59302

0.0066673236

0.0533576104

512.84698

-0.0018831372

0.0533781959

513.11102

0.0023920932

0.0533576104

513.36401

0.003180975

0.0533576104

513.63599

-0.000254478

0.0533576104

513.896

0.0043515738

0.0533576104

514.15802

0.0073544142

0.0533370249

514.41803

0.0001526868

0.0533370249

514.68701

0.0037153788

0.0533164394

514.94397

-0.0000508956

0.0533164394

515.20697

0.001781346

0.0532958539

515.47198

-0.000381717

0.0532958539

515.74103

0.0006870906

0.0532958539

516.00098

0.000381717

0.0532958539

516.26599

-0.0012978378

0.0532958539

516.51898

-0.0006616428

0.0533164394

516.77899

0.004962321

0.0533370249

517.04401

0.0017558982

0.0533576104

517.297

0.0024938844

0.0533781959

517.56897

0.0066673236

0.0534193669

517.828

0.0022139586

0.0534399524

518.08698

0.0015014202

0.0534811234

518.35199

0.0022394064

0.0535222944

518.61499

0.0007888818

0.0535634654

518.87799

0.0021885108

0.0536046364

519.14502

0.0017050026

0.0536252219

519.39099

0.0014505246

0.0536663929

519.65802

0.0013741812

0.0536869784

519.92499

-0.0022648542

0.0536869784

520.19702

-0.0052422468

0.0537075639

520.45599

0.0002799258

0.0537075639

520.70697

0.0038680656

0.0536869784

520.979

0.0025702278

0.0536869784

521.242

0.0008652252

0.0536663929

521.51001

0.0009415686

0.0536458074

521.76703

-0.0004580604

0.0536252219

522.03198

0.0003308214

0.0536046364

522.29401

0.0049368732

0.0536046364

522.54602

-0.0042243348

0.0535840509

522.82202

0.005852994

0.0535840509

523.08301

0.0023157498

0.0535840509

523.34198

0.000508956

0.0536046364

523.60901

0.0030791838

0.0536252219

523.85602

-0.0021885108

0.0536458074

524.12299

-0.0007125384

0.0536663929

524.38

0.0012214944

0.0536869784

524.65503

0.0028247058

0.0537281494

524.90503

-0.0023157498

0.0537487348

525.172

0.0040207524

0.0537899058

525.43903

-0.0029519448

0.0538104913

525.69598

-0.0011960466

0.0538516623

525.95599

0.0014759724

0.0538722478

526.21899

-0.0020103762

0.0538928333

526.48401

-0.0018067938

0.0539134188

526.75098

0.0026465712

0.0539340043

527.01398

0.0040207524

0.0539340043

527.27399

0.0028501536

0.0539545898

527.53699

0.0010688076

0.0539545898

527.79498

0.0003053736

0.0539751753

528.05402

-0.0022648542

0.0539751753

528.315

0.0014250768

0.0539957608

528.586

0.0059547852

0.0540163463

528.84601

0.000763434

0.0540163463

529.10797

-0.002926497

0.0540369318

529.37201

0.0033591096

0.0540575173

529.63397

-0.0012978378

0.0540986883

529.888

-0.000127239

0.0541192738

530.15002

0.0049368732

0.0541604448

530.414

0.0025702278

0.0542016158

530.67999

0.0007125384

0.0542633723

530.94501

-0.0008652252

0.0543045433

531.20599

0.0014250768

0.0543457143

531.466

-0.003308214

0.0543868853

531.73199

-0.0002799258

0.0544486418

531.992

-0.0006616428

0.0544898128

532.25897

0.0003562692

0.0545309838

532.52301

0.0001781346

0.0545721548

532.784

0.0006870906

0.0545927403

533.04498

0.0028247058

0.0546133258

533.30298

0.000127239

0.0546544968

533.57703

-0.0023157498

0.0546544968

533.83801

0.0007379862

0.0546750823

534.099

-0.002799258

0.0546750823

534.35602

-0.002799258

0.0546956677

534.61298

-0.000890673

0.0546956677

534.87598

0.0001017912

0.0546956677

535.14099

-0.0044788128

0.0546956677

535.40399

0.0019594806

0.0546750823

535.66998

0.0041734392

0.0546750823

535.93597

0.0022648542

0.0546750823

536.19299

0.002035824

0.0546750823

536.45502

0.0043770216

0.0546956677

536.72198

-0.0032827662

0.0546956677

536.97601

0.0004580604

0.0547162532

537.23901

0.0035117964

0.0547162532

537.50299

-0.0027738102

0.0547368387

537.76898

-0.0010433598

0.0547574242

538.02899

0.0038680656

0.0547985952

538.28699

0.00127239

0.0548191807

538.56799

0.000508956

0.0548603517

538.82202

0.0000508956

0.0549015227

539.078

-0.0001781346

0.0549426937

539.33301

-0.0016032114

0.0549838647

539.60303

-0.0002799258

0.0550250357

539.86401

-0.0041734392

0.0550662067

540.13

0.0023666454

0.0551073777

540.39697

0.002799258

0.0551485487

540.65802

0.004453365

0.0551897197

540.92499

-0.003053736

0.0552308907

541.17999

0.0017558982

0.0552720617

541.44397

0.00127239

0.0553132327

541.70203

0.0043006782

0.0553544037

541.96997

-0.0048096342

0.0553955747

542.22803

-0.0001017912

0.0554367457

542.49902

0.0002799258

0.0554573312

542.75098

-0.0005598516

0.0554779167

543.01801

0.0032573184

0.0555190877

543.27197

0.0060820242

0.0555396732

543.54303

-0.0004835082

0.0555396732

543.81799

0.0012469422

0.0555602587

544.06799

0.0013232856

0.0555602587

544.323

-0.0012978378

0.0555808442

544.58899

0.0066927714

0.0555808442

544.84998

0.006234711

0.0555808442

545.12201

0.003562692

0.0555808442

545.38397

0.0032827662

0.0556014297

545.64203

0.0060311286

0.0556014297

545.901

0.0059547852

0.0556220152

546.16901

0.0072017274

0.0556220152

546.42999

0.0087031476

0.0556426006

546.68799

0.003180975

0.0556631861

546.94598

0.0023157498

0.0556837716

547.21698

-0.0021121674

0.0557249426

547.47803

0.0012978378

0.0557455281

547.73102

0.0086013564

0.0557661136

548.00598

0.0060820242

0.0557866991

548.27502

-0.0001781346

0.0558072846

548.52802

-0.0002290302

0.0558278701

548.79797

-0.004962321

0.0558484556

549.04401

-0.0015014202

0.0558690411

549.31299

-0.000381717

0.0558690411

549.58398

0.0006107472

0.0558690411

549.84698

0.0009670164

0.0558690411

550.10699

0.0053949336

0.0558690411

550.36603

0.0029519448

0.0558690411

550.62598

0.0050386644

0.0558484556

550.896

0.0018831372

0.0558484556

551.15698

-0.0010433598

0.0558278701

551.41498

0.0016286592

0.0558072846

551.67902

-0.0017050026

0.0558072846

551.948

-0.000254478

0.0557866991

552.21301

0.0037153788

0.0557866991

552.48401

-0.0000508956

0.0557866991

552.73901

-0.0017558982

0.0557866991

553.00201

0.0031046316

0.0557866991

553.26703

0.001908585

0.0558072846

553.52502

0.0039698568

0.0558278701

553.78198

0.0033845574

0.0558690411

554.04999

0.0015014202

0.0559102121

554.31201

0.0021121674

0.0559513831

554.57397

0.0010942554

0.0559925541

554.841

0.0009924642

0.0560543106

555.10101

-0.0032573184

0.0561160671

555.37299

-0.0005852994

0.0561778236

555.633

0.0005344038

0.0562601656

555.89801

0.0008397774

0.0563219221

556.15399

0.0022394064

0.0563836786

556.414

-0.0007379862

0.0564454351

556.67999

-0.0047841864

0.0565071916

556.93799

-0.0015523158

0.0565689481

557.20099

0.0016286592

0.0566307045

557.46399

0.0051150078

0.0566718755

557.73602

-0.0035372442

0.0567130465

557.99103

0.000381717

0.0567542175

558.245

-0.0007125384

0.056774803

558.52002

-0.0047587386

0.056815974

558.78101

0.007379862

0.0568365595

559.04999

-0.0000508956

0.056857145

559.31299

0.0026974668

0.0568777305

559.57001

0.0029519448

0.056898316

559.84399

0.0039953046

0.056898316

560.09998

0.0065909802

0.0569189015

560.36298

0.0018576894

0.0569189015

560.62903

0.0014759724

0.056939487

560.89099

0.0048096342

0.056939487

561.15399

0.0042497826

0.056939487

561.41498

0.0007379862

0.056939487

561.68597

-0.0004071648

0.056939487

561.95203

0.0018831372

0.0569189015

562.20697

-0.0030282882

0.0569189015

562.46899

0.0001017912

0.0569189015

562.729

-0.0015777636

0.056898316

562.99103

0.0006616428

0.056898316

563.25702

0.0076088922

0.0568777305

563.534

-0.0018067938

0.0568777305

563.79303

-0.0018576894

0.056857145

564.05298

-0.0064637412

0.056857145

564.315

0.0024938844

0.056857145

564.578

-0.0022139586

0.056857145

564.84399

-0.0010433598

0.0568365595

565.10602

0.0025956756

0.0568365595

565.36603

-0.002163063

0.0568365595

565.63098

-0.000636195

0.0568365595

565.89203

-0.0046314996

0.056857145

566.15601

0.0061583676

0.056857145

566.41498

-0.0046823952

0.056857145

566.68298

0.0005598516

0.0568777305

566.94202

0.0038426178

0.0568777305

567.21198

-0.0023157498

0.056898316

567.47803

0.0004326126

0.0569189015

567.72998

-0.0030282882

0.056939487

567.99597

0.0020612718

0.0569600725

568.27002

-0.0014759724

0.056980658

568.547

-0.0058784418

0.0570012435

568.79102

0.0019849284

0.0570424145

569.05798

-0.0018067938

0.057063

569.32397

0.004707843

0.057104171

569.586

-0.000636195

0.057145342

569.84998

0.0039698568

0.0571659275

570.112

0.0029010492

0.0572070985

570.37402

0.0040462002

0.0572482695

570.63599

0.0038426178

0.0572894405

570.89301

-0.0011960466

0.0573306115

571.17102

0.0027738102

0.0573717825

571.42499

0.0062092632

0.0574129535

571.68903

0.001399629

0.057433539

571.948

-0.003435453

0.05747471

572.21301

-0.0044024694

0.057515881

572.46698

-0.0000508956

0.0575364665

572.73999

-0.0011705988

0.0575776374

573

-0.0004071648

0.0575982229

573.27002

-0.0004580604

0.0576188084

573.53198

-0.0032827662

0.0576393939

573.79303

0.0002799258

0.0576393939

574.065

-0.0011197032

0.0576599794

574.328

-0.002035824

0.0576599794

574.58398

0.0003562692

0.0576599794

574.84698

-0.0003308214

0.0576393939

575.11798

-0.0035881398

0.0576393939

575.37598

-0.0069218016

0.0576188084

575.64301

-0.0063110544

0.0576188084

575.90198

-0.0000763434

0.0575982229

576.17603

-0.0017304504

0.0575982229

576.43701

0.0060565764

0.0575776374

576.69897

-0.002799258

0.0575776374

576.96399

0.0039189612

0.0575776374

577.23102

-0.0088303866

0.0575982229

577.50098

0.006616428

0.0575982229

577.763

-0.0048605298

0.0576188084

578.02698

0.0025702278

0.0576393939

578.28101

0.002035824

0.0576805649

578.55298

0.003944409

0.0577011504

578.80701

-0.0029519448

0.0577423214

579.06702

-0.0000763434

0.0577834924

579.33698

-0.001908585

0.0578246634

579.59802

0.004326126

0.0578864199

579.85999

0.0027229146

0.0579275909

580.12799

-0.005471277

0.0579893474

580.39099

-0.0028756014

0.0580305184

580.64001

0.0047587386

0.0580716894

580.909

0.0028247058

0.0581128604

581.17798

-0.0048096342

0.0581540314

581.43701

-0.0009670164

0.0581746169

581.69897

-0.0028247058

0.0581952024

581.97198

-0.0063873978

0.0581952024

582.23499

0.0074816532

0.0581952024

582.49597

0.000127239

0.0581952024

582.75702

-0.0013232856

0.0581746169

583.01801

-0.0020867196

0.0581540314

583.28302

0.001399629

0.0581128604

583.54199

-0.001399629

0.0580716894

583.81

0.0005344038

0.0580511039

584.07397

-0.0010688076

0.0580099329

584.33502

-0.0005852994

0.0579687619

584.599

0.0006870906

0.0579481764

584.86798

-0.0022648542

0.0579275909

585.12701

-0.0051913512

0.0579070054

585.39502

-0.0002799258

0.0579070054

585.65802

-0.0022139586

0.0579070054

585.91498

0.0029773926

0.0579275909

586.17297

-0.0048859776

0.0579481764

586.43903

-0.0058275462

0.0579893474

586.70398

-0.0002290302

0.0580305184

586.96899

0.0049368732

0.0580922749

587.237

0.0016286592

0.0581540314

587.50299

0.0067945626

0.0582363734

587.758

-0.0034863486

0.0583187154

588.026

0.004962321

0.0583804719

588.28198

0.0043770216

0.0584628139

588.54498

0.0011197032

0.0585451558

588.81097

-0.0030282882

0.0586069123

589.06702

-0.0044279172

0.0586686688

589.33899

-0.0048605298

0.0587098398

589.59802

-0.0018067938

0.0587510108

589.85303

0.0006870906

0.0587715963

590.13

-0.0000763434

0.0587715963

590.39001

-0.0007888818

0.0587715963

590.646

0.004835082

0.0587304253

590.914

-0.0034609008

0.0587098398

591.17999

0.0002799258

0.0586480833

591.44098

-0.0034609008

0.0585863268

591.70203

0.0030282882

0.0585245703

591.96301

-0.0011705988

0.0584628139

592.23297

-0.0010688076

0.0584010574

592.5

0.0015523158

0.0583187154

592.76001

0.004326126

0.0582569589

593.026

0.0016286592

0.0582157879

593.28198

-0.0052422468

0.0581540314

593.54199

0.0036390354

0.0581334459

593.80603

-0.0033336618

0.0580922749

594.08002

-0.0003053736

0.0580716894

594.336

-0.0024684366

0.0580511039

594.59399

0.0012978378

0.0580511039

594.86298

0.0025702278

0.0580511039

595.12799

0.0031046316

0.0580716894

595.38098

-0.0000508956

0.0580922749

595.65802

0.0000508956

0.0581128604

595.914

-0.0007888818

0.0581334459

596.17603

-0.0002799258

0.0581540314

596.43799

0.0032573184

0.0581746169

596.70001

-0.0035881398

0.0581952024

596.97101

-0.0008397774

0.0582157879

597.23798

0.000636195

0.0582157879

597.49298

-0.0028756014

0.0582363734

597.758

0.0024684366

0.0582569589

598.013

-0.0031046316

0.0582569589

598.28198

0.0014250768

0.0582775444

598.54602

0.0001017912

0.0582775444

598.80402

-0.000381717

0.0582981299

599.06799

0.0062856066

0.0583187154

599.34302

-0.0000763434

0.0583393009

599.59698

0.0025956756

0.0583598864

599.86102

-0.0099755376

0.0584010574

600.125

0.0044279172

0.0584422284

600.38501

0.0022394064

0.0584833994

600.64203

0.001145151

0.0585451558

600.91302

0.0043515738

0.0586069123

601.17102

-0.0045042606

0.0586686688

601.42999

-0.0016032114

0.0587304253

601.69897

-0.0020867196

0.0588127673

601.966

0.0044279172

0.0588745238

602.22601

0.0008652252

0.0589362803

602.49799

-0.0011960466

0.0589980368

602.75299

-0.0018576894

0.0590392078

603.013

-0.0006870906

0.0590803788

603.27197

-0.0033591096

0.0591215498

603.54797

0.0021885108

0.0591421353

603.80603

-0.0010433598

0.0591627208

604.06598

0.00254478

0.0591627208

604.323

-0.0042497826

0.0591421353

604.58002

0.0022139586

0.0591421353

604.84998

0.0006107472

0.0591215498

605.11902

0.0083723262

0.0590803788

605.37598

0.0001526868

0.0590597933

605.63898

-0.0011197032

0.0590392078

605.90198

-0.0038680656

0.0589980368

606.17102

-0.0062092632

0.0589774513

606.43402

-0.0006107472

0.0589362803

606.69299

-0.005598516

0.0589156948

606.95203

0.0017304504

0.0588951093

607.224

0.0049877688

0.0588745238

607.48297

-0.0005598516

0.0588745238

607.74701

-0.0021376152

0.0588539383

608.01398

-0.0005344038

0.0588539383

608.26501

0.0004071648

0.0588539383

608.53198

-0.003180975

0.0588745238

608.79498

-0.0049114254

0.0588745238

609.05902

-0.0012214944

0.0588951093

609.31097

0.0033336618

0.0589156948

609.57599

-0.0051150078

0.0589362803

609.841

0.0047841864

0.0589568658

610.10303

-0.0015014202

0.0589980368

610.35797

-0.0004071648

0.0590186223

610.63

-0.0041225436

0.0590597933

610.888

0.002163063

0.0590803788

611.14801

0.0042497826

0.0591009643

611.414

-0.0047332908

0.0591421353

611.67999

0.0008652252

0.0591627208

611.93903

0.0050386644

0.0591833063

612.19202

0.0019594806

0.0592038918

612.46899

-0.00127239

0.0592038918

612.72601

-0.0009670164

0.0592244773

612.992

-0.0033591096

0.0592244773

613.24902

0.0022394064

0.0592450628

613.51599

0.0014505246

0.0592450628

613.77899

-0.0013487334

0.0592244773

614.03302

-0.0045297084

0.0592244773

614.289

-0.0032827662

0.0592038918

614.56299

-0.0014505246

0.0591833063

614.81799

0.009670164

0.0591627208

615.08301

0.0005344038

0.0591421353

615.33698

0.0028756014

0.0591009643

615.60498

0.0025193322

0.0590597933

615.87097

0.0038426178

0.0590186223

616.13898

0.0032827662

0.0589774513

616.38898

0.0009670164

0.0589362803

616.65601

-0.0033336618

0.0588951093

616.92102

0.0010688076

0.0588539383

617.17603

0.0054967248

0.0588127673

617.43799

-0.001654107

0.0587921818

617.69397

0.0013232856

0.0587715963

617.95398

0.0013487334

0.0587921818

618.229

-0.0027483624

0.0588127673

618.48297

0.0046823952

0.0588539383

618.74701

-0.0021376152

0.0588951093

619.01398

-0.0050386644

0.0589774513

619.27399

0.0006616428

0.0590597933

619.54401

-0.0011197032

0.0591421353

619.80701

-0.0023920932

0.0592450628

620.05798

-0.003562692

0.0593479903

620.33002

-0.0023920932

0.0594715032

620.59399

0.001145151

0.0595538452

620.849

0.0004071648

0.0596567727

621.11798

0.005216799

0.0597391147

621.383

0.007507101

0.0598214567

621.64203

-0.0044788128

0.0598832132

621.90198

0.0007379862

0.0599243842

622.15997

-0.0042497826

0.0599449697

622.42102

-0.0006107472

0.0599655552

622.68597

-0.0009670164

0.0599861407

622.94397

-0.001654107

0.0599861407

623.21002

-0.0010688076

0.0599861407

623.47302

0.0030791838

0.0599861407

623.73102

0.0027483624

0.0600067262

623.99298

0.0061583676

0.0600067262

624.25702

0.0044024694

0.0600067262

624.505

0.0012469422

0.0600273117

624.77802

-0.0044279172

0.0600478972

625.03998

-0.0013741812

0.0600684827

625.29901

0.0028501536

0.0601096537

625.56097

0.0025702278

0.0601302392

625.82898

0.003562692

0.0601714102

626.091

0.0002799258

0.0602125812

626.34998

-0.002417541

0.0602743377

626.60797

-0.0037917222

0.0603155087

626.86902

-0.0005598516

0.0603566797

627.13397

0.0008652252

0.0603978506

627.39899

0.0013487334

0.0604390216

627.65802

0.0002035824

0.0604596071

627.92902

-0.0009670164

0.0604801926

628.185

0.0011960466

0.0605007781

628.44098

0.006489189

0.0605213636

628.71399

0.003053736

0.0605007781

628.96997

0.006743667

0.0605007781

629.23297

0.0016795548

0.0604801926

629.48602

-0.0000763434

0.0604596071

629.74402

0.0010688076

0.0604184361

630.013

0.00127239

0.0603772652

630.27502

-0.002035824

0.0603360942

630.53497

-0.0019340328

0.0602743377

630.79303

-0.0018831372

0.0602331667

631.06

0.003435453

0.0601919957

631.32397

0.0019340328

0.0601508247

631.58698

-0.00636195

0.0601096537

631.849

0.0020867196

0.0600684827

632.10602

-0.0044279172

0.0600478972

632.37701

0.000254478

0.0600273117

632.633

-0.0004580604

0.0600273117

632.901

-0.0038426178

0.0600273117

633.15802

-0.0006870906

0.0600273117

633.41498

-0.0013232856

0.0600478972

633.68103

-0.0031046316

0.0600684827

633.94202

-0.0018831372

0.0600890682

634.20898

-0.0018322416

0.0601302392

634.46899

-0.000254478

0.0601714102

634.724

0.0029773926

0.0602125812

634.97998

-0.0102300156

0.0602537522

635.24701

-0.0030282882

0.0603155087

635.51202

-0.00381717

0.0603772652

635.771

-0.0036135876

0.0604390216

636.01898

-0.001399629

0.0605007781

636.29303

0.0007125384

0.0605625346

636.55798

-0.0023920932

0.0606448766

636.82001

0.0013487334

0.0607272186

637.08502

-0.001017912

0.0608095606

637.34497

0.0043515738

0.0608919026

637.60303

0.0053949336

0.0609948301

637.85901

0.0017050026

0.0610771721

638.12

-0.0043515738

0.0611800996

638.38501

-0.0036135876

0.0612624416

638.64301

-0.0028501536

0.0613447835

638.91302

-0.0009924642

0.0614271255

639.16199

-0.0034100052

0.0615094675

639.43103

0.001654107

0.061571224

639.68799

-0.0032318706

0.0616329805

639.94598

0.0011960466

0.0616741515

640.20801

0.002417541

0.0617153225

640.48102

-0.0014250768

0.061735908

640.73297

0.0038426178

0.0617564935

641.00598

0.0034863486

0.061777079

641.25598

0.0010433598

0.0617976645

641.51501

0.01017912

0.06181825

641.79401

0.001526868

0.0618388355

642.039

0.0007125384

0.0618388355

642.29901

0.0015777636

0.061859421

642.56403

0.0021885108

0.0618800065

642.83002

-0.004962321

0.061900592

643.08899

0.0025956756

0.0619211775

643.34802

-0.0080669526

0.061941763

643.60602

0.0020612718

0.0619623485

643.87201

0.0038680656

0.061982934

644.13202

-0.0038935134

0.061982934

644.40002

-0.0041225436

0.0620035195

644.66101

-0.00127239

0.0620035195

644.91901

0.003944409

0.061982934

645.18402

0.0024684366

0.061982934

645.45203

0.0003562692

0.061941763

645.70099

-0.0063365022

0.061900592

645.96301

-0.0042497826

0.061859421

646.22601

0.0017558982

0.0617976645

646.48499

0.0093647904

0.0617564935

646.74799

0.0069726972

0.061694737

647.021

0.009415686

0.0616329805

647.26801

0.0047332908

0.061571224

647.53998

0.0038680656

0.061530053

647.79199

-0.0045551562

0.061488882

648.05402

0.00381717

0.0614682965

648.31

-0.001017912

0.061447711

648.578

0.0042752304

0.061447711

648.82501

0.006489189

0.0614682965

649.09601

-0.0001017912

0.0615094675

649.35901

0.001908585

0.0615506385

649.62299

-0.0005344038

0.061612395

649.89001

-0.0007125384

0.0616741515

650.14697

0.0077361312

0.0617564935

650.40997

0.003562692

0.0618388355

650.672

-0.0027738102

0.0619211775

650.935

0.0046060518

0.061982934

651.20203

-0.0007379862

0.062065276

651.453

0.0056494116

0.062106447

651.71997

-0.0009415686

0.0621682035

651.974

0.0003308214

0.062188789

652.24298

-0.0019340328

0.06222996

652.50702

-0.0018067938

0.06222996

652.75598

-0.0034100052

0.06222996

653.02002

-0.0013232856

0.06222996

653.28198

0.0093902382

0.0622093745

653.547

0.0013232856

0.0621682035

653.81201

0.0066673236

0.062147618

654.07501

-0.004198887

0.062106447

654.33301

0.0063873978

0.0620858615

654.59399

0.0020867196

0.0620446905

654.85303

0.0003308214

0.062024105

655.11603

0.0020612718

0.061982934

655.37598

0.0084741174

0.061941763

655.63599

-0.0013741812

0.0619211775

655.896

0.0006107472

0.061900592

656.15698

-0.0004071648

0.0618800065

656.41101

0.0031046316

0.0618388355

656.67297

-0.0003308214

0.06181825

656.93597

-0.0046314996

0.0617976645

657.20203

0.002290302

0.061777079

657.46002

0.0024429888

0.0617564935

657.72302

-0.0024938844

0.0617153225

657.98499

0.0038680656

0.061694737

658.24402

-0.0010942554

0.0616741515

658.51099

-0.0024684366

0.061653566

658.77002

0.0034609008

0.0616329805

659.03601

-0.0040970958

0.061612395

659.28601

-0.000127239

0.0615918095

659.55402

-0.0046314996

0.061571224

659.82501

-0.0001781346

0.0615506385

660.08502

-0.0105862848

0.0615506385

660.33899

-0.008143296

0.061530053

660.604

0.0027483624

0.061530053

660.85797

-0.000127239

0.061530053

661.133

0.0019340328

0.0615506385

661.39001

0.0042243348

0.061571224

661.65198

-0.0004580604

0.0615918095

661.90399

0.005598516

0.0616329805

662.16901

-0.005598516

0.061694737

662.43201

0.008525013

0.061777079

662.68201

0.0027738102

0.061859421

662.95398

0.0011960466

0.0619623485

663.21002

0.0027483624

0.0620858615

663.47198

0.0023157498

0.0622093745

663.73297

0.00636195

0.0623534729

663.99902

0.0066673236

0.0624975714

664.25702

0.0071762796

0.0626416699

664.51202

0.00508956

0.0628063539

664.77899

-0.0018067938

0.0629504524

665.03699

-0.0009924642

0.0630739654

665.29199

-0.0000254478

0.0631974784

665.56097

0.0044788128

0.0633209913

665.82898

-0.0033845574

0.0634033333

666.08002

-0.0044788128

0.0634856753

666.34399

-0.000254478

0.0635268463

666.60199

-0.000636195

0.0635474318

666.86401

0.000763434

0.0635474318

667.13397

-0.0016795548

0.0635268463

667.39203

0.000254478

0.0634856753

667.64899

0.0002290302

0.0634445043

667.92102

-0.001399629

0.0633621623

668.17999

0.0034609008

0.0632798203

668.43597

0.0015777636

0.0631974784

668.70502

-0.0007379862

0.0631151364

668.96503

0.000763434

0.0630327944

669.22198

-0.004453365

0.0629504524

669.492

0.0028756014

0.0628681104

669.74298

-0.00254478

0.0628063539

670.01202

0.0011960466

0.0627445974

670.26898

0.0019594806

0.0627240119

670.53003

0.0001017912

0.0626828409

670.78802

0.006234711

0.0626828409

671.05298

0.0050641122

0.0626828409

671.30902

-0.003562692

0.0626828409

671.565

-0.0036390354

0.0627034264

671.83002

0.0019594806

0.0627240119

672.08899

-0.0001017912

0.0627240119

672.35101

0.0006616428

0.0627445974

672.61401

0.003689931

0.0627651829

672.87201

-0.000254478

0.0627651829

673.13501

-0.0007379862

0.0627651829

673.40601

0.0016795548

0.0627445974

673.66699

-0.0030028404

0.0627240119

673.92999

0.0021376152

0.0627034264

674.18799

0.0049877688

0.0626622554

674.44702

0.0002799258

0.0626416699

674.70697

0.0016286592

0.0626004989

674.97198

0.0026211234

0.0625593279

675.23102

0.0045042606

0.0625387424

675.48297

-0.0004326126

0.0625181569

675.74402

0.0006616428

0.0624975714

676.00299

-0.0017050026

0.0624975714

676.26703

0.001526868

0.0624975714

676.53101

0.000508956

0.0624975714

676.78699

0.0003308214

0.0625181569

677.05603

-0.0017304504

0.0625387424

677.30902

0.000636195

0.0625593279

677.57703

0.0043515738

0.0625799134

677.83801

0.00381717

0.0626210844

678.099

0.0016286592

0.0626622554

678.35901

-0.0000763434

0.0626828409

678.62201

-0.0020867196

0.0627240119

678.88599

-0.0033336618

0.0627651829

679.14398

0.0019340328

0.0627857684

679.409

0.0056748594

0.0628269394

679.659

0.0033845574

0.0628475249

679.92603

0.0053694858

0.0628681104

680.18597

0.0039189612

0.0628886959

680.45099

-0.0022394064

0.0629092814

680.70502

0.0010942554

0.0629298669

680.96899

0.0011705988

0.0629298669

681.229

-0.004962321

0.0629298669

681.49402

0.0001781346

0.0629298669

681.74799

0.0009161208

0.0629298669

682.01801

-0.001654107

0.0629092814

682.27502

-0.0044788128

0.0629092814

682.53601

0.0013741812

0.0628886959

682.79999

0.000381717

0.0628681104

683.05603

0

0.0628475249

683.31897

0.0015523158

0.0628063539

683.58197

-0.0002290302

0.0627857684

683.84198

0.0000254478

0.0627651829

684.10199

-0.003435453

0.0627240119

684.36102

-0.0005852994

0.0627034264

684.62299

0.0014250768

0.0626828409

684.88098

-0.0055221726

0.0626622554

685.14001

-0.0060820242

0.0626622554

685.39697

0.0040970958

0.0626416699

685.65997

0.0011197032

0.0626416699

685.91998

-0.0014759724

0.0626622554

686.18597

-0.0004071648

0.0626828409

686.44897

0.0013741812

0.0627034264

686.71301

0.0023666454

0.0627445974

686.97699

-0.003689931

0.0628063539

687.24103

0.0023920932

0.0628681104

687.505

0.0038935134

0.0629504524

687.76398

-0.0037153788

0.0630327944

688.01398

-0.0030791838

0.0631357219

688.27802

0.0025193322

0.0632386494

688.539

-0.0009924642

0.0633415768

688.79401

0.0018067938

0.0634239188

689.05798

-0.0026465712

0.0635268463

689.32202

0.0007379862

0.0635886028

689.578

0.0018576894

0.0636503593

689.841

-0.0018322416

0.0637121158

690.10797

-0.003180975

0.0637327013

690.36298

-0.0048096342

0.0637532868

690.625

0.000763434

0.0637327013

690.87903

0.0000508956

0.0637121158

691.14899

-0.0034609008

0.0636503593

691.41101

-0.0043515738

0.0635886028

691.677

-0.0023411976

0.0635268463

691.935

-0.0036644832

0.0634445043

692.19702

-0.0003308214

0.0633621623

692.44897

0.0003053736

0.0632798203

692.716

0.0043515738

0.0631974784

692.98199

0.0031046316

0.0631357219

693.24103

0.0004835082

0.0630739654

693.49799

0.0029010492

0.0630327944

693.76099

0.0027229146

0.0630122089

694.021

0.0021376152

0.0629916234

694.27301

0.0035372442

0.0630122089

694.534

0.0081178482

0.0630327944

694.79999

0.0013741812

0.0630533799

695.06

0.0029519448

0.0631151364

695.32397

-0.0024684366

0.0631563074

695.58801

0.0016032114

0.0631974784

695.85901

0.0045551562

0.0632592348

696.11499

-0.000381717

0.0633004058

696.36603

-0.004198887

0.0633621623

696.62903

0.0011197032

0.0634033333

696.89001

0.0037917222

0.0634239188

697.15399

0.0044279172

0.0634445043

697.41101

0.0032064228

0.0634650898

697.67499

-0.0021376152

0.0634856753

697.94098

0.0039189612

0.0634856753

698.20001

0.0008652252

0.0635062608

698.45697

-0.0005598516

0.0635062608

698.716

-0.0019594806

0.0635062608

698.97699

0.0013487334

0.0635268463

699.24298

-0.0023666454

0.0635474318

699.49298

0.0006616428

0.0635680173

699.76398

-0.0073035186

0.0635886028

700.01703

0.0058784418

0.0636091883

700.27698

-0.0038426178

0.0636503593

700.54401

0.0009670164

0.0636709448

700.80902

0.0021121674

0.0637121158

701.07202

0.0018322416

0.0637327013

701.33002

-0.0007888818

0.0637738723

701.591

0.0007379862

0.0637944578

701.854

-0.0021121674

0.0638150433

702.11102

0.0012978378

0.0638150433

702.37598

0.0025956756

0.0638356288

702.64001

-0.0075325488

0.0638356288

702.89697

0.0014250768

0.0638356288

703.14801

-0.0021376152

0.0638150433

703.41498

0.006743667

0.0637944578

703.67297

0.000636195

0.0637944578

703.935

0.0017050026

0.0637738723

704.19501

-0.000254478

0.0637738723

704.453

0.000254478

0.0637738723

704.71301

-0.0044279172

0.0637738723

704.97198

-0.002799258

0.0637738723

705.23901

0.0041225436

0.0637944578

705.50598

-0.0052422468

0.0638150433

705.76599

-0.0001781346

0.0638562143

706.026

-0.000508956

0.0638973853

706.28198

-0.0036135876

0.0639385563

706.55298

-0.0028501536

0.0640003128

706.81598

-0.0008652252

0.0640414838

707.07501

0.0058275462

0.0640826548

707.33301

0.0009670164

0.0641238258

707.58698

0.0007125384

0.0641649968

707.854

-0.0011197032

0.0641855823

708.117

-0.0035117964

0.0642061677

708.37799

-0.0019849284

0.0642061677

708.62903

-0.0058275462

0.0642061677

708.88501

-0.0003053736

0.0641855823

709.159

-0.0012469422

0.0641649968

709.414

0.002417541

0.0641238258

709.67798

-0.0027738102

0.0640826548

709.94

-0.002926497

0.0640414838

710.18799

-0.0053949336

0.0639797273

710.45099

-0.004071648

0.0639385563

710.71698

0.00127239

0.0639179708

710.97601

0.0003562692

0.0638767998

711.23401

0.002799258

0.0638767998

711.50403

-0.0035372442

0.0638562143

711.76202

-0.0057766506

0.0638767998

712.026

-0.0021376152

0.0638973853

712.27899

0.0066927714

0.0639179708

712.54999

-0.0018576894

0.0639591418

712.80499

-0.0007125384

0.0640003128

713.07098

-0.0016032114

0.0640414838

713.32599

0.0003562692

0.0640826548

713.586

0.0003562692

0.0641238258

713.83899

-0.0036135876

0.0641649968

714.10699

-0.0046569474

0.0641855823

714.36798

-0.0020103762

0.0642267532

714.62903

-0.0003053736

0.0642473387

714.888

-0.0054458292

0.0642473387

715.151

-0.0062092632

0.0642473387

715.414

0.0056748594

0.0642473387

715.66498

0.0006107472

0.0642473387

715.94

0.0047841864

0.0642473387

716.19397

-0.0010688076

0.0642267532

716.45502

0.0060820242

0.0642267532

716.71399

0.0008652252

0.0642267532

716.98297

0.0052422468

0.0642061677

717.23499

0.002799258

0.0642061677

717.50598

-0.0009924642

0.0641855823

717.76001

-0.0011705988

0.0641855823

718.02502

0.0047587386

0.0641855823

718.28101

-0.0031555272

0.0641855823

718.52698

-0.004326126

0.0641855823

718.797

0.0026465712

0.0641855823

719.06598

-0.0032827662

0.0641855823

719.32098

-0.0051913512

0.0641855823

719.57898

-0.0028247058

0.0641855823

719.83099

0.000890673

0.0642061677

720.09802

0.0009670164

0.0642061677

720.35699

-0.0027483624

0.0642267532

720.62201

-0.00254478

0.0642473387

720.883

0.0043515738

0.0642679242

721.14398

-0.0014505246

0.0643090952

721.40997

-0.0007379862

0.0643296807

721.67499

-0.0047587386

0.0643914372

721.92102

-0.0005852994

0.0644531937

722.18903

0.00636195

0.0645355357

722.44702

-0.0034609008

0.0646178777

722.71503

-0.0076088922

0.0647002197

722.97699

0.0006616428

0.0648031472

723.23102

0.0025956756

0.0649060747

723.49298

-0.0038426178

0.0650295877

723.74298

-0.0016286592

0.0651531006

724.005

-0.0018831372

0.0652560281

724.26898

-0.0004835082

0.0653795411

724.52301

-0.000254478

0.0654824686

724.78302

0.0002290302

0.0655853961

725.04602

-0.00127239

0.0656883236

725.315

0.0023411976

0.0657706656

725.56702

0.002290302

0.0658324221

725.82703

0.0024684366

0.0658735931

726.08899

-0.0043006782

0.0659147641

726.35199

0.000127239

0.0659559351

726.617

-0.0026465712

0.0659559351

726.88

-0.0013741812

0.0659765206

727.125

-0.0015014202

0.0659765206

727.38599

-0.0004835082

0.0659765206

727.66101

-0.001399629

0.0659559351

727.914

-0.0091866558

0.0659353496

728.17798

0.0013741812

0.0659353496

728.44202

-0.003180975

0.0659147641

728.69897

-0.0066418758

0.0658941786

728.953

0.0021376152

0.0658530076

729.211

-0.0011705988

0.0658324221

729.46899

-0.0009161208

0.0658118366

729.73999

-0.0079397136

0.0657912511

729.99597

-0.0059038896

0.0657706656

730.258

0.0006107472

0.0657500801

730.52899

0.0018831372

0.0657089091

730.776

-0.0030028404

0.0656883236

731.039

-0.0042752304

0.0656471526

731.30298

-0.0039698568

0.0656059816

731.565

-0.002163063

0.0655853961

731.82202

0.0019594806

0.0655442251

732.08099

-0.0037408266

0.0655236396

732.33502

0.003308214

0.0654824686

732.60101

-0.0032318706

0.0654618831

732.85797

-0.0052931424

0.0654412976

733.12201

0.0025702278

0.0654207121

733.37701

-0.0010433598

0.0654001266

733.64697

0.0032064228

0.0654001266

733.89801

0.00254478

0.0654001266

734.15503

-0.0044024694

0.0654207121

734.41498

0.0018067938

0.0654412976

734.68597

-0.00127239

0.0654824686

734.935

0.0021376152

0.0655236396

735.19598

-0.0058784418

0.0655853961

735.45398

-0.0013232856

0.0656471526

735.71802

0.0032318706

0.0657294946

735.97998

-0.008016057

0.0658118366

736.242

0.0019849284

0.0658941786

736.49799

0.0032827662

0.0659765206

736.75702

-0.0065909802

0.0660382771

737.01801

0.0012214944

0.066120619

737.276

0.0060820242

0.0661823755

737.53802

0.004071648

0.066244132

737.79401

0.0024429888

0.0663058885

738.05499

0.0046060518

0.0663470595

738.31897

-0.0025956756

0.0663882305

738.58002

0.0073035186

0.066408816

738.84302

0.0055730682

0.0664294015

739.09302

-0.0004071648

0.066449987

739.35999

-0.0009415686

0.0664705725

739.625

0.000381717

0.066491158

739.88098

0.0001781346

0.0665117435

740.14301

0.001908585

0.066532329

740.40302

0.007125384

0.0665529145

740.65997

-0.0051913512

0.0665940855

740.92102

0.0095683728

0.066614671

741.18103

0.0063365022

0.066655842

741.43799

0.0047587386

0.0666764275

741.70502

0.0061583676

0.0667175985

741.96399

0.0042497826

0.066738184

742.22101

0.00127239

0.066779355

742.47601

0.001017912

0.066779355

742.72998

0.0040207524

0.0667999405

742.99902

0.0028247058

0.0667999405

743.25897

0.0012214944

0.066820526

743.51801

0.0001781346

0.066820526

743.77899

0.0042752304

0.066820526

744.03802

0.0157012926

0.066820526

744.29602

0.0025702278

0.0668411115

744.55701

0.0033845574

0.0668411115

744.82202

0.0065400846

0.0668411115

745.07898

0.0041225436

0.066861697

745.34198

0.0070744884

0.0668822825

745.59601

0.0046060518

0.066902868

745.86902

0.00508956

0.0669234535

746.12598

0.0094665816

0.0669646245

746.38501

0.0003053736

0.0670057955

746.65002

0.0095938206

0.0670469665

746.91101

0.0081941916

0.0670881374

747.15399

-0.0031555272

0.0671498939

747.41199

0.0028247058

0.0671910649

747.67798

0.0075834444

0.0672322359

747.94

0.0122403918

0.0672939924

748.19202

0.0044279172

0.0673351634

748.466

0.003053736

0.0673763344

748.72498

0.0021376152

0.0673969199

748.97498

0.0048096342

0.0674380909

749.25201

0.0009670164

0.0674586764

749.50702

-0.0021376152

0.0674792619

749.77802

0.0067182192

0.0674998474

750.03003

0.0050641122

0.0675204329

750.28101

-0.0008143296

0.0675204329

750.534

-0.0000508956

0.0675410184

750.797

0.0029010492

0.0675616039

751.05603

-0.0057512028

0.0675616039

751.31897

0.0029519448

0.0676027749

751.56403

0.000381717

0.0676233604

751.83899

0.0026211234

0.0676645314

752.08899

0.0035117964

0.0677057024

752.35901

-0.0014505246

0.0677468734

752.61902

-0.0023411976

0.0677880444

752.87402

-0.0007125384

0.0678498009

753.133

-0.0038680656

0.0679115574

753.39697

0.0029010492

0.0679938994

753.66803

0.0045551562

0.0680556558

753.91699

0.0075579966

0.0681379978

754.177

0.0064637412

0.0681997543

754.43701

0.0081687438

0.0682820963

754.69598

0.0204091356

0.0683438528

754.961

-0.0037917222

0.0684261948

755.21503

0.009542925

0.0684879513

755.48999

-0.0106626282

0.0685291223

755.74799

-0.0016032114

0.0685908788

756.01099

0.0007125384

0.0686320498

756.26703

0.0105353892

0.0686732208

756.52502

-0.0056239638

0.0687143918

756.79199

0.0091866558

0.0687349773

757.047

0.0092121036

0.0687555628

757.29401

-0.0162611442

0.0687761483

757.56299

0.0149887542

0.0687967338

757.81897

0.0086776998

0.0688173193

758.08899

-0.0401566284

0.0688173193

758.33899

-0.0153450234

0.0688173193

758.604

0.000890673

0.0688173193

758.867

-0.0220886904

0.0688379048

759.12701

-0.0126984522

0.0688379048

759.388

-0.0061583676

0.0688584903

759.651

-0.0090085212

0.0688790758

759.91602

-0.0148106196

0.0688996613

760.17297

-0.0082196394

0.0689202468

760.43201

-0.0200274186

0.0689614177

760.68597

0.0216051822

0.0690231742

760.95001

0.0023920932

0.0690849307

761.20502

-0.0018576894

0.0691466872

761.46698

0.0464167872

0.0692290292

761.72998

0.0225976464

0.0693319567

761.98798

-0.02799258

0.0694142987

762.26001

0.014632485

0.0695172262

762.51202

0.0120368094

0.0695995682

762.76202

0.0202818966

0.0697024957

763.03601

0.0109680018

0.0697848377

763.29401

0.0002035824

0.0698671797

763.55402

-0.0010942554

0.0699495216

763.81

0.0068963538

0.0700112781

764.07397

0.014123529

0.0700524491

764.32898

0.0036135876

0.0700936201

764.60303

0.0054203814

0.0701347911

764.84399

-0.0066927714

0.0701553766

765.11603

0.0006870906

0.0701553766

765.37201

-0.0014250768

0.0701759621

765.63202

0.0020612718

0.0701759621

765.89099

-0.0007125384

0.0701759621

766.15399

-0.0001526868

0.0701759621

766.40802

-0.0031300794

0.0701965476

766.67102

-0.001399629

0.0702171331

766.93402

0.0040462002

0.0702377186

767.18701

0.0069726972

0.0702583041

767.44897

0.0037153788

0.0702994751

767.70697

-0.0014505246

0.0703406461

767.97498

0.0001526868

0.0704024026

768.23401

-0.0010942554

0.0704641591

768.49298

-0.0009670164

0.0705465011

768.74902

0.0029519448

0.0706082576

769.008

0.002799258

0.0706700141

769.27698

-0.0003562692

0.0707523561

769.54199

-0.003689931

0.0708141126

769.79303

0.0013232856

0.0708964545

770.04401

0.0020612718

0.070958211

770.31299

0.0020103762

0.0710199675

770.57397

0.0008652252

0.071081724

770.82501

0.0055730682

0.0711434805

771.091

0.0065909802

0.071205237

771.35901

0.0001781346

0.0712669935

771.61102

0.003689931

0.07132875

771.87799

0.0084995652

0.0713905065

772.13397

0.0024938844

0.0714728485

772.38599

-0.0037917222

0.071534605

772.64801

0.0023666454

0.071616947

772.90503

0.0030791838

0.0716787035

773.164

0.0065146368

0.0717610455

773.43597

-0.0032573184

0.0718433874

773.69501

-0.001399629

0.0719257294

773.95801

0.0019594806

0.0719874859

774.21002

0.0056748594

0.0720698279

774.47101

0.004071648

0.0721315844

774.72601

0.0015523158

0.0721933409

774.99402

0.002417541

0.0722550974

775.24701

0.0015014202

0.0722962684

775.50702

0.001399629

0.0723168539

775.76099

0.001017912

0.0723374394

776.02301

0.005471277

0.0723580249

776.27698

0.0004580604

0.0723580249

776.539

0.0028501536

0.0723374394

776.80402

0.0018831372

0.0722962684

777.07098

0.0034863486

0.0722550974

777.31897

0

0.0721933409

777.58698

-0.0014505246

0.0721315844

777.84601

0.0021376152

0.0720492424

778.11401

0.0058020984

0.0719669004

778.36902

0.0054458292

0.0719051439

778.62799

0.0048605298

0.0718228019

778.89203

0.0019340328

0.0717610455

779.146

-0.0023157498

0.071699289

779.40302

-0.0051150078

0.071658118

779.66602

0.0026465712

0.071616947

779.92902

0.0031300794

0.0715963615

780.17902

0.0060056808

0.071616947

780.44702

0.0037408266

0.071616947

780.71198

-0.0003562692

0.071658118

780.961

0.0021885108

0.071699289

781.224

0.0024684366

0.0717610455

781.5

0.0021885108

0.0718433874

781.73901

0.0012214944

0.0719257294

782.008

0.0016286592

0.0720080714

782.27002

0.0024429888

0.0720904134

782.52899

0.0007888818

0.0721933409

782.79303

-0.0033591096

0.0722962684

783.05103

0.0022648542

0.0723786104

783.30701

-0.0013741812

0.0724815379

783.56897

-0.0009161208

0.0725638799

783.83099

0.0003053736

0.0726668074

784.08698

0.0072780708

0.0727491494

784.35101

0.0025956756

0.0728314913

784.60699

-0.0016795548

0.0729344188

784.86499

-0.0024429888

0.0730167608

785.13098

0.000127239

0.0730785173

785.38

0.001017912

0.0731608593

785.646

0.0010942554

0.0732432013

785.90698

0.0071762796

0.0733049578

786.16699

0.004707843

0.0733872998

786.43799

0.0019849284

0.0734490563

786.68903

0.0010688076

0.0734902273

786.95001

-0.0007888818

0.0735519838

787.21503

0.0018067938

0.0735931548

787.46802

0.010433598

0.0736343258

787.72498

0.0046314996

0.0736549113

787.987

0.0021885108

0.0736960823

788.245

0.000508956

0.0737166677

788.505

-0.0009924642

0.0737372532

788.76801

0.0024938844

0.0737784242

789.03003

-0.0018322416

0.0737990097

789.29199

-0.0004071648

0.0738401807

789.55701

-0.0079142658

0.0738607662

789.82098

0.002799258

0.0739225227

790.08002

0.0021376152

0.0739636937

790.336

0.0027229146

0.0740254502

790.59601

0.0105353892

0.0740666212

790.85602

0.0013487334

0.0741283777

791.10999

-0.0014759724

0.0741695487

791.38202

-0.0014250768

0.0742313052

791.63702

0.0016032114

0.0742724762

791.89398

0.0029773926

0.0742930617

792.15698

0.0030028404

0.0743136472

792.41901

-0.0050132166

0.0743136472

792.67102

0.005344038

0.0743136472

792.93903

0.0086013564

0.0742930617

793.18903

-0.0002035824

0.0742930617

793.45801

-0.0091103124

0.0742518907

793.71198

-0.0022648542

0.0742313052

793.96802

-0.0035881398

0.0742107197

794.22998

-0.008016057

0.0742107197

794.48901

-0.001017912

0.0742107197

794.75702

0.0037408266

0.0742313052

795.01703

0.0065655324

0.0742518907

795.26801

0.0000763434

0.0742930617

795.52002

0.0051150078

0.0743548182

795.78198

0.0057003072

0.0744371602

796.04797

0.002163063

0.0745195022

796.32202

0.001781346

0.0746224297

796.57703

0.0006107472

0.0747459426

796.83698

0.0014759724

0.0748488701

797.09497

-0.0026465712

0.0749723831

797.36102

0.0032573184

0.0751164816

797.61603

0.0042243348

0.0752399946

797.87402

-0.0026211234

0.0753635076

798.13702

-0.0033336618

0.0754870206

798.39502

0.002035824

0.0756105335

798.659

0.0062601588

0.0757340465

798.91699

0.00254478

0.0758575595

799.17902

-0.0055476204

0.075960487

799.43402

-0.0044024694

0.0760634145

799.698

-0.000381717

0.076166342

799.95502

-0.0001781346

0.076248684

800.22601

0.0052422468

0.076331026

800.48102

0.004071648

0.076413368

800.742

0.0047332908

0.0764751245

801

0.002926497

0.0765162955

801.26801

0.003562692

0.0765574665

801.52197

-0.0025193322

0.0765780519

801.78302

0.0003308214

0.0765986374

802.04602

0.00254478

0.0765986374

802.29999

0.0015777636

0.0765986374

802.56201

0.0018576894

0.0765986374

802.82397

-0.0006870906

0.0765780519

803.08002

0.0014505246

0.0765574665

803.33899

-0.0018576894

0.076536881

803.60199

-0.0001781346

0.0765162955

803.875

0.0034863486

0.0765162955

804.12402

-0.0026465712

0.07649571

804.38397

0.0035372442

0.0764751245

804.64899

0.0009670164

0.0764751245

804.90997

-0.001654107

0.0764751245

805.17102

0.001017912

0.07649571

805.43402

-0.001017912

0.0765162955

805.69202

-0.0023920932

0.076536881

805.95502

0.0011197032

0.0765574665

806.20203

-0.003562692

0.0765986374

806.47302

0.0023666454

0.0766398084

806.72803

-0.0014759724

0.0766809794

806.99402

-0.0018831372

0.0767221504

807.25702

0.0017558982

0.0767839069

807.505

-0.0023411976

0.0768250779

807.76202

-0.0009924642

0.0768868344

808.02502

-0.0002290302

0.0769485909

808.289

0.0056748594

0.0769897619

808.55103

-0.0023666454

0.0770515184

808.80402

-0.0015523158

0.0771132749

809.06897

0.0028247058

0.0771956169

809.32599

0.0055730682

0.0772573734

809.59497

0.0007125384

0.0773191299

809.84497

0.0032318706

0.0773808864

810.10498

0.0031300794

0.0774632284

810.37097

-0.0009415686

0.0775249848

810.62402

0.0026974668

0.0776073268

810.89301

-0.0065909802

0.0776690833

811.14398

0.0005598516

0.0777308398

811.41699

0.002417541

0.0778131818

811.67297

0.0017304504

0.0778749383

811.93597

-0.0007379862

0.0779366948

812.19501

-0.0011197032

0.0779778658

812.45203

0.000254478

0.0780396223

812.71503

-0.0039953046

0.0780807933

812.966

0.0003562692

0.0781425498

813.224

0.0066418758

0.0781837208

813.48602

0.0018322416

0.0782454773

813.75

0.0015523158

0.0783072338

814.01703

-0.0012469422

0.0783689903

814.27698

-0.0000508956

0.0784307468

814.53497

0.0025193322

0.0785130887

814.78998

0.0016795548

0.0785748452

815.052

-0.00381717

0.0786777727

815.31702

0.0013232856

0.0787601147

815.57001

-0.0037408266

0.0788630422

815.841

-0.0010688076

0.0789453842

816.10602

-0.0052422468

0.0790483117

816.36499

0.0029010492

0.0791718247

816.62701

0.001526868

0.0792747522

816.87402

0.0013487334

0.0793776797

817.13898

0.0001781346

0.0794806071

817.40002

0.0007125384

0.0795629491

817.66803

0.0021376152

0.0796658766

817.91998

0.0007125384

0.0797482186

818.18701

0.0003308214

0.0798099751

818.44202

-0.0020867196

0.0798923171

818.69897

0.001781346

0.0799334881

818.96899

0.0034863486

0.0799952446

819.22498

-0.0045297084

0.0800364156

819.48999

-0.0044024694

0.0800775866

819.75201

-0.0037153788

0.0800981721

820.013

0.0011705988

0.0801393431

820.27502

0.0032064228

0.0801599286

820.53699

-0.001017912

0.0801805141

820.81299

0.0042752304

0.0802216851

821.06

0.0025702278

0.0802422706

821.31598

-0.0013741812

0.0802834416

821.57599

-0.0021376152

0.0803246126

821.84198

-0.0043515738

0.0803657835

822.10101

-0.0010433598

0.0804069545

822.362

-0.00254478

0.0804481255

822.61902

-0.0009924642

0.080509882

822.89001

0.0022394064

0.080551053

823.15198

-0.0072271752

0.0806128095

823.40802

0.0009161208

0.0806539805

823.66803

0.0036135876

0.080715737

823.92999

0.0049114254

0.080756908

824.19299

-0.0012469422

0.0807774935

824.44202

0.0004326126

0.0808186645

824.70801

0.0012214944

0.08083925

824.97601

-0.0018576894

0.0808598355

825.24402

-0.0009670164

0.0808598355

825.50598

0.0006616428

0.080880421

825.76202

0.0020867196

0.0809010065

826.026

0.000636195

0.0809010065

826.29102

0.0021376152

0.080921592

826.54401

-0.0020612718

0.0809421775

826.815

-0.0050641122

0.0809833485

827.07898

-0.002799258

0.081003934

827.336

-0.0012214944

0.081045105

827.599

-0.0007125384

0.081086276

827.849

0.0052931424

0.081127447

828.12299

-0.000890673

0.081168618

828.38898

0.0034609008

0.081209789

828.64801

0.0009924642

0.08125096

828.91302

0.0010688076

0.0812715455

829.177

0.0051913512

0.081292131

829.42499

-0.0051659034

0.081292131

829.67798

0.0078124746

0.0813127165

829.94501

-0.0050132166

0.0813127165

830.20801

-0.0039189612

0.081292131

830.45898

-0.0039189612

0.081292131

830.724

-0.0035117964

0.0812715455

830.98901

0.0072780708

0.0812715455

831.24597

0.0051913512

0.0812715455

831.50299

-0.0050386644

0.0812715455

831.76099

0.0001781346

0.081292131

832.02899

-0.002290302

0.0813127165

832.289

-0.0042243348

0.0813333019

832.56097

0.0034100052

0.0813744729

832.81702

-0.001654107

0.0814362294

833.078

0.0047332908

0.0814774004

833.34601

-0.0054458292

0.0815391569

833.60699

0.0008143296

0.0816214989

833.87

0.0026974668

0.0816832554

834.11902

0.0035881398

0.0817450119

834.38202

0.0007888818

0.0818273539

834.64697

0.001526868

0.0818891104

834.90503

0.0004580604

0.0819508669

835.15997

0.0019594806

0.0820126234

835.42999

0.0029519448

0.0820537944

835.67902

0.0007888818

0.0821155509

835.94897

0.0033591096

0.0821567219

836.20398

-0.0004326126

0.0822184784

836.47803

-0.0020867196

0.0822802348

836.72803

0.00127239

0.0823214058

836.995

0.0041734392

0.0823831623

837.26202

-0.0019849284

0.0824449188

837.51898

0.0009415686

0.0824860898

837.784

-0.0038680656

0.0825478463

838.047

-0.0031555272

0.0826096028

838.30499

0.006489189

0.0826713593

838.57703

0.0010433598

0.0827331158

838.83301

-0.0007125384

0.0827948723

839.086

-0.00254478

0.0828566288

839.35999

-0.0012214944

0.0829183853

839.61902

-0.001399629

0.0829801418

839.87701

-0.0045551562

0.0830213128

840.13898

0.0010688076

0.0830830693

840.39502

-0.0006107472

0.0831242403

840.64801

0.0081178482

0.0831859968

840.91699

0.0005344038

0.0832271677

841.18402

-0.0075325488

0.0832683387

841.43799

0.0019594806

0.0833095097

841.69897

-0.0084741174

0.0833712662

841.96997

-0.0051913512

0.0834330227

842.22498

-0.0050132166

0.0834947792

842.49103

-0.0032827662

0.0835565357

842.75201

0.0000508956

0.0836388777

843.021

-0.0025702278

0.0837212197

843.27698

0.001526868

0.0838035617

843.53699

-0.0001526868

0.0838859037

843.79901

-0.0004835082

0.0839888312

844.06403

-0.0017558982

0.0840917587

844.31799

-0.0032573184

0.0841946861

844.57397

0.0020103762

0.0842976136

844.84198

0.0059547852

0.0844005411

845.099

-0.0010942554

0.0845034686

845.36102

0.0021885108

0.0846063961

845.61499

0.0038680656

0.0846887381

845.88

-0.0017304504

0.0847710801

846.138

0.0021376152

0.0848534221

846.40601

-0.0027738102

0.0849151786

846.66602

0.0112733754

0.0849769351

846.92499

0.000127239

0.0850386916

847.19299

-0.0001526868

0.0850798626

847.44897

0.0033845574

0.0851210335

847.71301

0.0041225436

0.0851622045

847.96899

0.0004835082

0.0852033755

848.229

-0.0014759724

0.0852445465

848.49597

-0.002290302

0.085265132

848.75702

0.0032827662

0.0852857175

849.01898

0.0041225436

0.085306303

849.271

0.0032827662

0.0853268885

849.52899

0.0052422468

0.085347474

849.797

-0.0020103762

0.0853680595

850.05902

0.0026465712

0.085388645

850.31702

-0.0048859776

0.085388645

850.57501

-0.0004071648

0.0854092305

850.84399

-0.000763434

0.0854092305

851.09998

-0.0033845574

0.0854092305

851.35999

0.0029010492

0.0854092305

851.61603

-0.0011960466

0.0854092305

851.88599

0.000763434

0.085388645

852.14301

-0.0026465712

0.085388645

852.40698

-0.0004580604

0.0853680595

852.66998

0.0024938844

0.0853680595

852.93298

-0.0027229146

0.0853680595

853.19897

0.0032064228

0.0853680595

853.44897

0.0001526868

0.085388645

853.71997

0.0002290302

0.0854092305

853.98199

-0.0009670164

0.0854504015

854.24402

-0.0004580604

0.0854915725

854.50098

-0.0004580604

0.0855739145

854.763

0.0007888818

0.0856562565

855.01703

-0.0004326126

0.0857797695

855.28101

0.003562692

0.0859032825

855.54602

0.0000508956

0.0860679665

855.80298

-0.0070490406

0.0862326504

856.07001

-0.0020612718

0.0864179199

856.33197

-0.0014250768

0.0866031894

856.58801

0.0037153788

0.0868090444

856.85303

-0.0009924642

0.0870148994

857.10901

0.0030791838

0.0872001688

857.37299

-0.0026211234

0.0874060238

857.633

-0.0066418758

0.0875912933

857.901

0.000890673

0.0877559773

858.16101

0.0010433598

0.0879206613

858.42401

0.0030791838

0.0880441742

858.67999

-0.0038680656

0.0881676872

858.94702

-0.0083468784

0.0882500292

859.211

-0.0011960466

0.0883323712

859.47699

0.001017912

0.0883941277

859.73297

0.0004835082

0.0884352987

859.99103

-0.002035824

0.0884558842

860.25702

0.0002035824

0.0884764697

860.51501

-0.0045042606

0.0884764697

860.78302

-0.0026465712

0.0884970552

861.047

0.0013487334

0.0884970552

861.30298

-0.0023157498

0.0884970552

861.56702

0.0011705988

0.0884970552

861.83398

-0.003562692

0.0885176407

862.091

-0.0080669526

0.0885382262

862.35498

0.001145151

0.0885793972

862.612

-0.0005598516

0.0886205682

862.87701

0.003689931

0.0886823247

863.14099

0.0017050026

0.0887234957

863.409

-0.008270535

0.0888058377

863.67102

-0.0188059242

0.0888675942

863.92902

-0.0006616428

0.0889499361

864.18597

0.0158030838

0.0890116926

864.44598

-0.0004326126

0.0890940346

864.71399

0.0025702278

0.0891557911

864.97699

-0.003308214

0.0892175476

865.237

-0.0071762796

0.0892793041

865.50201

0.0001017912

0.0892998896

865.75299

0.0001781346

0.0893204751

866.02399

0.001017912

0.0893410606

866.27502

-0.004580604

0.0893410606

866.53601

-0.006743667

0.0893410606

866.80298

-0.0019594806

0.0893204751

867.07098

-0.000763434

0.0892793041

867.33099

0.0030282882

0.0892381331

867.59802

0.0009415686

0.0891969621

867.86102

0.000763434

0.0891352056

868.12201

0.0018831372

0.0890940346

868.38098

-0.0023666454

0.0890528636

868.651

-0.000381717

0.0890322781

868.90802

-0.0040970958

0.0890116926

869.17798

-0.0024429888

0.0890116926

869.435

-0.0030028404

0.0890116926

869.69397

0.00381717

0.0890528636

869.95898

0.004326126

0.0891352056

870.21399

-0.0025702278

0.0892381331

870.47101

-0.00127239

0.0893616461

870.73999

-0.0016032114

0.0895263301

870.99799

0.0051150078

0.0897321851

871.26001

0.0028756014

0.0899586255

871.53101

-0.0022394064

0.0902056515

871.79199

-0.007252623

0.0904938485

872.05103

-0.0010433598

0.0907820455

872.31403

0.0025193322

0.0910702424

872.57898

-0.0062092632

0.0913790249

872.84399

-0.0028756014

0.0916466364

873.09802

-0.000254478

0.0919142478

873.367

0.000763434

0.0921612738

873.625

0.0034100052

0.0923671288

873.883

-0.0001017912

0.0925318128

874.14301

-0.006234711

0.0926553258

874.41101

-0.0037408266

0.0927582532

874.66803

-0.0019849284

0.0927994242

874.93402

0.0007379862

0.0927994242

875.18701

-0.0051404556

0.0927788387

875.45398

-0.001654107

0.0927170823

875.71399

-0.0023666454

0.0926347403

875.979

0.0023666454

0.0925318128

876.245

-0.0017050026

0.0924288853

876.50702

0.0012978378

0.0923053723

876.77301

-0.0032064228

0.0922024448

877.03699

-0.0017558982

0.0920995173

877.29602

0.0010433598

0.0919965898

877.55798

-0.0025193322

0.0919348333

877.82202

0.0009924642

0.0918730768

878.09003

0.0036135876

0.0918524913

878.34998

-0.0003562692

0.0918319058

878.60199

-0.000127239

0.0918524913

878.87

0.0018576894

0.0918936623

879.12799

0.0015523158

0.0919554188

879.38898

0.0017304504

0.0920171753

879.65802

0.0022139586

0.0920995173

879.91199

-0.00763434

0.0922024448

880.17603

-0.0033336618

0.0923259578

880.44299

-0.0027229146

0.0924494708

880.70398

-0.004326126

0.0925729838

880.96399

-0.0090848646

0.0926964968

881.23199

0.0021121674

0.0928200097

881.49402

-0.0065909802

0.0929435227

881.76099

-0.0026465712

0.0930670357

882.01501

-0.0018322416

0.0931905487

882.27802

0.001654107

0.0932934762

882.54901

0.0013741812

0.0934169892

882.80902

-0.004580604

0.0935199167

883.06097

-0.0035881398

0.0936434297

883.328

-0.0031300794

0.0937669426

883.58698

0.0046823952

0.0938904556

883.85602

0.0030282882

0.0939933831

884.11603

0.0020103762

0.0941168961

884.37701

0.002926497

0.0942404091

884.64001

-0.000763434

0.0943639221

884.90002

0.0015014202

0.0944874351

885.17102

0.0025702278

0.0945903626

885.42603

0.0017304504

0.09469329

885.68402

-0.0063873978

0.0947962175

885.95697

-0.003562692

0.0948785595

886.20502

-0.0040970958

0.0949609015

886.47803

0.004962321

0.095022658

886.737

-0.0013741812

0.0950844145

887.01202

0.003689931

0.095146171

887.27002

0.0015014202

0.0952079275

887.52899

-0.0027229146

0.0952490985

887.79498

-0.0044279172

0.095310855

888.04797

0.0006616428

0.0953726115

888.31897

-0.0017558982

0.095434368

888.58398

0.0035372442

0.0954961245

888.84399

-0.003562692

0.0955784665

889.10699

-0.0005598516

0.0956608084

889.37402

0.0006870906

0.0957637359

889.62903

0.0009924642

0.0958666634

889.89001

0.0061838154

0.0959695909

890.15601

-0.000127239

0.0960725184

890.41699

0.0063110544

0.0961960314

890.68402

0.000890673

0.0962989589

890.94702

-0.0025956756

0.0964224719

891.21997

-0.0031555272

0.0965459848

891.48297

0.001526868

0.0966694978

891.75201

0.002926497

0.0967930108

892.00598

-0.0047332908

0.0969165238

892.26801

-0.0032573184

0.0970400368

892.52197

-0.0032318706

0.0971635498

892.79602

0.0004835082

0.0972870628

893.04797

-0.0040207524

0.0974105758

893.31702

0.000636195

0.0975340887

893.57397

0.0016032114

0.0976576017

893.83899

-0.0013232856

0.0977811147

894.10101

-0.003435453

0.0978840422

894.36603

-0.0075834444

0.0980075552

894.62701

-0.0016795548

0.0981104827

894.88501

-0.0001781346

0.0981928247

895.151

-0.0001526868

0.0982751667

895.422

-0.0007125384

0.0983575087

895.67902

0.0029773926

0.0984192652

895.94098

0.000127239

0.0984810216

896.211

0.001145151

0.0985221926

896.47101

-0.0032573184

0.0985633636

896.73199

-0.0007888818

0.0986045346

896.98999

0.000890673

0.0986457056

897.26001

-0.0017050026

0.0986662911

897.51398

-0.0018831372

0.0987074621

897.78198

0.0018322416

0.0987280476

898.04199

0.0019849284

0.0987692186

898.30798

0.0007125384

0.0988103896

898.578

-0.004707843

0.0988515606

898.828

0.0018322416

0.0988927316

899.09302

-0.0037153788

0.0989544881

899.35699

-0.004326126

0.0989956591

899.62598

-0.0029010492

0.0990574156

899.883

-0.0047332908

0.0991191721

900.151

-0.000763434

0.0991809286

900.40802

-0.0023666454

0.0992426851

900.67297

0.0010688076

0.0992838561

900.93103

-0.0009670164

0.0993456126

901.19

-0.0000763434

0.099407369

901.46802

-0.0037917222

0.09944854

901.73297

-0.0026974668

0.099489711

901.98999

0.0000254478

0.099530882

902.25299

-0.003053736

0.099572053

902.51898

-0.0081178482

0.099613224

902.78003

-0.0033845574

0.0996338095

903.04303

0.002672019

0.0996749805

903.30902

-0.0003562692

0.099695566

903.56299

0.0039953046

0.0997161515

903.82703

0.0013487334

0.0997573225

904.09399

0.0034100052

0.0997984935

904.35199

-0.0067691148

0.099819079

904.61298

0.0015777636

0.0998808355

904.88

-0.0018322416

0.0999220065

905.13898

-0.001781346

0.1000043485

905.40399

-0.0039698568

0.100066105

905.67297

-0.0041479914

0.1001690325

905.93402

0.0001526868

0.10027196

906.203

0.0031046316

0.1003954729

906.46698

-0.001145151

0.1005189859

906.72803

0.0022648542

0.1006836699

906.98901

-0.0010433598

0.1008483539

907.24103

0.0000254478

0.1010130379

907.51801

0.0037153788

0.1011777219

907.78101

0.0038935134

0.1013629913

908.03003

0.0021121674

0.1015276753

908.29401

0.0035372442

0.1017129448

908.55798

-0.0019340328

0.1018570433

908.82898

0.0063873978

0.1020011418

909.08801

-0.0063873978

0.1021452403

909.35797

0.0076852356

0.1022481677

909.62097

0.00508956

0.1023305097

909.88599

-0.0002035824

0.1024128517

910.151

-0.0061838154

0.1024951937

910.41602

0.0003053736

0.1025363647

910.67603

-0.000763434

0.1025981212

910.94299

-0.0009924642

0.1026392922

911.20502

0.0008143296

0.1027010487

911.466

-0.0012469422

0.1027628052

911.72302

0.0044788128

0.1028451472

911.987

0.004580604

0.1029274892

912.25201

0.0002290302

0.1030304167

912.51599

0.0023411976

0.1031539297

912.771

-0.0012214944

0.1032980281

913.03497

0.0056239638

0.1034627121

913.30603

-0.0025193322

0.1036273961

913.56299

-0.0001017912

0.1038126656

913.83002

-0.0000763434

0.1039979351

914.091

-0.003180975

0.104162619

914.36102

0.0044024694

0.1043478885

914.62299

-0.0023666454

0.1045125725

914.888

0.0013232856

0.1046772565

915.15302

-0.0040970958

0.1048007695

915.40997

-0.0024429888

0.104944868

915.672

0.0009161208

0.1050477955

915.94202

-0.0007125384

0.1051301374

916.20099

-0.0022648542

0.1052124794

916.45697

0.0003308214

0.1052742359

916.72803

0.002417541

0.1053359924

916.98499

0.0043006782

0.1053771634

917.24402

0.002926497

0.1053977489

917.51001

-0.002035824

0.1054389199

917.77502

0.002672019

0.1054800909

918.02802

-0.0006107472

0.1055006764

918.297

0.0010942554

0.1055418474

918.55402

0.0005852994

0.1055830184

918.81403

0.0007379862

0.1056447749

919.08698

0.0038426178

0.1057065314

919.35101

-0.0005852994

0.1057888734

919.61499

-0.003944409

0.1058712154

919.87799

0.003944409

0.1059535574

920.14001

0.0016032114

0.1060564848

920.40997

-0.001781346

0.1061594123

920.66699

0.0013232856

0.1062829253

920.92902

-0.0032573184

0.1064064383

921.20502

0.0015523158

0.1065505368

921.46503

0.002417541

0.1066740498

921.71899

0.0046314996

0.1067975628

921.98901

0.0022139586

0.1069416613

922.25403

-0.0014505246

0.1070651742

922.51703

0.001145151

0.1071886872

922.77502

0.0016795548

0.1072916147

923.03802

0.0000508956

0.1074151277

923.30298

0.0055221726

0.1075180552

923.57202

0.0009924642

0.1076209827

923.83398

0.0036135876

0.1077239102

924.08698

-0.0007125384

0.1078268377

924.35699

0.0040970958

0.1079297652

924.61401

0.0025702278

0.1080121071

924.88

0.003689931

0.1080944491

925.14301

0.0026211234

0.1081767911

925.41302

0.0012469422

0.1082797186

925.67499

-0.0009415686

0.1083620606

925.93799

0.0017304504

0.1084444026

926.20898

-0.0018576894

0.1085061591

926.46399

0.0003053736

0.1085885011

926.72803

-0.0052676946

0.1086708431

926.98602

0.0010433598

0.1087325996

927.24597

0.0031300794

0.1088149416

927.513

0.000254478

0.1088766981

927.76801

0.0040970958

0.108917869

928.03101

0.000636195

0.1089796255

928.29901

-0.0043515738

0.1090207965

928.55798

-0.0003308214

0.109082553

928.82898

0.0053185902

0.109123724

929.09497

-0.0007888818

0.1091443095

929.35101

0.000127239

0.109164895

929.61902

0.0017304504

0.109206066

929.88202

0.000763434

0.1092266515

930.14502

0.0007125384

0.1092266515

930.40997

-0.0028247058

0.109247237

930.66998

0.0034863486

0.1092678225

930.93701

-0.0015523158

0.1092678225

931.18799

-0.0006107472

0.109288408

931.46503

-0.0005852994

0.1093089935

931.71698

0.0008143296

0.1093501645

931.98901

-0.000636195

0.109411921

932.24402

-0.0009161208

0.1094736775

932.508

-0.0039189612

0.1095560195

932.77698

0.0021121674

0.109658947

933.04199

0.0008143296

0.1097618745

933.31

-0.003435453

0.1099059729

933.57202

-0.0003308214

0.1100500714

933.83502

-0.0003053736

0.1102147554

934.09998

-0.0030282882

0.1104000249

934.354

0.0015014202

0.1105852944

934.62097

0.0007888818

0.1107911494

934.88599

0.002926497

0.1109970043

935.14801

-0.0007125384

0.1112028593

935.41699

0.0014250768

0.1114087143

935.677

-0.002417541

0.1116145693

935.93103

0.001399629

0.1118204242

936.20599

-0.0001781346

0.1120468647

936.466

0.000127239

0.1122527197

936.73798

0.003435453

0.1124585747

936.98798

0.0025193322

0.1126644297

937.25897

-0.0001781346

0.1128702846

937.51501

-0.00127239

0.1130555541

937.78101

0.0026211234

0.1132614091

938.04602

0.001526868

0.1134672641

938.30402

0.0000763434

0.1136525335

938.573

-0.0011960466

0.113837803

938.83698

-0.0010688076

0.114002487

939.10303

0.0008143296

0.1141877565

939.36798

0.002163063

0.1143524405

939.63

0.0017304504

0.1145171245

939.89398

0.0020867196

0.1146612229

940.14801

0.004962321

0.1148053214

940.41998

0

0.1149494199

940.67603

-0.0014505246

0.1150729329

940.94299

-0.0001781346

0.1152170314

941.211

-0.005980233

0.1153405444

941.46698

-0.0031300794

0.1154640574

941.72699

-0.0013741812

0.1155875703

941.992

-0.0003053736

0.1156904978

942.25403

0.0009161208

0.1158140108

942.51599

0.0023157498

0.1159169383

942.78101

-0.0028501536

0.1160198658

943.04797

-0.0008397774

0.1161022078

943.31

0.0026211234

0.1161845498

943.57898

0.0006107472

0.1162668918

943.83698

-0.0000763434

0.1163286483

944.112

-0.0016286592

0.1163698193

944.37299

-0.0030282882

0.1164315758

944.63599

-0.0020867196

0.1164521613

944.90399

-0.0007379862

0.1164933323

945.16302

-0.002672019

0.1165139177

945.41998

-0.0001526868

0.1165345032

945.68903

-0.0022648542

0.1165550887

945.94702

0.0012469422

0.1165756742

946.21301

0.0021376152

0.1165962597

946.47601

0.0047841864

0.1166168452

946.737

0.0027738102

0.1166580162

947.00201

0.0013741812

0.1166786017

947.26398

-0.0016795548

0.1167197727

947.52502

0.000508956

0.1167609437

947.79102

0.0023666454

0.1168227002

948.05402

0.002799258

0.1168638712

948.32599

0.0007125384

0.1169256277

948.58899

0.0021376152

0.1170079697

948.841

0.0037662744

0.1170697262

949.10797

0.0055221726

0.1171520682

949.37201

0.0033845574

0.1172549957

949.64099

0.0005598516

0.1173373377

949.896

0.0055730682

0.1174608506

950.16498

0.0054967248

0.1175637781

950.43402

0.0011197032

0.1176872911

950.69897

-0.001908585

0.1178313896

950.95599

0.007888818

0.1179754881

951.22302

0.0014250768

0.1181401721

951.49103

0.0018576894

0.1183048561

951.745

-0.0037408266

0.11846954

952.01099

-0.0004071648

0.1186548095

952.27502

0.0012978378

0.118840079

952.54498

0.0014759724

0.1190253485

952.80402

0.0039953046

0.1192312035

953.07098

0.0017050026

0.1194164729

953.328

0.0014250768

0.1196017424

953.60101

0.0018322416

0.1197870119

953.86298

0.0008397774

0.1199516959

954.12903

-0.0035117964

0.1201163799

954.38501

0.0048605298

0.1202604784

954.65503

-0.0047841864

0.1204045768

954.91901

0.0024684366

0.1205280898

955.177

-0.0009415686

0.1206310173

955.43799

-0.0026211234

0.1207133593

955.70697

-0.0037408266

0.1208162868

955.96198

0.0002290302

0.1208780433

956.23901

0.0037153788

0.1209603853

956.49902

0.0050386644

0.1210221418

956.75403

0.00381717

0.1211044838

957.02502

0.0042497826

0.1211868258

957.29303

-0.0009415686

0.1212897532

957.55103

0.0021885108

0.1213926807

957.815

-0.003180975

0.1214956082

958.08301

0.0045551562

0.1216397067

958.34399

0.001781346

0.1217838052

958.60602

0.0054967248

0.1219484892

958.87097

0.0026211234

0.1221337587

959.14398

0.0096447162

0.1223190281

959.401

0.005344038

0.1225248831

959.66498

0.0028247058

0.1227307381

959.93402

-0.0018576894

0.1229365931

960.18701

-0.0003308214

0.1231424481

960.46198

0.0014505246

0.123348303

960.71503

-0.0017304504

0.1235335725

960.98602

0.0015014202

0.1236982565

961.24298

-0.0020612718

0.1238629405

961.51398

0.0029773926

0.1240276245

961.77502

0.0033591096

0.1241511374

962.039

0.0008652252

0.1242952359

962.30298

-0.001399629

0.1244393344

962.57703

0.0019849284

0.1245834329

962.83398

-0.0034863486

0.1247069459

963.10498

0.002672019

0.1248716299

963.36401

0.0131819604

0.1250363139

963.625

0.003435453

0.1252009978

963.89697

0.0172790562

0.1253862673

964.15802

-0.0016795548

0.1255921223

964.41803

0.0078124746

0.1258185628

964.68402

0.0078633702

0.1260244177

964.94897

0.0187550286

0.1262508582

965.216

0.0023411976

0.1264567132

965.48297

-0.0235137672

0.1266625682

965.74597

-0.0203327922

0.1268684232

966.013

0.0092375514

0.1270536926

966.27197

-0.0012978378

0.1271977911

966.52698

-0.0090848646

0.1273418896

966.80298

0.0197729406

0.1274654026

967.06201

0.0332348268

0.1275889156

967.32001

0.0092375514

0.1276918431

967.58301

-0.0138944988

0.1277741851

967.85101

-0.0196711494

0.1278771126

968.12299

0.018322416

0.12798004

968.37402

0.0040207524

0.1280829675

968.65002

0.0093138948

0.128185895

968.91101

0.0070235928

0.1283299935

969.16803

0.0091357602

0.128474092

969.44397

-0.0212234652

0.128638776

969.70398

-0.0078124746

0.1288240455

969.97198

0.04198887

0.1290093149

970.23102

-0.0208163004

0.1291945844

970.495

-0.013232856

0.1294004394

970.75897

0.0018831372

0.1296062944

971.02002

0.0190095066

0.1298121494

971.29303

0.00890673

0.1299974188

971.54999

-0.0074053098

0.1301621028

971.82001

0.0196965972

0.1303267868

972.09198

0.010942554

0.1304708853

972.349

-0.0145306938

0.1305738128

972.62201

0.0018067938

0.1306767403

972.87097

-0.0073035186

0.1307590823

973.146

0.0236410062

0.1308208387

973.409

-0.0080669526

0.1308620097

973.67102

-0.0081941916

0.1309031807

973.93298

0.0174571908

0.1309237662

974.198

0.0077106834

0.1309443517

974.45697

0.0021376152

0.1309649372

974.71503

0.013360095

0.1309855227

974.98401

0.0094920294

0.1310061082

975.25598

0.0048096342

0.1310266937

975.52698

0.024048171

0.1310472792

975.78998

0.0048605298

0.1310884502

976.05603

0.0111461364

0.1311296212

976.323

0.0191876412

0.1311707922

976.58099

-0.0141744246

0.1312325487

976.86102

-0.0145561416

0.1313148907

977.11902

-0.0064382934

0.1313766472

977.38397

-0.0031046316

0.1314589892

977.64502

0.0246589182

0.1315413312

977.909

0.0110952408

0.1316442587

978.18298

0.0076088922

0.1317471861

978.44702

-0.0068963538

0.1318501136

978.71002

0.0113751666

0.1319736266

978.98102

0.032827662

0.1320971396

979.23999

0.047460147

0.1322206526

979.49597

0.0198238362

0.1323441656

979.76501

0.0150396498

0.1324676786

980.034

0.0143525592

0.1325911916

980.29303

-0.0147342762

0.13273529

980.55298

-0.0123930786

0.1328793885

980.82898

-0.0039189612

0.133023487

981.09003

-0.0176098776

0.1331675855

981.34802

-0.0150650976

0.133311684

981.61902

0.0235137672

0.133476368

981.88202

-0.0222413772

0.1336204665

982.15399

-0.0033845574

0.1337851504

982.414

-0.0024684366

0.1339498344

982.67603

-0.015904875

0.1341351039

982.93903

-0.0154468146

0.1342997879

983.216

0.0399021504

0.1344850574

983.479

0.0189840588

0.1346703268

983.74103

0.0263639208

0.1348761818

984.00897

0.0114006144

0.1350614513

984.27301

-0.0266183988

0.1352673063

984.53802

-0.0048605298

0.1354731613

984.80499

-0.00636195

0.1356584307

985.06702

-0.0109171062

0.1358642857

985.323

0.0365430408

0.1360701407

985.59601

0.038553417

0.1362554102

985.85699

0.0400548372

0.1364406797

986.11902

-0.0055221726

0.1366259491

986.388

0.0091357602

0.1368112186

986.646

0.0341254998

0.1369964881

986.91998

0.0086776998

0.1371611721

987.17999

0.0224704074

0.1373258561

987.44598

-0.0123930786

0.1374699545

987.70898

0.0095938206

0.1376346385

987.98199

-0.0067182192

0.137778737

988.245

-0.0211725696

0.1379228355

988.51202

0.0074307576

0.138066934

988.78198

0.035754159

0.1382110325

989.04401

-0.0133091994

0.1383345455

989.30603

0.0345326646

0.1384786439

989.56299

0.0321151236

0.1386227424

989.83002

0.0136400208

0.1387462554

990.09399

-0.0081178482

0.1388903539

990.35303

0.0100009854

0.1390344524

990.62402

-0.0096447162

0.1391785509

990.89398

0.0183987594

0.1393432348

991.15997

0.0234374238

0.1395079188

991.42102

0.0057512028

0.1396726028

991.69

-0.0088558344

0.1398372868

991.953

0.0328785576

0.1400225563

992.22101

0.0023920932

0.1402284113

992.487

-0.0019340328

0.1404136807

992.75403

-0.0068963538

0.1406195357

993.02002

0.009288447

0.1408048052

993.28601

0.0292140744

0.1410106602

993.547

0.0121640484

0.1412165152

993.81403

0.0298757172

0.1414223701

994.07397

0.0155486058

0.1416076396

994.33801

-0.0012214944

0.1417929091

994.60101

0.0057512028

0.1419781786

994.867

-0.0070235928

0.1421634481

995.13202

-0.0164901744

0.1423487175

995.39697

0.0242772012

0.1425134015

995.66498

0.04326126

0.1426780855

995.92499

0.0310208682

0.1428427695

996.20099

0.0485798502

0.1430074535

996.46997

0.0323950494

0.1431515519

996.729

0.080033331

0.1432956504

996.99402

0.070617645

0.1434397489

997.25403

0.080033331

0.1435838474

997.526

0.0725007822

0.1437073604

997.78302

0.00381717

0.1438308734

998.05798

0.0700323456

0.1439749719

998.32001

0.0526514982

0.1440984848

998.578

0.0202818966

0.1442014123

998.841

0.0741294414

0.1443249253

999.09497

0.0819164682

0.1444278528

999.367

0.0089576256

0.1445307803

999.63

0.0700068978

0.1446337078

999.89801

0.080415048

0.1447366353

1000.16803

0.05980233

0.1448601483

1000.44

0.0766996692

0.1449424903

1000.70203

0.081687438

0.1450248323

1000.96997

0.031046316

0.1451071742

1001.23297

0.0387315516

0.1451895162

1001.49902

0.0108662106

0.1452718582

1001.76703

0.040970958

0.1453336147

1002.026

0.0538475448

0.1453953712

1002.28699

0.0707703318

0.1454571277

1002.56

0.037153788

0.1454982987

1002.81702

0.0365684886

0.1455600552

1003.08698

0.0458314878

0.1456218117

1003.34698

0.0813566166

0.1457041537

1003.61102

0.0708212274

0.1457659102

1003.87

0.0734932464

0.1458688377

1004.14203

0.0423451392

0.1459717652

1004.39801

0.054203814

0.1461158636

1004.65802

0.0850210998

0.1462599621

1004.92297

0.0551962782

0.1464452316

1005.19

0.0543565008

0.1466510866

1005.44897

0.0079397136

0.1468569416

1005.72302

0.1034962026

0.1471039675

1005.98901

0.0359577414

0.1473509935

1006.25

0.046314996

0.1475980195

1006.51703

0.043134021

0.1478450455

1006.78101

0.0202055532

0.1480920714

1007.04498

0.025829517

0.1483185119

1007.31201

0.0597259866

0.1485449524

1007.57501

0.0488852238

0.1487302219

1007.83801

0.0484017156

0.1489154913

1008.10498

0.0523970202

0.1490801753

1008.36499

0.0464167872

0.1492242738

1008.63397

0.0223177206

0.1493477868

1008.89203

0.0447117846

0.1494712998

1009.15802

0.0618890496

0.1495948128

1009.41901

0.0504375396

0.1497183258

1009.67603

0.0327513186

0.1498418387

1009.94501

0.030155643

0.1499653517

1010.21301

0.0435666336

0.1500888647

1010.48199

0.0592424784

0.1502535487

1010.74597

0.0680474172

0.1503976472

1011.01099

0.0580718796

0.1505623312

1011.276

0.0518626164

0.1507270152

1011.539

0.044915367

0.1508916991

1011.79797

0.0479945508

0.1510563831

1012.05902

0.0617363628

0.1512004816

1012.33099

0.0573084456

0.1513239946

1012.58801

0.0518880642

0.1514475076

1012.85797

0.0678692826

0.1515710206

1013.11499

0.0573593412

0.1516533626

1013.38

0.0608965854

0.151715119

1013.63702

0.0549926958

0.15175629

1013.90503

0.0625252446

0.151797461

1014.16901

0.0443300676

0.1518180465

1014.42499

0.0593188218

0.1518592175

1014.68903

0.0529059762

0.151879803

1014.95502

0.0448135758

0.1519003885

1015.21503

0.0469002954

0.1519415595

1015.48901

0.0298757172

0.1519827305

1015.758

0.0369502056

0.1520239015

1016.02698

0.0546873222

0.1521062435

1016.289

0.0604894206

0.1521885855

1016.53497

0.0580464318

0.152291513

1016.81

0.0577410582

0.1523944405

1017.07898

0.0556288908

0.152538539

1017.34198

0.054458292

0.1526826374

1017.60498

0.0618636018

0.1528267359

1017.86603

0.052040751

0.1529914199

1018.12

0.0509973912

0.1531766894

1018.39697

0.0587589702

0.1533619589

1018.66199

0.0583772532

0.1535266429

1018.91998

0.044788128

0.1537119123

1019.18298

0.0572321022

0.1538971818

1019.453

0.067309431

0.1540824513

1019.71399

0.0439992462

0.1542677208

1019.97803

0.0352706508

0.1544324048

1020.25299

0.0468748476

0.1545970887

1020.51099

0.061838154

0.1547617727

1020.78003

0.0551453826

0.1549264567

1021.03802

0.046951191

0.1550705552

1021.302

0.0518117208

0.1551940682

1021.57202

0.0621435276

0.1553175812

1021.82599

0.0771577296

0.1554410942

1022.09302

0.046442235

0.1555646071

1022.35303

0.0545346354

0.1556675346

1022.61603

0.072653469

0.1557704621

1022.875

0.0531095586

0.1558528041

1023.14301

0.060438525

0.1559557316

1023.40503

0.0462132048

0.1560586591

1023.66803

0.053058663

0.1561410011

1023.93799

0.0195693582

0.1562439286

1024.19995

0.0563159814

0.1563468561

1024.45996

0.0519389598

0.1564497835

1024.73499

0.0823490808

0.156552711

1025

0.0530841108

0.1566556385

1025.26794

0.0461623092

0.156758566

1025.521

0.053058663

0.1568614935

1025.78699

0.0848175174

0.1569438355

1026.05896

0.071126601

0.1570261775

1026.31995

0.0438465594

0.1571085195

1026.57996

0.052931424

0.1571908615

1026.85205

0.0670295052

0.157252618

1027.10498

0.0438720072

0.1573143745

1027.375

0.0604894206

0.1573555455

1027.63501

0.064382934

0.1574173019

1027.89905

0.0501067182

0.1574584729

1028.16895

0.0520661988

0.1575202294

1028.422

0.0304355688

0.1576025714

1028.68298

0.0521170944

0.1576643279

1028.94495

0.0562650858

0.1577672554

1029.20996

0.0645865164

0.1578701829

1029.474

0.0649173378

0.1580142814

1029.73499

0.0566976984

0.1581583799

1029.99402

0.0578682972

0.1583230639

1030.27002

0.0510991824

0.1585083333

1030.53296

0.0487070892

0.1587141883

1030.79602

0.0459841746

0.1589406288

1031.06396

0.0373573704

0.1591464838

1031.32202

0.0553744128

0.1593729242

1031.59094

0.0537966492

0.1596199502

1031.84802

0.066927714

0.1598463907

1032.11804

0.0332602746

0.1600728312

1032.37805

0.0404874498

0.1602786861

1032.63306

0.063873978

0.1604845411

1032.91199

0.0618890496

0.1606903961

1033.16895

0.0503357484

0.1608756656

1033.43201

0.0555270996

0.1610609351

1033.69104

0.05471277

0.161225619

1033.95703

0.0571557588

0.161390303

1034.21899

0.0583263576

0.161554987

1034.48901

0.0415817052

0.161719671

1034.74902

0.0569012808

0.1618637695

1035.01794

0.0561887424

0.1620284535

1035.28101

0.1068553122

0.1621931374

1035.55798

0.0668513706

0.1623578214

1035.81799

0.0439992462

0.1625225054

1036.08496

0.0434648424

0.1626871894

1036.33997

0.0645356208

0.1628518734

1036.61096

0.0556797864

0.1630165574

1036.86902

0.0514808994

0.1631812413

1037.13098

0.0390878208

0.1633459253

1037.396

0.054967248

0.1634900238

1037.66296

0.0343036344

0.1636341223

1037.92004

0.0574611324

0.1637782208

1038.18506

-0.0068963538

0.1639223193

1038.44397

0.0391641642

0.1640458323

1038.71301

0.0776412378

0.1641693452

1038.97803

0.0398003592

0.1642722727

1039.23706

0.0977958954

0.1643546147

1039.50305

0.074562054

0.1644575422

1039.76294

0.0003308214

0.1645398842

1040.03101

0.0969815658

0.1646016407

1040.29602

0.0597514344

0.1646633972

1040.56201

0.0740785458

0.1647251537

1040.82605

0.068200104

0.1647869102

1041.08801

0.0727552602

0.1648486667

1041.36304

0.06616428

0.1648898377

1041.61304

0.0713301834

0.1649310087

1041.88696

0.0548654568

0.1649721797

1042.15503

0.0780738504

0.1650133506

1042.41602

0.046951191

0.1650545216

1042.68005

0.0845375916

0.1651162781

1042.94397

0.06743667

0.1651574491

1043.20703

0.0642047994

0.1652192056

1043.46704

0.0576901626

0.1653015476

1043.72498

0.0331075878

0.1653838896

1043.98706

0.0476637294

0.1654662316

1044.245

0.0490888062

0.1655691591

1044.50696

0.0223686162

0.1656720866

1044.76904

0.059293374

0.1657955996

1045.03796

0.0319115412

0.1659396981

1045.29797

0.0568249374

0.166063211

1045.56494

0.0240990666

0.1662073095

1045.82898

0.0623725578

0.166351408

1046.09802

0.0488088804

0.166516092

1046.35803

0.0513027648

0.1666601905

1046.62305

0.029392209

0.166804289

1046.88794

0.0480199986

0.1669689729

1047.15503

0.0355505766

0.1671130714

1047.41699

0.0455006664

0.1672571699

1047.677

0.0548909046

0.1673806829

1047.93701

0.0703886148

0.1675247814

1048.20105

0.023030259

0.1676482944

1048.46899

0.0389860296

0.1677718074

1048.72302

0.0492923886

0.1678953203

1048.99097

0.0656298762

0.1680188333

1049.25403

0.0508701522

0.1681217608

1049.52502

0.0599550168

0.1682452738

1049.79199

0.0636958434

0.1683687868

1050.06104

0.0635686044

0.1684922998

1050.31799

0.0505393308

0.1686158128

1050.58105

0.0507429132

0.1687393258

1050.84595

0.0788627322

0.1688834242

1051.10999

0.0606675552

0.1690069372

1051.375

0.052549707

0.1691510357

1051.63403

0.0541529184

0.1692745487

1051.90002

0.0137163642

0.1694186472

1052.14905

0.057766506

0.1695627457

1052.40796

0.0287051184

0.1697068442

1052.672

0.083723262

0.1698509426

1052.93005

0.0608965854

0.1699744556

1053.20105

0.0665968926

0.1700979686

1053.46802

0.0490633584

0.1702008961

1053.73401

0.0493432842

0.1703038236

1054

0.0500558226

0.1703861656

1054.255

0.0304610166

0.1704685076

1054.52405

0.0545600832

0.1705508496

1054.78503

0.09161208

0.1706126061

1055.04895

0.0651718158

0.1706743626

1055.30798

0.0510482868

0.170736119

1055.57104

0.035881398

0.1707978755

1055.83398

0.0667495794

0.1708802175

1056.09497

0.0422179002

0.170941974

1056.35901

0.0417089442

0.171024316

1056.63

0.0754781748

0.171106658

1056.89502

0.0176098776

0.171189

1057.15295

0.0424723782

0.1712919275

1057.422

0.1116394986

0.171394855

1057.68506

0.093775143

0.171518368

1057.93994

0.082959828

0.171641881

1058.20605

0.050132166

0.1717448084

1058.46594

0.0465949218

0.1718683214

1058.73499

0.064764651

0.1719918344

1058.99805

0.1016385132

0.1721153474

1059.26001

0.0312498984

0.1722388604

1059.52405

0.046187757

0.1723417879

1059.78503

0.0638994258

0.1724447154

1060.04895

0.0659352498

0.1725476429

1060.31799

0.1062700128

0.1726505703

1060.58203

0.0789645234

0.1727329123

1060.83801

0.0472820124

0.1728152543

1061.11206

0.029137731

0.1728770108

1061.37305

0.026083995

0.1729387673

1061.64001

0.0277126542

0.1730005238

1061.896

0.0320133324

0.1730416948

1062.15906

0.0462895482

0.1730828658

1062.42798

0.052549707

0.1731240368

1062.68604

0.0546109788

0.1731446223

1062.95105

0.0714574224

0.1731857933

1063.21301

0.058148223

0.1732269643

1063.48303

0.0572321022

0.1732681353

1063.74402

0.0559088166

0.1733298918

1064.00903

0.1064226996

0.1733916483

1064.26794

0.0471802212

0.1734945758

1064.53296

0.0751219056

0.1735975032

1064.80603

0.0984320904

0.1737416017

1065.07397

0.0672839832

0.1739062857

1065.32104

0.0596241954

0.1741121407

1065.58203

0.099500898

0.1743385812

1065.84399

0.0476637294

0.1745856071

1066.12097

0.0958873104

0.1748738041

1066.38

0.0719154828

0.1751825866

1066.65002

0.0325986318

0.175491369

1066.91394

0.0669022662

0.175820737

1067.172

0.0333620658

0.176150105

1067.43896

0.049495971

0.1764588874

1067.68896

0.0396731202

0.1767676699

1067.96594

0.0806186304

0.1770764524

1068.22705

0.1231164564

0.1773440639

1068.48596

0.054458292

0.1775910898

1068.74902

0.0891181956

0.1777969448

1069.01904

0.0901361076

0.1779822143

1069.28296

0.0408691668

0.1781468983

1069.54395

0.0089321778

0.1782704113

1069.81201

0.0559597122

0.1783527532

1070.073

0.046187757

0.1784350952

1070.33997

0.046187757

0.1784762662

1070.604

0.0220632426

0.1784968517

1070.87305

0.0649427856

0.1784968517

1071.12903

0.0281452668

0.1784762662

1071.39404

0.0607184508

0.1784556807

1071.66504

0.0290613876

0.1784350952

1071.927

0.0593697174

0.1784145097

1072.18994

0.0565195638

0.1783733387

1072.44604

0.0616091238

0.1783527532

1072.703

0.0631614396

0.1783115823

1072.974

0.076597878

0.1782909968

1073.23901

0.065909802

0.1782498258

1073.50403

0.0552471738

0.1782498258

1073.76904

0.0292904178

0.1782292403

1074.02795

0.0761143698

0.1782292403

1074.30005

0.0790917624

0.1782498258

1074.55298

0.0524988114

0.1782498258

1074.82104

0.0547382178

0.1782909968

1075.07898

0.073416903

0.1783321677

1075.354

0.0802623612

0.1783939242

1075.604

0.072653469

0.1784762662

1075.86096

0.1065499386

0.1785791937

1076.12305

0.0559088166

0.1786821212

1076.38794

0.0757581006

0.1787850487

1076.65503

0.0618127062

0.1789085617

1076.91699

0.055348965

0.1790526602

1077.18506

0.0706430928

0.1791761732

1077.448

0.0815856468

0.1793202716

1077.70801

0.056494116

0.1794643701

1077.97498

0.0704140626

0.1796290541

1078.23401

0.0477400728

0.1797731526

1078.49597

0.0607947942

0.1799378366

1078.76196

0.062983305

0.1801231061

1079.02502

0.043642977

0.18028779

1079.28796

0.0759107874

0.1804730595

1079.55396

0.0369247578

0.1806789145

1079.81396

0.0363394584

0.180905355

1080.07898

0.049241493

0.1811317955

1080.33801

0.04962321

0.1813788214

1080.604

0.0339982608

0.1816258474

1080.86401

0.033845574

0.1818934589

1081.12695

0.0567231462

0.1821610703

1081.39905

0.0137163642

0.1824286818

1081.65906

0.0502339572

0.1826962933

1081.91699

0.0799824354

0.1829639048

1082.18396

0.100009854

0.1831903452

1082.44104

0.0410218536

0.1834167857

1082.71204

0.068581821

0.1836226407

1082.97205

0.0940550688

0.1837873247

1083.23596

0.0266947422

0.1839314232

1083.50403

0.0636703956

0.1840549361

1083.76501

0.0946912638

0.1841784491

1084.02405

0.0778448202

0.1842607911

1084.29895

0.058784418

0.1843431331

1084.55896

0.036008637

0.1844048896

1084.80798

0.0535421712

0.1844666461

1085.08105

0.0700577934

0.1845284026

1085.34705

0.0815093034

0.1845901591

1085.60303

0.0436938726

0.1846519156

1085.86304

0.054203814

0.1847342576

1086.14001

0.0705921972

0.1847960141

1086.39795

0.0849702042

0.1848577706

1086.66199

0.0784555674

0.1849401126

1086.927

0.0920955882

0.185001869

1087.19104

0.1159656246

0.18504304

1087.45898

0.0608711376

0.1851047965

1087.72705

0.0782265372

0.1851459675

1087.98303

0.0850974432

0.185166553

1088.24194

0.049750449

0.1851871385

1088.50806

0.0487070892

0.185207724

1088.77002

0.0433630512

0.185207724

1089.03796

0.0644338296

0.1851871385

1089.29797

0.052295229

0.1851871385

1089.56396

0.0674112222

0.1851871385

1089.82605

0.0619144974

0.1851871385

1090.10095

0.0867006546

0.1851871385

1090.36304

0.0934443216

0.1851871385

1090.62305

0.0459587268

0.185207724

1090.88196

0.0426505128

0.1852283095

1091.14099

0.0934188738

0.185248895

1091.40198

0.111206886

0.185290066

1091.66504

0.0269237724

0.1853518225

1091.93896

0.0719409306

0.1853929935

1092.18604

0.0912049152

0.18545475

1092.45898

0.061710915

0.1855165065

1092.73303

0.0684291342

0.1855988485

1093

0.0234374238

0.1856811905

1093.26794

0.0712283922

0.1857635325

1093.53003

0.0287051184

0.18586646

1093.78699

0.0575374758

0.1859899729

1094.05505

0.0705413016

0.1861134859

1094.31104

0.0589625526

0.1862575844

1094.57605

0.092375514

0.1864016829

1094.83606

0.036390354

0.1865869524

1095.09998

0.0378408786

0.1867722219

1095.36902

0.1029617988

0.1869780768

1095.63

0.0859117728

0.1872045173

1095.89197

0.0496486578

0.1874309578

1096.16797

0.0785319108

0.1876779838

1096.42297

0.0361613238

0.1879044242

1096.68896

0.0503103006

0.1881514502

1096.94897

0.0669022662

0.1883778907

1097.22205

0.0767505648

0.1886043312

1097.48206

0.0672839832

0.1888101861

1097.75098

0.051404556

0.1889748701

1098.02002

0.0728570514

0.1891395541

1098.27197

0.0768269082

0.1892630671

1098.54004

0.0235646628

0.1893454091

1098.80896

0.0435920814

0.1894071656

1099.06494

0.0500812704

0.1894483366

1099.33704

0.0579700884

0.1894689221

1099.59595

0.0382225956

0.1894689221

1099.86902

0.0551708304

0.1894277511

1100.12695

0.0583518054

0.1894071656

1100.39099

0.0647900988

0.1893659946

1100.65601

0.0828834846

0.1893248236

1100.91699

0.0513282126

0.1892836526

1101.18994

0.0690144336

0.1892630671

1101.45703

0.0620162886

0.1892424816

1101.72302

0.0673857744

0.1892424816

1101.98999

0.064255695

0.1892630671

1102.25403

0.050259405

0.1893042381

1102.51294

0.0617363628

0.1893454091

1102.78198

0.0639757692

0.1894071656

1103.04297

0.0652990548

0.1895100931

1103.30505

0.072017274

0.1896130206

1103.56897

0.0592424784

0.1897159481

1103.82996

0.0703122714

0.1898600465

1104.09705

0.067054953

0.190004145

1104.35803

0.0659861454

0.1901482435

1104.62903

0.0585808356

0.190292342

1104.88403

0.0730860816

0.1904364405

1105.15002

0.0702868236

0.190580539

1105.41003

0.0734423508

0.1907246374

1105.68005

0.068200104

0.1908481504

1105.94897

0.0661388322

0.1909716634

1106.20801

0.0686072688

0.1910745909

1106.46802

0.0725007822

0.1911569329

1106.74194

0.0698033154

0.1912186894

1107.01294

0.068581821

0.1912598604

1107.27502

0.0675130134

0.1912804459

1107.54395

0.0686836122

0.1912804459

1107.80896

0.06616428

0.1912804459

1108.06995

0.066291519

0.1912598604

1108.33496

0.0703122714

0.1912186894

1108.59705

0.0671058486

0.1911775184

1108.86206

0.0691162248

0.1911363474

1109.12402

0.0660624888

0.1910951764

1109.38501

0.0700323456

0.1910334199

1109.65002

0.0701595846

0.1909922489

1109.91199

0.0688617468

0.1909716634

1110.177

0.0656807718

0.1909304924

1110.44299

0.0732133206

0.1909099069

1110.70496

0.0716101092

0.1909099069

1110.97302

0.0679201782

0.1909099069

1111.23999

0.068200104

0.1909099069

1111.50696

0.0678438348

0.1909510779

1111.77405

0.073162425

0.1909716634

1112.03699

0.0747656364

0.1910334199

1112.302

0.06870906

0.1910951764

1112.57605

0.0681492084

0.1911569329

1112.83301

0.0739513068

0.1912392749

1113.09705

0.0672839832

0.1913216169

1113.36401

0.0701595846

0.1914039589

1113.62402

0.0677929392

0.1915068864

1113.88904

0.0698287632

0.1915892284

1114.15601

0.0730860816

0.1916921558

1114.41895

0.0713047356

0.1917950833

1114.68005

0.0731369772

0.1918774253

1114.95496

0.0602858382

0.1919597673

1115.203

0.0722208564

0.1920421093

1115.47498

0.0745111584

0.1921244513

1115.73901

0.0666477882

0.1921862078

1116.005

0.0686581644

0.1922685498

1116.276

0.0658589064

0.1923097208

1116.53601

0.0736204854

0.1923714773

1116.80701

0.0688108512

0.1924332338

1117.06995

0.0660624888

0.1924744048

1117.328

0.0634668132

0.1925361613

1117.59802

0.0672076398

0.1925979177

1117.86401

0.0730097382

0.1926596742

1118.12695

0.0676657002

0.1927214307

1118.38306

0.0711774966

0.1927831872

1118.65002

0.0615073326

0.1928449437

1118.91699

0.066545997

0.1929272857

1119.17603

0.0613037502

0.1930096277

1119.44104

0.0671567442

0.1930919697

1119.70605

0.0694979418

0.1931537262

1119.97095

0.0714065268

0.1932566537

1120.23901

0.0732133206

0.1933389957

1120.505

0.06743667

0.1934213377

1120.77502

0.0734423508

0.1935242652

1121.04102

0.0620417364

0.1936066071

1121.29895

0.0745111584

0.1937095346

1121.55603

0.0626779314

0.1938124621

1121.81995

0.0725516778

0.1939153896

1122.08997

0.0754781748

0.1940183171

1122.34302

0.0750201144

0.1941212446

1122.61597

0.071508318

0.1942241721

1122.87903

0.0695488374

0.1943476851

1123.14099

0.0744602628

0.1944506126

1123.39905

0.0694215984

0.19455354

1123.67102

0.0724244388

0.1946564675

1123.93005

0.069090777

0.194759395

1124.19495

0.0763434

0.1948623225

1124.46301

0.0711520488

0.1949446645

1124.72302

0.0730097382

0.1950270065

1124.99194

0.0712283922

0.1951093485

1125.26001

0.0672585354

0.1951916905

1125.521

0.0705921972

0.195253447

1125.78503

0.0700323456

0.1953152035

1126.05005

0.0660115932

0.19537696

1126.32703

0.0714065268

0.1954387165

1126.58606

0.0683527908

0.1954798874

1126.84302

0.069345255

0.1955210584

1127.10999

0.0650445768

0.1955416439

1127.37195

0.0726789168

0.1955828149

1127.63696

0.0715846614

0.1956034004

1127.90002

0.0674621178

0.1956239859

1128.16602

0.0671312964

0.1956445714

1128.427

0.0764197434

0.1956445714

1128.69604

0.067182192

0.1956651569

1128.948

0.072144513

0.1956857424

1129.21497

0.0723480954

0.1957063279

1129.474

0.0670040574

0.1957269134

1129.74304

0.0696506286

0.1957680844

1130.00903

0.0705921972

0.1958092554

1130.26697

0.0583009098

0.1958504264

1130.54102

0.0688617468

0.1959121829

1130.80505

0.0704649582

0.1959739394

1131.06396

0.0727043646

0.1960356959

1131.33105

0.07125384

0.1961180379

1131.60303

0.065273607

0.1962003799

1131.85901

0.0757581006

0.1962621364

1132.12402

0.0707957796

0.1963238929

1132.38501

0.0788627322

0.1963856494

1132.65698

0.0784555674

0.1964474058

1132.92297

0.0767760126

0.1964885768

1133.17798

0.065019129

0.1965297478

1133.44104

0.083468784

0.1965709188

1133.70398

0.0653753982

0.1965915043

1133.974

0.0829852758

0.1966326753

1134.23901

0.0717373482

0.1966532608

1134.5

0.0752491446

0.1966738463

1134.76697

0.0747656364

0.1967150173

1135.02795

0.0730860816

0.1967356028

1135.29297

0.0702104802

0.1967561883

1135.56104

0.0766233258

0.1967973593

1135.82703

0.0702868236

0.1968179448

1136.09399

0.0714065268

0.1968591158

1136.35095

0.0680219694

0.1969002868

1136.61096

0.0712792878

0.1969414578

1136.88501

0.0744857106

0.1969826288

1137.146

0.0666477882

0.1970443853

1137.40906

0.0797279574

0.1970855563

1137.67603

0.0766742214

0.1971473128

1137.93103

0.0797279574

0.1972090693

1138.19495

0.0724498866

0.1972502403

1138.46204

0.0678692826

0.1973325823

1138.72705

0.0641030082

0.1973943387

1138.98804

0.064128456

0.1974766807

1139.26001

0.0718136916

0.1975384372

1139.52405

0.072907947

0.1976207792

1139.78894

0.0745366062

0.1977031212

1140.05298

0.0713301834

0.1977854632

1140.31201

0.0745366062

0.1978883907

1140.58496

0.0778193724

0.1979707327

1140.84705

0.066927714

0.1980530747

1141.11304

0.0670040574

0.1981148312

1141.375

0.0746638452

0.1981971732

1141.63696

0.0702868236

0.1982589297

1141.896

0.0689889858

0.1983206861

1142.17004

0.0733151118

0.1983824426

1142.43005

0.0708212274

0.1984236136

1142.69104

0.071635557

0.1984441991

1142.95605

0.072398991

0.1984853701

1143.21497

0.0696506286

0.1984853701

1143.47998

0.07761579

0.1985059556

1143.74902

0.0780738504

0.1985059556

1144.01904

0.076725117

0.1985059556

1144.28003

0.07125384

0.1985265411

1144.54004

0.0746383974

0.1985265411

1144.80798

0.079142658

0.1985471266

1145.07703

0.0761143698

0.1985677121

1145.33606

0.0748928754

0.1986088831

1145.59802

0.0896017038

0.1986706396

1145.86902

0.0771322818

0.1987529816

1146.12402

0.074816532

0.1988353236

1146.39697

0.0730097382

0.1989588366

1146.66003

0.0653245026

0.1990617641

1146.92395

0.0791681058

0.1991852771

1147.18896

0.0789899712

0.1993293755

1147.45105

0.083850501

0.1994528885

1147.71594

0.0634413654

0.199596987

1147.97498

0.063110544

0.1997205

1148.23706

0.0692434638

0.1998234275

1148.51501

0.085122891

0.199926355

1148.77502

0.0757326528

0.200008697

1149.04199

0.0747910842

0.200091039

1149.30298

0.0832906494

0.20013221

1149.56494

0.0766996692

0.2001527955

1149.83704

0.0805168392

0.200173381

1150.09595

0.080796765

0.200173381

1150.37

0.081814677

0.2001527955

1150.63403

0.08397774

0.2001116245

1150.89099

0.078251985

0.200091039

1151.16003

0.0797279574

0.2000704535

1151.42004

0.073416903

0.2000292825

1151.68799

0.0764197434

0.200008697

1151.95105

0.0742821282

0.199967526

1152.20898

0.0792953448

0.1999469405

1152.48096

0.0850210998

0.1999469405

1152.74597

0.0797534052

0.1999469405

1153.00903

0.0714828702

0.1999469405

1153.26904

0.0751219056

0.199967526

1153.53894

0.0839013966

0.200008697

1153.80603

0.0785319108

0.200049868

1154.06494

0.0799315398

0.200091039

1154.33606

0.080796765

0.2001527955

1154.59094

0.0728061558

0.2002351374

1154.86401

0.0776921334

0.2002968939

1155.12195

0.0784810152

0.2003998214

1155.39001

0.0771322818

0.2004821634

1155.65698

0.0766487736

0.2005850909

1155.92004

0.0752491446

0.2006880184

1156.17798

0.0668513706

0.2007909459

1156.44202

0.0653753982

0.2008938734

1156.69995

0.071890035

0.2010173864

1156.95703

0.075452727

0.2011203139

1157.22205

0.0804659436

0.2012438268

1157.48303

0.0682255518

0.2013467543

1157.74805

0.0755545182

0.2014496818

1158.01196

0.0778448202

0.2015526093

1158.28699

0.0878203578

0.2016349513

1158.552

0.0825272154

0.2017172933

1158.81201

0.0794225838

0.2017996353

1159.07996

0.0800078832

0.2018613918

1159.34094

0.0754018314

0.2019025628

1159.61304

0.0742566804

0.2019643193

1159.86902

0.0825017676

0.2020054903

1160.13306

0.0721954086

0.2020466613

1160.40295

0.0739767546

0.2020878323

1160.67004

0.0792953448

0.2021290032

1160.92297

0.0727298124

0.2021701742

1161.19104

0.074307576

0.2022113452

1161.45703

0.0762416088

0.2022731017

1161.71899

0.0837741576

0.2023554437

1161.98303

0.0791681058

0.2024377857

1162.25

0.0805168392

0.2025407132

1162.50806

0.0878458056

0.2026436407

1162.77795

0.0748419798

0.2027671537

1163.04504

0.0797025096

0.2028906667

1163.30896

0.0756563094

0.2030141797

1163.57703

0.0827307978

0.2031376926

1163.84595

0.0713301834

0.2032817911

1164.11597

0.076470639

0.2034053041

1164.37305

0.0850210998

0.2035288171

1164.63599

0.0727043646

0.2036523301

1164.89795

0.0807713172

0.2037758431

1165.16296

0.0788627322

0.2038787706

1165.42896

0.0839522922

0.2039611126

1165.69702

0.0738749634

0.2040434545

1165.96204

0.0764197434

0.204105211

1166.22205

0.082323633

0.2041669675

1166.48401

0.0819164682

0.2042081385

1166.76099

0.0851737866

0.2042493095

1167.02295

0.0729842904

0.204269895

1167.28601

0.0797025096

0.204269895

1167.55396

0.0815347512

0.204269895

1167.81494

0.0751473534

0.2042493095

1168.08606

0.0809494518

0.2042081385

1168.34497

0.0808222128

0.2041669675

1168.60901

0.0801351222

0.2041257965

1168.88098

0.0792190014

0.2040846255

1169.146

0.0745366062

0.204022869

1169.41101

0.0775648944

0.2039816981

1169.68005

0.0800587788

0.2039199416

1169.94397

0.0861153552

0.2038581851

1170.20105

0.0737222766

0.2037964286

1170.46497

0.0792444492

0.2037346721

1170.73401

0.0766996692

0.2036935011

1170.99097

0.08270535

0.2036523301

1171.26001

0.0789645234

0.2036111591

1171.52405

0.0737222766

0.2035905736

1171.78699

0.0766233258

0.2035699881

1172.06104

0.0778448202

0.2035699881

1172.32202

0.0860390118

0.2035699881

1172.58496

0.0880748358

0.2035905736

1172.84998

0.0759362352

0.2036111591

1173.11597

0.0864970722

0.2036523301

1173.38501

0.081687438

0.2037140866

1173.64697

0.0858099816

0.2037964286

1173.91797

0.0800842266

0.2038993561

1174.18396

0.0846902784

0.2040022835

1174.44604

0.073671381

0.2041669675

1174.71497

0.0796261662

0.2043316515

1174.97803

0.0722463042

0.2045375065

1175.24597

0.085886325

0.204805118

1175.50598

0.0803387046

0.2050933149

1175.77502

0.0828834846

0.2054432684

1176.04102

0.087540432

0.2058549784

1176.29504

0.0819673638

0.2063284448

1176.56104

0.0873877452

0.2068430823

1176.81104

0.0812802732

0.2074606472

1177.08704

0.0745875018

0.2081399686

1177.34204

0.0805168392

0.2088810465

1177.61401

0.0871332672

0.2097044665

1177.88196

0.0848938608

0.2105896429

1178.14905

0.0812802732

0.2115571613

1178.41699

0.0760380264

0.2125658506

1178.69604

0.0789390756

0.213656882

1178.96106

0.0802369134

0.2147684989

1179.22705

0.0848175174

0.2159418723

1179.48303

0.0822981852

0.2171358312

1179.745

0.0845375916

0.2183503755

1180.00806

0.086776998

0.2195855054

1180.28003

0.0789899712

0.2208206353

1180.54102

0.0837996054

0.2220557652

1180.80505

0.0813820644

0.223290895

1181.06494

0.0804913914

0.2244848539

1181.276

0.0870823716

0.2256788128

1188.40698

0.089321778

0.2268316006

1192.70996

0.0924009618

0.227963803

1195.32605

0.095302011

0.2290754199

1197.02295

0.097719552

0.2301458658

1198.23303

0.1007223924

0.2311957262

1199.11694

0.1039288152

0.2322455866

1199.81201

0.1051248618

0.233254276

1200.36401

0.1092728532

0.2342423799

1200.80896

0.111334125

0.2352304838

1201.18701

0.1116394986

0.2362185877

1201.49902

0.115151295

0.2372066916

1201.75598

0.1169071932

0.2381947955

1201.98901

0.1184849568

0.2391828994

1202.17603

0.1222257834

0.2401710032

1202.34595

0.1239053382

0.2411796926

1202.49695

0.1257375798

0.242188382

1202.62805

0.1261956402

0.2432176569

1202.73901

0.1279515384

0.2442469318

1202.82202

0.1303945272

0.2452762067

1202.89795

0.1329138594

0.2463054816

1202.97998

0.1330410984

0.2473347565

1203.05603

0.1344152796

0.2483434459

1203.13

0.1377489414

0.2493521353

1203.19299

0.138308793

0.2503402392

1203.22803

0.140726334

0.2513077576

1203.24597

0.141617007

0.252275276

1203.29199

0.1441872348

0.2532016234

1203.33203

0.1453323858

0.2541279708

1203.36694

0.1453578336

0.2550131472

1203.40698

0.1459176852

0.2558983236

1203.42603

0.1477753746

0.2567629145

1203.453

0.1480044048

0.2576275054

1203.48499

0.1494803772

0.2584715108

1203.51001

0.1518215748

0.2592949307

1203.51294

0.1532975472

0.2601183506

1203.51501

0.1549262064

0.2609417706

1203.53406

0.1556641926

0.2617651905

1203.51404

0.1564530744

0.2625886104

1203.51099

0.1582089726

0.2634120303

1203.52405

0.1581071814

0.2642354502

1203.53406

0.1603974834

0.2650588701

1203.552

0.1618989036

0.2659028755

1203.54395

0.1609827828

0.2667262955

1203.55298

0.1622806206

0.2675703009

1203.57703

0.1656906258

0.2684143063

1203.57104

0.1647236094

0.2692788972

1203.55896

0.1665304032

0.2701434881

1203.55701

0.1665812988

0.271008079

1203.54797

0.1686425706

0.2718726699

1203.54199

0.1679300322

0.2727372608

1203.53796

0.1700167518

0.2736224372

1203.53601

0.1722561582

0.2745076136

1203.52698

0.1726887708

0.27539279

1203.51599

0.1767858666

0.2762985519

1203.54102

0.1751826552

0.2771837284

1203.55005

0.1768113144

0.2780689048

1203.547

0.1780328088

0.2789540812

1203.55396

0.1780328088

0.2798598431

1203.53296

0.1824352782

0.280724434

1203.55396

0.180933858

0.2816096104

1203.55103

0.1822571436

0.2824947868

1203.55396

0.1847001324

0.2833593777

1203.56799

0.1815446052

0.2842239686

1203.57202

0.1808320668

0.285067974

1203.578

0.1859979702

0.2859325649

1203.56897

0.186150657

0.2867559848

1203.54504

0.18831372

0.2875999903

1203.53198

0.1880846898

0.2884439957

1203.54102

0.1900441704

0.2892674156

1203.52905

0.1916728296

0.2900908355

1203.53699

0.19213089

0.2909142554

1203.52905

0.1948538046

0.2917376753

1203.54602

0.1943194008

0.2925405097

1203.54504

0.1957190298

0.2933433442

1203.52502

0.196711494

0.2941461786

1203.5

0.1971950022

0.294949013

1203.47803

0.1976530626

0.2957312619

1203.47705

0.1998415734

0.2964929253

1203.49304

0.201164859

0.2972751742

1203.49304

0.2019537408

0.2980368377

1203.47498

0.2046512076

0.2987779156

1203.44495

0.204218595

0.2995189935

1203.42102

0.2049565812

0.3002394859

1203.40906

0.2064325536

0.3009599784

1203.41394

0.2067124794

0.3016804708

1203.41101

0.2064834492

0.3024009632

1203.41101

0.2069160618

0.3031008701

1203.43298

0.209053677

0.3038007771

1203.41504

0.2090282292

0.304500684

1203.39197

0.2096389764

0.3052005909

1203.396

0.2095117374

0.3059210833

1203.41394

0.2096135286

0.3066209903

1203.41895

0.2115475614

0.3073208972

1203.40906

0.2131507728

0.3080413896

1203.38403

0.2145758496

0.308761882

1203.38098

0.2132016684

0.3094823745

1203.38306

0.2155174182

0.3102028669

1203.38196

0.2151102534

0.3109233593

1203.37195

0.2160009264

0.3116438517

1203.349

0.2175023466

0.3123643442

1203.33398

0.2168915994

0.3130848366

1203.33301

0.2187747366

0.313805329

1203.32605

0.2167389126

0.3145258214

1203.33398

0.2195381706

0.3152257284

1203.33704

0.22012347

0.3159256353

1203.32397

0.2211668298

0.3166049567

1203.31299

0.2239151922

0.3173048636

1203.29895

0.2237116098

0.3179841851

1203.30298

0.2265363156

0.318642921

1203.30603

0.2255692992

0.3193016569

1203.29504

0.2261545986

0.3199603929

1203.28796

0.2283431094

0.3206191288

1203.271

0.229539156

0.3212778647

1203.26294

0.2235334752

0.3219160152

1203.26294

0.2242205658

0.3225747511

1203.25903

0.2278596012

0.323233487

1203.26001

0.2287502742

0.3238922229

1203.27295

0.2307352026

0.3245715444

1203.25696

0.2284194528

0.3252508658

1203.25195

0.2297172906

0.3259507727

1203.23999

0.2307352026

0.3266506797

1203.23303

0.2368172268

0.3273711721

1203.22498

0.2322366228

0.3280916645

1203.21301

0.236791779

0.3288121569

1203.20203

0.2345778204

0.3295326494

1203.20496

0.2349340896

0.3302737273

1203.21704

0.2367663312

0.3309942197

1203.22498

0.2362573752

0.3317147121

1203.20898

0.2386494684

0.332414619

1203.20801

0.2384967816

0.3330939405

1203.20398

0.239718276

0.3337526764

1203.18896

0.240863427

0.3344114123

1203.20496

0.2423139516

0.3350289773

1203.20105

0.2411433528

0.3356259567

1203.20203

0.2436372372

0.3362023506

1203.17798

0.2429246988

0.3367581591

1203.18604

0.246334704

0.337293382

1203.19897

0.2438153718

0.337828605

1203.21497

0.2462838084

0.3383432424

1203.21204

0.246080226

0.3388578799

1203.20801

0.2480651544

0.3393725173

1203.19897

0.2489303796

0.3398871548

1203.18396

0.2484468714

0.3404223777

1203.17297

0.2489812752

0.3409576006

1203.15198

0.2520095634

0.3415134091

1203.13599

0.2507626212

0.342089803

1203.12097

0.2515260552

0.342666197

1203.10901

0.2497956048

0.3432425909

1203.12

0.2511952338

0.3438395703

1203.12097

0.2526203106

0.3444365498

1203.12805

0.2517041898

0.3450335292

1203.13306

0.2541217308

0.3456099232

1203.10596

0.253714566

0.3462069026

1203.08899

0.2541726264

0.3467832965

1203.07996

0.2544525522

0.347339105

1203.10303

0.25575039

0.3478743279

1203.12305

0.2578625574

0.3484095509

1203.10596

0.260712711

0.3489241883

1203.09802

0.2586259914

0.3494182403

1203.08704

0.2568191976

0.3498917067

1203.10706

0.2617051752

0.3503651732

1203.12195

0.2606872632

0.3508180541

1203.10596

0.2607381588

0.3512709351

1203.073

0.2587277826

0.3517032305

1203.07703

0.260458233

0.3521561115

1203.08301

0.263130252

0.3525884069

1203.08606

0.2639191338

0.3530207024

1203.08105

0.2642499552

0.3534529978

1203.073

0.2646825678

0.3538852933

1203.06702

0.2625195048

0.3543381742

1203.06494

0.2650897326

0.3547704697

1203.06201

0.2653442106

0.3552233506

1203.05396

0.2658786144

0.3556968171

1203.04102

0.2658277188

0.3561702835

1203.03198

0.266947422

0.35664375

1203.04395

0.2673036912

0.3571378019

1203.03101

0.2665402572

0.3576318539

1203.04004

0.2673545868

0.3581464913

1203.02698

0.2692122762

0.3586611288

1203.02698

0.268856007

0.3591963517

1203.04102

0.2693904108

0.3597315747

1203.05603

0.2699502624

0.3602667976

1203.05298

0.2709936222

0.3608020206

1203.04797

0.2708663832

0.361357829

1203.02502

0.2733857154

0.3619136374

1203.00903

0.2730294462

0.3624694459

1203.02405

0.2724695946

0.3630046688

1203.02502

0.273054894

0.3635810628

1203.00696

0.272673177

0.3641368712

1202.99805

0.273691089

0.3647132652

1203

0.2732584764

0.3652896591

1203.00598

0.2748616878

0.365866053

1202.995

0.275345196

0.3664630325

1202.97095

0.2766684816

0.3670600119

1202.97302

0.275981391

0.3676775768

1202.96106

0.2778645282

0.3683157273

1202.96802

0.2762613168

0.3689538777

1202.98499

0.2788060968

0.3695920281

1202.97705

0.2785770666

0.3702301786

1202.97205

0.2794931874

0.3708889145

1202.96899

0.280307517

0.3715270649

1202.98596

0.2799512478

0.3721446299

1202.98096

0.280816473

0.3727621948

1202.95398

0.2799258

0.3733591742

1202.92102

0.2807910252

0.3739355682

1202.88904

0.2808673686

0.3744913766

1202.87903

0.281834385

0.3750060141

1202.89001

0.2812490856

0.375500066

1202.89404

0.2818089372

0.3759735325

1202.89404

0.2828014014

0.3764058279

1202.91101

0.2845318518

0.3768175379

1202.93799

0.2844300606

0.3772086623

1202.92505

0.2839211046

0.3775997868

1202.91394

0.2861350632

0.3779497403

1202.91394

0.2848626732

0.3782996937

1202.89697

0.2853461814

0.3786496472

1202.896

0.2868221538

0.3789996006

1202.90796

0.2872038708

0.3793495541

1202.91296

0.2882726784

0.3797200931

1202.92505

0.2856770028

0.380090632

1202.91895

0.2858042418

0.3804817565

1202.91101

0.2865931236

0.3808934665

1202.90295

0.2882981262

0.3813051764

1202.896

0.288450813

0.3817580574

1202.87695

0.2879927526

0.3822109383

1202.86902

0.2889088734

0.3826844048

1202.87097

0.2895705162

0.3831578712

1202.87305

0.2903339502

0.3836519232

1202.89001

0.289595964

0.3841253896

1202.90198

0.2912755188

0.3846194416

1202.89294

0.2910464886

0.3851134935

1202.88306

0.291886266

0.38558696

1202.89905

0.2904611892

0.3860604264

1202.87305

0.2914027578

0.3865338929

1202.86694

0.2929296258

0.3869867738

1202.87695

0.2933622384

0.3874396548

1202.896

0.2936167164

0.3878719502

1202.901

0.295576197

0.3883042457

1202.89502

0.2952199278

0.3887365411

1202.88501

0.295067241

0.3891894221

1202.88696

0.2966704524

0.3896217175

1202.89294

0.2958561228

0.390054013

1202.89001

0.2971794084

0.3905068939

1202.87805

0.2972811996

0.3909391894

1202.854

0.2974338864

0.3913920703

1202.85205

0.2971794084

0.3918449513

1202.84204

0.2984263506

0.3923184177

1202.83704

0.2972048562

0.3927712987

1202.83301

0.2981464248

0.3932241797

1202.84399

0.2994697104

0.3936564751

1202.84204

0.2973066474

0.3941093561

1202.82104

0.2982736638

0.394521066

1202.81799

0.3000041142

0.3949533615

1202.83203

0.298375455

0.3953444859

1202.823

0.2981718726

0.3957561959

1202.81104

0.301301952

0.3961267348

1202.80103

0.3008184438

0.3964972738

1202.80603

0.3012510564

0.3968472273

1202.81104

0.3021162816

0.3971971807

1202.81396

0.3027779244

0.3975471342

1202.80103

0.301429191

0.3978765022

1202.80298

0.3020908338

0.3982058701

1202.81299

0.3033886716

0.3985352381

1202.81299

0.3024979986

0.3988646061

1202.81702

0.3054753912

0.399193974

1202.80396

0.3047883006

0.399523342

1202.79199

0.3041775534

0.39985271

1202.80298

0.3055517346

0.4002026634

1202.79199

0.3064424076

0.4005320314

1202.78601

0.3054499434

0.4009025703

1202.79199

0.304864644

0.4012731093

1202.77698

0.3068241246

0.4016436483

1202.77698

0.306518751

0.4020347727

1202.78101

0.3053481522

0.4024464827

1202.79297

0.3058062126

0.4028581926

1202.77698

0.3076130064

0.4032904881

1202.75806

0.3069513636

0.4037227835

1202.745

0.3087327096

0.4041756645

1202.75598

0.307663902

0.404649131

1202.76697

0.3087836052

0.4051225974

1202.78894

0.3100050996

0.4055960639

1202.802

0.3103613688

0.4060901158

1202.78101

0.3106158468

0.4065841677

1202.76404

0.313135179

0.4070782197

1202.76697

0.311099355

0.4075928571

1202.76099

0.3119391324

0.4080869091

1202.73596

0.3116337588

0.408580961

1202.745

0.3133387614

0.4090955985

1202.75903

0.3135677916

0.4095690649

1202.74902

0.312753462

0.4100631169

1202.73999

0.315043764

0.4105365833

1202.71594

0.3138477174

0.4109894643

1202.71802

0.3134660004

0.4114629307

1202.72998

0.3154763766

0.4118952262

1202.72498

0.313262418

0.4123481071

1202.72205

0.3130842834

0.4127804026

1202.72302

0.3134405526

0.4132126981

1202.71899

0.3165451842

0.413624408

1202.72705

0.3166724232

0.4140567035

1202.729

0.315679959

0.4144889989

1202.73206

0.316952349

0.4149212944

1202.74402

0.3171559314

0.4153535898

1202.74902

0.3169777968

0.4158064708

1202.73706

0.31555272

0.4162593517

1202.72595

0.3176648874

0.4167122327

1202.729

0.317079588

0.4171856991

1202.71301

0.3194207856

0.4176591656

1202.68994

0.3200315328

0.418132632

1202.68896

0.3192172032

0.418626684

1202.698

0.320515041

0.4191001504

1202.70398

0.320769519

0.4195942024

1202.70898

0.320896758

0.4200676688

1202.703

0.3217365354

0.4205411353

1202.71301

0.3233906424

0.4210146017

1202.70801

0.3240013896

0.4214674827

1202.698

0.322805343

0.4219203636

1202.70203

0.325350123

0.4223526591

1202.67896

0.3235942248

0.4227849545

1202.65601

0.3237978072

0.4231966645

1202.68604

0.3257827356

0.423587789

1202.70996

0.3258845268

0.4239789134

1202.70203

0.3274877382

0.4243700379

1202.69995

0.3262916916

0.4247611623

1202.67798

0.3278185596

0.4251317013

1202.65405

0.3282002766

0.4255228258

1202.67505

0.3283275156

0.4259139502

1202.68896

0.3265970652

0.4263256602

1202.68896

0.3281239332

0.4267373701

1202.69202

0.3278440074

0.4271696656

1202.69104

0.329421771

0.427643132

1202.67505

0.3299561748

0.4281165985

1202.69397

0.3293199798

0.4286106504

1202.68701

0.3303378918

0.4291458734

1202.70105

0.3313812516

0.4296810963

1202.69702

0.32954901

0.4302574903

1202.698

0.3317884164

0.4308338842

1202.68201

0.3324246114

0.4314308636

1202.65295

0.3317375208

0.4320484286

1202.64795

0.3326790894

0.432686579

1202.64001

0.3310249824

0.4333247294

1202.66003

0.332984463

0.4339628799

1202.68604

0.3321701334

0.4346216158

1202.67603

0.3353765562

0.4352803517

1202.65295

0.3336970014

0.4359390877

1202.64294

0.334129614

0.4365978236

1202.62805

0.335020287

0.4372565595

1202.63098

0.335020287

0.43789471

1202.62805

0.336547155

0.4385328604

1202.62

0.3380485752

0.4391504253

1202.60596

0.3401607426

0.4397474048

1202.62

0.3398808168

0.4403237987

1202.61804

0.3397026822

0.4408796071

1202.62097

0.3402879816

0.4413942446

1202.62195

0.3394482042

0.4418882965

1202.64502

0.339855369

0.4423823485

1202.64294

0.3407205942

0.4428146439

1202.62903

0.3385320834

0.4432469394

1202.625

0.3401607426

0.4436586494

1202.61597

0.3405170118

0.4440497738

1202.61804

0.341636715

0.4444203128

1202.58899

0.3430617918

0.4448114372

1202.599

0.3436470912

0.4451819762

1202.62805

0.3447413466

0.4455731006

1202.63501

0.34736247

0.4459642251

1202.63306

0.3439524648

0.4463759351

1202.64099

0.3440797038

0.4468082305

1202.64404

0.344690451

0.447240526

1202.64404

0.344563212

0.4477139924

1202.646

0.345962841

0.4481874589

1202.651

0.3469298574

0.4487020963

1202.67798

0.3438506736

0.4492167338

1202.67395

0.347107992

0.4497313712

1202.66199

0.3486857556

0.4502665942

1202.646

0.3486857556

0.4508018171

1202.63794

0.347871426

0.45133704

1202.62695

0.3481004562

0.451872263

1202.58997

0.3500599368

0.4524074859

1202.57703

0.3491692638

0.4529427089

1202.57104

0.3500599368

0.4534573463

1202.56604

0.3510269532

0.4539719838

1202.58203

0.3496782198

0.4544866212

1202.59204

0.3507724752

0.4549806732

1202.56702

0.3524774778

0.4554747251

1202.56006

0.3512814312

0.4559481916

1202.58398

0.3518667306

0.4564422435

1202.58997

0.3503907582

0.45691571

1202.57495

0.3500599368

0.4573685909

1202.58801

0.3503144148

0.4578214719

1202.58496

0.3519176262

0.4582743528

1202.59094

0.3517140438

0.4587272338

1202.60303

0.35117964

0.4591801147

1202.62903

0.3515868048

0.4596124102

1202.62195

0.35245203

0.4600447056

1202.61804

0.3535208376

0.4604975866

1202.63306

0.3523502388

0.4609504675

1202.64697

0.353215464

0.4614033485

1202.62305

0.354360615

0.4618768149

1202.58301

0.3551494968

0.4623502814

1202.57104

0.3554294226

0.4628443333

1202.56799

0.3552767358

0.4633589708

1202.59595

0.3545387496

0.4638736082

1202.62695

0.353469942

0.4644088312

1202.58606

0.3560401698

0.4649440541

1202.57397

0.357796068

0.4654998626

1202.57495

0.3584577108

0.466055671

1202.57495

0.3597301008

0.4666114794

1202.57898

0.3599082354

0.4671672879

1202.58899

0.3594247272

0.4677230963

1202.61304

0.359322936

0.4682583193

1202.62

0.3601372656

0.4687935422

1202.62903

0.3591448014

0.4693081797

1202.62695

0.3606716694

0.4698022316

1202.61597

0.3610279386

0.4702756981

1202.59399

0.360213609

0.470728579

1202.57703

0.3614351034

0.47118146

1202.58997

0.3626565978

0.4716137554

1202.60205

0.3630637626

0.4720254654

1202.58899

0.363267345

0.4724371753

1202.58997

0.3637254054

0.4728282998

1202.59204

0.3647433174

0.4732194242

1202.60596

0.3638526444

0.4736105487

1202.62805

0.3643616004

0.4740016732

1202.63306

0.3651504822

0.4743927976

1202.64404

0.3659139162

0.4747633366

1202.62402

0.3661683942

0.4751338755

1202.60999

0.3703418334

0.475525

1202.625

0.3700364598

0.4758749535

1202.61804

0.363012867

0.4762454924

1202.60803

0.3667536936

0.4766160314

1202.58398

0.3669827238

0.4769865703

1202.60706

0.3667791414

0.4773365238

1202.63599

0.367084515

0.4777070628

1202.65601

0.3681533226

0.4780570162

1202.64795

0.3668809326

0.4784275552

1202.61804

0.3679497402

0.4787775087

1202.62

0.369629295

0.4791480476

1202.61304

0.3699346686

0.4795185866

1202.61096

0.3682805616

0.479909711

1202.60095

0.369120339

0.48028025

1202.59802

0.3703163856

0.4806713745

1202.604

0.3711052674

0.4810830844

1202.60803

0.370392729

0.4814742089

1202.60095

0.3703418334

0.4818859188

1202.59802

0.370011012

0.4823182143

1202.604

0.3714869844

0.4827299242

1202.60901

0.3719450448

0.4831622197

1202.62097

0.3717669102

0.4835945152

1202.59094

0.3722758662

0.4840268106

1202.58105

0.3712579542

0.4844591061

1202.56201

0.3725048964

0.4848914015

1202.55896

0.3734210172

0.485323697

1202.55798

0.3727848222

0.4857559924

1202.58496

0.3737263908

0.4861882879

1202.60596

0.3732428826

0.4866205833

1202.61401

0.3747697506

0.4870528788

1202.651

0.37408266

0.4874645887

1202.62805

0.3745407204

0.4878762987

1202.63306

0.3748715418

0.4882880087

1202.63403

0.3756604236

0.4886997186

1202.62097

0.3761439318

0.4891114286

1202.63

0.3766528878

0.4895231385

1202.604

0.3772381872

0.4899348485

1202.59998

0.3759657972

0.4903671439

1202.61499

0.3771109482

0.4907788539

1202.62903

0.3771872916

0.4912111494

1202.62805

0.3787396074

0.4916434448

1202.58301

0.3793503546

0.4920757403

1202.56201

0.3775690086

0.4925286212

1202.57202

0.3797829672

0.4929609167

1202.59705

0.3778489344

0.4934137976

1202.62097

0.378790503

0.4938460931

1202.64001

0.3797829672

0.494298974

1202.61304

0.379935654

0.4947312695

1202.60596

0.3796302804

0.4951635649

1202.59595

0.3805464012

0.4955958604

1202.60596

0.3825567774

0.4960075703

1202.60205

0.3810553572

0.4964192803

1202.59802

0.3825822252

0.4968104048

1202.58496

0.3807754314

0.4972221147

1202.56396

0.3802664754

0.4975926537

1202.56396

0.3837273762

0.4979837781

1202.55505

0.383371107

0.4983337316

1202.56799

0.383371107

0.4987042706

1202.59094

0.3841854366

0.499054224

1202.59595

0.3857123046

0.499424763

1202.599

0.3844399146

0.499754131

1202.59802

0.3854832744

0.5001040844

1202.60205

0.384770736

0.5004334524

1202.60205

0.3852033486

0.5007834058

1202.59998

0.3834728982

0.5011127738

1202.62097

0.3846943926

0.5014421418

1202.62097

0.3867556644

0.5017715097

1202.625

0.3860176782

0.5021008777

1202.62195

0.386297604

0.5024096602

1202.60205

0.386424843

0.5027390281

1202.58997

0.3846689448

0.5030683961

1202.60999

0.386552082

0.5033771786

1202.61304

0.3882825324

0.5037065465

1202.59302

0.3871628292

0.5040359145

1202.59094

0.387315516

0.5043652825

1202.61206

0.3891477576

0.5046946504

1202.59497

0.3890205186

0.5050446039

1202.56201

0.3893258922

0.5053739719

1202.54102

0.3887914884

0.5057239253

1202.54297

0.3891732054

0.5060532933

1202.55701

0.3869592468

0.5064032468

1202.57397

0.3887660406

0.5067532002

1202.58496

0.3888932796

0.5071031537

1202.58398

0.3883843236

0.5074325216

1202.55798

0.389860296

0.5077824751

1202.578

0.389224101

0.5081118431

1202.57996

0.389860296

0.5084617965

1202.56897

0.3904201476

0.5087911645

1202.56799

0.3895549224

0.509099947

1202.57104

0.3916670898

0.5094293149

1202.59497

0.391259925

0.5097586829

1202.57898

0.3924559716

0.5100674654

1202.56494

0.3928885842

0.5103762478

1202.57898

0.3930921666

0.5106850303

1202.58801

0.3937538094

0.5109938128

1202.61694

0.3926850018

0.5113025952

1202.60901

0.3924814194

0.5115907922

1202.59204

0.3941100786

0.5118995747

1202.60706

0.3937792572

0.5122083571

1202.60498

0.3933975402

0.5124965541

1202.60303

0.3937283616

0.5128053366

1202.58997

0.3953824686

0.5131347045

1202.59302

0.3957641856

0.513443487

1202.59302

0.3962731416

0.513772855

1202.59399

0.3963749328

0.5141022229

1202.59998

0.3939573918

0.5144315909

1202.56604

0.3954842598

0.5147815444

1202.53101

0.3973419492

0.5151520833

1202.51404

0.397876353

0.5155020368

1202.53296

0.396095007

0.5158725758

1202.56995

0.3947717214

0.5162431147

1202.58606

0.4010318802

0.5166342392

1202.59302

0.3976727706

0.5170047781

1202.58301

0.3985379958

0.5173959026

1202.56104

0.4013627016

0.5177664416

1202.55103

0.40080285

0.5181369805

1202.56702

0.4010827758

0.518528105

1202.57104

0.4015408362

0.5188986439

1202.57495

0.4017189708

0.5192485974

1202.57104

0.4009046412

0.5196191364

1202.58606

0.4022533746

0.5199896753

1202.59497

0.4034239734

0.5203396288

1202.60706

0.403474869

0.5206895823

1202.61499

0.4026859872

0.5210395357

1202.62097

0.4041874074

0.5213894892

1202.63

0.4041365118

0.5217394426

1202.62305

0.4047727068

0.5220688106

1202.61499

0.403474869

0.5224187641

1202.59204

0.4042637508

0.5227687175

1202.58899

0.4040601684

0.523118671

1202.60498

0.4035512124

0.5234686245

1202.60095

0.405128976

0.5238185779

1202.57898

0.4057142754

0.5241891169

1202.55005

0.4058160666

0.5245596558

1202.54895

0.4067576352

0.5249301948

1202.57397

0.4064522616

0.5253007338

1202.59497

0.4065795006

0.5256918582

1202.60205

0.4065540528

0.5260829827

1202.61804

0.406910322

0.5264946926

1202.61902

0.4064777094

0.5269064026

1202.59802

0.4069357698

0.5273181126

1202.56604

0.4072156956

0.5277298225

1202.578

0.4069357698

0.5281415325

1202.58606

0.4085898768

0.5285532424

1202.57605

0.4062232314

0.5289855379

1202.55896

0.4131959286

0.5293972478

1202.56604

0.4127124204

0.5298089578

1202.58704

0.4114400304

0.5302206677

1202.60095

0.4094042064

0.5306117922

1202.62903

0.4100658492

0.5310235022

1202.62305

0.4107529398

0.5314146266

1202.59802

0.4111855524

0.5318057511

1202.58801

0.4114400304

0.5321968755

1202.59802

0.4116436128

0.532588

1202.58203

0.4116945084

0.5329791245

1202.58203

0.4123561512

0.5333908344

1202.57605

0.411109209

0.5337819589

1202.55396

0.4127378682

0.5341730833

1202.52795

0.4135013022

0.5345847933

1202.53406

0.4127378682

0.5349759177

1202.55798

0.4140866016

0.5353876277

1202.56201

0.4138066758

0.5357993377

1202.56299

0.415689813

0.5362110476

1202.56006

0.4143156318

0.5366227576

1202.56104

0.4149772746

0.5370344675

1202.55896

0.4145701098

0.537425592

1202.58606

0.4142392884

0.5378373019

1202.57898

0.415180857

0.5382490119

1202.57202

0.4161224256

0.5386607219

1202.55396

0.4121525688

0.5390518463

1202.552

0.4145701098

0.5394429708

1202.56897

0.4175729502

0.5398340952

1202.57605

0.4159697388

0.5402252197

1202.56396

0.4184127276

0.5405957587

1202.56995

0.4170385464

0.5409662976

1202.57202

0.4140866016

0.5413368366

1202.57397

0.4177001892

0.5417073755

1202.57996

0.4171657854

0.542057329

1202.57898

0.4174202634

0.5424072825

1202.58203

0.419125266

0.5427572359

1202.59094

0.4185145188

0.5430866039

1202.58704

0.4183363842

0.5434365574

1202.57397

0.4173948156

0.5437865108

1202.56201

0.4202958648

0.5441364643

1202.56799

0.4185399666

0.5444864177

1202.57495

0.4198378044

0.5448363712

1202.57996

0.4199904912

0.5451863247

1202.58203

0.4192016094

0.5455568636

1202.56494

0.4196087742

0.5459068171

1202.56104

0.4214919114

0.5462773561

1202.58496

0.420270417

0.546647895

1202.578

0.4225098234

0.5470390195

1202.59705

0.4212628812

0.5474095584

1202.59595

0.4208048208

0.5477800974

1202.59705

0.4223825844

0.5481506364

1202.59204

0.4230442272

0.5485417608

1202.59204

0.422179002

0.5489122998

1202.56104

0.4226370624

0.5492828387

1202.52405

0.4235022876

0.5496533777

1202.53296

0.4230442272

0.5500239167

1202.56006

0.4231460184

0.5503738701

1202.57202

0.423069675

0.5507444091

1202.57703

0.4257925896

0.5511149481

1202.57703

0.425105499

0.5515060725

1202.54895

0.4264287846

0.5518766115

1202.53699

0.4255126638

0.5522471504

1202.52295

0.4261743066

0.5526382749

1202.52502

0.4265560236

0.5530293994

1202.54504

0.42625065

0.5534205238

1202.573

0.4258180374

0.5538116483

1202.604

0.4253090814

0.5542027727

1202.63

0.4282355784

0.5546144827

1202.61694

0.4269122928

0.5550261926

1202.58203

0.4269631884

0.5554379026

1202.56201

0.426759606

0.5558701981

1202.54895

0.4287445344

0.556281908

1202.552

0.4273194576

0.5567142035

1202.56299

0.429177147

0.5571464989

1202.55798

0.4298387898

0.5575787944

1202.53699

0.4291008036

0.5580316753

1202.51794

0.4307549106

0.5584639708

1202.51501

0.4295843118

0.5588962662

1202.51599

0.4308058062

0.5593285617

1202.51697

0.429686103

0.5597608571

1202.547

0.4303477458

0.5601725671

1202.57397

0.4286936388

0.5605842771

1202.57202

0.4297115508

0.5609754015

1202.54004

0.4309330452

0.561366526

1202.53003

0.430704015

0.5617576504

1202.54004

0.4310093886

0.5621281894

1202.54102

0.4304240892

0.5624987284

1202.56299

0.4307549106

0.5628692673

1202.56201

0.4327652868

0.5632192208

1202.56702

0.4323835698

0.5635691742

1202.56396

0.4327652868

0.5639191277

1202.55505

0.4327143912

0.5642484957

1202.53796

0.4323835698

0.5645778636

1202.53406

0.4334014818

0.5649072316

1202.55701

0.4332742428

0.5652365996

1202.56604

0.4338086466

0.5655659675

1202.57202

0.4341140202

0.56587475

1202.56299

0.4329688692

0.5661835325

1202.55103

0.434393946

0.5664923149

1202.57605

0.4349537976

0.5668010974

1202.57202

0.4355136492

0.5671098799

1202.58398

0.4346738718

0.5673980768

1202.56897

0.4365061134

0.5677068593

1202.58899

0.4364806656

0.5679950563

1202.573

0.4361498442

0.5683038387

1202.578

0.4360735008

0.5686126212

1202.55603

0.4365061134

0.5689214037

1202.53894

0.4360735008

0.5692301861

1202.52905

0.4370405172

0.5695595541

1202.53296

0.4363788744

0.5698889221

1202.53003

0.4383129072

0.57021829

1202.54199

0.4367860392

0.5705682435

1202.54297

0.4357172316

0.570918197

1202.55103

0.4383892506

0.5712681504

1202.56104

0.4387964154

0.5716181039

1202.56897

0.4370150694

0.5719886429

1202.58301

0.43770216

0.5723591818

1202.57703

0.4406541048

0.5727503063

1202.57605

0.4393817148

0.5731208452

1202.57104

0.4382620116

0.5735119697

1202.57202

0.4425881376

0.5739030942

1202.56702

0.4398143274

0.5742942186

1202.56995

0.438592833

0.5746853431

1202.55005

0.4389236544

0.575097053

1202.55396

0.442155525

0.575508763

1202.56494

0.442028286

0.5759204729

1202.58301

0.441646569

0.5763321829

1202.573

0.442028286

0.5767438929

1202.55603

0.4410612696

0.5771761883

1202.55603

0.4404505224

0.5775878983

1202.573

0.4402214922

0.5780201937

1202.56897

0.4414684344

0.5784319037

1202.55701

0.4428171678

0.5788641991

1202.55798

0.44279172

0.5792759091

1202.56201

0.441010374

0.5797082045

1202.56897

0.4421046294

0.5801199145

1202.578

0.4420537338

0.58055221

1202.56494

0.4429953024

0.5809639199

1202.56995

0.4434024672

0.5813962154

1202.57495

0.4429953024

0.5818079253

1202.57605

0.4433770194

0.5822402208

1202.59497

0.4446494094

0.5826519307

1202.62195

0.4435806018

0.5830636407

1202.61499

0.4470669504

0.5834959361

1202.58203

0.4452601566

0.5839076461

1202.55103

0.4454382912

0.5843193561

1202.552

0.4463289642

0.5847516515

1202.58203

0.4453365

0.5851633615

1202.58105

0.450298821

0.5855750714

1202.56702

0.448771953

0.5859867814

1202.54895

0.4449293352

0.5864190768

1202.55505

0.4481866536

0.5868307868

1202.55505

0.4485938184

0.5872424968

1202.56299

0.4464562032

0.5876542067

1202.56897

0.4468888158

0.5880659167

1202.59399

0.448644714

0.5884982121

1202.61499

0.4476776976

0.5889099221

1202.60205

0.4483393404

0.589321632

1202.58105

0.4503242688

0.589733342

1202.604

0.4496117304

0.5901450519

1202.62695

0.4482884448

0.5905567619

1202.63501

0.4492300134

0.5909478864

1202.61694

0.4485683706

0.5913390108

1202.58203

0.449026431

0.5917301353

1202.56006

0.4500188952

0.5921212597

1202.54395

0.4501206864

0.5924917987

1202.55896

0.4502479254

0.5928623377

1202.57898

0.450807777

0.5932328766

1202.59204

0.4503497166

0.5936034156

1202.58203

0.451316733

0.593953369

1202.56799

0.4512149418

0.5943033225

1202.56104

0.452080167

0.5946326905

1202.52502

0.4509095682

0.5949826439

1202.54504

0.4528690488

0.5953120119

1202.55396

0.4524364362

0.5956413799

1202.55505

0.4529453922

0.5959707478

1202.53198

0.4531744224

0.5963001158

1202.52698

0.4541414388

0.5966294838

1202.50696

0.4538360652

0.5969382662

1202.53796

0.453861513

0.5972676342

1202.53699

0.454497708

0.5975764167

1202.53296

0.454624947

0.5978851991

1202.55505

0.4532507658

0.5982145671

1202.56494

0.4537851696

0.5985233496

1202.547

0.45424323

0.598832132

1202.53894

0.4543450212

0.5991409145

1202.55298

0.454497708

0.599449697

1202.58301

0.4549303206

0.5997584794

1202.61096

0.4557955458

0.6000672619

1202.56201

0.455642859

0.6003760444

1202.55505

0.4563299496

0.6006848268

1202.55603

0.4552356942

0.6009936093

1202.57397

0.4546758426

0.6013229773

1202.59705

0.4561772628

0.6016317597

1202.58899

0.4563553974

0.6019611277

1202.59399

0.455770098

0.6022699102

1202.55798

0.4566862188

0.6025786926

1202.53101

0.4585439082

0.6029080606

1202.56995

0.4577804742

0.6032374286

1202.59497

0.4576277874

0.603546211

1202.58997

0.4580095044

0.603875579

1202.58606

0.4576532352

0.604204947

1202.55298

0.459460029

0.6045343149

1202.54395

0.4597908504

0.6048636829

1202.56702

0.4586456994

0.6052136364

1202.53406

0.4580349522

0.6055430043

1202.52905

0.4597399548

0.6058929578

1202.52698

0.459205551

0.6062429113

1202.54199

0.4599435372

0.6065928647

1202.55603

0.4602743586

0.6069428182

1202.56201

0.4610886882

0.6072927716

1202.53796

0.46060518

0.6076427251

1202.53601

0.4610886882

0.6079926786

1202.55701

0.4611395838

0.6083220465

1202.58801

0.4612922706

0.6086514145

1202.604

0.4629972732

0.6089807825

1202.60596

0.4619030178

0.6093101504

1202.58997

0.4617248832

0.6096189329

1202.58496

0.4625392128

0.6099277154

1202.56897

0.4618012266

0.6102364978

1202.56604

0.4628445864

0.6105246948

1202.59399

0.4633280946

0.6108334773

1202.59302

0.4633535424

0.6111216742

1202.58801

0.463531677

0.6114098712

1202.57202

0.4644477978

0.6116980682

1202.55603

0.46314996

0.6119862652

1202.573

0.463531677

0.6122744621

1202.60901

0.4661019048

0.6125626591

1202.573

0.4645241412

0.6128714416

1202.53601

0.465821979

0.6131596385

1202.52197

0.4651094406

0.6134478355

1202.52405

0.4652875752

0.613756618

1202.55505

0.4655929488

0.6140448149

1202.57703

0.4655166054

0.6143535974

1202.58398

0.4664836218

0.6146623799

1202.56104

0.4652621274

0.6149711623

1202.55005

0.4657201878

0.6152593593

1202.52002

0.4658983224

0.6155681418

1202.49902

0.4656438444

0.6158975097

1202.51904

0.4673997426

0.6162062922

1202.54395

0.468112281

0.6165356602

1202.55103

0.4679341464

0.6168444426

1202.52405

0.4665090696

0.6171738106

1202.50098

0.467730564

0.6175031786

1202.52905

0.4680613854

0.617853132

1202.54102

0.4691810886

0.6181825

1202.52795

0.469130193

0.6185324535

1202.51501

0.4685448936

0.6188824069

1202.53101

0.4708097478

0.6192323604

1202.526

0.4691810886

0.6195823139

1202.56201

0.468875715

0.6199528528

1202.58606

0.468493998

0.6203233918

1202.56702

0.469893627

0.6206939307

1202.56604

0.4694355666

0.6210644697

1202.573

0.4713441516

0.6214350087

1202.58105

0.4708097478

0.6218261331

1202.58801

0.4710133302

0.6221966721

1202.59497

0.4707334044

0.622567211

1202.60095

0.4723875114

0.6229583355

1202.59595

0.4714459428

0.6233288745

1202.59705

0.4726165416

0.6236994134

1202.60999

0.4709878824

0.6240699524

1202.63599

0.4721075856

0.6244199058

1202.63904

0.4729982586

0.6247698593

1202.61597

0.4736344536

0.6250992273

1202.59094

0.473074602

0.6254285952

1202.58997

0.4740161706

0.6257579632

1202.57605

0.4737871404

0.6260667457

1202.573

0.4734054234

0.6263755281

1202.57104

0.4755939342

0.6266637251

1202.58997

0.473710797

0.6269725076

1202.57703

0.4755939342

0.6272607045

1202.52795

0.4741434096

0.6275489015

1202.52698

0.4756957254

0.6278370985

1202.52405

0.4753903518

0.6281252955

1202.53296

0.4766881896

0.6284134924

1202.54004

0.4762810248

0.6287016894

1202.54504

0.47714625

0.6289898864

1202.53198

0.4767390852

0.6292780833

1202.53503

0.4758993078

0.6295662803

1202.53101

0.4760519946

0.6298544773

1202.51196

0.4767390852

0.6301426742

1202.50696

0.4769935632

0.6304308712

1202.54199

0.4780878186

0.6307190682

1202.55798

0.477527967

0.6309866797

1202.55505

0.4774516236

0.6312748766

1202.54504

0.477909684

0.6315424881

1202.53406

0.4771971456

0.6318306851

1202.53296

0.4783168488

0.6320982965

1202.51404

0.4778078928

0.632365908

1202.50696

0.477909684

0.6326335195

1202.50903

0.4790293872

0.632901131

1202.51794

0.4784440878

0.6331687424

1202.50305

0.4798946124

0.6334363539

1202.50195

0.47969103

0.6337039654

1202.50903

0.4801490904

0.6339715768

1202.526

0.479818269

0.6342391883

1202.52405

0.4799964036

0.6344862143

1202.51001

0.4804035684

0.6347538258

1202.51099

0.4801490904

0.6350008517

1202.526

0.4809125244

0.6352684632

1202.526

0.481090659

0.6355154892

1202.55298

0.4804290162

0.6357625152

1202.54504

0.4808870766

0.6360301266

1202.50903

0.48223581

0.6362771526

1202.50195

0.4810652112

0.6365447641

1202.52905

0.4823884968

0.6368123755

1202.54199

0.4823376012

0.637079987

1202.56006

0.482363049

0.6373475985

1202.573

0.4819558842

0.63761521

1202.573

0.4827702138

0.6378828214

1202.573

0.4836099912

0.6381710184

1202.54004

0.4844497686

0.6384386299

1202.51501

0.4828211094

0.6387268268

1202.51794

0.4846024554

0.6390150238

1202.53601

0.4838390214

0.6393032208

1202.53894

0.4840680516

0.6395914177

1202.53198

0.4842970818

0.6398796147

1202.521

0.4841952906

0.6401678117

1202.526

0.4838135736

0.6404560087

1202.54395

0.4851114114

0.6407442056

1202.55298

0.485289546

0.6410529881

1202.56799

0.4853149938

0.6413411851

1202.53894

0.4854676806

0.641629382

1202.53601

0.4879361172

0.6419381645

1202.50195

0.4864092492

0.6422263615

1202.49902

0.4869691008

0.6425145584

1202.50403

0.4878088782

0.6428027554

1202.50903

0.4870963398

0.6430909524

1202.51794

0.4885468644

0.6433585639

1202.505

0.488470521

0.6436261753

1202.51904

0.487961565

0.6438937868

1202.52502

0.4877579826

0.6441613983

1202.53601

0.4891830594

0.6444084242

1202.55896

0.4886232078

0.6446760357

1202.56299

0.488343282

0.6449230617

1202.55005

0.488470521

0.6451700877

1202.58606

0.4884450732

0.6454171136

1202.60303

0.4887758946

0.6456641396

1202.59705

0.4882669386

0.6459111656

1202.58606

0.4895138808

0.6461581916

1202.56995

0.4891321638

0.6464052175

1202.55701

0.4902773148

0.646672829

1202.54602

0.48987015

0.646919855

1202.54297

0.4902009714

0.6471874665

1202.53894

0.4903282104

0.6474550779

1202.55396

0.4909644054

0.6477226894

1202.56799

0.4910407488

0.6479697154

1202.58105

0.4912952268

0.6482373268

1202.578

0.4911679878

0.6485049383

1202.58801

0.4909644054

0.6487725498

1202.59705

0.491015301

0.6490401613

1202.58301

0.4918805262

0.6493283582

1202.56702

0.4926439602

0.6495959697

1202.55603

0.492033213

0.6498635812

1202.57996

0.4928984382

0.6501517781

1202.60901

0.4923385866

0.6504399751

1202.60706

0.492796647

0.6507281721

1202.60205

0.4923385866

0.651016369

1202.58301

0.4930256772

0.651304566

1202.59204

0.4928475426

0.6516133485

1202.59094

0.4931274684

0.6519015455

1202.59302

0.492542169

0.6521897424

1202.60095

0.4937127678

0.6524985249

1202.58105

0.4935855288

0.6527867219

1202.54797

0.4928729904

0.6530749188

1202.53699

0.4936618722

0.6533631158

1202.50098

0.4949088144

0.6536513128

1202.50598

0.4935855288

0.6539395097

1202.52002

0.4942980672

0.6542071212

1202.50195

0.4942217238

0.6544953182

1202.48596

0.4946543364

0.6547629297

1202.48596

0.495086949

0.6550305411

1202.53601

0.4969446384

0.6553187381

1202.51794

0.4962321

0.6555863496

1202.50305

0.4980897894

0.655853961

1202.495

0.4971482208

0.6561215725

1202.53003

0.4969700862

0.656389184

1202.53296

0.4974790422

0.6566567955

1202.52905

0.497758968

0.6569244069

1202.54797

0.4993876272

0.6571714329

1202.55896

0.4977080724

0.6574390444

1202.61096

0.495977622

0.6577066558

1202.62598

0.4986241932

0.6579742673

1202.62

0.498649641

0.6582418788

1202.604

0.49877688

0.6585094903

1202.58704

0.497631729

0.6587771017

1202.55103

0.49750449

0.6590652987

1202.56604

0.4975299378

0.6593329102

1202.58899

0.4988023278

0.6596005216

1202.58301

0.4994639706

0.6598887186

1202.55396

0.4993367316

0.6601769156

1202.54395

0.4998202398

0.6604445271

1202.55798

0.5001001656

0.660732724

1202.56604

0.4983188196

0.6610003355

1202.56799

0.49877688

0.6612885325

1202.56897

0.5012198688

0.6615767294

1202.56995

0.5003546436

0.6618443409

1202.57495

0.5008635996

0.6621325379

1202.56897

0.5003291958

0.6624001494

1202.54797

0.4992349404

0.6626677608

1202.53601

0.5004055392

0.6629353723

1202.53796

0.5015252424

0.6632029838

1202.52197

0.5003546436

0.6634705952

1202.50903

0.502085094

0.6637382067

1202.49902

0.500430987

0.6640058182

1202.53296

0.501830616

0.6642734297

1202.57495

0.5030521104

0.6645410411

1202.599

0.5037646488

0.6647880671

1202.60095

0.503103006

0.6650556786

1202.59802

0.5026194978

0.6653027045

1202.59497

0.5018815116

0.6655497305

1202.59497

0.5019833028

0.6657967565

1202.59497

0.5027976324

0.6660437825

1202.58899

0.5024922588

0.6662702229

1202.56897

0.502721289

0.6665172489

1202.56897

0.5031284538

0.6667642749

1202.58203

0.5036883054

0.6670113009

1202.573

0.503993679

0.6672377413

1202.58496

0.5037646488

0.6674847673

1202.59302

0.5041972614

0.6677523788

1202.59595

0.502721289

0.6679994048

1202.59802

0.5037137532

0.6682464307

1202.60999

0.5048334564

0.6685140422

1202.58398

0.5046553218

0.6687816537

1202.547

0.5045535306

0.6690492652

1202.53101

0.504757113

0.6692962911

1202.55103

0.5050370388

0.6695639026

1202.53796

0.50513883

0.6698315141

1202.54895

0.5058004728

0.6700991255

1202.57605

0.5077854012

0.670366737

1202.57104

0.5060040552

0.670613763

1202.578

0.506156742

0.670860789

1202.573

0.506283981

0.6711078149

1202.57104

0.5050879344

0.6713754264

1202.54004

0.5058259206

0.6716224524

1202.53296

0.5078617446

0.6718694784

1202.54895

0.5065893546

0.6721165043

1202.56799

0.5081671182

0.6723635303

1202.55005

0.5069710716

0.6726105563

1202.53101

0.5080398792

0.6728575823

1202.54297

0.5076072666

0.6731251937

1202.55603

0.509337717

0.6733722197

1202.56702

0.5080398792

0.6736398312

1202.56799

0.5079635358

0.6738868571

1202.573

0.5093122692

0.6741544686

1202.56995

0.5084979396

0.6744220801

1202.55298

0.5094140604

0.6746896916

1202.54895

0.509210478

0.674957303

1202.53601

0.508447044

0.6752249145

1202.53101

0.5087778654

0.6755131115

1202.54504

0.509337717

0.6757807229

1202.54395

0.5096685384

0.6760483344

1202.54004

0.5094140604

0.6763365314

1202.53406

0.510355629

0.6766041429

1202.54102

0.5107627938

0.6768923398

1202.55798

0.511246302

0.6771805368

1202.56396

0.5105846592

0.6774481483

1202.578

0.5104065246

0.6777363452

1202.56897

0.5113989888

0.6780039567

1202.59094

0.511628019

0.6782715682

1202.56799

0.511628019

0.6785185942

1202.51294

0.5133584694

0.6787862056

1202.47205

0.5132057826

0.6790126461

1202.46997

0.511119063

0.6792596721

1202.45605

0.5131294392

0.6794861126

1202.45996

0.5121115272

0.679712553

1202.479

0.5126204832

0.679918408

1202.46997

0.5121878706

0.6801448485

1202.50098

0.5143509336

0.6803507035

1202.50403

0.5145799638

0.6805771439

1202.50305

0.5156233236

0.6807829989

1202.51501

0.5162849664

0.6810094394

1202.53198

0.5159286972

0.6812358799

1202.55396

0.5161577274

0.6814829058

1202.53101

0.516335862

0.6817093463

1202.53101

0.5160559362

0.6819769578

1202.52295

0.5166412356

0.6822239838

1202.53406

0.517226535

0.6824915952

1202.51697

0.5186770596

0.6827592067

1202.51501

0.517353774

0.6830268182

1202.51099

0.517099296

0.6832944297

1202.52002

0.5173792218

0.6835620411

1202.53894

0.5178372822

0.6838296526

1202.54004

0.5175064608

0.6840766786

1202.53503

0.5167430268

0.68434429

1202.51904

0.51786273

0.6846119015

1202.526

0.5170484004

0.6848589275

1202.55103

0.5184225816

0.6851059535

1202.54797

0.5174555652

0.6853323939

1202.56494

0.5180917602

0.6855794199

1202.57703

0.5183462382

0.6858058604

1202.55798

0.5177100432

0.6860528864

1202.56494

0.5181426558

0.6862793268

1202.56006

0.520153032

0.6864851818

1202.54797

0.5204838534

0.6867116223

1202.55603

0.5204838534

0.6869380628

1202.54895

0.5211454962

0.6871439177

1202.52405

0.5214508698

0.6873703582

1202.52698

0.5200766886

0.6875967987

1202.52502

0.5207128836

0.6878026537

1202.53894

0.5213745264

0.6880290942

1202.53101

0.521043705

0.6882555346

1202.52698

0.522061617

0.6885025606

1202.51904

0.5221125126

0.6887290011

1202.51697

0.5229268422

0.6889760271

1202.52698

0.522316095

0.689223053

1202.52002

0.5223669906

0.689470079

1202.52405

0.5233594548

0.689717105

1202.53296

0.5222651994

0.6899847165

1202.52405

0.5209419138

0.6902523279

1202.5

0.5219852736

0.6905199394

1202.50305

0.522570573

0.6907875509

1202.52295

0.5213999742

0.6910345768

1202.55103

0.5231304246

0.6913021883

1202.56702

0.5257006524

0.6915697998

1202.57996

0.5222397516

0.6918168258

1202.56897

0.5212472874

0.6920844372

1202.55798

0.522316095

0.6923314632

1202.56604

0.5220361692

0.6925784892

1202.55505

0.5219089302

0.6928255152

1202.52002

0.5227741554

0.6930725411

1202.54199

0.522697812

0.6933195671

1202.55603

0.5226469164

0.6935665931

1202.57996

0.5230286334

0.6937930335

1202.57605

0.521807139

0.6940400595

1202.55701

0.5213236308

0.6942870855

1202.56702

0.5223924384

0.694513526

1202.55005

0.5230031856

0.6947399665

1202.56897

0.5225960208

0.6949869924

1202.56006

0.5233085592

0.6952134329

1202.57104

0.5210182572

0.6954398734

1202.57397

0.5193132546

0.6956663139

1202.58496

0.5197458672

0.6958927543

1202.57703

0.5201275842

0.6961191948

1202.56897

0.5204838534

0.6963456353

1202.573

0.5208401226

0.6965720758

1202.57495

0.5223924384

0.6967985162

1202.57397

0.5206110924

0.6970249567

1202.56201

0.5227232598

0.6972513972

1202.55896

0.5220870648

0.6974778377

1202.56201

0.5222143038

0.6977042781

1202.58899

0.5207383314

0.6979307186

1202.57898

0.522825051

0.6981571591

1202.56995

0.5224178862

0.6983835996

1202.54504

0.521934378

0.69861004

1202.54004

0.5224942296

0.698815895

1202.547

0.5240465454

0.6990423355

1202.54504

0.5241228888

0.699268776

1202.53003

0.5237411718

0.6994952165

1202.52502

0.5235375894

0.6997216569

1202.547

0.524606397

0.6999275119

1202.56006

0.5239956498

0.7001539524

1202.56799

0.5224942296

0.7003803929

1202.55005

0.5231558724

0.7005862478

1202.50806

0.5243010234

0.7008126883

1202.51099

0.525624309

0.7010391288

1202.51294

0.5234357982

0.7012449838

1202.50903

0.5257769958

0.7014508387

1202.47803

0.5266167732

0.7016566937

1202.47595

0.5248354272

0.7018625487

1202.45996

0.524097441

0.7020684037

1202.49304

0.5259042348

0.7022742587

1202.495

0.5255988612

0.7024801136

1202.46997

0.5263113996

0.7026859686

1202.474

0.5264386386

0.7028918236

1202.49695

0.5271766248

0.7030976786

1202.48706

0.526896699

0.7033035335

1202.49097

0.5283726714

0.703529974

1202.46106

0.5277110286

0.703735829

1202.45703

0.5285253582

0.7039622695

1202.479

0.528678045

0.7042092955

1202.48706

0.5281945368

0.7044357359

1202.46899

0.5287798362

0.7046827619

1202.45605

0.5275837896

0.7049503734

1202.46802

0.5329787232

0.7051973994

1202.51001

0.5297723004

0.7054855963

1202.505

0.5271002814

0.7057532078

1202.48401

0.5327751408

0.7060208193

1202.45801

0.5298995394

0.7063090162

1202.44702

0.5288816274

0.7065972132

1202.46106

0.5287543884

0.7068854102

1202.45605

0.5291106576

0.7071736071

1202.43396

0.5301794652

0.7074823896

1202.427

0.5287798362

0.7077705866

1202.42896

0.5269475946

0.7080587835

1202.44202

0.5294160312

0.7083469805

1202.46802

0.5296196136

0.7086351775

1202.48401

0.5296705092

0.7089233745

1202.47302

0.5293396878

0.7092115714

1202.46204

0.528805284

0.7094791829

1202.44702

0.529950435

0.7097673799

1202.44702

0.5297977482

0.7100349913

1202.47095

0.5309174514

0.7103026028

1202.47595

0.5315790942

0.7105702143

1202.45801

0.5309174514

0.7108172403

1202.453

0.5310446904

0.7110642662

1202.47595

0.532367976

0.7113112922

1202.49597

0.5312482728

0.7115377327

1202.51794

0.5319099156

0.7117641732

1202.521

0.5329023798

0.7119906136

1202.52698

0.5341747698

0.7122170541

1202.54602

0.5365414152

0.7124229091

1202.54602

0.5358797724

0.7126493496

1202.55505

0.53694858

0.7128552045

1202.54602

0.5369231322

0.7130610595

1202.53406

0.5366686542

0.7132669145

1202.526

0.537584775

0.713452184

1202.53503

0.5374066404

0.713658039

1202.53101

0.538348209

0.7138433084

1202.54602

0.5375084316

0.7140285779

1202.53699

0.5388826128

0.7141932619

1202.53003

0.538602687

0.7143785314

1202.51904

0.5390352996

0.7145432154

1202.51794

0.54076575

0.7147078994

1202.51294

0.5388317172

0.7148725833

1202.52502

0.5392134342

0.7150372673

1202.53406

0.5396969424

0.7152019513

1202.52502

0.5395697034

0.7153666353

1202.50903

0.5409693324

0.7155313193

1202.50305

0.5423689614

0.7156960032

1202.50195

0.5387808216

0.7158606872

1202.48596

0.5382464178

0.7160253712

1202.47095

0.5404349286

0.7162106407

1202.48706

0.5402058984

0.7163959102

1202.49402

0.5405876154

0.7165811797

1202.53894

0.5398496292

0.7167870346

1202.54504

0.5406130632

0.7169928896

1202.52502

0.5411220192

0.7171987446

1202.52698

0.5410711236

0.7174251851

1202.53503

0.5415546318

0.7176516255

1202.55603

0.5430814998

0.717878066

1202.56201

0.541656423

0.718125092

1202.54199

0.5415037362

0.7183515325

1202.54004

0.5432341866

0.7185985584

1202.52795

0.5433614256

0.7188455844

1202.50903

0.5431069476

0.7190720249

1202.49597

0.5425979916

0.7193190509

1202.51697

0.5419363488

0.7195660768

1202.54004

0.5419872444

0.7197925173

1202.52197

0.5419617966

0.7200189578

1202.526

0.5432596344

0.7202453983

1202.56494

0.5446338156

0.7204718387

1202.59497

0.5443793376

0.7206776937

1202.578

0.5471022522

0.7208835487

1202.55798

0.5511230046

0.7210894037

1202.54199

0.551835543

0.7212746732

1202.55298

0.553871367

0.7214599426

1202.54504

0.554125845

0.7216452121

1202.552

0.5548638312

0.7218304816

1202.55298

0.5524462902

0.7219951656

1202.56799

0.5541003972

0.7221598496

1202.56494

0.5547111444

0.7223245335

1202.57898

0.5542021884

0.722509803

1202.59705

0.557052342

0.7226539015

1202.59998

0.557179581

0.7228185855

1202.59998

0.556288908

0.7229832695

1202.61804

0.5566197294

0.7231479535

1202.58704

0.5576376414

0.7233126374

1202.58301

0.5580193584

0.7234773214

1202.54504

0.5574849546

0.7236420054

1202.54199

0.5577903282

0.7238272749

1202.55005

0.5600806302

0.7240125444

1202.55896

0.5593680918

0.7241978139

1202.56799

0.5590627182

0.7243830833

1202.56006

0.559088166

0.7245889383

1202.55798

0.5617347372

0.7248153788

1202.54797

0.56112399

0.7250418193

1202.55103

0.5619128718

0.7252682597

1202.55896

0.5639995914

0.7255152857

1202.56702

0.563796009

0.7257623117

1202.59204

0.5647630254

0.7260299232

1202.58398

0.5646103386

0.7262769491

1202.58801

0.5647375776

0.7265445606

1202.58398

0.5658572808

0.7267915866

1202.56799

0.566340789

0.7270591981

1202.58496

0.564686682

0.7273268095

1202.60901

0.5654246682

0.7275738355

1202.599

0.5639486958

0.7278208615

1202.60803

0.565704594

0.7280884729

1202.58801

0.5656536984

0.7283354989

1202.61304

0.5660608632

0.7285825249

1202.63599

0.5664934758

0.7288295509

1202.64795

0.5653737726

0.7290765768

1202.64905

0.565831833

0.7293236028

1202.65198

0.5678422092

0.7295706288

1202.62402

0.5671805664

0.7298176548

1202.59497

0.568376613

0.7300646807

1202.60303

0.566722506

0.7303117067

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999

1202.60999



Sheet1

						Kanthal AF		PX-C		Kanthal A1						Kanthal APM						Riken PC-C						PVD Kanthal AF 620°C						PVD Kanthal AF 770°C								masa		površina

		##Temp./ｰC		Time/min		Mass/%		Mass/%		##Temp./ｰC		Time/min		Mass/%		##Temp./ｰC		Time/min		Mass/%		##Temp./ｰC		Time/min		Mass/%		##Temp./ｰC		Time/min		Mass/%		##Temp./ｰC		Time/min		Mass/%				mg		mm2

		28.836		0		100		100		26.096		0.00E+00		100		25.5		0.00E+00		100		28.059		0.00E+00		100		28.059		0.00E+00		100		25.172		0.00E+00		100		Kanthal AF		954.050		468.23

		28.84		0.025		99.99345		100.00001		26.098		2.50E-02		99.99991		25.497		2.50E-02		99.99971		28.059		2.50E-02		100.00001		28.059		2.50E-02		100.00027		25.167		2.50E-02		99.99986		Kanthal A1		1020.900		487.31

		28.835		0.05		99.99362		99.99987		26.108		5.00E-02		100.00147		25.499		5.00E-02		99.99961		28.059		5.00E-02		99.99987		28.059		5.00E-02		100.00043		25.1676		5.00E-02		99.99993		Kanthal APM		1272.390		499.69

		28.836		0.075		99.99092		99.9997		26.108		7.50E-02		99.9994		25.501		7.50E-02		99.99781		28.059		7.50E-02		99.9997		28.059		7.50E-02		100.00047		25.16886		7.50E-02		99.99997		Riken PX-C		951.050		453.00

		28.83		0.1		99.99041		99.99959		26.115		0.1		99.9981		25.504		0.1		99.99768		28.059		0.1		99.99959		28.059		0.1		100.0004		25.17544		0.1		100.00002		PVD AF 620°C		992.670		450.96

		28.832		0.125		99.9911		99.99951		26.113		0.125		100.00099		25.495		0.125		99.99942		28.059		0.125		99.99951		28.059		0.125		100.00038		25.17767		0.125		100.00009		PVD AF 770°C		1008.030		461.71

		28.828		0.15		99.99442		99.99945		26.113		0.15		100.00228		25.497		0.15		100.00184		28.059		0.15		99.99945		28.059		0.15		100.00042		25.18689		0.15		100.00014

		28.836		0.175		99.9927		99.99934		26.116		0.175		99.99919		25.501		0.175		100.00515		28.059		0.175		99.99934		28.059		0.175		100.0004		25.19011		0.175		100.00019		ŽELENA KRIVULJA

		28.825		0.2		99.99236		99.99927		26.104		0.2		100.00404		25.491		0.2		100.00218		28.059		0.2		99.99927		28.059		0.2		100.00038		25.19744		0.2		100.00023

		28.827		0.225		99.98886		99.99921		26.113		0.225		99.99884		25.485		0.225		100.00363		28.059		0.225		99.99921		28.059		0.225		100.00037		25.20222		0.225		100.00028

		28.831		0.25		99.98565		99.99914		26.105		0.25		99.99595		25.479		0.25		100.00332		28.059		0.25		99.99914		28.059		0.25		100.00036		25.20778		0.25		100.00032

		28.833		0.275		99.98721		99.99907		26.108		0.275		100.00239		25.489		0.275		100.0038		28.059		0.275		99.99907		28.059		0.275		100.00033		25.21356		0.275		100.00036

		28.834		0.3		99.98724		99.999		26.107		0.3		99.99653		25.482		0.3		100.00475		28.059		0.3		99.999		28.059		0.3		100.0003		25.21611		0.3		100.0004

		28.839		0.325		99.98636		99.99892		26.104		0.325		99.9987		25.489		0.325		100.00292		28.059		0.325		99.99892		28.059		0.325		100.00027		25.219		0.325		100.00043

		28.833		0.35		99.98353		99.99884		26.113		0.35		99.99445		25.485		0.35		100.00253		28.059		0.35		99.99884		28.059		0.35		100.00023		25.22244		0.35		100.00045

		28.833		0.375		99.98484		99.99875		26.116		0.375		99.9983		25.479		0.375		100.0034		28.059		0.375		99.99875		28.061		0.375		100.00019		25.22289		0.375		100.00047

		28.831		0.4		99.97902		99.99867		26.104		0.4		99.9972		25.485		0.4		100.00211		28.059		0.4		99.99867		28.06189		0.4		100.00016		25.223		0.4		100.00049

		28.846		0.425		99.98029		99.9986		26.099		0.425		100.00039		25.485		0.425		100.00305		28.059		0.425		99.9986		28.062		0.425		100.00012		25.223		0.425		100.00051

		28.837		0.45		99.97919		99.99852		26.12		0.45		99.9976		25.489		0.45		100.00259		28.059		0.45		99.99852		28.06878		0.45		100.00008		25.22633		0.45		100.00052

		28.848		0.475		99.97879		99.99844		26.115		0.475		99.99696		25.487		0.475		100.00226		28.059		0.475		99.99844		28.07244		0.475		100.00004		25.23633		0.475		100.00053

		28.84		0.5		99.97686		99.99836		26.125		0.5		99.99712		25.492		0.5		100.00234		28.059		0.5		99.99836		28.08533		0.5		99.99999		25.24922		0.5		100.00054

		28.843		0.525		99.97825		99.99829		26.122		0.525		99.99974		25.5		0.525		100.00271		28.059		0.525		99.99829		28.10011		0.525		99.99995		25.26533		0.525		100.00054

		28.846		0.55		99.97912		99.99821		26.124		0.55		100.0013		25.507		0.55		100.0045		28.06278		0.55		99.99821		28.11644		0.55		99.99991		25.28189		0.55		100.00055

		28.839		0.575		99.9786		99.99813		26.133		0.575		99.9969		25.504		0.575		100.00141		28.07211		0.575		99.99813		28.133		0.575		99.99986		25.29856		0.575		100.00055		Na sekundarno os bi morali dati tempearturo, čas pa v min., ker so bili materiali izpostavljeni 24 ur.

		28.851		0.6		99.9815		99.99806		26.131		0.6		99.99683		25.51		0.6		100.00169		28.08567		0.6		99.99806		28.14756		0.6		99.99982		25.31522		0.6		100.00054

		28.854		0.625		99.9798		99.99799		26.128		0.625		99.99647		25.509		0.625		100.00014		28.10178		0.625		99.99799		28.16322		0.625		99.99978		25.33189		0.625		100.00054

		28.855		0.65		99.98071		99.99792		26.132		0.65		99.9939		25.512		0.65		100.00044		28.11833		0.65		99.99792		28.17967		0.65		99.99974		25.34944		0.65		100.00054

		28.864		0.675		99.98327		99.99785		26.145		0.675		99.99564		25.518		0.675		100.00214		28.13489		0.675		99.99785		28.18944		0.675		99.9997		25.36567		0.675		100.00053

		28.87		0.7		99.98061		99.99779		26.154		0.7		99.99573		25.524		0.7		100.00061		28.15144		0.7		99.99779		28.20233		0.7		99.99967		25.38567		0.7		100.00052

		28.87		0.725		99.98315		99.99774		26.157		0.725		99.99734		25.526		0.725		100.00161		28.168		0.725		99.99774		28.20678		0.725		99.99964		25.40556		0.725		100.00052

		28.873		0.75		99.97991		99.99768		26.172		0.75		99.99568		25.532		0.75		100.00007		28.18456		0.75		99.99768		28.20867		0.75		99.99961		25.42922		0.75		100.00051

		28.876		0.775		99.98285		99.99764		26.172		0.775		99.99825		25.54		0.775		100.00141		28.19733		0.775		99.99764		28.21389		0.775		99.99959		25.46056		0.775		100.00051

		28.875		0.8		99.98137		99.99759		26.173		0.8		99.99533		25.545		0.8		99.99971		28.20667		0.8		99.99759		28.22811		0.8		99.99957		25.49344		0.8		100.0005

		28.89		0.825		99.98366		99.99756		26.182		0.825		99.99936		25.551		0.825		100.00206		28.22078		0.825		99.99756		28.24444		0.825		99.99956		25.52656		0.825		100.0005

		28.894		0.85		99.98036		99.99752		26.195		0.85		99.99412		25.552		0.85		99.99997		28.23489		0.85		99.99752		28.26111		0.85		99.99955		25.55967		0.85		100.0005

		28.897		0.875		99.98181		99.99749		26.201		0.875		99.99556		25.567		0.875		99.99785		28.25111		0.875		99.99749		28.28056		0.875		99.99955		25.59433		0.875		100.00051

		28.898		0.9		99.98054		99.99747		26.206		0.9		99.99341		25.58		0.9		100.00005		28.27111		0.9		99.99747		28.305		0.9		99.99956		25.63356		0.9		100.00051

		28.906		0.925		99.98079		99.99745		26.221		0.925		99.99631		25.589		0.925		100		28.28922		0.925		99.99745		28.33667		0.925		99.99957		25.66767		0.925		100.00052

		28.915		0.95		99.9824		99.99744		26.232		0.95		99.99549		25.6		0.95		100.00144		28.31711		0.95		99.99744		28.36889		0.95		99.99959		25.70411		0.95		100.00053

		28.915		0.975		99.98028		99.99743		26.235		0.975		99.99952		25.607		0.975		100.00318		28.34811		0.975		99.99743		28.402		0.975		99.99961		25.74544		0.975		100.00055

		28.93		1		99.98061		99.99743		26.247		1		100.00058		25.613		1		100.00166		28.38067		1		99.99743		28.43022		1		99.99965		25.78033		1		100.00056

		28.934		1.025		99.98362		99.99743		26.25		1.025		99.99842		25.624		1.025		100.00251		28.41167		1.025		99.99743		28.44922		1.025		99.99968		25.81378		1.025		100.00058

		28.941		1.05		99.9853		99.99743		26.267		1.05		99.99432		25.635		1.05		100.00088		28.43378		1.05		99.99743		28.47667		1.05		99.99972		25.847		1.05		100.0006

		28.956		1.075		99.98915		99.99744		26.276		1.075		99.99638		25.647		1.075		100.00071		28.45333		1.075		99.99744		28.50656		1.075		99.99976		25.88022		1.075		100.00063

		28.948		1.1		99.99399		99.99745		26.284		1.1		99.99769		25.666		1.1		100.00178		28.47033		1.1		99.99745		28.53644		1.1		99.99981		25.92167		1.1		100.00065

		28.96		1.125		100.00232		99.99747		26.296		1.125		99.99529		25.679		1.125		100.00069		28.48533		1.125		99.99747		28.56178		1.125		99.99986		25.96167		1.125		100.00068

		28.964		1.15		100.00685		99.9975		26.304		1.15		99.9959		25.695		1.15		100.00101		28.51089		1.15		99.9975		28.57989		1.15		99.99991		25.997		1.15		100.00071

		28.985		1.175		100.0111		99.99752		26.325		1.175		99.99979		25.694		1.175		100.00102		28.532		1.175		99.99752		28.59667		1.175		99.99996		26.02733		1.175		100.00074

		28.993		1.2		100.01301		99.99755		26.332		1.2		99.99503		25.706		1.2		100.00266		28.55067		1.2		99.99755		28.61322		1.2		100		26.04756		1.2		100.00077

		29.003		1.225		100.00873		99.99758		26.334		1.225		99.99748		25.727		1.225		100.00093		28.56789		1.225		99.99758		28.63756		1.225		100.00005		26.07356		1.225		100.00081

		29.018		1.25		100.0109		99.99762		26.358		1.25		99.99881		25.739		1.25		100.00055		28.58456		1.25		99.99762		28.66911		1.25		100.00009		26.10256		1.25		100.00084

		29.017		1.275		100.01457		99.99765		26.359		1.275		99.99286		25.756		1.275		100.00225		28.60111		1.275		99.99765		28.69311		1.275		100.00013		26.13511		1.275		100.00087

		29.024		1.3		100.01149		99.99769		26.373		1.3		99.99363		25.766		1.3		99.99992		28.62622		1.3		99.99769		28.72244		1.3		100.00017		26.18011		1.3		100.00091

		29.035		1.325		100.01297		99.99773		26.383		1.325		99.99693		25.776		1.325		100.00304		28.65733		1.325		99.99773		28.75522		1.325		100.0002		26.21844		1.325		100.00094

		29.042		1.35		100.01091		99.99777		26.392		1.35		99.99628		25.789		1.35		100.00126		28.68833		1.35		99.99777		28.78833		1.35		100.00023		26.25222		1.35		100.00097

		29.054		1.375		100.01038		99.99781		26.411		1.375		99.9989		25.803		1.375		100.00448		28.71633		1.375		99.99781		28.82156		1.375		100.00026		26.28544		1.375		100.001

		29.056		1.4		100.01056		99.99785		26.427		1.4		99.99329		25.824		1.4		100.00175		28.74422		1.4		99.99785		28.85478		1.4		100.00028		26.31856		1.4		100.00103

		29.08		1.425		100.01026		99.99789		26.438		1.425		99.99633		25.835		1.425		100.00018		28.77489		1.425		99.99789		28.89178		1.425		100.0003		26.35778		1.425		100.00106

		29.09		1.45		100.00985		99.99793		26.449		1.45		99.99627		25.845		1.45		100.00062		28.80778		1.45		99.99793		28.93067		1.45		100.00032		26.39711		1.45		100.00109

		29.1		1.475		100.01038		99.99797		26.463		1.475		99.99398		25.857		1.475		100.00191		28.841		1.475		99.99797		28.965		1.475		100.00034		26.43433		1.475		100.00112

		29.112		1.5		100.00837		99.99801		26.474		1.5		99.9963		25.865		1.5		99.99972		28.87811		1.5		99.99801		28.99678		1.5		100.00035		26.46811		1.5		100.00115

		29.121		1.525		100.0107		99.99805		26.488		1.525		99.99647		25.881		1.525		100.00247		28.91267		1.525		99.99805		29.02044		1.525		100.00037		26.49533		1.525		100.00117

		29.144		1.55		100.01116		99.99809		26.501		1.55		99.99776		25.912		1.55		100.0039		28.94656		1.55		99.99809		29.04767		1.55		100.00039		26.52778		1.55		100.0012

		29.152		1.575		100.00859		99.99813		26.509		1.575		99.99619		25.915		1.575		100.00332		28.97989		1.575		99.99813		29.08		1.575		100.00041		26.57033		1.575		100.00122

		29.16		1.6		100.01023		99.99817		26.538		1.6		99.9965		25.928		1.6		100.00398		29.00778		1.6		99.99817		29.12244		1.6		100.00043		26.61856		1.6		100.00125

		29.178		1.625		100.00918		99.99821		26.546		1.625		99.99656		25.947		1.625		100.00521		29.03044		1.625		99.99821		29.17111		1.625		100.00045		26.66811		1.625		100.00127

		29.183		1.65		100.01039		99.99825		26.556		1.65		99.99616		25.969		1.65		100.0017		29.06244		1.65		99.99825		29.21689		1.65		100.00047		26.71		1.65		100.0013

		29.195		1.675		100.01408		99.99828		26.576		1.675		99.99503		25.975		1.675		100.00055		29.09533		1.675		99.99828		29.25311		1.675		100.0005		26.75267		1.675		100.00132

		29.208		1.7		100.01271		99.99832		26.601		1.7		99.99958		25.994		1.7		99.99975		29.13333		1.7		99.99832		29.29167		1.7		100.00053		26.80133		1.7		100.00135

		29.231		1.725		100.01131		99.99835		26.619		1.725		99.99366		26.009		1.725		99.99842		29.17756		1.725		99.99835		29.33989		1.725		100.00056		26.85089		1.725		100.00138

		29.241		1.75		100.00987		99.99838		26.628		1.75		99.9983		26.025		1.75		99.99556		29.21711		1.75		99.99838		29.39311		1.75		100.00059		26.89467		1.75		100.0014

		29.253		1.775		100.01232		99.99841		26.642		1.775		99.9945		26.038		1.775		100.00131		29.25156		1.775		99.99841		29.44556		1.775		100.00062		26.94244		1.775		100.00143

		29.267		1.8		100.00912		99.99844		26.661		1.8		99.99595		26.054		1.8		99.99802		29.28967		1.8		99.99844		29.49567		1.8		100.00065		26.98711		1.8		100.00145

		29.285		1.825		100.01129		99.99847		26.677		1.825		99.99592		26.074		1.825		99.99974		29.33689		1.825		99.99847		29.536		1.825		100.00068		27.03622		1.825		100.00148

		29.307		1.85		100.00887		99.99849		26.69		1.85		99.99748		26.088		1.85		100.00005		29.39144		1.85		99.99849		29.57222		1.85		100.00071		27.08589		1.85		100.0015

		29.316		1.875		100.00976		99.99852		26.707		1.875		99.99754		26.113		1.875		100.00055		29.43989		1.875		99.99852		29.61556		1.875		100.00074		27.13567		1.875		100.00153

		29.341		1.9		100.00984		99.99854		26.729		1.9		99.99762		26.137		1.9		100.00209		29.48956		1.9		99.99854		29.66444		1.9		100.00076		27.18922		1.9		100.00155

		29.344		1.925		100.01087		99.99856		26.743		1.925		99.99346		26.155		1.925		100.00116		29.53433		1.925		99.99856		29.70911		1.925		100.00079		27.24156		1.925		100.00158

		29.358		1.95		100.0093		99.99858		26.772		1.95		99.99509		26.164		1.95		100.00277		29.57189		1.95		99.99858		29.74378		1.95		100.00081		27.306		1.95		100.0016

		29.369		1.975		100.00925		99.9986		26.781		1.975		99.99893		26.195		1.975		100.00041		29.619		1.975		99.9986		29.77733		1.975		100.00083		27.37211		1.975		100.00162

		29.391		2		100.01067		99.99863		26.808		2		99.9936		26.213		2		100.0029		29.66833		2		99.99863		29.80744		2		100.00086		27.426		2		100.00165

		29.413		2.025		100.0107		99.99865		26.829		2.025		99.99653		26.235		2.025		99.99957		29.71333		2.025		99.99865		29.84222		2.025		100.00088		27.48178		2.025		100.00167

		29.427		2.05		100.01017		99.99868		26.847		2.05		99.99437		26.249		2.05		100.00276		29.75289		2.05		99.99868		29.88744		2.05		100.0009		27.53289		2.05		100.00169

		29.437		2.075		100.01011		99.9987		26.864		2.075		99.9966		26.268		2.075		100.00371		29.78578		2.075		99.9987		29.93411		2.075		100.00093		27.58289		2.075		100.00172

		29.458		2.1		100.01132		99.99873		26.879		2.1		99.9984		26.284		2.1		100.00305		29.824		2.1		99.99873		29.97322		2.1		100.00096		27.63789		2.1		100.00174

		29.475		2.125		100.01		99.99876		26.904		2.125		99.9954		26.305		2.125		100.00276		29.868		2.125		99.99876		30.01689		2.125		100.00099		27.68822		2.125		100.00177

		29.504		2.15		100.00751		99.99879		26.923		2.15		99.99586		26.321		2.15		99.99979		29.91656		2.15		99.99879		30.065		2.15		100.00102		27.74256		2.15		100.0018

		29.525		2.175		100.00897		99.99883		26.933		2.175		99.99309		26.355		2.175		100.00322		29.96289		2.175		99.99883		30.11367		2.175		100.00105		27.79289		2.175		100.00183

		29.533		2.2		100.0097		99.99886		26.95		2.2		99.99559		26.367		2.2		100.00123		30.00333		2.2		99.99886		30.16933		2.2		100.00108		27.84367		2.2		100.00186

		29.552		2.225		100.01008		99.9989		26.981		2.225		99.99751		26.401		2.225		100.00251		30.04989		2.225		99.9989		30.22578		2.225		100.00112		27.90633		2.225		100.00189

		29.575		2.25		100.012		99.99893		27		2.25		99.99365		26.425		2.25		100.00069		30.09833		2.25		99.99893		30.28711		2.25		100.00115		27.962		2.25		100.00192

		29.6		2.275		100.01034		99.99897		27.023		2.275		100.00151		26.449		2.275		100.00244		30.14422		2.275		99.99897		30.33933		2.275		100.00119		28.01956		2.275		100.00195

		29.601		2.3		100.00998		99.99901		27.041		2.3		99.99586		26.469		2.3		100.00303		30.20178		2.3		99.99901		30.396		2.3		100.00123		28.08822		2.3		100.00199

		29.633		2.325		100.00966		99.99904		27.066		2.325		99.99412		26.489		2.325		99.99814		30.25956		2.325		99.99904		30.45867		2.325		100.00127		28.164		2.325		100.00202

		29.654		2.35		100.01157		99.99908		27.087		2.35		99.99924		26.505		2.35		100.00181		30.31289		2.35		99.99908		30.51278		2.35		100.0013		28.234		2.35		100.00206

		29.668		2.375		100.01268		99.99911		27.115		2.375		99.99256		26.533		2.375		99.99898		30.36189		2.375		99.99911		30.56389		2.375		100.00134		28.29933		2.375		100.00209

		29.686		2.4		100.01048		99.99914		27.13		2.4		99.9981		26.563		2.4		99.99921		30.41033		2.4		99.99914		30.62389		2.4		100.00138		28.36522		2.4		100.00212

		29.71		2.425		100.0125		99.99917		27.151		2.425		99.99924		26.584		2.425		100.00444		30.46767		2.425		99.99917		30.67844		2.425		100.00141		28.43056		2.425		100.00216

		29.739		2.45		100.00884		99.9992		27.175		2.45		99.99066		26.609		2.45		100.00026		30.51833		2.45		99.9992		30.73956		2.45		100.00145		28.49511		2.45		100.00219

		29.745		2.475		100.01019		99.99923		27.208		2.475		99.99661		26.618		2.475		100.00149		30.567		2.475		99.99923		30.78956		2.475		100.00148		28.56656		2.475		100.00222

		29.774		2.5		100.01179		99.99925		27.221		2.5		99.99749		26.656		2.5		100.00023		30.62989		2.5		99.99925		30.84678		2.5		100.00151		28.64089		2.5		100.00226

		29.796		2.525		100.01107		99.99928		27.244		2.525		99.99365		26.682		2.525		99.99843		30.69278		2.525		99.99928		30.90444		2.525		100.00155		28.70778		2.525		100.00229

		29.825		2.55		100.00935		99.9993		27.271		2.55		99.9982		26.711		2.55		100.00233		30.74722		2.55		99.9993		30.96833		2.55		100.00158		28.772		2.55		100.00232

		29.852		2.575		100.01025		99.99933		27.297		2.575		99.99418		26.744		2.575		100.00363		30.79944		2.575		99.99933		31.03267		2.575		100.00161		28.838		2.575		100.00235

		29.876		2.6		100.01145		99.99935		27.331		2.6		99.99667		26.762		2.6		100		30.86089		2.6		99.99935		31.10133		2.6		100.00164		28.90589		2.6		100.00237

		29.896		2.625		100.0109		99.99937		27.343		2.625		99.99796		26.793		2.625		99.9976		30.93411		2.625		99.99937		31.169		2.625		100.00167		28.97489		2.625		100.0024

		29.919		2.65		100.01082		99.99939		27.373		2.65		99.99553		26.82		2.65		99.99988		30.99978		2.65		99.99939		31.239		2.65		100.00171		29.055		2.65		100.00243

		29.949		2.675		100.01032		99.99941		27.411		2.675		99.99813		26.842		2.675		100.00279		31.06444		2.675		99.99941		31.30567		2.675		100.00174		29.12556		2.675		100.00245

		29.972		2.7		100.01246		99.99944		27.429		2.7		99.99754		26.879		2.7		100.00042		31.14044		2.7		99.99944		31.38367		2.7		100.00177		29.19744		2.7		100.00248

		29.986		2.725		100.01161		99.99946		27.463		2.725		99.99945		26.903		2.725		100.00172		31.20478		2.725		99.99946		31.45511		2.725		100.0018		29.26822		2.725		100.0025

		30.01		2.75		100.01195		99.99948		27.489		2.75		99.99227		26.922		2.75		99.99661		31.25933		2.75		99.99948		31.52833		2.75		100.00183		29.34611		2.75		100.00252

		30.048		2.775		100.00859		99.9995		27.513		2.775		99.99623		26.963		2.775		99.99838		31.32067		2.775		99.9995		31.59433		2.775		100.00187		29.41611		2.775		100.00255

		30.069		2.8		100.00892		99.99952		27.545		2.8		99.99627		26.993		2.8		100.00116		31.394		2.8		99.99952		31.661		2.8		100.0019		29.495		2.8		100.00257

		30.09		2.825		100.01111		99.99954		27.563		2.825		99.99677		27.02		2.825		99.99974		31.461		2.825		99.99954		31.733		2.825		100.00193		29.57067		2.825		100.00259

		30.102		2.85		100.00869		99.99956		27.6		2.85		99.99766		27.058		2.85		100.0044		31.52678		2.85		99.99956		31.81056		2.85		100.00196		29.639		2.85		100.00262

		30.135		2.875		100.01264		99.99958		27.617		2.875		99.99486		27.085		2.875		100.00154		31.59144		2.875		99.99958		31.884		2.875		100.002		29.70444		2.875		100.00264

		30.167		2.9		100.01191		99.9996		27.653		2.9		99.99748		27.116		2.9		100.00021		31.65767		2.9		99.9996		31.95944		2.9		100.00203		29.78233		2.9		100.00266

		30.195		2.925		100.01049		99.99963		27.676		2.925		99.99631		27.136		2.925		100.00164		31.72567		2.925		99.99963		32.026		2.925		100.00206		29.85389		2.925		100.00269

		30.219		2.95		100.00875		99.99965		27.709		2.95		99.99661		27.175		2.95		100.00217		31.80233		2.95		99.99965		32.09811		2.95		100.00209		29.92833		2.95		100.00271

		30.251		2.975		100.00858		99.99967		27.734		2.975		99.99878		27.208		2.975		100.00086		31.88033		2.975		99.99967		32.16755		2.975		100.00212		29.99522		2.975		100.00274

		30.272		3		100.00821		99.99969		27.766		3		99.99432		27.236		3		100.00254		31.955		3		99.99969		32.24611		3		100.00215		30.07367		3		100.00276

		30.304		3.025		100.01039		99.99972		27.8		3.025		99.99447		27.263		3.025		100.00271		32.02233		3.025		99.99972		32.32433		3.025		100.00218		30.15411		3.025		100.00279

		30.339		3.05		100.00867		99.99974		27.83		3.05		99.99105		27.299		3.05		99.99833		32.087		3.05		99.99974		32.40222		3.05		100.00221		30.23511		3.05		100.00282

		30.359		3.075		100.01048		99.99977		27.863		3.075		99.99507		27.331		3.075		100.00257		32.15256		3.075		99.99977		32.47911		3.075		100.00224		30.31656		3.075		100.00284

		30.398		3.1		100.0087		99.99979		27.886		3.1		99.99655		27.365		3.1		99.99801		32.22644		3.1		99.99979		32.559		3.1		100.00226		30.399		3.1		100.00287

		30.426		3.125		100.01052		99.99982		27.917		3.125		99.99743		27.397		3.125		100.00307		32.30422		3.125		99.99982		32.63478		3.125		100.00228		30.47167		3.125		100.0029

		30.452		3.15		100.01177		99.99985		27.961		3.15		99.99601		27.42		3.15		100.00295		32.37722		3.15		99.99985		32.71467		3.15		100.00231		30.55289		3.15		100.00292

		30.489		3.175		100.00994		99.99989		27.984		3.175		99.99568		27.456		3.175		100.00032		32.451		3.175		99.99989		32.78767		3.175		100.00233		30.63589		3.175		100.00295

		30.521		3.2		100.0123		99.99993		28.023		3.2		99.99535		27.494		3.2		100.00309		32.53056		3.2		99.99993		32.86922		3.2		100.00235		30.72211		3.2		100.00297

		30.553		3.225		100.01032		99.99997		28.051		3.225		99.99908		27.532		3.225		100.00318		32.61144		3.225		99.99997		32.95		3.225		100.00236		30.80878		3.225		100.00299

		30.589		3.25		100.01275		100.00001		28.083		3.25		99.99786		27.576		3.25		100.00121		32.692		3.25		100.00001		33.03389		3.25		100.00238		30.89222		3.25		100.00301

		30.617		3.275		100.0073		100.00005		28.125		3.275		99.99574		27.603		3.275		100.00152		32.77467		3.275		100.00005		33.11711		3.275		100.00239		30.97311		3.275		100.00303

		30.633		3.3		100.00926		100.0001		28.155		3.3		99.9969		27.643		3.3		99.99637		32.85878		3.3		100.0001		33.18911		3.3		100.00241		31.06322		3.3		100.00304

		30.671		3.325		100.00938		100.00015		28.183		3.325		99.99849		27.673		3.325		100.00239		32.944		3.325		100.00015		33.26756		3.325		100.00242		31.14533		3.325		100.00306

		30.699		3.35		100.01074		100.00019		28.224		3.35		99.99545		27.718		3.35		100.00151		33.029		3.35		100.00019		33.35467		3.35		100.00243		31.23589		3.35		100.00307

		30.739		3.375		100.01153		100.00024		28.256		3.375		99.99568		27.742		3.375		100.00001		33.11633		3.375		100.00024		33.43611		3.375		100.00245		31.33		3.375		100.00308

		30.761		3.4		100.00964		100.00029		28.293		3.4		99.99711		27.776		3.4		99.99824		33.19378		3.4		100.00029		33.52967		3.4		100.00246		31.414		3.4		100.00309

		30.807		3.425		100.00856		100.00034		28.318		3.425		99.99308		27.817		3.425		100.00327		33.27333		3.425		100.00034		33.61		3.425		100.00248		31.50367		3.425		100.0031

		30.834		3.45		100.01025		100.00039		28.356		3.45		99.99645		27.856		3.45		100.00038		33.36044		3.45		100.00039		33.68744		3.45		100.00249		31.58356		3.45		100.00311

		30.87		3.475		100.01178		100.00044		28.389		3.475		99.994		27.889		3.475		100.00638		33.44478		3.475		100.00044		33.775		3.475		100.00251		31.66822		3.475		100.00313

		30.904		3.5		100.01292		100.00049		28.431		3.5		99.99527		27.925		3.5		100.00115		33.53722		3.5		100.00049		33.85689		3.5		100.00253		31.76289		3.5		100.00314

		30.931		3.525		100.0138		100.00053		28.461		3.525		99.99508		27.966		3.525		100.00467		33.62067		3.525		100.00053		33.94656		3.525		100.00255		31.85422		3.525		100.00316

		30.97		3.55		100.01234		100.00058		28.494		3.55		99.99947		28.002		3.55		100.00054		33.70189		3.55		100.00058		34.03911		3.55		100.00257		31.95011		3.55		100.00318

		31		3.575		100.01188		100.00062		28.527		3.575		99.99592		28.042		3.575		100.0014		33.79211		3.575		100.00062		34.12189		3.575		100.0026		32.04078		3.575		100.0032

		31.026		3.6		100.01292		100.00067		28.571		3.6		99.99644		28.078		3.6		100.00065		33.87389		3.6		100.00067		34.21056		3.6		100.00263		32.13144		3.6		100.00323

		31.074		3.625		100.01044		100.00071		28.606		3.625		99.99378		28.119		3.625		100.00127		33.974		3.625		100.00071		34.29322		3.625		100.00267		32.22567		3.625		100.00327

		31.111		3.65		100.01125		100.00076		28.656		3.65		99.99666		28.158		3.65		100.00277		34.07122		3.65		100.00076		34.38567		3.65		100.0027		32.31956		3.65		100.0033

		31.146		3.675		100.01266		100.00081		28.682		3.675		99.99606		28.203		3.675		100.00377		34.16011		3.675		100.00081		34.48433		3.675		100.00274		32.427		3.675		100.00334

		31.171		3.7		100.0108		100.00085		28.72		3.7		99.99772		28.232		3.7		100.00161		34.25267		3.7		100.00085		34.57044		3.7		100.00279		32.52744		3.7		100.00339

		31.217		3.725		100.01119		100.0009		28.754		3.725		99.99558		28.285		3.725		100.00115		34.34056		3.725		100.0009		34.66478		3.725		100.00284		32.62489		3.725		100.00344

		31.25		3.75		100.01207		100.00095		28.8		3.75		99.99434		28.325		3.75		100.00259		34.44033		3.75		100.00095		34.75389		3.75		100.00289		32.72344		3.75		100.00349

		31.29		3.775		100.01039		100.00099		28.836		3.775		99.99762		28.361		3.775		100.00201		34.53733		3.775		100.00099		34.84622		3.775		100.00294		32.83133		3.775		100.00355

		31.331		3.8		100.01209		100.00104		28.876		3.8		99.99663		28.412		3.8		100.00232		34.63067		3.8		100.00104		34.94233		3.8		100.003		32.938		3.8		100.0036

		31.366		3.825		100.01215		100.00108		28.912		3.825		99.99587		28.447		3.825		100.00019		34.72678		3.825		100.00108		35.03833		3.825		100.00306		33.04078		3.825		100.00366

		31.4		3.85		100.01032		100.00113		28.947		3.85		99.99958		28.476		3.85		100.00223		34.81367		3.85		100.00113		35.13489		3.85		100.00312		33.14578		3.85		100.00371

		31.44		3.875		100.01038		100.00117		28.989		3.875		99.99476		28.527		3.875		100.00095		34.90767		3.875		100.00117		35.22433		3.875		100.00318		33.25511		3.875		100.00377

		31.481		3.9		100.00928		100.0012		29.044		3.9		99.99579		28.57		3.9		99.99994		35.00089		3.9		100.0012		35.30622		3.9		100.00324		33.35378		3.9		100.00382

		31.516		3.925		100.01182		100.00124		29.08		3.925		99.99624		28.618		3.925		100.00363		35.09644		3.925		100.00124		35.40011		3.925		100.0033		33.45733		3.925		100.00386

		31.561		3.95		100.01284		100.00127		29.122		3.95		100.00066		28.656		3.95		100.00154		35.19267		3.95		100.00127		35.48711		3.95		100.00336		33.55811		3.95		100.00391

		31.602		3.975		100.01139		100.0013		29.154		3.975		99.99496		28.704		3.975		100.00322		35.27956		3.975		100.0013		35.58067		3.975		100.00343		33.66733		3.975		100.00395

		31.638		4		100.01106		100.00133		29.197		4		99.99336		28.741		4		99.9992		35.37122		4		100.00133		35.66567		4		100.00349		33.76856		4		100.00399

		31.674		4.025		100.01111		100.00136		29.244		4.025		99.99995		28.783		4.025		100.00453		35.45911		4.025		100.00136		35.75911		4.025		100.00355		33.87333		4.025		100.00402

		31.724		4.05		100.01		100.00138		29.279		4.05		99.9953		28.828		4.05		100.00684		35.55433		4.05		100.00138		35.84989		4.05		100.00361		33.98189		4.05		100.00405

		31.757		4.075		100.01211		100.00141		29.326		4.075		99.99749		28.871		4.075		100.00051		35.64567		4.075		100.00141		35.94767		4.075		100.00368		34.08822		4.075		100.00408

		31.8		4.1		100.01399		100.00143		29.374		4.1		99.99677		28.907		4.1		100.00247		35.738		4.1		100.00143		36.05378		4.1		100.00374		34.19044		4.1		100.00411

		31.843		4.125		100.00983		100.00146		29.412		4.125		99.99836		28.956		4.125		100.00013		35.83089		4.125		100.00146		36.16356		4.125		100.0038		34.29444		4.125		100.00414

		31.88		4.15		100.00869		100.00148		29.457		4.15		99.99342		29.005		4.15		100.00271		35.92689		4.15		100.00148		36.26267		4.15		100.00387		34.40367		4.15		100.00416

		31.923		4.175		100.00911		100.00151		29.504		4.175		99.99601		29.046		4.175		100.0006		36.03144		4.175		100.00151		36.36811		4.175		100.00393		34.51278		4.175		100.00419

		31.972		4.2		100.00845		100.00154		29.537		4.2		99.99753		29.088		4.2		100.00251		36.13322		4.2		100.00154		36.47878		4.2		100.004		34.61656		4.2		100.00422

		32.014		4.225		100.01068		100.00158		29.583		4.225		99.99865		29.125		4.225		100.00175		36.23422		4.225		100.00158		36.58733		4.225		100.00407		34.72367		4.225		100.00425

		32.051		4.25		100.01256		100.00161		29.621		4.25		99.99573		29.18		4.25		100.00006		36.33578		4.25		100.00161		36.68711		4.25		100.00413		34.83733		4.25		100.00428

		32.093		4.275		100.01192		100.00165		29.674		4.275		99.99827		29.225		4.275		100.00398		36.44244		4.275		100.00165		36.79078		4.275		100.0042		34.94344		4.275		100.00431

		32.13		4.3		100.01239		100.00169		29.724		4.3		99.99704		29.273		4.3		100.00158		36.54767		4.3		100.00169		36.89667		4.3		100.00427		35.05356		4.3		100.00434

		32.173		4.325		100.01072		100.00174		29.771		4.325		99.99832		29.326		4.325		100.00134		36.64922		4.325		100.00174		36.99467		4.325		100.00434		35.156		4.325		100.00437

		32.217		4.35		100.00858		100.00179		29.822		4.35		99.99673		29.368		4.35		100.00482		36.74856		4.35		100.00179		37.09411		4.35		100.00441		35.26678		4.35		100.0044

		32.27		4.375		100.01209		100.00183		29.858		4.375		99.99747		29.424		4.375		100.00419		36.85356		4.375		100.00183		37.2		4.375		100.00448		35.36878		4.375		100.00444

		32.311		4.4		100.01099		100.00188		29.909		4.4		99.99833		29.473		4.4		100.00207		36.95222		4.4		100.00188		37.31078		4.4		100.00454		35.47856		4.4		100.00447

		32.354		4.425		100.0098		100.00193		29.954		4.425		99.99851		29.52		4.425		99.99892		37.05989		4.425		100.00193		37.41222		4.425		100.0046		35.58411		4.425		100.0045

		32.403		4.45		100.01405		100.00197		29.994		4.45		99.99767		29.571		4.45		100.0052		37.16056		4.45		100.00197		37.52178		4.45		100.00466		35.69756		4.45		100.00452

		32.458		4.475		100.01275		100.00202		30.038		4.475		99.99881		29.618		4.475		100.00746		37.26978		4.475		100.00202		37.63411		4.475		100.00472		35.80278		4.475		100.00455

		32.49		4.5		100.01136		100.00206		30.1		4.5		99.9978		29.672		4.5		100.00122		37.373		4.5		100.00206		37.75055		4.5		100.00477		35.91956		4.5		100.00458

		32.536		4.525		100.0111		100.0021		30.151		4.525		99.99966		29.72		4.525		99.99996		37.48344		4.525		100.0021		37.86011		4.525		100.00482		36.03278		4.525		100.0046

		32.578		4.55		100.0136		100.00214		30.19		4.55		99.99803		29.771		4.55		100.00772		37.59611		4.55		100.00214		37.98244		4.55		100.00486		36.15556		4.55		100.00462

		32.631		4.575		100.01228		100.00218		30.229		4.575		99.99833		29.822		4.575		100.00527		37.71567		4.575		100.00218		38.09644		4.575		100.0049		36.27433		4.575		100.00464

		32.684		4.6		100.01031		100.00221		30.295		4.6		99.99537		29.878		4.6		100.00158		37.82211		4.6		100.00221		38.21433		4.6		100.00493		36.40022		4.6		100.00466

		32.731		4.625		100.01154		100.00224		30.34		4.625		99.99825		29.92		4.625		100.00318		37.93467		4.625		100.00224		38.324		4.625		100.00496		36.52589		4.625		100.00468

		32.768		4.65		100.01106		100.00226		30.392		4.65		99.99494		29.969		4.65		100.00255		38.04978		4.65		100.00226		38.444		4.65		100.00499		36.65144		4.65		100.00469

		32.814		4.675		100.01228		100.00228		30.435		4.675		99.99935		30.024		4.675		100.00233		38.16989		4.675		100.00228		38.55611		4.675		100.00502		36.77755		4.675		100.00471

		32.861		4.7		100.00998		100.0023		30.488		4.7		99.99685		30.077		4.7		100.00295		38.28444		4.7		100.0023		38.66878		4.7		100.00504		36.90411		4.7		100.00472

		32.91		4.725		100.00996		100.00232		30.541		4.725		99.99767		30.129		4.725		100.00392		38.40722		4.725		100.00232		38.78144		4.725		100.00506		37.02344		4.725		100.00474

		32.969		4.75		100.01094		100.00233		30.586		4.75		99.99739		30.173		4.75		99.99952		38.52222		4.75		100.00233		38.90056		4.75		100.00509		37.14589		4.75		100.00475

		33.015		4.775		100.0107		100.00235		30.647		4.775		99.99649		30.224		4.775		100.00304		38.63589		4.775		100.00235		39.01189		4.775		100.00511		37.27267		4.775		100.00477

		33.068		4.8		100.00554		100.00236		30.71		4.8		99.99689		30.286		4.8		99.99786		38.75044		4.8		100.00236		39.13611		4.8		100.00514		37.40022		4.8		100.00479

		33.119		4.825		100.0093		100.00238		30.76		4.825		99.99917		30.333		4.825		100.00416		38.87533		4.825		100.00238		39.25711		4.825		100.00516		37.53		4.825		100.00481

		33.167		4.85		100.01042		100.00239		30.816		4.85		99.99804		30.39		4.85		100.0014		38.99567		4.85		100.00239		39.37744		4.85		100.00519		37.655		4.85		100.00483

		33.209		4.875		100.01073		100.00241		30.862		4.875		99.99531		30.446		4.875		100.00056		39.12111		4.875		100.00241		39.49656		4.875		100.00522		37.78167		4.875		100.00485

		33.254		4.9		100.00928		100.00242		30.904		4.9		99.99733		30.506		4.9		99.99805		39.24644		4.9		100.00242		39.62156		4.9		100.00525		37.90689		4.9		100.00487

		33.314		4.925		100.00751		100.00244		30.956		4.925		99.99545		30.568		4.925		100.00088		39.36944		4.925		100.00244		39.748		4.925		100.00528		38.03344		4.925		100.0049

		33.376		4.95		100.01245		100.00246		31.013		4.95		99.99895		30.627		4.95		99.99992		39.48789		4.95		100.00246		39.873		4.95		100.00532		38.16022		4.95		100.00492

		33.424		4.975		100.00913		100.00248		31.075		4.975		99.99591		30.674		4.975		99.99802		39.615		4.975		100.00248		39.99867		4.975		100.00535		38.28978		4.975		100.00495

		33.476		5		100.00983		100.0025		31.12		5		99.99503		30.728		5		99.9982		39.73989		5		100.0025		40.11967		5		100.00538		38.41867		5		100.00497

		33.534		5.025		100.01128		100.00252		31.175		5.025		99.99762		30.787		5.025		100.00068		39.86167		5.025		100.00252		40.23389		5.025		100.00541		38.54511		5.025		100.005

		33.585		5.05		100.00848		100.00254		31.227		5.05		99.99082		30.842		5.05		100.00235		39.98667		5.05		100.00254		40.35433		5.05		100.00544		38.66389		5.05		100.00503

		33.64		5.075		100.01074		100.00256		31.288		5.075		99.99504		30.9		5.075		100.00102		40.11322		5.075		100.00256		40.47878		5.075		100.00547		38.79444		5.075		100.00505

		33.687		5.1		100.01122		100.00259		31.342		5.1		99.99556		30.956		5.1		100.00394		40.22811		5.1		100.00259		40.60467		5.1		100.0055		38.92944		5.1		100.00508

		33.754		5.125		100.00921		100.00261		31.388		5.125		99.99766		31.004		5.125		100.00175		40.34956		5.125		100.00261		40.72967		5.125		100.00552		39.06322		5.125		100.0051

		33.8		5.15		100.01334		100.00263		31.447		5.15		99.99623		31.079		5.15		99.99831		40.47456		5.15		100.00263		40.85244		5.15		100.00554		39.19633		5.15		100.00513

		33.855		5.175		100.01029		100.00265		31.503		5.175		99.99743		31.121		5.175		100.00191		40.59667		5.175		100.00265		40.97122		5.175		100.00556		39.32956		5.175		100.00515

		33.904		5.2		100.01069		100.00268		31.56		5.2		99.99701		31.176		5.2		100.00998		40.72078		5.2		100.00268		41.09267		5.2		100.00557		39.47178		5.2		100.00517

		33.958		5.225		100.01099		100.0027		31.616		5.225		99.99613		31.236		5.225		99.99973		40.83911		5.225		100.0027		41.21889		5.225		100.00558		39.60522		5.225		100.0052

		34.021		5.25		100.01352		100.00272		31.665		5.25		99.99522		31.298		5.25		100.00055		40.96056		5.25		100.00272		41.34411		5.25		100.00559		39.74044		5.25		100.00522

		34.069		5.275		100.01025		100.00275		31.73		5.275		99.99748		31.345		5.275		99.99947		41.076		5.275		100.00275		41.47		5.275		100.0056		39.882		5.275		100.00524

		34.128		5.3		100.01201		100.00278		31.784		5.3		99.99884		31.414		5.3		100.008		41.19344		5.3		100.00278		41.59567		5.3		100.00561		40.01611		5.3		100.00526

		34.188		5.325		100.01068		100.00281		31.85		5.325		100.00163		31.473		5.325		100.00262		41.31678		5.325		100.00281		41.71767		5.325		100.00562		40.149		5.325		100.00528

		34.239		5.35		100.01068		100.00285		31.905		5.35		99.99764		31.53		5.35		100.00028		41.43489		5.35		100.00285		41.83733		5.35		100.00562		40.27678		5.35		100.0053

		34.297		5.375		100.01105		100.00289		31.967		5.375		99.99728		31.593		5.375		100.00008		41.55856		5.375		100.00289		41.96322		5.375		100.00563		40.41267		5.375		100.00532

		34.351		5.4		100.0123		100.00293		32.032		5.4		99.99771		31.658		5.4		100.00398		41.68289		5.4		100.00293		42.09133		5.4		100.00563		40.54811		5.4		100.00534

		34.418		5.425		100.01141		100.00298		32.089		5.425		99.99844		31.719		5.425		100.00225		41.80344		5.425		100.00298		42.21		5.425		100.00564		40.67922		5.425		100.00537

		34.458		5.45		100.0133		100.00303		32.151		5.45		100.00089		31.77		5.45		100.00441		41.93678		5.45		100.00303		42.33689		5.45		100.00565		40.80967		5.45		100.00539

		34.533		5.475		100.01031		100.00309		32.21		5.475		100.00029		31.836		5.475		100.00143		42.06744		5.475		100.00309		42.46744		5.475		100.00566		40.94078		5.475		100.00541

		34.578		5.5		100.01183		100.00314		32.268		5.5		99.99439		31.893		5.5		100.00626		42.19411		5.5		100.00314		42.6		5.5		100.00567		41.07544		5.5		100.00544

		34.636		5.525		100.00998		100.0032		32.33		5.525		99.999		31.964		5.525		100.00654		42.31978		5.525		100.0032		42.731		5.525		100.00569		41.21044		5.525		100.00547

		34.7		5.55		100.00962		100.00326		32.397		5.55		99.99715		32.03		5.55		100.002		42.44578		5.55		100.00326		42.85856		5.55		100.00571		41.34522		5.55		100.00549

		34.766		5.575		100.0115		100.00332		32.459		5.575		99.99374		32.083		5.575		100.00175		42.578		5.575		100.00332		42.99211		5.575		100.00573		41.48644		5.575		100.00552

		34.823		5.6		100.00882		100.00337		32.521		5.6		99.99961		32.151		5.6		100.00029		42.70478		5.6		100.00337		43.12033		5.6		100.00575		41.62356		5.6		100.00555

		34.881		5.625		100.01131		100.00343		32.59		5.625		99.99726		32.214		5.625		100.00191		42.83289		5.625		100.00343		43.25289		5.625		100.00578		41.75889		5.625		100.00558

		34.938		5.65		100.01238		100.00348		32.64		5.65		99.9993		32.279		5.65		100.00552		42.96111		5.65		100.00348		43.39244		5.65		100.00581		41.89611		5.65		100.00561

		34.998		5.675		100.01069		100.00353		32.713		5.675		99.99918		32.333		5.675		100.00325		43.08778		5.675		100.00353		43.527		5.675		100.00585		42.03878		5.675		100.00564

		35.053		5.7		100.00937		100.00357		32.772		5.7		99.99767		32.401		5.7		100.00086		43.21922		5.7		100.00357		43.66189		5.7		100.00589		42.17967		5.7		100.00567

		35.115		5.725		100.01047		100.00361		32.83		5.725		99.99734		32.463		5.725		100.00533		43.35367		5.725		100.00361		43.79422		5.725		100.00593		42.31978		5.725		100.0057

		35.187		5.75		100.01306		100.00365		32.895		5.75		99.99638		32.527		5.75		100.00053		43.49267		5.75		100.00365		43.93111		5.75		100.00598		42.46022		5.75		100.00574

		35.25		5.775		100.01047		100.00369		32.962		5.775		99.9966		32.584		5.775		100.00547		43.63222		5.775		100.00369		44.07933		5.775		100.00603		42.60478		5.775		100.00577

		35.306		5.8		100.00862		100.00372		33.03		5.8		99.99799		32.646		5.8		100.00168		43.766		5.8		100.00372		44.22222		5.8		100.00608		42.74333		5.8		100.0058

		35.368		5.825		100.01272		100.00375		33.091		5.825		100.00168		32.714		5.825		100.00033		43.90467		5.825		100.00375		44.363		5.825		100.00614		42.881		5.825		100.00584

		35.435		5.85		100.01165		100.00378		33.152		5.85		99.99928		32.797		5.85		100.00394		44.04233		5.85		100.00378		44.50678		5.85		100.0062		43.02778		5.85		100.00587

		35.487		5.875		100.01187		100.00382		33.217		5.875		99.99911		32.851		5.875		100.00111		44.185		5.875		100.00382		44.64644		5.875		100.00625		43.16933		5.875		100.0059

		35.56		5.9		100.012		100.00385		33.281		5.9		99.9971		32.917		5.9		100.00306		44.32456		5.9		100.00385		44.78689		5.9		100.00631		43.30822		5.9		100.00594

		35.624		5.925		100.01222		100.00389		33.345		5.925		99.99993		32.989		5.925		100.00592		44.46311		5.925		100.00389		44.93233		5.925		100.00637		43.45533		5.925		100.00597

		35.686		5.95		100.01073		100.00393		33.404		5.95		99.99946		33.053		5.95		100.0041		44.60678		5.95		100.00393		45.07156		5.95		100.00643		43.59567		5.95		100.00601

		35.747		5.975		100.01119		100.00397		33.469		5.975		99.99702		33.125		5.975		100.01079		44.74767		5.975		100.00397		45.21022		5.975		100.00648		43.73578		5.975		100.00604

		35.812		6		100.01052		100.00402		33.535		6		99.99443		33.198		6		100.00376		44.88867		6		100.00402		45.34689		6		100.00654		43.87844		6		100.00608

		35.875		6.025		100.013		100.00407		33.605		6.025		99.99963		33.257		6.025		100.00538		45.03289		6.025		100.00407		45.48722		6.025		100.00658		44.02444		6.025		100.00611

		35.943		6.05		100.01428		100.00412		33.672		6.05		99.99669		33.328		6.05		100.00745		45.17511		6.05		100.00412		45.63789		6.05		100.00662		44.17489		6.05		100.00614

		36.005		6.075		100.01208		100.00418		33.743		6.075		100.0016		33.398		6.075		100.00555		45.32189		6.075		100.00418		45.77944		6.075		100.00666		44.319		6.075		100.00617

		36.067		6.1		100.01034		100.00423		33.812		6.1		99.99687		33.458		6.1		100.00102		45.46578		6.1		100.00423		45.924		6.1		100.00669		44.47156		6.1		100.0062

		36.138		6.125		100.00892		100.00428		33.878		6.125		99.99725		33.526		6.125		100		45.61578		6.125		100.00428		46.07322		6.125		100.00671		44.62467		6.125		100.00622

		36.209		6.15		100.0104		100.00434		33.937		6.15		99.99678		33.602		6.15		100.00189		45.76456		6.15		100.00434		46.21056		6.15		100.00673		44.77433		6.15		100.00625

		36.276		6.175		100.0089		100.00439		34.009		6.175		99.99646		33.664		6.175		100.00774		45.90678		6.175		100.00439		46.34989		6.175		100.00673		44.93067		6.175		100.00627

		36.333		6.2		100.00859		100.00444		34.078		6.2		99.99671		33.722		6.2		100.004		46.05811		6.2		100.00444		46.48856		6.2		100.00674		45.08567		6.2		100.00628

		36.406		6.225		100.01021		100.00449		34.158		6.225		100.00001		33.802		6.225		100.00072		46.20133		6.225		100.00449		46.62656		6.225		100.00673		45.23233		6.225		100.0063

		36.469		6.25		100.0096		100.00454		34.217		6.25		99.99608		33.864		6.25		100.00095		46.34189		6.25		100.00454		46.76267		6.25		100.00672		45.38567		6.25		100.00631

		36.543		6.275		100.0118		100.00458		34.289		6.275		99.99402		33.947		6.275		100.00184		46.488		6.275		100.00458		46.89133		6.275		100.00671		45.53578		6.275		100.00632

		36.604		6.3		100.0108		100.00462		34.364		6.3		100.00064		34.02		6.3		100.00479		46.63111		6.3		100.00462		47.02856		6.3		100.0067		45.69344		6.3		100.00633

		36.667		6.325		100.01166		100.00465		34.423		6.325		100.00043		34.084		6.325		100.00333		46.772		6.325		100.00465		47.17367		6.325		100.00668		45.84155		6.325		100.00634

		36.735		6.35		100.01006		100.00468		34.494		6.35		99.99658		34.164		6.35		100.00264		46.91611		6.35		100.00468		47.31267		6.35		100.00668		45.99878		6.35		100.00634

		36.813		6.375		100.00977		100.00471		34.563		6.375		99.99527		34.232		6.375		100.0039		47.06244		6.375		100.00471		47.45844		6.375		100.00667		46.15011		6.375		100.00635

		36.878		6.4		100.01141		100.00473		34.639		6.4		99.99852		34.3		6.4		100.0013		47.21489		6.4		100.00473		47.61211		6.4		100.00668		46.29533		6.4		100.00636

		36.95		6.425		100.01		100.00475		34.706		6.425		99.99676		34.379		6.425		100.00263		47.35822		6.425		100.00475		47.76422		6.425		100.00669		46.44867		6.425		100.00636

		37.018		6.45		100.01034		100.00477		34.79		6.45		99.99893		34.457		6.45		100.00809		47.50678		6.45		100.00477		47.91267		6.45		100.00672		46.60311		6.45		100.00637

		37.086		6.475		100.01177		100.00479		34.858		6.475		99.99765		34.525		6.475		100.00117		47.66211		6.475		100.00479		48.06744		6.475		100.00676		46.74967		6.475		100.00638

		37.154		6.5		100.01055		100.0048		34.924		6.5		99.99991		34.606		6.5		100.01014		47.81178		6.5		100.0048		48.22478		6.5		100.00681		46.90533		6.5		100.0064

		37.226		6.525		100.01015		100.00481		35.001		6.525		99.99568		34.669		6.525		100.00301		47.96233		6.525		100.00481		48.37933		6.525		100.00688		47.05844		6.525		100.00641

		37.292		6.55		100.01069		100.00482		35.071		6.55		99.99929		34.747		6.55		100.00197		48.116		6.55		100.00482		48.52722		6.55		100.00696		47.217		6.55		100.00643

		37.359		6.575		100.01163		100.00483		35.155		6.575		100.00065		34.816		6.575		100.00398		48.26089		6.575		100.00483		48.67622		6.575		100.00705		47.36811		6.575		100.00645

		37.443		6.6		100.01067		100.00484		35.234		6.6		99.99582		34.899		6.6		100.00124		48.40822		6.6		100.00484		48.83022		6.6		100.00715		47.53344		6.6		100.00647

		37.506		6.625		100.01122		100.00485		35.296		6.625		99.99761		34.971		6.625		100.00052		48.55456		6.625		100.00485		48.97844		6.625		100.00726		47.69889		6.625		100.00649

		37.586		6.65		100.009		100.00486		35.366		6.65		100.00039		35.056		6.65		100.00303		48.69878		6.65		100.00486		49.13578		6.65		100.00738		47.85967		6.65		100.00652

		37.656		6.675		100.0114		100.00487		35.445		6.675		99.99772		35.124		6.675		100.00596		48.85267		6.675		100.00487		49.29433		6.675		100.0075		48.02667		6.675		100.00654

		37.726		6.7		100.01061		100.00488		35.515		6.7		100.0007		35.195		6.7		99.99749		49.00244		6.7		100.00488		49.447		6.7		100.00763		48.19556		6.7		100.00657

		37.802		6.725		100.01232		100.0049		35.588		6.725		99.99772		35.269		6.725		100.0017		49.15722		6.725		100.0049		49.60289		6.725		100.00776		48.35889		6.725		100.0066

		37.87		6.75		100.01026		100.00491		35.671		6.75		99.997		35.342		6.75		100.00586		49.31211		6.75		100.00491		49.75944		6.75		100.00789		48.51756		6.75		100.00662

		37.95		6.775		100.01029		100.00492		35.749		6.775		99.99607		35.421		6.775		100.00692		49.46511		6.775		100.00492		49.91722		6.775		100.00801		48.67233		6.775		100.00665

		38.025		6.8		100.01301		100.00493		35.829		6.8		99.9977		35.499		6.8		100.00104		49.62089		6.8		100.00493		50.07411		6.8		100.00813		48.83611		6.8		100.00667

		38.108		6.825		100.01132		100.00495		35.89		6.825		99.9964		35.578		6.825		99.99881		49.77367		6.825		100.00495		50.22533		6.825		100.00824		48.98844		6.825		100.0067

		38.161		6.85		100.01135		100.00496		35.98		6.85		99.994		35.658		6.85		100.00034		49.93033		6.85		100.00496		50.384		6.85		100.00835		49.149		6.85		100.00672

		38.243		6.875		100.013		100.00497		36.06		6.875		99.99466		35.729		6.875		100.00483		50.08789		6.875		100.00497		50.53844		6.875		100.00845		49.30878		6.875		100.00674

		38.308		6.9		100.00983		100.00498		36.125		6.9		99.99843		35.807		6.9		100.00367		50.23656		6.9		100.00498		50.69311		6.9		100.00855		49.46767		6.9		100.00676

		38.38		6.925		100.00938		100.00499		36.199		6.925		100.00195		35.892		6.925		100.00534		50.39222		6.925		100.00499		50.84878		6.925		100.00863		49.62833		6.925		100.00678

		38.451		6.95		100.00993		100.005		36.281		6.95		100.00055		35.967		6.95		100.00662		50.54311		6.95		100.005		51.00522		6.95		100.0087		49.78711		6.95		100.0068

		38.543		6.975		100.01191		100.00501		36.356		6.975		100.00058		36.037		6.975		100.00398		50.69578		6.975		100.00501		51.16233		6.975		100.00877		49.95267		6.975		100.00681

		38.612		7		100.00918		100.00502		36.44		7		99.99215		36.133		7		100.00039		50.84867		7		100.00502		51.31722		7		100.00883		50.11811		7		100.00683

		38.698		7.025		100.01069		100.00503		36.506		7.025		99.99243		36.207		7.025		100.00296		51.00433		7.025		100.00503		51.47722		7.025		100.00887		50.27989		7.025		100.00684

		38.773		7.05		100.01073		100.00503		36.579		7.05		99.99928		36.279		7.05		100.00279		51.15733		7.05		100.00503		51.63278		7.05		100.00892		50.44544		7.05		100.00686

		38.847		7.075		100.00963		100.00504		36.672		7.075		100.00262		36.361		7.075		99.9985		51.30489		7.075		100.00504		51.78		7.075		100.00895		50.61011		7.075		100.00687

		38.925		7.1		100.00912		100.00505		36.747		7.1		100.00169		36.448		7.1		100.00123		51.46067		7.1		100.00505		51.92978		7.1		100.00897		50.776		7.1		100.00688

		38.997		7.125		100.0123		100.00506		36.819		7.125		99.99476		36.523		7.125		99.99939		51.61167		7.125		100.00506		52.08456		7.125		100.00899		50.93644		7.125		100.0069

		39.083		7.15		100.01173		100.00507		36.908		7.15		99.99514		36.595		7.15		100.0044		51.75489		7.15		100.00507		52.23978		7.15		100.00901		51.09822		7.15		100.00691

		39.146		7.175		100.00905		100.00508		36.979		7.175		99.99792		36.692		7.175		100.0026		51.90311		7.175		100.00508		52.38856		7.175		100.00902		51.26056		7.175		100.00693

		39.223		7.2		100.01019		100.0051		37.066		7.2		99.99807		36.763		7.2		100.00459		52.05289		7.2		100.0051		52.54411		7.2		100.00903		51.42278		7.2		100.00694

		39.313		7.225		100.01152		100.00512		37.15		7.225		99.99952		36.846		7.225		100.00646		52.20333		7.225		100.00512		52.69933		7.225		100.00904		51.58322		7.225		100.00696

		39.392		7.25		100.01237		100.00514		37.235		7.25		99.99956		36.932		7.25		100.00249		52.34811		7.25		100.00514		52.856		7.25		100.00904		51.73944		7.25		100.00697

		39.48		7.275		100.00878		100.00517		37.317		7.275		99.9975		37.004		7.275		100.01067		52.50456		7.275		100.00517		53.01922		7.275		100.00905		51.89844		7.275		100.00699

		39.547		7.3		100.00968		100.00519		37.391		7.3		99.99853		37.091		7.3		100.00189		52.662		7.3		100.00519		53.18089		7.3		100.00906		52.05656		7.3		100.00701

		39.637		7.325		100.01321		100.00523		37.48		7.325		99.99942		37.174		7.325		100.00806		52.814		7.325		100.00523		53.34556		7.325		100.00907		52.21822		7.325		100.00703

		39.719		7.35		100.01238		100.00526		37.554		7.35		100.00083		37.259		7.35		100.00898		52.97522		7.35		100.00526		53.50744		7.35		100.00908		52.37989		7.35		100.00705

		39.794		7.375		100.01292		100.0053		37.634		7.375		100.00141		37.344		7.375		100.00425		53.13567		7.375		100.0053		53.66911		7.375		100.0091		52.54278		7.375		100.00707

		39.873		7.4		100.00971		100.00534		37.718		7.4		99.99756		37.42		7.4		100.0039		53.29867		7.4		100.00534		53.83033		7.4		100.00912		52.704		7.4		100.00709

		39.954		7.425		100.01154		100.00538		37.804		7.425		100.0024		37.518		7.425		100.00676		53.459		7.425		100.00538		53.99367		7.425		100.00915		52.86822		7.425		100.00711

		40.034		7.45		100.0107		100.00542		37.888		7.45		99.99887		37.596		7.45		100.00198		53.62356		7.45		100.00542		54.15667		7.45		100.00918		53.03756		7.45		100.00713

		40.101		7.475		100.01218		100.00547		37.967		7.475		99.99947		37.679		7.475		100.00546		53.78867		7.475		100.00547		54.32		7.475		100.00921		53.20778		7.475		100.00715

		40.189		7.5		100.01018		100.00551		38.06		7.5		100.00107		37.759		7.5		100.00395		53.95233		7.5		100.00551		54.48189		7.5		100.00924		53.37644		7.5		100.00716

		40.279		7.525		100.0137		100.00556		38.143		7.525		99.99672		37.854		7.525		100.00464		54.11711		7.525		100.00556		54.64544		7.525		100.00928		53.54844		7.525		100.00718

		40.365		7.55		100.01123		100.0056		38.219		7.55		99.99963		37.937		7.55		100.0045		54.28144		7.55		100.0056		54.80867		7.55		100.00932		53.717		7.55		100.0072

		40.442		7.575		100.01503		100.00565		38.312		7.575		100.00034		38.026		7.575		100.00347		54.44967		7.575		100.00565		54.969		7.575		100.00936		53.89044		7.575		100.00722

		40.517		7.6		100.01245		100.00569		38.389		7.6		99.99793		38.105		7.6		100.00195		54.61533		7.6		100.00569		55.13133		7.6		100.0094		54.06311		7.6		100.00724

		40.608		7.625		100.01205		100.00573		38.477		7.625		100.0014		38.196		7.625		100.00763		54.78022		7.625		100.00573		55.29544		7.625		100.00945		54.23522		7.625		100.00725

		40.687		7.65		100.0115		100.00576		38.568		7.65		99.99803		38.294		7.65		99.99937		54.94611		7.65		100.00576		55.46011		7.65		100.00949		54.40444		7.65		100.00727

		40.776		7.675		100.0093		100.0058		38.66		7.675		99.99772		38.363		7.675		100.00269		55.11244		7.675		100.0058		55.62711		7.675		100.00953		54.57178		7.675		100.00729

		40.864		7.7		100.01373		100.00583		38.737		7.7		99.99634		38.452		7.7		100.00314		55.27967		7.7		100.00583		55.79222		7.7		100.00957		54.74711		7.7		100.0073

		40.948		7.725		100.01087		100.00585		38.816		7.725		99.99605		38.537		7.725		100.00491		55.44967		7.725		100.00585		55.96044		7.725		100.00962		54.92133		7.725		100.00731

		41.033		7.75		100.00967		100.00588		38.908		7.75		99.99946		38.63		7.75		100.00274		55.61833		7.75		100.00588		56.13244		7.75		100.00966		55.08889		7.75		100.00733

		41.115		7.775		100.01031		100.0059		39.005		7.775		99.9996		38.713		7.775		100.00427		55.78989		7.775		100.0059		56.30111		7.775		100.0097		55.26044		7.775		100.00734

		41.203		7.8		100.00947		100.00591		39.075		7.8		99.99667		38.801		7.8		100.00128		55.95655		7.8		100.00591		56.46956		7.8		100.00973		55.43667		7.8		100.00736

		41.29		7.825		100.01276		100.00593		39.175		7.825		99.99753		38.888		7.825		100.00796		56.12744		7.825		100.00593		56.64478		7.825		100.00977		55.60822		7.825		100.00737

		41.37		7.85		100.01118		100.00594		39.255		7.85		100.00239		38.983		7.85		100.00547		56.29689		7.85		100.00594		56.818		7.85		100.00981		55.78633		7.85		100.00739

		41.453		7.875		100.00934		100.00596		39.34		7.875		100.00152		39.056		7.875		100.00296		56.46433		7.875		100.00596		56.98489		7.875		100.00985		55.96333		7.875		100.0074

		41.533		7.9		100.01034		100.00597		39.427		7.9		99.99793		39.142		7.9		100.00072		56.63633		7.9		100.00597		57.15022		7.9		100.00988		56.13911		7.9		100.00742

		41.624		7.925		100.01112		100.00598		39.521		7.925		99.99843		39.241		7.925		100.00586		56.80111		7.925		100.00598		57.31844		7.925		100.00992		56.31078		7.925		100.00743

		41.715		7.95		100.01166		100.006		39.605		7.95		99.99781		39.342		7.95		100.00481		56.96589		7.95		100.006		57.48256		7.95		100.00995		56.48255		7.95		100.00745

		41.807		7.975		100.01125		100.00601		39.692		7.975		99.99824		39.422		7.975		100.00354		57.13056		7.975		100.00601		57.64667		7.975		100.00998		56.65978		7.975		100.00747

		41.891		8		100.01239		100.00603		39.8		8		99.99851		39.51		8		100.00261		57.29278		8		100.00603		57.81167		8		100.01001		56.83544		8		100.00749

		41.978		8.025		100.01029		100.00605		39.869		8.025		99.99895		39.609		8.025		100.00835		57.45756		8.025		100.00605		57.98		8.025		100.01004		57.00367		8.025		100.00751

		42.065		8.05		100.01173		100.00607		39.967		8.05		99.99969		39.694		8.05		100.00527		57.624		8.05		100.00607		58.14656		8.05		100.01007		57.17444		8.05		100.00753

		42.159		8.075		100.01026		100.00609		40.062		8.075		100.00162		39.791		8.075		100.00484		57.79078		8.075		100.00609		58.32311		8.075		100.0101		57.34789		8.075		100.00755

		42.248		8.1		100.00988		100.00612		40.151		8.1		99.99723		39.878		8.1		100.00531		57.95989		8.1		100.00612		58.49856		8.1		100.01012		57.51867		8.1		100.00757

		42.344		8.125		100.01228		100.00614		40.235		8.125		99.99963		39.979		8.125		100.00206		58.12778		8.125		100.00614		58.67756		8.125		100.01014		57.69833		8.125		100.00759

		42.421		8.15		100.0119		100.00617		40.334		8.15		99.99947		40.064		8.15		100.00748		58.31156		8.15		100.00617		58.85244		8.15		100.01016		57.87622		8.15		100.00761

		42.515		8.175		100.00922		100.0062		40.422		8.175		99.9977		40.154		8.175		100.00154		58.48767		8.175		100.0062		59.03		8.175		100.01018		58.056		8.175		100.00763

		42.6		8.2		100.01237		100.00623		40.518		8.2		99.99982		40.243		8.2		100.00401		58.66589		8.2		100.00623		59.21444		8.2		100.0102		58.231		8.2		100.00765

		42.702		8.225		100.0116		100.00626		40.611		8.225		100.00037		40.342		8.225		100.00424		58.85		8.225		100.00626		59.39456		8.225		100.01022		58.40967		8.225		100.00766

		42.79		8.25		100.01055		100.00629		40.696		8.25		100.00251		40.435		8.25		100.00542		59.03211		8.25		100.00629		59.579		8.25		100.01024		58.58878		8.25		100.00768

		42.888		8.275		100.01188		100.00632		40.794		8.275		99.99753		40.534		8.275		100.00697		59.21678		8.275		100.00632		59.75844		8.275		100.01026		58.77189		8.275		100.00769

		42.972		8.3		100.01027		100.00635		40.879		8.3		99.99804		40.619		8.3		100.00563		59.39589		8.3		100.00635		59.93378		8.3		100.01028		58.95078		8.3		100.0077

		43.06		8.325		100.01321		100.00638		40.977		8.325		99.99747		40.711		8.325		100.00448		59.57844		8.325		100.00638		60.11222		8.325		100.01031		59.13289		8.325		100.00771

		43.152		8.35		100.01008		100.00641		41.069		8.35		99.99946		40.813		8.35		100.00606		59.75789		8.35		100.00641		60.29156		8.35		100.01034		59.30944		8.35		100.00772

		43.245		8.375		100.01262		100.00645		41.165		8.375		100.00153		40.914		8.375		100.00383		59.92978		8.375		100.00645		60.469		8.375		100.01037		59.48456		8.375		100.00773

		43.332		8.4		100.01158		100.00648		41.26		8.4		99.99938		41.01		8.4		99.99761		60.10167		8.4		100.00648		60.65444		8.4		100.01041		59.663		8.4		100.00773

		43.415		8.425		100.0123		100.00651		41.358		8.425		99.99911		41.092		8.425		100.00467		60.28044		8.425		100.00651		60.83122		8.425		100.01045		59.84222		8.425		100.00774

		43.51		8.45		100.01258		100.00655		41.443		8.45		100.00029		41.19		8.45		100.00236		60.45344		8.45		100.00655		61.01289		8.45		100.01049		60.022		8.45		100.00775

		43.608		8.475		100.01293		100.00658		41.539		8.475		99.99794		41.285		8.475		100.00464		60.63278		8.475		100.00658		61.18989		8.475		100.01053		60.21244		8.475		100.00777

		43.702		8.5		100.01105		100.00661		41.633		8.5		100.00132		41.378		8.5		100.00599		60.80867		8.5		100.00661		61.36744		8.5		100.01058		60.39533		8.5		100.00778

		43.799		8.525		100.01388		100.00665		41.719		8.525		99.99927		41.478		8.525		100.00195		60.98556		8.525		100.00665		61.54456		8.525		100.01063		60.58144		8.525		100.00779

		43.892		8.55		100.01238		100.00668		41.827		8.55		99.99835		41.573		8.55		100.00199		61.16333		8.55		100.00668		61.72556		8.55		100.01068		60.766		8.55		100.00781

		43.989		8.575		100.01065		100.00671		41.931		8.575		99.9978		41.664		8.575		100.01163		61.33711		8.575		100.00671		61.904		8.575		100.01073		60.952		8.575		100.00782

		44.083		8.6		100.00886		100.00674		42.032		8.6		99.99856		41.764		8.6		99.99674		61.51733		8.6		100.00674		62.085		8.6		100.01077		61.14411		8.6		100.00784

		44.172		8.625		100.00833		100.00677		42.118		8.625		99.99605		41.864		8.625		100.00178		61.70422		8.625		100.00677		62.26033		8.625		100.01082		61.33078		8.625		100.00785

		44.262		8.65		100.00922		100.0068		42.212		8.65		99.99799		41.96		8.65		100.00051		61.88089		8.65		100.0068		62.43867		8.65		100.01086		61.51933		8.65		100.00787

		44.357		8.675		100.00907		100.00683		42.324		8.675		99.99886		42.055		8.675		100.00944		62.05989		8.675		100.00683		62.61967		8.675		100.0109		61.71011		8.675		100.00788

		44.462		8.7		100.0107		100.00686		42.404		8.7		99.99573		42.158		8.7		100.01036		62.23556		8.7		100.00686		62.79644		8.7		100.01093		61.89044		8.7		100.00789

		44.555		8.725		100.012		100.00688		42.513		8.725		100.00037		42.254		8.725		100.0001		62.413		8.725		100.00688		62.97733		8.725		100.01097		62.077		8.725		100.0079

		44.655		8.75		100.01063		100.00691		42.609		8.75		99.99821		42.349		8.75		100.0015		62.59578		8.75		100.00691		63.16411		8.75		100.01099		62.26144		8.75		100.00791

		44.743		8.775		100.01394		100.00693		42.718		8.775		100.00163		42.45		8.775		100.00246		62.77489		8.775		100.00693		63.34389		8.775		100.01102		62.44811		8.775		100.00792

		44.847		8.8		100.01243		100.00695		42.819		8.8		99.99647		42.545		8.8		99.99973		62.95878		8.8		100.00695		63.52967		8.8		100.01104		62.63489		8.8		100.00793

		44.947		8.825		100.01317		100.00697		42.918		8.825		99.99967		42.641		8.825		100.00672		63.14278		8.825		100.00697		63.71556		8.825		100.01106		62.81644		8.825		100.00793

		45.039		8.85		100.01108		100.007		43.01		8.85		100.00016		42.735		8.85		100.0014		63.32233		8.85		100.007		63.89967		8.85		100.01108		63.00289		8.85		100.00794

		45.132		8.875		100.01103		100.00702		43.103		8.875		100.002		42.846		8.875		100.00767		63.50655		8.875		100.00702		64.08522		8.875		100.0111		63.19178		8.875		100.00794

		45.235		8.9		100.01105		100.00704		43.226		8.9		100.00077		42.952		8.9		100.00047		63.69044		8.9		100.00704		64.26689		8.9		100.01111		63.371		8.9		100.00794

		45.318		8.925		100.01013		100.00706		43.304		8.925		99.99794		43.048		8.925		100.00475		63.87244		8.925		100.00706		64.45822		8.925		100.01113		63.55689		8.925		100.00795

		45.434		8.95		100.01123		100.00708		43.406		8.95		100.00049		43.16		8.95		100.00504		64.05711		8.95		100.00708		64.65033		8.95		100.01115		63.74144		8.95		100.00795

		45.514		8.975		100.01198		100.0071		43.506		8.975		99.99788		43.246		8.975		100.00635		64.23878		8.975		100.0071		64.834		8.975		100.01117		63.92856		8.975		100.00796

		45.622		9		100.00994		100.00712		43.599		9		99.99833		43.35		9		100.00305		64.424		9		100.00712		65.026		9		100.0112		64.11333		9		100.00796

		45.721		9.025		100.00963		100.00714		43.706		9.025		99.99758		43.451		9.025		100.00313		64.61222		9.025		100.00714		65.20933		9.025		100.01123		64.30078		9.025		100.00797

		45.828		9.05		100.01022		100.00715		43.802		9.05		100.00044		43.548		9.05		100.00846		64.79544		9.05		100.00715		65.39856		9.05		100.01126		64.48978		9.05		100.00798

		45.925		9.075		100.01038		100.00717		43.9		9.075		99.99718		43.652		9.075		100.00927		64.97989		9.075		100.00717		65.58978		9.075		100.01129		64.67933		9.075		100.00799

		46.019		9.1		100.0108		100.00719		44.011		9.1		99.99867		43.767		9.1		100.00313		65.16567		9.1		100.00719		65.78045		9.1		100.01133		64.86967		9.1		100.008

		46.127		9.125		100.00899		100.0072		44.101		9.125		99.99821		43.865		9.125		100.00463		65.35055		9.125		100.0072		65.97111		9.125		100.01138		65.06733		9.125		100.00802

		46.225		9.15		100.01014		100.00722		44.216		9.15		99.99835		43.958		9.15		100.00259		65.53878		9.15		100.00722		66.15867		9.15		100.01142		65.26056		9.15		100.00803

		46.326		9.175		100.01174		100.00723		44.314		9.175		100.00084		44.057		9.175		100.00406		65.72167		9.175		100.00723		66.34222		9.175		100.01147		65.455		9.175		100.00804

		46.411		9.2		100.00863		100.00724		44.413		9.2		99.99709		44.155		9.2		100.0009		65.90744		9.2		100.00724		66.53355		9.2		100.01151		65.64722		9.2		100.00806

		46.524		9.225		100.00932		100.00725		44.514		9.225		99.99778		44.268		9.225		99.99893		66.08833		9.225		100.00725		66.71667		9.225		100.01156		65.843		9.225		100.00808

		46.62		9.25		100.01055		100.00726		44.624		9.25		99.99628		44.376		9.25		100.00228		66.26878		9.25		100.00726		66.90855		9.25		100.01161		66.03611		9.25		100.00809

		46.726		9.275		100.01253		100.00727		44.724		9.275		100.00045		44.476		9.275		100.0019		66.45555		9.275		100.00727		67.09211		9.275		100.01165		66.23356		9.275		100.00811

		46.822		9.3		100.01085		100.00728		44.833		9.3		99.99843		44.581		9.3		100.00418		66.64055		9.3		100.00728		67.27778		9.3		100.01169		66.43522		9.3		100.00812

		46.932		9.325		100.01266		100.00729		44.935		9.325		100.00403		44.684		9.325		100.00383		66.82867		9.325		100.00729		67.46333		9.325		100.01173		66.63011		9.325		100.00814

		47.032		9.35		100.01099		100.00731		45.033		9.35		99.9983		44.799		9.35		100.00218		67.01722		9.35		100.00731		67.65		9.35		100.01177		66.82589		9.35		100.00815

		47.134		9.375		100.00901		100.00732		45.142		9.375		99.99655		44.896		9.375		100.00184		67.198		9.375		100.00732		67.83667		9.375		100.0118		67.023		9.375		100.00817

		47.243		9.4		100.01052		100.00733		45.253		9.4		99.99911		44.997		9.4		100.00156		67.38711		9.4		100.00733		68.02656		9.4		100.01183		67.21722		9.4		100.00818

		47.349		9.425		100.0117		100.00735		45.362		9.425		99.99745		45.112		9.425		100.00249		67.57189		9.425		100.00735		68.21267		9.425		100.01186		67.41156		9.425		100.00819

		47.452		9.45		100.01136		100.00736		45.46		9.45		99.99951		45.206		9.45		100.00405		67.76178		9.45		100.00736		68.40389		9.45		100.01188		67.60378		9.45		100.0082

		47.552		9.475		100.00829		100.00738		45.56		9.475		99.99842		45.318		9.475		100.00217		67.95367		9.475		100.00738		68.58878		9.475		100.0119		67.798		9.475		100.00821

		47.652		9.5		100.0097		100.0074		45.671		9.5		99.99797		45.423		9.5		100.00277		68.13811		9.5		100.0074		68.78178		9.5		100.01192		67.99467		9.5		100.00822

		47.765		9.525		100.01191		100.00742		45.775		9.525		100.00012		45.541		9.525		100.00533		68.33011		9.525		100.00742		68.974		9.525		100.01194		68.18422		9.525		100.00823

		47.862		9.55		100.01046		100.00744		45.889		9.55		99.99853		45.64		9.55		100.00428		68.51589		9.55		100.00744		69.16822		9.55		100.01195		68.37789		9.55		100.00824

		47.972		9.575		100.01167		100.00746		45.992		9.575		100.00109		45.748		9.575		100.00257		68.70756		9.575		100.00746		69.36878		9.575		100.01197		68.56889		9.575		100.00824

		48.08		9.6		100.00987		100.00749		46.107		9.6		99.99827		45.865		9.6		100.00733		68.90478		9.6		100.00749		69.56489		9.6		100.01198		68.76322		9.6		100.00825

		48.174		9.625		100.01091		100.00751		46.213		9.625		99.99994		45.968		9.625		100.00243		69.10211		9.625		100.00751		69.76356		9.625		100.01199		68.96067		9.625		100.00826

		48.291		9.65		100.01357		100.00754		46.314		9.65		100.00141		46.065		9.65		100.00841		69.30322		9.65		100.00754		69.95933		9.65		100.01201		69.16122		9.65		100.00827

		48.39		9.675		100.01073		100.00757		46.415		9.675		99.99972		46.19		9.675		100.00334		69.502		9.675		100.00757		70.15622		9.675		100.01203		69.36667		9.675		100.00829

		48.503		9.7		100.01201		100.0076		46.534		9.7		100.00071		46.295		9.7		100.00312		69.69378		9.7		100.0076		70.35278		9.7		100.01205		69.56644		9.7		100.0083

		48.614		9.725		100.01237		100.00763		46.65		9.725		100.00287		46.395		9.725		100.00486		69.88756		9.725		100.00763		70.54878		9.725		100.01207		69.76655		9.725		100.00831

		48.714		9.75		100.0108		100.00766		46.747		9.75		100.00042		46.505		9.75		100.00414		70.07389		9.75		100.00766		70.749		9.75		100.01209		69.96722		9.75		100.00832

		48.821		9.775		100.01077		100.0077		46.86		9.775		100.00072		46.616		9.775		100.00446		70.26522		9.775		100.0077		70.94544		9.775		100.01212		70.169		9.775		100.00834

		48.93		9.8		100.01259		100.00774		46.984		9.8		100.00022		46.728		9.8		100.00284		70.45189		9.8		100.00774		71.13567		9.8		100.01214		70.37		9.8		100.00835

		49.038		9.825		100.0104		100.00777		47.087		9.825		99.99998		46.832		9.825		100.00698		70.643		9.825		100.00777		71.33122		9.825		100.01217		70.56989		9.825		100.00837

		49.148		9.85		100.01005		100.00781		47.19		9.85		99.99804		46.957		9.85		100.00303		70.83233		9.85		100.00781		71.52056		9.85		100.0122		70.77378		9.85		100.00838

		49.242		9.875		100.01123		100.00785		47.292		9.875		99.9987		47.05		9.875		99.99972		71.01867		9.875		100.00785		71.71356		9.875		100.01223		70.97222		9.875		100.0084

		49.36		9.9		100.01084		100.00789		47.391		9.9		99.99918		47.164		9.9		100.0031		71.20956		9.9		100.00789		71.90367		9.9		100.01226		71.17033		9.9		100.00841

		49.463		9.925		100.01166		100.00793		47.518		9.925		100.0014		47.284		9.925		100.00088		71.4		9.925		100.00793		72.098		9.925		100.01229		71.37111		9.925		100.00843

		49.578		9.95		100.00972		100.00797		47.63		9.95		99.99889		47.385		9.95		99.99965		71.59367		9.95		100.00797		72.28178		9.95		100.01232		71.56922		9.95		100.00844

		49.689		9.975		100.01182		100.00801		47.739		9.975		100.00255		47.504		9.975		100.0026		71.78756		9.975		100.00801		72.46345		9.975		100.01235		71.763		9.975		100.00845

		49.799		10		100.01013		100.00804		47.851		10		99.99969		47.612		10		100.00156		71.98289		10		100.00804		72.65078		10		100.01238		71.95889		10		100.00846

		49.909		10.025		100.01184		100.00808		47.966		10.025		99.99934		47.725		10.025		100.00497		72.17478		10.025		100.00808		72.83689		10.025		100.0124		72.153		10.025		100.00847

		50.013		10.05		100.0096		100.00811		48.076		10.05		99.99859		47.835		10.05		99.99979		72.36778		10.05		100.00811		73.02344		10.05		100.01242		72.349		10.05		100.00848

		50.139		10.075		100.00964		100.00814		48.186		10.075		99.99966		47.942		10.075		100.00001		72.56144		10.075		100.00814		73.20967		10.075		100.01245		72.54511		10.075		100.00849

		50.243		10.1		100.01167		100.00817		48.294		10.1		99.99836		48.061		10.1		100.00344		72.75611		10.1		100.00817		73.40011		10.1		100.01246		72.74267		10.1		100.0085

		50.359		10.125		100.00849		100.0082		48.414		10.125		99.9975		48.173		10.125		100.00162		72.95122		10.125		100.0082		73.59078		10.125		100.01248		72.93967		10.125		100.00851

		50.47		10.15		100.01091		100.00823		48.526		10.15		100.0002		48.284		10.15		100.00211		73.14567		10.15		100.00823		73.78589		10.15		100.0125		73.13644		10.15		100.00852

		50.576		10.175		100.0095		100.00826		48.643		10.175		99.9953		48.4		10.175		100.00276		73.34178		10.175		100.00826		73.99055		10.175		100.01251		73.33589		10.175		100.00853

		50.678		10.2		100.01085		100.00829		48.757		10.2		99.99973		48.501		10.2		100.00261		73.53644		10.2		100.00829		74.19022		10.2		100.01253		73.53978		10.2		100.00854

		50.8		10.225		100.01013		100.00832		48.885		10.225		99.9999		48.615		10.225		100.00349		73.73078		10.225		100.00832		74.39022		10.225		100.01254		73.74267		10.225		100.00856

		50.915		10.25		100.0123		100.00835		48.978		10.25		99.99918		48.737		10.25		100.00348		73.93333		10.25		100.00835		74.59011		10.25		100.01256		73.95233		10.25		100.00857

		51.025		10.275		100.00945		100.00838		49.094		10.275		100.00285		48.867		10.275		100.0029		74.13289		10.275		100.00838		74.79222		10.275		100.01257		74.15889		10.275		100.00859

		51.136		10.3		100.01146		100.00841		49.209		10.3		100.00365		48.968		10.3		100.00546		74.32833		10.3		100.00841		74.99467		10.3		100.01259		74.36244		10.3		100.00861

		51.249		10.325		100.01014		100.00844		49.322		10.325		100.00097		49.083		10.325		100.00268		74.52656		10.325		100.00844		75.19811		10.325		100.01262		74.56856		10.325		100.00863

		51.357		10.35		100.01266		100.00848		49.431		10.35		100.00148		49.196		10.35		100.00381		74.72167		10.35		100.00848		75.40333		10.35		100.01264		74.773		10.35		100.00865

		51.485		10.375		100.0082		100.00851		49.564		10.375		100.00009		49.315		10.375		100.0032		74.91789		10.375		100.00851		75.60089		10.375		100.01267		74.97967		10.375		100.00868

		51.582		10.4		100.01114		100.00855		49.664		10.4		99.99863		49.427		10.4		100.00325		75.114		10.4		100.00855		75.79989		10.4		100.01269		75.182		10.4		100.0087

		51.692		10.425		100.01225		100.00859		49.78		10.425		100.0004		49.534		10.425		100.00312		75.31322		10.425		100.00859		76.00278		10.425		100.01272		75.39033		10.425		100.00873

		51.813		10.45		100.01072		100.00863		49.9		10.45		99.99722		49.657		10.45		100.00261		75.51356		10.45		100.00863		76.20222		10.45		100.01275		75.59544		10.45		100.00875

		51.931		10.475		100.00998		100.00867		50.02		10.475		100.00244		49.776		10.475		100.00373		75.71189		10.475		100.00867		76.40333		10.475		100.01279		75.79822		10.475		100.00878

		52.065		10.5		100.00984		100.00871		50.13		10.5		99.99614		49.896		10.5		100.00284		75.90756		10.5		100.00871		76.60133		10.5		100.01282		76.00133		10.5		100.0088

		52.17		10.525		100.01087		100.00874		50.251		10.525		99.99994		50.003		10.525		100.00299		76.10511		10.525		100.00874		76.80744		10.525		100.01285		76.20533		10.525		100.00883

		52.283		10.55		100.01242		100.00877		50.367		10.55		100.00018		50.131		10.55		100.00609		76.30256		10.55		100.00877		77.00955		10.55		100.01289		76.40622		10.55		100.00885

		52.4		10.575		100.01112		100.0088		50.49		10.575		99.99732		50.26		10.575		100.00424		76.49889		10.575		100.0088		77.21033		10.575		100.01292		76.61156		10.575		100.00887

		52.516		10.6		100.01052		100.00883		50.602		10.6		100.00082		50.358		10.6		100.00435		76.69989		10.6		100.00883		77.41355		10.6		100.01296		76.81744		10.6		100.00889

		52.625		10.625		100.01022		100.00885		50.719		10.625		100.00018		50.485		10.625		100.00349		76.90133		10.625		100.00885		77.61367		10.625		100.01299		77.023		10.625		100.00891

		52.748		10.65		100.01218		100.00887		50.834		10.65		100.00168		50.602		10.65		100.0034		77.10622		10.65		100.00887		77.81589		10.65		100.01302		77.22411		10.65		100.00893

		52.848		10.675		100.00926		100.00889		50.962		10.675		99.99767		50.716		10.675		100.00397		77.30633		10.675		100.00889		78.02222		10.675		100.01305		77.42378		10.675		100.00895

		52.975		10.7		100.00873		100.0089		51.073		10.7		99.99623		50.842		10.7		100.00297		77.50611		10.7		100.0089		78.22744		10.7		100.01308		77.62511		10.7		100.00896

		53.099		10.725		100.0119		100.0089		51.191		10.725		100.00042		50.956		10.725		100.00326		77.70756		10.725		100.0089		78.436		10.725		100.0131		77.829		10.725		100.00897

		53.212		10.75		100.01094		100.00891		51.314		10.75		100.0004		51.076		10.75		100.0038		77.91111		10.75		100.00891		78.64056		10.75		100.01313		78.03445		10.75		100.00899

		53.321		10.775		100.01078		100.00891		51.439		10.775		100.00062		51.204		10.775		100.00282		78.11178		10.775		100.00891		78.84622		10.775		100.01314		78.24322		10.775		100.009

		53.435		10.8		100.01084		100.00891		51.547		10.8		100.00147		51.307		10.8		100.006		78.31145		10.8		100.00891		79.05367		10.8		100.01316		78.44545		10.8		100.00901

		53.558		10.825		100.01424		100.00891		51.668		10.825		99.99789		51.428		10.825		100.00568		78.51089		10.825		100.00891		79.26044		10.825		100.01317		78.65411		10.825		100.00901

		53.674		10.85		100.01106		100.0089		51.791		10.85		99.99982		51.554		10.85		100.00479		78.71134		10.85		100.0089		79.47011		10.85		100.01318		78.86522		10.85		100.00902

		53.782		10.875		100.01305		100.0089		51.914		10.875		99.99759		51.686		10.875		100.00557		78.90867		10.875		100.0089		79.67967		10.875		100.01319		79.07656		10.875		100.00903

		53.915		10.9		100.00996		100.0089		52.035		10.9		99.99887		51.802		10.9		100.0036		79.10878		10.9		100.0089		79.88878		10.9		100.01319		79.29256		10.9		100.00903

		54.041		10.925		100.01125		100.0089		52.152		10.925		100.00273		51.917		10.925		100.00603		79.31322		10.925		100.0089		80.1		10.925		100.01319		79.50378		10.925		100.00903

		54.151		10.95		100.01229		100.0089		52.262		10.95		100.00295		52.03		10.95		100.00599		79.515		10.95		100.0089		80.31045		10.95		100.01318		79.71589		10.95		100.00904

		54.274		10.975		100.00899		100.0089		52.385		10.975		100.00111		52.167		10.975		100.00485		79.71867		10.975		100.0089		80.516		10.975		100.01318		79.93011		10.975		100.00904

		54.384		11		100.01102		100.0089		52.519		11		100.0001		52.271		11		100.00281		79.92933		11		100.0089		80.72433		11		100.01317		80.14		11		100.00904

		54.506		11.025		100.01187		100.0089		52.641		11.025		100.00087		52.397		11.025		100.00409		80.13867		11.025		100.0089		80.927		11.025		100.01316		80.35444		11.025		100.00904

		54.638		11.05		100.01042		100.0089		52.761		11.05		100.00027		52.523		11.05		100.0038		80.35056		11.05		100.0089		81.13378		11.05		100.01316		80.55867		11.05		100.00904

		54.747		11.075		100.01188		100.00891		52.881		11.075		100.00051		52.647		11.075		100.00319		80.55567		11.075		100.00891		81.34289		11.075		100.01315		80.76433		11.075		100.00904

		54.869		11.1		100.01288		100.00891		53.006		11.1		99.99925		52.764		11.1		100.00304		80.76111		11.1		100.00891		81.55		11.1		100.01314		80.971		11.1		100.00904

		54.994		11.125		100.01085		100.00892		53.123		11.125		100.00114		52.886		11.125		100.00494		80.963		11.125		100.00892		81.75622		11.125		100.01314		81.17811		11.125		100.00904

		55.119		11.15		100.01162		100.00892		53.254		11.15		99.99903		53.015		11.15		100.00299		81.16533		11.15		100.00892		81.962		11.15		100.01314		81.39089		11.15		100.00904

		55.234		11.175		100.01161		100.00893		53.387		11.175		100.0004		53.139		11.175		100.00355		81.37455		11.175		100.00893		82.16389		11.175		100.01314		81.60267		11.175		100.00904

		55.365		11.2		100.00962		100.00894		53.497		11.2		99.99922		53.264		11.2		100.00394		81.57756		11.2		100.00894		82.36822		11.2		100.01314		81.81089		11.2		100.00905

		55.493		11.225		100.01006		100.00894		53.618		11.225		100.00185		53.384		11.225		100.00307		81.78144		11.225		100.00894		82.56922		11.225		100.01314		82.02344		11.225		100.00905

		55.605		11.25		100.00921		100.00895		53.754		11.25		100.0011		53.495		11.25		100.00521		81.98744		11.25		100.00895		82.77933		11.25		100.01315		82.23178		11.25		100.00906

		55.727		11.275		100.01203		100.00896		53.866		11.275		100.0037		53.633		11.275		100.00434		82.18711		11.275		100.00896		82.98533		11.275		100.01316		82.44678		11.275		100.00907

		55.863		11.3		100.01021		100.00897		53.986		11.3		100.00092		53.759		11.3		100.00515		82.38678		11.3		100.00897		83.193		11.3		100.01318		82.66278		11.3		100.00908

		55.977		11.325		100.01101		100.00899		54.121		11.325		99.99652		53.89		11.325		100.00429		82.58978		11.325		100.00899		83.39867		11.325		100.01319		82.87655		11.325		100.00909

		56.104		11.35		100.00874		100.009		54.242		11.35		100.00089		54.006		11.35		100.00553		82.80222		11.35		100.009		83.607		11.35		100.01321		83.09156		11.35		100.0091

		56.231		11.375		100.00808		100.00902		54.366		11.375		100.00135		54.135		11.375		100.00118		83.01289		11.375		100.00902		83.81767		11.375		100.01323		83.30078		11.375		100.00912

		56.35		11.4		100.00983		100.00904		54.48		11.4		100.00073		54.253		11.4		100.00257		83.22156		11.4		100.00904		84.02922		11.4		100.01325		83.51267		11.4		100.00913

		56.482		11.425		100.01038		100.00906		54.628		11.425		100.00061		54.388		11.425		100.00458		83.43367		11.425		100.00906		84.24689		11.425		100.01328		83.72178		11.425		100.00915

		56.604		11.45		100.01123		100.00908		54.746		11.45		100.00125		54.513		11.45		100.00559		83.64089		11.45		100.00908		84.46856		11.45		100.0133		83.93644		11.45		100.00917

		56.73		11.475		100.00997		100.0091		54.876		11.475		100.00124		54.632		11.475		100.00423		83.85344		11.475		100.0091		84.68078		11.475		100.01333		84.15144		11.475		100.00919

		56.842		11.5		100.0119		100.00913		55.001		11.5		99.99904		54.769		11.5		100.00446		84.064		11.5		100.00913		84.89711		11.5		100.01335		84.36722		11.5		100.00921

		56.978		11.525		100.00711		100.00915		55.131		11.525		100.00234		54.885		11.525		100.00466		84.27978		11.525		100.00915		85.10811		11.525		100.01338		84.58222		11.525		100.00923

		57.103		11.55		100.01238		100.00918		55.259		11.55		99.99945		55.017		11.55		100.00449		84.49689		11.55		100.00918		85.32622		11.55		100.0134		84.79789		11.55		100.00926

		57.233		11.575		100.01182		100.00921		55.389		11.575		100.00214		55.143		11.575		100.00342		84.70378		11.575		100.00921		85.54		11.575		100.01343		85.01089		11.575		100.00928

		57.356		11.6		100.01081		100.00924		55.512		11.6		100.00162		55.274		11.6		100.00455		84.912		11.6		100.00924		85.75411		11.6		100.01345		85.22833		11.6		100.0093

		57.485		11.625		100.00975		100.00926		55.645		11.625		100.00171		55.386		11.625		100.00304		85.118		11.625		100.00926		85.97222		11.625		100.01348		85.44122		11.625		100.00932

		57.605		11.65		100.01173		100.00929		55.764		11.65		99.99878		55.528		11.65		100.00311		85.32833		11.65		100.00929		86.18622		11.65		100.0135		85.65933		11.65		100.00935

		57.742		11.675		100.00886		100.00932		55.907		11.675		99.99874		55.661		11.675		100.00617		85.53956		11.675		100.00932		86.39744		11.675		100.01352		85.87667		11.675		100.00937

		57.864		11.7		100.0116		100.00934		56.035		11.7		100.00159		55.785		11.7		100.00298		85.74811		11.7		100.00934		86.61578		11.7		100.01355		86.09544		11.7		100.00939

		57.994		11.725		100.00938		100.00937		56.157		11.725		99.99767		55.909		11.725		100.00286		85.96411		11.725		100.00937		86.82856		11.725		100.01357		86.31555		11.725		100.00941

		58.124		11.75		100.01243		100.0094		56.287		11.75		99.99936		56.047		11.75		100.00481		86.18078		11.75		100.0094		87.04389		11.75		100.01358		86.53411		11.75		100.00943

		58.239		11.775		100.01077		100.00942		56.415		11.775		100.00072		56.177		11.775		100.00341		86.39311		11.775		100.00942		87.25444		11.775		100.0136		86.75411		11.775		100.00945

		58.364		11.8		100.00987		100.00945		56.546		11.8		99.99849		56.318		11.8		100.0035		86.60933		11.8		100.00945		87.46433		11.8		100.01361		86.97722		11.8		100.00946

		58.509		11.825		100.00887		100.00948		56.677		11.825		100.00067		56.442		11.825		100.00347		86.819		11.825		100.00948		87.676		11.825		100.01363		87.19855		11.825		100.00948

		58.625		11.85		100.01234		100.00951		56.812		11.85		100.00299		56.574		11.85		100.00512		87.03344		11.85		100.00951		87.88422		11.85		100.01364		87.42078		11.85		100.00949

		58.755		11.875		100.00765		100.00954		56.943		11.875		99.99732		56.701		11.875		100.00288		87.24389		11.875		100.00954		88.095		11.875		100.01364		87.64233		11.875		100.0095

		58.886		11.9		100.01382		100.00956		57.075		11.9		99.99901		56.837		11.9		100.00469		87.45344		11.9		100.00956		88.30222		11.9		100.01365		87.85611		11.9		100.0095

		59.019		11.925		100.01292		100.0096		57.2		11.925		100.00098		56.961		11.925		100.00476		87.66589		11.925		100.0096		88.51033		11.925		100.01365		88.073		11.925		100.00951

		59.155		11.95		100.01116		100.00963		57.315		11.95		100.00393		57.085		11.95		100.00505		87.87489		11.95		100.00963		88.72922		11.95		100.01365		88.28689		11.95		100.00951

		59.283		11.975		100.01063		100.00966		57.453		11.975		99.99909		57.218		11.975		100.00545		88.08556		11.975		100.00966		88.947		11.975		100.01365		88.50433		11.975		100.00951

		59.405		12		100.00953		100.00969		57.584		12		99.99969		57.355		12		100.00268		88.29822		12		100.00969		89.16645		12		100.01364		88.72644		12		100.00951

		59.535		12.025		100.01154		100.00972		57.714		12.025		100.00206		57.483		12.025		100.00633		88.51422		12.025		100.00972		89.38944		12.025		100.01364		88.94544		12.025		100.00951

		59.67		12.05		100.01013		100.00975		57.848		12.05		99.9982		57.622		12.05		100.00564		88.73267		12.05		100.00975		89.606		12.05		100.01363		89.16511		12.05		100.00951

		59.804		12.075		100.0108		100.00979		57.98		12.075		100.00222		57.754		12.075		100.00475		88.94978		12.075		100.00979		89.82622		12.075		100.01363		89.38811		12.075		100.0095

		59.936		12.1		100.01256		100.00982		58.116		12.1		100.00149		57.89		12.1		100.00406		89.168		12.1		100.00982		90.04411		12.1		100.01362		89.607		12.1		100.0095

		60.077		12.125		100.0104		100.00985		58.241		12.125		100.00026		58.016		12.125		100.00487		89.38867		12.125		100.00985		90.26756		12.125		100.01362		89.83533		12.125		100.00949

		60.197		12.15		100.0112		100.00988		58.374		12.15		99.99995		58.155		12.15		100.00438		89.60311		12.15		100.00988		90.49322		12.15		100.01361		90.057		12.15		100.00949

		60.332		12.175		100.01266		100.00991		58.52		12.175		100.00087		58.298		12.175		100.00438		89.82156		12.175		100.00991		90.71155		12.175		100.01361		90.28278		12.175		100.00949

		60.466		12.2		100.01005		100.00994		58.641		12.2		99.99968		58.42		12.2		100.00334		90.03822		12.2		100.00994		90.93044		12.2		100.01361		90.50711		12.2		100.00949

		60.597		12.225		100.01255		100.00997		58.775		12.225		99.99813		58.549		12.225		100.0033		90.25622		12.225		100.00997		91.14744		12.225		100.01361		90.72878		12.225		100.00949

		60.726		12.25		100.01444		100.01		58.914		12.25		99.99978		58.687		12.25		100.00567		90.47444		12.25		100.01		91.35967		12.25		100.01361		90.94744		12.25		100.0095

		60.865		12.275		100.01208		100.01003		59.044		12.275		99.99966		58.816		12.275		100.00468		90.69455		12.275		100.01003		91.57822		12.275		100.01362		91.16944		12.275		100.0095

		60.997		12.3		100.00807		100.01006		59.175		12.3		99.99887		58.943		12.3		100.00182		90.91255		12.3		100.01006		91.79756		12.3		100.01362		91.38778		12.3		100.00951

		61.124		12.325		100.01398		100.01008		59.319		12.325		100.00104		59.09		12.325		100.00317		91.13144		12.325		100.01008		92.01233		12.325		100.01363		91.61022		12.325		100.00953

		61.246		12.35		100.00895		100.01011		59.443		12.35		99.99792		59.225		12.35		100.00497		91.34644		12.35		100.01011		92.22822		12.35		100.01364		91.82922		12.35		100.00954

		61.397		12.375		100.0108		100.01013		59.596		12.375		100.0001		59.358		12.375		100.00415		91.56678		12.375		100.01013		92.43967		12.375		100.01366		92.04967		12.375		100.00956

		61.526		12.4		100.01209		100.01016		59.709		12.4		100.00029		59.496		12.4		100.00309		91.78956		12.4		100.01016		92.65445		12.4		100.01367		92.26989		12.4		100.00958

		61.668		12.425		100.01122		100.01018		59.852		12.425		99.99971		59.631		12.425		100.00526		92.004		12.425		100.01018		92.86978		12.425		100.01369		92.48867		12.425		100.0096

		61.793		12.45		100.00853		100.0102		60		12.45		100.00002		59.761		12.45		100.00462		92.21956		12.45		100.0102		93.09067		12.45		100.01371		92.70367		12.45		100.00962

		61.934		12.475		100.00662		100.01022		60.13		12.475		99.99947		59.907		12.475		100.00443		92.43167		12.475		100.01022		93.31278		12.475		100.01372		92.92456		12.475		100.00964

		62.074		12.5		100.00989		100.01023		60.266		12.5		100.0012		60.037		12.5		100.00567		92.64678		12.5		100.01023		93.53189		12.5		100.01374		93.147		12.5		100.00967

		62.202		12.525		100.01101		100.01025		60.402		12.525		100.00181		60.18		12.525		100.00542		92.86456		12.525		100.01025		93.74767		12.525		100.01376		93.37411		12.525		100.00969

		62.341		12.55		100.01402		100.01026		60.55		12.55		99.99976		60.325		12.55		100.00588		93.08567		12.55		100.01026		93.96967		12.55		100.01378		93.60078		12.55		100.00971

		62.471		12.575		100.01086		100.01027		60.678		12.575		100.00159		60.463		12.575		100.00412		93.30722		12.575		100.01027		94.18611		12.575		100.0138		93.82711		12.575		100.00973

		62.618		12.6		100.0122		100.01028		60.817		12.6		100.00127		60.599		12.6		100.00384		93.52933		12.6		100.01028		94.40467		12.6		100.01382		94.05733		12.6		100.00975

		62.747		12.625		100.01192		100.01029		60.947		12.625		100.00157		60.738		12.625		100.00273		93.74622		12.625		100.01029		94.62511		12.625		100.01384		94.28356		12.625		100.00977

		62.875		12.65		100.01154		100.0103		61.094		12.65		100.00006		60.878		12.65		100.00431		93.97178		12.65		100.0103		94.84656		12.65		100.01385		94.51233		12.65		100.00978

		63.015		12.675		100.01014		100.0103		61.232		12.675		99.99793		61.017		12.675		100.00382		94.19256		12.675		100.0103		95.06167		12.675		100.01387		94.74278		12.675		100.0098

		63.147		12.7		100.01504		100.0103		61.365		12.7		99.99989		61.162		12.7		100.00418		94.42		12.7		100.0103		95.28222		12.7		100.01388		94.97444		12.7		100.00981

		63.299		12.725		100.00865		100.01031		61.511		12.725		100.00028		61.287		12.725		100.00468		94.643		12.725		100.01031		95.50478		12.725		100.0139		95.20311		12.725		100.00981

		63.427		12.75		100.00934		100.01031		61.651		12.75		100.0007		61.425		12.75		100.00477		94.86667		12.75		100.01031		95.73022		12.75		100.01391		95.42622		12.75		100.00982

		63.576		12.775		100.01008		100.01031		61.78		12.775		100.00065		61.579		12.775		100.00407		95.08289		12.775		100.01031		95.95856		12.775		100.01392		95.65111		12.775		100.00982

		63.705		12.8		100.01142		100.01031		61.921		12.8		100.00242		61.717		12.8		100.00408		95.30344		12.8		100.01031		96.19422		12.8		100.01392		95.87244		12.8		100.00982

		63.847		12.825		100.01093		100.01031		62.054		12.825		100.00086		61.841		12.825		100.00374		95.52067		12.825		100.01031		96.42333		12.825		100.01393		96.09755		12.825		100.00982

		63.979		12.85		100.01331		100.01032		62.198		12.85		100.00002		61.987		12.85		100.00401		95.73833		12.85		100.01032		96.65044		12.85		100.01394		96.32355		12.85		100.00982

		64.125		12.875		100.01008		100.01032		62.339		12.875		99.99962		62.117		12.875		100.00407		95.95589		12.875		100.01032		96.87456		12.875		100.01394		96.54978		12.875		100.00982

		64.257		12.9		100.01285		100.01033		62.48		12.9		100.00222		62.265		12.9		100.00478		96.17667		12.9		100.01033		97.10056		12.9		100.01395		96.77567		12.9		100.00982

		64.403		12.925		100.01133		100.01034		62.61		12.925		100.00027		62.408		12.925		100.00353		96.39545		12.925		100.01034		97.32289		12.925		100.01395		96.99944		12.925		100.00981

		64.54		12.95		100.0109		100.01036		62.757		12.95		100.00059		62.548		12.95		100.00437		96.61644		12.95		100.01036		97.54622		12.95		100.01395		97.22156		12.95		100.00981

		64.664		12.975		100.01049		100.01037		62.913		12.975		100.00234		62.69		12.975		100.00628		96.83089		12.975		100.01037		97.76955		12.975		100.01396		97.44922		12.975		100.00981

		64.821		13		100.01173		100.01039		63.043		13		100.00272		62.834		13		100.00419		97.05122		13		100.01039		97.99367		13		100.01396		97.67911		13		100.0098

		64.946		13.025		100.00964		100.01041		63.177		13.025		100.00065		62.975		13.025		100.0046		97.26844		13.025		100.01041		98.21067		13.025		100.01397		97.91456		13.025		100.0098

		65.079		13.05		100.00848		100.01044		63.321		13.05		100.001		63.12		13.05		100.00298		97.49111		13.05		100.01044		98.43267		13.05		100.01398		98.14367		13.05		100.00979

		65.235		13.075		100.01262		100.01047		63.459		13.075		100.00274		63.263		13.075		100.00421		97.71756		13.075		100.01047		98.65522		13.075		100.014		98.37322		13.075		100.00979

		65.37		13.1		100.01038		100.0105		63.612		13.1		100.00143		63.41		13.1		100.00484		97.94556		13.1		100.0105		98.88055		13.1		100.01401		98.60067		13.1		100.00979

		65.511		13.125		100.01591		100.01053		63.75		13.125		100.00131		63.543		13.125		100.00657		98.17056		13.125		100.01053		99.11011		13.125		100.01403		98.83133		13.125		100.00978

		65.651		13.15		100.01234		100.01056		63.897		13.15		100.00168		63.68		13.15		100.00386		98.39467		13.15		100.01056		99.34167		13.15		100.01405		99.06311		13.15		100.00978

		65.794		13.175		100.00913		100.01059		64.046		13.175		100.00402		63.833		13.175		100.00441		98.61933		13.175		100.01059		99.56878		13.175		100.01407		99.29867		13.175		100.00978

		65.941		13.2		100.01528		100.01062		64.186		13.2		100.00007		63.969		13.2		100.00567		98.85233		13.2		100.01062		99.79744		13.2		100.0141		99.52922		13.2		100.00979

		66.082		13.225		100.01069		100.01065		64.321		13.225		99.99995		64.106		13.225		100.00615		99.08378		13.225		100.01065		100.02622		13.225		100.01413		99.75689		13.225		100.00979

		66.226		13.25		100.01228		100.01068		64.458		13.25		100.0001		64.267		13.25		100.00547		99.31767		13.25		100.01068		100.25844		13.25		100.01415		99.97978		13.25		100.0098

		66.36		13.275		100.01211		100.01071		64.612		13.275		99.99924		64.414		13.275		100.00451		99.54656		13.275		100.01071		100.48944		13.275		100.01418		100.20689		13.275		100.00981

		66.504		13.3		100.01293		100.01073		64.754		13.3		100.00378		64.552		13.3		100.00461		99.77356		13.3		100.01073		100.72044		13.3		100.01421		100.43633		13.3		100.00982

		66.658		13.325		100.01052		100.01075		64.905		13.325		100.00324		64.687		13.325		100.00407		99.99589		13.325		100.01075		100.94922		13.325		100.01424		100.66589		13.325		100.00983

		66.797		13.35		100.01105		100.01077		65.042		13.35		100.00202		64.836		13.35		100.0046		100.22433		13.35		100.01077		101.17578		13.35		100.01426		100.89056		13.35		100.00984

		66.952		13.375		100.00892		100.01078		65.182		13.375		100.00004		64.998		13.375		100.00464		100.45344		13.375		100.01078		101.40111		13.375		100.01429		101.11533		13.375		100.00986

		67.081		13.4		100.01322		100.0108		65.329		13.4		100.00148		65.134		13.4		100.00543		100.68111		13.4		100.0108		101.62744		13.4		100.01431		101.337		13.4		100.00987

		67.227		13.425		100.01095		100.01081		65.488		13.425		100.00402		65.276		13.425		100.00609		100.90289		13.425		100.01081		101.85		13.425		100.01433		101.56211		13.425		100.00989

		67.372		13.45		100.01153		100.01082		65.63		13.45		99.99996		65.421		13.45		100.0031		101.12456		13.45		100.01082		102.07311		13.45		100.01435		101.78967		13.45		100.0099

		67.51		13.475		100.01148		100.01083		65.76		13.475		100.00064		65.572		13.475		100.00451		101.34689		13.475		100.01083		102.294		13.475		100.01436		102.01989		13.475		100.00992

		67.651		13.5		100.01026		100.01084		65.921		13.5		100.00151		65.722		13.5		100.00633		101.57133		13.5		100.01084		102.51922		13.5		100.01437		102.248		13.5		100.00993

		67.793		13.525		100.01258		100.01084		66.063		13.525		100.00219		65.856		13.525		100.00636		101.798		13.525		100.01084		102.74378		13.525		100.01438		102.47656		13.525		100.00994

		67.945		13.55		100.0123		100.01085		66.207		13.55		100.00242		65.997		13.55		100.00457		102.029		13.55		100.01085		102.96489		13.55		100.01439		102.70611		13.55		100.00996

		68.089		13.575		100.00802		100.01086		66.364		13.575		100.00061		66.154		13.575		100.00369		102.25278		13.575		100.01086		103.18822		13.575		100.01439		102.93667		13.575		100.00997

		68.233		13.6		100.01017		100.01088		66.508		13.6		100.00361		66.295		13.6		100.00394		102.47656		13.6		100.01088		103.41644		13.6		100.0144		103.16833		13.6		100.00998

		68.373		13.625		100.01131		100.01089		66.644		13.625		100.00162		66.444		13.625		100.00494		102.69733		13.625		100.01089		103.64845		13.625		100.0144		103.40244		13.625		100.00999

		68.519		13.65		100.01002		100.0109		66.797		13.65		99.99863		66.587		13.65		100.00772		102.92344		13.65		100.0109		103.88		13.65		100.0144		103.63256		13.65		100.00999

		68.653		13.675		100.00964		100.01092		66.961		13.675		100.00021		66.739		13.675		100.00197		103.14955		13.675		100.01092		104.10867		13.675		100.0144		103.86233		13.675		100.01

		68.807		13.7		100.00814		100.01094		67.103		13.7		100.00215		66.889		13.7		100.00475		103.37789		13.7		100.01094		104.33533		13.7		100.0144		104.09178		13.7		100.01001

		68.955		13.725		100.01213		100.01096		67.249		13.725		100.00249		67.037		13.725		100.00235		103.60389		13.725		100.01096		104.56244		13.725		100.01439		104.32044		13.725		100.01001

		69.099		13.75		100.00821		100.01097		67.401		13.75		100.00387		67.174		13.75		100.003		103.83044		13.75		100.01097		104.79244		13.75		100.01439		104.55011		13.75		100.01002

		69.238		13.775		100.00967		100.01099		67.557		13.775		100.00105		67.323		13.775		100.00217		104.05755		13.775		100.01099		105.02744		13.775		100.01438		104.78167		13.775		100.01002

		69.397		13.8		100.00904		100.01101		67.702		13.8		100.00061		67.467		13.8		100.00721		104.28533		13.8		100.01101		105.25678		13.8		100.01438		105.01378		13.8		100.01003

		69.542		13.825		100.01292		100.01103		67.835		13.825		100.00239		67.627		13.825		100.00963		104.513		13.825		100.01103		105.48378		13.825		100.01437		105.24456		13.825		100.01003

		69.685		13.85		100.01133		100.01105		67.988		13.85		100.00244		67.766		13.85		100.00865		104.74633		13.85		100.01105		105.70633		13.85		100.01436		105.47444		13.85		100.01003

		69.823		13.875		100.0101		100.01107		68.138		13.875		100.00189		67.918		13.875		100.00592		104.97522		13.875		100.01107		105.93456		13.875		100.01435		105.71056		13.875		100.01003

		69.986		13.9		100.00912		100.01108		68.285		13.9		100.00056		68.071		13.9		100.00446		105.20478		13.9		100.01108		106.16567		13.9		100.01434		105.94645		13.9		100.01003

		70.136		13.925		100.01346		100.0111		68.429		13.925		100.00425		68.217		13.925		100.00397		105.43044		13.925		100.0111		106.40033		13.925		100.01433		106.18144		13.925		100.01003

		70.289		13.95		100.0104		100.01112		68.585		13.95		99.99803		68.369		13.95		100.00605		105.65733		13.95		100.01112		106.62845		13.95		100.01432		106.41933		13.95		100.01002

		70.427		13.975		100.01026		100.01113		68.737		13.975		100.00251		68.508		13.975		100.00531		105.88189		13.975		100.01113		106.85456		13.975		100.01431		106.65256		13.975		100.01002

		70.575		14		100.01373		100.01114		68.882		14		100.00138		68.655		14		100.00438		106.108		14		100.01114		107.08233		14		100.0143		106.88522		14		100.01001

		70.721		14.025		100.0141		100.01116		69.032		14.025		100.00024		68.82		14.025		100.00208		106.33811		14.025		100.01116		107.313		14.025		100.01429		107.12		14.025		100.01

		70.863		14.05		100.01072		100.01117		69.184		14.05		100.002		68.977		14.05		100.00464		106.56567		14.05		100.01117		107.54322		14.05		100.01428		107.35389		14.05		100.00999

		71.008		14.075		100.0106		100.01118		69.337		14.075		100.00061		69.127		14.075		100.00456		106.79167		14.075		100.01118		107.78111		14.075		100.01427		107.58867		14.075		100.00998

		71.158		14.1		100.00731		100.01119		69.485		14.1		100.00409		69.273		14.1		100.00406		107.02067		14.1		100.01119		108.01478		14.1		100.01426		107.82422		14.1		100.00997

		71.311		14.125		100.01091		100.0112		69.646		14.125		100.0001		69.417		14.125		100.00567		107.24756		14.125		100.0112		108.24633		14.125		100.01425		108.05678		14.125		100.00995

		71.468		14.15		100.00953		100.01121		69.792		14.15		100.00255		69.562		14.15		100.00007		107.47711		14.15		100.01121		108.47844		14.15		100.01424		108.28867		14.15		100.00993

		71.614		14.175		100.01233		100.01121		69.95		14.175		100.00333		69.727		14.175		100.00414		107.71211		14.175		100.01121		108.71211		14.175		100.01423		108.52056		14.175		100.00992

		71.763		14.2		100.00924		100.01122		70.098		14.2		100.00442		69.867		14.2		100.00346		107.94667		14.2		100.01122		108.94567		14.2		100.01423		108.75444		14.2		100.0099

		71.903		14.225		100.01246		100.01122		70.247		14.225		100.00459		70.032		14.225		100.00472		108.17989		14.225		100.01122		109.18011		14.225		100.01422		108.99056		14.225		100.00988

		72.061		14.25		100.01799		100.01122		70.404		14.25		99.99837		70.181		14.25		100.00586		108.41422		14.25		100.01122		109.41522		14.25		100.01422		109.22533		14.25		100.00986

		72.215		14.275		100.01182		100.01122		70.558		14.275		100.00156		70.32		14.275		100.00518		108.64722		14.275		100.01122		109.645		14.275		100.01422		109.46022		14.275		100.00984

		72.384		14.3		100.0079		100.01122		70.711		14.3		100.00187		70.478		14.3		100.00578		108.88145		14.3		100.01122		109.87		14.3		100.01422		109.69156		14.3		100.00983

		72.528		14.325		100.01087		100.01121		70.853		14.325		100.00051		70.625		14.325		100.00577		109.11867		14.325		100.01121		110.09778		14.325		100.01423		109.92133		14.325		100.00981

		72.689		14.35		100.01208		100.01121		71.001		14.35		100.00288		70.792		14.35		100.00463		109.35611		14.35		100.01121		110.32422		14.35		100.01424		110.15289		14.35		100.0098

		72.824		14.375		100.01184		100.0112		71.166		14.375		100.00244		70.929		14.375		100.0053		109.59211		14.375		100.0112		110.55111		14.375		100.01425		110.38733		14.375		100.00978

		72.965		14.4		100.01377		100.01119		71.323		14.4		100.00222		71.104		14.4		100.00408		109.82322		14.4		100.01119		110.78067		14.4		100.01426		110.61789		14.4		100.00977

		73.123		14.425		100.01136		100.01118		71.479		14.425		100.00213		71.245		14.425		100.004		110.05333		14.425		100.01118		111.00744		14.425		100.01427		110.84767		14.425		100.00976

		73.266		14.45		100.01401		100.01117		71.636		14.45		100.00469		71.401		14.45		100.00153		110.28133		14.45		100.01117		111.23289		14.45		100.01429		111.07344		14.45		100.00976

		73.42		14.475		100.00708		100.01116		71.771		14.475		99.99934		71.549		14.475		100.00734		110.51055		14.475		100.01116		111.45933		14.475		100.01432		111.30222		14.475		100.00975

		73.574		14.5		100.00643		100.01114		71.937		14.5		100.00227		71.696		14.5		100.00629		110.73755		14.5		100.01114		111.68722		14.5		100.01434		111.53144		14.5		100.00975

		73.723		14.525		100.01043		100.01113		72.093		14.525		100.00055		71.852		14.525		100.00268		110.96022		14.525		100.01113		111.91789		14.525		100.01437		111.76433		14.525		100.00976

		73.881		14.55		100.00835		100.01113		72.248		14.55		100.00327		72.009		14.55		100.00458		111.17922		14.55		100.01113		112.14756		14.55		100.0144		111.998		14.55		100.00976

		74.026		14.575		100.01208		100.01112		72.398		14.575		100.00458		72.172		14.575		100.00741		111.39822		14.575		100.01112		112.37589		14.575		100.01444		112.22856		14.575		100.00977

		74.182		14.6		100.00987		100.01111		72.553		14.6		100.00007		72.312		14.6		100.00685		111.62		14.6		100.01111		112.59978		14.6		100.01447		112.46011		14.6		100.00978

		74.335		14.625		100.01478		100.01111		72.705		14.625		100.003		72.467		14.625		100.00357		111.84378		14.625		100.01111		112.82722		14.625		100.01451		112.69467		14.625		100.00979

		74.488		14.65		100.01201		100.01111		72.863		14.65		99.99826		72.635		14.65		100.00825		112.06933		14.65		100.01111		113.05489		14.65		100.01455		112.92556		14.65		100.00981

		74.647		14.675		100.00774		100.01111		73.014		14.675		100.00269		72.785		14.675		100.00457		112.29433		14.675		100.01111		113.28522		14.675		100.01458		113.15956		14.675		100.00982

		74.798		14.7		100.01292		100.01111		73.18		14.7		100.00437		72.948		14.7		100.00488		112.518		14.7		100.01111		113.51178		14.7		100.01462		113.39778		14.7		100.00984

		74.968		14.725		100.0118		100.01112		73.324		14.725		99.99927		73.102		14.725		100.00499		112.746		14.725		100.01112		113.74555		14.725		100.01465		113.63545		14.725		100.00985

		75.108		14.75		100.00835		100.01113		73.485		14.75		100.0017		73.246		14.75		100.00346		112.97644		14.75		100.01113		113.978		14.75		100.01468		113.86989		14.75		100.00987

		75.248		14.775		100.00942		100.01114		73.637		14.775		99.99929		73.411		14.775		100.00675		113.20767		14.775		100.01114		114.20556		14.775		100.01471		114.10578		14.775		100.00989

		75.407		14.8		100.01023		100.01115		73.8		14.8		99.99962		73.557		14.8		100.00094		113.44244		14.8		100.01115		114.43756		14.8		100.01474		114.343		14.8		100.0099

		75.564		14.825		100.0089		100.01117		73.955		14.825		100.00299		73.72		14.825		100.00793		113.67466		14.825		100.01117		114.677		14.825		100.01477		114.58211		14.825		100.00992

		75.72		14.85		100.01292		100.01118		74.115		14.85		99.99935		73.88		14.85		100.00412		113.90166		14.85		100.01118		114.91211		14.85		100.01479		114.81933		14.85		100.00993

		75.879		14.875		100.01276		100.01119		74.27		14.875		100.00322		74.054		14.875		100.00371		114.13011		14.875		100.01119		115.14645		14.875		100.01481		115.06222		14.875		100.00995

		76.018		14.9		100.01175		100.01121		74.438		14.9		99.99785		74.207		14.9		100.00273		114.35966		14.9		100.01121		115.37756		14.9		100.01483		115.30089		14.9		100.00996

		76.182		14.925		100.01213		100.01122		74.587		14.925		100.00258		74.368		14.925		100.00492		114.58722		14.925		100.01122		115.60989		14.925		100.01484		115.52867		14.925		100.00998

		76.342		14.95		100.01224		100.01123		74.749		14.95		100.00335		74.517		14.95		100.00763		114.81211		14.95		100.01123		115.83578		14.95		100.01485		115.75678		14.95		100.00999

		76.493		14.975		100.0093		100.01124		74.91		14.975		100.00059		74.674		14.975		100.00292		115.03978		14.975		100.01124		116.06233		14.975		100.01487		115.99311		14.975		100.01001

		76.642		15		100.00815		100.01125		75.069		15		100.00449		74.828		15		100.00285		115.26733		15		100.01125		116.29411		15		100.01488		116.22633		15		100.01002

		76.807		15.025		100.01072		100.01125		75.22		15.025		99.99982		74.987		15.025		100.00743		115.49211		15.025		100.01125		116.52211		15.025		100.01489		116.45589		15.025		100.01003

		76.97		15.05		100.00656		100.01125		75.388		15.05		99.99734		75.142		15.05		100.00606		115.71678		15.05		100.01125		116.74878		15.05		100.01489		116.68556		15.05		100.01005

		77.127		15.075		100.01285		100.01125		75.534		15.075		100.0002		75.302		15.075		100.00465		115.94733		15.075		100.01125		116.977		15.075		100.0149		116.91811		15.075		100.01006

		77.269		15.1		100.01373		100.01125		75.699		15.1		100.00277		75.459		15.1		100.00558		116.17389		15.1		100.01125		117.20745		15.1		100.01491		117.15		15.1		100.01007

		77.433		15.125		100.01221		100.01125		75.847		15.125		100.00275		75.62		15.125		100.00427		116.403		15.125		100.01125		117.44133		15.125		100.01491		117.38467		15.125		100.01008

		77.589		15.15		100.01326		100.01124		76.009		15.15		100.00168		75.781		15.15		100.00685		116.63445		15.15		100.01124		117.67711		15.15		100.01492		117.62556		15.15		100.01009

		77.742		15.175		100.00956		100.01124		76.166		15.175		99.99978		75.938		15.175		100.00559		116.86789		15.175		100.01124		117.91645		15.175		100.01492		117.86911		15.175		100.01009

		77.896		15.2		100.01729		100.01123		76.314		15.2		100.00387		76.099		15.2		100.00699		117.09967		15.2		100.01123		118.15478		15.2		100.01493		118.10233		15.2		100.0101

		78.051		15.225		100.00828		100.01122		76.487		15.225		100.00011		76.258		15.225		100.00417		117.332		15.225		100.01122		118.39222		15.225		100.01493		118.33689		15.225		100.0101

		78.208		15.25		100.01038		100.01121		76.638		15.25		100.00087		76.418		15.25		100.00569		117.56633		15.25		100.01121		118.63378		15.25		100.01493		118.57644		15.25		100.01011

		78.371		15.275		100.0116		100.0112		76.81		15.275		100.0067		76.573		15.275		100.0054		117.79744		15.275		100.0112		118.87433		15.275		100.01493		118.81367		15.275		100.01011

		78.528		15.3		100.01242		100.01119		76.966		15.3		100.00082		76.739		15.3		100.00634		118.02756		15.3		100.01119		119.11411		15.3		100.01493		119.04867		15.3		100.01011

		78.697		15.325		100.0097		100.01118		77.144		15.325		99.99808		76.893		15.325		100.0064		118.26144		15.325		100.01118		119.35244		15.325		100.01492		119.28655		15.325		100.01011

		78.852		15.35		100.00956		100.01117		77.296		15.35		99.99996		77.059		15.35		100.00279		118.48867		15.35		100.01117		119.58722		15.35		100.01492		119.52311		15.35		100.01011

		79.008		15.375		100.01467		100.01116		77.45		15.375		100.00454		77.208		15.375		100.002		118.71655		15.375		100.01116		119.82222		15.375		100.01492		119.75644		15.375		100.01011

		79.169		15.4		100.01051		100.01115		77.61		15.4		100.00331		77.371		15.4		100.00143		118.94767		15.4		100.01115		120.05833		15.4		100.01491		119.99033		15.4		100.01011

		79.338		15.425		100.01247		100.01114		77.779		15.425		100.00186		77.546		15.425		99.99907		119.18055		15.425		100.01114		120.28878		15.425		100.01491		120.22811		15.425		100.0101

		79.498		15.45		100.01388		100.01114		77.937		15.45		99.99924		77.706		15.45		100.00321		119.41189		15.45		100.01114		120.51989		15.45		100.01491		120.46656		15.45		100.0101

		79.649		15.475		100.01069		100.01113		78.11		15.475		100.00408		77.87		15.475		100.01124		119.643		15.475		100.01113		120.74933		15.475		100.0149		120.706		15.475		100.01009

		79.806		15.5		100.00742		100.01113		78.26		15.5		100.00271		78.035		15.5		100.00947		119.87844		15.5		100.01113		120.97811		15.5		100.0149		120.94411		15.5		100.01009

		79.981		15.525		100.00473		100.01113		78.421		15.525		100.00382		78.195		15.525		100.00566		120.11422		15.525		100.01113		121.20978		15.525		100.01491		121.18289		15.525		100.01009

		80.117		15.55		100.00895		100.01113		78.587		15.55		100.00219		78.35		15.55		100.00482		120.34378		15.55		100.01113		121.44622		15.55		100.01491		121.42		15.55		100.01008

		80.282		15.575		100.01102		100.01113		78.742		15.575		100.00345		78.511		15.575		100.00815		120.58033		15.575		100.01113		121.68033		15.575		100.01491		121.65311		15.575		100.01008

		80.452		15.6		100.0123		100.01113		78.906		15.6		100.00108		78.682		15.6		100.01059		120.81733		15.6		100.01113		121.91311		15.6		100.01492		121.88978		15.6		100.01008

		80.608		15.625		100.01437		100.01113		79.081		15.625		100.00065		78.856		15.625		99.99985		121.04867		15.625		100.01113		122.14511		15.625		100.01493		122.12545		15.625		100.01008

		80.761		15.65		100.00975		100.01113		79.243		15.65		99.99982		79.005		15.65		100.00992		121.27978		15.65		100.01113		122.37867		15.65		100.01494		122.35822		15.65		100.01007

		80.921		15.675		100.0115		100.01114		79.405		15.675		100.00302		79.165		15.675		100.00821		121.51422		15.675		100.01114		122.61267		15.675		100.01496		122.592		15.675		100.01007

		81.091		15.7		100.01068		100.01114		79.569		15.7		100.00345		79.331		15.7		100.00733		121.74722		15.7		100.01114		122.84645		15.7		100.01497		122.82489		15.7		100.01007

		81.256		15.725		100.00991		100.01114		79.727		15.725		100.00083		79.492		15.725		100.00845		121.98		15.725		100.01114		123.08456		15.725		100.01499		123.06178		15.725		100.01007

		81.42		15.75		100.01294		100.01115		79.892		15.75		99.99976		79.656		15.75		100.00248		122.21344		15.75		100.01115		123.32089		15.75		100.01501		123.29933		15.75		100.01008

		81.594		15.775		100.01271		100.01115		80.055		15.775		100.00498		79.82		15.775		99.99552		122.45233		15.775		100.01115		123.54933		15.775		100.01502		123.53444		15.775		100.01008

		81.743		15.8		100.01027		100.01116		80.219		15.8		100.00388		79.989		15.8		99.99861		122.68456		15.8		100.01116		123.78178		15.8		100.01504		123.777		15.8		100.01008

		81.909		15.825		100.00942		100.01116		80.386		15.825		99.99973		80.144		15.825		100.00866		122.91833		15.825		100.01116		124.01589		15.825		100.01505		124.01855		15.825		100.01009

		82.075		15.85		100.01427		100.01116		80.557		15.85		100.00239		80.306		15.85		100.00115		123.15755		15.85		100.01116		124.25045		15.85		100.01507		124.26044		15.85		100.0101

		82.229		15.875		100.01551		100.01116		80.729		15.875		100.0049		80.482		15.875		100.00326		123.39611		15.875		100.01116		124.486		15.875		100.01508		124.50489		15.875		100.0101

		82.406		15.9		100.01218		100.01116		80.878		15.9		99.99924		80.645		15.9		100.00389		123.63222		15.9		100.01116		124.72011		15.9		100.01509		124.74644		15.9		100.01011

		82.558		15.925		100.00734		100.01117		81.06		15.925		100.00066		80.809		15.925		100.00488		123.86755		15.925		100.01117		124.95289		15.925		100.0151		124.98822		15.925		100.01012

		82.728		15.95		100.01052		100.01117		81.211		15.95		100.00275		80.979		15.95		99.99793		124.10233		15.95		100.01117		125.18144		15.95		100.0151		125.22311		15.95		100.01013

		82.88		15.975		100.00967		100.01116		81.382		15.975		99.99988		81.137		15.975		100.0028		124.33833		15.975		100.01116		125.41111		15.975		100.01511		125.463		15.975		100.01013

		83.061		16		100.0076		100.01116		81.549		16		99.99901		81.307		16		100.00881		124.57189		16		100.01116		125.65078		16		100.01511		125.70378		16		100.01014

		83.214		16.025		100.01507		100.01116		81.718		16.025		100.00362		81.477		16.025		99.99989		124.80833		16.025		100.01116		125.88967		16.025		100.01512		125.94156		16.025		100.01015

		83.382		16.05		100.01146		100.01116		81.878		16.05		100.00478		81.635		16.05		100.01227		125.04255		16.05		100.01116		126.12767		16.05		100.01512		126.18134		16.05		100.01015

		83.542		16.075		100.00988		100.01116		82.053		16.075		100.00214		81.81		16.075		100.00353		125.27511		16.075		100.01116		126.36378		16.075		100.01512		126.41889		16.075		100.01016

		83.715		16.1		100.01165		100.01116		82.224		16.1		100.003		81.973		16.1		100.00232		125.51055		16.1		100.01116		126.60211		16.1		100.01512		126.663		16.1		100.01016

		83.886		16.125		100.01183		100.01115		82.399		16.125		100.00082		82.139		16.125		100.00446		125.74422		16.125		100.01115		126.84422		16.125		100.01511		126.90767		16.125		100.01016

		84.046		16.15		100.01234		100.01115		82.559		16.15		99.99927		82.309		16.15		100.00646		125.98067		16.15		100.01115		127.08556		16.15		100.01511		127.153		16.15		100.01016

		84.209		16.175		100.00917		100.01115		82.731		16.175		100.00383		82.477		16.175		100.00561		126.21722		16.175		100.01115		127.32889		16.175		100.01511		127.40045		16.175		100.01016

		84.369		16.2		100.01022		100.01115		82.9		16.2		100.00229		82.651		16.2		100.00294		126.45044		16.2		100.01115		127.57067		16.2		100.01511		127.64378		16.2		100.01015

		84.544		16.225		100.00947		100.01115		83.059		16.225		100.00316		82.81		16.225		100.00507		126.68867		16.225		100.01115		127.80367		16.225		100.01511		127.88878		16.225		100.01015

		84.714		16.25		100.00863		100.01115		83.225		16.25		99.99911		82.975		16.25		100.00611		126.93022		16.25		100.01115		128.03867		16.25		100.01512		128.13145		16.25		100.01015

		84.873		16.275		100.00846		100.01115		83.391		16.275		99.99781		83.138		16.275		100.00589		127.172		16.275		100.01115		128.27322		16.275		100.01512		128.37245		16.275		100.01014

		85.048		16.3		100.01095		100.01115		83.574		16.3		100.00159		83.317		16.3		100.00553		127.41144		16.3		100.01115		128.51055		16.3		100.01512		128.616		16.3		100.01014

		85.21		16.325		100.01026		100.01115		83.73		16.325		100.00395		83.48		16.325		100.00469		127.64944		16.325		100.01115		128.74633		16.325		100.01513		128.85389		16.325		100.01014

		85.375		16.35		100.01308		100.01115		83.915		16.35		99.99946		83.651		16.35		100.00392		127.89122		16.35		100.01115		128.97955		16.35		100.01514		129.08822		16.35		100.01013

		85.544		16.375		100.00908		100.01116		84.08		16.375		99.9999		83.812		16.375		100.00663		128.131		16.375		100.01116		129.21367		16.375		100.01515		129.32267		16.375		100.01013

		85.72		16.4		100.00897		100.01116		84.245		16.4		100.00193		83.98		16.4		100.0056		128.37422		16.4		100.01116		129.44689		16.4		100.01516		129.55745		16.4		100.01014

		85.889		16.425		100.01294		100.01117		84.415		16.425		99.99999		84.158		16.425		100.00886		128.617		16.425		100.01117		129.68444		16.425		100.01517		129.79322		16.425		100.01014

		86.058		16.45		100.01053		100.01118		84.586		16.45		100.00342		84.318		16.45		100.01098		128.86033		16.45		100.01118		129.92233		16.45		100.01519		130.02734		16.45		100.01015

		86.226		16.475		100.01021		100.01118		84.757		16.475		100.0001		84.497		16.475		100.00056		129.101		16.475		100.01118		130.16078		16.475		100.0152		130.26289		16.475		100.01015

		86.387		16.5		100.01048		100.01119		84.922		16.5		100.00133		84.664		16.5		100.00938		129.33722		16.5		100.01119		130.40222		16.5		100.01522		130.50267		16.5		100.01016

		86.561		16.525		100.00967		100.0112		85.087		16.525		100.00415		84.834		16.525		100.0077		129.57644		16.525		100.0112		130.64056		16.525		100.01524		130.74145		16.525		100.01017

		86.726		16.55		100.01247		100.01121		85.262		16.55		100.00256		85.008		16.55		100.00038		129.81989		16.55		100.01121		130.88267		16.55		100.01525		130.98434		16.55		100.01019

		86.89		16.575		100.01053		100.01122		85.428		16.575		99.99893		85.178		16.575		100.00554		130.06211		16.575		100.01122		131.12533		16.575		100.01527		131.23045		16.575		100.0102

		87.058		16.6		100.01284		100.01124		85.608		16.6		100.00153		85.342		16.6		100.00367		130.30033		16.6		100.01124		131.369		16.6		100.01529		131.474		16.6		100.01021

		87.231		16.625		100.01334		100.01125		85.783		16.625		100.00667		85.524		16.625		100.00417		130.537		16.625		100.01125		131.60911		16.625		100.01531		131.72022		16.625		100.01023

		87.409		16.65		100.00911		100.01126		85.958		16.65		100.00132		85.688		16.65		100.00403		130.77633		16.65		100.01126		131.84656		16.65		100.01533		131.96411		16.65		100.01024

		87.569		16.675		100.0106		100.01127		86.124		16.675		100.00047		85.857		16.675		100.0048		131.01333		16.675		100.01127		132.08755		16.675		100.01535		132.21144		16.675		100.01026

		87.736		16.7		100.00996		100.01128		86.297		16.7		100.00376		86.029		16.7		100.00642		131.24855		16.7		100.01128		132.32578		16.7		100.01537		132.45867		16.7		100.01028

		87.915		16.725		100.00963		100.01129		86.467		16.725		99.998		86.208		16.725		100.00722		131.48833		16.725		100.01129		132.56422		16.725		100.01539		132.70333		16.725		100.01029

		88.088		16.75		100.00776		100.0113		86.625		16.75		99.99616		86.38		16.75		100.00351		131.72855		16.75		100.0113		132.80078		16.75		100.0154		132.94711		16.75		100.01031

		88.269		16.775		100.01111		100.01131		86.797		16.775		100.00043		86.546		16.775		100.00484		131.96044		16.775		100.01131		133.03644		16.775		100.01542		133.18578		16.775		100.01032

		88.439		16.8		100.00959		100.01131		86.972		16.8		100.00414		86.725		16.8		100.0067		132.19744		16.8		100.01131		133.27211		16.8		100.01544		133.426		16.8		100.01033

		88.602		16.825		100.01055		100.01132		87.157		16.825		100.00104		86.895		16.825		100.00671		132.43889		16.825		100.01132		133.50433		16.825		100.01545		133.66811		16.825		100.01034

		88.771		16.85		100.01322		100.01133		87.312		16.85		99.99993		87.069		16.85		100.0095		132.68233		16.85		100.01133		133.74355		16.85		100.01547		133.90855		16.85		100.01035

		88.957		16.875		100.00967		100.01133		87.497		16.875		100.00392		87.256		16.875		100.00437		132.92455		16.875		100.01133		133.98422		16.875		100.01548		134.15411		16.875		100.01036

		89.132		16.9		100.00718		100.01134		87.659		16.9		100.00242		87.424		16.9		100.00503		133.163		16.9		100.01134		134.22555		16.9		100.01549		134.39289		16.9		100.01037

		89.305		16.925		100.0074		100.01134		87.844		16.925		100.00209		87.597		16.925		100.00262		133.40389		16.925		100.01134		134.46433		16.925		100.01551		134.63545		16.925		100.01037

		89.472		16.95		100.01422		100.01134		88.017		16.95		99.99856		87.783		16.95		100.00272		133.64478		16.95		100.01134		134.70256		16.95		100.01552		134.87845		16.95		100.01037

		89.655		16.975		100.01372		100.01134		88.206		16.975		100.00369		87.949		16.975		100.00664		133.88644		16.975		100.01134		134.94378		16.975		100.01552		135.12245		16.975		100.01038

		89.828		17		100.01103		100.01134		88.364		17		100.00246		88.131		17		100.00573		134.12867		17		100.01134		135.19033		17		100.01553		135.36756		17		100.01038

		90.009		17.025		100.01068		100.01134		88.546		17.025		100.00244		88.301		17.025		100.00924		134.36578		17.025		100.01134		135.43633		17.025		100.01554		135.61234		17.025		100.01038

		90.178		17.05		100.01226		100.01134		88.729		17.05		99.9996		88.471		17.05		100.00364		134.60211		17.05		100.01134		135.68245		17.05		100.01554		135.85689		17.05		100.01038

		90.352		17.075		100.01074		100.01133		88.899		17.075		100.0022		88.654		17.075		100.00405		134.83344		17.075		100.01133		135.92589		17.075		100.01555		136.10356		17.075		100.01038

		90.533		17.1		100.00778		100.01133		89.078		17.1		100.00269		88.829		17.1		99.99763		135.06855		17.1		100.01133		136.16711		17.1		100.01555		136.35011		17.1		100.01037

		90.695		17.125		100.00989		100.01132		89.244		17.125		99.99821		89.004		17.125		100.00334		135.30722		17.125		100.01132		136.40856		17.125		100.01556		136.59844		17.125		100.01037

		90.87		17.15		100.00634		100.01131		89.428		17.15		100.00321		89.198		17.15		100.00587		135.54978		17.15		100.01131		136.65211		17.15		100.01556		136.84333		17.15		100.01037

		91.051		17.175		100.01087		100.0113		89.593		17.175		100.00209		89.349		17.175		100.00508		135.79089		17.175		100.0113		136.89511		17.175		100.01557		137.08755		17.175		100.01038

		91.228		17.2		100.00638		100.01129		89.775		17.2		100.00073		89.534		17.2		100.00777		136.03167		17.2		100.01129		137.13833		17.2		100.01557		137.33022		17.2		100.01038

		91.405		17.225		100.00897		100.01128		89.963		17.225		100.00083		89.707		17.225		100.00385		136.27433		17.225		100.01128		137.37533		17.225		100.01558		137.57455		17.225		100.01038

		91.581		17.25		100.00862		100.01127		90.127		17.25		100.00366		89.873		17.25		100.00553		136.51955		17.25		100.01127		137.61622		17.25		100.01559		137.81744		17.25		100.01038

		91.753		17.275		100.00884		100.01126		90.304		17.275		99.99914		90.048		17.275		100.00611		136.76567		17.275		100.01126		137.85756		17.275		100.0156		138.06022		17.275		100.01039

		91.925		17.3		100.00967		100.01125		90.485		17.3		100.00225		90.241		17.3		100.00911		137.01344		17.3		100.01125		138.09989		17.3		100.01561		138.30333		17.3		100.01039

		92.109		17.325		100.0089		100.01123		90.673		17.325		100.00167		90.419		17.325		100.00421		137.25655		17.325		100.01123		138.34244		17.325		100.01563		138.53911		17.325		100.0104

		92.277		17.35		100.01039		100.01122		90.839		17.35		100.00419		90.589		17.35		100.00548		137.50111		17.35		100.01122		138.58533		17.35		100.01565		138.78122		17.35		100.0104

		92.453		17.375		100.01149		100.0112		91.026		17.375		100.00133		90.771		17.375		100.00746		137.743		17.375		100.0112		138.82911		17.375		100.01566		139.02411		17.375		100.01041

		92.628		17.4		100.01035		100.01119		91.198		17.4		99.99811		90.949		17.4		100.00623		137.98622		17.4		100.01119		139.07245		17.4		100.01568		139.26745		17.4		100.01041

		92.808		17.425		100.00953		100.01117		91.382		17.425		100.004		91.129		17.425		100.0081		138.22589		17.425		100.01117		139.31878		17.425		100.0157		139.51334		17.425		100.01042

		92.992		17.45		100.01035		100.01115		91.565		17.45		100.00376		91.297		17.45		100.00787		138.46822		17.45		100.01115		139.56745		17.45		100.01572		139.75611		17.45		100.01042

		93.162		17.475		100.00858		100.01114		91.739		17.475		99.99918		91.483		17.475		100.00557		138.70911		17.475		100.01114		139.81167		17.475		100.01574		140.003		17.475		100.01043

		93.334		17.5		100.01101		100.01112		91.93		17.5		100.00298		91.67		17.5		100.00551		138.94711		17.5		100.01112		140.06045		17.5		100.01576		140.24934		17.5		100.01043

		93.517		17.525		100.00635		100.01111		92.093		17.525		100.003		91.845		17.525		100.00598		139.18867		17.525		100.01111		140.30689		17.525		100.01578		140.49434		17.525		100.01044

		93.701		17.55		100.00853		100.01109		92.273		17.55		99.99927		92.032		17.55		100.00417		139.42978		17.55		100.01109		140.55356		17.55		100.0158		140.74289		17.55		100.01044

		93.879		17.575		100.00976		100.01108		92.449		17.575		100.00313		92.203		17.575		100.00549		139.67034		17.575		100.01108		140.8		17.575		100.01581		140.98734		17.575		100.01045

		94.058		17.6		100.00608		100.01106		92.626		17.6		99.99941		92.382		17.6		100.00903		139.91278		17.6		100.01106		141.04322		17.6		100.01583		141.23033		17.6		100.01045

		94.238		17.625		100.01407		100.01105		92.818		17.625		100.00301		92.562		17.625		100.00409		140.14967		17.625		100.01105		141.28978		17.625		100.01584		141.47289		17.625		100.01045

		94.403		17.65		100.01049		100.01104		93		17.65		100.00442		92.74		17.65		100.00193		140.38833		17.65		100.01104		141.53022		17.65		100.01585		141.71589		17.65		100.01046

		94.593		17.675		100.01026		100.01104		93.175		17.675		100.00144		92.929		17.675		100.00805		140.62911		17.675		100.01104		141.77133		17.675		100.01586		141.95945		17.675		100.01046

		94.771		17.7		100.01153		100.01103		93.365		17.7		100.00553		93.109		17.7		99.99973		140.86922		17.7		100.01103		142.00889		17.7		100.01587		142.20067		17.7		100.01046

		94.949		17.725		100.00993		100.01103		93.543		17.725		100.00062		93.294		17.725		100.00381		141.11322		17.725		100.01103		142.24633		17.725		100.01588		142.44311		17.725		100.01046

		95.129		17.75		100.01085		100.01103		93.73		17.75		100.00175		93.459		17.75		100.00373		141.35389		17.75		100.01103		142.48389		17.75		100.01588		142.68756		17.75		100.01046

		95.305		17.775		100.00799		100.01104		93.916		17.775		100.00323		93.646		17.775		100.00737		141.59633		17.775		100.01104		142.72056		17.775		100.01588		142.93567		17.775		100.01046

		95.484		17.8		100.01205		100.01104		94.091		17.8		100.00084		93.84		17.8		100.00474		141.84067		17.8		100.01104		142.96311		17.8		100.01588		143.18311		17.8		100.01046

		95.663		17.825		100.01224		100.01105		94.27		17.825		100.00529		94.009		17.825		100.00598		142.08211		17.825		100.01105		143.20667		17.825		100.01588		143.43278		17.825		100.01046

		95.841		17.85		100.01124		100.01106		94.463		17.85		99.99971		94.188		17.85		99.99754		142.326		17.85		100.01106		143.44711		17.85		100.01588		143.68211		17.85		100.01047

		96.026		17.875		100.0117		100.01108		94.645		17.875		100.00154		94.362		17.875		100.00383		142.57044		17.875		100.01108		143.68978		17.875		100.01588		143.93233		17.875		100.01047

		96.216		17.9		100.01256		100.01109		94.83		17.9		100.00338		94.556		17.9		100.01025		142.81111		17.9		100.01109		143.931		17.9		100.01588		144.18411		17.9		100.01047

		96.399		17.925		100.00854		100.01111		95.008		17.925		100.00032		94.735		17.925		100.00596		143.05178		17.925		100.01111		144.17645		17.925		100.01588		144.43622		17.925		100.01047

		96.574		17.95		100.00971		100.01112		95.185		17.95		100.00044		94.915		17.95		100.0044		143.29522		17.95		100.01112		144.42134		17.95		100.01588		144.68956		17.95		100.01047

		96.756		17.975		100.00746		100.01114		95.36		17.975		100.00105		95.113		17.975		99.99823		143.535		17.975		100.01114		144.66945		17.975		100.01589		144.94389		17.975		100.01048

		96.95		18		100.00683		100.01116		95.547		18		99.99955		95.294		18		99.99623		143.77544		18		100.01116		144.918		18		100.01589		145.19589		18		100.01048

		97.12		18.025		100.00943		100.01117		95.739		18.025		100.00099		95.469		18.025		100.0034		144.01489		18.025		100.01117		145.15978		18.025		100.0159		145.44611		18.025		100.01048

		97.309		18.05		100.01		100.01119		95.922		18.05		99.9993		95.666		18.05		100.00858		144.25155		18.05		100.01119		145.403		18.05		100.01591		145.69889		18.05		100.01049

		97.495		18.075		100.00793		100.0112		96.089		18.075		100.0032		95.852		18.075		100.00195		144.49111		18.075		100.0112		145.64867		18.075		100.01592		145.95178		18.075		100.01049

		97.668		18.1		100.01266		100.01121		96.285		18.1		100.00045		96.032		18.1		100.00582		144.73344		18.1		100.01121		145.89934		18.1		100.01593		146.20256		18.1		100.0105

		97.853		18.125		100.0109		100.01122		96.476		18.125		100.00143		96.218		18.125		100.00473		144.97744		18.125		100.01122		146.14956		18.125		100.01595		146.45356		18.125		100.0105

		98.04		18.15		100.01099		100.01123		96.659		18.15		100.00162		96.392		18.15		100.00582		145.22366		18.15		100.01123		146.40334		18.15		100.01596		146.702		18.15		100.01051

		98.225		18.175		100.00916		100.01124		96.838		18.175		100.00058		96.579		18.175		100.00554		145.464		18.175		100.01124		146.65378		18.175		100.01598		146.94978		18.175		100.01051

		98.411		18.2		100.00591		100.01124		97.017		18.2		100.00138		96.777		18.2		100.00582		145.708		18.2		100.01124		146.90234		18.2		100.01599		147.19544		18.2		100.01052

		98.587		18.225		100.01013		100.01124		97.21		18.225		100.00001		96.959		18.225		100.0051		145.95211		18.225		100.01124		147.15333		18.225		100.01601		147.44322		18.225		100.01052

		98.776		18.25		100.01332		100.01124		97.392		18.25		100.00381		97.153		18.25		100.005		146.19511		18.25		100.01124		147.40378		18.25		100.01602		147.695		18.25		100.01052

		98.971		18.275		100.00946		100.01125		97.591		18.275		100.00167		97.351		18.275		100.00494		146.44444		18.275		100.01125		147.65567		18.275		100.01603		147.93922		18.275		100.01052

		99.137		18.3		100.00983		100.01125		97.778		18.3		100.00372		97.514		18.3		100.00596		146.69144		18.3		100.01125		147.903		18.3		100.01604		148.18889		18.3		100.01052

		99.337		18.325		100.0108		100.01125		97.957		18.325		100.00236		97.71		18.325		100.00654		146.94022		18.325		100.01125		148.14944		18.325		100.01605		148.43522		18.325		100.01052

		99.524		18.35		100.01059		100.01125		98.146		18.35		100.00244		97.89		18.35		100.00458		147.18578		18.35		100.01125		148.39789		18.35		100.01605		148.682		18.35		100.01052

		99.713		18.375		100.01001		100.01125		98.333		18.375		100.00096		98.079		18.375		100.00711		147.43311		18.375		100.01125		148.64278		18.375		100.01605		148.93056		18.375		100.01052

		99.885		18.4		100.00833		100.01125		98.527		18.4		100.00109		98.265		18.4		100.0048		147.68333		18.4		100.01125		148.89044		18.4		100.01606		149.17578		18.4		100.01052

		100.063		18.425		100.00949		100.01125		98.692		18.425		100.00073		98.45		18.425		100.00675		147.93133		18.425		100.01125		149.13722		18.425		100.01605		149.42233		18.425		100.01052

		100.262		18.45		100.01106		100.01125		98.892		18.45		100.00283		98.638		18.45		100.00469		148.18067		18.45		100.01125		149.38222		18.45		100.01605		149.667		18.45		100.01052

		100.439		18.475		100.0059		100.01125		99.084		18.475		100.00163		98.824		18.475		100.0023		148.42933		18.475		100.01125		149.63022		18.475		100.01605		149.91178		18.475		100.01052

		100.618		18.5		100.00647		100.01125		99.268		18.5		100.00144		99.012		18.5		100.00347		148.67533		18.5		100.01125		149.881		18.5		100.01604		150.162		18.5		100.01052

		100.819		18.525		100.01116		100.01125		99.45		18.525		100.00024		99.203		18.525		100.0051		148.92089		18.525		100.01125		150.13444		18.525		100.01604		150.40211		18.525		100.01052

		100.991		18.55		100.00943		100.01125		99.65		18.55		100.00452		99.374		18.55		100.00486		149.16122		18.55		100.01125		150.38067		18.55		100.01604		150.64844		18.55		100.01052

		101.185		18.575		100.0095		100.01125		99.83		18.575		100.00258		99.575		18.575		100.00302		149.40745		18.575		100.01125		150.625		18.575		100.01603		150.89455		18.575		100.01053

		101.364		18.6		100.00953		100.01125		100.008		18.6		100.00293		99.756		18.6		100.00688		149.64967		18.6		100.01125		150.87033		18.6		100.01603		151.14144		18.6		100.01053

		101.56		18.625		100.0073		100.01125		100.21		18.625		100.00153		99.956		18.625		100.00602		149.89322		18.625		100.01125		151.11811		18.625		100.01604		151.39255		18.625		100.01054

		101.757		18.65		100.01031		100.01125		100.398		18.65		99.99922		100.141		18.65		100.00745		150.14245		18.65		100.01125		151.36333		18.65		100.01604		151.64089		18.65		100.01054

		101.945		18.675		100.01049		100.01125		100.585		18.675		99.99737		100.329		18.675		100.00447		150.38511		18.675		100.01125		151.60833		18.675		100.01605		151.89078		18.675		100.01055

		102.117		18.7		100.00895		100.01125		100.79		18.7		100.00318		100.521		18.7		100.00289		150.62622		18.7		100.01125		151.85633		18.7		100.01606		152.13922		18.7		100.01056

		102.311		18.725		100.00664		100.01125		100.976		18.725		100.0049		100.711		18.725		100.0053		150.867		18.725		100.01125		152.10322		18.725		100.01607		152.39144		18.725		100.01057

		102.501		18.75		100.0078		100.01124		101.164		18.75		100.00136		100.908		18.75		100.00642		151.11444		18.75		100.01124		152.35033		18.75		100.01608		152.64922		18.75		100.01058

		102.683		18.775		100.00878		100.01124		101.356		18.775		100.00105		101.106		18.775		100.00506		151.36244		18.775		100.01124		152.60122		18.775		100.0161		152.90267		18.775		100.01059

		102.876		18.8		100.01296		100.01124		101.541		18.8		100.00059		101.289		18.8		100.00519		151.60522		18.8		100.01124		152.85022		18.8		100.01612		153.15678		18.8		100.0106

		103.071		18.825		100.00926		100.01124		101.724		18.825		99.99829		101.481		18.825		100.00604		151.85389		18.825		100.01124		153.101		18.825		100.01614		153.40989		18.825		100.01061

		103.254		18.85		100.00749		100.01124		101.922		18.85		100.0067		101.671		18.85		100.01175		152.10244		18.85		100.01124		153.35167		18.85		100.01616		153.66656		18.85		100.01061

		103.432		18.875		100.009		100.01123		102.1		18.875		100.00132		101.873		18.875		100.00591		152.34944		18.875		100.01123		153.60522		18.875		100.01618		153.925		18.875		100.01062

		103.626		18.9		100.00791		100.01123		102.303		18.9		100.00129		102.062		18.9		100.00512		152.60166		18.9		100.01123		153.85922		18.9		100.0162		154.18111		18.9		100.01063

		103.805		18.925		100.01047		100.01123		102.501		18.925		100.00358		102.244		18.925		100.00477		152.85389		18.925		100.01123		154.10978		18.925		100.01621		154.43589		18.925		100.01063

		104.01		18.95		100.00874		100.01123		102.683		18.95		100.00097		102.44		18.95		100.01095		153.10922		18.95		100.01123		154.35978		18.95		100.01623		154.68856		18.95		100.01063

		104.202		18.975		100.01036		100.01123		102.876		18.975		100.00115		102.635		18.975		100.00521		153.36033		18.975		100.01123		154.60933		18.975		100.01625		154.94011		18.975		100.01064

		104.387		19		100.00725		100.01123		103.075		19		100.0038		102.817		19		100.00206		153.61667		19		100.01123		154.86144		19		100.01626		155.19767		19		100.01063

		104.581		19.025		100.01162		100.01122		103.267		19.025		100.00186		103.025		19.025		100.00648		153.87644		19.025		100.01122		155.11789		19.025		100.01627		155.45611		19.025		100.01063

		104.769		19.05		100.00844		100.01122		103.451		19.05		99.99754		103.207		19.05		100.00478		154.12656		19.05		100.01122		155.37189		19.05		100.01628		155.71211		19.05		100.01063

		104.958		19.075		100.00947		100.01121		103.657		19.075		100.00282		103.399		19.075		100.00752		154.37789		19.075		100.01121		155.62578		19.075		100.01629		155.96422		19.075		100.01062

		105.143		19.1		100.00962		100.0112		103.844		19.1		100.00312		103.596		19.1		100.00918		154.62867		19.1		100.0112		155.87811		19.1		100.01629		156.21511		19.1		100.01062

		105.339		19.125		100.01069		100.01119		104.037		19.125		99.99985		103.777		19.125		99.99856		154.87811		19.125		100.01119		156.13078		19.125		100.01629		156.46878		19.125		100.01061

		105.531		19.15		100.0108		100.01118		104.226		19.15		100.00238		103.981		19.15		100.00509		155.131		19.15		100.01118		156.38478		19.15		100.01629		156.72466		19.15		100.0106

		105.721		19.175		100.00832		100.01117		104.431		19.175		100.00302		104.17		19.175		100.00238		155.37933		19.175		100.01117		156.63589		19.175		100.01629		156.97711		19.175		100.0106

		105.915		19.2		100.009		100.01116		104.62		19.2		99.9994		104.371		19.2		100.00456		155.62989		19.2		100.01116		156.88789		19.2		100.01629		157.23066		19.2		100.01059

		106.099		19.225		100.00865		100.01115		104.822		19.225		100.00104		104.564		19.225		100.00558		155.87644		19.225		100.01115		157.13956		19.225		100.01629		157.48366		19.225		100.01058

		106.306		19.25		100.0108		100.01114		105.009		19.25		100.00332		104.759		19.25		100.00665		156.12		19.25		100.01114		157.39256		19.25		100.01628		157.73822		19.25		100.01057

		106.493		19.275		100.00858		100.01112		105.225		19.275		100.00513		104.946		19.275		100.00541		156.37178		19.275		100.01112		157.64856		19.275		100.01628		157.99811		19.275		100.01056

		106.678		19.3		100.01106		100.01111		105.407		19.3		100.00293		105.146		19.3		100.00548		156.62033		19.3		100.01111		157.90611		19.3		100.01628		158.25789		19.3		100.01055

		106.872		19.325		100.0115		100.0111		105.605		19.325		100.00064		105.34		19.325		100.00396		156.87089		19.325		100.0111		158.163		19.325		100.01628		158.51278		19.325		100.01055

		107.063		19.35		100.01132		100.01108		105.79		19.35		100.00126		105.543		19.35		100.00714		157.12755		19.35		100.01108		158.42022		19.35		100.01628		158.769		19.35		100.01054

		107.261		19.375		100.0122		100.01107		105.979		19.375		100.00365		105.728		19.375		100.00742		157.38111		19.375		100.01107		158.675		19.375		100.01628		159.023		19.375		100.01054

		107.461		19.4		100.0106		100.01106		106.181		19.4		100.00589		105.922		19.4		100.00563		157.63844		19.4		100.01106		158.93333		19.4		100.01628		159.27945		19.4		100.01053

		107.644		19.425		100.01067		100.01105		106.372		19.425		100.00502		106.122		19.425		100.00449		157.89211		19.425		100.01105		159.19322		19.425		100.01628		159.53667		19.425		100.01053

		107.832		19.45		100.00955		100.01104		106.576		19.45		100.00096		106.318		19.45		99.99992		158.14378		19.45		100.01104		159.44756		19.45		100.01628		159.78645		19.45		100.01052

		108.033		19.475		100.00904		100.01104		106.768		19.475		99.99767		106.513		19.475		100.00514		158.39756		19.475		100.01104		159.69778		19.475		100.01629		160.03445		19.475		100.01052

		108.23		19.5		100.00728		100.01103		106.973		19.5		100.00076		106.712		19.5		100.00518		158.64878		19.5		100.01103		159.944		19.5		100.01629		160.27867		19.5		100.01052

		108.419		19.525		100.00825		100.01102		107.162		19.525		99.99871		106.914		19.525		100.00412		158.9		19.525		100.01102		160.18633		19.525		100.01629		160.52444		19.525		100.01052

		108.611		19.55		100.00632		100.01102		107.352		19.55		99.99952		107.108		19.55		100.01359		159.15189		19.55		100.01102		160.43322		19.55		100.0163		160.77489		19.55		100.01051

		108.808		19.575		100.00848		100.01102		107.552		19.575		100.00224		107.298		19.575		99.99716		159.39811		19.575		100.01102		160.67733		19.575		100.0163		161.02122		19.575		100.01051

		109.004		19.6		100.00787		100.01101		107.748		19.6		99.99813		107.494		19.6		100.00047		159.64578		19.6		100.01101		160.92189		19.6		100.01631		161.26789		19.6		100.01051

		109.209		19.625		100.00828		100.01101		107.953		19.625		100.00269		107.703		19.625		100.00925		159.89267		19.625		100.01101		161.16733		19.625		100.01631		161.51422		19.625		100.01051

		109.396		19.65		100.0116		100.01101		108.146		19.65		100.00016		107.901		19.65		100.01267		160.13633		19.65		100.01101		161.411		19.65		100.01631		161.75967		19.65		100.0105

		109.599		19.675		100.0078		100.01101		108.344		19.675		99.99919		108.088		19.675		100.00808		160.38578		19.675		100.01101		161.65733		19.675		100.01632		162.00767		19.675		100.0105

		109.776		19.7		100.0082		100.01101		108.54		19.7		100.00451		108.296		19.7		100.00984		160.63111		19.7		100.01101		161.90844		19.7		100.01632		162.25611		19.7		100.0105

		109.979		19.725		100.01156		100.01101		108.742		19.725		100.00253		108.49		19.725		99.99665		160.87566		19.725		100.01101		162.15744		19.725		100.01632		162.50322		19.725		100.01049

		110.171		19.75		100.01209		100.01101		108.938		19.75		100.00092		108.698		19.75		100.00463		161.12078		19.75		100.01101		162.40889		19.75		100.01631		162.75045		19.75		100.01049

		110.372		19.775		100.00972		100.01101		109.141		19.775		100.00515		108.895		19.775		99.99809		161.36089		19.775		100.01101		162.65544		19.775		100.01631		162.99578		19.775		100.01048

		110.563		19.8		100.00814		100.01101		109.338		19.8		99.99928		109.09		19.8		100.00078		161.60555		19.8		100.01101		162.90278		19.8		100.01631		163.24467		19.8		100.01047

		110.772		19.825		100.00896		100.01102		109.545		19.825		100.00502		109.286		19.825		100.0034		161.84733		19.825		100.01102		163.15144		19.825		100.01631		163.49411		19.825		100.01047

		110.968		19.85		100.01114		100.01102		109.732		19.85		100.00198		109.49		19.85		100.01119		162.08866		19.85		100.01102		163.39566		19.85		100.0163		163.741		19.85		100.01046

		111.159		19.875		100.01144		100.01102		109.934		19.875		100.0026		109.695		19.875		100.01089		162.335		19.875		100.01102		163.63966		19.875		100.0163		163.98589		19.875		100.01046

		111.351		19.9		100.01225		100.01103		110.132		19.9		100.0018		109.874		19.9		99.99842		162.58022		19.9		100.01103		163.88366		19.9		100.0163		164.235		19.9		100.01045

		111.548		19.925		100.01302		100.01103		110.338		19.925		100.00206		110.09		19.925		100.01074		162.82889		19.925		100.01103		164.12433		19.925		100.01629		164.48145		19.925		100.01045

		111.747		19.95		100.01247		100.01104		110.535		19.95		100.00071		110.28		19.95		100.00838		163.07711		19.95		100.01104		164.36988		19.95		100.01629		164.73422		19.95		100.01044

		111.931		19.975		100.00887		100.01105		110.739		19.975		100.00278		110.48		19.975		100.0076		163.32444		19.975		100.01105		164.61489		19.975		100.01629		164.98533		19.975		100.01044

		112.14		20		100.00904		100.01105		110.934		20		100.00131		110.69		20		99.99448		163.574		20		100.01105		164.86211		20		100.01629		165.237		20		100.01044

		112.33		20.025		100.01171		100.01106		111.139		20.025		99.9987		110.883		20.025		100.00426		163.81955		20.025		100.01106		165.10989		20.025		100.01629		165.48867		20.025		100.01044

		112.532		20.05		100.01291		100.01107		111.333		20.05		99.9992		111.073		20.05		100.0027		164.06322		20.05		100.01107		165.35644		20.05		100.01629		165.73978		20.05		100.01044

		112.72		20.075		100.00895		100.01109		111.539		20.075		99.99751		111.278		20.075		100.00106		164.30689		20.075		100.01109		165.606		20.075		100.01629		165.99356		20.075		100.01044

		112.922		20.1		100.00877		100.0111		111.736		20.1		100.00038		111.487		20.1		99.99982		164.54967		20.1		100.0111		165.856		20.1		100.01629		166.24845		20.1		100.01045

		113.125		20.125		100.00856		100.01111		111.931		20.125		100.00023		111.687		20.125		100.00024		164.79311		20.125		100.01111		166.10567		20.125		100.01629		166.50067		20.125		100.01045

		113.323		20.15		100.00962		100.01113		112.132		20.15		100.00369		111.886		20.15		100.00159		165.03378		20.15		100.01113		166.35567		20.15		100.0163		166.75622		20.15		100.01046

		113.522		20.175		100.00683		100.01114		112.341		20.175		99.99972		112.08		20.175		100.00552		165.26989		20.175		100.01114		166.60367		20.175		100.0163		167.00644		20.175		100.01046

		113.722		20.2		100.0153		100.01116		112.545		20.2		100.00246		112.296		20.2		100.00605		165.51189		20.2		100.01116		166.853		20.2		100.0163		167.25433		20.2		100.01046

		113.919		20.225		100.01031		100.01117		112.752		20.225		100.00359		112.485		20.225		100.005		165.75256		20.225		100.01117		167.10289		20.225		100.0163		167.50489		20.225		100.01047

		114.136		20.25		100.00793		100.01119		112.946		20.25		100.00053		112.701		20.25		100.00426		165.99456		20.25		100.01119		167.35589		20.25		100.0163		167.75267		20.25		100.01047

		114.323		20.275		100.00608		100.0112		113.16		20.275		99.99929		112.901		20.275		100.00377		166.24245		20.275		100.0112		167.60556		20.275		100.01631		168.00211		20.275		100.01048

		114.532		20.3		100.00594		100.01122		113.361		20.3		100.00138		113.099		20.3		100.00009		166.49111		20.3		100.01122		167.85622		20.3		100.01631		168.25222		20.3		100.01048

		114.729		20.325		100.00997		100.01124		113.56		20.325		100.00272		113.31		20.325		100.00575		166.74289		20.325		100.01124		168.10667		20.325		100.01631		168.50022		20.325		100.01049

		114.924		20.35		100.00913		100.01125		113.761		20.35		100.00387		113.512		20.35		100.0053		166.99078		20.35		100.01125		168.36		20.35		100.01632		168.747		20.35		100.01049

		115.127		20.375		100.00744		100.01127		113.96		20.375		100.00244		113.703		20.375		100.00691		167.239		20.375		100.01127		168.60922		20.375		100.01633		168.99278		20.375		100.01049

		115.324		20.4		100.00846		100.01128		114.161		20.4		100.00408		113.917		20.4		100.00463		167.49111		20.4		100.01128		168.85844		20.4		100.01633		169.242		20.4		100.0105

		115.516		20.425		100.01095		100.0113		114.356		20.425		100.00175		114.11		20.425		100.00531		167.73911		20.425		100.0113		169.10667		20.425		100.01635		169.49511		20.425		100.0105

		115.727		20.45		100.01011		100.01132		114.575		20.45		100.00071		114.317		20.45		100.00269		167.98889		20.45		100.01132		169.35644		20.45		100.01636		169.747		20.45		100.0105

		115.932		20.475		100.0068		100.01133		114.76		20.475		99.99815		114.53		20.475		100.00429		168.23289		20.475		100.01133		169.60667		20.475		100.01637		169.99766		20.475		100.01051

		116.138		20.5		100.01035		100.01134		114.98		20.5		99.99871		114.725		20.5		100.0052		168.47766		20.5		100.01134		169.86022		20.5		100.01639		170.24878		20.5		100.01051

		116.334		20.525		100.00985		100.01135		115.175		20.525		99.99925		114.933		20.525		100.00357		168.72367		20.525		100.01135		170.11478		20.525		100.01641		170.496		20.525		100.01052

		116.547		20.55		100.00807		100.01136		115.384		20.55		100.00157		115.14		20.55		100.00754		168.96778		20.55		100.01136		170.36489		20.55		100.01643		170.74856		20.55		100.01052

		116.743		20.575		100.00915		100.01137		115.585		20.575		100.00274		115.338		20.575		100.00488		169.21066		20.575		100.01137		170.61866		20.575		100.01645		171.004		20.575		100.01053

		116.94		20.6		100.01011		100.01138		115.796		20.6		100.0029		115.54		20.6		100.00425		169.45855		20.6		100.01138		170.87433		20.6		100.01647		171.25833		20.6		100.01053

		117.139		20.625		100.01182		100.01138		116.002		20.625		100.00182		115.748		20.625		100.00373		169.70522		20.625		100.01138		171.13211		20.625		100.01649		171.50956		20.625		100.01054

		117.336		20.65		100.01178		100.01138		116.201		20.65		100.00255		115.963		20.65		100.00932		169.95378		20.65		100.01138		171.38611		20.65		100.01651		171.76067		20.65		100.01055

		117.55		20.675		100.01076		100.01137		116.408		20.675		100.00262		116.155		20.675		100.00304		170.20355		20.675		100.01137		171.64034		20.675		100.01653		172.01378		20.675		100.01056

		117.752		20.7		100.00958		100.01136		116.618		20.7		100.00115		116.354		20.7		100.0035		170.45989		20.7		100.01136		171.89356		20.7		100.01654		172.271		20.7		100.01057

		117.954		20.725		100.0095		100.01135		116.813		20.725		100.00266		116.559		20.725		100.00614		170.71656		20.725		100.01135		172.14845		20.725		100.01656		172.52711		20.725		100.01058

		118.143		20.75		100.00696		100.01133		117.032		20.75		100.0019		116.774		20.75		100.00623		170.97122		20.75		100.01133		172.39789		20.75		100.01657		172.78244		20.75		100.01059

		118.355		20.775		100.01061		100.01131		117.238		20.775		100.00376		116.992		20.775		100.00396		171.22245		20.775		100.01131		172.65245		20.775		100.01658		173.039		20.775		100.0106

		118.561		20.8		100.01312		100.01128		117.452		20.8		99.99971		117.187		20.8		100.00466		171.47556		20.8		100.01128		172.90022		20.8		100.01659		173.29333		20.8		100.01061

		118.755		20.825		100.01018		100.01126		117.652		20.825		100.00309		117.393		20.825		100.00705		171.72467		20.825		100.01126		173.15067		20.825		100.01659		173.54822		20.825		100.01063

		118.956		20.85		100.01133		100.01123		117.867		20.85		100.00353		117.586		20.85		100.0066		171.97622		20.85		100.01123		173.39944		20.85		100.01659		173.806		20.85		100.01064

		119.179		20.875		100.00735		100.0112		118.083		20.875		100.00069		117.812		20.875		100.00474		172.22522		20.875		100.0112		173.64722		20.875		100.01659		174.06244		20.875		100.01066

		119.384		20.9		100.01025		100.01118		118.27		20.9		100.00091		118.008		20.9		100.00475		172.47122		20.9		100.01118		173.89455		20.9		100.01658		174.31311		20.9		100.01068

		119.582		20.925		100.0084		100.01115		118.479		20.925		100.00108		118.232		20.925		100.00525		172.71678		20.925		100.01115		174.14211		20.925		100.01657		174.56767		20.925		100.01069

		119.792		20.95		100.01127		100.01113		118.693		20.95		100.00091		118.415		20.95		100.00463		172.96078		20.95		100.01113		174.38989		20.95		100.01656		174.81911		20.95		100.01071

		120		20.975		100.00787		100.01112		118.899		20.975		100.00242		118.641		20.975		100.00459		173.206		20.975		100.01112		174.63978		20.975		100.01654		175.07589		20.975		100.01073

		120.199		21		100.01073		100.01111		119.106		21		100.002		118.841		21		100.00419		173.45656		21		100.01111		174.89011		21		100.01652		175.32633		21		100.01075

		120.405		21.025		100.00828		100.01111		119.308		21.025		100.00026		119.046		21.025		100.00251		173.70789		21.025		100.01111		175.14156		21.025		100.0165		175.57944		21.025		100.01076

		120.618		21.05		100.01199		100.01111		119.52		21.05		100.00235		119.262		21.05		100.00731		173.95689		21.05		100.01111		175.39167		21.05		100.01649		175.834		21.05		100.01077

		120.81		21.075		100.01343		100.01113		119.724		21.075		100.00531		119.464		21.075		100.00734		174.20611		21.075		100.01113		175.64078		21.075		100.01647		176.08589		21.075		100.01079

		121.027		21.1		100.01347		100.01114		119.935		21.1		100.00306		119.685		21.1		100.00728		174.45556		21.1		100.01114		175.89744		21.1		100.01645		176.33611		21.1		100.01079

		121.22		21.125		100.0097		100.01117		120.142		21.125		100.00062		119.882		21.125		100.00339		174.70789		21.125		100.01117		176.15211		21.125		100.01643		176.59278		21.125		100.0108

		121.428		21.15		100.00797		100.0112		120.349		21.15		99.99953		120.089		21.15		100.00674		174.95956		21.15		100.0112		176.40444		21.15		100.01642		176.84178		21.15		100.0108

		121.633		21.175		100.00888		100.01123		120.559		21.175		100.00135		120.301		21.175		100.00741		175.20678		21.175		100.01123		176.65344		21.175		100.01641		177.09589		21.175		100.01081

		121.856		21.2		100.01057		100.01127		120.755		21.2		100.00227		120.513		21.2		100.00613		175.45334		21.2		100.01127		176.90555		21.2		100.0164		177.34933		21.2		100.0108

		122.042		21.225		100.00857		100.0113		120.971		21.225		99.99963		120.721		21.225		100.00599		175.69822		21.225		100.0113		177.15655		21.225		100.0164		177.60722		21.225		100.0108

		122.251		21.25		100.00713		100.01134		121.184		21.25		100.00136		120.934		21.25		100.00566		175.94556		21.25		100.01134		177.41011		21.25		100.0164		177.86122		21.25		100.01079

		122.461		21.275		100.01276		100.01138		121.393		21.275		100.0055		121.141		21.275		100.00473		176.19845		21.275		100.01138		177.66267		21.275		100.0164		178.11533		21.275		100.01078

		122.681		21.3		100.01055		100.01141		121.603		21.3		100.00245		121.353		21.3		100.00769		176.44934		21.3		100.01141		177.91578		21.3		100.01641		178.37045		21.3		100.01077

		122.882		21.325		100.01101		100.01144		121.813		21.325		100.00302		121.565		21.325		100.00587		176.69934		21.325		100.01144		178.169		21.325		100.01642		178.62911		21.325		100.01075

		123.092		21.35		100.01057		100.01147		122.03		21.35		100.00203		121.772		21.35		100.00722		176.94767		21.35		100.01147		178.42178		21.35		100.01644		178.88644		21.35		100.01074

		123.307		21.375		100.01049		100.01149		122.246		21.375		100.00203		121.973		21.375		100.00529		177.19422		21.375		100.01149		178.67589		21.375		100.01645		179.146		21.375		100.01072

		123.5		21.4		100.01213		100.01151		122.45		21.4		100.0028		122.176		21.4		100.00529		177.449		21.4		100.01151		178.93311		21.4		100.01647		179.399		21.4		100.0107

		123.72		21.425		100.01149		100.01152		122.649		21.425		100.00262		122.399		21.425		100.00443		177.70245		21.425		100.01152		179.18678		21.425		100.01649		179.65622		21.425		100.01068

		123.92		21.45		100.0067		100.01153		122.861		21.45		100.00036		122.612		21.45		100.00533		177.957		21.45		100.01153		179.43734		21.45		100.01652		179.90678		21.45		100.01066

		124.136		21.475		100.0115		100.01154		123.064		21.475		100.00066		122.828		21.475		100.00676		178.21067		21.475		100.01154		179.688		21.475		100.01654		180.162		21.475		100.01065

		124.351		21.5		100.00992		100.01154		123.283		21.5		100.00006		123.046		21.5		100.00764		178.45867		21.5		100.01154		179.937		21.5		100.01656		180.41522		21.5		100.01063

		124.557		21.525		100.00687		100.01154		123.506		21.525		100.00197		123.257		21.525		100.00482		178.70789		21.525		100.01154		180.18922		21.525		100.01659		180.66655		21.525		100.01061

		124.759		21.55		100.00976		100.01153		123.71		21.55		100.00306		123.458		21.55		100.00589		178.95989		21.55		100.01153		180.43822		21.55		100.01661		180.91811		21.55		100.0106

		124.979		21.575		100.01167		100.01153		123.93		21.575		99.99906		123.673		21.575		100.00418		179.21178		21.575		100.01153		180.69056		21.575		100.01663		181.16611		21.575		100.01058

		125.187		21.6		100.0049		100.01153		124.143		21.6		100.00283		123.886		21.6		100.006		179.464		21.6		100.01153		180.94156		21.6		100.01665		181.413		21.6		100.01057

		125.403		21.625		100.00939		100.01152		124.354		21.625		99.99993		124.104		21.625		100.00432		179.71545		21.625		100.01152		181.18944		21.625		100.01666		181.66711		21.625		100.01056

		125.611		21.65		100.01116		100.01152		124.562		21.65		100.00312		124.313		21.65		100.00221		179.96644		21.65		100.01152		181.43545		21.65		100.01668		181.91533		21.65		100.01055

		125.822		21.675		100.00721		100.01151		124.78		21.675		100.00012		124.527		21.675		100.00603		180.21567		21.675		100.01151		181.68756		21.675		100.01669		182.171		21.675		100.01055

		126.04		21.7		100.00833		100.01151		124.99		21.7		100.0008		124.739		21.7		100.00402		180.46378		21.7		100.01151		181.93689		21.7		100.0167		182.423		21.7		100.01055

		126.244		21.725		100.01048		100.0115		125.206		21.725		100.00275		124.948		21.725		100.00541		180.71455		21.725		100.0115		182.19333		21.725		100.01671		182.67389		21.725		100.01055

		126.456		21.75		100.01055		100.0115		125.415		21.75		99.9984		125.164		21.75		100.00637		180.96389		21.75		100.0115		182.44756		21.75		100.01672		182.927		21.75		100.01055

		126.672		21.775		100.01002		100.0115		125.638		21.775		100.00424		125.373		21.775		100.00486		181.21055		21.775		100.0115		182.70156		21.775		100.01672		183.17989		21.775		100.01056

		126.878		21.8		100.00844		100.01149		125.842		21.8		100.00323		125.589		21.8		100.0068		181.45444		21.8		100.01149		182.94967		21.8		100.01672		183.43511		21.8		100.01057

		127.097		21.825		100.00942		100.01149		126.052		21.825		100.00438		125.805		21.825		100.00696		181.70378		21.825		100.01149		183.20033		21.825		100.01672		183.69156		21.825		100.01058

		127.312		21.85		100.00743		100.01149		126.263		21.85		100.00311		126.026		21.85		100.00566		181.94944		21.85		100.01149		183.44978		21.85		100.01671		183.946		21.85		100.01059

		127.526		21.875		100.00926		100.01148		126.482		21.875		99.99939		126.235		21.875		100.00778		182.19711		21.875		100.01148		183.70222		21.875		100.01671		184.20322		21.875		100.0106

		127.736		21.9		100.01097		100.01148		126.69		21.9		99.99999		126.451		21.9		100.00633		182.44711		21.9		100.01148		183.952		21.9		100.0167		184.45833		21.9		100.01061

		127.946		21.925		100.00735		100.01148		126.912		21.925		100.00005		126.656		21.925		100.00783		182.69478		21.925		100.01148		184.20167		21.925		100.0167		184.71255		21.925		100.01062

		128.155		21.95		100.00928		100.01148		127.125		21.95		100.00304		126.881		21.95		100.00602		182.93989		21.95		100.01148		184.44611		21.95		100.01669		184.96822		21.95		100.01063

		128.379		21.975		100.00638		100.01148		127.341		21.975		100.00076		127.092		21.975		100.00485		183.18778		21.975		100.01148		184.693		21.975		100.01668		185.22533		21.975		100.01064

		128.59599		22		100.00883		100.01148		127.561		22		100.00202		127.318		22		100.00615		183.43844		22		100.01148		184.93855		22		100.01667		185.47855		22		100.01065

		128.811		22.025		100.01136		100.01148		127.773		22.025		100.00469		127.529		22.025		100.00564		183.69367		22.025		100.01148		185.18822		22.025		100.01666		185.73244		22.025		100.01066

		129.028		22.05		100.01334		100.01148		127.991		22.05		100.00443		127.746		22.05		100.00745		183.94511		22.05		100.01148		185.435		22.05		100.01666		185.987		22.05		100.01066

		129.242		22.075		100.01049		100.01148		128.21899		22.075		100.00372		127.961		22.075		100.00288		184.19655		22.075		100.01148		185.67911		22.075		100.01665		186.24111		22.075		100.01067

		129.457		22.1		100.0096		100.01148		128.43201		22.1		100.00146		128.166		22.1		100.00729		184.44578		22.1		100.01148		185.92878		22.1		100.01665		186.48911		22.1		100.01067

		129.67		22.125		100.00861		100.01148		128.658		22.125		100.0026		128.392		22.125		100.00356		184.69311		22.125		100.01148		186.17678		22.125		100.01664		186.73989		22.125		100.01068

		129.89301		22.15		100.00967		100.01149		128.868		22.15		100.00315		128.605		22.15		100.00733		184.94266		22.15		100.01149		186.42667		22.15		100.01664		186.98989		22.15		100.01068

		130.097		22.175		100.01115		100.01149		129.08099		22.175		100.00437		128.826		22.175		100.00749		185.19411		22.175		100.01149		186.67967		22.175		100.01664		187.24455		22.175		100.01068

		130.306		22.2		100.00821		100.01149		129.287		22.2		100.00214		129.039		22.2		100.00602		185.44455		22.2		100.01149		186.93133		22.2		100.01664		187.49766		22.2		100.01068

		130.534		22.225		100.00924		100.0115		129.508		22.225		100.00399		129.26601		22.225		100.00633		185.68889		22.225		100.0115		187.18355		22.225		100.01664		187.75455		22.225		100.01068

		130.754		22.25		100.01046		100.0115		129.724		22.25		100.00293		129.48		22.25		100.00467		185.93922		22.25		100.0115		187.43578		22.25		100.01664		188.00844		22.25		100.01068

		130.979		22.275		100.01048		100.01151		129.94901		22.275		100.00209		129.689		22.275		100.00765		186.18789		22.275		100.01151		187.68622		22.275		100.01665		188.26267		22.275		100.01068

		131.18401		22.3		100.01139		100.01151		130.161		22.3		100.00419		129.909		22.3		100.00387		186.43655		22.3		100.01151		187.94289		22.3		100.01666		188.51467		22.3		100.01068

		131.397		22.325		100.0085		100.01151		130.38		22.325		100.00342		130.127		22.325		100.0058		186.68366		22.325		100.01151		188.19333		22.325		100.01666		188.77089		22.325		100.01069

		131.62801		22.35		100.01035		100.01152		130.601		22.35		100.00193		130.34801		22.35		100.00677		186.93178		22.35		100.01152		188.44711		22.35		100.01667		189.02355		22.35		100.01069

		131.834		22.375		100.01034		100.01152		130.814		22.375		100.00231		130.569		22.375		100.00392		187.18078		22.375		100.01152		188.69944		22.375		100.01668		189.28033		22.375		100.01069

		132.04601		22.4		100.00795		100.01152		131.033		22.4		99.99996		130.776		22.4		100.00359		187.43089		22.4		100.01152		188.94955		22.4		100.0167		189.52944		22.4		100.0107

		132.26801		22.425		100.0089		100.01152		131.257		22.425		100.00125		130.998		22.425		100.00842		187.67933		22.425		100.01152		189.19622		22.425		100.01671		189.77867		22.425		100.0107

		132.489		22.45		100.01059		100.01153		131.46201		22.45		100.00149		131.203		22.45		100.00565		187.93544		22.45		100.01153		189.444		22.45		100.01673		190.02333		22.45		100.0107

		132.70399		22.475		100.00725		100.01153		131.686		22.475		100.00287		131.44501		22.475		100.00467		188.18333		22.475		100.01153		189.69056		22.475		100.01674		190.27289		22.475		100.01071

		132.93201		22.5		100.01001		100.01153		131.899		22.5		100.00414		131.66499		22.5		100.00449		188.43478		22.5		100.01153		189.94211		22.5		100.01676		190.52022		22.5		100.01072

		133.14		22.525		100.01		100.01154		132.13499		22.525		100.00162		131.867		22.525		100.0035		188.68611		22.525		100.01154		190.19311		22.525		100.01678		190.77011		22.525		100.01072

		133.368		22.55		100.00836		100.01154		132.343		22.55		99.99887		132.08		22.55		99.99674		188.94289		22.55		100.01154		190.44578		22.55		100.0168		191.02278		22.55		100.01073

		133.571		22.575		100.00576		100.01155		132.56599		22.575		100.00132		132.308		22.575		99.99947		189.19522		22.575		100.01155		190.69422		22.575		100.01682		191.272		22.575		100.01074

		133.795		22.6		100.00879		100.01156		132.78799		22.6		99.99849		132.53101		22.6		100.00202		189.445		22.6		100.01156		190.94889		22.6		100.01685		191.51967		22.6		100.01075

		134.01401		22.625		100.01191		100.01157		133.013		22.625		100.00023		132.73199		22.625		100.00757		189.69433		22.625		100.01157		191.201		22.625		100.01687		191.77245		22.625		100.01076

		134.241		22.65		100.00941		100.01158		133.23199		22.65		100.0042		132.97701		22.65		100.00444		189.94889		22.65		100.01158		191.45789		22.65		100.0169		192.02333		22.65		100.01077

		134.451		22.675		100.00634		100.01159		133.44099		22.675		100.00155		133.18201		22.675		100.00798		190.20089		22.675		100.01159		191.713		22.675		100.01692		192.27911		22.675		100.01078

		134.67799		22.7		100.01025		100.01161		133.67599		22.7		100.0052		133.408		22.7		100.00504		190.45522		22.7		100.01161		191.96967		22.7		100.01694		192.53245		22.7		100.01078

		134.897		22.725		100.01102		100.01162		133.88901		22.725		100.00273		133.631		22.725		100.00221		190.70311		22.725		100.01162		192.22489		22.725		100.01697		192.78644		22.725		100.01079

		135.129		22.75		100.01052		100.01164		134.106		22.75		100.00213		133.84		22.75		100.00558		190.95733		22.75		100.01164		192.47789		22.75		100.01699		193.03745		22.75		100.0108

		135.34		22.775		100.00824		100.01166		134.33		22.775		100.00116		134.069		22.775		100.00312		191.20722		22.775		100.01166		192.72744		22.775		100.01701		193.28756		22.775		100.01081

		135.576		22.8		100.01194		100.01167		134.54201		22.8		100.00072		134.29401		22.8		100.00578		191.46144		22.8		100.01167		192.98111		22.8		100.01703		193.54122		22.8		100.01081

		135.797		22.825		100.01152		100.01169		134.77299		22.825		100.00222		134.502		22.825		100.00717		191.71689		22.825		100.01169		193.228		22.825		100.01705		193.79411		22.825		100.01082

		136.01401		22.85		100.00979		100.0117		134.99001		22.85		100.00148		134.726		22.85		100.00519		191.97256		22.85		100.0117		193.48033		22.85		100.01707		194.04467		22.85		100.01082

		136.231		22.875		100.0089		100.01172		135.20799		22.875		100.00372		134.94901		22.875		100.00808		192.22678		22.875		100.01172		193.72867		22.875		100.01708		194.30023		22.875		100.01082

		136.44901		22.9		100.0044		100.01173		135.438		22.9		100.00105		135.164		22.9		100.00617		192.47845		22.9		100.01173		193.97511		22.9		100.01709		194.55345		22.9		100.01082

		136.683		22.925		100.00928		100.01174		135.658		22.925		100.00207		135.39301		22.925		100.00593		192.729		22.925		100.01174		194.22033		22.925		100.0171		194.80889		22.925		100.01083

		136.899		22.95		100.01025		100.01175		135.888		22.95		100.00631		135.616		22.95		100.00561		192.98367		22.95		100.01175		194.46711		22.95		100.01711		195.06234		22.95		100.01083

		137.121		22.975		100.00869		100.01176		136.097		22.975		100.00306		135.84399		22.975		100.00432		193.23145		22.975		100.01176		194.71522		22.975		100.01711		195.31978		22.975		100.01083

		137.351		23		100.01089		100.01176		136.32899		23		100.00487		136.07001		23		100.00683		193.48367		23		100.01176		194.96955		23		100.01712		195.57522		23		100.01083

		137.571		23.025		100.01122		100.01176		136.552		23.025		100.00049		136.284		23.025		100.00436		193.73455		23.025		100.01176		195.22222		23.025		100.01712		195.83155		23.025		100.01083

		137.79201		23.05		100.01124		100.01177		136.76601		23.05		100.00465		136.508		23.05		100.00735		193.98167		23.05		100.01177		195.47544		23.05		100.01712		196.09011		23.05		100.01082

		138.01401		23.075		100.00878		100.01177		137.00101		23.075		100.00152		136.72301		23.075		100.00493		194.23067		23.075		100.01177		195.72266		23.075		100.01712		196.34955		23.075		100.01082

		138.23		23.1		100.0152		100.01177		137.224		23.1		100.00463		136.952		23.1		100.00633		194.48011		23.1		100.01177		195.97422		23.1		100.01712		196.60344		23.1		100.01082

		138.459		23.125		100.01245		100.01177		137.45		23.125		100.00247		137.186		23.125		100.00668		194.73267		23.125		100.01177		196.22878		23.125		100.01712		196.85833		23.125		100.01082

		138.685		23.15		100.01101		100.01177		137.658		23.15		100.00395		137.408		23.15		100.00545		194.98722		23.15		100.01177		196.48255		23.15		100.01711		197.10989		23.15		100.01081

		138.905		23.175		100.0104		100.01176		137.892		23.175		99.99896		137.62		23.175		100.00546		195.24067		23.175		100.01176		196.733		23.175		100.01711		197.36589		23.175		100.01081

		139.12199		23.2		100.00877		100.01176		138.11301		23.2		100.00332		137.84801		23.2		100.00281		195.49578		23.2		100.01176		196.98444		23.2		100.01711		197.619		23.2		100.01081

		139.366		23.225		100.01065		100.01176		138.336		23.225		100.00202		138.08099		23.225		100.00631		195.74311		23.225		100.01176		197.23467		23.225		100.01712		197.87066		23.225		100.01081

		139.58299		23.25		100.00683		100.01176		138.567		23.25		100.00271		138.291		23.25		100.0062		195.99667		23.25		100.01176		197.48422		23.25		100.01712		198.12011		23.25		100.01081

		139.80499		23.275		100.00675		100.01176		138.783		23.275		100.00154		138.52499		23.275		100.00876		196.25033		23.275		100.01176		197.73589		23.275		100.01713		198.368		23.275		100.01081

		140.033		23.3		100.00802		100.01176		139.017		23.3		100		138.73801		23.3		100.00904		196.50222		23.3		100.01176		197.99234		23.3		100.01714		198.61911		23.3		100.01081

		140.24899		23.325		100.01258		100.01177		139.229		23.325		99.9983		138.97701		23.325		100.00451		196.75356		23.325		100.01177		198.24556		23.325		100.01715		198.87322		23.325		100.01082

		140.47501		23.35		100.00842		100.01177		139.465		23.35		100.00151		139.194		23.35		100.00857		197.00567		23.35		100.01177		198.50045		23.35		100.01716		199.12511		23.35		100.01082

		140.703		23.375		100.01057		100.01178		139.69099		23.375		100.00372		139.42599		23.375		100.00899		197.25722		23.375		100.01178		198.756		23.375		100.01718		199.38022		23.375		100.01083

		140.93201		23.4		100.0107		100.01179		139.90601		23.4		100.00096		139.63901		23.4		100.0077		197.50855		23.4		100.01179		199.01167		23.4		100.0172		199.63111		23.4		100.01083

		141.15401		23.425		100.00877		100.0118		140.133		23.425		100.00062		139.879		23.425		100.00438		197.75677		23.425		100.0118		199.26456		23.425		100.01722		199.88645		23.425		100.01084

		141.38901		23.45		100.01019		100.01181		140.36301		23.45		99.99624		140.09599		23.45		100.00489		198.00878		23.45		100.01181		199.51545		23.45		100.01725		200.13956		23.45		100.01085

		141.608		23.475		100.01084		100.01182		140.578		23.475		100.00506		140.315		23.475		100.00806		198.25466		23.475		100.01182		199.76578		23.475		100.01728		200.39478		23.475		100.01087

		141.827		23.5		100.0116		100.01183		140.813		23.5		100.00283		140.535		23.5		99.99899		198.50744		23.5		100.01183		200.016		23.5		100.01731		200.65022		23.5		100.01088

		142.067		23.525		100.01321		100.01184		141.039		23.525		100.00644		140.77299		23.525		100.00883		198.76178		23.525		100.01184		200.26422		23.525		100.01734		200.89933		23.525		100.01089

		142.289		23.55		100.0077		100.01185		141.27699		23.55		100.00208		140.993		23.55		100.00266		199.01055		23.55		100.01185		200.50967		23.55		100.01737		201.14944		23.55		100.0109

		142.502		23.575		100.00899		100.01186		141.495		23.575		100.00369		141.23		23.575		100.0045		199.25766		23.575		100.01186		200.75278		23.575		100.0174		201.39989		23.575		100.01092

		142.729		23.6		100.01183		100.01187		141.71899		23.6		100.00073		141.44901		23.6		100.00441		199.50533		23.6		100.01187		200.99845		23.6		100.01744		201.64711		23.6		100.01093

		142.967		23.625		100.01304		100.01188		141.939		23.625		100.00517		141.683		23.625		100.00426		199.75322		23.625		100.01188		201.24434		23.625		100.01747		201.89489		23.625		100.01095

		143.19099		23.65		100.01208		100.01189		142.18201		23.65		100.00398		141.916		23.65		100.00463		200.003		23.65		100.01189		201.49389		23.65		100.01751		202.14022		23.65		100.01096

		143.423		23.675		100.00672		100.01189		142.40401		23.675		100.0006		142.13699		23.675		100.00317		200.25456		23.675		100.01189		201.74211		23.675		100.01754		202.38711		23.675		100.01098

		143.64799		23.7		100.01022		100.0119		142.633		23.7		100.0018		142.351		23.7		100.00494		200.50678		23.7		100.0119		201.98967		23.7		100.01758		202.63478		23.7		100.01099

		143.881		23.725		100.00841		100.0119		142.85899		23.725		99.99884		142.577		23.725		100.00499		200.75155		23.725		100.0119		202.23756		23.725		100.01761		202.88078		23.725		100.011

		144.092		23.75		100.00922		100.01191		143.089		23.75		100.00163		142.80701		23.75		100.00572		200.99678		23.75		100.01191		202.48478		23.75		100.01764		203.12567		23.75		100.01102

		144.327		23.775		100.00643		100.01191		143.311		23.775		100.00251		143.041		23.775		100.00521		201.245		23.775		100.01191		202.73278		23.775		100.01768		203.36845		23.775		100.01103

		144.56		23.8		100.00871		100.01192		143.537		23.8		100.00066		143.274		23.8		100.006		201.49333		23.8		100.01192		202.98011		23.8		100.01771		203.617		23.8		100.01104

		144.79201		23.825		100.01001		100.01192		143.77299		23.825		100.00493		143.496		23.825		100.00698		201.73867		23.825		100.01192		203.22711		23.825		100.01774		203.86556		23.825		100.01105

		145.00999		23.85		100.00645		100.01193		144.009		23.85		100.00178		143.72099		23.85		100.00624		201.98089		23.85		100.01193		203.47367		23.85		100.01777		204.11522		23.85		100.01106

		145.233		23.875		100.00747		100.01193		144.224		23.875		100.00291		143.95		23.875		100.00672		202.22656		23.875		100.01193		203.72022		23.875		100.01779		204.365		23.875		100.01107

		145.47301		23.9		100.01004		100.01193		144.446		23.9		100.00048		144.194		23.9		100.00501		202.47056		23.9		100.01193		203.96678		23.9		100.01782		204.61756		23.9		100.01108

		145.705		23.925		100.00867		100.01194		144.69299		23.925		100.00195		144.41499		23.925		100.00537		202.71378		23.925		100.01194		204.21544		23.925		100.01784		204.87056		23.925		100.01109

		145.927		23.95		100.00621		100.01194		144.91499		23.95		100.00027		144.646		23.95		100.00397		202.96111		23.95		100.01194		204.46122		23.95		100.01787		205.12356		23.95		100.0111

		146.157		23.975		100.00743		100.01194		145.14301		23.975		100.00312		144.871		23.975		100.00528		203.20678		23.975		100.01194		204.70933		23.975		100.01789		205.37755		23.975		100.0111

		146.384		24		100.01043		100.01194		145.368		24		100.0017		145.105		24		100.0049		203.44978		24		100.01194		204.95833		24		100.01791		205.63178		24		100.01111

		146.619		24.025		100.01064		100.01194		145.59399		24.025		99.99908		145.33299		24.025		100.00472		203.69656		24.025		100.01194		205.20744		24.025		100.01793		205.88011		24.025		100.01111

		146.83099		24.05		100.01386		100.01194		145.83501		24.05		100.00327		145.558		24.05		100.00736		203.94167		24.05		100.01194		205.45377		24.05		100.01794		206.13011		24.05		100.01112

		147.071		24.075		100.01297		100.01194		146.062		24.075		100.00076		145.784		24.075		100.0054		204.189		24.075		100.01194		205.69922		24.075		100.01796		206.37778		24.075		100.01112

		147.31		24.1		100.01135		100.01193		146.283		24.1		100.00307		146.01199		24.1		100.00307		204.43511		24.1		100.01193		205.94377		24.1		100.01797		206.62622		24.1		100.01113

		147.524		24.125		100.00862		100.01193		146.519		24.125		99.99985		146.231		24.125		100.00506		204.681		24.125		100.01193		206.18788		24.125		100.01798		206.87022		24.125		100.01113

		147.765		24.15		100.00549		100.01192		146.737		24.15		100.00116		146.474		24.15		100.005		204.93167		24.15		100.01192		206.43266		24.15		100.01799		207.11733		24.15		100.01113

		147.991		24.175		100.00869		100.01192		146.963		24.175		100.0038		146.67999		24.175		100.004		205.18056		24.175		100.01192		206.67889		24.175		100.01799		207.36278		24.175		100.01114

		148.22099		24.2		100.0069		100.01191		147.189		24.2		100.00053		146.92101		24.2		100.00547		205.431		24.2		100.01191		206.924		24.2		100.018		207.61122		24.2		100.01114

		148.44701		24.225		100.00798		100.01191		147.438		24.225		99.99952		147.151		24.225		100.00669		205.68044		24.225		100.01191		207.17177		24.225		100.018		207.86178		24.225		100.01114

		148.66499		24.25		100.00877		100.0119		147.66499		24.25		100.00305		147.375		24.25		100.00613		205.926		24.25		100.0119		207.42078		24.25		100.018		208.11244		24.25		100.01115

		148.905		24.275		100.00928		100.0119		147.88699		24.275		100.00107		147.614		24.275		100.00576		206.17255		24.275		100.0119		207.67022		24.275		100.01801		208.36211		24.275		100.01116

		149.13901		24.3		100.00728		100.01189		148.123		24.3		99.99906		147.842		24.3		100.00488		206.41933		24.3		100.01189		207.92133		24.3		100.01801		208.61578		24.3		100.01116

		149.362		24.325		100.00768		100.01189		148.35201		24.325		100.00073		148.07001		24.325		100.00323		206.66544		24.325		100.01189		208.17222		24.325		100.01801		208.86822		24.325		100.01117

		149.58701		24.35		100.01215		100.01189		148.58		24.35		100.00165		148.308		24.35		100.00748		206.91078		24.35		100.01189		208.42445		24.35		100.01802		209.12255		24.35		100.01118

		149.832		24.375		100.00905		100.01189		148.808		24.375		100.00441		148.53101		24.375		100.00805		207.15433		24.375		100.01189		208.67611		24.375		100.01802		209.37189		24.375		100.01119

		150.062		24.4		100.00983		100.01188		149.034		24.4		100.00266		148.774		24.4		100.00762		207.39744		24.4		100.01188		208.92811		24.4		100.01803		209.62256		24.4		100.0112

		150.285		24.425		100.01005		100.01188		149.276		24.425		100.00037		148.99899		24.425		100.00337		207.63778		24.425		100.01188		209.17767		24.425		100.01805		209.87478		24.425		100.01122

		150.511		24.45		100.00558		100.01188		149.505		24.45		100.00345		149.226		24.45		100.00581		207.88422		24.45		100.01188		209.42445		24.45		100.01806		210.12456		24.45		100.01123

		150.74899		24.475		100.00793		100.01188		149.735		24.475		100.00409		149.461		24.475		100.00125		208.128		24.475		100.01188		209.67389		24.475		100.01809		210.37511		24.475		100.01124

		150.983		24.5		100.00693		100.01188		149.97099		24.5		99.99794		149.67999		24.5		100.00873		208.374		24.5		100.01188		209.92211		24.5		100.01811		210.62345		24.5		100.01126

		151.214		24.525		100.0051		100.01188		150.19299		24.525		99.99535		149.914		24.525		100.00149		208.62189		24.525		100.01188		210.17078		24.525		100.01814		210.87378		24.525		100.01127

		151.436		24.55		100.0076		100.01187		150.429		24.55		100.00084		150.151		24.55		100.006		208.86633		24.55		100.01187		210.41933		24.55		100.01818		211.12289		24.55		100.01128

		151.677		24.575		100.00934		100.01187		150.67101		24.575		100.0049		150.379		24.575		100.00324		209.11156		24.575		100.01187		210.66389		24.575		100.01821		211.37189		24.575		100.01129

		151.911		24.6		100.01002		100.01186		150.89101		24.6		100.00347		150.60699		24.6		100.00921		209.35711		24.6		100.01186		210.91133		24.6		100.01825		211.62156		24.6		100.01131

		152.14301		24.625		100.01001		100.01186		151.13		24.625		99.99895		150.834		24.625		100.00041		209.60333		24.625		100.01186		211.15555		24.625		100.0183		211.87211		24.625		100.01132

		152.368		24.65		100.01036		100.01185		151.37		24.65		100.00159		151.07401		24.65		100.00218		209.85322		24.65		100.01185		211.40078		24.65		100.01834		212.12311		24.65		100.01132

		152.599		24.675		100.0123		100.01184		151.597		24.675		100.00572		151.32001		24.675		100.00449		210.10189		24.675		100.01184		211.64811		24.675		100.01839		212.37534		24.675		100.01133

		152.843		24.7		100.01029		100.01183		151.83299		24.7		100.00355		151.548		24.7		100.00982		210.35378		24.7		100.01183		211.893		24.7		100.01844		212.62678		24.7		100.01134

		153.073		24.725		100.00946		100.01182		152.064		24.725		100.00249		151.77		24.725		100.0091		210.60122		24.725		100.01182		212.14067		24.725		100.01848		212.88034		24.725		100.01135

		153.299		24.75		100.01031		100.01181		152.293		24.75		100.00441		151.995		24.75		100.00631		210.85422		24.75		100.01181		212.38789		24.75		100.01853		213.13056		24.75		100.01135

		153.537		24.775		100.01319		100.0118		152.528		24.775		100.00504		152.241		24.775		100.00817		211.10789		24.775		100.0118		212.63533		24.775		100.01858		213.38167		24.775		100.01136

		153.756		24.8		100.01035		100.01179		152.756		24.8		100.00468		152.47099		24.8		100.00583		211.36334		24.8		100.01179		212.88155		24.8		100.01862		213.63411		24.8		100.01136

		153.98399		24.825		100.00525		100.01178		152.98199		24.825		100.00113		152.698		24.825		100.0046		211.61667		24.825		100.01178		213.12633		24.825		100.01866		213.88678		24.825		100.01137

		154.22099		24.85		100.01026		100.01178		153.224		24.85		100.00771		152.92999		24.85		100.00562		211.871		24.85		100.01178		213.374		24.85		100.01871		214.141		24.85		100.01137

		154.44901		24.875		100.01161		100.01177		153.461		24.875		100.0013		153.157		24.875		100.0066		212.12467		24.875		100.01177		213.62322		24.875		100.01875		214.38956		24.875		100.01137

		154.69099		24.9		100.01137		100.01177		153.689		24.9		100.00169		153.397		24.9		100.00525		212.375		24.9		100.01177		213.87256		24.9		100.01878		214.63889		24.9		100.01138

		154.92101		24.925		100.00942		100.01176		153.914		24.925		99.99789		153.619		24.925		100.00332		212.62311		24.925		100.01176		214.12067		24.925		100.01882		214.89045		24.925		100.01138

		155.158		24.95		100.00874		100.01176		154.151		24.95		99.99733		153.85699		24.95		100.00552		212.87356		24.95		100.01176		214.36322		24.95		100.01886		215.14089		24.95		100.01139

		155.396		24.975		100.01144		100.01176		154.394		24.975		100.0037		154.105		24.975		100.00186		213.11856		24.975		100.01176		214.60745		24.975		100.01889		215.39256		24.975		100.01139

		155.62199		25		100.00774		100.01177		154.62		25		100.00328		154.332		25		100.00461		213.36411		25		100.01177		214.85378		25		100.01892		215.644		25		100.0114

		155.86		25.025		100.00857		100.01177		154.85699		25.025		100.00135		154.562		25.025		100.00418		213.61389		25.025		100.01177		215.10734		25.025		100.01895		215.89711		25.025		100.0114

		156.077		25.05		100.01051		100.01178		155.086		25.05		100.00321		154.79401		25.05		100.00541		213.86333		25.05		100.01178		215.35611		25.05		100.01897		216.14833		25.05		100.01141

		156.30701		25.075		100.01025		100.01178		155.32401		25.075		100.00436		155.02901		25.075		100.00508		214.11278		25.075		100.01178		215.60389		25.075		100.019		216.39744		25.075		100.01142

		156.549		25.1		100.00784		100.01179		155.55099		25.1		100.00201		155.26199		25.1		100.00479		214.35444		25.1		100.01179		215.853		25.1		100.01902		216.64989		25.1		100.01142

		156.786		25.125		100.00532		100.0118		155.787		25.125		100.0026		155.493		25.125		100.00471		214.60045		25.125		100.0118		216.10111		25.125		100.01904		216.90422		25.125		100.01143

		157.013		25.15		100.00913		100.01181		156.02901		25.15		100.00222		155.726		25.15		100.00574		214.84978		25.15		100.01181		216.34711		25.15		100.01906		217.15744		25.15		100.01143

		157.239		25.175		100.00559		100.01182		156.25		25.175		100.003		155.97099		25.175		100.00593		215.10322		25.175		100.01182		216.59867		25.175		100.01908		217.41244		25.175		100.01144

		157.48		25.2		100.00955		100.01183		156.498		25.2		100.00208		156.19501		25.2		100.00492		215.35867		25.2		100.01183		216.84978		25.2		100.01909		217.66378		25.2		100.01144

		157.716		25.225		100.00718		100.01185		156.722		25.225		100.00296		156.42101		25.225		100.00624		215.61367		25.225		100.01185		217.09933		25.225		100.01911		217.91489		25.225		100.01145

		157.95		25.25		100.00782		100.01186		156.957		25.25		100.00163		156.653		25.25		100.00687		215.86511		25.25		100.01186		217.34433		25.25		100.01912		218.16155		25.25		100.01146

		158.17799		25.275		100.00761		100.01187		157.187		25.275		100.00192		156.89301		25.275		100.00467		216.118		25.275		100.01187		217.59155		25.275		100.01913		218.41278		25.275		100.01146

		158.42101		25.3		100.00954		100.01188		157.425		25.3		100.00154		157.125		25.3		100.00448		216.36889		25.3		100.01188		217.83944		25.3		100.01914		218.66278		25.3		100.01147

		158.661		25.325		100.00867		100.01189		157.659		25.325		100.00359		157.355		25.325		100.00377		216.62333		25.325		100.01189		218.08444		25.325		100.01915		218.914		25.325		100.01148

		158.886		25.35		100.00886		100.01191		157.899		25.35		100.00389		157.592		25.35		100.00526		216.87455		25.35		100.01191		218.32689		25.35		100.01916		219.16489		25.35		100.01149

		159.127		25.375		100.01258		100.01192		158.133		25.375		100.00202		157.825		25.375		100.00433		217.12666		25.375		100.01192		218.57489		25.375		100.01917		219.41322		25.375		100.0115

		159.345		25.4		100.01059		100.01193		158.35899		25.4		99.99972		158.058		25.4		100.00535		217.37333		25.4		100.01193		218.82011		25.4		100.01918		219.66555		25.4		100.01151

		159.589		25.425		100.00932		100.01194		158.601		25.425		100.00097		158.289		25.425		100.00392		217.61711		25.425		100.01194		219.068		25.425		100.01919		219.91844		25.425		100.01152

		159.823		25.45		100.00934		100.01195		158.83		25.45		100.00227		158.526		25.45		100.00377		217.86178		25.45		100.01195		219.31566		25.45		100.0192		220.17211		25.45		100.01154

		160.064		25.475		100.00875		100.01196		159.07001		25.475		99.99847		158.75101		25.475		100.00372		218.10578		25.475		100.01196		219.56644		25.475		100.01921		220.42722		25.475		100.01156

		160.3		25.5		100.01063		100.01197		159.31599		25.5		100.00457		158.992		25.5		100.00621		218.34855		25.5		100.01197		219.81544		25.5		100.01922		220.683		25.5		100.01157

		160.535		25.525		100.0085		100.01198		159.55099		25.525		100.001		159.235		25.525		100.00609		218.59356		25.525		100.01198		220.06422		25.525		100.01923		220.94022		25.525		100.01159

		160.763		25.55		100.00755		100.01199		159.77901		25.55		100.00239		159.45399		25.55		100.00567		218.84333		25.55		100.01199		220.31566		25.55		100.01925		221.19511		25.55		100.01161

		160.99899		25.575		100.00966		100.01199		160.008		25.575		100.00136		159.70599		25.575		100.00498		219.09378		25.575		100.01199		220.56955		25.575		100.01926		221.44855		25.575		100.01163

		161.23801		25.6		100.01047		100.012		160.243		25.6		100.00107		159.93201		25.6		100.00445		219.34356		25.6		100.012		220.82189		25.6		100.01928		221.70211		25.6		100.01165

		161.472		25.625		100.00291		100.012		160.479		25.625		100.00332		160.16701		25.625		100.00449		219.59778		25.625		100.012		221.07589		25.625		100.01929		221.952		25.625		100.01167

		161.709		25.65		100.00618		100.01201		160.69901		25.65		99.9999		160.39101		25.65		100.00543		219.85311		25.65		100.01201		221.32333		25.65		100.01931		222.20333		25.65		100.01169

		161.944		25.675		100.0076		100.01201		160.957		25.675		99.9998		160.64301		25.675		100.00551		220.10589		25.675		100.01201		221.56933		25.675		100.01932		222.45278		25.675		100.01171

		162.17799		25.7		100.00819		100.01202		161.185		25.7		100.00399		160.879		25.7		100.00435		220.35811		25.7		100.01202		221.815		25.7		100.01934		222.70278		25.7		100.01172

		162.40199		25.725		100.00894		100.01202		161.42999		25.725		100.00159		161.103		25.725		100.00403		220.61122		25.725		100.01202		222.06267		25.725		100.01935		222.95078		25.725		100.01174

		162.65401		25.75		100.01182		100.01203		161.668		25.75		100.00296		161.342		25.75		100.00558		220.86522		25.75		100.01203		222.31211		25.75		100.01937		223.20044		25.75		100.01175

		162.89101		25.775		100.00909		100.01203		161.899		25.775		100.00212		161.57899		25.775		100.00595		221.11511		25.775		100.01203		222.55922		25.775		100.01939		223.45278		25.775		100.01177

		163.121		25.8		100.00934		100.01204		162.133		25.8		99.99751		161.817		25.8		100.00353		221.36656		25.8		100.01204		222.80611		25.8		100.0194		223.70433		25.8		100.01178

		163.351		25.825		100.01026		100.01205		162.366		25.825		100.0008		162.05099		25.825		100.00543		221.61444		25.825		100.01205		223.05267		25.825		100.01942		223.95967		25.825		100.01179

		163.59		25.85		100.00731		100.01206		162.605		25.85		100.00027		162.28101		25.85		100.00492		221.86444		25.85		100.01206		223.30378		25.85		100.01944		224.21056		25.85		100.0118

		163.82001		25.875		100.01061		100.01208		162.838		25.875		100.00476		162.524		25.875		100.00556		222.11133		25.875		100.01208		223.555		25.875		100.01946		224.46278		25.875		100.01181

		164.063		25.9		100.0097		100.0121		163.07401		25.9		100.00042		162.748		25.9		100.00592		222.36011		25.9		100.0121		223.80644		25.9		100.01948		224.71556		25.9		100.01182

		164.299		25.925		100.01029		100.01212		163.312		25.925		100.00398		162.989		25.925		100.00193		222.61189		25.925		100.01212		224.05644		25.925		100.0195		224.96867		25.925		100.01183

		164.53		25.95		100.00524		100.01214		163.54401		25.95		100.00056		163.224		25.95		100.00698		222.85989		25.95		100.01214		224.30689		25.95		100.01953		225.22011		25.95		100.01183

		164.761		25.975		100.00947		100.01217		163.787		25.975		100.00229		163.466		25.975		100.0057		223.107		25.975		100.01217		224.55722		25.975		100.01956		225.46933		25.975		100.01184

		164.993		26		100.00508		100.0122		164.017		26		99.99924		163.702		26		100.00371		223.359		26		100.0122		224.80811		26		100.01959		225.71889		26		100.01185

		165.237		26.025		100.0052		100.01223		164.252		26.025		100		163.933		26.025		100.00579		223.61111		26.025		100.01223		225.05778		26.025		100.01962		225.96567		26.025		100.01186

		165.47		26.05		100.00685		100.01227		164.48399		26.05		100.00339		164.175		26.05		100.00307		223.86211		26.05		100.01227		225.304		26.05		100.01966		226.21122		26.05		100.01186

		165.69901		26.075		100.01108		100.0123		164.731		26.075		99.99792		164.405		26.075		100.00546		224.11111		26.075		100.0123		225.54689		26.075		100.0197		226.45889		26.075		100.01187

		165.94099		26.1		100.01137		100.01233		164.96001		26.1		100.0042		164.645		26.1		100.00526		224.36156		26.1		100.01233		225.79122		26.1		100.01974		226.706		26.1		100.01188

		166.17799		26.125		100.00989		100.01236		165.194		26.125		100.00203		164.882		26.125		100.00411		224.61467		26.125		100.01236		226.03567		26.125		100.01979		226.95222		26.125		100.01189

		166.405		26.15		100.00675		100.01239		165.44701		26.15		100.00219		165.108		26.15		100.00545		224.86444		26.15		100.01239		226.279		26.15		100.01984		227.20066		26.15		100.0119

		166.642		26.175		100.0052		100.01242		165.67799		26.175		100.00058		165.35201		26.175		100.00002		225.11567		26.175		100.01242		226.51745		26.175		100.01989		227.44867		26.175		100.0119

		166.884		26.2		100.00772		100.01244		165.91		26.2		99.99971		165.591		26.2		100.00496		225.36333		26.2		100.01244		226.75845		26.2		100.01994		227.69656		26.2		100.01191

		167.11501		26.225		100.00989		100.01246		166.14101		26.225		100.00497		165.82401		26.225		100.00597		225.61167		26.225		100.01246		226.99789		26.225		100.01999		227.94222		26.225		100.01192

		167.36		26.25		100.00778		100.01247		166.383		26.25		100.00326		166.062		26.25		100.00568		225.85645		26.25		100.01247		227.24134		26.25		100.02004		228.19278		26.25		100.01193

		167.58299		26.275		100.00604		100.01248		166.616		26.275		100.00209		166.289		26.275		100.00304		226.10367		26.275		100.01248		227.48889		26.275		100.02009		228.44267		26.275		100.01194

		167.82001		26.3		100.00565		100.01249		166.851		26.3		99.99946		166.536		26.3		100.00329		226.34833		26.3		100.01249		227.73389		26.3		100.02015		228.69345		26.3		100.01195

		168.064		26.325		100.00846		100.01249		167.09801		26.325		100.00182		166.759		26.325		100.007		226.59222		26.325		100.01249		227.97956		26.325		100.0202		228.942		26.325		100.01196

		168.285		26.35		100.00655		100.01249		167.34		26.35		100.00272		167.009		26.35		100.00715		226.83378		26.35		100.01249		228.22545		26.35		100.02026		229.19223		26.35		100.01196

		168.52699		26.375		100.00683		100.01249		167.576		26.375		100.00358		167.248		26.375		100.00397		227.07844		26.375		100.01249		228.47478		26.375		100.02031		229.44189		26.375		100.01197

		168.765		26.4		100.00891		100.01248		167.817		26.4		100.00296		167.48399		26.4		100.00239		227.31889		26.4		100.01248		228.72634		26.4		100.02036		229.69122		26.4		100.01198

		169.015		26.425		100.0074		100.01247		168.039		26.425		100.00118		167.722		26.425		100.00634		227.56244		26.425		100.01247		228.97445		26.425		100.02042		229.94267		26.425		100.01199

		169.256		26.45		100.00918		100.01245		168.28999		26.45		100.00195		167.944		26.45		100.00551		227.80267		26.45		100.01245		229.22456		26.45		100.02046		230.19222		26.45		100.01201

		169.495		26.475		100.00529		100.01243		168.52901		26.475		99.99864		168.18401		26.475		100.00483		228.04289		26.475		100.01243		229.47167		26.475		100.02051		230.43956		26.475		100.01202

		169.731		26.5		100.01271		100.01241		168.776		26.5		100.00012		168.42799		26.5		100.00267		228.285		26.5		100.01241		229.719		26.5		100.02055		230.68367		26.5		100.01203

		169.968		26.525		100.00715		100.01239		168.991		26.525		100.00093		168.658		26.525		100.00426		228.52822		26.525		100.01239		229.967		26.525		100.02059		230.929		26.525		100.01204

		170.20799		26.55		100.00389		100.01237		169.233		26.55		99.99852		168.90401		26.55		100.00625		228.77311		26.55		100.01237		230.21278		26.55		100.02062		231.17689		26.55		100.01205

		170.44		26.575		100.00389		100.01234		169.467		26.575		99.99952		169.14799		26.575		100.00119		229.02011		26.575		100.01234		230.45967		26.575		100.02064		231.424		26.575		100.01207

		170.689		26.6		100.00473		100.01232		169.72		26.6		100.00165		169.381		26.6		100.00742		229.26734		26.6		100.01232		230.702		26.6		100.02066		231.67367		26.6		100.01208

		170.92599		26.625		100.00672		100.0123		169.952		26.625		99.99869		169.60699		26.625		100.004		229.51722		26.625		100.0123		230.94789		26.625		100.02067		231.92122		26.625		100.01209

		171.158		26.65		100.0062		100.01228		170.19099		26.65		99.99804		169.843		26.65		100.00376		229.76734		26.65		100.01228		231.19433		26.65		100.02068		232.16655		26.65		100.0121

		171.397		26.675		100.00932		100.01226		170.42101		26.675		100.00054		170.08		26.675		100.00375		230.01634		26.675		100.01226		231.44067		26.675		100.02067		232.41133		26.675		100.01212

		171.632		26.7		100.00962		100.01225		170.657		26.7		100.00391		170.336		26.7		100.00539		230.26622		26.7		100.01225		231.68955		26.7		100.02067		232.65522		26.7		100.01213

		171.88		26.725		100.00962		100.01224		170.909		26.725		100.00255		170.56599		26.725		100.00487		230.516		26.725		100.01224		231.93478		26.725		100.02065		232.90078		26.725		100.01214

		172.095		26.75		100.00684		100.01224		171.13901		26.75		100.00165		170.802		26.75		100.00408		230.76422		26.75		100.01224		232.18111		26.75		100.02064		233.14845		26.75		100.01215

		172.342		26.775		100.00824		100.01225		171.381		26.775		99.99951		171.03999		26.775		100.00329		231.01178		26.775		100.01225		232.42644		26.775		100.02061		233.39345		26.775		100.01216

		172.575		26.8		100.00656		100.01227		171.616		26.8		100.00153		171.286		26.8		100.00394		231.25589		26.8		100.01227		232.66956		26.8		100.02059		233.64		26.8		100.01217

		172.82401		26.825		100.00865		100.01229		171.854		26.825		100.00467		171.526		26.825		100.00281		231.50022		26.825		100.01229		232.91644		26.825		100.02057		233.88011		26.825		100.01218

		173.05901		26.85		100.00789		100.01231		172.10001		26.85		99.99892		171.746		26.85		100.00416		231.74856		26.85		100.01231		233.16311		26.85		100.02054		234.12622		26.85		100.01219

		173.297		26.875		100.00764		100.01235		172.33501		26.875		100.00103		171.996		26.875		100.00373		231.996		26.875		100.01235		233.41133		26.875		100.02052		234.37056		26.875		100.0122

		173.528		26.9		100.01103		100.01238		172.573		26.9		100.00148		172.24001		26.9		100.0044		232.24344		26.9		100.01238		233.659		26.9		100.0205		234.616		26.9		100.01221

		173.772		26.925		100.00612		100.01242		172.80701		26.925		100.00034		172.47301		26.925		100.00429		232.49333		26.925		100.01242		233.904		26.925		100.02049		234.86156		26.925		100.01222

		174.005		26.95		100.00753		100.01247		173.045		26.95		99.99825		172.705		26.95		100.00309		232.73878		26.95		100.01247		234.15233		26.95		100.02048		235.10911		26.95		100.01223

		174.241		26.975		100.00878		100.01251		173.289		26.975		100.00196		172.94299		26.975		100.00429		232.98711		26.975		100.01251		234.39933		26.975		100.02048		235.35778		26.975		100.01224

		174.474		27		100.00552		100.01255		173.526		27		99.99979		173.194		27		100.00348		233.23267		27		100.01255		234.64822		27		100.02048		235.60822		27		100.01226

		174.73199		27.025		100.0104		100.01258		173.767		27.025		100.00022		173.41701		27.025		100.00483		233.48		27.025		100.01258		234.89933		27.025		100.02048		235.85678		27.025		100.01227

		174.957		27.05		100.00731		100.01261		174.015		27.05		99.99952		173.664		27.05		100.00177		233.72211		27.05		100.01261		235.15033		27.05		100.0205		236.10644		27.05		100.01228

		175.198		27.075		100.01013		100.01263		174.25301		27.075		100.00598		173.907		27.075		100.00457		233.96422		27.075		100.01263		235.40033		27.075		100.02051		236.35678		27.075		100.01229

		175.435		27.1		100.00863		100.01265		174.494		27.1		100.00107		174.131		27.1		100.00338		234.20644		27.1		100.01265		235.64722		27.1		100.02054		236.61022		27.1		100.01231

		175.67101		27.125		100.00622		100.01265		174.743		27.125		100.00407		174.382		27.125		100.00427		234.44856		27.125		100.01265		235.89355		27.125		100.02057		236.86477		27.125		100.01232

		175.91701		27.15		100.00899		100.01265		174.965		27.15		100.00212		174.62199		27.15		100.00555		234.69033		27.15		100.01265		236.13844		27.15		100.0206		237.11844		27.15		100.01234

		176.142		27.175		100.00991		100.01264		175.205		27.175		100.00645		174.867		27.175		100.00533		234.93467		27.175		100.01264		236.38478		27.175		100.02063		237.373		27.175		100.01235

		176.383		27.2		100.01031		100.01263		175.45799		27.2		100.00373		175.10001		27.2		100.00409		235.18133		27.2		100.01263		236.63244		27.2		100.02067		237.62322		27.2		100.01237

		176.62601		27.225		100.00654		100.01261		175.705		27.225		100.00054		175.345		27.225		100.0052		235.43189		27.225		100.01261		236.88		27.225		100.02071		237.87222		27.225		100.01239

		176.87		27.25		100.00842		100.01258		175.938		27.25		99.99939		175.57401		27.25		100.00459		235.68278		27.25		100.01258		237.12833		27.25		100.02075		238.12477		27.25		100.0124

		177.10899		27.275		100.0109		100.01255		176.192		27.275		100.00207		175.82899		27.275		100.00123		235.935		27.275		100.01255		237.37433		27.275		100.0208		238.37489		27.275		100.01242

		177.34599		27.3		100.00763		100.01252		176.42999		27.3		100.00056		176.064		27.3		100.00479		236.18567		27.3		100.01252		237.62122		27.3		100.02084		238.61922		27.3		100.01243

		177.593		27.325		100.00759		100.01249		176.65601		27.325		99.99897		176.30901		27.325		100.00651		236.43789		27.325		100.01249		237.87167		27.325		100.02089		238.86144		27.325		100.01245

		177.83299		27.35		100.00915		100.01246		176.905		27.35		100.00249		176.547		27.35		100.0063		236.692		27.35		100.01246		238.12222		27.35		100.02093		239.10767		27.35		100.01246

		178.077		27.375		100.00793		100.01243		177.153		27.375		100.00036		176.79201		27.375		100.00728		236.94522		27.375		100.01243		238.37056		27.375		100.02098		239.356		27.375		100.01248

		178.306		27.4		100.00873		100.01241		177.388		27.4		100.00269		177.03		27.4		100.00216		237.19656		27.4		100.01241		238.614		27.4		100.02103		239.60222		27.4		100.01249

		178.534		27.425		100.0114		100.01239		177.633		27.425		100.00222		177.278		27.425		100.00417		237.443		27.425		100.01239		238.85756		27.425		100.02107		239.85045		27.425		100.0125

		178.789		27.45		100.00815		100.01237		177.871		27.45		100.00149		177.521		27.45		100.009		237.68933		27.45		100.01237		239.10456		27.45		100.02112		240.09911		27.45		100.01252

		179.022		27.475		100.0059		100.01236		178.11501		27.475		99.99754		177.75301		27.475		100.0057		237.936		27.475		100.01236		239.35278		27.475		100.02117		240.34578		27.475		100.01253

		179.269		27.5		100.00715		100.01236		178.349		27.5		100.00108		177.995		27.5		100.00543		238.18233		27.5		100.01236		239.60089		27.5		100.02122		240.59445		27.5		100.01254

		179.498		27.525		100.00389		100.01236		178.59599		27.525		99.99694		178.23399		27.525		100.0018		238.42922		27.525		100.01236		239.84878		27.525		100.02127		240.844		27.525		100.01256

		179.745		27.55		100.00557		100.01236		178.839		27.55		100.00191		178.478		27.55		100.00582		238.67233		27.55		100.01236		240.09489		27.55		100.02132		241.09622		27.55		100.01257

		179.989		27.575		100.00735		100.01237		179.082		27.575		100.0007		178.72301		27.575		100.00433		238.91867		27.575		100.01237		240.34156		27.575		100.02137		241.34556		27.575		100.01258

		180.23399		27.6		100.00728		100.01239		179.314		27.6		100.00234		178.963		27.6		100.00513		239.16245		27.6		100.01239		240.59156		27.6		100.02142		241.59556		27.6		100.01259

		180.46899		27.625		100.01091		100.01241		179.56599		27.625		100.00364		179.19901		27.625		100.00322		239.41044		27.625		100.01241		240.84389		27.625		100.02147		241.84445		27.625		100.0126

		180.71201		27.65		100.00932		100.01243		179.81		27.65		100.00033		179.452		27.65		100.00337		239.65967		27.65		100.01243		241.09667		27.65		100.02151		242.09122		27.65		100.01262

		180.946		27.675		100.00749		100.01245		180.056		27.675		99.99807		179.69099		27.675		100.00587		239.908		27.675		100.01245		241.34767		27.675		100.02156		242.33667		27.675		100.01263

		181.196		27.7		100.00713		100.01247		180.29201		27.7		99.99811		179.93401		27.7		100.00532		240.15589		27.7		100.01247		241.59578		27.7		100.0216		242.58067		27.7		100.01264

		181.42799		27.725		100.00971		100.0125		180.545		27.725		99.99955		180.17799		27.725		100.00581		240.40522		27.725		100.0125		241.84522		27.725		100.02164		242.825		27.725		100.01265

		181.67599		27.75		100.00702		100.01252		180.78		27.75		100.00229		180.424		27.75		100.00443		240.65555		27.75		100.01252		242.09489		27.75		100.02168		243.07345		27.75		100.01266

		181.91701		27.775		100.00656		100.01254		181.02699		27.775		100.00256		180.65601		27.775		100.00391		240.90667		27.775		100.01254		242.34211		27.775		100.02171		243.32133		27.775		100.01267

		182.16299		27.8		100.01247		100.01257		181.263		27.8		100.00024		180.911		27.8		100.00575		241.15289		27.8		100.01257		242.59155		27.8		100.02174		243.57055		27.8		100.01269

		182.395		27.825		100.00773		100.01259		181.51401		27.825		99.99807		181.147		27.825		100.00578		241.40078		27.825		100.01259		242.83911		27.825		100.02177		243.81822		27.825		100.0127

		182.629		27.85		100.00782		100.01261		181.77		27.85		100.00449		181.39		27.85		100.00287		241.64811		27.85		100.01261		243.08744		27.85		100.02179		244.06755		27.85		100.01271

		182.883		27.875		100.00964		100.01263		182.007		27.875		100.00065		181.63499		27.875		100.00253		241.897		27.875		100.01263		243.336		27.875		100.02181		244.31911		27.875		100.01273

		183.12801		27.9		100.00873		100.01264		182.255		27.9		100.001		181.881		27.9		100.00695		242.14467		27.9		100.01264		243.58511		27.9		100.02183		244.57122		27.9		100.01274

		183.356		27.925		100.0103		100.01266		182.49001		27.925		100.0011		182.114		27.925		100.00359		242.39034		27.925		100.01266		243.83744		27.925		100.02184		244.82822		27.925		100.01276

		183.61301		27.95		100.00953		100.01268		182.748		27.95		100.00528		182.371		27.95		100.00399		242.637		27.95		100.01268		244.08878		27.95		100.02186		245.08478		27.95		100.01277

		183.85899		27.975		100.00546		100.0127		182.985		27.975		100.00163		182.60001		27.975		100.00531		242.883		27.975		100.0127		244.34078		27.975		100.02187		245.33644		27.975		100.01279

		184.105		28		100.00815		100.01272		183.23		28		100.00507		182.85699		28		100.00529		243.13178		28		100.01272		244.59167		28		100.02188		245.58911		28		100.01281

		184.345		28.025		100.00994		100.01274		183.481		28.025		100.00023		183.095		28.025		100.00592		243.382		28.025		100.01274		244.84523		28.025		100.02189		245.839		28.025		100.01283

		184.57899		28.05		100.00879		100.01277		183.72301		28.05		100.00026		183.33701		28.05		100.00538		243.635		28.05		100.01277		245.09945		28.05		100.02191		246.08844		28.05		100.01285

		184.821		28.075		100.00698		100.01279		183.957		28.075		100.00088		183.58299		28.075		100.0047		243.88767		28.075		100.01279		245.35067		28.075		100.02192		246.33955		28.075		100.01287

		185.069		28.1		100.00803		100.01282		184.217		28.1		99.99818		183.83501		28.1		100.00513		244.139		28.1		100.01282		245.60256		28.1		100.02194		246.58733		28.1		100.0129

		185.314		28.125		100.00793		100.01285		184.452		28.125		100.00569		184.07899		28.125		100.00334		244.39045		28.125		100.01285		245.85245		28.125		100.02195		246.83233		28.125		100.01292

		185.562		28.15		100.01055		100.01287		184.703		28.15		99.99891		184.31799		28.15		100.0051		244.64611		28.15		100.01287		246.10033		28.15		100.02197		247.07667		28.15		100.01295

		185.80499		28.175		100.01005		100.0129		184.94099		28.175		100.0023		184.564		28.175		100.00511		244.90056		28.175		100.0129		246.34878		28.175		100.02199		247.325		28.175		100.01297

		186.04201		28.2		100.00518		100.01294		185.2		28.2		99.99854		184.812		28.2		100.00219		245.15133		28.2		100.01294		246.59733		28.2		100.02201		247.575		28.2		100.01299

		186.282		28.225		100.00478		100.01297		185.44		28.225		100.00197		185.058		28.225		100.00297		245.40133		28.225		100.01297		246.84456		28.225		100.02204		247.82589		28.225		100.01302

		186.533		28.25		100.00797		100.013		185.68401		28.25		99.99942		185.314		28.25		100.00131		245.65033		28.25		100.013		247.08889		28.25		100.02207		248.07722		28.25		100.01304

		186.787		28.275		100.0096		100.01303		185.938		28.275		99.99946		185.554		28.275		100.00441		245.89844		28.275		100.01303		247.33655		28.275		100.0221		248.32978		28.275		100.01307

		187.022		28.3		100.00698		100.01306		186.172		28.3		99.9977		185.78999		28.3		100.00438		246.146		28.3		100.01306		247.58733		28.3		100.02213		248.58122		28.3		100.01309

		187.27		28.325		100.0068		100.01309		186.42599		28.325		100.00233		186.04601		28.325		100.00524		246.393		28.325		100.01309		247.83711		28.325		100.02216		248.83533		28.325		100.01311

		187.511		28.35		100.00428		100.01312		186.66499		28.35		100.00321		186.28799		28.35		100.00066		246.64078		28.35		100.01312		248.08789		28.35		100.02219		249.09078		28.35		100.01313

		187.76199		28.375		100.0066		100.01314		186.92		28.375		100.00013		186.539		28.375		100.00685		246.884		28.375		100.01314		248.33778		28.375		100.02223		249.34156		28.375		100.01315

		187.994		28.4		100.00694		100.01317		187.157		28.4		100.00421		186.79601		28.4		100.00426		247.12622		28.4		100.01317		248.58878		28.4		100.02226		249.59045		28.4		100.01316

		188.23801		28.425		100.01173		100.01319		187.41901		28.425		100.001		187.03		28.425		100.00082		247.37511		28.425		100.01319		248.83878		28.425		100.0223		249.83911		28.425		100.01318

		188.502		28.45		100.00679		100.01322		187.653		28.45		100.00104		187.28		28.45		100.00327		247.62422		28.45		100.01322		249.09178		28.45		100.02233		250.08389		28.45		100.0132

		188.729		28.475		100.00634		100.01324		187.90401		28.475		99.99942		187.52299		28.475		100.00853		247.87422		28.475		100.01324		249.34244		28.475		100.02237		250.33111		28.475		100.01321

		188.981		28.5		100.00917		100.01326		188.145		28.5		99.9987		187.77		28.5		100.00659		248.12467		28.5		100.01326		249.59289		28.5		100.02241		250.57567		28.5		100.01322

		189.228		28.525		100.00687		100.01328		188.405		28.525		99.9988		188.019		28.525		100.00399		248.37356		28.525		100.01328		249.84255		28.525		100.02244		250.81689		28.525		100.01324

		189.47501		28.55		100.00904		100.01329		188.644		28.55		100.00256		188.267		28.55		100.00803		248.62122		28.55		100.01329		250.09244		28.55		100.02248		251.06244		28.55		100.01325

		189.71001		28.575		100.00751		100.01331		188.886		28.575		99.99796		188.5		28.575		100.00338		248.87089		28.575		100.01331		250.34133		28.575		100.02251		251.30855		28.575		100.01326

		189.959		28.6		100.00928		100.01333		189.13901		28.6		99.99957		188.756		28.6		100.00496		249.121		28.6		100.01333		250.589		28.6		100.02254		251.55566		28.6		100.01328

		190.201		28.625		100.00734		100.01334		189.39		28.625		100.00295		189.00101		28.625		100.00285		249.37078		28.625		100.01334		250.83122		28.625		100.02257		251.80389		28.625		100.01329

		190.46201		28.65		100.00763		100.01336		189.638		28.65		100.00418		189.256		28.65		100.00761		249.61989		28.65		100.01336		251.07733		28.65		100.0226		252.051		28.65		100.0133

		190.702		28.675		100.00821		100.01337		189.88699		28.675		99.99979		189.5		28.675		100.0053		249.86811		28.675		100.01337		251.32178		28.675		100.02263		252.30155		28.675		100.01332

		190.94901		28.7		100.00507		100.01339		190.14		28.7		100.00238		189.755		28.7		100.00597		250.11378		28.7		100.01339		251.56789		28.7		100.02266		252.54811		28.7		100.01333

		191.196		28.725		100.00781		100.01341		190.38901		28.725		100.00359		189.991		28.725		100.00378		250.35589		28.725		100.01341		251.81455		28.725		100.02268		252.79511		28.725		100.01335

		191.442		28.75		100.00861		100.01343		190.633		28.75		100		190.237		28.75		100.00239		250.59878		28.75		100.01343		252.059		28.75		100.02271		253.042		28.75		100.01337

		191.687		28.775		100.00755		100.01345		190.87601		28.775		99.99931		190.496		28.775		100.00475		250.83811		28.775		100.01345		252.30456		28.775		100.02273		253.28667		28.775		100.01339

		191.935		28.8		100.0066		100.01347		191.129		28.8		99.99995		190.737		28.8		100.0026		251.08245		28.8		100.01347		252.54911		28.8		100.02275		253.53033		28.8		100.01341

		192.187		28.825		100.00956		100.0135		191.373		28.825		100.00429		190.992		28.825		100.00226		251.32656		28.825		100.0135		252.79322		28.825		100.02277		253.77611		28.825		100.01343

		192.435		28.85		100.00966		100.01352		191.62601		28.85		100.00471		191.244		28.85		100.00183		251.57211		28.85		100.01352		253.04178		28.85		100.0228		254.02255		28.85		100.01345

		192.679		28.875		100.00561		100.01355		191.87199		28.875		100.00632		191.48599		28.875		100.00646		251.81644		28.875		100.01355		253.28789		28.875		100.02282		254.26822		28.875		100.01347

		192.923		28.9		100.00183		100.01358		192.127		28.9		99.99963		191.73199		28.9		100.00455		252.05944		28.9		100.01358		253.537		28.9		100.02284		254.51378		28.9		100.0135

		193.17599		28.925		100.00531		100.01361		192.375		28.925		99.99945		191.97501		28.925		100.0074		252.30522		28.925		100.01361		253.78289		28.925		100.02286		254.75844		28.925		100.01353

		193.42101		28.95		100.00869		100.01365		192.627		28.95		99.99979		192.215		28.95		100.00628		252.55266		28.95		100.01365		254.02911		28.95		100.02289		255.00711		28.95		100.01355

		193.677		28.975		100.00622		100.01368		192.87601		28.975		99.99722		192.48		28.975		100.00639		252.80144		28.975		100.01368		254.27656		28.975		100.02292		255.25656		28.975		100.01358

		193.91		29		100.00746		100.01371		193.116		29		99.99904		192.724		29		100.00602		253.05266		29		100.01371		254.52089		29		100.02294		255.50233		29		100.01361

		194.17101		29.025		100.00225		100.01374		193.377		29.025		99.99953		192.97501		29.025		100.00638		253.3		29.025		100.01374		254.76734		29.025		100.02297		255.755		29.025		100.01363

		194.407		29.05		100.00394		100.01377		193.631		29.05		100.00294		193.22301		29.05		100.00348		253.55		29.05		100.01377		255.01645		29.05		100.02301		256.007		29.05		100.01366

		194.658		29.075		100.00704		100.01381		193.87199		29.075		100.00295		193.46899		29.075		100.00436		253.79689		29.075		100.01381		255.26433		29.075		100.02304		256.25655		29.075		100.01369

		194.91299		29.1		100.00476		100.01384		194.117		29.1		99.99914		193.718		29.1		100.00413		254.043		29.1		100.01384		255.50933		29.1		100.02308		256.50667		29.1		100.01371

		195.157		29.125		100.00616		100.01386		194.37601		29.125		100.00129		193.966		29.125		100.00249		254.28933		29.125		100.01386		255.75522		29.125		100.02312		256.75544		29.125		100.01374

		195.397		29.15		100.00766		100.01389		194.61501		29.15		99.99819		194.217		29.15		100.00415		254.53367		29.15		100.01389		256.003		29.15		100.02316		257.00555		29.15		100.01376

		195.64101		29.175		100.00793		100.01391		194.86301		29.175		99.99793		194.461		29.175		100.00552		254.77867		29.175		100.01391		256.25011		29.175		100.0232		257.25344		29.175		100.01379

		195.88		29.2		100.00928		100.01393		195.116		29.2		99.99969		194.73		29.2		100.00344		255.02544		29.2		100.01393		256.49611		29.2		100.02325		257.50277		29.2		100.01381

		196.149		29.225		100.00656		100.01395		195.36501		29.225		99.99705		194.97		29.225		100.00295		255.276		29.225		100.01395		256.74244		29.225		100.02329		257.74988		29.225		100.01384

		196.39301		29.25		100.00702		100.01396		195.618		29.25		99.99764		195.209		29.25		100.00348		255.52289		29.25		100.01396		256.98877		29.25		100.02334		257.99289		29.25		100.01386

		196.647		29.275		100.00358		100.01397		195.87399		29.275		99.99967		195.472		29.275		100.00346		255.77278		29.275		100.01397		257.23555		29.275		100.02338		258.23478		29.275		100.01389

		196.897		29.3		100.00802		100.01398		196.12601		29.3		99.99906		195.716		29.3		100.00394		256.02334		29.3		100.01398		257.48089		29.3		100.02342		258.47511		29.3		100.01391

		197.147		29.325		100.00908		100.01398		196.373		29.325		100.00496		195.963		29.325		100.00491		256.271		29.325		100.01398		257.72677		29.325		100.02347		258.71811		29.325		100.01394

		197.38499		29.35		100.0057		100.01398		196.62399		29.35		100.00273		196.214		29.35		100.00289		256.52334		29.35		100.01398		257.97188		29.35		100.02351		258.96177		29.35		100.01396

		197.631		29.375		100.00558		100.01397		196.864		29.375		100.0035		196.467		29.375		100.00574		256.77567		29.375		100.01397		258.21699		29.375		100.02355		259.20933		29.375		100.01399

		197.87601		29.4		100.00692		100.01396		197.119		29.4		100.0007		196.72		29.4		100.0054		257.02967		29.4		100.01396		258.46288		29.4		100.02359		259.45533		29.4		100.01401

		198.129		29.425		100.00516		100.01395		197.37601		29.425		100.0022		196.96899		29.425		100.00373		257.27977		29.425		100.01395		258.70855		29.425		100.02362		259.70155		29.425		100.01403

		198.38699		29.45		100.00697		100.01394		197.619		29.45		100.00182		197.224		29.45		100.00569		257.52844		29.45		100.01394		258.95855		29.45		100.02366		259.94888		29.45		100.01405

		198.63499		29.475		100.00744		100.01392		197.87		29.475		100.00361		197.48199		29.475		100.00196		257.77444		29.475		100.01392		259.20833		29.475		100.02369		260.19744		29.475		100.01407

		198.879		29.5		100.00738		100.01391		198.127		29.5		100.00476		197.72099		29.5		100.0029		258.02		29.5		100.01391		259.45699		29.5		100.02372		260.44622		29.5		100.01408

		199.13		29.525		100.00595		100.0139		198.37		29.525		100.00329		197.98399		29.525		100.00036		258.26466		29.525		100.0139		259.70722		29.525		100.02374		260.69933		29.525		100.01409

		199.38699		29.55		100.00415		100.01388		198.62601		29.55		100.0044		198.23399		29.55		100.00612		258.50888		29.55		100.01388		259.95455		29.55		100.02377		260.95256		29.55		100.0141

		199.632		29.575		100.00676		100.01388		198.882		29.575		100.00245		198.479		29.575		100.00582		258.751		29.575		100.01388		260.20344		29.575		100.02379		261.204		29.575		100.01411

		199.871		29.6		100.00846		100.01387		199.13		29.6		100.00383		198.728		29.6		100.00387		258.99422		29.6		100.01387		260.45166		29.6		100.02381		261.45245		29.6		100.01411

		200.12399		29.625		100.00735		100.01387		199.38499		29.625		100.00447		198.995		29.625		100.00417		259.23633		29.625		100.01387		260.69966		29.625		100.02382		261.70134		29.625		100.01411

		200.37801		29.65		100.00507		100.01387		199.627		29.65		100.00454		199.239		29.65		100.00616		259.48133		29.65		100.01387		260.95044		29.65		100.02384		261.95223		29.65		100.01411

		200.625		29.675		100.00776		100.01388		199.879		29.675		100.00157		199.485		29.675		100.00359		259.72556		29.675		100.01388		261.197		29.675		100.02385		262.20067		29.675		100.0141

		200.868		29.7		100.00799		100.01389		200.13901		29.7		100.00283		199.742		29.7		100.00361		259.97245		29.7		100.01389		261.44556		29.7		100.02386		262.44767		29.7		100.0141

		201.121		29.725		100.00561		100.01391		200.386		29.725		100.00054		199.98599		29.725		100.00426		260.21678		29.725		100.01391		261.69389		29.725		100.02387		262.69322		29.725		100.0141

		201.37199		29.75		100.00607		100.01393		200.63699		29.75		100.00053		200.233		29.75		100.00474		260.46289		29.75		100.01393		261.94422		29.75		100.02388		262.93878		29.75		100.0141

		201.619		29.775		100.00727		100.01395		200.897		29.775		99.99818		200.485		29.775		100.00418		260.71323		29.775		100.01395		262.19767		29.775		100.02388		263.18156		29.775		100.01411

		201.873		29.8		100.00538		100.01398		201.149		29.8		99.99831		200.744		29.8		100.00457		260.963		29.8		100.01398		262.44667		29.8		100.02389		263.42733		29.8		100.01412

		202.11301		29.825		100.00487		100.01401		201.388		29.825		100.00153		200.983		29.825		100.00381		261.21289		29.825		100.01401		262.69767		29.825		100.0239		263.67433		29.825		100.01413

		202.371		29.85		100.00469		100.01405		201.64101		29.85		100.00295		201.24001		29.85		100.00442		261.45912		29.85		100.01405		262.94956		29.85		100.0239		263.92111		29.85		100.01415

		202.623		29.875		100.00859		100.01408		201.901		29.875		100.00522		201.495		29.875		100.00434		261.706		29.875		100.01408		263.20078		29.875		100.02391		264.164		29.875		100.01417

		202.895		29.9		100.00529		100.01412		202.153		29.9		100.00238		201.74899		29.9		100.00468		261.95078		29.9		100.01412		263.45434		29.9		100.02391		264.41		29.9		100.01419

		203.131		29.925		100.00895		100.01416		202.40601		29.925		100.00525		201.991		29.925		100.00443		262.19522		29.925		100.01416		263.70611		29.925		100.02392		264.65711		29.925		100.01422

		203.36501		29.95		100.0071		100.0142		202.655		29.95		99.99942		202.256		29.95		100.00241		262.44067		29.95		100.0142		263.95933		29.95		100.02392		264.90678		29.95		100.01425

		203.633		29.975		100.007		100.01423		202.905		29.975		99.99836		202.50301		29.975		100.00557		262.68844		29.975		100.01423		264.21233		29.975		100.02393		265.15255		29.975		100.01428

		203.87801		30		100.00687		100.01427		203.157		30		99.9984		202.75999		30		100.00355		262.93666		30		100.01427		264.46344		30		100.02393		265.40111		30		100.01432

		204.13		30.025		100.0058		100.0143		203.412		30.025		99.99751		203.007		30.025		100.00267		263.18689		30.025		100.0143		264.71689		30.025		100.02394		265.64722		30.025		100.01435

		204.379		30.05		100.00677		100.01434		203.66701		30.05		100.00135		203.257		30.05		100.00525		263.43477		30.05		100.01434		264.96822		30.05		100.02395		265.89111		30.05		100.01439

		204.629		30.075		100.0078		100.01437		203.924		30.075		100.00451		203.513		30.075		100.00366		263.68666		30.075		100.01437		265.21755		30.075		100.02396		266.13289		30.075		100.01442

		204.894		30.1		100.00753		100.01439		204.17101		30.1		100.00447		203.772		30.1		100.00388		263.938		30.1		100.01439		265.46678		30.1		100.02397		266.37911		30.1		100.01446

		205.132		30.125		100.00748		100.01442		204.42799		30.125		99.99942		204.022		30.125		100.00501		264.19133		30.125		100.01442		265.71422		30.125		100.02398		266.62666		30.125		100.01449

		205.39301		30.15		100.00916		100.01443		204.683		30.15		100.00081		204.272		30.15		100.00543		264.44289		30.15		100.01443		265.96111		30.15		100.024		266.87633		30.15		100.01452

		205.636		30.175		100.00639		100.01445		204.93401		30.175		100.00313		204.52499		30.175		100.00383		264.69344		30.175		100.01445		266.207		30.175		100.02402		267.12689		30.175		100.01455

		205.899		30.2		100.00789		100.01446		205.192		30.2		100.00459		204.776		30.2		100.00557		264.94278		30.2		100.01446		266.45244		30.2		100.02405		267.37945		30.2		100.01457

		206.157		30.225		100.00672		100.01447		205.439		30.225		99.99815		205.03999		30.225		100.00317		265.19078		30.225		100.01447		266.70389		30.225		100.02407		267.632		30.225		100.0146

		206.42		30.25		100.00559		100.01447		205.69299		30.25		99.99913		205.289		30.25		100.00334		265.43622		30.25		100.01447		266.951		30.25		100.0241		267.88589		30.25		100.01462

		206.66299		30.275		100.00584		100.01447		205.936		30.275		100.00159		205.54401		30.275		100.00661		265.68422		30.275		100.01447		267.19789		30.275		100.02414		268.14044		30.275		100.01464

		206.91		30.3		100.01065		100.01447		206.19901		30.3		100.0036		205.798		30.3		100.00715		265.93189		30.3		100.01447		267.44855		30.3		100.02417		268.397		30.3		100.01466

		207.157		30.325		100.00831		100.01447		206.45399		30.325		100.00309		206.05299		30.325		100.00419		266.17555		30.325		100.01447		267.70044		30.325		100.02421		268.65255		30.325		100.01468

		207.40601		30.35		100.00641		100.01446		206.70599		30.35		100.00312		206.30299		30.35		100.0061		266.42311		30.35		100.01446		267.95311		30.35		100.02424		268.90555		30.35		100.0147

		207.66901		30.375		100.00635		100.01446		206.96001		30.375		100.00192		206.56		30.375		100.00394		266.67711		30.375		100.01446		268.20655		30.375		100.02428		269.15667		30.375		100.01472

		207.912		30.4		100.00702		100.01446		207.216		30.4		99.99936		206.814		30.4		100.00246		266.93011		30.4		100.01446		268.46		30.4		100.02432		269.40444		30.4		100.01473

		208.172		30.425		100.00953		100.01445		207.47301		30.425		100.00088		207.06599		30.425		100.00475		267.18444		30.425		100.01445		268.71666		30.425		100.02435		269.65189		30.425		100.01475

		208.41299		30.45		100.00704		100.01445		207.72301		30.45		99.99699		207.314		30.45		100.00304		267.44022		30.45		100.01445		268.96722		30.45		100.02439		269.89678		30.45		100.01477

		208.674		30.475		100.00901		100.01446		207.97301		30.475		100.00032		207.573		30.475		100.00572		267.69522		30.475		100.01446		269.22355		30.475		100.02442		270.14244		30.475		100.01479

		208.929		30.5		100.00409		100.01446		208.228		30.5		99.99857		207.821		30.5		100.00349		267.95023		30.5		100.01446		269.48055		30.5		100.02445		270.38711		30.5		100.01481

		209.20399		30.525		100.00468		100.01447		208.48199		30.525		100.00116		208.076		30.525		100.00435		268.20445		30.525		100.01447		269.72967		30.525		100.02448		270.633		30.525		100.01483

		209.43201		30.55		100.0039		100.01448		208.742		30.55		100.00181		208.33		30.55		100.00554		268.45945		30.55		100.01448		269.97788		30.55		100.0245		270.87733		30.55		100.01485

		209.673		30.575		100.00743		100.01449		208.99001		30.575		100.00215		208.58501		30.575		100.00306		268.71367		30.575		100.01449		270.22478		30.575		100.02452		271.12789		30.575		100.01487

		209.938		30.6		100.00595		100.01451		209.259		30.6		99.996		208.842		30.6		100.00175		268.96389		30.6		100.01451		270.47255		30.6		100.02454		271.37522		30.6		100.01489

		210.189		30.625		100.00538		100.01452		209.509		30.625		100.00016		209.10001		30.625		100.00733		269.21389		30.625		100.01452		270.72378		30.625		100.02456		271.62322		30.625		100.01491

		210.433		30.65		100.0088		100.01454		209.76199		30.65		99.99964		209.353		30.65		100.0062		269.46166		30.65		100.01454		270.97189		30.65		100.02457		271.87211		30.65		100.01493

		210.694		30.675		100.00563		100.01456		210.01401		30.675		99.99885		209.60201		30.675		100.00512		269.70689		30.675		100.01456		271.22355		30.675		100.02458		272.12		30.675		100.01495

		210.94901		30.7		100.00866		100.01458		210.26801		30.7		100.00051		209.86		30.7		100.00439		269.95422		30.7		100.01458		271.473		30.7		100.02458		272.36833		30.7		100.01496

		211.202		30.725		100.00852		100.01459		210.515		30.725		100.00081		210.11301		30.725		100.00592		270.20077		30.725		100.01459		271.724		30.725		100.02458		272.61777		30.725		100.01498

		211.464		30.75		100.00766		100.01461		210.769		30.75		100.00189		210.37399		30.75		100.00514		270.44877		30.75		100.01461		271.97544		30.75		100.02458		272.86755		30.75		100.01499

		211.705		30.775		100.00523		100.01463		211.024		30.775		99.99882		210.62199		30.775		100.00502		270.69799		30.775		100.01463		272.22956		30.775		100.02457		273.11689		30.775		100.01501

		211.95599		30.8		100.00599		100.01465		211.278		30.8		100.00082		210.87		30.8		100.00314		270.94622		30.8		100.01465		272.48311		30.8		100.02456		273.36622		30.8		100.01502

		212.217		30.825		100.00537		100.01466		211.539		30.825		99.99884		211.13499		30.825		100.00473		271.19544		30.825		100.01466		272.73578		30.825		100.02454		273.61422		30.825		100.01503

		212.474		30.85		100.00776		100.01468		211.793		30.85		99.9994		211.38901		30.85		100.00494		271.44755		30.85		100.01468		272.98478		30.85		100.02453		273.86055		30.85		100.01504

		212.73		30.875		100.00883		100.01469		212.045		30.875		99.99953		211.65199		30.875		100.00559		271.70122		30.875		100.01469		273.23489		30.875		100.02451		274.107		30.875		100.01505

		212.98		30.9		100.00759		100.01471		212.30099		30.9		100.00013		211.89799		30.9		100.00448		271.95189		30.9		100.01471		273.48555		30.9		100.02449		274.35355		30.9		100.01505

		213.23599		30.925		100.0089		100.01472		212.55299		30.925		100.0019		212.15401		30.925		100.00408		272.20634		30.925		100.01472		273.73589		30.925		100.02446		274.60111		30.925		100.01506

		213.479		30.95		100.00727		100.01473		212.80901		30.95		99.99693		212.411		30.95		100.00418		272.45734		30.95		100.01473		273.98489		30.95		100.02444		274.85289		30.95		100.01507

		213.73599		30.975		100.00624		100.01474		213.065		30.975		100.00105		212.66901		30.975		100.00486		272.70845		30.975		100.01474		274.23467		30.975		100.02442		275.10211		30.975		100.01507

		213.993		31		100.00646		100.01475		213.326		31		100.00562		212.92599		31		100.00484		272.96012		31		100.01475		274.48033		31		100.0244		275.35288		31		100.01508

		214.24899		31.025		100.00854		100.01476		213.584		31.025		99.99869		213.17799		31.025		100.00462		273.20867		31.025		100.01476		274.73189		31.025		100.02438		275.59955		31.025		100.01508

		214.49899		31.05		100.0041		100.01476		213.834		31.05		100.00056		213.42101		31.05		100.00358		273.45845		31.05		100.01476		274.98422		31.05		100.02436		275.85044		31.05		100.01509

		214.755		31.075		100.00604		100.01476		214.097		31.075		99.99684		213.685		31.075		100.00507		273.70789		31.075		100.01476		275.23511		31.075		100.02434		276.10545		31.075		100.0151

		215.00101		31.1		100.005		100.01476		214.354		31.1		99.99754		213.944		31.1		100.00388		273.95645		31.1		100.01476		275.48656		31.1		100.02433		276.35622		31.1		100.01511

		215.27299		31.125		100.00664		100.01476		214.61301		31.125		100.00171		214.19099		31.125		100.00519		274.20578		31.125		100.01476		275.734		31.125		100.02432		276.60855		31.125		100.01512

		215.51801		31.15		100.00812		100.01476		214.86301		31.15		100.00055		214.444		31.15		100.00467		274.452		31.15		100.01476		275.98467		31.15		100.02431		276.85745		31.15		100.01513

		215.769		31.175		100.00778		100.01475		215.12601		31.175		100.00114		214.70399		31.175		100.00455		274.70589		31.175		100.01475		276.23556		31.175		100.02431		277.10356		31.175		100.01514

		216.028		31.2		100.00514		100.01474		215.383		31.2		100.00078		214.97		31.2		100.00666		274.95722		31.2		100.01474		276.48911		31.2		100.02431		277.35278		31.2		100.01515

		216.27901		31.225		100.00916		100.01473		215.642		31.225		99.99946		215.23		31.225		100.00471		275.20644		31.225		100.01473		276.74455		31.225		100.02431		277.59922		31.225		100.01516

		216.53999		31.25		100.00947		100.01472		215.892		31.25		100.0006		215.472		31.25		100.00401		275.45856		31.25		100.01472		276.99578		31.25		100.02431		277.84611		31.25		100.01518

		216.791		31.275		100.00515		100.01471		216.14301		31.275		100.00255		215.733		31.275		100.00319		275.70845		31.275		100.01471		277.24467		31.275		100.02432		278.09222		31.275		100.01519

		217.05499		31.3		100.00457		100.01471		216.407		31.3		99.9986		215.98199		31.3		100.00475		275.95845		31.3		100.01471		277.49245		31.3		100.02434		278.33478		31.3		100.0152

		217.315		31.325		100.00687		100.0147		216.66499		31.325		99.997		216.25		31.325		100.00594		276.20978		31.325		100.0147		277.737		31.325		100.02435		278.57944		31.325		100.01522

		217.556		31.35		100.0087		100.01469		216.91499		31.35		99.99709		216.51199		31.35		100.00555		276.46233		31.35		100.01469		277.983		31.35		100.02437		278.82411		31.35		100.01523

		217.81599		31.375		100.00869		100.01468		217.17599		31.375		99.99935		216.757		31.375		100.00212		276.71422		31.375		100.01468		278.22611		31.375		100.0244		279.06966		31.375		100.01524

		218.071		31.4		100.00638		100.01468		217.42799		31.4		99.99859		217.011		31.4		100.0007		276.96333		31.4		100.01468		278.47145		31.4		100.02442		279.31355		31.4		100.01526

		218.32401		31.425		100.00662		100.01468		217.686		31.425		100.00071		217.27699		31.425		100.003		277.21222		31.425		100.01468		278.71822		31.425		100.02445		279.55666		31.425		100.01527

		218.582		31.45		100.00428		100.01468		217.948		31.45		100.00138		217.53		31.45		100.00206		277.45989		31.45		100.01468		278.96222		31.45		100.02448		279.80522		31.45		100.01528

		218.839		31.475		100.00646		100.01469		218.207		31.475		100.00299		217.778		31.475		100.00473		277.70611		31.475		100.01469		279.20667		31.475		100.02452		280.05344		31.475		100.01529

		219.104		31.5		100.00774		100.01469		218.453		31.5		100.0018		218.041		31.5		100.00623		277.95566		31.5		100.01469		279.45245		31.5		100.02455		280.30044		31.5		100.0153

		219.356		31.525		100.00947		100.0147		218.72501		31.525		99.99945		218.29201		31.525		100.00697		278.20222		31.525		100.0147		279.69878		31.525		100.02458		280.55033		31.525		100.01531

		219.60899		31.55		100.00825		100.01471		218.972		31.55		99.99683		218.55099		31.55		100.00611		278.44944		31.55		100.01471		279.94578		31.55		100.02462		280.80045		31.55		100.01532

		219.864		31.575		100.00451		100.01471		219.22501		31.575		99.99766		218.804		31.575		100.00426		278.69578		31.575		100.01471		280.19223		31.575		100.02465		281.04978		31.575		100.01533

		220.11		31.6		100.00647		100.01472		219.493		31.6		100.00236		219.05901		31.6		100.00394		278.94178		31.6		100.01472		280.439		31.6		100.02468		281.29644		31.6		100.01534

		220.377		31.625		100.00186		100.01473		219.745		31.625		100.00359		219.32401		31.625		100.00189		279.18355		31.625		100.01473		280.68311		31.625		100.02471		281.54578		31.625		100.01536

		220.625		31.65		100.00563		100.01474		220.00301		31.65		99.99669		219.586		31.65		100.00263		279.42855		31.65		100.01474		280.92789		31.65		100.02474		281.791		31.65		100.01537

		220.88699		31.675		100.00673		100.01475		220.261		31.675		99.99536		219.84		31.675		100.00478		279.67778		31.675		100.01475		281.17256		31.675		100.02477		282.03467		31.675		100.01538

		221.147		31.7		100.00706		100.01476		220.51601		31.7		99.99766		220.095		31.7		100.00481		279.92411		31.7		100.01476		281.41745		31.7		100.02479		282.27822		31.7		100.01539

		221.39301		31.725		100.00647		100.01477		220.778		31.725		100.00152		220.34599		31.725		100.00456		280.16811		31.725		100.01477		281.66289		31.725		100.02481		282.52333		31.725		100.0154

		221.64999		31.75		100.00802		100.01477		221.037		31.75		99.99961		220.604		31.75		100.00423		280.41178		31.75		100.01477		281.90966		31.75		100.02483		282.76944		31.75		100.01541

		221.916		31.775		100.00499		100.01478		221.29201		31.775		99.99862		220.867		31.775		100.00589		280.65533		31.775		100.01478		282.15533		31.775		100.02485		283.014		31.775		100.01542

		222.168		31.8		100.00725		100.01478		221.55499		31.8		100.00157		221.12		31.8		100.00217		280.89989		31.8		100.01478		282.403		31.8		100.02486		283.26033		31.8		100.01543

		222.42		31.825		100.00599		100.01478		221.804		31.825		100.00311		221.382		31.825		100.00495		281.144		31.825		100.01478		282.65311		31.825		100.02488		283.50622		31.825		100.01544

		222.67999		31.85		100.00224		100.01478		222.062		31.85		100.00372		221.634		31.85		100.00647		281.38933		31.85		100.01478		282.90367		31.85		100.02489		283.74867		31.85		100.01545

		222.93201		31.875		100.00828		100.01478		222.32201		31.875		100.00083		221.89301		31.875		100.00516		281.63389		31.875		100.01478		283.15189		31.875		100.0249		283.99478		31.875		100.01546

		223.19099		31.9		100.0079		100.01478		222.577		31.9		100.00339		222.15601		31.9		100.00163		281.87611		31.9		100.01478		283.40256		31.9		100.02491		284.23812		31.9		100.01547

		223.44099		31.925		100.00425		100.01477		222.838		31.925		99.9992		222.408		31.925		100.00181		282.11522		31.925		100.01477		283.65333		31.925		100.02492		284.48323		31.925		100.01548

		223.702		31.95		100.00582		100.01476		223.09399		31.95		99.99918		222.67		31.95		100.00398		282.35777		31.95		100.01476		283.90222		31.95		100.02493		284.72656		31.95		100.01548

		223.95799		31.975		100.00734		100.01476		223.349		31.975		99.9957		222.92101		31.975		100.00326		282.60889		31.975		100.01476		284.15422		31.975		100.02495		284.96778		31.975		100.01549

		224.211		32		100.00711		100.01475		223.608		32		100.00446		223.175		32		100.00272		282.85644		32		100.01475		284.40667		32		100.02496		285.21		32		100.0155

		224.47099		32.025		100.00515		100.01473		223.87399		32.025		100.0013		223.438		32.025		100.00767		283.10389		32.025		100.01473		284.65944		32.025		100.02497		285.45167		32.025		100.01551

		224.73199		32.05		100.00481		100.01472		224.133		32.05		99.99804		223.69701		32.05		100.00349		283.35188		32.05		100.01472		284.90689		32.05		100.02498		285.69389		32.05		100.01552

		224.981		32.075		100.00468		100.01471		224.381		32.075		99.99328		223.948		32.075		100.0023		283.60022		32.075		100.01471		285.15689		32.075		100.02499		285.936		32.075		100.01553

		225.23801		32.1		100.00528		100.01469		224.649		32.1		99.99892		224.214		32.1		100.00482		283.84878		32.1		100.01469		285.40189		32.1		100.025		286.18077		32.1		100.01555

		225.502		32.125		100.0078		100.01468		224.905		32.125		100.00421		224.46899		32.125		100.00358		284.10011		32.125		100.01468		285.646		32.125		100.02501		286.42722		32.125		100.01556

		225.76601		32.15		100.00531		100.01467		225.162		32.15		99.99982		224.73399		32.15		100.00079		284.35789		32.15		100.01467		285.89011		32.15		100.02503		286.67099		32.15		100.01558

		226.00999		32.175		100.00679		100.01466		225.41701		32.175		99.99586		224.993		32.175		100.00405		284.60789		32.175		100.01466		286.135		32.175		100.02504		286.9171		32.175		100.0156

		226.27		32.2		100.00649		100.01465		225.67101		32.2		99.99871		225.23801		32.2		100.00472		284.85089		32.2		100.01465		286.37789		32.2		100.02505		287.16255		32.2		100.01562

		226.52299		32.225		100.00971		100.01465		225.938		32.225		100.00313		225.508		32.225		100.00887		285.09789		32.225		100.01465		286.62188		32.225		100.02506		287.40977		32.225		100.01564

		226.78999		32.25		100.00549		100.01465		226.192		32.25		100.00133		225.761		32.25		100.00515		285.34311		32.25		100.01465		286.86388		32.25		100.02508		287.65711		32.25		100.01566

		227.039		32.275		100.00803		100.01466		226.451		32.275		99.99476		226.01199		32.275		100.00427		285.58845		32.275		100.01466		287.11066		32.275		100.02509		287.90766		32.275		100.01569

		227.29601		32.3		100.00667		100.01467		226.70599		32.3		100.00062		226.28101		32.3		100.00497		285.83289		32.3		100.01467		287.35244		32.3		100.0251		288.16144		32.3		100.01571

		227.562		32.325		100.00639		100.01469		226.97099		32.325		99.99979		226.541		32.325		100.00245		286.07478		32.325		100.01469		287.60155		32.325		100.02512		288.41066		32.325		100.01574

		227.81		32.35		100.00476		100.01471		227.224		32.35		99.99502		226.806		32.35		100.00915		286.31967		32.35		100.01471		287.84944		32.35		100.02513		288.66066		32.35		100.01576

		228.073		32.375		100.00494		100.01473		227.487		32.375		99.99968		227.061		32.375		100.0087		286.56523		32.375		100.01473		288.09411		32.375		100.02514		288.91056		32.375		100.01579

		228.32899		32.4		100.00725		100.01476		227.748		32.4		100.00307		227.323		32.4		100.00766		286.81312		32.4		100.01476		288.34022		32.4		100.02516		289.15745		32.4		100.01581

		228.577		32.425		100.00839		100.0148		228.005		32.425		99.99974		227.575		32.425		100.00374		287.06034		32.425		100.0148		288.58367		32.425		100.02517		289.40555		32.425		100.01584

		228.83299		32.45		100.00823		100.01483		228.26601		32.45		99.99685		227.834		32.45		100.00839		287.30634		32.45		100.01483		288.82911		32.45		100.02518		289.65211		32.45		100.01586

		229.093		32.475		100.00603		100.01487		228.51801		32.475		100.00251		228.095		32.475		100.00287		287.55667		32.475		100.01487		289.07589		32.475		100.02519		289.89778		32.475		100.01588

		229.355		32.5		100.00567		100.0149		228.791		32.5		99.99704		228.34801		32.5		100.00578		287.80534		32.5		100.0149		289.32178		32.5		100.02521		290.14322		32.5		100.0159

		229.614		32.525		100.00811		100.01494		229.043		32.525		100.00044		228.599		32.525		100.00255		288.05622		32.525		100.01494		289.56945		32.525		100.02522		290.38933		32.525		100.01592

		229.879		32.55		100.0022		100.01498		229.306		32.55		99.99813		228.86		32.55		100.00406		288.30844		32.55		100.01498		289.81589		32.55		100.02523		290.63633		32.55		100.01594

		230.132		32.575		100.01057		100.01501		229.561		32.575		100.00272		229.13		32.575		100.00635		288.55567		32.575		100.01501		290.06467		32.575		100.02524		290.88422		32.575		100.01596

		230.40199		32.6		100.00553		100.01505		229.82201		32.6		99.99711		229.388		32.6		100.00455		288.80155		32.6		100.01505		290.31367		32.6		100.02525		291.13278		32.6		100.01598

		230.647		32.625		100.00637		100.01508		230.078		32.625		100.00022		229.646		32.625		100.00303		289.04922		32.625		100.01508		290.56045		32.625		100.02526		291.38278		32.625		100.01599

		230.903		32.65		100.00599		100.01511		230.34		32.65		99.99641		229.903		32.65		99.99849		289.29678		32.65		100.01511		290.80956		32.65		100.02528		291.63222		32.65		100.01601

		231.16499		32.675		100.00726		100.01514		230.60699		32.675		100.00087		230.168		32.675		100.00308		289.53933		32.675		100.01514		291.05944		32.675		100.02529		291.884		32.675		100.01602

		231.427		32.7		100.00431		100.01516		230.85699		32.7		99.99548		230.42599		32.7		100.00909		289.78377		32.7		100.01516		291.309		32.7		100.0253		292.135		32.7		100.01604

		231.687		32.725		100.00869		100.01519		231.121		32.725		100.00258		230.686		32.725		99.99678		290.03111		32.725		100.01519		291.55866		32.725		100.02532		292.38612		32.725		100.01605

		231.94299		32.75		100.0076		100.0152		231.394		32.75		100.00051		230.94501		32.75		99.99924		290.27622		32.75		100.0152		291.808		32.75		100.02533		292.63378		32.75		100.01607

		232.198		32.775		100.00494		100.01522		231.63901		32.775		99.99727		231.214		32.775		100.008		290.52278		32.775		100.01522		292.05711		32.775		100.02535		292.88178		32.775		100.01608

		232.46201		32.8		100.00447		100.01524		231.90601		32.8		100.00165		231.459		32.8		99.99875		290.77066		32.8		100.01524		292.30333		32.8		100.02536		293.126		32.8		100.01609

		232.716		32.825		100.00646		100.01525		232.172		32.825		99.99744		231.726		32.825		100.00566		291.01955		32.825		100.01525		292.553		32.825		100.02538		293.37233		32.825		100.01611

		232.97501		32.85		99.99893		100.01526		232.42799		32.85		99.99928		231.98599		32.85		100.00314		291.27066		32.85		100.01526		292.80144		32.85		100.0254		293.61845		32.85		100.01612

		233.23		32.875		100.00673		100.01527		232.68201		32.875		100.00203		232.248		32.875		100.00135		291.523		32.875		100.01527		293.04755		32.875		100.02542		293.86344		32.875		100.01614

		233.483		32.9		100.00574		100.01527		232.94299		32.9		99.99847		232.504		32.9		100.005		291.78033		32.9		100.01527		293.29211		32.9		100.02544		294.10555		32.9		100.01615

		233.745		32.925		100.00613		100.01528		233.202		32.925		99.99537		232.76401		32.925		100.00426		292.03411		32.925		100.01528		293.53455		32.925		100.02546		294.34933		32.925		100.01617

		234.004		32.95		100.00276		100.01528		233.468		32.95		99.9953		233.02901		32.95		100.00464		292.28533		32.95		100.01528		293.77544		32.95		100.02549		294.59333		32.95		100.01618

		234.26801		32.975		100.00469		100.01528		233.716		32.975		100.00157		233.293		32.975		100.00168		292.53855		32.975		100.01528		294.02122		32.975		100.02551		294.83866		32.975		100.0162

		234.53799		33		100.00689		100.01528		233.974		33		100.00238		233.552		33		100.00475		292.78733		33		100.01528		294.26722		33		100.02554		295.08444		33		100.01621

		234.786		33.025		100.00629		100.01527		234.239		33.025		99.99804		233.821		33.025		100.00158		293.034		33.025		100.01527		294.51677		33.025		100.02556		295.33289		33.025		100.01623

		235.045		33.05		100.00456		100.01527		234.49899		33.05		99.99563		234.063		33.05		100.00364		293.28088		33.05		100.01527		294.76489		33.05		100.02559		295.57889		33.05		100.01625

		235.30299		33.075		100.00701		100.01526		234.757		33.075		99.99833		234.32899		33.075		100.00255		293.52544		33.075		100.01526		295.01567		33.075		100.02562		295.82733		33.075		100.01626

		235.558		33.1		100.00877		100.01525		235.02299		33.1		100.0006		234.589		33.1		100.00271		293.77044		33.1		100.01525		295.26633		33.1		100.02564		296.07467		33.1		100.01628

		235.81599		33.125		100.00576		100.01524		235.27699		33.125		100.00089		234.84399		33.125		100.00303		294.018		33.125		100.01524		295.51811		33.125		100.02567		296.324		33.125		100.01629

		236.084		33.15		100.00793		100.01523		235.53799		33.15		99.99804		235.114		33.15		100.0024		294.265		33.15		100.01523		295.77044		33.15		100.02569		296.57189		33.15		100.0163

		236.33501		33.175		100.00533		100.01522		235.804		33.175		99.99771		235.373		33.175		100.00478		294.51411		33.175		100.01522		296.02144		33.175		100.02572		296.82044		33.175		100.01632

		236.595		33.2		100.0063		100.01521		236.063		33.2		100.00081		235.636		33.2		100.00455		294.764		33.2		100.01521		296.26911		33.2		100.02574		297.06856		33.2		100.01633

		236.854		33.225		100.0058		100.0152		236.327		33.225		99.99667		235.895		33.225		100.0022		295.01733		33.225		100.0152		296.51578		33.225		100.02576		297.31745		33.225		100.01634

		237.117		33.25		100.00549		100.01519		236.58099		33.25		100.00215		236.151		33.25		100.00525		295.27033		33.25		100.01519		296.75933		33.25		100.02579		297.56356		33.25		100.01635

		237.379		33.275		100.00628		100.01518		236.83501		33.275		100.0012		236.422		33.275		100.00207		295.52611		33.275		100.01518		297.00278		33.275		100.02581		297.81345		33.275		100.01636

		237.636		33.3		100.00401		100.01518		237.112		33.3		99.99357		236.67999		33.3		100.00299		295.77755		33.3		100.01518		297.24733		33.3		100.02583		298.06245		33.3		100.01637

		237.897		33.325		100.00512		100.01518		237.375		33.325		99.9996		236.937		33.325		99.99973		296.02733		33.325		100.01518		297.49244		33.325		100.02585		298.31311		33.325		100.01637

		238.153		33.35		100.00659		100.01518		237.634		33.35		99.99519		237.205		33.35		99.99909		296.274		33.35		100.01518		297.73666		33.35		100.02587		298.56478		33.35		100.01638

		238.416		33.375		100.00216		100.01518		237.89		33.375		99.99785		237.466		33.375		99.99875		296.52077		33.375		100.01518		297.98422		33.375		100.0259		298.81678		33.375		100.01639

		238.66499		33.4		100.00812		100.01518		238.155		33.4		100.00149		237.72701		33.4		100.00143		296.76633		33.4		100.01518		298.235		33.4		100.02592		299.06889		33.4		100.0164

		238.93401		33.425		100.00744		100.01519		238.405		33.425		99.99679		237.99001		33.425		100.00207		297.01189		33.425		100.01519		298.48311		33.425		100.02594		299.31944		33.425		100.01641

		239.20399		33.45		100.00587		100.01519		238.67999		33.45		100.0025		238.243		33.45		100.00199		297.25578		33.45		100.01519		298.731		33.45		100.02596		299.56811		33.45		100.01641

		239.452		33.475		100.00584		100.01519		238.929		33.475		99.99793		238.507		33.475		100.00465		297.50022		33.475		100.01519		298.98145		33.475		100.02598		299.81755		33.475		100.01642

		239.71899		33.5		100.00418		100.01519		239.19501		33.5		99.99665		238.76601		33.5		100.00541		297.74489		33.5		100.01519		299.23045		33.5		100.026		300.06466		33.5		100.01643

		239.98		33.525		100.00688		100.01518		239.45599		33.525		99.99826		239.028		33.525		100.00012		297.99733		33.525		100.01518		299.47722		33.525		100.02602		300.30933		33.525		100.01644

		240.243		33.55		100.00388		100.01517		239.715		33.55		99.99668		239.28999		33.55		99.99871		298.25133		33.55		100.01517		299.724		33.55		100.02604		300.55389		33.55		100.01644

		240.502		33.575		100.00697		100.01516		239.987		33.575		99.99886		239.556		33.575		99.99952		298.50222		33.575		100.01516		299.96822		33.575		100.02606		300.79644		33.575		100.01645

		240.759		33.6		100.00301		100.01514		240.24899		33.6		99.99602		239.814		33.6		100.00752		298.75333		33.6		100.01514		300.21111		33.6		100.02608		301.03878		33.6		100.01646

		241.01401		33.625		100.00895		100.01511		240.509		33.625		100.00093		240.07899		33.625		100.00443		299.00767		33.625		100.01511		300.45289		33.625		100.0261		301.27411		33.625		100.01647

		241.27699		33.65		100.00393		100.01508		240.76199		33.65		100.00005		240.33299		33.65		99.99764		299.25967		33.65		100.01508		300.69367		33.65		100.02611		301.51533		33.65		100.01648

		241.548		33.675		100.00819		100.01505		241.028		33.675		99.99742		240.604		33.675		100.00286		299.51189		33.675		100.01505		300.93478		33.675		100.02612		301.75922		33.675		100.01648

		241.80099		33.7		100.00795		100.01501		241.28799		33.7		99.99712		240.867		33.7		100.00809		299.76533		33.7		100.01501		301.17522		33.7		100.02613		302.003		33.7		100.01649

		242.058		33.725		100.00453		100.01498		241.55499		33.725		99.99912		241.12801		33.725		100.00151		300.01078		33.725		100.01498		301.41411		33.725		100.02615		302.245		33.725		100.0165

		242.315		33.75		100.00603		100.01494		241.815		33.75		99.99867		241.384		33.75		100.00276		300.25467		33.75		100.01494		301.65689		33.75		100.02616		302.48922		33.75		100.0165

		242.57899		33.775		100.00671		100.0149		242.07201		33.775		99.99614		241.649		33.775		100.00184		300.49678		33.775		100.0149		301.90178		33.775		100.02616		302.73277		33.775		100.01651

		242.83501		33.8		100.00214		100.01486		242.338		33.8		99.99656		241.90401		33.8		100.00365		300.74134		33.8		100.01486		302.14733		33.8		100.02617		302.97766		33.8		100.01652

		243.101		33.825		100.00123		100.01483		242.595		33.825		100.00202		242.168		33.825		100.00388		300.98089		33.825		100.01483		302.39122		33.825		100.02618		303.22233		33.825		100.01653

		243.367		33.85		100.00673		100.0148		242.849		33.85		100.0007		242.433		33.85		100.00367		301.21545		33.85		100.0148		302.63566		33.85		100.02619		303.47144		33.85		100.01654

		243.623		33.875		100.00721		100.01478		243.131		33.875		99.99873		242.69099		33.875		99.99964		301.451		33.875		100.01478		302.88255		33.875		100.0262		303.71433		33.875		100.01654

		243.875		33.9		100.0038		100.01476		243.38901		33.9		100.0017		242.951		33.9		100.0008		301.69023		33.9		100.01476		303.12833		33.9		100.02621		303.95644		33.9		100.01655

		244.12801		33.925		100.00411		100.01475		243.655		33.925		99.9975		243.215		33.925		100.00815		301.92911		33.925		100.01475		303.37322		33.925		100.02622		304.20011		33.925		100.01656

		244.409		33.95		100.00355		100.01474		243.908		33.95		100.00305		243.472		33.95		99.99862		302.17267		33.95		100.01474		303.62334		33.95		100.02623		304.43766		33.95		100.01657

		244.661		33.975		100.00414		100.01474		244.175		33.975		100.00271		243.742		33.975		100.0085		302.41367		33.975		100.01474		303.86711		33.975		100.02625		304.67666		33.975		100.01659

		244.92101		34		100.00875		100.01474		244.43201		34		100.00039		244.00301		34		99.99911		302.65711		34		100.01474		304.10945		34		100.02627		304.91477		34		100.0166

		245.187		34.025		100.00419		100.01475		244.696		34.025		99.9954		244.26601		34.025		100.00561		302.89944		34.025		100.01475		304.35334		34.025		100.02629		305.15144		34.025		100.01661

		245.444		34.05		100.00456		100.01477		244.968		34.05		99.99787		244.528		34.05		100.00834		303.14744		34.05		100.01477		304.59667		34.05		100.02631		305.39011		34.05		100.01663

		245.707		34.075		100.0063		100.01479		245.222		34.075		99.99808		244.78999		34.075		100.00336		303.39556		34.075		100.01479		304.84022		34.075		100.02633		305.62944		34.075		100.01664

		245.96001		34.1		100.00489		100.01481		245.487		34.1		100.00302		245.048		34.1		100.00147		303.64589		34.1		100.01481		305.08433		34.1		100.02635		305.87089		34.1		100.01666

		246.22301		34.125		100.00692		100.01483		245.745		34.125		99.9999		245.314		34.125		100.00287		303.89233		34.125		100.01483		305.33011		34.125		100.02637		306.11266		34.125		100.01668

		246.48801		34.15		100.00884		100.01486		246.013		34.15		100.00015		245.57001		34.15		100.00209		304.13611		34.15		100.01486		305.57667		34.15		100.02639		306.35355		34.15		100.01669

		246.746		34.175		100.00625		100.01488		246.263		34.175		99.99732		245.83		34.175		100.0028		304.37933		34.175		100.01488		305.81933		34.175		100.02641		306.60089		34.175		100.01671

		247.01199		34.2		100.00597		100.0149		246.54201		34.2		99.99728		246.10699		34.2		100.00146		304.62466		34.2		100.0149		306.06733		34.2		100.02643		306.84333		34.2		100.01673

		247.269		34.225		100.00751		100.01493		246.797		34.225		100.00239		246.36501		34.225		100.00264		304.86767		34.225		100.01493		306.316		34.225		100.02645		307.09133		34.225		100.01675

		247.53999		34.25		100.00394		100.01494		247.061		34.25		99.9975		246.627		34.25		100.00354		305.112		34.25		100.01494		306.56111		34.25		100.02648		307.33856		34.25		100.01677

		247.79401		34.275		100.00525		100.01496		247.327		34.275		99.99836		246.897		34.275		100.00312		305.35689		34.275		100.01496		306.80533		34.275		100.0265		307.58467		34.275		100.01679

		248.06		34.3		100.00524		100.01497		247.59		34.3		100.0012		247.161		34.3		100.00131		305.602		34.3		100.01497		307.05144		34.3		100.02652		307.82811		34.3		100.01681

		248.32201		34.325		100.00687		100.01498		247.856		34.325		99.99876		247.41499		34.325		100.0044		305.84567		34.325		100.01498		307.29478		34.325		100.02654		308.07144		34.325		100.01683

		248.58		34.35		100.0076		100.01499		248.12601		34.35		99.99505		247.685		34.35		100.00414		306.09		34.35		100.01499		307.53778		34.35		100.02656		308.31366		34.35		100.01685

		248.841		34.375		100.00527		100.01499		248.37601		34.375		100.00077		247.948		34.375		100.00417		306.338		34.375		100.01499		307.78022		34.375		100.02658		308.55622		34.375		100.01687

		249.112		34.4		100.00793		100.015		248.64101		34.4		99.99658		248.207		34.4		100.00308		306.58533		34.4		100.015		308.02433		34.4		100.0266		308.79878		34.4		100.01689

		249.37		34.425		100.00604		100.015		248.905		34.425		100.0044		248.47301		34.425		100.00662		306.82822		34.425		100.015		308.26522		34.425		100.02662		309.04322		34.425		100.01691

		249.627		34.45		100.00784		100.015		249.159		34.45		99.99918		248.731		34.45		100.00395		307.07333		34.45		100.015		308.50511		34.45		100.02665		309.287		34.45		100.01692

		249.88499		34.475		100.00909		100.015		249.435		34.475		100.00012		248.992		34.475		100.00642		307.31822		34.475		100.015		308.74555		34.475		100.02668		309.53222		34.475		100.01694

		250.14301		34.5		100.00789		100.015		249.687		34.5		100.00083		249.26401		34.5		100.0031		307.56022		34.5		100.015		308.98678		34.5		100.02671		309.77733		34.5		100.01696

		250.40601		34.525		100.00413		100.015		249.95399		34.525		99.99623		249.522		34.525		99.99967		307.80455		34.525		100.015		309.22967		34.525		100.02675		310.02345		34.525		100.01698

		250.67		34.55		100.00573		100.015		250.22301		34.55		99.99596		249.782		34.55		100.00085		308.04544		34.55		100.015		309.47456		34.55		100.02678		310.26823		34.55		100.017

		250.938		34.575		100.0063		100.01501		250.481		34.575		100.00459		250.049		34.575		100.00662		308.28777		34.575		100.01501		309.71711		34.575		100.02682		310.51178		34.575		100.01702

		251.192		34.6		100.00645		100.01502		250.745		34.6		99.99736		250.311		34.6		100.00115		308.52811		34.6		100.01502		309.961		34.6		100.02686		310.75589		34.6		100.01704

		251.45399		34.625		100.00402		100.01504		251.004		34.625		99.99934		250.57201		34.625		100.00164		308.76578		34.625		100.01504		310.20512		34.625		100.02691		311.00089		34.625		100.01706

		251.71201		34.65		100.00738		100.01505		251.271		34.65		99.99892		250.836		34.65		100.00372		309.004		34.65		100.01505		310.44911		34.65		100.02695		311.24523		34.65		100.01708

		251.97501		34.675		100.00935		100.01507		251.52901		34.675		99.99758		251.104		34.675		100.00217		309.24756		34.675		100.01507		310.69434		34.675		100.027		311.48734		34.675		100.0171

		252.241		34.7		100.00341		100.0151		251.8		34.7		99.99859		251.36099		34.7		100.00174		309.49267		34.7		100.0151		310.94033		34.7		100.02704		311.72823		34.7		100.01711

		252.50301		34.725		100.00461		100.01512		252.063		34.725		99.99858		251.63901		34.725		100.00427		309.73589		34.725		100.01512		311.18855		34.725		100.02709		311.971		34.725		100.01713

		252.771		34.75		100.00426		100.01515		252.328		34.75		99.99658		251.905		34.75		100.00439		309.97744		34.75		100.01515		311.429		34.75		100.02714		312.21234		34.75		100.01715

		253.02299		34.775		100.00659		100.01518		252.58299		34.775		100.00036		252.16499		34.775		100.00336		310.22133		34.775		100.01518		311.67378		34.775		100.02718		312.454		34.775		100.01717

		253.291		34.8		100.00578		100.0152		252.849		34.8		99.99942		252.427		34.8		100.00295		310.46289		34.8		100.0152		311.91956		34.8		100.02723		312.69778		34.8		100.01719

		253.55299		34.825		100.00591		100.01523		253.106		34.825		99.99933		252.69099		34.825		100.00361		310.70556		34.825		100.01523		312.16355		34.825		100.02727		312.94123		34.825		100.0172

		253.814		34.85		100.00473		100.01526		253.38		34.85		99.99595		252.95799		34.85		100.0021		310.95089		34.85		100.01526		312.40578		34.85		100.02731		313.18367		34.85		100.01722

		254.078		34.875		100.01001		100.01529		253.64101		34.875		99.99481		253.22701		34.875		100.00393		311.19878		34.875		100.01529		312.64911		34.875		100.02735		313.42778		34.875		100.01723

		254.341		34.9		100.00709		100.01531		253.908		34.9		99.99829		253.47		34.9		100.00337		311.43956		34.9		100.01531		312.893		34.9		100.02738		313.67211		34.9		100.01725

		254.601		34.925		100.00282		100.01533		254.174		34.925		99.99973		253.74001		34.925		100.00457		311.68034		34.925		100.01533		313.13867		34.925		100.02741		313.91767		34.925		100.01727

		254.869		34.95		100.00493		100.01536		254.44		34.95		99.99625		254.006		34.95		100.00191		311.923		34.95		100.01536		313.38356		34.95		100.02744		314.16134		34.95		100.01728

		255.131		34.975		100.00738		100.01538		254.701		34.975		100.00327		254.27299		34.975		100.00403		312.164		34.975		100.01538		313.63267		34.975		100.02747		314.40533		34.975		100.01729

		255.39		35		100.00363		100.01539		254.966		35		100.00032		254.533		35		100.00307		312.40656		35		100.01539		313.88011		35		100.0275		314.65134		35		100.01731

		255.64799		35.025		100.00414		100.01541		255.22701		35.025		99.99485		254.79601		35.025		100.00158		312.65112		35.025		100.01541		314.126		35.025		100.02752		314.89333		35.025		100.01732

		255.91499		35.05		100.00573		100.01542		255.49699		35.05		99.9975		255.054		35.05		100.00121		312.89645		35.05		100.01542		314.37311		35.05		100.02754		315.13822		35.05		100.01733

		256.181		35.075		100.00545		100.01543		255.759		35.075		100.00081		255.313		35.075		100.00327		313.14212		35.075		100.01543		314.62167		35.075		100.02756		315.38177		35.075		100.01734

		256.439		35.1		100.00603		100.01543		256.01599		35.1		100.00163		255.58299		35.1		100.00485		313.38767		35.1		100.01543		314.86811		35.1		100.02758		315.62222		35.1		100.01735

		256.70801		35.125		100.00673		100.01544		256.28799		35.125		99.99695		255.84399		35.125		100.00237		313.63445		35.125		100.01544		315.116		35.125		100.0276		315.86389		35.125		100.01736

		256.97198		35.15		100.00853		100.01544		256.548		35.15		99.99673		256.10901		35.15		100.00153		313.88		35.15		100.01544		315.36133		35.15		100.02761		316.10422		35.15		100.01737

		257.23499		35.175		100.00836		100.01544		256.814		35.175		99.99908		256.37601		35.175		100.0041		314.129		35.175		100.01544		315.60534		35.175		100.02762		316.34633		35.175		100.01738

		257.48499		35.2		100.00337		100.01544		257.069		35.2		100.00066		256.646		35.2		100.00223		314.37778		35.2		100.01544		315.84889		35.2		100.02764		316.59111		35.2		100.0174

		257.74799		35.225		100.00641		100.01544		257.349		35.225		100.00143		256.91		35.225		100.00508		314.62456		35.225		100.01544		316.08789		35.225		100.02765		316.83633		35.225		100.01741

		258.01401		35.25		100.0059		100.01544		257.61301		35.25		100.00005		257.168		35.25		100.0027		314.86878		35.25		100.01544		316.33144		35.25		100.02767		317.085		35.25		100.01742

		258.28		35.275		100.00791		100.01544		257.862		35.275		99.99837		257.444		35.275		100.00241		315.11245		35.275		100.01544		316.57333		35.275		100.02768		317.33178		35.275		100.01743

		258.534		35.3		100.00672		100.01544		258.13501		35.3		99.99695		257.69199		35.3		100.00342		315.35434		35.3		100.01544		316.81644		35.3		100.02769		317.57989		35.3		100.01744

		258.80701		35.325		100.00613		100.01543		258.405		35.325		99.99841		257.96799		35.325		100.00247		315.59611		35.325		100.01543		317.06333		35.325		100.0277		317.82989		35.325		100.01744

		259.06699		35.35		100.00457		100.01543		258.664		35.35		100.00104		258.23499		35.35		100.00357		315.83845		35.35		100.01543		317.30722		35.35		100.02772		318.07411		35.35		100.01745

		259.32999		35.375		100.00373		100.01543		258.922		35.375		99.99259		258.495		35.375		100.00161		316.07711		35.375		100.01543		317.554		35.375		100.02773		318.32422		35.375		100.01746

		259.59399		35.4		100.00664		100.01543		259.19199		35.4		99.99869		258.76199		35.4		100.0044		316.31589		35.4		100.01543		317.79989		35.4		100.02774		318.57111		35.4		100.01747

		259.858		35.425		100.00634		100.01542		259.46701		35.425		100.00142		259.022		35.425		100.00586		316.556		35.425		100.01542		318.04311		35.425		100.02776		318.81456		35.425		100.01748

		260.11401		35.45		100.00435		100.01542		259.715		35.45		99.99323		259.29901		35.45		100.00206		316.79945		35.45		100.01542		318.29055		35.45		100.02777		319.05811		35.45		100.01749

		260.37799		35.475		100.00701		100.01541		259.98999		35.475		99.99748		259.55801		35.475		100.00424		317.04622		35.475		100.01541		318.532		35.475		100.02778		319.29922		35.475		100.01749

		260.63901		35.5		100.00362		100.0154		260.24399		35.5		100.00127		259.82001		35.5		100.00249		317.29178		35.5		100.0154		318.77577		35.5		100.02779		319.53945		35.5		100.0175

		260.90701		35.525		100.00452		100.01539		260.51999		35.525		99.99589		260.07999		35.525		100.00254		317.54011		35.525		100.01539		319.01878		35.525		100.0278		319.78156		35.525		100.0175

		261.16901		35.55		100.00642		100.01537		260.78101		35.55		99.99796		260.35001		35.55		100.00549		317.78667		35.55		100.01537		319.26011		35.55		100.02781		320.02434		35.55		100.0175

		261.43701		35.575		100.00477		100.01536		261.05099		35.575		99.99691		260.61099		35.575		100.0018		318.02955		35.575		100.01536		319.49933		35.575		100.02781		320.27123		35.575		100.0175

		261.69601		35.6		100.00717		100.01534		261.31		35.6		99.99698		260.883		35.6		100.00408		318.27777		35.6		100.01534		319.73766		35.6		100.02782		320.51612		35.6		100.0175

		261.96201		35.625		100.00552		100.01532		261.57999		35.625		99.99993		261.14801		35.625		100.00328		318.52411		35.625		100.01532		319.97911		35.625		100.02782		320.76334		35.625		100.01749

		262.233		35.65		100.00396		100.0153		261.82901		35.65		99.99183		261.40701		35.65		99.99973		318.77144		35.65		100.0153		320.21922		35.65		100.02782		321.01445		35.65		100.01749

		262.48999		35.675		100.00592		100.01528		262.10699		35.675		99.999		261.67899		35.675		100.00385		319.01622		35.675		100.01528		320.45966		35.675		100.02782		321.26267		35.675		100.01749

		262.75101		35.7		100.00452		100.01525		262.37201		35.7		99.99679		261.94699		35.7		100.00298		319.25755		35.7		100.01525		320.70611		35.7		100.02782		321.51378		35.7		100.01748

		263.021		35.725		100.00541		100.01524		262.63501		35.725		99.99645		262.20801		35.725		100.00488		319.49933		35.725		100.01524		320.95144		35.725		100.02782		321.76611		35.725		100.01748

		263.28699		35.75		100.0069		100.01522		262.897		35.75		100.00088		262.47299		35.75		100.00486		319.74022		35.75		100.01522		321.19622		35.75		100.02783		322.01478		35.75		100.01748

		263.54401		35.775		100.00519		100.01521		263.16101		35.775		99.99449		262.729		35.775		100.00211		319.984		35.775		100.01521		321.44188		35.775		100.02783		322.26289		35.775		100.01749

		263.81201		35.8		100.00833		100.0152		263.42599		35.8		100.00054		262.995		35.8		100.00376		320.22544		35.8		100.0152		321.68877		35.8		100.02784		322.51189		35.8		100.01749

		264.073		35.825		100.00493		100.0152		263.68701		35.825		99.99624		263.26199		35.825		100.00203		320.46677		35.825		100.0152		321.93544		35.825		100.02785		322.756		35.825		100.0175

		264.33401		35.85		100.00516		100.0152		263.95999		35.85		99.99607		263.53201		35.85		100.00291		320.71211		35.85		100.0152		322.183		35.85		100.02787		322.99989		35.85		100.01752

		264.599		35.875		100.00532		100.01521		264.229		35.875		99.99895		263.797		35.875		100.00264		320.95633		35.875		100.01521		322.43222		35.875		100.02789		323.24155		35.875		100.01753

		264.854		35.9		100.0074		100.01523		264.48901		35.9		99.99492		264.06201		35.9		100.00134		321.20155		35.9		100.01523		322.68		35.9		100.02791		323.48444		35.9		100.01755

		265.121		35.925		100.00461		100.01525		264.75		35.925		99.99909		264.336		35.925		100.00138		321.44799		35.925		100.01525		322.92545		35.925		100.02794		323.72289		35.925		100.01758

		265.38199		35.95		100.00652		100.01528		265.02802		35.95		99.99514		264.58401		35.95		100.00343		321.69344		35.95		100.01528		323.17178		35.95		100.02797		323.95966		35.95		100.0176

		265.651		35.975		100.00368		100.01531		265.28101		35.975		100.00088		264.85501		35.975		100.00241		321.94088		35.975		100.01531		323.41678		35.975		100.028		324.20366		35.975		100.01763

		265.914		36		100.0039		100.01535		265.54901		36		99.99581		265.10699		36		100.00483		322.18855		36		100.01535		323.66011		36		100.02803		324.44855		36		100.01765

		266.17801		36.025		100.00444		100.01538		265.81299		36.025		100.00001		265.38501		36.025		100.00305		322.43944		36.025		100.01538		323.90311		36.025		100.02806		324.69033		36.025		100.01768

		266.431		36.05		100.00288		100.01542		266.07501		36.05		99.99847		265.65701		36.05		100.00256		322.69011		36.05		100.01542		324.14922		36.05		100.02809		324.93444		36.05		100.0177

		266.69501		36.075		100.00578		100.01545		266.34399		36.075		99.996		265.931		36.075		100.00327		322.938		36.075		100.01545		324.39478		36.075		100.02812		325.17833		36.075		100.01772

		266.96701		36.1		100.00445		100.01549		266.60999		36.1		99.99576		266.19		36.1		100.00139		323.18444		36.1		100.01549		324.64211		36.1		100.02814		325.42455		36.1		100.01774

		267.22501		36.125		100.00514		100.01552		266.87399		36.125		99.99587		266.45401		36.125		100.00174		323.42666		36.125		100.01552		324.88789		36.125		100.02817		325.672		36.125		100.01776

		267.483		36.15		100.00605		100.01555		267.14499		36.15		100.00044		266.72299		36.15		100.00495		323.66666		36.15		100.01555		325.13278		36.15		100.02819		325.92267		36.15		100.01777

		267.75299		36.175		100.00744		100.01557		267.40399		36.175		100.00624		266.97501		36.175		100.00349		323.90855		36.175		100.01557		325.37922		36.175		100.0282		326.17322		36.175		100.01778

		268.02301		36.2		100.00827		100.01559		267.67401		36.2		100.00055		267.242		36.2		100.00424		324.15033		36.2		100.01559		325.626		36.2		100.02822		326.42		36.2		100.01779

		268.293		36.225		100.00664		100.01561		267.94101		36.225		99.99496		267.504		36.225		100.00022		324.39366		36.225		100.01561		325.874		36.225		100.02823		326.66511		36.225		100.01779

		268.54901		36.25		100.0069		100.01562		268.20499		36.25		100.00004		267.76901		36.25		100.00537		324.639		36.25		100.01562		326.12056		36.25		100.02824		326.91256		36.25		100.01779

		268.81		36.275		100.00397		100.01564		268.47299		36.275		99.99896		268.04199		36.275		100.00246		324.88355		36.275		100.01564		326.36823		36.275		100.02825		327.157		36.275		100.0178

		269.08801		36.3		100.00445		100.01565		268.737		36.3		99.99292		268.30301		36.3		99.99895		325.12566		36.3		100.01565		326.61522		36.3		100.02826		327.40078		36.3		100.0178

		269.34201		36.325		100.00487		100.01565		268.99399		36.325		99.99688		268.57199		36.325		100.00087		325.37222		36.325		100.01565		326.85989		36.325		100.02827		327.64256		36.325		100.0178

		269.61099		36.35		100.00723		100.01566		269.26099		36.35		100.00192		268.82901		36.35		100.00283		325.62078		36.35		100.01566		327.10522		36.35		100.02828		327.88345		36.35		100.0178

		269.87		36.375		100.00474		100.01566		269.53299		36.375		100.00058		269.099		36.375		100.00261		325.87245		36.375		100.01566		327.35122		36.375		100.02829		328.12545		36.375		100.0178

		270.14001		36.4		100.00387		100.01566		269.793		36.4		99.995		269.36899		36.4		100.00062		326.12267		36.4		100.01566		327.59445		36.4		100.02831		328.367		36.4		100.0178

		270.40201		36.425		100.00423		100.01566		270.06601		36.425		99.99747		269.63901		36.425		100.00341		326.37344		36.425		100.01566		327.838		36.425		100.02832		328.60889		36.425		100.01781

		270.66		36.45		100.005		100.01566		270.33301		36.45		99.99592		269.90302		36.45		100.0018		326.62256		36.45		100.01566		328.08356		36.45		100.02834		328.85522		36.45		100.01781

		270.93399		36.475		100.00911		100.01566		270.582		36.475		99.99649		270.164		36.475		100.00154		326.86878		36.475		100.01566		328.33222		36.475		100.02836		329.10056		36.475		100.01782

		271.19699		36.5		100.00445		100.01566		270.854		36.5		99.99885		270.43201		36.5		100.00422		327.11467		36.5		100.01566		328.57622		36.5		100.02838		329.34978		36.5		100.01783

		271.44299		36.525		100.00561		100.01565		271.12299		36.525		99.99903		270.69101		36.525		100.00177		327.36089		36.525		100.01565		328.822		36.525		100.0284		329.59823		36.525		100.01783

		271.71399		36.55		100.00558		100.01565		271.38199		36.55		99.99805		270.95999		36.55		100.00272		327.60367		36.55		100.01565		329.071		36.55		100.02842		329.84989		36.55		100.01784

		271.979		36.575		100.00349		100.01566		271.646		36.575		99.9994		271.23099		36.575		100.00258		327.84933		36.575		100.01566		329.31989		36.575		100.02844		330.102		36.575		100.01785

		272.25299		36.6		100.00611		100.01566		271.91299		36.6		99.99527		271.50101		36.6		100.00452		328.09667		36.6		100.01566		329.56689		36.6		100.02847		330.35122		36.6		100.01786

		272.51001		36.625		100.00438		100.01566		272.173		36.625		100.0004		271.763		36.625		100.00338		328.34289		36.625		100.01566		329.81723		36.625		100.02849		330.59966		36.625		100.01788

		272.78101		36.65		100.0014		100.01566		272.43799		36.65		100.00027		272.01999		36.65		100.00226		328.58811		36.65		100.01566		330.06822		36.65		100.02851		330.84911		36.65		100.01789

		273.04001		36.675		100.00311		100.01567		272.71201		36.675		99.99685		272.28699		36.675		100.00153		328.834		36.675		100.01567		330.31645		36.675		100.02853		331.095		36.675		100.0179

		273.30399		36.7		100.00544		100.01568		272.979		36.7		99.99847		272.55399		36.7		100.00497		329.08256		36.7		100.01568		330.56323		36.7		100.02856		331.34088		36.7		100.01791

		273.569		36.725		100.00687		100.01569		273.23801		36.725		99.99847		272.81601		36.725		100.00097		329.329		36.725		100.01569		330.81045		36.725		100.02858		331.58655		36.725		100.01793

		273.83499		36.75		100.00512		100.0157		273.513		36.75		99.99974		273.086		36.75		100.00414		329.57444		36.75		100.0157		331.05578		36.75		100.0286		331.83244		36.75		100.01794

		274.08701		36.775		100.00472		100.01571		273.772		36.775		99.9945		273.35001		36.775		99.99781		329.823		36.775		100.01571		331.29945		36.775		100.02863		332.07678		36.775		100.01795

		274.358		36.8		100.00384		100.01572		274.03601		36.8		99.99772		273.617		36.8		100.0019		330.07133		36.8		100.01572		331.54233		36.8		100.02865		332.32111		36.8		100.01797

		274.62399		36.825		100.00362		100.01573		274.302		36.825		99.99977		273.88101		36.825		100.00213		330.31622		36.825		100.01573		331.79033		36.825		100.02867		332.56767		36.825		100.01798

		274.892		36.85		100.00427		100.01574		274.57001		36.85		99.99545		274.151		36.85		100.00325		330.56211		36.85		100.01574		332.03611		36.85		100.02869		332.81511		36.85		100.01799

		275.14899		36.875		100.00474		100.01575		274.83099		36.875		99.99633		274.414		36.875		100.00079		330.80456		36.875		100.01575		332.28167		36.875		100.02871		333.059		36.875		100.018

		275.41299		36.9		100.00656		100.01576		275.10199		36.9		99.99837		274.68399		36.9		100.00373		331.04678		36.9		100.01576		332.53044		36.9		100.02873		333.30644		36.9		100.01802

		275.67401		36.925		100.00426		100.01577		275.358		36.925		100.00176		274.94		36.925		100.00302		331.28745		36.925		100.01577		332.77855		36.925		100.02875		333.55433		36.925		100.01803

		275.948		36.95		100.00304		100.01578		275.62601		36.95		99.99767		275.22		36.95		100.00369		331.52989		36.95		100.01578		333.02733		36.95		100.02877		333.80167		36.95		100.01804

		276.20801		36.975		100.00527		100.01578		275.89301		36.975		100.00069		275.48801		36.975		100.00342		331.77434		36.975		100.01578		333.27933		36.975		100.02878		334.04944		36.975		100.01805

		276.46799		37		100.00397		100.01578		276.16501		37		99.99389		275.75201		37		100.00232		332.01867		37		100.01578		333.52878		37		100.0288		334.29644		37		100.01806

		276.73499		37.025		100.00787		100.01578		276.43301		37.025		99.99776		276.013		37.025		100.00118		332.26367		37.025		100.01578		333.77989		37.025		100.02882		334.54222		37.025		100.01807

		277.005		37.05		100.00705		100.01578		276.698		37.05		99.99955		276.26901		37.05		100.00734		332.51167		37.05		100.01578		334.02855		37.05		100.02883		334.78789		37.05		100.01808

		277.26999		37.075		100.00617		100.01578		276.96399		37.075		99.99829		276.53699		37.075		100.0024		332.75811		37.075		100.01578		334.27722		37.075		100.02885		335.03145		37.075		100.01808

		277.52899		37.1		100.00541		100.01577		277.22101		37.1		100.00018		276.797		37.1		100.00337		333.00545		37.1		100.01577		334.52511		37.1		100.02887		335.27622		37.1		100.01809

		277.79599		37.125		100.00331		100.01577		277.487		37.125		99.9974		277.073		37.125		99.99936		333.25445		37.125		100.01577		334.77111		37.125		100.02888		335.52133		37.125		100.0181

		278.06699		37.15		100.00232		100.01576		277.76599		37.15		99.9978		277.33401		37.15		100.00062		333.50422		37.15		100.01576		335.01755		37.15		100.0289		335.76677		37.15		100.01811

		278.332		37.175		100.00333		100.01575		278.01901		37.175		99.99821		277.603		37.175		100.00196		333.754		37.175		100.01575		335.26455		37.175		100.02892		336.01311		37.175		100.01811

		278.58899		37.2		100.0065		100.01574		278.284		37.2		99.99848		277.87201		37.2		100.00161		334.00233		37.2		100.01574		335.50922		37.2		100.02894		336.25967		37.2		100.01812

		278.85999		37.225		100.00271		100.01574		278.54901		37.225		99.99551		278.13699		37.225		100.00312		334.24766		37.225		100.01574		335.75899		37.225		100.02896		336.50389		37.225		100.01813

		279.12201		37.25		100.00448		100.01573		278.81201		37.25		99.99694		278.38901		37.25		100.00092		334.49333		37.25		100.01573		336.01055		37.25		100.02898		336.75222		37.25		100.01814

		279.388		37.275		100.00533		100.01572		279.08401		37.275		99.99907		278.66501		37.275		100.00062		334.73633		37.275		100.01572		336.25822		37.275		100.029		336.99934		37.275		100.01814

		279.64899		37.3		100.00341		100.01572		279.354		37.3		99.99988		278.93799		37.3		100.00001		334.98211		37.3		100.01572		336.50555		37.3		100.02902		337.24867		37.3		100.01815

		279.91101		37.325		100.00499		100.01572		279.61301		37.325		99.99822		279.198		37.325		100.00218		335.22744		37.325		100.01572		336.75755		37.325		100.02904		337.49878		37.325		100.01815

		280.17801		37.35		100.00409		100.01572		279.87799		37.35		99.99531		279.47101		37.35		100.00169		335.47322		37.35		100.01572		337.00622		37.35		100.02907		337.74511		37.35		100.01816

		280.44601		37.375		100.00583		100.01572		280.14899		37.375		99.99666		279.73401		37.375		100.00135		335.722		37.375		100.01572		337.25778		37.375		100.02909		337.99222		37.375		100.01817

		280.71201		37.4		100.00681		100.01572		280.422		37.4		99.99874		279.98599		37.4		100.00144		335.97156		37.4		100.01572		337.50833		37.4		100.02911		338.23967		37.4		100.01817

		280.97101		37.425		100.00274		100.01573		280.689		37.425		99.99777		280.25601		37.425		100.00223		336.21878		37.425		100.01573		337.75589		37.425		100.02913		338.48667		37.425		100.01818

		281.237		37.45		100.00532		100.01573		280.94901		37.45		100.00027		280.522		37.45		100.00149		336.46712		37.45		100.01573		338.00267		37.45		100.02916		338.73633		37.45		100.01819

		281.49701		37.475		100.00224		100.01574		281.216		37.475		99.99395		280.80499		37.475		100.00226		336.71667		37.475		100.01574		338.24844		37.475		100.02918		338.98144		37.475		100.01819

		281.76501		37.5		100.00739		100.01575		281.483		37.5		99.9945		281.05801		37.5		100.00094		336.96656		37.5		100.01575		338.49655		37.5		100.0292		339.22722		37.5		100.0182

		282.03299		37.525		100.0078		100.01576		281.74301		37.525		99.99669		281.33099		37.525		100.00263		337.217		37.525		100.01576		338.744		37.525		100.02922		339.47488		37.525		100.0182

		282.29001		37.55		100.01005		100.01577		282.01099		37.55		99.99935		281.595		37.55		100.00651		337.46856		37.55		100.01577		338.98656		37.55		100.02924		339.72133		37.55		100.01821

		282.55701		37.575		100.00516		100.01578		282.27499		37.575		99.99869		281.85699		37.575		100.00118		337.71567		37.575		100.01578		339.22944		37.575		100.02926		339.97111		37.575		100.01821

		282.828		37.6		100.00565		100.0158		282.53699		37.6		99.998		282.11801		37.6		100.0012		337.96245		37.6		100.0158		339.47245		37.6		100.02928		340.22033		37.6		100.01822

		283.09201		37.625		100.00333		100.01581		282.80801		37.625		99.99563		282.38199		37.625		100.00022		338.20667		37.625		100.01581		339.71656		37.625		100.0293		340.467		37.625		100.01822

		283.35501		37.65		100.00497		100.01582		283.07001		37.65		99.99778		282.664		37.65		100.00139		338.45578		37.65		100.01582		339.96634		37.65		100.02931		340.71422		37.65		100.01823

		283.61099		37.675		100.00369		100.01583		283.332		37.675		99.998		282.93201		37.675		100.0007		338.70022		37.675		100.01583		340.213		37.675		100.02932		340.96278		37.675		100.01823

		283.88		37.7		100.00307		100.01584		283.603		37.7		99.99707		283.18201		37.7		100.00255		338.94444		37.7		100.01584		340.45756		37.7		100.02933		341.21222		37.7		100.01824

		284.14401		37.725		100.00214		100.01586		283.875		37.725		99.9976		283.466		37.725		100.00129		339.18822		37.725		100.01586		340.70334		37.725		100.02934		341.46233		37.725		100.01824

		284.41199		37.75		100.00473		100.01587		284.133		37.75		99.99797		283.72501		37.75		100.00368		339.43556		37.75		100.01587		340.94956		37.75		100.02934		341.71178		37.75		100.01824

		284.68201		37.775		100.007		100.01588		284.40399		37.775		99.99657		283.995		37.775		100.00303		339.68256		37.775		100.01588		341.19689		37.775		100.02934		341.96022		37.775		100.01825

		284.94101		37.8		100.00742		100.0159		284.66501		37.8		99.99797		284.25299		37.8		100.00581		339.93144		37.8		100.0159		341.44856		37.8		100.02934		342.20578		37.8		100.01825

		285.21899		37.825		100.00656		100.01591		284.92499		37.825		99.99824		284.51999		37.825		100.00099		340.17833		37.825		100.01591		341.69833		37.825		100.02933		342.45122		37.825		100.01826

		285.48099		37.85		100.00865		100.01593		285.19501		37.85		99.99886		284.78799		37.85		100.00474		340.42722		37.85		100.01593		341.94711		37.85		100.02932		342.698		37.85		100.01826

		285.75201		37.875		100.00597		100.01594		285.46301		37.875		99.99755		285.05301		37.875		100.00283		340.67578		37.875		100.01594		342.19211		37.875		100.02931		342.94188		37.875		100.01826

		286.00101		37.9		100.0046		100.01596		285.728		37.9		99.99815		285.31799		37.9		100.00265		340.927		37.9		100.01596		342.43889		37.9		100.0293		343.18644		37.9		100.01827

		286.25601		37.925		100.00402		100.01598		285.98499		37.925		100.00059		285.591		37.925		100.00172		341.17511		37.925		100.01598		342.68745		37.925		100.02929		343.43389		37.925		100.01827

		286.53699		37.95		100.00508		100.016		286.26099		37.95		99.99766		285.84399		37.95		100.0011		341.42667		37.95		100.016		342.93267		37.95		100.02928		343.67989		37.95		100.01827

		286.793		37.975		100.0062		100.01601		286.50299		37.975		99.99565		286.11499		37.975		100.00392		341.67378		37.975		100.01601		343.18089		37.975		100.02927		343.92555		37.975		100.01827

		287.05701		38		100.00377		100.01603		286.772		38		99.99478		286.38199		38		100.00359		341.92211		38		100.01603		343.43422		38		100.02926		344.17389		38		100.01827

		287.328		38.025		100.00387		100.01605		287.04599		38.025		99.99401		286.63901		38.025		100.00209		342.16789		38.025		100.01605		343.68433		38.025		100.02925		344.42355		38.025		100.01827

		287.58499		38.05		100.00472		100.01607		287.30899		38.05		99.99666		286.91299		38.05		100.0022		342.415		38.05		100.01607		343.93411		38.05		100.02924		344.67444		38.05		100.01827

		287.85001		38.075		100.00766		100.01609		287.57901		38.075		100.00011		287.16901		38.075		100.00335		342.66056		38.075		100.01609		344.18378		38.075		100.02924		344.92566		38.075		100.01827

		288.11499		38.1		100.00549		100.01611		287.84799		38.1		99.99625		287.44299		38.1		100.00202		342.90289		38.1		100.01611		344.437		38.1		100.02924		345.17611		38.1		100.01827

		288.379		38.125		100.00223		100.01613		288.12		38.125		99.99311		287.71301		38.125		100.00098		343.15022		38.125		100.01613		344.68734		38.125		100.02924		345.42422		38.125		100.01827

		288.64999		38.15		100.00601		100.01615		288.38		38.15		99.99638		287.974		38.15		100.00154		343.40067		38.15		100.01615		344.93812		38.15		100.02924		345.67033		38.15		100.01827

		288.90701		38.175		100.00487		100.01617		288.646		38.175		99.99756		288.242		38.175		100.00349		343.65		38.175		100.01617		345.1939		38.175		100.02925		345.91955		38.175		100.01827

		289.17999		38.2		100.00354		100.01619		288.922		38.2		99.99805		288.51001		38.2		100.00406		343.89855		38.2		100.01619		345.44512		38.2		100.02926		346.16666		38.2		100.01827

		289.435		38.225		100.00749		100.01621		289.17499		38.225		99.99797		288.76999		38.225		100.00439		344.14666		38.225		100.01621		345.69334		38.225		100.02927		346.41066		38.225		100.01827

		289.70401		38.25		100.00731		100.01623		289.44601		38.25		99.9962		289.04099		38.25		100.00339		344.39633		38.25		100.01623		345.94279		38.25		100.02928		346.65289		38.25		100.01827

		289.97601		38.275		100.00548		100.01625		289.711		38.275		99.99798		289.30099		38.275		100.00312		344.647		38.275		100.01625		346.19334		38.275		100.02929		346.89789		38.275		100.01826

		290.22699		38.3		100.00376		100.01627		289.98099		38.3		99.99593		289.57101		38.3		100.00161		344.899		38.3		100.01627		346.44201		38.3		100.02931		347.14278		38.3		100.01826

		290.508		38.325		100.00603		100.0163		290.241		38.325		99.99947		289.84299		38.325		100.00197		345.15233		38.325		100.0163		346.685		38.325		100.02932		347.39133		38.325		100.01826

		290.76501		38.35		100.00318		100.01633		290.50299		38.35		99.99721		290.11301		38.35		100.00119		345.40411		38.35		100.01633		346.936		38.35		100.02933		347.64267		38.35		100.01826

		291.04001		38.375		100.00406		100.01635		290.76401		38.375		99.99886		290.37701		38.375		100.00355		345.65189		38.375		100.01635		347.18689		38.375		100.02935		347.89455		38.375		100.01826

		291.29199		38.4		100.00706		100.01638		291.03799		38.4		100.0005		290.64001		38.4		100.00469		345.90067		38.4		100.01638		347.43445		38.4		100.02936		348.145		38.4		100.01826

		291.56601		38.425		100.00778		100.01641		291.298		38.425		99.99934		290.90201		38.425		100.00339		346.15078		38.425		100.01641		347.68312		38.425		100.02937		348.39733		38.425		100.01825

		291.828		38.45		100.00621		100.01643		291.55801		38.45		99.99685		291.172		38.45		100.00298		346.39845		38.45		100.01643		347.93089		38.45		100.02939		348.65122		38.45		100.01825

		292.09299		38.475		100.0055		100.01646		291.836		38.475		99.99885		291.42401		38.475		100.00372		346.64322		38.475		100.01646		348.17922		38.475		100.0294		348.90422		38.475		100.01826

		292.366		38.5		100.00379		100.01649		292.103		38.5		99.99849		291.69601		38.5		100.00336		346.89078		38.5		100.01649		348.42722		38.5		100.02941		349.15433		38.5		100.01826

		292.629		38.525		100.00629		100.01652		292.36499		38.525		99.9981		291.966		38.525		100.00477		347.13878		38.525		100.01652		348.67589		38.525		100.02943		349.40533		38.525		100.01826

		292.90399		38.55		100.00507		100.01655		292.61801		38.55		99.99503		292.242		38.55		100.00091		347.387		38.55		100.01655		348.92711		38.55		100.02944		349.65467		38.55		100.01826

		293.155		38.575		100.00554		100.01657		292.901		38.575		99.99792		292.49301		38.575		100.0022		347.63612		38.575		100.01657		349.17611		38.575		100.02946		349.89856		38.575		100.01826

		293.422		38.6		100.00553		100.0166		293.16101		38.6		99.99617		292.76801		38.6		100.00149		347.88567		38.6		100.0166		349.42056		38.6		100.02947		350.13956		38.6		100.01826

		293.68201		38.625		100.00287		100.01663		293.42801		38.625		99.99471		293.03699		38.625		100.00096		348.13556		38.625		100.01663		349.66678		38.625		100.02949		350.38156		38.625		100.01826

		293.95999		38.65		100.00241		100.01665		293.702		38.65		99.99856		293.29901		38.65		100.00024		348.38467		38.65		100.01665		349.91067		38.65		100.02951		350.62589		38.65		100.01827

		294.22101		38.675		100.00445		100.01668		293.966		38.675		99.99736		293.57101		38.675		99.99949		348.63422		38.675		100.01668		350.15189		38.675		100.02953		350.871		38.675		100.01827

		294.491		38.7		100.00354		100.0167		294.229		38.7		99.99773		293.82901		38.7		100.00098		348.88656		38.7		100.0167		350.39645		38.7		100.02955		351.11811		38.7		100.01827

		294.75101		38.725		100.00349		100.01672		294.48999		38.725		99.99803		294.091		38.725		100.00205		349.13467		38.725		100.01672		350.64045		38.725		100.02957		351.36256		38.725		100.01827

		295.02499		38.75		100.00442		100.01674		294.74799		38.75		99.99684		294.35901		38.75		100.00114		349.38189		38.75		100.01674		350.88611		38.75		100.02958		351.60789		38.75		100.01827

		295.27399		38.775		100.00161		100.01676		295.02301		38.775		99.9934		294.629		38.775		100.00011		349.63122		38.775		100.01676		351.132		38.775		100.0296		351.85433		38.775		100.01827

		295.54501		38.8		100.0059		100.01678		295.28201		38.8		99.99633		294.89801		38.8		100.00211		349.87266		38.8		100.01678		351.37633		38.8		100.02962		352.10366		38.8		100.01827

		295.81601		38.825		100.00362		100.0168		295.55899		38.825		99.99716		295.164		38.825		100.00066		350.11422		38.825		100.0168		351.62467		38.825		100.02963		352.35356		38.825		100.01828

		296.069		38.85		100.00421		100.01682		295.82999		38.85		99.99912		295.42899		38.85		100.00132		350.35411		38.85		100.01682		351.87089		38.85		100.02964		352.60356		38.85		100.01828

		296.33801		38.875		100.00626		100.01683		296.086		38.875		99.99818		295.69601		38.875		100.00479		350.59666		38.875		100.01683		352.12078		38.875		100.02965		352.85067		38.875		100.01828

		296.60101		38.9		100.00587		100.01684		296.35101		38.9		99.9975		295.952		38.9		100.00071		350.84111		38.9		100.01684		352.37244		38.9		100.02966		353.09633		38.9		100.01828

		296.87399		38.925		100.00532		100.01685		296.616		38.925		99.99781		296.23099		38.925		100.00244		351.08511		38.925		100.01685		352.61911		38.925		100.02966		353.339		38.925		100.01828

		297.14301		38.95		100.00435		100.01686		296.888		38.95		100.00087		296.49399		38.95		100.00116		351.32833		38.95		100.01686		352.86777		38.95		100.02967		353.58278		38.95		100.01829

		297.41101		38.975		100.00481		100.01686		297.146		38.975		99.99374		296.75201		38.975		100.00009		351.57311		38.975		100.01686		353.11677		38.975		100.02967		353.82422		38.975		100.01829

		297.67099		39		100.00485		100.01686		297.409		39		99.99713		297.02301		39		100.00208		351.81644		39		100.01686		353.36333		39		100.02967		354.06433		39		100.01829

		297.935		39.025		100.00477		100.01686		297.67899		39.025		99.99788		297.29199		39.025		100.00154		352.065		39.025		100.01686		353.61022		39.025		100.02967		354.305		39.025		100.0183

		298.19901		39.05		100.00411		100.01685		297.94501		39.05		99.99792		297.55399		39.05		100.00096		352.31433		39.05		100.01685		353.85433		39.05		100.02967		354.54956		39.05		100.0183

		298.46201		39.075		100.00518		100.01684		298.21201		39.075		99.99767		297.815		39.075		100.00368		352.56222		39.075		100.01684		354.09933		39.075		100.02968		354.79167		39.075		100.0183

		298.72601		39.1		100.00311		100.01682		298.491		39.1		99.99676		298.08301		39.1		100.00479		352.80811		39.1		100.01682		354.34366		39.1		100.02968		355.03367		39.1		100.01831

		298.995		39.125		100.00573		100.0168		298.74899		39.125		99.99968		298.353		39.125		100.0032		353.055		39.125		100.0168		354.58755		39.125		100.02969		355.27745		39.125		100.01831

		299.26001		39.15		100.0025		100.01678		299.01001		39.15		99.99651		298.62		39.15		100.00162		353.30166		39.15		100.01678		354.836		39.15		100.0297		355.52234		39.15		100.01832

		299.52399		39.175		100.00326		100.01676		299.28101		39.175		99.99575		298.87601		39.175		100.00213		353.54988		39.175		100.01676		355.07933		39.175		100.02971		355.76634		39.175		100.01832

		299.784		39.2		100.00401		100.01673		299.539		39.2		99.99633		299.16101		39.2		100.00139		353.79522		39.2		100.01673		355.32267		39.2		100.02973		356.01222		39.2		100.01832

		300.048		39.225		100.00428		100.01671		299.81799		39.225		99.99717		299.40799		39.225		100.00209		354.03755		39.225		100.01671		355.56722		39.225		100.02975		356.25778		39.225		100.01833

		300.32401		39.25		100.00436		100.01668		300.07501		39.25		99.99845		299.67801		39.25		100.00281		354.28066		39.25		100.01668		355.81123		39.25		100.02976		356.50411		39.25		100.01833

		300.58499		39.275		100.00301		100.01666		300.34299		39.275		99.99668		299.94199		39.275		100.00131		354.52555		39.275		100.01666		356.05656		39.275		100.02978		356.74489		39.275		100.01833

		300.849		39.3		100.00428		100.01664		300.60501		39.3		99.99699		300.215		39.3		100.00008		354.77011		39.3		100.01664		356.30423		39.3		100.0298		356.98778		39.3		100.01833

		301.11801		39.325		100.00237		100.01663		300.87399		39.325		99.99569		300.48401		39.325		100.00036		355.015		39.325		100.01663		356.54922		39.325		100.02982		357.23111		39.325		100.01833

		301.37601		39.35		100.00173		100.01661		301.14499		39.35		99.99575		300.74301		39.35		100.00182		355.26078		39.35		100.01661		356.79411		39.35		100.02984		357.47067		39.35		100.01833

		301.64499		39.375		100.00383		100.0166		301.39801		39.375		99.99537		301.01599		39.375		99.99934		355.50667		39.375		100.0166		357.03711		39.375		100.02986		357.70967		39.375		100.01834

		301.91101		39.4		100.00295		100.0166		301.672		39.4		99.99672		301.27802		39.4		100.00235		355.75056		39.4		100.0166		357.28256		39.4		100.02987		357.95422		39.4		100.01834

		302.17499		39.425		100.00262		100.0166		301.935		39.425		99.99459		301.552		39.425		100.00111		355.998		39.425		100.0166		357.52711		39.425		100.02989		358.19844		39.425		100.01834

		302.448		39.45		100.00311		100.0166		302.19299		39.45		99.99693		301.823		39.45		100.00215		356.24756		39.45		100.0166		357.77134		39.45		100.0299		358.44466		39.45		100.01834

		302.716		39.475		100.00562		100.0166		302.46701		39.475		99.99811		302.08099		39.475		100.00419		356.49678		39.475		100.0166		358.01822		39.475		100.02991		358.68855		39.475		100.01834

		302.97601		39.5		100.00419		100.0166		302.733		39.5		99.99541		302.354		39.5		100.00036		356.74322		39.5		100.0166		358.26878		39.5		100.02992		358.93689		39.5		100.01834

		303.23901		39.525		100.00485		100.01661		302.99899		39.525		99.99718		302.61301		39.525		100.00102		356.99067		39.525		100.01661		358.51745		39.525		100.02993		359.18278		39.525		100.01834

		303.49701		39.55		100.00487		100.01662		303.26599		39.55		99.99465		302.87		39.55		100.00186		357.23822		39.55		100.01662		358.76745		39.55		100.02994		359.42933		39.55		100.01834

		303.76001		39.575		100.00388		100.01664		303.534		39.575		99.99751		303.159		39.575		100.00205		357.48111		39.575		100.01664		359.01778		39.575		100.02994		359.67878		39.575		100.01834

		304.035		39.6		100.00208		100.01665		303.789		39.6		99.99563		303.414		39.6		100.00319		357.72277		39.6		100.01665		359.26889		39.6		100.02995		359.92933		39.6		100.01834

		304.30399		39.625		100.00297		100.01666		304.05801		39.625		99.99864		303.68399		39.625		100.00333		357.96822		39.625		100.01666		359.51734		39.625		100.02996		360.17467		39.625		100.01834

		304.57001		39.65		100.00422		100.01668		304.32401		39.65		99.99629		303.953		39.65		100.00251		358.21566		39.65		100.01668		359.76489		39.65		100.02997		360.41978		39.65		100.01834

		304.83401		39.675		100.00608		100.0167		304.60101		39.675		99.99808		304.21899		39.675		100.00054		358.46389		39.675		100.0167		360.01345		39.675		100.02998		360.66445		39.675		100.01834

		305.104		39.7		100.00389		100.01672		304.85599		39.7		99.99856		304.48001		39.7		100.00051		358.709		39.7		100.01672		360.25645		39.7		100.02999		360.90811		39.7		100.01835

		305.362		39.725		100.0047		100.01674		305.12701		39.725		99.99934		304.75201		39.725		100.00273		358.95722		39.725		100.01674		360.499		39.725		100.03001		361.14656		39.725		100.01835

		305.625		39.75		100.00381		100.01676		305.38901		39.75		99.9962		305.022		39.75		100.00096		359.20534		39.75		100.01676		360.742		39.75		100.03002		361.38933		39.75		100.01836

		305.89801		39.775		100.00377		100.01679		305.65799		39.775		99.99519		305.29099		39.775		100.00221		359.452		39.775		100.01679		360.98422		39.775		100.03003		361.62789		39.775		100.01836

		306.15201		39.8		100.00165		100.01681		305.92999		39.8		99.99669		305.55899		39.8		100.00358		359.70322		39.8		100.01681		361.22667		39.8		100.03005		361.87045		39.8		100.01837

		306.414		39.825		100.00578		100.01684		306.19501		39.825		99.99822		305.81299		39.825		100.00354		359.955		39.825		100.01684		361.46667		39.825		100.03006		362.11278		39.825		100.01838

		306.68799		39.85		100.0063		100.01687		306.45801		39.85		100.00071		306.08401		39.85		100.00347		360.20256		39.85		100.01687		361.71067		39.85		100.03007		362.35711		39.85		100.01839

		306.95401		39.875		100.00389		100.01689		306.72601		39.875		99.99553		306.354		39.875		99.9995		360.44733		39.875		100.01689		361.95911		39.875		100.03008		362.60044		39.875		100.0184

		307.215		39.9		100.00362		100.01692		306.97501		39.9		99.99423		306.61899		39.9		100.001		360.69078		39.9		100.01692		362.20589		39.9		100.03009		362.84489		39.9		100.01841

		307.48999		39.925		100.00114		100.01695		307.258		39.925		99.99761		306.88901		39.925		100.00163		360.93866		39.925		100.01695		362.458		39.925		100.0301		363.09156		39.925		100.01843

		307.75601		39.95		100.00249		100.01697		307.52301		39.95		99.99454		307.14099		39.95		100.00122		361.17866		39.95		100.01697		362.70722		39.95		100.03011		363.34033		39.95		100.01844

		308.02301		39.975		100.00363		100.017		307.797		39.975		99.99535		307.41199		39.975		100.00305		361.41955		39.975		100.017		362.95334		39.975		100.03011		363.58833		39.975		100.01845

		308.29099		40		100.00683		100.01702		308.05399		40		99.99871		307.67801		40		100.00316		361.65977		40		100.01702		363.20034		40		100.03011		363.84011		40		100.01846

		308.54599		40.025		100.00472		100.01704		308.32901		40.025		99.99547		307.95001		40.025		100.00119		361.90255		40.025		100.01704		363.44678		40.025		100.03011		364.08855		40.025		100.01846

		308.82501		40.05		100.00398		100.01705		308.59201		40.05		99.99605		308.215		40.05		100.00328		362.14622		40.05		100.01705		363.69567		40.05		100.03011		364.33633		40.05		100.01847

		309.08499		40.075		100.00443		100.01707		308.849		40.075		99.99729		308.479		40.075		100.00228		362.39389		40.075		100.01707		363.94256		40.075		100.03011		364.58077		40.075		100.01848

		309.34399		40.1		100.00552		100.01708		309.117		40.1		99.9965		308.73599		40.1		99.99889		362.63945		40.1		100.01708		364.18645		40.1		100.0301		364.82611		40.1		100.01848

		309.621		40.125		100.00223		100.01708		309.383		40.125		99.99701		309.01501		40.125		100.00036		362.88511		40.125		100.01708		364.43123		40.125		100.0301		365.06744		40.125		100.01848

		309.88101		40.15		100.00288		100.01709		309.64899		40.15		99.99641		309.28799		40.15		100.00203		363.12912		40.15		100.01709		364.67067		40.15		100.0301		365.307		40.15		100.01848

		310.14401		40.175		100.00415		100.01709		309.91901		40.175		99.9965		309.54199		40.175		100.00233		363.38023		40.175		100.01709		364.91245		40.175		100.0301		365.55055		40.175		100.01848

		310.40399		40.2		100.00176		100.01709		310.186		40.2		99.99848		309.814		40.2		100.00123		363.63056		40.2		100.01709		365.15523		40.2		100.0301		365.79344		40.2		100.01848

		310.67099		40.225		100.00448		100.01708		310.461		40.225		99.99797		310.07401		40.225		100.00027		363.88301		40.225		100.01708		365.40067		40.225		100.0301		366.03522		40.225		100.01848

		310.94501		40.25		100.00296		100.01708		310.716		40.25		99.99787		310.35199		40.25		100.00058		364.13201		40.25		100.01708		365.64845		40.25		100.03011		366.27611		40.25		100.01848

		311.20001		40.275		100.005		100.01707		310.98199		40.275		99.99788		310.612		40.275		100.00212		364.37989		40.275		100.01707		365.89589		40.275		100.03011		366.51833		40.275		100.01847

		311.46701		40.3		100.00372		100.01707		311.23999		40.3		99.99521		310.879		40.3		100.00078		364.62289		40.3		100.01707		366.14411		40.3		100.03012		366.76167		40.3		100.01847

		311.733		40.325		100.00569		100.01706		311.51401		40.325		99.99678		311.146		40.325		100.00269		364.86567		40.325		100.01706		366.39133		40.325		100.03013		367.00378		40.325		100.01847

		311.99701		40.35		100.00364		100.01706		311.78		40.35		99.99722		311.40799		40.35		99.99945		365.10723		40.35		100.01706		366.63877		40.35		100.03014		367.25112		40.35		100.01847

		312.263		40.375		100.00266		100.01705		312.05301		40.375		99.99627		311.67499		40.375		100.00275		365.34811		40.375		100.01705		366.88899		40.375		100.03015		367.49911		40.375		100.01847

		312.53799		40.4		100.00308		100.01705		312.323		40.4		99.99562		311.94699		40.4		100.00157		365.59045		40.4		100.01705		367.13944		40.4		100.03017		367.74222		40.4		100.01847

		312.79599		40.425		100.00318		100.01705		312.58301		40.425		99.99614		312.207		40.425		100.00245		365.83601		40.425		100.01705		367.39199		40.425		100.03018		367.98145		40.425		100.01847

		313.065		40.45		100.0038		100.01705		312.854		40.45		99.99804		312.478		40.45		100.00246		366.08156		40.45		100.01705		367.64122		40.45		100.0302		368.22378		40.45		100.01848

		313.34201		40.475		100.00198		100.01706		313.10999		40.475		99.99423		312.742		40.475		100.0021		366.32423		40.475		100.01706		367.88677		40.475		100.03022		368.46811		40.475		100.01848

		313.59698		40.5		100.00313		100.01707		313.383		40.5		99.99505		313.008		40.5		100.00043		366.56745		40.5		100.01707		368.12777		40.5		100.03024		368.70934		40.5		100.01849

		313.85001		40.525		100.00533		100.01708		313.64999		40.525		99.99586		313.27399		40.525		100.00203		366.81245		40.525		100.01708		368.37266		40.525		100.03026		368.95023		40.525		100.0185

		314.12399		40.55		100.00404		100.01709		313.91501		40.55		99.99796		313.53299		40.55		100.00171		367.05822		40.55		100.01709		368.61733		40.55		100.03028		369.19589		40.55		100.01851

		314.39301		40.575		100.00223		100.01711		314.17999		40.575		99.99362		313.80701		40.575		100.00146		367.30778		40.575		100.01711		368.86033		40.575		100.0303		369.44022		40.575		100.01852

		314.65701		40.6		100.00491		100.01713		314.44901		40.6		99.9964		314.07001		40.6		99.9992		367.55856		40.6		100.01713		369.10366		40.6		100.03033		369.686		40.6		100.01853

		314.92499		40.625		100.00567		100.01715		314.711		40.625		99.99682		314.33301		40.625		100.00319		367.80467		40.625		100.01715		369.34966		40.625		100.03035		369.93411		40.625		100.01854

		315.19199		40.65		100.0047		100.01717		314.97501		40.65		99.99612		314.608		40.65		100.00247		368.04933		40.65		100.01717		369.59689		40.65		100.03037		370.18389		40.65		100.01855

		315.44901		40.675		100.00238		100.01719		315.23901		40.675		99.99581		314.88501		40.675		100.00096		368.29211		40.675		100.01719		369.84255		40.675		100.03039		370.43145		40.675		100.01856

		315.711		40.7		100.0046		100.01722		315.517		40.7		99.99787		315.146		40.7		100.00166		368.53667		40.7		100.01722		370.08922		40.7		100.03041		370.67856		40.7		100.01858

		315.979		40.725		100.00346		100.01724		315.78101		40.725		99.99606		315.41501		40.725		100.00084		368.78122		40.725		100.01724		370.339		40.725		100.03043		370.92856		40.725		100.01859

		316.25201		40.75		100.0002		100.01727		316.047		40.75		99.99232		315.681		40.75		99.99961		369.02133		40.75		100.01727		370.587		40.75		100.03045		371.18011		40.75		100.0186

		316.51401		40.775		100.00305		100.01729		316.31601		40.775		99.99749		315.94		40.775		100.00198		369.26789		40.775		100.01729		370.83633		40.775		100.03047		371.42567		40.775		100.01861

		316.77701		40.8		100.00444		100.01731		316.577		40.8		99.99853		316.21201		40.8		100.001		369.516		40.8		100.01731		371.08467		40.8		100.03048		371.671		40.8		100.01862

		317.04901		40.825		100.00415		100.01733		316.84299		40.825		99.9972		316.47299		40.825		100.00442		369.76256		40.825		100.01733		371.33056		40.825		100.0305		371.91556		40.825		100.01863

		317.30301		40.85		100.00497		100.01735		317.112		40.85		99.99833		316.755		40.85		100.00176		370.01045		40.85		100.01735		371.57367		40.85		100.03051		372.15711		40.85		100.01864

		317.57401		40.875		100.00229		100.01736		317.384		40.875		99.99455		317.01501		40.875		100.00184		370.26		40.875		100.01736		371.81356		40.875		100.03052		372.39789		40.875		100.01864

		317.841		40.9		100.00193		100.01737		317.64499		40.9		99.99558		317.289		40.9		100.003		370.50789		40.9		100.01737		372.05689		40.9		100.03053		372.64022		40.9		100.01865

		318.099		40.925		100.00263		100.01738		317.91		40.925		99.99635		317.54999		40.925		100.00183		370.75645		40.925		100.01738		372.3		40.925		100.03055		372.88167		40.925		100.01865

		318.37799		40.95		100.00266		100.01738		318.17599		40.95		99.99543		317.82401		40.95		100.00066		371.00555		40.95		100.01738		372.54089		40.95		100.03056		373.12545		40.95		100.01866

		318.62299		40.975		100.0038		100.01738		318.42999		40.975		99.99722		318.08701		40.975		100.00055		371.25967		40.975		100.01738		372.78356		40.975		100.03057		373.369		40.975		100.01867

		318.901		41		100.00451		100.01738		318.711		41		99.99623		318.33899		41		100.00138		371.50622		41		100.01738		373.02745		41		100.03058		373.61711		41		100.01867

		319.16599		41.025		100.00329		100.01737		318.979		41.025		99.99674		318.616		41.025		100.0009		371.74944		41.025		100.01737		373.27301		41.025		100.0306		373.86478		41.025		100.01868

		319.431		41.05		100.00339		100.01737		319.24799		41.05		99.99694		318.867		41.05		100.00081		371.996		41.05		100.01737		373.52056		41.05		100.03061		374.11156		41.05		100.01868

		319.69901		41.075		100.00427		100.01735		319.517		41.075		99.99586		319.14999		41.075		100.00001		372.241		41.075		100.01735		373.76845		41.075		100.03062		374.36256		41.075		100.01869

		319.95999		41.1		100.00368		100.01734		319.77802		41.1		99.99611		319.414		41.1		100.00092		372.48344		41.1		100.01734		374.01678		41.1		100.03064		374.612		41.1		100.01869

		320.23801		41.125		100.00456		100.01733		320.05499		41.125		99.99707		319.67999		41.125		100.00176		372.72933		41.125		100.01733		374.265		41.125		100.03065		374.86211		41.125		100.0187

		320.495		41.15		100.0038		100.01731		320.31601		41.15		99.99595		319.93799		41.15		100.00185		372.97578		41.15		100.01731		374.51211		41.15		100.03066		375.11244		41.15		100.01871

		320.76401		41.175		100.00635		100.0173		320.57901		41.175		99.99787		320.20801		41.175		100.00364		373.22311		41.175		100.0173		374.76122		41.175		100.03067		375.35855		41.175		100.01872

		321.02701		41.2		100.00274		100.01729		320.84399		41.2		99.99546		320.47299		41.2		100.00163		373.46756		41.2		100.01729		375.00667		41.2		100.03069		375.603		41.2		100.01873

		321.298		41.225		100.00535		100.01728		321.116		41.225		99.99554		320.74399		41.225		100.00157		373.71578		41.225		100.01728		375.24978		41.225		100.0307		375.84078		41.225		100.01874

		321.561		41.25		100.00282		100.01726		321.37799		41.25		99.99651		321.00699		41.25		100.00096		373.96311		41.25		100.01726		375.49233		41.25		100.03071		376.08133		41.25		100.01875

		321.82599		41.275		100.00366		100.01725		321.642		41.275		99.99596		321.26199		41.275		100.00155		374.20589		41.275		100.01725		375.73522		41.275		100.03072		376.32		41.275		100.01875

		322.07901		41.3		100.00221		100.01725		321.91599		41.3		99.99649		321.54999		41.3		100.00167		374.44823		41.3		100.01725		375.97567		41.3		100.03073		376.55978		41.3		100.01876

		322.35901		41.325		100.00422		100.01724		322.185		41.325		99.99616		321.806		41.325		100.00105		374.69156		41.325		100.01724		376.21722		41.325		100.03074		376.80189		41.325		100.01877

		322.621		41.35		100.00224		100.01724		322.44101		41.35		99.99667		322.08499		41.35		100.00008		374.93212		41.35		100.01724		376.45911		41.35		100.03075		377.04211		41.35		100.01877

		322.88699		41.375		100.00147		100.01724		322.71301		41.375		99.99673		322.34		41.375		100.00164		375.17222		41.375		100.01724		376.70611		41.375		100.03076		377.28234		41.375		100.01878

		323.159		41.4		100.00045		100.01724		322.979		41.4		99.99398		322.60999		41.4		100.00221		375.41111		41.4		100.01724		376.95222		41.4		100.03077		377.52544		41.4		100.01878

		323.422		41.425		100.00333		100.01724		323.24399		41.425		99.9965		322.87601		41.425		100.00366		375.65056		41.425		100.01724		377.19956		41.425		100.03078		377.77033		41.425		100.01878

		323.69199		41.45		100.0039		100.01725		323.509		41.45		99.99773		323.14099		41.45		100.00171		375.88978		41.45		100.01725		377.44611		41.45		100.03079		378.01911		41.45		100.01877

		323.95599		41.475		100.00303		100.01726		323.78201		41.475		99.99481		323.41		41.475		100.00297		376.132		41.475		100.01726		377.69356		41.475		100.0308		378.26723		41.475		100.01877

		324.22101		41.5		100.00442		100.01727		324.04501		41.5		99.99688		323.67599		41.5		100.00153		376.37633		41.5		100.01727		377.93855		41.5		100.03081		378.51745		41.5		100.01877

		324.48099		41.525		100.00138		100.01728		324.31299		41.525		99.99867		323.935		41.525		100.00054		376.62433		41.525		100.01728		378.186		41.525		100.03082		378.76489		41.525		100.01876

		324.746		41.55		100.00519		100.01729		324.578		41.55		99.99657		324.21201		41.55		100.00162		376.86989		41.55		100.01729		378.434		41.55		100.03083		379.01156		41.55		100.01876

		325.01501		41.575		100.00267		100.01731		324.84		41.575		99.99503		324.47198		41.575		100.00013		377.11822		41.575		100.01731		378.68134		41.575		100.03085		379.25755		41.575		100.01875

		325.28799		41.6		100.00421		100.01732		325.10999		41.6		99.99671		324.73901		41.6		100.00197		377.36744		41.6		100.01732		378.92389		41.6		100.03086		379.50311		41.6		100.01875

		325.55701		41.625		100.00215		100.01734		325.367		41.625		99.99551		325.01001		41.625		100.00164		377.61544		41.625		100.01734		379.16744		41.625		100.03087		379.74667		41.625		100.01875

		325.80801		41.65		100.0041		100.01736		325.642		41.65		99.99925		325.27899		41.65		100.0016		377.86355		41.65		100.01736		379.40644		41.65		100.03088		379.98912		41.65		100.01875

		326.086		41.675		100.00236		100.01737		325.901		41.675		99.99456		325.547		41.675		100.001		378.11066		41.675		100.01737		379.64778		41.675		100.0309		380.23312		41.675		100.01875

		326.34601		41.7		100.00334		100.01739		326.17599		41.7		99.99622		325.80099		41.7		100.00204		378.35466		41.7		100.01739		379.89		41.7		100.03091		380.47867		41.7		100.01875

		326.61301		41.725		100.00206		100.01741		326.45001		41.725		99.99557		326.07999		41.725		100.00027		378.59888		41.725		100.01741		380.13011		41.725		100.03093		380.72412		41.725		100.01876

		326.87299		41.75		100.00185		100.01742		326.703		41.75		99.99771		326.34		41.75		100.00133		378.84233		41.75		100.01742		380.372		41.75		100.03094		380.96978		41.75		100.01876

		327.13501		41.775		100.00673		100.01744		326.97101		41.775		99.99811		326.60599		41.775		100.00176		379.08355		41.775		100.01744		380.61589		41.775		100.03096		381.21612		41.775		100.01877

		327.41101		41.8		100.00516		100.01746		327.23199		41.8		99.9966		326.884		41.8		100.00236		379.32688		41.8		100.01746		380.85877		41.8		100.03098		381.46356		41.8		100.01878

		327.66101		41.825		100.00267		100.01748		327.50699		41.825		99.99634		327.14899		41.825		100.0006		379.568		41.825		100.01748		381.10411		41.825		100.031		381.71034		41.825		100.01878

		327.93301		41.85		100.0029		100.0175		327.77701		41.85		99.99712		327.41501		41.85		100.00266		379.81111		41.85		100.0175		381.34911		41.85		100.03102		381.961		41.85		100.01879

		328.194		41.875		100.00212		100.01752		328.03601		41.875		99.99646		327.67499		41.875		100.00059		380.05489		41.875		100.01752		381.60078		41.875		100.03104		382.21189		41.875		100.0188

		328.466		41.9		100.00607		100.01754		328.30899		41.9		99.99679		327.94601		41.9		100.00319		380.29933		41.9		100.01754		381.85167		41.9		100.03107		382.46011		41.9		100.01881

		328.73999		41.925		100.00503		100.01756		328.57101		41.925		99.99683		328.216		41.925		100.00251		380.54678		41.925		100.01756		382.10134		41.925		100.0311		382.70733		41.925		100.01882

		329.00601		41.95		100.00282		100.01759		328.82901		41.95		99.99655		328.483		41.95		99.99998		380.79423		41.95		100.01759		382.35222		41.95		100.03113		382.956		41.95		100.01883

		329.26599		41.975		100.00301		100.01761		329.09201		41.975		99.9958		328.745		41.975		99.99973		381.04456		41.975		100.01761		382.60134		41.975		100.03116		383.20389		41.975		100.01884

		329.534		42		100.00073		100.01763		329.371		42		99.99765		329.009		42		100.00109		381.29534		42		100.01763		382.84756		42		100.0312		383.45223		42		100.01885

		329.80099		42.025		100.00335		100.01766		329.63501		42.025		99.99804		329.29099		42.025		100.00181		381.54489		42.025		100.01766		383.09467		42.025		100.03123		383.69834		42.025		100.01886

		330.06299		42.05		100.00333		100.01768		329.90799		42.05		99.99859		329.54901		42.05		100.00244		381.79222		42.05		100.01768		383.33911		42.05		100.03127		383.94845		42.05		100.01887

		330.33899		42.075		100.0024		100.0177		330.17401		42.075		99.99642		329.81799		42.075		100.00065		382.03811		42.075		100.0177		383.58445		42.075		100.03131		384.19889		42.075		100.01887

		330.59601		42.1		100.00453		100.01772		330.43399		42.1		99.9938		330.08899		42.1		100.00024		382.28544		42.1		100.01772		383.82722		42.1		100.03135		384.44889		42.1		100.01888

		330.86499		42.125		100.00304		100.01774		330.702		42.125		99.99394		330.35599		42.125		100.00154		382.53278		42.125		100.01774		384.07455		42.125		100.03139		384.69945		42.125		100.01889

		331.13501		42.15		100.00363		100.01776		330.97		42.15		99.99712		330.62		42.15		100.00116		382.78133		42.15		100.01776		384.32355		42.15		100.03142		384.95001		42.15		100.01889

		331.39899		42.175		100.00235		100.01778		331.23599		42.175		99.99786		330.884		42.175		100.00088		383.02889		42.175		100.01778		384.574		42.175		100.03146		385.19834		42.175		100.0189

		331.66699		42.2		100.00352		100.01779		331.49799		42.2		99.99693		331.15701		42.2		100.00134		383.27289		42.2		100.01779		384.82311		42.2		100.03149		385.44756		42.2		100.0189

		331.92599		42.225		100.00417		100.0178		331.76501		42.225		99.99665		331.41299		42.225		100.00155		383.51689		42.225		100.0178		385.07467		42.225		100.03153		385.69611		42.225		100.01891

		332.19299		42.25		100.00355		100.01781		332.03101		42.25		99.99585		331.68399		42.25		100.00157		383.76111		42.25		100.01781		385.32589		42.25		100.03156		385.94556		42.25		100.01891

		332.45599		42.275		100.00364		100.01782		332.29199		42.275		99.99826		331.94699		42.275		100.00307		384.01178		42.275		100.01782		385.58011		42.275		100.03159		386.18967		42.275		100.01891

		332.71899		42.3		100.00148		100.01783		332.57001		42.3		99.99461		332.22101		42.3		99.99966		384.265		42.3		100.01783		385.83244		42.3		100.03162		386.43056		42.3		100.01891

		332.99899		42.325		100.00214		100.01783		332.82999		42.325		99.9963		332.48401		42.325		100.00299		384.51667		42.325		100.01783		386.08544		42.325		100.03164		386.67189		42.325		100.01892

		333.25299		42.35		100.00563		100.01784		333.095		42.35		99.99412		332.75101		42.35		100.00204		384.76711		42.35		100.01784		386.33378		42.35		100.03167		386.91333		42.35		100.01892

		333.51901		42.375		100.00449		100.01784		333.367		42.375		99.99611		333.01801		42.375		100.00228		385.01711		42.375		100.01784		386.57922		42.375		100.03169		387.15289		42.375		100.01892

		333.785		42.4		100.00301		100.01784		333.64099		42.4		99.99669		333.29501		42.4		100.00165		385.26623		42.4		100.01784		386.82411		42.4		100.03171		387.39255		42.4		100.01893

		334.052		42.425		100.00269		100.01785		333.90799		42.425		99.99491		333.54501		42.425		100.00229		385.517		42.425		100.01785		387.06956		42.425		100.03173		387.63289		42.425		100.01893

		334.31601		42.45		100.00546		100.01785		334.16901		42.45		99.99826		333.82401		42.45		100.00309		385.76922		42.45		100.01785		387.311		42.45		100.03176		387.87711		42.45		100.01894

		334.58701		42.475		100.00341		100.01786		334.41599		42.475		99.99653		334.08499		42.475		100.00086		386.02211		42.475		100.01786		387.55056		42.475		100.03178		388.12145		42.475		100.01895

		334.84799		42.5		100.00255		100.01787		334.70599		42.5		99.99653		334.35001		42.5		100.00061		386.27022		42.5		100.01787		387.79311		42.5		100.0318		388.36845		42.5		100.01895

		335.12		42.525		100.00219		100.01788		334.96899		42.525		99.99492		334.61301		42.525		100.00095		386.51389		42.525		100.01788		388.03889		42.525		100.03181		388.615		42.525		100.01896

		335.37799		42.55		100.0027		100.01789		335.23599		42.55		99.99864		334.88199		42.55		100.0013		386.75922		42.55		100.01789		388.28345		42.55		100.03183		388.86078		42.55		100.01898

		335.647		42.575		100.00147		100.01791		335.50601		42.575		99.99432		335.142		42.575		100.00107		387.00256		42.575		100.01791		388.52767		42.575		100.03185		389.10645		42.575		100.01899

		335.92001		42.6		100.00387		100.01793		335.76599		42.6		99.9965		335.422		42.6		100.00105		387.24267		42.6		100.01793		388.77434		42.6		100.03187		389.35312		42.6		100.01901

		336.18399		42.625		100.00389		100.01795		336.035		42.625		99.99895		335.68701		42.625		100.00238		387.48444		42.625		100.01795		389.02278		42.625		100.03188		389.60056		42.625		100.01903

		336.444		42.65		100.00295		100.01798		336.29501		42.65		99.99505		335.95001		42.65		100.00182		387.72689		42.65		100.01798		389.26945		42.65		100.0319		389.84889		42.65		100.01905

		336.707		42.675		100.00351		100.01801		336.56299		42.675		99.99837		336.21899		42.675		100.00138		387.971		42.675		100.01801		389.52122		42.675		100.03191		390.093		42.675		100.01907

		336.98401		42.7		100.00261		100.01804		336.82599		42.7		99.99459		336.48999		42.7		99.99985		388.214		42.7		100.01804		389.77389		42.7		100.03193		390.33589		42.7		100.01909

		337.23499		42.725		100.0024		100.01808		337.103		42.725		99.99619		336.74899		42.725		100.0013		388.46023		42.725		100.01808		390.02245		42.725		100.03194		390.57977		42.725		100.01912

		337.50699		42.75		100.0021		100.01811		337.358		42.75		99.99751		337.009		42.75		99.99985		388.70911		42.75		100.01811		390.26467		42.75		100.03195		390.82422		42.75		100.01914

		337.76999		42.775		100.00321		100.01815		337.625		42.775		99.99422		337.28101		42.775		100.00072		388.95656		42.775		100.01815		390.51045		42.775		100.03196		391.07089		42.775		100.01917

		338.04501		42.8		100.00347		100.01818		337.892		42.8		99.99645		337.54999		42.8		100.00173		389.20422		42.8		100.01818		390.75567		42.8		100.03197		391.31844		42.8		100.01919

		338.297		42.825		100.00322		100.01821		338.15601		42.825		99.99663		337.811		42.825		100.00171		389.45467		42.825		100.01821		390.99811		42.825		100.03197		391.56789		42.825		100.01921

		338.578		42.85		100.00328		100.01824		338.414		42.85		99.99494		338.09		42.85		100.00231		389.70489		42.85		100.01824		391.24333		42.85		100.03198		391.81811		42.85		100.01923

		338.84		42.875		100.00397		100.01826		338.69299		42.875		99.99691		338.34799		42.875		100.00128		389.95167		42.875		100.01826		391.49389		42.875		100.03198		392.06722		42.875		100.01925

		339.091		42.9		100.00389		100.01828		338.948		42.9		99.99691		338.61499		42.9		100.00612		390.19744		42.9		100.01828		391.74289		42.9		100.03198		392.317		42.9		100.01927

		339.36401		42.925		100.00262		100.0183		339.22		42.925		99.99449		338.884		42.925		100.00144		390.44444		42.925		100.0183		391.99433		42.925		100.03198		392.57011		42.925		100.01928

		339.63501		42.95		100.00311		100.0183		339.48199		42.95		99.99698		339.14899		42.95		100.0037		390.688		42.95		100.0183		392.24445		42.95		100.03198		392.82211		42.95		100.01929

		339.90601		42.975		100.0016		100.0183		339.74799		42.975		99.99749		339.41		42.975		100.00261		390.92977		42.975		100.0183		392.49967		42.975		100.03198		393.07467		42.975		100.0193

		340.16		43		100.00325		100.0183		340.01099		43		99.99531		339.67899		43		100.00182		391.17322		43		100.0183		392.752		43		100.03198		393.32556		43		100.0193

		340.43201		43.025		99.99941		100.01829		340.28799		43.025		99.99567		339.94199		43.025		100.00005		391.427		43.025		100.01829		393.00611		43.025		100.03198		393.575		43.025		100.01931

		340.698		43.05		100.00238		100.01828		340.55701		43.05		99.99713		340.207		43.05		100.00196		391.678		43.05		100.01828		393.26089		43.05		100.03198		393.82533		43.05		100.01931

		340.95901		43.075		100.00571		100.01826		340.81601		43.075		99.99919		340.483		43.075		100.00256		391.93055		43.075		100.01826		393.51389		43.075		100.03198		394.07334		43.075		100.01931

		341.22601		43.1		100.00463		100.01825		341.077		43.1		99.99913		340.74301		43.1		100.00439		392.18444		43.1		100.01825		393.76134		43.1		100.03198		394.31945		43.1		100.01931

		341.48999		43.125		100.00588		100.01823		341.345		43.125		99.99832		341.017		43.125		100.00253		392.43922		43.125		100.01823		394.00911		43.125		100.03198		394.56656		43.125		100.01931

		341.75201		43.15		100.00287		100.01821		341.61801		43.15		99.99646		341.276		43.15		100.00205		392.69044		43.15		100.01821		394.25433		43.15		100.03197		394.811		43.15		100.01931

		342.01599		43.175		100.0028		100.0182		341.88		43.175		99.99432		341.552		43.175		100.00163		392.94233		43.175		100.0182		394.49867		43.175		100.03197		395.05845		43.175		100.01931

		342.28601		43.2		100.00366		100.01818		342.147		43.2		99.9951		341.81699		43.2		100.00187		393.19578		43.2		100.01818		394.73911		43.2		100.03197		395.30589		43.2		100.01931

		342.55301		43.225		100.00371		100.01817		342.409		43.225		99.99729		342.08801		43.225		99.99983		393.448		43.225		100.01817		394.98445		43.225		100.03197		395.55445		43.225		100.01931

		342.82199		43.25		100.00284		100.01816		342.67999		43.25		99.99538		342.35599		43.25		100.00158		393.68955		43.25		100.01816		395.23022		43.25		100.03197		395.80467		43.25		100.01931

		343.082		43.275		100.00282		100.01816		342.94501		43.275		99.99496		342.61401		43.275		100.00039		393.93144		43.275		100.01816		395.47934		43.275		100.03197		396.05167		43.275		100.01931

		343.35101		43.3		100.00351		100.01815		343.20999		43.3		99.99437		342.88101		43.3		100.00016		394.16856		43.3		100.01815		395.72556		43.3		100.03198		396.30134		43.3		100.01931

		343.61099		43.325		100.00439		100.01815		343.48499		43.325		99.99722		343.14801		43.325		100.00268		394.40566		43.325		100.01815		395.97478		43.325		100.03198		396.55178		43.325		100.01931

		343.879		43.35		100.0032		100.01815		343.742		43.35		99.99508		343.41299		43.35		100.00231		394.64011		43.35		100.01815		396.22355		43.35		100.03198		396.80023		43.35		100.01931

		344.14999		43.375		100.00402		100.01816		344.00201		43.375		99.99897		343.66901		43.375		100.00346		394.87544		43.375		100.01816		396.47277		43.375		100.03199		397.05011		43.375		100.01932

		344.41		43.4		100.00293		100.01816		344.27399		43.4		99.99576		343.93701		43.4		100.00282		395.11677		43.4		100.01816		396.72255		43.4		100.03199		397.29689		43.4		100.01932

		344.67899		43.425		100.00221		100.01817		344.54501		43.425		99.99592		344.20499		43.425		100.00081		395.36078		43.425		100.01817		396.97866		43.425		100.032		397.54189		43.425		100.01933

		344.94299		43.45		100.00642		100.01818		344.811		43.45		99.99661		344.48199		43.45		100.00183		395.605		43.45		100.01818		397.229		43.45		100.03201		397.78533		43.45		100.01933

		345.20901		43.475		100.00219		100.01819		345.07501		43.475		99.99587		344.737		43.475		100.00301		395.85056		43.475		100.01819		397.47644		43.475		100.03201		398.02655		43.475		100.01934

		345.48199		43.5		100.00165		100.0182		345.33801		43.5		99.99578		345.01001		43.5		100.00083		396.09755		43.5		100.0182		397.72322		43.5		100.03203		398.26911		43.5		100.01935

		345.73801		43.525		100.0019		100.01822		345.599		43.525		99.99324		345.284		43.525		100		396.34878		43.525		100.01822		397.97244		43.525		100.03204		398.50844		43.525		100.01936

		346.017		43.55		100.00435		100.01823		345.866		43.55		99.99665		345.53799		43.55		100.00294		396.60011		43.55		100.01823		398.21789		43.55		100.03206		398.75355		43.55		100.01938

		346.26599		43.575		100.00169		100.01825		346.13699		43.575		99.99402		345.81799		43.575		100.00006		396.85378		43.575		100.01825		398.46322		43.575		100.03207		399.00178		43.575		100.01939

		346.543		43.6		100.00084		100.01827		346.41199		43.6		99.99759		346.08401		43.6		99.99997		397.10811		43.6		100.01827		398.71111		43.6		100.0321		399.24833		43.6		100.01941

		346.811		43.625		100.00436		100.01829		346.659		43.625		99.99749		346.34201		43.625		100.00198		397.35778		43.625		100.01829		398.96189		43.625		100.03212		399.49544		43.625		100.01942

		347.06699		43.65		100.00398		100.01831		346.93799		43.65		99.99478		346.60501		43.65		100.0002		397.60344		43.65		100.01831		399.20767		43.65		100.03215		399.74389		43.65		100.01944

		347.32901		43.675		100.00434		100.01834		347.20901		43.675		99.99814		346.87799		43.675		100.00122		397.84922		43.675		100.01834		399.45622		43.675		100.03218		399.99511		43.675		100.01946

		347.59299		43.7		100.003		100.01837		347.46201		43.7		100.00012		347.138		43.7		100.00158		398.09189		43.7		100.01837		399.70645		43.7		100.03221		400.24778		43.7		100.01948

		347.867		43.725		100.00043		100.0184		347.73001		43.725		99.99661		347.41		43.725		99.99934		398.33511		43.725		100.0184		399.95622		43.725		100.03225		400.49789		43.725		100.0195

		348.12201		43.75		100.00345		100.01844		347.99701		43.75		99.99591		347.66699		43.75		100.00093		398.57656		43.75		100.01844		400.20356		43.75		100.03229		400.75011		43.75		100.01952

		348.39801		43.775		100.00388		100.01848		348.263		43.775		99.99666		347.93201		43.775		100.0017		398.82355		43.775		100.01848		400.45189		43.775		100.03233		400.99578		43.775		100.01954

		348.65799		43.8		100.00076		100.01852		348.54099		43.8		99.99398		348.207		43.8		99.99917		399.07145		43.8		100.01852		400.69922		43.8		100.03237		401.24011		43.8		100.01956

		348.927		43.825		100.00301		100.01857		348.79599		43.825		99.9974		348.45901		43.825		99.99989		399.32111		43.825		100.01857		400.94544		43.825		100.03242		401.48656		43.825		100.01958

		349.20099		43.85		100.00326		100.01861		349.056		43.85		99.9974		348.741		43.85		100.002		399.56844		43.85		100.01861		401.18777		43.85		100.03246		401.73145		43.85		100.0196

		349.457		43.875		100.00056		100.01866		349.32501		43.875		99.99849		349.00299		43.875		100.00231		399.81644		43.875		100.01866		401.43144		43.875		100.03251		401.97533		43.875		100.01963

		349.711		43.9		100.00232		100.01871		349.59299		43.9		99.99478		349.27301		43.9		100.00291		400.06467		43.9		100.01871		401.66944		43.9		100.03256		402.21633		43.9		100.01965

		349.98499		43.925		100.00466		100.01877		349.86401		43.925		99.99842		349.53201		43.925		100.00245		400.31922		43.925		100.01877		401.90633		43.925		100.03261		402.45722		43.925		100.01967

		350.255		43.95		100.00425		100.01882		350.12299		43.95		100.00036		349.80301		43.95		100.00185		400.57145		43.95		100.01882		402.14177		43.95		100.03266		402.70078		43.95		100.01969

		350.51199		43.975		100.00278		100.01887		350.38901		43.975		99.99284		350.078		43.975		100.00012		400.823		43.975		100.01887		402.37889		43.975		100.03271		402.94544		43.975		100.01971

		350.79001		44		100.0025		100.01893		350.65701		44		99.99439		350.33701		44		100.00076		401.06978		44		100.01893		402.62011		44		100.03276		403.19111		44		100.01973

		351.052		44.025		100.00278		100.01898		350.918		44.025		99.9941		350.60699		44.025		100.0018		401.31389		44.025		100.01898		402.86156		44.025		100.03281		403.43422		44.025		100.01975

		351.314		44.05		100.00305		100.01903		351.19199		44.05		99.99619		350.862		44.05		100.00065		401.55567		44.05		100.01903		403.102		44.05		100.03286		403.67822		44.05		100.01976

		351.586		44.075		100.00064		100.01908		351.45801		44.075		99.99488		351.13599		44.075		99.99955		401.79834		44.075		100.01908		403.34489		44.075		100.03292		403.92278		44.075		100.01978

		351.854		44.1		100.00024		100.01912		351.733		44.1		99.99428		351.405		44.1		99.99891		402.04123		44.1		100.01912		403.58744		44.1		100.03297		404.16756		44.1		100.01979

		352.112		44.125		100.00345		100.01916		351.987		44.125		99.99758		351.673		44.125		100.00264		402.28289		44.125		100.01916		403.834		44.125		100.03302		404.41444		44.125		100.0198

		352.37601		44.15		100.00066		100.0192		352.26199		44.15		99.99531		351.94		44.15		99.99992		402.52467		44.15		100.0192		404.08234		44.15		100.03308		404.66089		44.15		100.01982

		352.646		44.175		100.00248		100.01923		352.526		44.175		99.99465		352.20001		44.175		100.00335		402.76689		44.175		100.01923		404.33034		44.175		100.03313		404.905		44.175		100.01983

		352.914		44.2		100.00339		100.01926		352.80099		44.2		99.99651		352.466		44.2		100.00111		403.01167		44.2		100.01926		404.57844		44.2		100.03318		405.14955		44.2		100.01984

		353.177		44.225		100.00236		100.01928		353.05301		44.225		99.99623		352.745		44.225		99.99992		403.25067		44.225		100.01928		404.82289		44.225		100.03324		405.39422		44.225		100.01985

		353.439		44.25		100.00417		100.0193		353.32599		44.25		99.99625		352.99899		44.25		100.0014		403.49011		44.25		100.0193		405.06544		44.25		100.03329		405.63944		44.25		100.01986

		353.703		44.275		100.00388		100.01932		353.58401		44.275		99.99876		353.267		44.275		100.0002		403.73167		44.275		100.01932		405.30744		44.275		100.03334		405.88144		44.275		100.01988

		353.966		44.3		100.00352		100.01933		353.86301		44.3		99.99558		353.534		44.3		100.0004		403.97167		44.3		100.01933		405.54633		44.3		100.03339		406.12811		44.3		100.01989

		354.233		44.325		100.00152		100.01934		354.12201		44.325		99.9938		353.79901		44.325		100.00001		404.21178		44.325		100.01934		405.78556		44.325		100.03344		406.37633		44.325		100.01991

		354.50101		44.35		100.00318		100.01935		354.384		44.35		99.99955		354.064		44.35		99.99927		404.45133		44.35		100.01935		406.02745		44.35		100.03348		406.62311		44.35		100.01993

		354.77499		44.375		100.00442		100.01935		354.647		44.375		99.99856		354.33801		44.375		100.00218		404.68889		44.375		100.01935		406.26733		44.375		100.03353		406.86955		44.375		100.01995

		355.034		44.4		100.00296		100.01936		354.923		44.4		99.99502		354.591		44.4		100.00186		404.92778		44.4		100.01936		406.50778		44.4		100.03357		407.11544		44.4		100.01997

		355.29501		44.425		100.00295		100.01936		355.18201		44.425		99.99449		354.86099		44.425		100.00184		405.16633		44.425		100.01936		406.74934		44.425		100.03362		407.36045		44.425		100.01999

		355.55801		44.45		100.00278		100.01937		355.45801		44.45		99.99579		355.12399		44.45		100.0017		405.41011		44.45		100.01937		406.99078		44.45		100.03366		407.60722		44.45		100.02002

		355.83401		44.475		100.00318		100.01938		355.72198		44.475		99.99645		355.39499		44.475		100.00134		405.654		44.475		100.01938		407.23289		44.475		100.0337		407.85256		44.475		100.02004

		356.08899		44.5		100.00355		100.01939		355.98599		44.5		99.9964		355.66901		44.5		100.00287		405.895		44.5		100.01939		407.47656		44.5		100.03374		408.102		44.5		100.02006

		356.358		44.525		100.0032		100.01941		356.254		44.525		99.99488		355.939		44.525		100.00222		406.144		44.525		100.01941		407.723		44.525		100.03378		408.34456		44.525		100.02009

		356.62701		44.55		100.0025		100.01942		356.51401		44.55		99.99591		356.20099		44.55		99.99912		406.395		44.55		100.01942		407.96755		44.55		100.03381		408.58389		44.55		100.02011

		356.88901		44.575		100.00214		100.01944		356.78299		44.575		99.99873		356.47198		44.575		100.00073		406.64567		44.575		100.01944		408.211		44.575		100.03385		408.82367		44.575		100.02013

		357.14801		44.6		100.00322		100.01946		357.04501		44.6		99.99788		356.73401		44.6		100.00287		406.89511		44.6		100.01946		408.45433		44.6		100.03388		409.064		44.6		100.02016

		357.41		44.625		100.00401		100.01949		357.314		44.625		99.99961		356.98801		44.625		100.00247		407.14567		44.625		100.01949		408.69811		44.625		100.03392		409.30267		44.625		100.02018

		357.68399		44.65		100.00592		100.01951		357.57501		44.65		99.99582		357.259		44.65		100.002		407.396		44.65		100.01951		408.93944		44.65		100.03395		409.54211		44.65		100.0202

		357.95099		44.675		100.00342		100.01953		357.841		44.675		99.99761		357.52399		44.675		99.9986		407.64511		44.675		100.01953		409.17966		44.675		100.03398		409.78367		44.675		100.02021

		358.203		44.7		100.00434		100.01956		358.10599		44.7		99.99653		357.79401		44.7		100.00152		407.89344		44.7		100.01956		409.421		44.7		100.034		410.02933		44.7		100.02023

		358.487		44.725		100.00262		100.01958		358.36801		44.725		99.99606		358.06601		44.725		100.00021		408.14277		44.725		100.01958		409.66467		44.725		100.03403		410.27111		44.725		100.02024

		358.745		44.75		100.00132		100.0196		358.646		44.75		99.99347		358.32401		44.75		99.99938		408.38655		44.75		100.0196		409.90978		44.75		100.03405		410.51733		44.75		100.02026

		359.013		44.775		100.00242		100.01962		358.909		44.775		99.9954		358.58401		44.775		99.99932		408.62711		44.775		100.01962		410.15711		44.775		100.03407		410.766		44.775		100.02027

		359.267		44.8		100.00261		100.01964		359.177		44.8		99.99549		358.85699		44.8		99.99894		408.86711		44.8		100.01964		410.40289		44.8		100.03409		411.01444		44.8		100.02028

		359.53799		44.825		100.00173		100.01965		359.44199		44.825		99.99699		359.12299		44.825		100.00133		409.11		44.825		100.01965		410.65011		44.825		100.03411		411.26322		44.825		100.0203

		359.79599		44.85		100.00216		100.01967		359.70401		44.85		99.99612		359.388		44.85		100.001		409.349		44.85		100.01967		410.895		44.85		100.03412		411.51533		44.85		100.02031

		360.06299		44.875		100.00299		100.01968		359.974		44.875		99.99509		359.65201		44.875		100.00253		409.58811		44.875		100.01968		411.13822		44.875		100.03413		411.76578		44.875		100.02032

		360.336		44.9		100.00316		100.01969		360.233		44.9		99.99799		359.92099		44.9		100.00222		409.82867		44.9		100.01969		411.38411		44.9		100.03414		412.01122		44.9		100.02034

		360.59399		44.925		100.00595		100.0197		360.50601		44.925		99.99394		360.189		44.925		100.0019		410.07189		44.925		100.0197		411.62989		44.925		100.03415		412.25577		44.925		100.02035

		360.867		44.95		100.00375		100.01971		360.76001		44.95		99.99548		360.46399		44.95		100.00201		410.31611		44.95		100.01971		411.87211		44.95		100.03416		412.50177		44.95		100.02037

		361.13101		44.975		100.00079		100.01972		361.03101		44.975		99.99518		360.728		44.975		99.99898		410.55933		44.975		100.01972		412.11244		44.975		100.03417		412.74544		44.975		100.02039

		361.405		45		100.00123		100.01972		361.30399		45		99.99787		360.98599		45		100.00118		410.806		45		100.01972		412.35044		45		100.03418		412.98555		45		100.02041

		361.664		45.025		100.00287		100.01973		361.552		45.025		99.99938		361.254		45.025		99.99981		411.05478		45.025		100.01973		412.58989		45.025		100.03419		413.23089		45.025		100.02044

		361.92099		45.05		100.00261		100.01974		361.82401		45.05		99.99385		361.52301		45.05		100.00085		411.29978		45.05		100.01974		412.82822		45.05		100.0342		413.47955		45.05		100.02046

		362.19199		45.075		100.0014		100.01975		362.09		45.075		99.99687		361.78101		45.075		100.0024		411.54667		45.075		100.01975		413.06778		45.075		100.0342		413.72655		45.075		100.02049

		362.45599		45.1		99.99983		100.01976		362.362		45.1		99.99485		362.04999		45.1		99.9991		411.79367		45.1		100.01976		413.313		45.1		100.03421		413.97366		45.1		100.02051

		362.729		45.125		100.00056		100.01978		362.617		45.125		99.99312		362.315		45.125		99.99943		412.039		45.125		100.01978		413.55967		45.125		100.03423		414.22289		45.125		100.02054

		362.979		45.15		100.00286		100.01979		362.88901		45.15		99.99451		362.59201		45.15		100.00122		412.28145		45.15		100.01979		413.80433		45.15		100.03424		414.47044		45.15		100.02056

		363.254		45.175		100.00291		100.0198		363.16101		45.175		99.99837		362.85199		45.175		100.00216		412.52222		45.175		100.0198		414.05022		45.175		100.03425		414.71967		45.175		100.02059

		363.51501		45.2		100.0044		100.01982		363.42099		45.2		99.99486		363.112		45.2		100.00097		412.764		45.2		100.01982		414.29566		45.2		100.03426		414.96689		45.2		100.02062

		363.78299		45.225		100.00062		100.01984		363.69601		45.225		99.99207		363.383		45.225		100.00039		412.99911		45.225		100.01984		414.541		45.225		100.03428		415.21711		45.225		100.02064

		364.056		45.25		100.00155		100.01986		363.95499		45.25		99.9912		363.646		45.25		100.00046		413.23656		45.25		100.01986		414.78822		45.25		100.03429		415.46433		45.25		100.02066

		364.315		45.275		100.00204		100.01988		364.216		45.275		99.99596		363.91699		45.275		100.00228		413.47967		45.275		100.01988		415.03655		45.275		100.03431		415.70622		45.275		100.02069

		364.58099		45.3		100.00436		100.01991		364.48901		45.3		99.99558		364.18201		45.3		100.00198		413.71989		45.3		100.01991		415.28377		45.3		100.03433		415.94967		45.3		100.02071

		364.84299		45.325		100.00367		100.01994		364.755		45.325		99.9996		364.44699		45.325		99.9995		413.96022		45.325		100.01994		415.52733		45.325		100.03435		416.19389		45.325		100.02073

		365.11301		45.35		100.00255		100.01997		365.01599		45.35		99.99567		364.70599		45.35		100.00065		414.20078		45.35		100.01997		415.77033		45.35		100.03437		416.43456		45.35		100.02075

		365.38101		45.375		100.00142		100.02		365.297		45.375		99.99666		364.98099		45.375		100.00205		414.44422		45.375		100.02		416.01333		45.375		100.03439		416.67656		45.375		100.02077

		365.64499		45.4		100.0021		100.02004		365.54599		45.4		99.99578		365.23401		45.4		100.00218		414.686		45.4		100.02004		416.25533		45.4		100.03441		416.91989		45.4		100.02078

		365.91501		45.425		100.00269		100.02007		365.815		45.425		99.99831		365.51501		45.425		100.00299		414.92856		45.425		100.02007		416.49956		45.425		100.03443		417.16756		45.425		100.0208

		366.17899		45.45		100.0016		100.02011		366.082		45.45		99.99525		365.76599		45.45		100.00259		415.17845		45.45		100.02011		416.745		45.45		100.03446		417.41478		45.45		100.02082

		366.44		45.475		100.00287		100.02015		366.34698		45.475		99.99365		366.03601		45.475		100.00115		415.42556		45.475		100.02015		416.99167		45.475		100.03448		417.66056		45.475		100.02083

		366.70901		45.5		100.00249		100.02019		366.612		45.5		99.99302		366.30301		45.5		100.00095		415.667		45.5		100.02019		417.23822		45.5		100.0345		417.90811		45.5		100.02085

		366.97101		45.525		100.00187		100.02023		366.88101		45.525		99.99438		366.57199		45.525		99.99886		415.912		45.525		100.02023		417.48833		45.525		100.03453		418.15411		45.525		100.02086

		367.24301		45.55		100.00043		100.02027		367.142		45.55		99.99469		366.84399		45.55		100.00374		416.15834		45.55		100.02027		417.74133		45.55		100.03456		418.40111		45.55		100.02088

		367.50101		45.575		100.00519		100.0203		367.409		45.575		99.99598		367.10101		45.575		100.00104		416.40323		45.575		100.0203		417.99122		45.575		100.03459		418.64978		45.575		100.02089

		367.76599		45.6		100.00047		100.02034		367.67401		45.6		99.99713		367.371		45.6		99.9981		416.64578		45.6		100.02034		418.24255		45.6		100.03461		418.89544		45.6		100.0209

		368.034		45.625		100.00335		100.02038		367.936		45.625		99.99657		367.63699		45.625		100.00083		416.89333		45.625		100.02038		418.49477		45.625		100.03465		419.14089		45.625		100.02092

		368.29199		45.65		100.00121		100.02041		368.202		45.65		99.99863		367.90302		45.65		100.00113		417.143		45.65		100.02041		418.74344		45.65		100.03468		419.38155		45.65		100.02093

		368.55499		45.675		100.00195		100.02045		368.46701		45.675		99.99804		368.16299		45.675		100.00027		417.39011		45.675		100.02045		418.99178		45.675		100.03471		419.62322		45.675		100.02094

		368.82501		45.7		100.00193		100.02048		368.746		45.7		99.99369		368.41901		45.7		100.00189		417.63678		45.7		100.02048		419.23611		45.7		100.03474		419.86422		45.7		100.02096

		369.09201		45.725		100.0016		100.02052		368.991		45.725		99.99743		368.69299		45.725		100.00039		417.88544		45.725		100.02052		419.481		45.725		100.03478		420.10567		45.725		100.02097

		369.35101		45.75		99.99962		100.02055		369.26501		45.75		99.99285		368.957		45.75		99.99857		418.13344		45.75		100.02055		419.726		45.75		100.03481		420.34722		45.75		100.02099

		369.61499		45.775		100.0028		100.02058		369.53101		45.775		99.99372		369.22501		45.775		100.003		418.37878		45.775		100.02058		419.96478		45.775		100.03485		420.59111		45.775		100.021

		369.88901		45.8		100.00232		100.02062		369.80301		45.8		99.99569		369.5		45.8		100.0012		418.625		45.8		100.02062		420.20633		45.8		100.03488		420.83722		45.8		100.02102

		370.15399		45.825		100.00204		100.02065		370.05701		45.825		99.99396		369.75201		45.825		99.99973		418.871		45.825		100.02065		420.446		45.825		100.03491		421.08411		45.825		100.02104

		370.422		45.85		100.00279		100.02069		370.323		45.85		99.99319		370.01999		45.85		100.00475		419.11634		45.85		100.02069		420.68989		45.85		100.03494		421.32789		45.85		100.02106

		370.694		45.875		100.00343		100.02072		370.591		45.875		99.99553		370.29199		45.875		100.00105		419.35845		45.875		100.02072		420.936		45.875		100.03497		421.57455		45.875		100.02108

		370.94601		45.9		100.00338		100.02076		370.85599		45.9		99.99567		370.564		45.9		99.99905		419.59856		45.9		100.02076		421.18567		45.9		100.03499		421.82155		45.9		100.0211

		371.21701		45.925		99.99949		100.02079		371.117		45.925		99.9951		370.82199		45.925		100.00071		419.84045		45.925		100.02079		421.43178		45.925		100.03501		422.06933		45.925		100.02113

		371.495		45.95		100.00041		100.02082		371.38		45.95		99.99609		371.08301		45.95		100.00017		420.07822		45.95		100.02082		421.67611		45.95		100.03503		422.31955		45.95		100.02115

		371.74701		45.975		100.00312		100.02086		371.65399		45.975		99.99733		371.35501		45.975		100.00709		420.31744		45.975		100.02086		421.92044		45.975		100.03504		422.56988		45.975		100.02118

		372.01401		46		100.00325		100.02088		371.918		46		99.99488		371.621		46		99.99753		420.564		46		100.02088		422.16967		46		100.03505		422.81599		46		100.0212

		372.28299		46.025		100.00172		100.02091		372.185		46.025		99.99558		371.884		46.025		100.00062		420.81289		46.025		100.02091		422.41655		46.025		100.03506		423.06155		46.025		100.02122

		372.55099		46.05		100.003		100.02094		372.45001		46.05		99.99876		372.14001		46.05		100.00329		421.06389		46.05		100.02094		422.66411		46.05		100.03507		423.30666		46.05		100.02125

		372.81201		46.075		100.00371		100.02096		372.71399		46.075		99.99836		372.40799		46.075		100.00532		421.31078		46.075		100.02096		422.90778		46.075		100.03508		423.55289		46.075		100.02127

		373.064		46.1		100.00097		100.02099		372.978		46.1		99.99553		372.68399		46.1		99.99965		421.55844		46.1		100.02099		423.15067		46.1		100.03509		423.79811		46.1		100.02129

		373.33301		46.125		100.00122		100.02101		373.245		46.125		99.9954		372.95001		46.125		100.00235		421.80878		46.125		100.02101		423.39122		46.125		100.0351		424.039		46.125		100.02132

		373.59299		46.15		100.00273		100.02103		373.50699		46.15		99.9975		373.20999		46.15		99.99913		422.05778		46.15		100.02103		423.63433		46.15		100.03511		424.28711		46.15		100.02134

		373.87701		46.175		100.00187		100.02106		373.771		46.175		99.9945		373.46799		46.175		100.0019		422.31167		46.175		100.02106		423.87711		46.175		100.03512		424.53589		46.175		100.02135

		374.13599		46.2		100.00238		100.02108		374.04099		46.2		99.99624		373.73801		46.2		100.00137		422.563		46.2		100.02108		424.12122		46.2		100.03513		424.78622		46.2		100.02137

		374.40799		46.225		99.99895		100.0211		374.31		46.225		99.9923		374.008		46.225		99.99695		422.80844		46.225		100.0211		424.36889		46.225		100.03514		425.03489		46.225		100.02138

		374.66699		46.25		100.0001		100.02113		374.577		46.25		99.99658		374.27701		46.25		100.00212		423.05122		46.25		100.02113		424.618		46.25		100.03516		425.28156		46.25		100.0214

		374.93399		46.275		100.00191		100.02115		374.83701		46.275		99.99529		374.53299		46.275		100.0014		423.28911		46.275		100.02115		424.86755		46.275		100.03518		425.53434		46.275		100.02141

		375.20001		46.3		100.00121		100.02118		375.10001		46.3		99.99701		374.80099		46.3		99.99982		423.53167		46.3		100.02118		425.11667		46.3		100.0352		425.786		46.3		100.02142

		375.45901		46.325		100.00221		100.0212		375.36301		46.325		99.99619		375.06799		46.325		100.00173		423.77067		46.325		100.0212		425.366		46.325		100.03522		426.03734		46.325		100.02143

		375.73001		46.35		100.004		100.02123		375.62701		46.35		99.99722		375.33801		46.35		100.00235		424.00811		46.35		100.02123		425.61644		46.35		100.03525		426.29167		46.35		100.02144

		375.98599		46.375		100.00483		100.02125		375.89301		46.375		99.99786		375.59698		46.375		100.00424		424.24989		46.375		100.02125		425.86578		46.375		100.03527		426.53967		46.375		100.02144

		376.25		46.4		100.00258		100.02128		376.14999		46.4		99.99478		375.86899		46.4		100.00177		424.49467		46.4		100.02128		426.11689		46.4		100.03529		426.78178		46.4		100.02145

		376.51599		46.425		100.00229		100.0213		376.42099		46.425		99.99661		376.12399		46.425		100.00294		424.73911		46.425		100.0213		426.36366		46.425		100.03532		427.02333		46.425		100.02146

		376.798		46.45		99.99969		100.02133		376.68701		46.45		99.99537		376.39401		46.45		99.99916		424.98333		46.45		100.02133		426.60844		46.45		100.03534		427.268		46.45		100.02147

		377.04999		46.475		100.00142		100.02135		376.95401		46.475		99.99638		376.66501		46.475		99.99917		425.22778		46.475		100.02135		426.85022		46.475		100.03536		427.51078		46.475		100.02148

		377.32101		46.5		100.00324		100.02136		377.22699		46.5		99.99613		376.923		46.5		100.00044		425.47989		46.5		100.02136		427.09189		46.5		100.03539		427.75078		46.5		100.02149

		377.586		46.525		100.00379		100.02138		377.48199		46.525		99.99538		377.18799		46.525		100.00159		425.72789		46.525		100.02138		427.33144		46.525		100.03541		427.99644		46.525		100.02151

		377.85001		46.55		100.00085		100.02139		377.75201		46.55		99.99586		377.45401		46.55		100.00307		425.97822		46.55		100.02139		427.572		46.55		100.03543		428.24267		46.55		100.02152

		378.11499		46.575		100.00236		100.0214		378.01401		46.575		99.99738		377.72699		46.575		100.00516		426.23078		46.575		100.0214		427.81533		46.575		100.03545		428.49133		46.575		100.02154

		378.37399		46.6		100.0003		100.0214		378.28101		46.6		99.99553		377.98801		46.6		100.00456		426.47633		46.6		100.0214		428.06089		46.6		100.03547		428.73889		46.6		100.02155

		378.64099		46.625		100.00177		100.0214		378.543		46.625		99.99858		378.24701		46.625		100.00224		426.71967		46.625		100.0214		428.30588		46.625		100.03549		428.99033		46.625		100.02157

		378.91599		46.65		100.00278		100.0214		378.81601		46.65		99.99401		378.509		46.65		100.0004		426.96389		46.65		100.0214		428.554		46.65		100.03551		429.23844		46.65		100.02158

		379.17499		46.675		100.0001		100.0214		379.08099		46.675		99.99597		378.776		46.675		100.00051		427.20611		46.675		100.0214		428.80044		46.675		100.03553		429.48656		46.675		100.0216

		379.448		46.7		100.0017		100.02139		379.33899		46.7		99.99142		379.05099		46.7		99.9947		427.44856		46.7		100.02139		429.04844		46.7		100.03554		429.73911		46.7		100.02161

		379.70901		46.725		100.0017		100.02138		379.608		46.725		99.99511		379.31		46.725		100.0034		427.68767		46.725		100.02138		429.29722		46.725		100.03556		429.99177		46.725		100.02163

		379.97501		46.75		100.00182		100.02137		379.867		46.75		99.99596		379.57101		46.75		100.00999		427.93322		46.75		100.02137		429.54933		46.75		100.03558		430.23855		46.75		100.02164

		380.24399		46.775		99.99919		100.02136		380.134		46.775		99.99285		379.845		46.775		100.00183		428.17933		46.775		100.02136		429.80089		46.775		100.0356		430.48544		46.775		100.02165

		380.513		46.8		100.00092		100.02135		380.39301		46.8		99.99521		380.10501		46.8		100.00483		428.42544		46.8		100.02135		430.04811		46.8		100.03562		430.73022		46.8		100.02167

		380.76999		46.825		100.00375		100.02134		380.66501		46.825		99.99609		380.367		46.825		99.994		428.67289		46.825		100.02134		430.29422		46.825		100.03564		430.97511		46.825		100.02168

		381.047		46.85		100.0006		100.02133		380.92899		46.85		99.99289		380.63599		46.85		99.99697		428.92122		46.85		100.02133		430.54189		46.85		100.03566		431.21855		46.85		100.02169

		381.29901		46.875		100.00102		100.02132		381.19901		46.875		99.99631		380.89999		46.875		99.9967		429.17022		46.875		100.02132		430.78767		46.875		100.03568		431.46822		46.875		100.0217

		381.569		46.9		100.0009		100.02132		381.461		46.9		99.99455		381.15201		46.9		99.99374		429.42299		46.9		100.02132		431.03111		46.9		100.03571		431.71722		46.9		100.02172

		381.84399		46.925		100.00208		100.02132		381.72699		46.925		99.99308		381.42899		46.925		100.00588		429.67577		46.925		100.02132		431.27244		46.925		100.03573		431.96467		46.925		100.02173

		382.104		46.95		100.00227		100.02132		381.98401		46.95		99.99245		381.69299		46.95		100.00074		429.92955		46.95		100.02132		431.52022		46.95		100.03576		432.21467		46.95		100.02175

		382.35699		46.975		100.00275		100.02133		382.25		46.975		99.99431		381.952		46.975		99.99651		430.1771		46.975		100.02133		431.76411		46.975		100.03578		432.46378		46.975		100.02176

		382.61899		47		100.00038		100.02134		382.52301		47		99.99492		382.22198		47		100.00283		430.42199		47		100.02134		432.00833		47		100.03581		432.71355		47		100.02178

		382.90399		47.025		100.00025		100.02136		382.793		47.025		99.99271		382.487		47.025		99.99562		430.66499		47.025		100.02136		432.25555		47.025		100.03584		432.96255		47.025		100.0218

		383.16501		47.05		100.001		100.02138		383.05099		47.05		99.99634		382.76099		47.05		99.999		430.913		47.05		100.02138		432.50211		47.05		100.03586		433.21178		47.05		100.02181

		383.41699		47.075		100.00097		100.02141		383.31299		47.075		99.99456		383.01901		47.075		99.99591		431.15378		47.075		100.02141		432.74733		47.075		100.03589		433.46011		47.075		100.02183

		383.68701		47.1		100.00368		100.02145		383.57599		47.1		100.00114		383.27399		47.1		100.00756		431.396		47.1		100.02145		432.99199		47.1		100.03591		433.705		47.1		100.02185

		383.95499		47.125		100.00414		100.02149		383.845		47.125		99.99442		383.55099		47.125		99.99594		431.63822		47.125		100.02149		433.24089		47.125		100.03593		433.95189		47.125		100.02187

		384.22		47.15		100.00166		100.02154		384.10999		47.15		99.99818		383.811		47.15		99.99604		431.88267		47.15		100.02154		433.491		47.15		100.03595		434.199		47.15		100.02189

		384.487		47.175		100.00245		100.0216		384.36401		47.175		99.99589		384.07001		47.175		100.00555		432.12845		47.175		100.0216		433.73455		47.175		100.03597		434.44234		47.175		100.02191

		384.759		47.2		100.00307		100.02165		384.64099		47.2		99.99336		384.34399		47.2		100.00512		432.37589		47.2		100.02165		433.98056		47.2		100.03598		434.68678		47.2		100.02193

		385.02701		47.225		100.00286		100.02171		384.90701		47.225		99.99531		384.603		47.225		99.99936		432.62734		47.225		100.02171		434.22656		47.225		100.03599		434.93067		47.225		100.02194

		385.27802		47.25		100.00237		100.02178		385.17499		47.25		99.99636		384.86899		47.25		100.00025		432.87911		47.25		100.02178		434.47022		47.25		100.03601		435.17945		47.25		100.02196

		385.548		47.275		100.00227		100.02184		385.43799		47.275		99.99702		385.12601		47.275		100.00246		433.12667		47.275		100.02184		434.71456		47.275		100.03602		435.43034		47.275		100.02198

		385.81601		47.3		100.00008		100.0219		385.70401		47.3		99.99529		385.39801		47.3		100.00351		433.37789		47.3		100.0219		434.95811		47.3		100.03603		435.68244		47.3		100.02199

		386.07999		47.325		100.00047		100.02197		385.96701		47.325		99.99354		385.66599		47.325		99.99731		433.62711		47.325		100.02197		435.20767		47.325		100.03603		435.93367		47.325		100.02201

		386.34201		47.35		100.00229		100.02203		386.23401		47.35		99.99605		385.92401		47.35		99.9972		433.87411		47.35		100.02203		435.45489		47.35		100.03604		436.18278		47.35		100.02202

		386.61301		47.375		100.00269		100.02209		386.5		47.375		99.99585		386.19199		47.375		99.99403		434.11722		47.375		100.02209		435.70467		47.375		100.03605		436.43422		47.375		100.02204

		386.879		47.4		100.00261		100.02215		386.76099		47.4		99.99438		386.45801		47.4		99.99989		434.35945		47.4		100.02215		435.95478		47.4		100.03605		436.687		47.4		100.02205

		387.133		47.425		100.00278		100.0222		387.03699		47.425		99.99351		386.715		47.425		100.00711		434.60134		47.425		100.0222		436.20367		47.425		100.03606		436.93922		47.425		100.02206

		387.40601		47.45		100.00207		100.02226		387.30301		47.45		99.9921		386.98599		47.45		99.99431		434.83833		47.45		100.02226		436.45445		47.45		100.03607		437.19156		47.45		100.02208

		387.67001		47.475		100.00128		100.0223		387.561		47.475		99.99492		387.258		47.475		100.00466		435.08278		47.475		100.0223		436.70667		47.475		100.03607		437.439		47.475		100.02209

		387.93701		47.5		100.00208		100.02235		387.82901		47.5		99.99365		387.52499		47.5		100.00295		435.33		47.5		100.02235		436.95834		47.5		100.03608		437.68555		47.5		100.02211

		388.19101		47.525		100.00041		100.02239		388.08801		47.525		99.99491		387.78799		47.525		100.00374		435.57711		47.525		100.02239		437.21001		47.525		100.03608		437.92878		47.525		100.02212

		388.45401		47.55		100.0016		100.02243		388.35101		47.55		99.99498		388.04199		47.55		99.99936		435.82356		47.55		100.02243		437.45812		47.55		100.03609		438.17178		47.55		100.02214

		388.72501		47.575		100.00202		100.02246		388.608		47.575		99.99592		388.31601		47.575		100.00196		436.06745		47.575		100.02246		437.70623		47.575		100.0361		438.41522		47.575		100.02215

		388.99399		47.6		100.00075		100.0225		388.888		47.6		99.99797		388.57501		47.6		100.00182		436.314		47.6		100.0225		437.95412		47.6		100.03611		438.65966		47.6		100.02216

		389.258		47.625		99.99961		100.02253		389.155		47.625		99.9948		388.84601		47.625		100.0051		436.564		47.625		100.02253		438.20133		47.625		100.03612		438.90633		47.625		100.02217

		389.52301		47.65		100.00037		100.02256		389.41101		47.65		99.99624		389.11499		47.65		99.9998		436.81189		47.65		100.02256		438.44867		47.65		100.03613		439.15333		47.65		100.02218

		389.78699		47.675		100.00358		100.02258		389.67499		47.675		99.99753		389.37701		47.675		100.00181		437.06333		47.675		100.02258		438.70022		47.675		100.03614		439.39955		47.675		100.02219

		390.064		47.7		100.00139		100.02261		389.94901		47.7		99.99323		389.63599		47.7		100.00272		437.30789		47.7		100.02261		438.95022		47.7		100.03616		439.65089		47.7		100.0222

		390.31799		47.725		99.99902		100.02263		390.20801		47.725		99.99462		389.90601		47.725		99.99916		437.54978		47.725		100.02263		439.2		47.725		100.03618		439.89967		47.725		100.02221

		390.58099		47.75		100.00206		100.02266		390.474		47.75		99.99291		390.16501		47.75		100.00291		437.79267		47.75		100.02266		439.44967		47.75		100.0362		440.15078		47.75		100.02221

		390.85699		47.775		100.00172		100.02268		390.737		47.775		99.99603		390.44501		47.775		99.99272		438.03489		47.775		100.02268		439.69989		47.775		100.03622		440.402		47.775		100.02222

		391.12799		47.8		100.00216		100.0227		391.009		47.8		99.99533		390.70599		47.8		100.00196		438.27922		47.8		100.0227		439.94967		47.8		100.03624		440.65278		47.8		100.02223

		391.38199		47.825		100.0001		100.02272		391.26501		47.825		99.99295		390.97299		47.825		100.00118		438.52356		47.825		100.02272		440.19945		47.825		100.03626		440.90123		47.825		100.02223

		391.64499		47.85		100.00183		100.02274		391.53799		47.85		99.99612		391.228		47.85		100.0032		438.76733		47.85		100.02274		440.44867		47.85		100.03629		441.14723		47.85		100.02224

		391.91101		47.875		100.00104		100.02277		391.798		47.875		99.99571		391.50699		47.875		100.00289		439.01344		47.875		100.02277		440.69733		47.875		100.03632		441.39401		47.875		100.02224

		392.16901		47.9		100.00143		100.02278		392.06799		47.9		99.99286		391.767		47.9		99.99968		439.25889		47.9		100.02278		440.94222		47.9		100.03635		441.64023		47.9		100.02225

		392.435		47.925		100.00089		100.0228		392.327		47.925		99.99412		392.03201		47.925		99.99853		439.505		47.925		100.0228		441.186		47.925		100.03637		441.88145		47.925		100.02225

		392.711		47.95		100.00079		100.02281		392.591		47.95		99.99551		392.30099		47.95		100.00124		439.75655		47.95		100.02281		441.42933		47.95		100.0364		442.12612		47.95		100.02226

		392.966		47.975		100.00156		100.02283		392.84799		47.975		99.9935		392.55801		47.975		100.00066		440.00633		47.975		100.02283		441.675		47.975		100.03642		442.37467		47.975		100.02227

		393.23599		48		99.99988		100.02283		393.11099		48		99.9942		392.82401		48		99.99751		440.25755		48		100.02283		441.91622		48		100.03644		442.62578		48		100.02228

		393.49799		48.025		100.00014		100.02284		393.392		48.025		99.99487		393.08899		48.025		100.00148		440.51088		48.025		100.02284		442.15856		48.025		100.03646		442.87712		48.025		100.02229

		393.76099		48.05		100.00193		100.02284		393.64499		48.05		99.99584		393.353		48.05		99.99598		440.76289		48.05		100.02284		442.404		48.05		100.03647		443.12956		48.05		100.0223

		394.02802		48.075		100.00127		100.02284		393.92099		48.075		99.99623		393.62299		48.075		100.00183		441.01099		48.075		100.02284		442.65289		48.075		100.03648		443.38211		48.075		100.02231

		394.29199		48.1		100.00287		100.02284		394.18301		48.1		99.99737		393.884		48.1		100.00197		441.25944		48.1		100.02284		442.90355		48.1		100.03649		443.63545		48.1		100.02233

		394.55399		48.125		100.00307		100.02283		394.44699		48.125		99.99556		394.15201		48.125		100.00235		441.50444		48.125		100.02283		443.15222		48.125		100.0365		443.88878		48.125		100.02235

		394.827		48.15		100.00259		100.02283		394.71799		48.15		99.99551		394.41299		48.15		99.99999		441.74978		48.15		100.02283		443.403		48.15		100.03651		444.14456		48.15		100.02237

		395.095		48.175		100.00342		100.02282		394.98001		48.175		99.99429		394.68301		48.175		100.00054		441.99111		48.175		100.02282		443.65378		48.175		100.03652		444.40056		48.175		100.02239

		395.35199		48.2		100.00092		100.02282		395.23801		48.2		99.99433		394.952		48.2		99.9993		442.235		48.2		100.02282		443.90544		48.2		100.03653		444.65056		48.2		100.02242

		395.62399		48.225		100.00114		100.02281		395.51599		48.225		99.99791		395.211		48.225		100.00084		442.48222		48.225		100.02281		444.16033		48.225		100.03655		444.89911		48.225		100.02245

		395.89001		48.25		100.00254		100.02282		395.772		48.25		99.99498		395.46899		48.25		100.00041		442.72889		48.25		100.02282		444.41467		48.25		100.03657		445.14778		48.25		100.02248

		396.14401		48.275		100.00174		100.02283		396.04501		48.275		99.99585		395.745		48.275		100.0008		442.98111		48.275		100.02283		444.66322		48.275		100.03659		445.39533		48.275		100.02252

		396.409		48.3		100.00157		100.02285		396.29501		48.3		99.99559		396.00601		48.3		100.0023		443.23345		48.3		100.02285		444.91022		48.3		100.03661		445.64156		48.3		100.02256

		396.672		48.325		100.00273		100.02287		396.565		48.325		99.99649		396.27802		48.325		99.99999		443.48189		48.325		100.02287		445.15456		48.325		100.03664		445.88967		48.325		100.0226

		396.944		48.35		100.00244		100.0229		396.83401		48.35		99.99547		396.534		48.35		99.99903		443.73333		48.35		100.0229		445.4		48.35		100.03668		446.14123		48.35		100.02265

		397.20599		48.375		100.00215		100.02294		397.09201		48.375		99.99591		396.79999		48.375		99.99859		443.98511		48.375		100.02294		445.64278		48.375		100.03671		446.39223		48.375		100.0227

		397.47101		48.4		100.00085		100.02299		397.35999		48.4		99.99524		397.07599		48.4		100.00178		444.23522		48.4		100.02299		445.88967		48.4		100.03676		446.64256		48.4		100.02275

		397.73199		48.425		100.00111		100.02304		397.62201		48.425		99.99449		397.32599		48.425		100.00236		444.48511		48.425		100.02304		446.13812		48.425		100.0368		446.89601		48.425		100.02281

		398.005		48.45		99.99974		100.0231		397.89899		48.45		99.99596		397.603		48.45		100.00085		444.73145		48.45		100.0231		446.38734		48.45		100.03684		447.14689		48.45		100.02286

		398.26501		48.475		100.00252		100.02316		398.16		48.475		99.99891		397.86301		48.475		100.00345		444.97778		48.475		100.02316		446.63589		48.475		100.03689		447.401		48.475		100.02291

		398.526		48.5		100.00007		100.02322		398.41199		48.5		99.99456		398.12399		48.5		99.9977		445.21812		48.5		100.02322		446.888		48.5		100.03693		447.65545		48.5		100.02296

		398.793		48.525		100.00071		100.02327		398.685		48.525		99.99529		398.38699		48.525		99.99934		445.45867		48.525		100.02327		447.13911		48.525		100.03697		447.90912		48.525		100.02301

		399.056		48.55		100.0009		100.02332		398.944		48.55		99.99314		398.64999		48.55		100.00365		445.70222		48.55		100.02332		447.39445		48.55		100.03701		448.15934		48.55		100.02305

		399.327		48.575		100.00114		100.02337		399.20599		48.575		99.99607		398.92401		48.575		100.00147		445.95233		48.575		100.02337		447.64912		48.575		100.03705		448.40489		48.575		100.0231

		399.59201		48.6		100.00138		100.02341		399.47198		48.6		99.99355		399.19199		48.6		99.99959		446.20144		48.6		100.02341		447.90234		48.6		100.03709		448.65189		48.6		100.02314

		399.85199		48.625		100.00174		100.02344		399.73599		48.625		99.99902		399.461		48.625		100.0009		446.45311		48.625		100.02344		448.154		48.625		100.03712		448.89589		48.625		100.02317

		400.11899		48.65		100.00039		100.02346		400.00699		48.65		99.99493		399.716		48.65		100.00056		446.70355		48.65		100.02346		448.401		48.65		100.03716		449.139		48.65		100.0232

		400.38199		48.675		100.00113		100.02347		400.271		48.675		99.99349		399.99701		48.675		100.00259		446.95411		48.675		100.02347		448.64811		48.675		100.03719		449.38411		48.675		100.02323

		400.647		48.7		100.0019		100.02348		400.53		48.7		99.9976		400.26001		48.7		100.00242		447.20388		48.7		100.02348		448.89489		48.7		100.03722		449.63078		48.7		100.02325

		400.918		48.725		100.00001		100.02348		400.79599		48.725		99.99269		400.513		48.725		99.99848		447.45699		48.725		100.02348		449.13789		48.725		100.03725		449.87734		48.725		100.02327

		401.18799		48.75		100.00322		100.02347		401.065		48.75		99.99767		400.784		48.75		99.99982		447.70955		48.75		100.02347		449.38045		48.75		100.03729		450.12367		48.75		100.02329

		401.44501		48.775		100.00076		100.02346		401.32501		48.775		99.99575		401.052		48.775		99.99825		447.96255		48.775		100.02346		449.62456		48.775		100.03732		450.37022		48.775		100.0233

		401.70901		48.8		100.00206		100.02345		401.59299		48.8		99.99889		401.314		48.8		99.99827		448.20777		48.8		100.02345		449.86767		48.8		100.03735		450.62044		48.8		100.02331

		401.97501		48.825		100.00253		100.02344		401.85901		48.825		99.99289		401.582		48.825		100.00311		448.45233		48.825		100.02344		450.11444		48.825		100.03738		450.86878		48.825		100.02332

		402.24301		48.85		100.00139		100.02343		402.11801		48.85		99.99726		401.84399		48.85		99.99883		448.69744		48.85		100.02343		450.35978		48.85		100.03742		451.11867		48.85		100.02333

		402.505		48.875		100.00067		100.02343		402.38901		48.875		99.99287		402.108		48.875		99.99958		448.94056		48.875		100.02343		450.60433		48.875		100.03745		451.36889		48.875		100.02333

		402.76099		48.9		100.00149		100.02343		402.651		48.9		99.99387		402.375		48.9		100.00037		449.183		48.9		100.02343		450.84911		48.9		100.03748		451.61789		48.9		100.02334

		403.02899		48.925		100.0021		100.02344		402.918		48.925		99.99489		402.64001		48.925		99.99731		449.42655		48.925		100.02344		451.09544		48.925		100.03751		451.86278		48.925		100.02334

		403.30399		48.95		100.00055		100.02346		403.18399		48.95		99.99394		402.89801		48.95		99.99991		449.67611		48.95		100.02346		451.34367		48.95		100.03755		452.10811		48.95		100.02334

		403.57199		48.975		100.00214		100.02349		403.44501		48.975		99.99385		403.17599		48.975		100.00233		449.92467		48.975		100.02349		451.59155		48.975		100.03758		452.35511		48.975		100.02334

		403.83401		49		99.99971		100.02352		403.71201		49		99.99456		403.42401		49		100.00031		450.17033		49		100.02352		451.83744		49		100.0376		452.59989		49		100.02334

		404.09399		49.025		100.00012		100.02356		403.987		49.025		99.99478		403.69299		49.025		99.99818		450.41956		49.025		100.02356		452.08478		49.025		100.03763		452.84344		49.025		100.02334

		404.366		49.05		100.0002		100.0236		404.24399		49.05		99.99541		403.953		49.05		99.99856		450.67267		49.05		100.0236		452.32744		49.05		100.03765		453.09011		49.05		100.02335

		404.62701		49.075		100.00102		100.02365		404.508		49.075		99.99575		404.23199		49.075		99.9997		450.92244		49.075		100.02365		452.57022		49.075		100.03767		453.33967		49.075		100.02335

		404.88901		49.1		100.00261		100.02369		404.78299		49.1		99.99603		404.49301		49.1		99.99941		451.17178		49.1		100.02369		452.81478		49.1		100.03769		453.58744		49.1		100.02335

		405.147		49.125		100.00303		100.02374		405.047		49.125		99.99687		404.76099		49.125		100.00037		451.42144		49.125		100.02374		453.06034		49.125		100.0377		453.83755		49.125		100.02335

		405.427		49.15		100.00339		100.02379		405.298		49.15		99.99704		405.01999		49.15		100.00244		451.673		49.15		100.02379		453.30589		49.15		100.03771		454.08833		49.15		100.02336

		405.689		49.175		100.00249		100.02384		405.56		49.175		99.997		405.28699		49.175		100.00237		451.91511		49.175		100.02384		453.55256		49.175		100.03771		454.33889		49.175		100.02336

		405.94901		49.2		100.00223		100.02388		405.827		49.2		99.99564		405.55099		49.2		99.99872		452.15755		49.2		100.02388		453.80212		49.2		100.03772		454.589		49.2		100.02336

		406.22		49.225		100.0029		100.02393		406.10001		49.225		99.99567		405.823		49.225		100.00013		452.40233		49.225		100.02393		454.05067		49.225		100.03772		454.84144		49.225		100.02337

		406.48199		49.25		100.00088		100.02396		406.35901		49.25		99.99391		406.08301		49.25		100.0009		452.64566		49.25		100.02396		454.29734		49.25		100.03771		455.09533		49.25		100.02337

		406.745		49.275		99.99999		100.024		406.62799		49.275		99.99456		406.345		49.275		100.00006		452.88478		49.275		100.024		454.54767		49.275		100.03771		455.34567		49.275		100.02338

		407.00699		49.3		100.00039		100.02403		406.901		49.3		99.99585		406.612		49.3		100.00105		453.13033		49.3		100.02403		454.79478		49.3		100.0377		455.592		49.3		100.02338

		407.276		49.325		100.00387		100.02406		407.14899		49.325		99.99499		406.87601		49.325		100.00066		453.37755		49.325		100.02406		455.04445		49.325		100.03769		455.84		49.325		100.02339

		407.54599		49.35		100.00153		100.02409		407.41599		49.35		99.99475		407.13599		49.35		99.99944		453.626		49.35		100.02409		455.29089		49.35		100.03769		456.08711		49.35		100.02339

		407.79999		49.375		100.00214		100.02411		407.67599		49.375		99.99601		407.40701		49.375		100.00057		453.86989		49.375		100.02411		455.537		49.375		100.03768		456.33411		49.375		100.0234

		408.07599		49.4		99.99962		100.02414		407.94699		49.4		99.99726		407.664		49.4		100.00049		454.11644		49.4		100.02414		455.77845		49.4		100.03767		456.57878		49.4		100.0234

		408.32901		49.425		100.00426		100.02416		408.21301		49.425		99.993		407.93399		49.425		100.00075		454.36322		49.425		100.02416		456.01967		49.425		100.03767		456.82722		49.425		100.02341

		408.603		49.45		100.00346		100.02419		408.47501		49.45		99.99503		408.20099		49.45		100.00172		454.61066		49.45		100.02419		456.26		49.45		100.03767		457.07744		49.45		100.02342

		408.85999		49.475		100.00322		100.02421		408.74701		49.475		99.99748		408.46301		49.475		100.00122		454.85766		49.475		100.02421		456.50022		49.475		100.03767		457.32944		49.475		100.02343

		409.12701		49.5		100.00304		100.02424		409.01001		49.5		99.99727		408.72501		49.5		100.00206		455.10499		49.5		100.02424		456.74233		49.5		100.03768		457.58311		49.5		100.02344

		409.38101		49.525		100.00055		100.02427		409.26599		49.525		99.99737		408.99799		49.525		100.00157		455.34633		49.525		100.02427		456.987		49.525		100.03769		457.836		49.525		100.02345

		409.65302		49.55		100.00012		100.0243		409.53699		49.55		99.99602		409.26401		49.55		100.00055		455.58811		49.55		100.0243		457.23189		49.55		100.0377		458.08966		49.55		100.02347

		409.92001		49.575		100.0028		100.02433		409.79901		49.575		99.99388		409.51901		49.575		100.00066		455.829		49.575		100.02433		457.47589		49.575		100.03772		458.34611		49.575		100.02349

		410.18399		49.6		100.00236		100.02437		410.06699		49.6		99.99656		409.79001		49.6		100.00069		456.07166		49.6		100.02437		457.71978		49.6		100.03774		458.59933		49.6		100.02352

		410.44901		49.625		100.00263		100.02441		410.32999		49.625		99.99655		410.05301		49.625		100.00205		456.31355		49.625		100.02441		457.967		49.625		100.03777		458.85444		49.625		100.02355

		410.71201		49.65		100.00359		100.02445		410.60001		49.65		99.99754		410.31201		49.65		100.00131		456.55389		49.65		100.02445		458.21301		49.65		100.0378		459.10556		49.65		100.02359

		410.978		49.675		99.99988		100.0245		410.871		49.675		99.99439		410.59799		49.675		99.99951		456.79967		49.675		100.0245		458.46067		49.675		100.03783		459.35389		49.675		100.02362

		411.24399		49.7		100.00339		100.02454		411.12399		49.7		99.99748		410.853		49.7		100.00241		457.04411		49.7		100.02454		458.70834		49.7		100.03787		459.59978		49.7		100.02366

		411.504		49.725		100.00189		100.02458		411.392		49.725		99.99449		411.11801		49.725		100.00021		457.29067		49.725		100.02458		458.9559		49.725		100.0379		459.84222		49.725		100.0237

		411.76599		49.75		100.00503		100.02462		411.65399		49.75		99.99864		411.37601		49.75		100.00284		457.53733		49.75		100.02462		459.20401		49.75		100.03794		460.08356		49.75		100.02374

		412.035		49.775		100.00083		100.02465		411.91699		49.775		99.99382		411.64999		49.775		100.00086		457.78322		49.775		100.02465		459.44867		49.775		100.03798		460.33267		49.775		100.02378

		412.29501		49.8		100.00193		100.02468		412.177		49.8		99.99591		411.91699		49.8		100.00269		458.02833		49.8		100.02468		459.69534		49.8		100.03802		460.579		49.8		100.02381

		412.56201		49.825		100.00055		100.0247		412.44299		49.825		99.99545		412.17999		49.825		100.00315		458.27745		49.825		100.0247		459.94134		49.825		100.03806		460.82767		49.825		100.02385

		412.82999		49.85		100.00333		100.02471		412.711		49.85		99.9978		412.44199		49.85		100.00283		458.52456		49.85		100.02471		460.18567		49.85		100.03809		461.07689		49.85		100.02387

		413.09		49.875		100.00271		100.02472		412.98599		49.875		99.99579		412.70499		49.875		100.00054		458.77167		49.875		100.02472		460.43467		49.875		100.03812		461.32733		49.875		100.0239

		413.35901		49.9		100.00443		100.02471		413.237		49.9		99.99628		412.97501		49.9		100.00213		459.01211		49.9		100.02471		460.68222		49.9		100.03815		461.57866		49.9		100.02391

		413.621		49.925		100.00123		100.0247		413.49799		49.925		99.99593		413.237		49.925		100.00166		459.25711		49.925		100.0247		460.93156		49.925		100.03817		461.82955		49.925		100.02392

		413.88501		49.95		100.00221		100.02468		413.763		49.95		99.99699		413.504		49.95		100.00026		459.49745		49.95		100.02468		461.17767		49.95		100.03819		462.07955		49.95		100.02393

		414.15701		49.975		100.00164		100.02466		414.03201		49.975		99.99525		413.76599		49.975		100.00112		459.73789		49.975		100.02466		461.42378		49.975		100.0382		462.33222		49.975		100.02393

		414.423		50		100.00316		100.02463		414.29599		50		99.99622		414.035		50		100.00417		459.97889		50		100.02463		461.67166		50		100.03821		462.58044		50		100.02393

		414.67999		50.025		100.00173		100.0246		414.564		50.025		99.99762		414.30399		50.025		100.00165		460.22611		50.025		100.0246		461.91889		50.025		100.03822		462.82799		50.025		100.02392

		414.948		50.05		100.00334		100.02457		414.82101		50.05		99.99624		414.57101		50.05		100.00091		460.47122		50.05		100.02457		462.16511		50.05		100.03822		463.07233		50.05		100.02391

		415.21201		50.075		100.0016		100.02454		415.08499		50.075		99.99722		414.828		50.075		100.00206		460.71766		50.075		100.02454		462.41411		50.075		100.03822		463.31633		50.075		100.0239

		415.47699		50.1		100.00164		100.02452		415.36099		50.1		99.99695		415.09601		50.1		99.99982		460.96522		50.1		100.02452		462.656		50.1		100.03822		463.56355		50.1		100.02389

		415.74399		50.125		100.00007		100.0245		415.62201		50.125		99.99587		415.358		50.125		100.0014		461.21422		50.125		100.0245		462.89878		50.125		100.03822		463.81444		50.125		100.02388

		416.00299		50.15		100.00105		100.02449		415.89001		50.15		99.99687		415.62201		50.15		100.00125		461.46033		50.15		100.02449		463.14033		50.15		100.03822		464.06677		50.15		100.02388

		416.26801		50.175		100.00346		100.02448		416.14899		50.175		99.99706		415.88901		50.175		100.00226		461.71044		50.175		100.02448		463.38067		50.175		100.03822		464.32111		50.175		100.02388

		416.52399		50.2		100.00342		100.02447		416.41299		50.2		99.99889		416.16		50.2		100.00277		461.96244		50.2		100.02447		463.62245		50.2		100.03822		464.57688		50.2		100.02388

		416.798		50.225		100.00305		100.02448		416.67401		50.225		99.99605		416.41901		50.225		100.00271		462.21355		50.225		100.02448		463.86722		50.225		100.03822		464.82988		50.225		100.02388

		417.06299		50.25		100.00254		100.02449		416.94299		50.25		99.99597		416.681		50.25		100.00296		462.45988		50.25		100.02449		464.11234		50.25		100.03823		465.08266		50.25		100.02389

		417.33099		50.275		99.99908		100.0245		417.20801		50.275		99.99438		416.953		50.275		100.00213		462.705		50.275		100.0245		464.35645		50.275		100.03824		465.33955		50.275		100.0239

		417.582		50.3		99.99885		100.02451		417.47101		50.3		99.99249		417.21399		50.3		100.00163		462.95		50.3		100.02451		464.60266		50.3		100.03825		465.59499		50.3		100.02392

		417.85199		50.325		100.00185		100.02453		417.73401		50.325		99.99481		417.47699		50.325		100.00005		463.19388		50.325		100.02453		464.85166		50.325		100.03826		465.84966		50.325		100.02394

		418.116		50.35		100.00092		100.02454		417.99701		50.35		99.99527		417.742		50.35		100.00052		463.43822		50.35		100.02454		465.10144		50.35		100.03827		466.10033		50.35		100.02396

		418.384		50.375		100.00102		100.02455		418.26901		50.375		99.99625		418.01401		50.375		100.00101		463.68266		50.375		100.02455		465.35011		50.375		100.03828		466.34744		50.375		100.02398

		418.64999		50.4		100.00024		100.02456		418.51901		50.4		99.99436		418.28299		50.4		100.00092		463.93111		50.4		100.02456		465.60044		50.4		100.03829		466.59555		50.4		100.024

		418.914		50.425		100.00317		100.02457		418.802		50.425		99.99785		418.54099		50.425		100.00118		464.17822		50.425		100.02457		465.85033		50.425		100.0383		466.84433		50.425		100.02402

		419.173		50.45		100.00312		100.02458		419.05399		50.45		99.99606		418.80899		50.45		100.00088		464.42633		50.45		100.02458		466.09633		50.45		100.0383		467.08966		50.45		100.02404

		419.44199		50.475		100.00286		100.02458		419.32199		50.475		99.99531		419.064		50.475		100.00175		464.67433		50.475		100.02458		466.33933		50.475		100.0383		467.34122		50.475		100.02406

		419.70999		50.5		100.00145		100.02457		419.57999		50.5		99.99622		419.32999		50.5		100.00039		464.92278		50.5		100.02457		466.58589		50.5		100.0383		467.594		50.5		100.02408

		419.97101		50.525		100.00232		100.02456		419.85101		50.525		99.99542		419.603		50.525		100.00203		465.17044		50.525		100.02456		466.82744		50.525		100.03829		467.84855		50.525		100.0241

		420.23199		50.55		100.00092		100.02455		420.11401		50.55		99.99683		419.85901		50.55		99.99923		465.42111		50.55		100.02455		467.06589		50.55		100.03828		468.10267		50.55		100.02412

		420.50201		50.575		100.00183		100.02454		420.38599		50.575		99.99652		420.134		50.575		99.99736		465.66789		50.575		100.02454		467.30411		50.575		100.03827		468.35656		50.575		100.02414

		420.76999		50.6		100.00313		100.02452		420.64001		50.6		99.99511		420.39099		50.6		100.00018		465.91567		50.6		100.02452		467.54789		50.6		100.03826		468.61223		50.6		100.02416

		421.02399		50.625		100.0038		100.02451		420.90799		50.625		99.99739		420.65399		50.625		100.00276		466.16022		50.625		100.02451		467.79578		50.625		100.03825		468.86956		50.625		100.02418

		421.29599		50.65		100.00254		100.02449		421.17099		50.65		99.99893		420.927		50.65		100.00702		466.403		50.65		100.02449		468.04245		50.65		100.03823		469.12389		50.65		100.0242

		421.556		50.675		100.00249		100.02448		421.439		50.675		99.99644		421.18701		50.675		100.00289		466.64322		50.675		100.02448		468.28656		50.675		100.03822		469.37845		50.675		100.02422

		421.82101		50.7		100.00131		100.02447		421.70499		50.7		99.99487		421.44101		50.7		99.99764		466.886		50.7		100.02447		468.53434		50.7		100.03821		469.627		50.7		100.02424

		422.078		50.725		100.00426		100.02447		421.96799		50.725		99.99782		421.70999		50.725		100.00483		467.12356		50.725		100.02447		468.77956		50.725		100.0382		469.87356		50.725		100.02427

		422.34299		50.75		100.00191		100.02448		422.22		50.75		99.99497		421.97501		50.75		100.00331		467.36845		50.75		100.02448		469.02811		50.75		100.0382		470.12133		50.75		100.0243

		422.612		50.775		100.00081		100.02449		422.492		50.775		99.99414		422.233		50.775		100.00378		467.61322		50.775		100.02449		469.27867		50.775		100.0382		470.36478		50.775		100.02433

		422.883		50.8		100.00333		100.0245		422.755		50.8		99.9986		422.508		50.8		100.00119		467.86289		50.8		100.0245		469.52689		50.8		100.0382		470.60955		50.8		100.02436

		423.138		50.825		100.00257		100.02452		423.01901		50.825		99.99673		422.76999		50.825		99.99878		468.11255		50.825		100.02452		469.77178		50.825		100.03821		470.85567		50.825		100.0244

		423.39999		50.85		100.00216		100.02454		423.28201		50.85		99.99685		423.039		50.85		99.99978		468.35711		50.85		100.02454		470.01256		50.85		100.03822		471.10355		50.85		100.02443

		423.67599		50.875		100.00241		100.02456		423.55301		50.875		99.99624		423.30499		50.875		100.00353		468.60233		50.875		100.02456		470.253		50.875		100.03823		471.35344		50.875		100.02446

		423.935		50.9		100.00123		100.02459		423.815		50.9		99.99453		423.564		50.9		100.00044		468.85366		50.9		100.02459		470.49433		50.9		100.03825		471.60622		50.9		100.02449

		424.20499		50.925		100.00153		100.02461		424.07999		50.925		99.99781		423.828		50.925		99.99941		469.10233		50.925		100.02461		470.73455		50.925		100.03826		471.85955		50.925		100.02452

		424.47501		50.95		100.00224		100.02464		424.34		50.95		99.99677		424.09399		50.95		99.99802		469.35411		50.95		100.02464		470.97811		50.95		100.03828		472.11611		50.95		100.02455

		424.72699		50.975		100.00098		100.02466		424.60599		50.975		99.9936		424.35901		50.975		100.00135		469.599		50.975		100.02466		471.22478		50.975		100.0383		472.37034		50.975		100.02457

		424.992		51		100.0021		100.02468		424.87701		51		99.99744		424.62399		51		99.99753		469.84389		51		100.02468		471.47122		51		100.03831		472.62567		51		100.02459

		425.25601		51.025		100.001		100.0247		425.14001		51.025		99.99678		424.89099		51.025		100.00541		470.08622		51.025		100.0247		471.71978		51.025		100.03833		472.87922		51.025		100.02461

		425.53101		51.05		100.00235		100.02472		425.41		51.05		99.99701		425.147		51.05		100.00409		470.32866		51.05		100.02472		471.96634		51.05		100.03834		473.135		51.05		100.02463

		425.79999		51.075		100.00626		100.02473		425.66599		51.075		99.99831		425.42899		51.075		99.99782		470.57378		51.075		100.02473		472.21478		51.075		100.03835		473.38734		51.075		100.02464

		426.05701		51.1		100.00189		100.02475		425.93799		51.1		99.99554		425.677		51.1		99.99708		470.82011		51.1		100.02475		472.46533		51.1		100.03837		473.63767		51.1		100.02465

		426.32101		51.125		100.00288		100.02476		426.19299		51.125		99.99782		425.948		51.125		100.00556		471.06811		51.125		100.02476		472.71544		51.125		100.03838		473.88678		51.125		100.02465

		426.58499		51.15		100.00293		100.02477		426.45099		51.15		99.99613		426.207		51.15		100.00011		471.31711		51.15		100.02477		472.96322		51.15		100.03839		474.13522		51.15		100.02466

		426.85101		51.175		100.00094		100.02479		426.72101		51.175		99.99638		426.48001		51.175		100.00504		471.56789		51.175		100.02479		473.21078		51.175		100.03841		474.38044		51.175		100.02467

		427.108		51.2		100.00199		100.0248		426.991		51.2		99.99849		426.741		51.2		100.00247		471.819		51.2		100.0248		473.45256		51.2		100.03842		474.63255		51.2		100.02467

		427.36801		51.225		99.99962		100.02482		427.25601		51.225		99.994		427.009		51.225		100.00172		472.072		51.225		100.02482		473.69567		51.225		100.03843		474.88488		51.225		100.02467

		427.64099		51.25		100.00068		100.02484		427.517		51.25		99.99767		427.26801		51.25		99.99529		472.32444		51.25		100.02484		473.93478		51.25		100.03845		475.13788		51.25		100.02468

		427.89801		51.275		99.99931		100.02487		427.77301		51.275		99.99765		427.53101		51.275		99.99937		472.57467		51.275		100.02487		474.174		51.275		100.03846		475.38955		51.275		100.02468

		428.16901		51.3		100.00177		100.0249		428.043		51.3		99.99344		427.79401		51.3		99.99797		472.82589		51.3		100.0249		474.41267		51.3		100.03847		475.64199		51.3		100.02468

		428.436		51.325		100.00263		100.02493		428.30301		51.325		99.9952		428.06799		51.325		99.99878		473.07844		51.325		100.02493		474.65311		51.325		100.03849		475.89488		51.325		100.02468

		428.70099		51.35		100.00227		100.02496		428.57101		51.35		99.99133		428.332		51.35		100.00324		473.32444		51.35		100.02496		474.89511		51.35		100.0385		476.14866		51.35		100.02468

		428.95801		51.375		100.00148		100.02499		428.83801		51.375		99.99687		428.59		51.375		100.00579		473.56955		51.375		100.02499		475.13955		51.375		100.03851		476.40666		51.375		100.02468

		429.224		51.4		100.00033		100.02501		429.09698		51.4		99.99713		428.862		51.4		99.99583		473.81488		51.4		100.02501		475.38489		51.4		100.03852		476.66389		51.4		100.02468

		429.48999		51.425		99.99991		100.02503		429.358		51.425		99.99516		429.11899		51.425		99.9991		474.05811		51.425		100.02503		475.63089		51.425		100.03853		476.91367		51.425		100.02467

		429.76001		51.45		100.00063		100.02505		429.62201		51.45		99.99564		429.38699		51.45		99.99931		474.29744		51.45		100.02505		475.87589		51.45		100.03854		477.16211		51.45		100.02466

		430.021		51.475		100.00034		100.02506		429.884		51.475		99.99623		429.64999		51.475		100.00392		474.54133		51.475		100.02506		476.12444		51.475		100.03854		477.412		51.475		100.02465

		430.28699		51.5		100.00124		100.02507		430.15201		51.5		99.99728		429.91501		51.5		100.00218		474.78911		51.5		100.02507		476.37511		51.5		100.03855		477.66111		51.5		100.02463

		430.552		51.525		100.00197		100.02506		430.41299		51.525		99.99518		430.17999		51.525		100.00032		475.03667		51.525		100.02506		476.62544		51.525		100.03855		477.90789		51.525		100.02462

		430.81299		51.55		100.00207		100.02506		430.68301		51.55		99.99645		430.439		51.55		99.99788		475.28322		51.55		100.02506		476.87289		51.55		100.03855		478.158		51.55		100.0246

		431.07401		51.575		100.00083		100.02504		430.952		51.575		99.99732		430.71201		51.575		99.99756		475.533		51.575		100.02504		477.12055		51.575		100.03856		478.408		51.575		100.02458

		431.341		51.6		100.00206		100.02503		431.21701		51.6		99.99431		430.96701		51.6		99.99771		475.78133		51.6		100.02503		477.36745		51.6		100.03856		478.65656		51.6		100.02457

		431.603		51.625		100.00246		100.02501		431.479		51.625		99.99813		431.23401		51.625		99.99637		476.02745		51.625		100.02501		477.61044		51.625		100.03857		478.90489		51.625		100.02456

		431.87399		51.65		100.00244		100.02499		431.74799		51.65		99.9963		431.50101		51.65		100.00108		476.27822		51.65		100.02499		477.85467		51.65		100.03858		479.15467		51.65		100.02455

		432.138		51.675		100.00107		100.02496		432.009		51.675		99.99395		431.76099		51.675		100.00135		476.52989		51.675		100.02496		478.10122		51.675		100.0386		479.40678		51.675		100.02454

		432.39999		51.7		100.00292		100.02494		432.26401		51.7		99.99568		432.02399		51.7		99.99645		476.77611		51.7		100.02494		478.34956		51.7		100.03862		479.65911		51.7		100.02454

		432.66299		51.725		100.00046		100.02492		432.52899		51.725		99.99423		432.29099		51.725		99.99707		477.02033		51.725		100.02492		478.59667		51.725		100.03865		479.90867		51.725		100.02455

		432.92499		51.75		100.00104		100.0249		432.79501		51.75		99.99513		432.55899		51.75		99.99845		477.26311		51.75		100.0249		478.84467		51.75		100.03869		480.16044		51.75		100.02456

		433.19101		51.775		100.00084		100.02488		433.06601		51.775		99.99416		432.82401		51.775		100.00146		477.50577		51.775		100.02488		479.09411		51.775		100.03873		480.40878		51.775		100.02458

		433.45401		51.8		100.00085		100.02487		433.32901		51.8		99.99533		433.08701		51.8		100.00114		477.74622		51.8		100.02487		479.34211		51.8		100.03877		480.65856		51.8		100.0246

		433.71399		51.825		100.00225		100.02485		433.59698		51.825		99.99586		433.358		51.825		100.00166		477.98588		51.825		100.02485		479.591		51.825		100.03882		480.90811		51.825		100.02462

		433.979		51.85		100.0024		100.02485		433.858		51.85		99.99438		433.61401		51.85		100.00289		478.23211		51.85		100.02485		479.843		51.85		100.03887		481.15722		51.85		100.02465

		434.25201		51.875		100.00042		100.02484		434.12601		51.875		99.99553		433.88199		51.875		100.00147		478.47511		51.875		100.02484		480.093		51.875		100.03892		481.40567		51.875		100.02468

		434.513		51.9		100.00034		100.02483		434.383		51.9		99.99471		434.13699		51.9		99.9982		478.72166		51.9		100.02483		480.33967		51.9		100.03898		481.65533		51.9		100.02471

		434.77701		51.925		100.00096		100.02483		434.647		51.925		99.99377		434.41199		51.925		100.00099		478.97044		51.925		100.02483		480.58367		51.925		100.03903		481.90834		51.925		100.02473

		435.035		51.95		100.00004		100.02482		434.90701		51.95		99.99494		434.66501		51.95		100.00059		479.21677		51.95		100.02482		480.82789		51.95		100.03908		482.16345		51.95		100.02476

		435.29501		51.975		100.0008		100.02482		435.17001		51.975		99.99526		434.94		51.975		100.00143		479.46366		51.975		100.02482		481.07067		51.975		100.03913		482.41911		51.975		100.02478

		435.56201		52		100.00008		100.02482		435.43799		52		99.99575		435.21201		52		99.99997		479.71366		52		100.02482		481.31167		52		100.03918		482.67422		52		100.0248

		435.83401		52.025		100.00279		100.02483		435.698		52.025		99.99818		435.46301		52.025		100.00268		479.96188		52.025		100.02483		481.55311		52.025		100.03922		482.93111		52.025		100.02482

		436.10001		52.05		100.0025		100.02484		435.97198		52.05		99.99608		435.73499		52.05		99.9993		480.21088		52.05		100.02484		481.80089		52.05		100.03926		483.18456		52.05		100.02484

		436.35999		52.075		100.00138		100.02485		436.23199		52.075		99.99522		436.00101		52.075		100.00037		480.45433		52.075		100.02485		482.04689		52.075		100.0393		483.44056		52.075		100.02485

		436.621		52.1		100.00124		100.02487		436.495		52.1		99.99748		436.25601		52.1		100.00067		480.70033		52.1		100.02487		482.29422		52.1		100.03933		483.69544		52.1		100.02486

		436.892		52.125		100.00118		100.0249		436.75601		52.125		99.99518		436.51901		52.125		100.00121		480.94244		52.125		100.0249		482.54233		52.125		100.03937		483.95322		52.125		100.02486

		437.15601		52.15		100.00276		100.02494		437.03201		52.15		99.99598		436.797		52.15		100.0011		481.182		52.15		100.02494		482.79089		52.15		100.03939		484.20422		52.15		100.02486

		437.41299		52.175		99.99969		100.02498		437.29001		52.175		99.99525		437.05301		52.175		100.00117		481.42122		52.175		100.02498		483.03844		52.175		100.03942		484.45345		52.175		100.02487

		437.69101		52.2		99.9997		100.02503		437.547		52.2		99.9958		437.31601		52.2		100.00194		481.66744		52.2		100.02503		483.28822		52.2		100.03945		484.70111		52.2		100.02487

		437.952		52.225		100.00127		100.02508		437.82199		52.225		99.99647		437.57599		52.225		99.99896		481.91378		52.225		100.02508		483.53744		52.225		100.03947		484.94689		52.225		100.02487

		438.21799		52.25		99.99967		100.02514		438.082		52.25		99.9947		437.849		52.25		100.00163		482.16278		52.25		100.02514		483.78599		52.25		100.03949		485.19545		52.25		100.02487

		438.487		52.275		100.00136		100.0252		438.34201		52.275		99.99574		438.112		52.275		99.9968		482.41156		52.275		100.0252		484.03144		52.275		100.03951		485.44956		52.275		100.02487

		438.74301		52.3		99.99944		100.02526		438.60101		52.3		99.99478		438.367		52.3		99.99933		482.66089		52.3		100.02526		484.27655		52.3		100.03952		485.70189		52.3		100.02486

		438.99799		52.325		100.00068		100.02532		438.86899		52.325		99.99518		438.64001		52.325		100.00245		482.91056		52.325		100.02532		484.51611		52.325		100.03953		485.95522		52.325		100.02486

		439.271		52.35		100.00007		100.02538		439.13		52.35		99.99593		438.89899		52.35		100.0033		483.16078		52.35		100.02538		484.75733		52.35		100.03954		486.20889		52.35		100.02486

		439.52499		52.375		100.00217		100.02544		439.397		52.375		99.99907		439.16699		52.375		100.00007		483.41234		52.375		100.02544		485.00056		52.375		100.03955		486.46344		52.375		100.02485

		439.793		52.4		100.00229		100.02549		439.668		52.4		99.99531		439.427		52.4		100.00152		483.66589		52.4		100.02549		485.25078		52.4		100.03955		486.71878		52.4		100.02485

		440.061		52.425		100.00252		100.02553		439.92499		52.425		99.99811		439.689		52.425		100.0027		483.91333		52.425		100.02553		485.49922		52.425		100.03955		486.97344		52.425		100.02485

		440.32501		52.45		100.00176		100.02556		440.19901		52.45		99.99407		439.95901		52.45		100.00123		484.15833		52.45		100.02556		485.745		52.45		100.03955		487.23289		52.45		100.02484

		440.58899		52.475		100.00183		100.02559		440.45499		52.475		99.99584		440.22299		52.475		100.00181		484.40233		52.475		100.02559		485.993		52.475		100.03955		487.48544		52.475		100.02484

		440.86099		52.5		100.00159		100.02561		440.71899		52.5		99.996		440.47299		52.5		100.0018		484.64644		52.5		100.02561		486.242		52.5		100.03954		487.73299		52.5		100.02483

		441.12		52.525		100.00157		100.02562		440.98599		52.525		99.99612		440.745		52.525		99.99956		484.88778		52.525		100.02562		486.49		52.525		100.03954		487.98189		52.525		100.02483

		441.38199		52.55		100.00058		100.02563		441.23901		52.55		99.99388		441.02802		52.55		99.99799		485.13033		52.55		100.02563		486.74122		52.55		100.03953		488.23		52.55		100.02483

		441.64899		52.575		100.00185		100.02563		441.517		52.575		99.99827		441.28601		52.575		100.00273		485.37522		52.575		100.02563		486.99144		52.575		100.03953		488.47166		52.575		100.02482

		441.918		52.6		100.00155		100.02563		441.76901		52.6		99.99815		441.54999		52.6		100.00283		485.62033		52.6		100.02563		487.24033		52.6		100.03954		488.71977		52.6		100.02482

		442.17999		52.625		100.00237		100.02563		442.039		52.625		99.99684		441.81601		52.625		100.00394		485.86522		52.625		100.02563		487.48377		52.625		100.03954		488.97255		52.625		100.02483

		442.44199		52.65		100.00241		100.02563		442.29999		52.65		99.9963		442.07901		52.65		99.99898		486.109		52.65		100.02563		487.72644		52.65		100.03955		489.22766		52.65		100.02483

		442.716		52.675		100.0029		100.02563		442.56601		52.675		99.99751		442.34698		52.675		100.00275		486.35244		52.675		100.02563		487.972		52.675		100.03957		489.48189		52.675		100.02484

		442.979		52.7		100.00101		100.02562		442.832		52.7		99.9951		442.60101		52.7		100.00295		486.59667		52.7		100.02562		488.21488		52.7		100.03959		489.73544		52.7		100.02485

		443.23499		52.725		100.00127		100.02562		443.08499		52.725		99.99564		442.87299		52.725		100.00054		486.84178		52.725		100.02562		488.45544		52.725		100.03961		489.98789		52.725		100.02487

		443.50101		52.75		100.00161		100.02562		443.35699		52.75		99.99655		443.129		52.75		100.00108		487.08655		52.75		100.02562		488.69844		52.75		100.03964		490.24		52.75		100.02488

		443.76401		52.775		100.00086		100.02562		443.62201		52.775		99.99537		443.39801		52.775		100.00077		487.332		52.775		100.02562		488.94644		52.775		100.03967		490.49311		52.775		100.0249

		444.02499		52.8		100.00435		100.02563		443.87799		52.8		100.00016		443.66299		52.8		100.00126		487.575		52.8		100.02563		489.195		52.8		100.0397		490.74878		52.8		100.02492

		444.293		52.825		100.00001		100.02563		444.14999		52.825		99.99525		443.92599		52.825		100.00126		487.81444		52.825		100.02563		489.44377		52.825		100.03973		490.99911		52.825		100.02494

		444.55499		52.85		100.00097		100.02564		444.41699		52.85		99.99682		444.19		52.85		100.00151		488.05478		52.85		100.02564		489.69222		52.85		100.03977		491.24467		52.85		100.02496

		444.82401		52.875		99.99993		100.02565		444.67999		52.875		99.99653		444.45999		52.875		100.00194		488.29789		52.875		100.02565		489.94366		52.875		100.0398		491.48834		52.875		100.02498

		445.09		52.9		100.0005		100.02566		444.94199		52.9		99.99496		444.72101		52.9		100.00099		488.53933		52.9		100.02566		490.19489		52.9		100.03983		491.73122		52.9		100.02501

		445.35001		52.925		100.00231		100.02567		445.20801		52.925		99.99722		444.983		52.925		100.00156		488.78255		52.925		100.02567		490.44667		52.925		100.03985		491.97522		52.925		100.02503

		445.612		52.95		100.00169		100.02568		445.47601		52.95		99.99357		445.255		52.95		100.00077		489.02744		52.95		100.02568		490.69822		52.95		100.03988		492.221		52.95		100.02505

		445.87601		52.975		99.99928		100.02569		445.737		52.975		99.99581		445.51801		52.975		99.99858		489.27955		52.975		100.02569		490.94656		52.975		100.0399		492.47167		52.975		100.02507

		446.14499		53		100.00066		100.0257		446.01001		53		99.99557		445.78		53		99.99914		489.52767		53		100.0257		491.19167		53		100.03992		492.72311		53		100.02509

		446.39801		53.025		100.00039		100.02571		446.263		53.025		99.99616		446.043		53.025		100.00024		489.77567		53.025		100.02571		491.43645		53.025		100.03993		492.97333		53.025		100.0251

		446.66699		53.05		99.99986		100.02572		446.52499		53.05		99.99756		446.315		53.05		99.99981		490.02544		53.05		100.02572		491.67967		53.05		100.03995		493.22534		53.05		100.02511

		446.94		53.075		100.00421		100.02573		446.798		53.075		99.99871		446.57199		53.075		100.00305		490.27544		53.075		100.02573		491.921		53.075		100.03995		493.47656		53.075		100.02513

		447.198		53.1		100.00012		100.02574		447.05801		53.1		99.99837		446.82901		53.1		100.00011		490.524		53.1		100.02574		492.15956		53.1		100.03996		493.73		53.1		100.02513

		447.47		53.125		100.003		100.02575		447.31601		53.125		99.9958		447.103		53.125		100.00195		490.77244		53.125		100.02575		492.40433		53.125		100.03997		493.98256		53.125		100.02514

		447.733		53.15		100.00149		100.02576		447.57501		53.15		99.99327		447.36899		53.15		99.99884		491.01989		53.15		100.02576		492.65355		53.15		100.03997		494.2349		53.15		100.02514

		447.98901		53.175		100.00127		100.02576		447.84299		53.175		99.9975		447.62399		53.175		100.00156		491.26489		53.175		100.02576		492.89978		53.175		100.03997		494.48734		53.175		100.02515

		448.25699		53.2		100.00187		100.02577		448.10699		53.2		99.99412		447.89801		53.2		100.00129		491.50489		53.2		100.02577		493.14822		53.2		100.03996		494.73501		53.2		100.02515

		448.521		53.225		99.99954		100.02577		448.375		53.225		99.99319		448.159		53.225		99.99904		491.74578		53.225		100.02577		493.396		53.225		100.03996		494.9829		53.225		100.02514

		448.79099		53.25		100.00089		100.02577		448.63599		53.25		99.99761		448.42401		53.25		100.00189		491.98711		53.25		100.02577		493.64367		53.25		100.03995		495.23123		53.25		100.02514

		449.04099		53.275		100.00113		100.02577		448.91299		53.275		99.99522		448.68799		53.275		100.0016		492.22978		53.275		100.02577		493.893		53.275		100.03994		495.47645		53.275		100.02514

		449.31201		53.3		100.00229		100.02577		449.172		53.3		99.99401		448.95099		53.3		100.00281		492.47911		53.3		100.02577		494.14478		53.3		100.03993		495.72101		53.3		100.02513

		449.57101		53.325		99.99912		100.02577		449.436		53.325		99.99531		449.21301		53.325		99.99964		492.72811		53.325		100.02577		494.39511		53.325		100.03991		495.97001		53.325		100.02512

		449.84399		53.35		99.99948		100.02577		449.70099		53.35		99.99605		449.47699		53.35		100.00122		492.978		53.35		100.02577		494.63834		53.35		100.03989		496.22134		53.35		100.02511

		450.10101		53.375		100.00093		100.02577		449.96899		53.375		99.99445		449.745		53.375		99.99939		493.228		53.375		100.02577		494.88178		53.375		100.03987		496.47223		53.375		100.0251

		450.367		53.4		100.00052		100.02576		450.23401		53.4		99.99522		450.00601		53.4		99.99958		493.47644		53.4		100.02576		495.12423		53.4		100.03985		496.72212		53.4		100.02509

		450.629		53.425		99.99996		100.02576		450.48901		53.425		99.99489		450.272		53.425		100.00093		493.72611		53.425		100.02576		495.36445		53.425		100.03982		496.97278		53.425		100.02508

		450.90399		53.45		100.00034		100.02575		450.754		53.45		99.99585		450.53299		53.45		99.99878		493.97478		53.45		100.02575		495.60434		53.45		100.0398		497.22267		53.45		100.02507

		451.172		53.475		100.00186		100.02575		451.01599		53.475		99.99646		450.793		53.475		100.00029		494.22444		53.475		100.02575		495.84856		53.475		100.03977		497.47145		53.475		100.02506

		451.42499		53.5		100.00142		100.02574		451.27301		53.5		99.99568		451.06		53.5		99.99839		494.473		53.5		100.02574		496.092		53.5		100.03975		497.72133		53.5		100.02504

		451.689		53.525		100.00231		100.02574		451.54199		53.525		99.99665		451.32101		53.525		100.00213		494.71456		53.525		100.02574		496.33467		53.525		100.03972		497.97478		53.525		100.02503

		451.95801		53.55		100.00316		100.02573		451.798		53.55		100.00012		451.60001		53.55		100.00226		494.95644		53.55		100.02573		496.57834		53.55		100.0397		498.22245		53.55		100.02501

		452.22101		53.575		99.99745		100.02573		452.06799		53.575		99.9946		451.85999		53.575		100.00002		495.198		53.575		100.02573		496.82222		53.575		100.03968		498.46567		53.575		100.025

		452.479		53.6		100.00028		100.02572		452.33401		53.6		99.99674		452.117		53.6		100.00059		495.43689		53.6		100.02572		497.06445		53.6		100.03967		498.70978		53.6		100.02498

		452.74701		53.625		100.00134		100.02572		452.59601		53.625		99.99401		452.392		53.625		100.0027		495.67655		53.625		100.02572		497.30911		53.625		100.03965		498.95522		53.625		100.02496

		453.013		53.65		100.00093		100.02572		452.866		53.65		99.99405		452.64899		53.65		100.00122		495.91889		53.65		100.02572		497.55634		53.65		100.03964		499.19944		53.65		100.02495

		453.27802		53.675		100.00096		100.02571		453.13101		53.675		100.00004		452.91199		53.675		100.00272		496.16533		53.675		100.02571		497.80411		53.675		100.03964		499.44544		53.675		100.02493

		453.539		53.7		99.99944		100.02571		453.38599		53.7		99.99486		453.18201		53.7		99.99845		496.41		53.7		100.02571		498.04789		53.7		100.03964		499.69411		53.7		100.02492

		453.80301		53.725		100.00183		100.02571		453.64499		53.725		99.99351		453.44199		53.725		100.00375		496.657		53.725		100.02571		498.29089		53.725		100.03964		499.94333		53.725		100.02491

		454.06299		53.75		99.99718		100.02571		453.91599		53.75		99.9928		453.703		53.75		99.99863		496.90433		53.75		100.02571		498.53378		53.75		100.03965		500.19278		53.75		100.0249

		454.33801		53.775		100.00102		100.02571		454.18399		53.775		99.99358		453.97		53.775		99.99727		497.15189		53.775		100.02571		498.77622		53.775		100.03965		500.44078		53.775		100.02489

		454.60101		53.8		99.99849		100.02571		454.44299		53.8		99.99234		454.237		53.8		100.00103		497.39978		53.8		100.02571		499.02		53.8		100.03966		500.691		53.8		100.02488

		454.866		53.825		100.00022		100.02571		454.69699		53.825		99.99513		454.50699		53.825		100.00005		497.64778		53.825		100.02571		499.26133		53.825		100.03968		500.94033		53.825		100.02488

		455.125		53.85		100.00041		100.02571		454.97		53.85		99.9962		454.76599		53.85		99.99979		497.89967		53.85		100.02571		499.50878		53.85		100.03969		501.19322		53.85		100.02488

		455.38699		53.875		100.00241		100.02572		455.23801		53.875		99.99257		455.03699		53.875		100.00067		498.14678		53.875		100.02572		499.75667		53.875		100.0397		501.445		53.875		100.02488

		455.65701		53.9		100.00414		100.02572		455.495		53.9		99.99644		455.306		53.9		100.00055		498.38778		53.9		100.02572		500.00345		53.9		100.03972		501.69433		53.9		100.02488

		455.91699		53.925		100.00055		100.02573		455.76501		53.925		99.99438		455.56601		53.925		99.99873		498.62789		53.925		100.02573		500.253		53.925		100.03974		501.943		53.925		100.02488

		456.17099		53.95		100.00207		100.02574		456.021		53.95		99.99505		455.82501		53.95		100.00013		498.86834		53.95		100.02574		500.50256		53.95		100.03975		502.19089		53.95		100.02489

		456.44199		53.975		100.00142		100.02575		456.289		53.975		99.99458		456.091		53.975		100.00113		499.107		53.975		100.02575		500.75067		53.975		100.03977		502.43689		53.975		100.02489

		456.70099		54		100.0017		100.02576		456.55801		54		99.99556		456.349		54		100.00108		499.34844		54		100.02576		500.99989		54		100.03979		502.68366		54		100.0249

		456.96701		54.025		100.00428		100.02578		456.81201		54.025		99.99601		456.62399		54.025		100.00282		499.59422		54.025		100.02578		501.25078		54.025		100.0398		502.93389		54.025		100.02491

		457.23001		54.05		99.99861		100.02579		457.082		54.05		99.99586		456.88699		54.05		99.99956		499.84156		54.05		100.02579		501.50111		54.05		100.03982		503.18811		54.05		100.02492

		457.49799		54.075		100.00104		100.02581		457.34601		54.075		99.99498		457.15302		54.075		100.0023		500.09		54.075		100.02581		501.74522		54.075		100.03985		503.43989		54.075		100.02494

		457.76099		54.1		99.99969		100.02582		457.60699		54.1		99.99518		457.41299		54.1		99.99942		500.33989		54.1		100.02582		501.98778		54.1		100.03987		503.691		54.1		100.02495

		458.02701		54.125		100.0002		100.02584		457.87299		54.125		99.99587		457.677		54.125		99.99995		500.59044		54.125		100.02584		502.233		54.125		100.0399		503.94278		54.125		100.02497

		458.28		54.15		100.00021		100.02586		458.13699		54.15		99.99439		457.94299		54.15		100.00006		500.84222		54.15		100.02586		502.47266		54.15		100.03993		504.19244		54.15		100.02498

		458.54501		54.175		100.00052		100.02587		458.397		54.175		99.99462		458.202		54.175		100.00291		501.09689		54.175		100.02587		502.712		54.175		100.03996		504.44444		54.175		100.02499

		458.82101		54.2		100.00178		100.02589		458.66699		54.2		99.99819		458.47501		54.2		100.00395		501.34989		54.2		100.02589		502.95477		54.2		100.04		504.69533		54.2		100.02501

		459.07101		54.225		100.00161		100.0259		458.93399		54.225		99.99622		458.73599		54.225		100.00044		501.59889		54.225		100.0259		503.20188		54.225		100.04004		504.94622		54.225		100.02502

		459.33899		54.25		99.99874		100.02592		459.19		54.25		99.99665		458.99301		54.25		99.99974		501.84289		54.25		100.02592		503.44622		54.25		100.04008		505.19167		54.25		100.02503

		459.604		54.275		100.00059		100.02593		459.452		54.275		99.99551		459.263		54.275		100		502.08733		54.275		100.02593		503.692		54.275		100.04012		505.43489		54.275		100.02504

		459.86899		54.3		100.00046		100.02594		459.72501		54.3		99.99656		459.52802		54.3		100.0004		502.32833		54.3		100.02594		503.93877		54.3		100.04017		505.67733		54.3		100.02505

		460.129		54.325		100.00005		100.02594		459.98801		54.325		99.99593		459.79001		54.325		99.99933		502.56855		54.325		100.02594		504.18711		54.325		100.04022		505.91934		54.325		100.02505

		460.397		54.35		100.00111		100.02595		460.241		54.35		99.99733		460.05701		54.35		100.0014		502.80967		54.35		100.02595		504.43422		54.35		100.04027		506.15745		54.35		100.02505

		460.66501		54.375		100.00035		100.02595		460.509		54.375		99.9954		460.31699		54.375		99.99975		503.05444		54.375		100.02595		504.68333		54.375		100.04031		506.39767		54.375		100.02505

		460.92999		54.4		100.00059		100.02594		460.78		54.4		99.99504		460.58401		54.4		99.99999		503.29733		54.4		100.02594		504.93144		54.4		100.04036		506.64211		54.4		100.02504

		461.186		54.425		100.00223		100.02594		461.03799		54.425		99.99865		460.85101		54.425		100.00148		503.54388		54.425		100.02594		505.17567		54.425		100.0404		506.88767		54.425		100.02503

		461.452		54.45		100.00022		100.02594		461.31		54.45		99.99576		461.108		54.45		100.00021		503.79089		54.45		100.02594		505.41733		54.45		100.04045		507.13367		54.45		100.02502

		461.716		54.475		100.00014		100.02594		461.56299		54.475		99.99635		461.375		54.475		99.99947		504.03822		54.475		100.02594		505.65744		54.475		100.04049		507.37878		54.475		100.02501

		461.97501		54.5		100.00138		100.02594		461.83099		54.5		99.9974		461.64099		54.5		100.00132		504.28511		54.5		100.02594		505.89611		54.5		100.04053		507.62522		54.5		100.025

		462.24701		54.525		100.00039		100.02594		462.095		54.525		99.99608		461.901		54.525		100.00027		504.53233		54.525		100.02594		506.13222		54.525		100.04057		507.87144		54.525		100.02499

		462.513		54.55		100.00202		100.02594		462.36499		54.55		99.99567		462.17099		54.55		100.00199		504.781		54.55		100.02594		506.36589		54.55		100.0406		508.11778		54.55		100.02497

		462.78		54.575		100.00077		100.02594		462.62799		54.575		99.99451		462.431		54.575		99.99755		505.02955		54.575		100.02594		506.60722		54.575		100.04064		508.36811		54.575		100.02496

		463.04001		54.6		99.99987		100.02595		462.888		54.6		99.99516		462.698		54.6		100.0017		505.27144		54.6		100.02595		506.84766		54.6		100.04067		508.61989		54.6		100.02496

		463.29599		54.625		100.0003		100.02596		463.15201		54.625		99.99496		462.96701		54.625		100.00056		505.51089		54.625		100.02596		507.08822		54.625		100.04069		508.86689		54.625		100.02495

		463.564		54.65		100.00096		100.02597		463.41		54.65		99.99502		463.22601		54.65		100.00285		505.74878		54.65		100.02597		507.33033		54.65		100.04071		509.11166		54.65		100.02495

		463.832		54.675		100.00138		100.02598		463.67099		54.675		99.99578		463.48499		54.675		99.99988		505.98566		54.675		100.02598		507.57199		54.675		100.04073		509.35467		54.675		100.02494

		464.10001		54.7		99.99946		100.026		463.944		54.7		99.99376		463.75299		54.7		99.99703		506.22144		54.7		100.026		507.81688		54.7		100.04075		509.603		54.7		100.02495

		464.362		54.725		99.99877		100.02601		464.19699		54.725		99.99166		464.022		54.725		99.99805		506.45955		54.725		100.02601		508.06366		54.725		100.04077		509.84622		54.725		100.02495

		464.621		54.75		100.00024		100.02603		464.452		54.75		99.99467		464.29501		54.75		100.00103		506.701		54.75		100.02603		508.31166		54.75		100.04078		510.09555		54.75		100.02496

		464.88199		54.775		99.99999		100.02605		464.72601		54.775		99.99417		464.55701		54.775		100.00047		506.94233		54.775		100.02605		508.56177		54.775		100.04079		510.34566		54.775		100.02497

		465.146		54.8		100.00199		100.02607		464.99301		54.8		99.99322		464.81201		54.8		99.99966		507.18522		54.8		100.02607		508.80544		54.8		100.0408		510.59811		54.8		100.02498

		465.41199		54.825		100.00055		100.02609		465.25201		54.825		99.99464		465.08701		54.825		100.00004		507.43088		54.825		100.02609		509.05033		54.825		100.04081		510.84633		54.825		100.02499

		465.67801		54.85		99.99983		100.02612		465.526		54.85		99.99616		465.354		54.85		99.99889		507.67766		54.85		100.02612		509.29633		54.85		100.04082		511.09144		54.85		100.02501

		465.935		54.875		100.0013		100.02615		465.78101		54.875		99.99682		465.60901		54.875		100.0017		507.92467		54.875		100.02615		509.54422		54.875		100.04084		511.33911		54.875		100.02503

		466.20099		54.9		100.00051		100.02618		466.04599		54.9		99.99685		465.86301		54.9		100.00115		508.17322		54.9		100.02618		509.78911		54.9		100.04085		511.58688		54.9		100.02505

		466.46399		54.925		99.99826		100.02621		466.30899		54.925		99.99568		466.13199		54.925		100.0026		508.42311		54.925		100.02621		510.038		54.925		100.04087		511.83555		54.925		100.02507

		466.73999		54.95		100.00042		100.02625		466.573		54.95		99.99414		466.39499		54.95		99.9994		508.67133		54.95		100.02625		510.288		54.95		100.04089		512.08722		54.95		100.02509

		466.99701		54.975		99.99885		100.02629		466.832		54.975		99.99571		466.66501		54.975		99.99952		508.91622		54.975		100.02629		510.54256		54.975		100.04092		512.33111		54.975		100.02512

		467.26501		55		100.00052		100.02634		467.09299		55		99.99448		466.92899		55		99.9995		509.15967		55		100.02634		510.79545		55		100.04095		512.57433		55		100.02515

		467.522		55.025		100.00132		100.02639		467.35901		55.025		99.99676		467.186		55.025		100.00131		509.401		55.025		100.02639		511.04656		55.025		100.04098		512.814		55.025		100.02518

		467.79099		55.05		100.0013		100.02644		467.62701		55.05		99.99671		467.45599		55.05		99.99905		509.64455		55.05		100.02644		511.29712		55.05		100.04102		513.05545		55.05		100.02521

		468.05399		55.075		100.00181		100.02649		467.89001		55.075		99.99529		467.71701		55.075		99.99912		509.88622		55.075		100.02649		511.54723		55.075		100.04106		513.29678		55.075		100.02524

		468.31		55.1		100.00098		100.02654		468.15201		55.1		99.99462		467.98499		55.1		100.00015		510.13534		55.1		100.02654		511.79456		55.1		100.0411		513.54245		55.1		100.02526

		468.56		55.125		100.00093		100.02659		468.42099		55.125		99.99531		468.24799		55.125		99.99972		510.38645		55.125		100.02659		512.045		55.125		100.04114		513.794		55.125		100.02529

		468.82599		55.15		100.00001		100.02663		468.677		55.15		99.99281		468.51599		55.15		99.99889		510.63889		55.15		100.02663		512.29023		55.15		100.04117		514.04222		55.15		100.02532

		469.10199		55.175		99.9997		100.02667		468.93399		55.175		99.99342		468.767		55.175		100.00106		510.88912		55.175		100.02667		512.53345		55.175		100.04121		514.28911		55.175		100.02534

		469.371		55.2		100.00114		100.0267		469.198		55.2		99.99373		469.03601		55.2		100.00132		511.13922		55.2		100.0267		512.76945		55.2		100.04125		514.53633		55.2		100.02536

		469.629		55.225		100.00131		100.02673		469.45401		55.225		99.99483		469.30399		55.225		100.00106		511.38945		55.225		100.02673		513.00711		55.225		100.04128		514.78488		55.225		100.02537

		469.89401		55.25		100.00194		100.02676		469.729		55.25		99.99535		469.55801		55.25		99.99953		511.63845		55.25		100.02676		513.24622		55.25		100.0413		515.03278		55.25		100.02538

		470.14099		55.275		100.00257		100.02677		469.987		55.275		99.99715		469.82901		55.275		100.00058		511.88756		55.275		100.02677		513.48489		55.275		100.04133		515.282		55.275		100.02539

		470.40601		55.3		100.00139		100.02678		470.25299		55.3		99.99478		470.086		55.3		100.00376		512.13889		55.3		100.02678		513.72556		55.3		100.04135		515.53288		55.3		100.02539

		470.67499		55.325		100.00187		100.02679		470.513		55.325		99.99445		470.35199		55.325		100.00119		512.37945		55.325		100.02679		513.96945		55.325		100.04136		515.78033		55.325		100.02539

		470.94199		55.35		100.00331		100.02679		470.772		55.35		99.99411		470.617		55.35		100.00169		512.61767		55.35		100.02679		514.21178		55.35		100.04137		516.02289		55.35		100.02538

		471.211		55.375		100.00187		100.02679		471.03601		55.375		99.99328		470.879		55.375		99.99898		512.857		55.375		100.02679		514.45467		55.375		100.04138		516.26434		55.375		100.02537

		471.47699		55.4		99.99986		100.02678		471.30801		55.4		99.99354		471.14899		55.4		100.00043		513.09333		55.4		100.02678		514.69767		55.4		100.04139		516.50755		55.4		100.02536

		471.737		55.425		99.99857		100.02677		471.57501		55.425		99.9927		471.41599		55.425		100.00231		513.32778		55.425		100.02677		514.94522		55.425		100.0414		516.75022		55.425		100.02535

		471.995		55.45		100.00347		100.02676		471.82901		55.45		99.99652		471.67401		55.45		100.0008		513.56622		55.45		100.02676		515.19122		55.45		100.04141		516.99611		55.45		100.02534

		472.26001		55.475		99.99916		100.02675		472.09799		55.475		99.99322		471.94199		55.475		99.99623		513.81067		55.475		100.02675		515.43578		55.475		100.04141		517.24567		55.475		100.02532

		472.521		55.5		100.00329		100.02673		472.36401		55.5		99.99557		472.20499		55.5		100.00363		514.05089		55.5		100.02673		515.68256		55.5		100.04142		517.49478		55.5		100.02531

		472.789		55.525		100.00055		100.02671		472.625		55.525		99.99366		472.46301		55.525		100.00176		514.29145		55.525		100.02671		515.92733		55.525		100.04143		517.74367		55.525		100.02529

		473.05499		55.55		100.0002		100.02669		472.888		55.55		99.9952		472.73401		55.55		100.00025		514.53556		55.55		100.02669		516.17133		55.55		100.04144		517.99434		55.55		100.02528

		473.314		55.575		100.00314		100.02667		473.14401		55.575		99.99718		472.99701		55.575		100.00028		514.78178		55.575		100.02667		516.41567		55.575		100.04145		518.24445		55.575		100.02526

		473.577		55.6		100.00056		100.02665		473.41699		55.6		99.99322		473.26199		55.6		99.99972		515.02467		55.6		100.02665		516.65866		55.6		100.04146		518.49678		55.6		100.02525

		473.83701		55.625		100.00079		100.02663		473.67999		55.625		99.99682		473.522		55.625		99.99994		515.271		55.625		100.02663		516.89855		55.625		100.04147		518.74756		55.625		100.02524

		474.10999		55.65		100.00088		100.02662		473.94101		55.65		99.99496		473.79599		55.65		100.00138		515.51822		55.65		100.02662		517.14678		55.65		100.04148		519.00111		55.65		100.02524

		474.36499		55.675		100.00052		100.0266		474.211		55.675		99.99705		474.05301		55.675		100.00295		515.76166		55.675		100.0266		517.39711		55.675		100.04149		519.252		55.675		100.02523

		474.621		55.7		100.00069		100.02658		474.47101		55.7		99.99568		474.314		55.7		99.99662		516.00066		55.7		100.02658		517.64678		55.7		100.0415		519.50067		55.7		100.02522

		474.89801		55.725		100.00034		100.02657		474.742		55.725		99.99406		474.577		55.725		99.99825		516.24289		55.725		100.02657		517.89555		55.725		100.04151		519.74689		55.725		100.02521

		475.15302		55.75		100.00028		100.02656		475.00201		55.75		99.99388		474.83899		55.75		99.99819		516.48444		55.75		100.02656		518.14477		55.75		100.04152		519.99356		55.75		100.0252

		475.41901		55.775		100.00131		100.02655		475.26599		55.775		99.99526		475.103		55.775		100.00124		516.724		55.775		100.02655		518.39322		55.775		100.04153		520.23467		55.775		100.0252

		475.68201		55.8		99.99976		100.02655		475.522		55.8		99.99597		475.37299		55.8		100.0005		516.96311		55.8		100.02655		518.64221		55.8		100.04153		520.48123		55.8		100.02519

		475.94101		55.825		99.99906		100.02655		475.776		55.825		99.99503		475.64001		55.825		99.99956		517.20767		55.825		100.02655		518.89155		55.825		100.04154		520.73145		55.825		100.02519

		476.19901		55.85		100.00009		100.02656		476.047		55.85		99.99721		475.897		55.85		100.00221		517.45467		55.85		100.02656		519.1421		55.85		100.04154		520.98079		55.85		100.02518

		476.461		55.875		99.99961		100.02657		476.311		55.875		99.9965		476.15601		55.875		100.00213		517.70167		55.875		100.02657		519.38477		55.875		100.04155		521.22923		55.875		100.02518

		476.72101		55.9		99.99798		100.02658		476.57501		55.9		99.99513		476.42599		55.9		99.99839		517.94934		55.9		100.02658		519.62566		55.9		100.04155		521.47801		55.9		100.02517

		476.98999		55.925		100.00089		100.0266		476.84299		55.925		99.99644		476.68799		55.925		99.99967		518.19934		55.925		100.0266		519.86699		55.925		100.04155		521.72567		55.925		100.02517

		477.26099		55.95		99.99877		100.02662		477.09299		55.95		99.99464		476.952		55.95		100.0008		518.44623		55.95		100.02662		520.10777		55.95		100.04155		521.97467		55.95		100.02517

		477.51599		55.975		100.00142		100.02665		477.354		55.975		99.99488		477.21399		55.975		100.00135		518.69267		55.975		100.02665		520.35044		55.975		100.04154		522.22323		55.975		100.02516

		477.78699		56		99.99987		100.02668		477.61301		56		99.99462		477.478		56		99.99869		518.94156		56		100.02668		520.598		56		100.04154		522.47456		56		100.02516

		478.048		56.025		99.99957		100.0267		477.884		56.025		99.99224		477.73499		56.025		99.99999		519.18867		56.025		100.0267		520.84733		56.025		100.04154		522.72222		56.025		100.02516

		478.31699		56.05		100.00007		100.02673		478.15399		56.05		99.99646		478.00201		56.05		99.99782		519.43401		56.05		100.02673		521.09711		56.05		100.04154		522.96556		56.05		100.02516

		478.56799		56.075		100.00229		100.02676		478.41699		56.075		99.99571		478.26599		56.075		100.0016		519.67701		56.075		100.02676		521.34888		56.075		100.04153		523.21111		56.075		100.02516

		478.83401		56.1		100.00173		100.02679		478.68201		56.1		99.99611		478.53699		56.1		99.99936		519.91945		56.1		100.02679		521.59999		56.1		100.04153		523.45521		56.1		100.02516

		479.09		56.125		100.001		100.02681		478.93701		56.125		99.99698		478.797		56.125		100.00272		520.15878		56.125		100.02681		521.85066		56.125		100.04153		523.69889		56.125		100.02515

		479.358		56.15		100.00101		100.02684		479.20801		56.15		99.99548		479.064		56.15		99.99832		520.39878		56.15		100.02684		522.10211		56.15		100.04153		523.94333		56.15		100.02515

		479.63101		56.175		100.00149		100.02686		479.47699		56.175		99.99494		479.32101		56.175		99.99646		520.644		56.175		100.02686		522.35422		56.175		100.04153		524.19411		56.175		100.02515

		479.88699		56.2		99.99972		100.02688		479.728		56.2		99.99379		479.586		56.2		99.99989		520.89011		56.2		100.02688		522.60544		56.2		100.04153		524.448		56.2		100.02514

		480.14301		56.225		99.99936		100.02689		479.995		56.225		99.99702		479.85599		56.225		99.993		521.13722		56.225		100.02689		522.85266		56.225		100.04154		524.70167		56.225		100.02513

		480.41599		56.25		100.00109		100.0269		480.26199		56.25		99.99726		480.12299		56.25		99.99289		521.38566		56.25		100.0269		523.09544		56.25		100.04155		524.953		56.25		100.02513

		480.68701		56.275		100.00014		100.0269		480.52301		56.275		99.99668		480.38		56.275		99.99833		521.63188		56.275		100.0269		523.33733		56.275		100.04156		525.20456		56.275		100.02512

		480.935		56.3		100.0006		100.0269		480.784		56.3		99.99286		480.638		56.3		100.0019		521.87877		56.3		100.0269		523.581		56.3		100.04157		525.45478		56.3		100.0251

		481.19601		56.325		99.99844		100.0269		481.04999		56.325		99.99412		480.89499		56.325		100.00247		522.12633		56.325		100.0269		523.82134		56.325		100.04158		525.708		56.325		100.02509

		481.466		56.35		100.00055		100.0269		481.31201		56.35		99.99565		481.16299		56.35		100.00089		522.37777		56.35		100.0269		524.06567		56.35		100.04159		525.96055		56.35		100.02508

		481.72299		56.375		100.00169		100.02689		481.56799		56.375		99.99602		481.42999		56.375		99.9998		522.62822		56.375		100.02689		524.30956		56.375		100.04161		526.21344		56.375		100.02507

		481.98599		56.4		100.00001		100.02688		481.823		56.4		99.99418		481.69101		56.4		99.99708		522.87455		56.4		100.02688		524.55578		56.4		100.04162		526.45978		56.4		100.02506

		482.241		56.425		100.00041		100.02687		482.09399		56.425		99.99445		481.95801		56.425		100.00144		523.11855		56.425		100.02687		524.80189		56.425		100.04163		526.70433		56.425		100.02505

		482.51999		56.45		99.99944		100.02686		482.36401		56.45		99.99548		482.22699		56.45		99.9991		523.35767		56.45		100.02686		525.04645		56.45		100.04163		526.94845		56.45		100.02504

		482.76501		56.475		100.00144		100.02685		482.62201		56.475		99.99639		482.48901		56.475		100.00088		523.59789		56.475		100.02685		525.29201		56.475		100.04164		527.19556		56.475		100.02504

		483.039		56.5		100.00033		100.02684		482.88599		56.5		99.99743		482.74301		56.5		100.0035		523.83744		56.5		100.02684		525.54068		56.5		100.04164		527.43856		56.5		100.02503

		483.30301		56.525		100.00151		100.02683		483.15799		56.525		99.99607		483.00601		56.525		99.99857		524.08255		56.525		100.02683		525.78745		56.525		100.04164		527.68955		56.525		100.02503

		483.56601		56.55		99.99849		100.02682		483.41101		56.55		99.99505		483.27399		56.55		99.99621		524.32833		56.55		100.02682		526.03778		56.55		100.04163		527.94189		56.55		100.02503

		483.82199		56.575		100.00045		100.02682		483.672		56.575		99.99323		483.534		56.575		100.00461		524.57488		56.575		100.02682		526.28412		56.575		100.04162		528.19301		56.575		100.02503

		484.091		56.6		100.00052		100.02681		483.939		56.6		99.99462		483.797		56.6		100.00431		524.82121		56.6		100.02681		526.53189		56.6		100.04161		528.4449		56.6		100.02503

		484.35999		56.625		99.99899		100.02681		484.20499		56.625		99.99303		484.06201		56.625		100.00106		525.06544		56.625		100.02681		526.77567		56.625		100.0416		528.69723		56.625		100.02504

		484.62		56.65		99.99921		100.02681		484.47		56.65		99.9927		484.32101		56.65		99.99841		525.31199		56.65		100.02681		527.01866		56.65		100.04158		528.95001		56.65		100.02504

		484.88501		56.675		99.99995		100.02681		484.73001		56.675		99.99502		484.59201		56.675		100.00028		525.5621		56.675		100.02681		527.26066		56.675		100.04157		529.202		56.675		100.02505

		485.14401		56.7		99.99999		100.02682		485		56.7		99.99367		484.85599		56.7		99.99703		525.8091		56.7		100.02682		527.50233		56.7		100.04156		529.45289		56.7		100.02506

		485.41		56.725		99.99771		100.02682		485.255		56.725		99.99548		485.11499		56.725		99.99848		526.05465		56.725		100.02682		527.74832		56.725		100.04155		529.70667		56.725		100.02507

		485.66299		56.75		100.00025		100.02683		485.51801		56.75		99.99707		485.383		56.75		100.00126		526.29332		56.75		100.02683		527.99366		56.75		100.04155		529.95211		56.75		100.02508

		485.927		56.775		99.99946		100.02684		485.785		56.775		99.99767		485.646		56.775		100.00109		526.5361		56.775		100.02684		528.23688		56.775		100.04155		530.19567		56.775		100.02509

		486.186		56.8		100.00059		100.02685		486.04501		56.8		99.99483		485.90201		56.8		100.00299		526.7751		56.8		100.02685		528.48244		56.8		100.04156		530.44122		56.8		100.0251

		486.453		56.825		99.9998		100.02686		486.31201		56.825		99.99351		486.16299		56.825		99.99969		527.01232		56.825		100.02686		528.72699		56.825		100.04157		530.68433		56.825		100.02512

		486.72101		56.85		100.00093		100.02688		486.57101		56.85		99.99556		486.435		56.85		99.99716		527.25288		56.85		100.02688		528.97455		56.85		100.04159		530.929		56.85		100.02513

		486.97501		56.875		100.00093		100.02689		486.84399		56.875		99.99482		486.70001		56.875		100.00251		527.4911		56.875		100.02689		529.22266		56.875		100.04161		531.17767		56.875		100.02514

		487.241		56.9		100.00231		100.02691		487.091		56.9		99.99391		486.96899		56.9		100.0009		527.73722		56.9		100.02691		529.47122		56.9		100.04164		531.42634		56.9		100.02516

		487.51001		56.925		99.99916		100.02692		487.36801		56.925		99.99433		487.22299		56.925		100.00124		527.98355		56.925		100.02692		529.72089		56.925		100.04167		531.67533		56.925		100.02517

		487.76401		56.95		100.00003		100.02694		487.629		56.95		99.99565		487.49301		56.95		100.00114		528.23111		56.95		100.02694		529.96356		56.95		100.04169		531.92556		56.95		100.02518

		488.034		56.975		99.9997		100.02696		487.897		56.975		99.99415		487.75101		56.975		100.00236		528.48022		56.975		100.02696		530.20856		56.975		100.04172		532.17645		56.975		100.02519

		488.29401		57		100.00162		100.02698		488.16		57		99.99549		488.01599		57		100.00005		528.72755		57		100.02698		530.45489		57		100.04175		532.42601		57		100.0252

		488.552		57.025		100.00033		100.02701		488.40701		57.025		99.99691		488.27899		57.025		100.0011		528.97811		57.025		100.02701		530.69744		57.025		100.04178		532.67223		57.025		100.02521

		488.80899		57.05		100.00079		100.02703		488.681		57.05		99.99597		488.54501		57.05		100.00118		529.22766		57.05		100.02703		530.94044		57.05		100.0418		532.92156		57.05		100.02522

		489.07901		57.075		99.99948		100.02706		488.936		57.075		99.99575		488.80099		57.075		100.00303		529.47688		57.075		100.02706		531.18433		57.075		100.04182		533.17001		57.075		100.02523

		489.35199		57.1		99.99945		100.02709		489.19901		57.1		99.993		489.07001		57.1		100.00343		529.73055		57.1		100.02709		531.43089		57.1		100.04184		533.4139		57.1		100.02523

		489.61401		57.125		100.00194		100.02711		489.46701		57.125		99.99592		489.32599		57.125		99.99909		529.97566		57.125		100.02711		531.67723		57.125		100.04185		533.6599		57.125		100.02524

		489.87		57.15		100.00199		100.02715		489.72501		57.15		99.99387		489.58899		57.15		100.00111		530.22044		57.15		100.02715		531.92367		57.15		100.04186		533.90257		57.15		100.02525

		490.13599		57.175		100.00081		100.02718		490.00101		57.175		99.99493		489.862		57.175		100.00123		530.46699		57.175		100.02718		532.17145		57.175		100.04187		534.14735		57.175		100.02525

		490.39499		57.2		100.00055		100.02721		490.259		57.2		99.99591		490.11801		57.2		100.00087		530.71288		57.2		100.02721		532.41889		57.2		100.04188		534.39145		57.2		100.02526

		490.66		57.225		99.99974		100.02723		490.51599		57.225		99.99836		490.38901		57.225		100.00141		530.95655		57.225		100.02723		532.66767		57.225		100.04188		534.63978		57.225		100.02526

		490.91901		57.25		100.00215		100.02726		490.77701		57.25		99.99416		490.64999		57.25		100.00203		531.20566		57.25		100.02726		532.91857		57.25		100.04189		534.89356		57.25		100.02527

		491.185		57.275		100.00026		100.02729		491.04401		57.275		99.99316		490.91699		57.275		99.99996		531.45944		57.275		100.02729		533.16912		57.275		100.04189		535.14712		57.275		100.02528

		491.44601		57.3		100.00067		100.02731		491.31		57.3		99.99518		491.177		57.3		99.99932		531.71466		57.3		100.02731		533.41745		57.3		100.0419		535.40112		57.3		100.02529

		491.707		57.325		100.0006		100.02734		491.57401		57.325		99.99715		491.435		57.325		100.00061		531.96811		57.325		100.02734		533.66423		57.325		100.04191		535.65445		57.325		100.0253

		491.97198		57.35		100.00042		100.02736		491.82001		57.35		99.99662		491.702		57.35		100.00123		532.2231		57.35		100.02736		533.91212		57.35		100.04192		535.90723		57.35		100.02531

		492.23099		57.375		100.00246		100.02738		492.09201		57.375		99.99524		491.95901		57.375		100.00178		532.47744		57.375		100.02738		534.15923		57.375		100.04193		536.16222		57.375		100.02532

		492.496		57.4		99.99733		100.02739		492.36801		57.4		99.99507		492.228		57.4		100		532.72965		57.4		100.02739		534.40445		57.4		100.04195		536.41423		57.4		100.02533

		492.76599		57.425		99.99974		100.02741		492.62601		57.425		99.9945		492.491		57.425		100.00403		532.98421		57.425		100.02741		534.65201		57.425		100.04196		536.66745		57.425		100.02534

		493.03		57.45		100.00094		100.02742		492.89099		57.45		99.99388		492.74899		57.45		100.00174		533.23821		57.45		100.02742		534.89979		57.45		100.04198		536.91501		57.45		100.02535

		493.28101		57.475		100.00169		100.02744		493.14999		57.475		99.99573		493.00699		57.475		99.99954		533.48399		57.475		100.02744		535.14767		57.475		100.042		537.15823		57.475		100.02536

		493.54099		57.5		99.99928		100.02745		493.42099		57.5		99.99284		493.27802		57.5		100.00002		533.72699		57.5		100.02745		535.39712		57.5		100.04202		537.40146		57.5		100.02537

		493.811		57.525		100.00025		100.02746		493.67401		57.525		99.99535		493.53799		57.525		100.0004		533.97032		57.525		100.02746		535.64667		57.525		100.04204		537.64323		57.525		100.02539

		494.069		57.55		100.00021		100.02747		493.94101		57.55		99.99482		493.80301		57.55		100.00138		534.2111		57.55		100.02747		535.89456		57.55		100.04207		537.88489		57.55		100.0254

		494.34201		57.575		99.99927		100.02748		494.19901		57.575		99.99324		494.065		57.575		100.0004		534.45132		57.575		100.02748		536.14133		57.575		100.04209		538.12778		57.575		100.0254

		494.603		57.6		100.00096		100.02749		494.466		57.6		99.99259		494.32401		57.6		100.00101		534.69866		57.6		100.02749		536.39133		57.6		100.04212		538.37523		57.6		100.02541

		494.858		57.625		100.00124		100.0275		494.72699		57.625		99.99402		494.59601		57.625		100.00084		534.95166		57.625		100.0275		536.64155		57.625		100.04215		538.62367		57.625		100.02541

		495.134		57.65		100.00101		100.02751		494.98499		57.65		99.99536		494.85101		57.65		100.00397		535.20421		57.65		100.02751		536.887		57.65		100.04218		538.87233		57.65		100.02541

		495.38501		57.675		99.99872		100.02751		495.254		57.675		99.99483		495.11899		57.675		99.99916		535.45643		57.675		100.02751		537.13177		57.675		100.04222		539.12455		57.675		100.02541

		495.66		57.7		99.99886		100.02751		495.513		57.7		99.99475		495.39099		57.7		99.99714		535.70866		57.7		100.02751		537.37722		57.7		100.04225		539.37889		57.7		100.02541

		495.91		57.725		99.99934		100.02751		495.78101		57.725		99.99601		495.64801		57.725		99.99764		535.95966		57.725		100.02751		537.62189		57.725		100.04229		539.63199		57.725		100.0254

		496.17899		57.75		100.00142		100.02751		496.04099		57.75		99.99698		495.91101		57.75		99.99793		536.20789		57.75		100.02751		537.86356		57.75		100.04233		539.88577		57.75		100.02539

		496.43799		57.775		100.00089		100.0275		496.30399		57.775		99.99698		496.17499		57.775		100.00143		536.45755		57.775		100.0275		538.10411		57.775		100.04237		540.14022		57.775		100.02538

		496.70099		57.8		99.99832		100.0275		496.56201		57.8		99.99306		496.436		57.8		99.9966		536.70767		57.8		100.0275		538.35289		57.8		100.04241		540.39166		57.8		100.02536

		496.96201		57.825		100.00145		100.02748		496.83401		57.825		99.99597		496.71201		57.825		100.00248		536.95311		57.825		100.02748		538.603		57.825		100.04245		540.64044		57.825		100.02535

		497.22699		57.85		99.99929		100.02747		497.09399		57.85		99.99317		496.96899		57.85		100.00327		537.19378		57.85		100.02747		538.85333		57.85		100.04249		540.88866		57.85		100.02534

		497.48901		57.875		99.99878		100.02746		497.34601		57.875		99.99459		497.22198		57.875		99.99983		537.43256		57.875		100.02746		539.10511		57.875		100.04253		541.13666		57.875		100.02532

		497.74799		57.9		100.00297		100.02745		497.61099		57.9		99.99563		497.483		57.9		100.00024		537.67245		57.9		100.02745		539.35567		57.9		100.04256		541.3821		57.9		100.02532

		498.021		57.925		100.00156		100.02743		497.88199		57.925		99.99663		497.74701		57.925		100.00137		537.91323		57.925		100.02743		539.60512		57.925		100.0426		541.63022		57.925		100.02531

		498.27701		57.95		100.00024		100.02742		498.14999		57.95		99.99598		498.01901		57.95		99.99989		538.16212		57.95		100.02742		539.85256		57.95		100.04263		541.87899		57.95		100.02531

		498.54401		57.975		99.99883		100.02741		498.40201		57.975		99.99554		498.26901		57.975		100.00016		538.41311		57.975		100.02741		540.10356		57.975		100.04266		542.12866		57.975		100.02531

		498.802		58		99.99938		100.02741		498.664		58		99.99411		498.54001		58		99.99933		538.66334		58		100.02741		540.355		58		100.04268		542.37821		58		100.02532

		499.06201		58.025		100.00051		100.0274		498.92401		58.025		99.99391		498.79901		58.025		100.00302		538.913		58.025		100.0274		540.60044		58.025		100.0427		542.62821		58.025		100.02533

		499.33499		58.05		99.99792		100.0274		499.194		58.05		99.99373		499.069		58.05		99.9995		539.1629		58.05		100.0274		540.84222		58.05		100.04272		542.87855		58.05		100.02534

		499.59799		58.075		99.99962		100.0274		499.452		58.075		99.99471		499.32901		58.075		100.00125		539.41234		58.075		100.0274		541.08489		58.075		100.04273		543.13066		58.075		100.02536

		499.85901		58.1		100.00071		100.0274		499.72		58.1		99.99569		499.59601		58.1		100.00618		539.66212		58.1		100.0274		541.32556		58.1		100.04274		543.38399		58.1		100.02539

		500.12299		58.125		100.00042		100.0274		499.987		58.125		99.99415		499.85999		58.125		100.00023		539.91222		58.125		100.0274		541.56578		58.125		100.04274		543.63844		58.125		100.02541

		500.38101		58.15		100.00071		100.02741		500.242		58.15		99.99478		500.13		58.15		100.00008		540.16412		58.15		100.02741		541.81378		58.15		100.04275		543.88933		58.15		100.02544

		500.64801		58.175		100.00059		100.02742		500.50299		58.175		99.99691		500.38		58.175		100.00052		540.40889		58.175		100.02742		542.06356		58.175		100.04274		544.13911		58.175		100.02547

		500.91101		58.2		99.99806		100.02742		500.771		58.2		99.99246		500.64001		58.2		100.00069		540.65234		58.2		100.02742		542.31222		58.2		100.04274		544.38844		58.2		100.0255

		501.17001		58.225		99.99857		100.02743		501.03299		58.225		99.99459		500.90799		58.225		100.00145		540.89712		58.225		100.02743		542.56544		58.225		100.04273		544.63578		58.225		100.02553

		501.43799		58.25		99.99952		100.02744		501.293		58.25		99.99438		501.18301		58.25		100.00242		541.14079		58.25		100.02744		542.81723		58.25		100.04272		544.88444		58.25		100.02556

		501.69		58.275		100.00016		100.02745		501.55899		58.275		99.99325		501.43701		58.275		100.00169		541.38357		58.275		100.02745		543.06922		58.275		100.0427		545.132		58.275		100.02559

		501.95999		58.3		100.00059		100.02745		501.823		58.3		99.99436		501.69501		58.3		100.00191		541.6299		58.3		100.02745		543.32067		58.3		100.04268		545.38211		58.3		100.02561

		502.22101		58.325		100.00059		100.02746		502.08099		58.325		99.99464		501.965		58.325		100.00029		541.87845		58.325		100.02746		543.57477		58.325		100.04266		545.63411		58.325		100.02563

		502.483		58.35		100.00084		100.02746		502.34201		58.35		99.99444		502.22198		58.35		100.00077		542.1289		58.35		100.02746		543.82678		58.35		100.04263		545.88723		58.35		100.02565

		502.74301		58.375		100.00144		100.02747		502.608		58.375		99.9956		502.48901		58.375		100.00317		542.37634		58.375		100.02747		544.07277		58.375		100.0426		546.14145		58.375		100.02567

		503.00601		58.4		100.00021		100.02747		502.87		58.4		99.99521		502.745		58.4		100.00017		542.62523		58.4		100.02747		544.31844		58.4		100.04257		546.39501		58.4		100.02568

		503.27499		58.425		100.00164		100.02747		503.129		58.425		99.99456		503.00299		58.425		99.99946		542.87456		58.425		100.02747		544.55956		58.425		100.04254		546.64968		58.425		100.0257

		503.53		58.45		99.9998		100.02747		503.39401		58.45		99.99387		503.267		58.45		99.99799		543.12389		58.45		100.02747		544.8		58.45		100.0425		546.90557		58.45		100.02571

		503.79599		58.475		99.99972		100.02747		503.664		58.475		99.99354		503.54199		58.475		100.0001		543.37389		58.475		100.02747		545.03989		58.475		100.04247		547.1619		58.475		100.02572

		504.06299		58.5		99.99873		100.02747		503.927		58.5		99.99432		503.80301		58.5		100.00006		543.62344		58.5		100.02747		545.2859		58.5		100.04244		547.41668		58.5		100.02573

		504.323		58.525		100.00107		100.02747		504.19501		58.525		99.99607		504.06299		58.525		99.99918		543.87111		58.525		100.02747		545.53389		58.525		100.0424		547.66779		58.525		100.02573

		504.582		58.55		100.00004		100.02747		504.461		58.55		99.99362		504.32599		58.55		100.00228		544.11666		58.55		100.02747		545.78423		58.55		100.04237		547.9159		58.55		100.02574

		504.85199		58.575		99.99858		100.02746		504.72299		58.575		99.99376		504.58899		58.575		99.99932		544.35999		58.575		100.02746		546.03489		58.575		100.04235		548.16145		58.575		100.02574

		505.10901		58.6		99.99938		100.02746		504.98199		58.6		99.99587		504.85199		58.6		99.99961		544.60466		58.6		100.02746		546.28411		58.6		100.04232		548.40645		58.6		100.02574

		505.37399		58.625		100.00009		100.02746		505.237		58.625		99.9956		505.10901		58.625		99.99973		544.8501		58.625		100.02746		546.53411		58.625		100.0423		548.65322		58.625		100.02575

		505.634		58.65		100.00224		100.02746		505.51001		58.65		99.99564		505.371		58.65		100.00013		545.09655		58.65		100.02746		546.79022		58.65		100.04229		548.90689		58.65		100.02575

		505.896		58.675		100.00142		100.02745		505.76199		58.675		99.99524		505.646		58.675		100.00134		545.34833		58.675		100.02745		547.04133		58.675		100.04227		549.16011		58.675		100.02575

		506.15601		58.7		100.00142		100.02745		506.02301		58.7		99.9929		505.901		58.7		99.99852		545.59889		58.7		100.02745		547.29489		58.7		100.04227		549.41111		58.7		100.02575

		506.418		58.725		100.00045		100.02745		506.28201		58.725		99.99556		506.155		58.725		99.99883		545.85089		58.725		100.02745		547.54244		58.725		100.04226		549.66322		58.725		100.02575

		506.686		58.75		99.99952		100.02745		506.54199		58.75		99.99421		506.42401		58.75		99.99908		546.10278		58.75		100.02745		547.78655		58.75		100.04226		549.91844		58.75		100.02575

		506.948		58.775		100.0001		100.02746		506.81699		58.775		99.99389		506.686		58.775		100.00075		546.35456		58.775		100.02746		548.029		58.775		100.04227		550.17144		58.775		100.02575

		507.21799		58.8		100.00118		100.02746		507.08401		58.8		99.99627		506.95901		58.8		100.00089		546.60623		58.8		100.02746		548.27134		58.8		100.04228		550.42322		58.8		100.02575

		507.47601		58.825		99.99945		100.02747		507.33899		58.825		99.99658		507.211		58.825		100.00015		546.85733		58.825		100.02747		548.51034		58.825		100.04229		550.67567		58.825		100.02575

		507.733		58.85		99.99902		100.02748		507.60199		58.85		99.99387		507.479		58.85		99.99896		547.10756		58.85		100.02748		548.75467		58.85		100.04231		550.92778		58.85		100.02575

		507.996		58.875		99.99801		100.02749		507.86801		58.875		99.9962		507.74301		58.875		100.00119		547.35367		58.875		100.02749		549.00178		58.875		100.04233		551.17		58.875		100.02576

		508.26099		58.9		99.99915		100.0275		508.12601		58.9		99.99129		507.99899		58.9		100.00068		547.59433		58.9		100.0275		549.25156		58.9		100.04236		551.41112		58.9		100.02576

		508.53101		58.925		99.99788		100.02752		508.383		58.925		99.99215		508.259		58.925		100.00032		547.83866		58.925		100.02752		549.49811		58.925		100.04239		551.65212		58.925		100.02577

		508.78299		58.95		100.00096		100.02754		508.647		58.95		99.99685		508.53101		58.95		100.00156		548.08089		58.95		100.02754		549.74423		58.95		100.04243		551.89312		58.95		100.02577

		509.04901		58.975		100.00194		100.02756		508.90701		58.975		99.99603		508.789		58.975		100.00176		548.32145		58.975		100.02756		549.992		58.975		100.04246		552.13289		58.975		100.02578

		509.311		59		100.00185		100.02759		509.17999		59		99.99696		509.05899		59		100.0014		548.56355		59		100.02759		550.24012		59		100.0425		552.37945		59		100.02579

		509.569		59.025		100.00204		100.02762		509.44		59.025		99.99663		509.31699		59.025		100.00175		548.80977		59.025		100.02762		550.48867		59.025		100.04255		552.62645		59.025		100.0258

		509.845		59.05		99.99889		100.02765		509.702		59.05		99.99524		509.57501		59.05		99.99992		549.06066		59.05		100.02765		550.74123		59.05		100.04259		552.87111		59.05		100.02581

		510.103		59.075		99.99986		100.02769		509.96701		59.075		99.99335		509.841		59.075		100.00121		549.3111		59.075		100.02769		550.98701		59.075		100.04263		553.11678		59.075		100.02582

		510.371		59.1		100.00271		100.02773		510.23001		59.1		99.99253		510.10699		59.1		100.00089		549.56399		59.1		100.02773		551.22767		59.1		100.04267		553.36245		59.1		100.02584

		510.62399		59.125		99.99962		100.02777		510.48599		59.125		99.99605		510.37		59.125		100.0017		549.81533		59.125		100.02777		551.46589		59.125		100.04271		553.60933		59.125		100.02585

		510.896		59.15		99.99874		100.02781		510.754		59.15		99.99545		510.63199		59.15		100.00171		550.06577		59.15		100.02781		551.70423		59.15		100.04275		553.85855		59.15		100.02586

		511.14899		59.175		100.00026		100.02785		511.017		59.175		99.99396		510.89801		59.175		100.00127		550.3171		59.175		100.02785		551.94034		59.175		100.04279		554.11056		59.175		100.02587

		511.405		59.2		100.00287		100.02789		511.27899		59.2		99.99699		511.155		59.2		100.00118		550.56999		59.2		100.02789		552.18312		59.2		100.04282		554.36156		59.2		100.02588

		511.673		59.225		99.99883		100.02793		511.54501		59.225		99.99132		511.42099		59.225		99.9995		550.81978		59.225		100.02793		552.42811		59.225		100.04284		554.60468		59.225		100.02589

		511.93701		59.25		99.99895		100.02796		511.80301		59.25		99.99444		511.673		59.25		100.00048		551.06778		59.25		100.02796		552.67667		59.25		100.04286		554.8469		59.25		100.0259

		512.19897		59.275		100.00075		100.028		512.065		59.275		99.99616		511.944		59.275		100.00133		551.31323		59.275		100.028		552.92167		59.275		100.04288		555.09434		59.275		100.02591

		512.46198		59.3		100		100.02803		512.32898		59.3		99.99514		512.20099		59.3		100.00106		551.55701		59.3		100.02803		553.16901		59.3		100.04289		555.33823		59.3		100.02592

		512.72601		59.325		99.99885		100.02806		512.59302		59.325		99.9918		512.46899		59.325		100.00065		551.80023		59.325		100.02806		553.41823		59.325		100.04289		555.58545		59.325		100.02592

		512.99402		59.35		100.00249		100.02808		512.84698		59.35		99.994		512.74103		59.35		100.00262		552.04267		59.35		100.02808		553.66779		59.35		100.04289		555.83723		59.35		100.02592

		513.25098		59.375		99.99828		100.0281		513.11102		59.375		99.99366		512.99799		59.375		99.99926		552.29212		59.375		100.0281		553.91634		59.375		100.04289		556.08689		59.375		100.02593

		513.51001		59.4		100.00008		100.02811		513.36401		59.4		99.99382		513.25702		59.4		100.00094		552.54245		59.4		100.02811		554.16989		59.4		100.04288		556.33678		59.4		100.02592

		513.78003		59.425		100.00415		100.02812		513.63599		59.425		99.99404		513.52399		59.425		100.00125		552.79223		59.425		100.02812		554.41767		59.425		100.04287		556.58722		59.425		100.02592

		514.03802		59.45		100.003		100.02812		513.896		59.45		99.99445		513.789		59.45		99.9999		553.04434		59.45		100.02812		554.65956		59.45		100.04285		556.83944		59.45		100.02592

		514.30701		59.475		99.99984		100.02812		514.15802		59.475		99.99516		514.05402		59.475		100.00171		553.29556		59.475		100.02812		554.89534		59.475		100.04284		557.09466		59.475		100.02592

		514.56799		59.5		100.0024		100.02812		514.41803		59.5		99.99461		514.31702		59.5		100.00289		553.54456		59.5		100.02812		555.13734		59.5		100.04282		557.34711		59.5		100.02591

		514.83301		59.525		100.00009		100.02811		514.68701		59.525		99.99556		514.57202		59.525		100.00006		553.79611		59.525		100.02811		555.37278		59.525		100.0428		557.60211		59.525		100.02591

		515.08801		59.55		100.00051		100.02809		514.94397		59.55		99.99507		514.84003		59.55		100.00146		554.04811		59.55		100.02809		555.609		59.55		100.04278		557.85088		59.55		100.0259

		515.34998		59.575		99.99954		100.02808		515.20697		59.575		99.99474		515.10303		59.575		99.99998		554.30122		59.575		100.02808		555.84911		59.575		100.04276		558.095		59.575		100.0259

		515.62402		59.6		100.0008		100.02806		515.47198		59.6		99.99521		515.36298		59.6		100.0007		554.54633		59.6		100.02806		556.09199		59.6		100.04275		558.34322		59.6		100.02589

		515.88599		59.625		100.00026		100.02804		515.74103		59.625		99.99378		515.62903		59.625		99.99985		554.791		59.625		100.02804		556.33366		59.625		100.04273		558.58733		59.625		100.02589

		516.146		59.65		100.00083		100.02803		516.00098		59.65		99.99567		515.888		59.65		100.00027		555.03256		59.65		100.02803		556.57499		59.65		100.04272		558.829		59.65		100.02589

		516.40503		59.675		99.99903		100.02801		516.26599		59.675		99.99618		516.15002		59.675		100.00015		555.274		59.675		100.02801		556.817		59.675		100.04271		559.07567		59.675		100.02589

		516.66803		59.7		100.00007		100.028		516.51898		59.7		99.99383		516.42102		59.7		99.99949		555.51433		59.7		100.028		557.06344		59.7		100.04271		559.32734		59.7		100.02589

		516.93298		59.725		99.99712		100.02799		516.77899		59.725		99.99284		516.67999		59.725		99.99974		555.76244		59.725		100.02799		557.30878		59.725		100.04271		559.57845		59.725		100.0259

		517.19598		59.75		100.0002		100.02799		517.04401		59.75		99.9945		516.93799		59.75		100.00195		556.00967		59.75		100.02799		557.55811		59.75		100.04271		559.828		59.75		100.02591

		517.45599		59.775		99.99907		100.02799		517.297		59.775		99.99666		517.19897		59.775		100.00069		556.26		59.775		100.02799		557.80256		59.775		100.04272		560.08256		59.775		100.02592

		517.71198		59.8		99.99914		100.028		517.56897		59.8		99.99511		517.46503		59.8		100.00098		556.51067		59.8		100.028		558.04356		59.8		100.04274		560.33689		59.8		100.02593

		517.98499		59.825		100.00153		100.028		517.828		59.825		99.99422		517.72498		59.825		100.00262		556.76078		59.825		100.028		558.28611		59.825		100.04276		560.58944		59.825		100.02595

		518.24103		59.85		100.00279		100.02802		518.08698		59.85		99.99418		517.992		59.85		100.00087		557.00878		59.85		100.02802		558.52523		59.85		100.04278		560.84222		59.85		100.02596

		518.51202		59.875		100.00128		100.02803		518.35199		59.875		99.99474		518.25098		59.875		100.00059		557.26022		59.875		100.02803		558.76278		59.875		100.0428		561.09566		59.875		100.02598

		518.77002		59.9		99.99927		100.02805		518.61499		59.9		99.99357		518.526		59.9		100.00088		557.51178		59.9		100.02805		559.00144		59.9		100.04283		561.34655		59.9		100.026

		519.021		59.925		100.00071		100.02807		518.87799		59.925		99.99462		518.78302		59.925		100.00031		557.76322		59.925		100.02807		559.2491		59.925		100.04287		561.59166		59.925		100.02602

		519.28998		59.95		99.99903		100.02809		519.14502		59.95		99.99488		519.04498		59.95		100.00086		558.00711		59.95		100.02809		559.49599		59.95		100.0429		561.83499		59.95		100.02604

		519.55499		59.975		100.00063		100.0281		519.39099		59.975		99.99478		519.30902		59.975		100.00067		558.25289		59.975		100.0281		559.74299		59.975		100.04293		562.07888		59.975		100.02605

		519.81598		60		99.99874		100.02811		519.65802		60		99.99404		519.56201		60		100.00057		558.49478		60		100.02811		559.99122		60		100.04296		562.32022		60		100.02607

		520.08301		60.025		100.00113		100.02812		519.92499		60.025		99.99407		519.83197		60.025		100.00054		558.73456		60.025		100.02812		560.24088		60.025		100.04299		562.56444		60.025		100.02608

		520.35999		60.05		100.00093		100.02812		520.19702		60.05		99.9948		520.099		60.05		99.99911		558.97401		60.05		100.02812		560.49032		60.05		100.04301		562.812		60.05		100.02608

		520.617		60.075		100.00079		100.02812		520.45599		60.075		99.99394		520.35303		60.075		99.99794		559.22245		60.075		100.02812		560.74321		60.075		100.04303		563.05878		60.075		100.02609

		520.87701		60.1		100.00223		100.02812		520.70697		60.1		99.99573		520.62		60.1		100.00011		559.47078		60.1		100.02812		560.99632		60.1		100.04304		563.30589		60.1		100.02609

		521.13202		60.125		100.00117		100.0281		520.979		60.125		99.9975		520.88397		60.125		100.00152		559.71733		60.125		100.0281		561.2491		60.125		100.04305		563.55355		60.125		100.02608

		521.40698		60.15		99.99839		100.02809		521.242		60.15		99.99608		521.14899		60.15		100.00101		559.964		60.15		100.02809		561.49411		60.15		100.04306		563.8		60.15		100.02608

		521.65997		60.175		100.0017		100.02807		521.51001		60.175		99.99323		521.40802		60.175		100.00034		560.21278		60.175		100.02807		561.73589		60.175		100.04306		564.04867		60.175		100.02607

		521.922		60.2		99.99845		100.02805		521.76703		60.2		99.99371		521.664		60.2		100.00037		560.45978		60.2		100.02805		561.97766		60.2		100.04306		564.29734		60.2		100.02606

		522.18597		60.225		99.99949		100.02803		522.03198		60.225		99.99354		521.92603		60.225		99.99982		560.70711		60.225		100.02803		562.22011		60.225		100.04306		564.54744		60.225		100.02605

		522.44299		60.25		100.00028		100.02802		522.29401		60.25		99.99175		522.18799		60.25		100.00013		560.95689		60.25		100.02802		562.46233		60.25		100.04306		564.79733		60.25		100.02604

		522.71399		60.275		100.00161		100.028		522.54602		60.275		99.99634		522.453		60.275		100.00194		561.20733		60.275		100.028		562.71		60.275		100.04305		565.04256		60.275		100.02604

		522.97803		60.3		100.00162		100.02799		522.82202		60.3		99.99175		522.71899		60.3		99.99834		561.452		60.3		100.02799		562.95778		60.3		100.04304		565.28733		60.3		100.02603

		523.23999		60.325		100.00385		100.02798		523.08301		60.325		99.99356		522.98102		60.325		100.0023		561.69467		60.325		100.02798		563.20644		60.325		100.04304		565.53156		60.325		100.02603

		523.50098		60.35		99.99986		100.02797		523.34198		60.35		99.99362		523.242		60.35		100.00091		561.93722		60.35		100.02797		563.45711		60.35		100.04304		565.77589		60.35		100.02603

		523.76001		60.375		100.00029		100.02797		523.60901		60.375		99.99519		523.50098		60.375		100.0002		562.18022		60.375		100.02797		563.70555		60.375		100.04304		566.02477		60.375		100.02604

		524.02698		60.4		100.00261		100.02797		523.85602		60.4		99.99459		523.771		60.4		100.00121		562.42011		60.4		100.02797		563.95611		60.4		100.04304		566.27744		60.4		100.02605

		524.29102		60.425		100.00109		100.02798		524.12299		60.425		99.99377		524.02502		60.425		99.99914		562.668		60.425		100.02798		564.20656		60.425		100.04304		566.52977		60.425		100.02606

		524.55103		60.45		100.0011		100.028		524.38		60.45		99.99398		524.29102		60.45		99.99972		562.91767		60.45		100.028		564.45656		60.45		100.04305		566.78066		60.45		100.02607

		524.81598		60.475		100.00242		100.02801		524.65503		60.475		99.99347		524.55499		60.475		100.00048		563.16734		60.475		100.02801		564.70833		60.475		100.04306		567.03078		60.475		100.02608

		525.08002		60.5		100.00148		100.02803		524.90503		60.5		99.99385		524.81		60.5		100.00111		563.41867		60.5		100.02803		564.94923		60.5		100.04307		567.28066		60.5		100.0261

		525.349		60.525		100.00331		100.02805		525.172		60.525		99.99313		525.08698		60.525		99.99909		563.66934		60.525		100.02805		565.18856		60.525		100.04308		567.53066		60.525		100.02611

		525.60303		60.55		100.00466		100.02808		525.43903		60.55		99.99518		525.349		60.55		100.00158		563.92167		60.55		100.02808		565.42623		60.55		100.04309		567.78078		60.55		100.02613

		525.86499		60.575		100.00305		100.0281		525.69598		60.575		99.9941		525.59802		60.575		99.99884		564.174		60.575		100.0281		565.6639		60.575		100.0431		568.03078		60.575		100.02614

		526.12799		60.6		100.00343		100.02812		525.95599		60.6		99.99425		525.86603		60.6		99.99953		564.42523		60.6		100.02812		565.89968		60.6		100.04312		568.27822		60.6		100.02616

		526.39899		60.625		100.00081		100.02814		526.21899		60.625		99.99371		526.12799		60.625		100.00058		564.67889		60.625		100.02814		566.14312		60.625		100.04313		568.52222		60.625		100.02617

		526.65601		60.65		100.00217		100.02815		526.48401		60.65		99.99401		526.39203		60.65		99.99921		564.92556		60.65		100.02815		566.38934		60.65		100.04314		568.76611		60.65		100.02618

		526.91498		60.675		99.99963		100.02817		526.75098		60.675		99.99461		526.66101		60.675		99.99929		565.16945		60.675		100.02817		566.63879		60.675		100.04315		569.01156		60.675		100.02619

		527.19098		60.7		100.00178		100.02818		527.01398		60.7		99.99373		526.92401		60.7		100.00104		565.41178		60.7		100.02818		566.88701		60.7		100.04316		569.25477		60.7		100.0262

		527.448		60.725		100.0028		100.02819		527.27399		60.725		99.99567		527.18597		60.725		100.00158		565.65311		60.725		100.02819		567.13823		60.725		100.04317		569.50022		60.725		100.0262

		527.70502		60.75		100.00363		100.02819		527.53699		60.75		99.99554		527.45001		60.75		100.00112		565.89233		60.75		100.02819		567.38923		60.75		100.04318		569.75222		60.75		100.02621

		527.97601		60.775		100.0006		100.0282		527.79498		60.775		99.99443		527.70898		60.775		100.00042		566.13689		60.775		100.0282		567.64246		60.775		100.04319		570.00422		60.775		100.02621

		528.23199		60.8		99.999		100.0282		528.05402		60.8		99.99238		527.96198		60.8		100.00012		566.38367		60.8		100.0282		567.89535		60.8		100.04321		570.25422		60.8		100.02622

		528.49402		60.825		100.00145		100.02821		528.315		60.825		99.99356		528.23102		60.825		99.99911		566.63378		60.825		100.02821		568.14745		60.825		100.04322		570.50455		60.825		100.02622

		528.75403		60.85		99.99988		100.02821		528.586		60.85		99.9918		528.49103		60.85		100.00056		566.883		60.85		100.02821		568.39101		60.85		100.04324		570.75477		60.85		100.02623

		529.01202		60.875		100.00122		100.02822		528.84601		60.875		99.99248		528.755		60.875		100.00234		567.12911		60.875		100.02822		568.63146		60.875		100.04327		571.00566		60.875		100.02624

		529.27502		60.9		100.00001		100.02822		529.10797		60.9		99.99166		529.02399		60.9		100.0003		567.37466		60.9		100.02822		568.87145		60.9		100.04329		571.25388		60.9		100.02624

		529.54401		60.925		99.99944		100.02823		529.37201		60.925		99.99258		529.28302		60.925		99.99885		567.62478		60.925		100.02823		569.10901		60.925		100.04332		571.50344		60.925		100.02625

		529.80499		60.95		100.00122		100.02824		529.63397		60.95		99.99633		529.54199		60.95		100.00132		567.87466		60.95		100.02824		569.34656		60.95		100.04336		571.755		60.95		100.02626

		530.07098		60.975		100.0016		100.02825		529.888		60.975		99.99579		529.802		60.975		99.99949		568.12689		60.975		100.02825		569.59112		60.975		100.0434		572.00189		60.975		100.02628

		530.328		61		100.0006		100.02826		530.15002		61		99.99344		530.07098		61		99.99995		568.37066		61		100.02826		569.84001		61		100.04344		572.24921		61		100.02629

		530.59003		61.025		99.99903		100.02828		530.414		61.025		99.99285		530.33002		61.025		100.00194		568.6141		61.025		100.02828		570.08645		61.025		100.04348		572.49488		61.025		100.02631

		530.85199		61.05		100.00003		100.0283		530.67999		61.05		99.99406		530.60101		61.05		100.00101		568.85744		61.05		100.0283		570.336		61.05		100.04353		572.73922		61.05		100.02633

		531.11499		61.075		99.99815		100.02831		530.94501		61.075		99.99181		530.85199		61.075		100.00028		569.10021		61.075		100.02831		570.58577		61.075		100.04357		572.98655		61.075		100.02636

		531.37299		61.1		100.00004		100.02833		531.20599		61.1		99.99361		531.12097		61.1		99.99966		569.34299		61.1		100.02833		570.83755		61.1		100.04362		573.23677		61.1		100.02638

		531.63702		61.125		100.00014		100.02834		531.466		61.125		99.99331		531.37402		61.125		100.00056		569.59255		61.125		100.02834		571.09089		61.125		100.04366		573.48888		61.125		100.0264

		531.90198		61.15		99.99828		100.02835		531.73199		61.15		99.99489		531.64899		61.15		99.9987		569.84266		61.15		100.02835		571.34477		61.15		100.0437		573.7411		61.15		100.02642

		532.15698		61.175		99.99912		100.02836		531.992		61.175		99.99494		531.90698		61.175		99.99989		570.09344		61.175		100.02836		571.60055		61.175		100.04374		573.99099		61.175		100.02645

		532.42401		61.2		99.9989		100.02837		532.25897		61.2		99.99451		532.15997		61.2		99.99974		570.34233		61.2		100.02837		571.84966		61.2		100.04377		574.23899		61.2		100.02647

		532.69		61.225		99.99936		100.02837		532.52301		61.225		99.9934		532.42798		61.225		100.00014		570.59233		61.225		100.02837		572.09389		61.225		100.0438		574.48711		61.225		100.02649

		532.94897		61.25		99.99868		100.02838		532.784		61.25		99.99221		532.69		61.25		100.00007		570.8441		61.25		100.02838		572.33889		61.25		100.04383		574.73611		61.25		100.02651

		533.20599		61.275		100.00075		100.02838		533.04498		61.275		99.99456		532.94598		61.275		100.00027		571.09377		61.275		100.02838		572.58289		61.275		100.04385		574.989		61.275		100.02652

		533.47498		61.3		100.00217		100.02838		533.30298		61.3		99.99545		533.21198		61.3		100.00111		571.34444		61.3		100.02838		572.82489		61.3		100.04386		575.23733		61.3		100.02653

		533.73199		61.325		100.00017		100.02839		533.57703		61.325		99.99338		533.474		61.325		100.00005		571.59644		61.325		100.02839		573.07533		61.325		100.04386		575.47989		61.325		100.02655

		533.99799		61.35		100.00079		100.02839		533.83801		61.35		99.99644		533.73102		61.35		99.99909		571.845		61.35		100.02839		573.32444		61.35		100.04387		575.723		61.35		100.02655

		534.26202		61.375		100.00199		100.0284		534.099		61.375		99.99237		533.99701		61.375		100.00029		572.09011		61.375		100.0284		573.57511		61.375		100.04386		575.96701		61.375		100.02656

		534.521		61.4		100.0014		100.0284		534.35602		61.4		99.99436		534.26099		61.4		99.9989		572.33266		61.4		100.0284		573.82533		61.4		100.04385		576.20823		61.4		100.02656

		534.784		61.425		100.00198		100.02841		534.61298		61.425		99.99344		534.52002		61.425		99.9989		572.57655		61.425		100.02841		574.07678		61.425		100.04384		576.45756		61.425		100.02657

		535.04498		61.45		99.99967		100.02842		534.87598		61.45		99.99227		534.79102		61.45		99.99965		572.81889		61.45		100.02842		574.32811		61.45		100.04382		576.70878		61.45		100.02657

		535.30701		61.475		99.99915		100.02844		535.14099		61.475		99.9929		535.03998		61.475		100.00004		573.06834		61.475		100.02844		574.57978		61.475		100.0438		576.96334		61.475		100.02657

		535.58002		61.5		100.00079		100.02845		535.40399		61.5		99.99338		535.31702		61.5		99.99824		573.31823		61.5		100.02845		574.83377		61.5		100.04378		577.21456		61.5		100.02657

		535.836		61.525		100.00004		100.02846		535.66998		61.525		99.99322		535.56897		61.525		100.00077		573.56845		61.525		100.02846		575.09122		61.525		100.04376		577.46745		61.525		100.02656

		536.09302		61.55		100.00124		100.02848		535.93597		61.55		99.99362		535.82898		61.55		100.00164		573.81801		61.55		100.02848		575.33589		61.55		100.04374		577.72356		61.55		100.02656

		536.36298		61.575		100.00266		100.02849		536.19299		61.575		99.99374		536.09698		61.575		100.00089		574.06867		61.575		100.02849		575.58067		61.575		100.04371		577.97922		61.575		100.02656

		536.61798		61.6		100.00147		100.02851		536.45502		61.6		99.99644		536.362		61.6		100.0008		574.31856		61.6		100.02851		575.82501		61.6		100.04369		578.23366		61.6		100.02656

		536.88397		61.625		99.99912		100.02852		536.72198		61.625		99.99526		536.61798		61.625		100.00172		574.57056		61.625		100.02852		576.06923		61.625		100.04367		578.49		61.625		100.02657

		537.14697		61.65		99.9989		100.02853		536.97601		61.65		99.99489		536.88501		61.65		99.99871		574.82201		61.65		100.02853		576.31178		61.65		100.04366		578.741		61.65		100.02657

		537.41101		61.675		100.00295		100.02855		537.23901		61.675		99.99409		537.14502		61.675		100.00018		575.07834		61.675		100.02855		576.56156		61.675		100.04364		578.98733		61.675		100.02658

		537.66803		61.7		99.99861		100.02856		537.50299		61.7		99.99636		537.40503		61.7		100.00138		575.323		61.7		100.02856		576.81445		61.7		100.04363		579.23199		61.7		100.02658

		537.93402		61.725		100.00056		100.02857		537.76898		61.725		99.99314		537.672		61.725		99.99891		575.56622		61.725		100.02857		577.06601		61.725		100.04363		579.477		61.725		100.02659

		538.20099		61.75		100.00442		100.02858		538.02899		61.75		99.9962		537.93402		61.75		99.99959		575.80855		61.75		100.02858		577.31601		61.75		100.04363		579.71922		61.75		100.0266

		538.461		61.775		100.00293		100.0286		538.28699		61.775		99.9963		538.20099		61.775		100.00152		576.05155		61.775		100.0286		577.57079		61.775		100.04363		579.96889		61.775		100.02662

		538.72699		61.8		100.00189		100.02861		538.56799		61.8		99.99352		538.46503		61.8		100.0005		576.29333		61.8		100.02861		577.82479		61.8		100.04365		580.22056		61.8		100.02663

		538.98999		61.825		100.00102		100.02863		538.82202		61.825		99.99429		538.72498		61.825		100.0002		576.54256		61.825		100.02863		578.07712		61.825		100.04366		580.47334		61.825		100.02665

		539.258		61.85		100.00181		100.02865		539.078		61.85		99.99292		538.97699		61.85		100.00002		576.79144		61.85		100.02865		578.32834		61.85		100.04369		580.7259		61.85		100.02667

		539.51801		61.875		100.00138		100.02867		539.33301		61.875		99.99477		539.23999		61.875		99.99993		577.04066		61.875		100.02867		578.58145		61.875		100.04372		580.97567		61.875		100.02669

		539.77698		61.9		100.00109		100.02869		539.60303		61.9		99.99349		539.505		61.9		99.99937		577.29066		61.9		100.02869		578.82768		61.9		100.04375		581.2279		61.9		100.02671

		540.039		61.925		100.00241		100.02872		539.86401		61.925		99.99511		539.76703		61.925		99.99989		577.54122		61.925		100.02872		579.06901		61.925		100.0438		581.48035		61.925		100.02673

		540.29999		61.95		100.00139		100.02874		540.13		61.95		99.99559		540.03601		61.95		99.99836		577.79245		61.95		100.02874		579.31179		61.95		100.04385		581.73357		61.95		100.02675

		540.56897		61.975		100.00431		100.02877		540.39697		61.975		99.99524		540.29498		61.975		100.00093		578.045		61.975		100.02877		579.55579		61.975		100.0439		581.9869		61.975		100.02677

		540.815		62		100.00164		100.0288		540.65802		62		99.99554		540.55402		62		100.0011		578.29922		62		100.0288		579.79601		62		100.04396		582.23267		62		100.02679

		541.08698		62.025		100.0009		100.02883		540.92499		62.025		99.99568		540.82397		62.025		100.00175		578.55322		62.025		100.02883		580.04345		62.025		100.04402		582.47856		62.025		100.02681

		541.34198		62.05		100.003		100.02886		541.17999		62.05		99.99465		541.08099		62.05		99.9988		578.80023		62.05		100.02886		580.29478		62.05		100.04409		582.72156		62.05		100.02683

		541.60797		62.075		100.00076		100.0289		541.44397		62.075		99.99467		541.34698		62.075		100.00069		579.04567		62.075		100.0289		580.54645		62.075		100.04416		582.96289		62.075		100.02685

		541.86798		62.1		100.0005		100.02893		541.70203		62.1		99.99376		541.612		62.1		100.0005		579.29279		62.1		100.02893		580.79633		62.1		100.04422		583.20612		62.1		100.02687

		542.12598		62.125		100.00114		100.02896		541.96997		62.125		99.99546		541.86499		62.125		100.00169		579.53656		62.125		100.02896		581.04733		62.125		100.04429		583.45456		62.125		100.02689

		542.396		62.15		99.99952		100.029		542.22803		62.15		99.99286		542.13599		62.15		99.99811		579.78045		62.15		100.029		581.30055		62.15		100.04436		583.70401		62.15		100.02691

		542.65997		62.175		100.00174		100.02903		542.49902		62.175		99.9958		542.39697		62.175		99.99996		580.03078		62.175		100.02903		581.55166		62.175		100.04442		583.95345		62.175		100.02693

		542.92499		62.2		100.00301		100.02907		542.75098		62.2		99.99567		542.66101		62.2		100.00011		580.28033		62.2		100.02907		581.80111		62.2		100.04447		584.20367		62.2		100.02694

		543.19		62.225		100.00127		100.02911		543.01801		62.225		99.99111		542.92603		62.225		99.99978		580.52923		62.225		100.02911		582.05322		62.225		100.04453		584.45357		62.225		100.02695

		543.44397		62.25		100.00228		100.02915		543.27197		62.25		99.99367		543.17999		62.25		100.00128		580.77778		62.25		100.02915		582.29633		62.25		100.04457		584.70357		62.25		100.02697

		543.70599		62.275		100.00179		100.02919		543.54303		62.275		99.99574		543.44299		62.275		100.00239		581.027		62.275		100.02919		582.53855		62.275		100.04462		584.95424		62.275		100.02698

		543.96399		62.3		100.00358		100.02923		543.81799		62.3		99.99391		543.70697		62.3		99.99981		581.27767		62.3		100.02923		582.77932		62.3		100.04465		585.20624		62.3		100.02698

		544.23401		62.325		99.99811		100.02927		544.06799		62.325		99.99358		543.96002		62.325		100.00049		581.52711		62.325		100.02927		583.02055		62.325		100.04468		585.45812		62.325		100.02699

		544.49597		62.35		100.00152		100.02931		544.323		62.35		99.99278		544.23999		62.35		100.00052		581.77823		62.35		100.02931		583.25855		62.35		100.0447		585.70401		62.35		100.02699

		544.77002		62.375		100.0006		100.02935		544.58899		62.375		99.9924		544.50299		62.375		99.99949		582.03167		62.375		100.02935		583.50688		62.375		100.04472		585.94824		62.375		100.027

		545.03101		62.4		100.00088		100.02939		544.84998		62.4		99.9952		544.758		62.4		100.00263		582.27955		62.4		100.02939		583.75722		62.4		100.04474		586.19046		62.4		100.027

		545.29102		62.425		100.00193		100.02944		545.12201		62.425		99.99447		545.02698		62.425		100.00245		582.527		62.425		100.02944		584.00833		62.425		100.04475		586.43146		62.425		100.027

		545.54498		62.45		100.0011		100.02948		545.38397		62.45		99.99377		545.29401		62.45		100.0014		582.77267		62.45		100.02948		584.26177		62.45		100.04476		586.67268		62.45		100.027

		545.80701		62.475		100.00138		100.02952		545.64203		62.475		99.99329		545.55603		62.475		100.00129		583.019		62.475		100.02952		584.51622		62.475		100.04477		586.91634		62.475		100.02701

		546.07599		62.5		100.00533		100.02957		545.901		62.5		99.99404		545.80798		62.5		100.00237		583.26322		62.5		100.02957		584.768		62.5		100.04478		587.16478		62.5		100.02701

		546.34497		62.525		100.00231		100.02961		546.16901		62.525		99.99409		546.07703		62.525		100.00234		583.51312		62.525		100.02961		585.02		62.525		100.04479		587.413		62.525		100.02702

		546.60602		62.55		100.0021		100.02965		546.42999		62.55		99.99377		546.34198		62.55		100.00283		583.76367		62.55		100.02965		585.27188		62.55		100.04481		587.66212		62.55		100.02702

		546.862		62.575		100.00035		100.0297		546.68799		62.575		99.99325		546.59998		62.575		100.00342		584.01356		62.575		100.0297		585.52644		62.575		100.04483		587.913		62.575		100.02703

		547.13098		62.6		100.00387		100.02974		546.94598		62.6		99.99575		546.86298		62.6		100.00125		584.26356		62.6		100.02974		585.76944		62.6		100.04485		588.16356		62.6		100.02704

		547.388		62.625		100.00056		100.02978		547.21698		62.625		99.99345		547.12701		62.625		100.00091		584.51279		62.625		100.02978		586.008		62.625		100.04488		588.41511		62.625		100.02705

		547.65198		62.65		100.00206		100.02982		547.47803		62.65		99.995		547.38702		62.65		99.99917		584.76201		62.65		100.02982		586.24711		62.65		100.04491		588.66878		62.65		100.02707

		547.92102		62.675		100.0016		100.02986		547.73102		62.675		99.99425		547.66199		62.675		100.00051		585.01145		62.675		100.02986		586.48267		62.675		100.04494		588.92389		62.675		100.02708

		548.17499		62.7		100.00162		100.0299		548.00598		62.7		99.99725		547.92102		62.7		100.00338		585.2609		62.7		100.0299		586.719		62.7		100.04498		589.17422		62.7		100.02709

		548.43298		62.725		100.00282		100.02994		548.27502		62.725		99.99631		548.177		62.725		100.00239		585.5119		62.725		100.02994		586.96577		62.725		100.04502		589.42112		62.725		100.0271

		548.70001		62.75		100.0027		100.02998		548.52802		62.75		99.99527		548.44299		62.75		99.99993		585.756		62.75		100.02998		587.2141		62.75		100.04506		589.66734		62.75		100.02711

		548.953		62.775		100.00152		100.03001		548.79797		62.775		99.99368		548.711		62.775		99.99991		585.99822		62.775		100.03001		587.46689		62.775		100.04511		589.91323		62.775		100.02712

		549.22601		62.8		100.00312		100.03004		549.04401		62.8		99.99164		548.97198		62.8		99.99805		586.241		62.8		100.03004		587.71821		62.8		100.04515		590.15689		62.8		100.02713

		549.487		62.825		100.00174		100.03006		549.31299		62.825		99.99422		549.23798		62.825		99.99941		586.48189		62.825		100.03006		587.96988		62.825		100.04518		590.40756		62.825		100.02714

		549.75702		62.85		100.00101		100.03009		549.58398		62.85		99.994		549.49902		62.85		99.99985		586.72133		62.85		100.03009		588.22477		62.85		100.04522		590.66256		62.85		100.02714

		550.013		62.875		99.99941		100.03011		549.84698		62.875		99.99677		549.76501		62.875		100.00024		586.96877		62.875		100.03011		588.47911		62.875		100.04525		590.91834		62.875		100.02714

		550.27301		62.9		100.00312		100.03012		550.10699		62.9		99.99546		550.02301		62.9		100.00038		587.21966		62.9		100.03012		588.736		62.9		100.04527		591.1729		62.9		100.02714

		550.54102		62.925		100.00273		100.03013		550.36603		62.925		99.99524		550.28601		62.925		100.00212		587.47099		62.925		100.03013		588.99155		62.925		100.04529		591.42568		62.925		100.02714

		550.80402		62.95		100.00039		100.03013		550.62598		62.95		99.99363		550.55701		62.95		100.00116		587.72322		62.95		100.03013		589.23622		62.95		100.0453		591.68157		62.95		100.02714

		551.06299		62.975		100.00121		100.03013		550.896		62.975		99.99398		550.81598		62.975		100.00198		587.97311		62.975		100.03013		589.48145		62.975		100.0453		591.94034		62.975		100.02713

		551.33002		63		100.00182		100.03012		551.15698		63		99.99432		551.08502		63		100.00074		588.22323		63		100.03012		589.72378		63		100.0453		592.19923		63		100.02713

		551.591		63.025		100.00164		100.03011		551.41498		63.025		99.99322		551.34399		63.025		99.99959		588.47245		63.025		100.03011		589.96534		63.025		100.04529		592.45778		63.025		100.02712

		551.85901		63.05		100.00309		100.0301		551.67902		63.05		99.99417		551.604		63.05		100.00064		588.72656		63.05		100.0301		590.20634		63.05		100.04528		592.70989		63.05		100.02711

		552.13202		63.075		100.00143		100.03008		551.948		63.075		99.99503		551.86798		63.075		99.99933		588.97978		63.075		100.03008		590.45423		63.075		100.04526		592.95933		63.075		100.02711

		552.388		63.1		99.99965		100.03005		552.21301		63.1		99.9929		552.13599		63.1		99.9999		589.22611		63.1		100.03005		590.705		63.1		100.04524		593.207		63.1		100.0271

		552.64502		63.125		100.00186		100.03003		552.48401		63.125		99.99619		552.39301		63.125		100.00146		589.46823		63.125		100.03003		590.95645		63.125		100.04521		593.45166		63.125		100.0271

		552.90399		63.15		99.99955		100.03		552.73901		63.15		99.99398		552.65997		63.15		99.99998		589.71367		63.15		100.03		591.20956		63.15		100.04519		593.69677		63.15		100.0271

		553.16199		63.175		100.00144		100.02997		553.00201		63.175		99.99219		552.93103		63.175		99.99931		589.95723		63.175		100.02997		591.46423		63.175		100.04516		593.95032		63.175		100.0271

		553.42999		63.2		100.0022		100.02994		553.26703		63.2		99.99559		553.19		63.2		100.00122		590.20256		63.2		100.02994		591.71834		63.2		100.04513		594.20043		63.2		100.0271

		553.70001		63.225		100.00245		100.02991		553.52502		63.225		99.99322		553.45697		63.225		100.00075		590.45601		63.225		100.02991		591.97055		63.225		100.04511		594.44944		63.225		100.02711

		553.961		63.25		100.00067		100.02988		553.78198		63.25		99.9916		553.72101		63.25		100.00156		590.71079		63.25		100.02988		592.22567		63.25		100.04509		594.70121		63.25		100.02712

		554.21198		63.275		100.00481		100.02985		554.04999		63.275		99.99781		553.98798		63.275		100.00133		590.96134		63.275		100.02985		592.48133		63.275		100.04508		594.95433		63.275		100.02714

		554.48499		63.3		100.00232		100.02983		554.31201		63.3		99.99657		554.237		63.3		100.00059		591.21412		63.3		100.02983		592.72788		63.3		100.04507		595.20466		63.3		100.02716

		554.74902		63.325		100.00071		100.02981		554.57397		63.325		99.99486		554.50201		63.325		100.00083		591.4679		63.325		100.02981		592.97422		63.325		100.04507		595.4561		63.325		100.02718

		555.00098		63.35		100.00293		100.02979		554.841		63.35		99.99461		554.77197		63.35		100.00043		591.72389		63.35		100.02979		593.21889		63.35		100.04507		595.71044		63.35		100.0272

		555.26398		63.375		100.0003		100.02978		555.10101		63.375		99.99362		555.039		63.375		100.00039		591.97589		63.375		100.02978		593.46067		63.375		100.04508		595.96832		63.375		100.02723

		555.53601		63.4		100.0017		100.02977		555.37299		63.4		99.99634		555.30902		63.4		99.99872		592.228		63.4		100.02977		593.70256		63.4		100.0451		596.21444		63.4		100.02726

		555.79602		63.425		100.00221		100.02976		555.633		63.425		99.99545		555.573		63.425		99.99977		592.48044		63.425		100.02976		593.95334		63.425		100.04511		596.46055		63.425		100.02729

		556.05603		63.45		100.00292		100.02976		555.89801		63.45		99.99585		555.83002		63.45		100.00021		592.72388		63.45		100.02976		594.2049		63.45		100.04514		596.707		63.45		100.02733

		556.32501		63.475		100.00147		100.02977		556.15399		63.475		99.99188		556.09601		63.475		100.00033		592.9691		63.475		100.02977		594.45456		63.475		100.04516		596.95089		63.475		100.02736

		556.58698		63.5		100.00287		100.02978		556.414		63.5		99.99317		556.36499		63.5		100.00088		593.21544		63.5		100.02978		594.70579		63.5		100.04519		597.19711		63.5		100.02739

		556.84399		63.525		100.00242		100.0298		556.67999		63.525		99.99404		556.62201		63.525		99.99971		593.46088		63.525		100.0298		594.96035		63.525		100.04522		597.45022		63.525		100.02742

		557.10797		63.55		99.99962		100.02982		556.93799		63.55		99.99197		556.88702		63.55		99.99812		593.70322		63.55		100.02982		595.21279		63.55		100.04525		597.70378		63.55		100.02745

		557.37402		63.575		100.00313		100.02985		557.20099		63.575		99.99459		557.15302		63.575		99.99939		593.95355		63.575		100.02985		595.46524		63.575		100.04528		597.9579		63.575		100.02748

		557.633		63.6		100.00004		100.02988		557.46399		63.6		99.99402		557.40997		63.6		100.00064		594.20289		63.6		100.02988		595.71912		63.6		100.04532		598.2109		63.6		100.02751

		557.90601		63.625		100.00262		100.02992		557.73602		63.625		99.99753		557.67499		63.625		100.00201		594.45522		63.625		100.02992		595.97446		63.625		100.04535		598.46324		63.625		100.02753

		558.15997		63.65		100.00228		100.02995		557.99103		63.65		99.99516		557.94598		63.65		99.99861		594.70856		63.65		100.02995		596.22057		63.65		100.04539		598.71823		63.65		100.02755

		558.42499		63.675		100.0006		100.02999		558.245		63.675		99.99241		558.20898		63.675		100.00015		594.96478		63.675		100.02999		596.46412		63.675		100.04543		598.97612		63.675		100.02757

		558.69202		63.7		99.9999		100.03003		558.52002		63.7		99.99431		558.47803		63.7		99.99972		595.21911		63.7		100.03003		596.70789		63.7		100.04547		599.23412		63.7		100.02758

		558.95898		63.725		99.99997		100.03007		558.78101		63.725		99.993		558.73602		63.725		99.99813		595.47111		63.725		100.03007		596.94967		63.725		100.04551		599.48635		63.725		100.0276

		559.21399		63.75		100.00258		100.03011		559.04999		63.75		99.99608		558.99298		63.75		100.0029		595.72466		63.75		100.03011		597.19011		63.75		100.04556		599.73301		63.75		100.02761

		559.48499		63.775		100.00307		100.03015		559.31299		63.775		99.99696		559.26001		63.775		99.99998		595.97999		63.775		100.03015		597.43689		63.775		100.0456		599.98056		63.775		100.02762

		559.74799		63.8		100.00113		100.03018		559.57001		63.8		99.99733		559.52899		63.8		100.00106		596.22766		63.8		100.03018		597.68433		63.8		100.04564		600.227		63.8		100.02763

		560.008		63.825		100.00371		100.03021		559.84399		63.825		99.9959		559.79401		63.825		100.00116		596.47277		63.825		100.03021		597.932		63.825		100.04569		600.47245		63.825		100.02764

		560.27802		63.85		100.00149		100.03024		560.09998		63.85		99.99355		560.05298		63.85		100.00157		596.71722		63.85		100.03024		598.17922		63.85		100.04573		600.72255		63.85		100.02764

		560.54102		63.875		99.99925		100.03026		560.36298		63.875		99.99225		560.31299		63.875		100.00259		596.96188		63.875		100.03026		598.42655		63.875		100.04577		600.97511		63.875		100.02765

		560.80103		63.9		99.99986		100.03028		560.62903		63.9		99.99405		560.58801		63.9		100.00073		597.2081		63.9		100.03028		598.67723		63.9		100.04581		601.227		63.9		100.02765

		561.05603		63.925		100.00089		100.0303		560.89099		63.925		99.99323		560.84802		63.925		100.00058		597.45777		63.925		100.0303		598.92879		63.925		100.04584		601.47967		63.925		100.02766

		561.32397		63.95		100.00265		100.03031		561.15399		63.95		99.99341		561.11298		63.95		100.00189		597.71066		63.95		100.03031		599.18256		63.95		100.04587		601.73378		63.95		100.02766

		561.59198		63.975		100.00124		100.03032		561.41498		63.975		99.9942		561.38098		63.975		100.00167		597.96233		63.975		100.03032		599.43745		63.975		100.04589		601.98423		63.975		100.02766

		561.84698		64		100.00207		100.03033		561.68597		64		99.99426		561.64301		64		100.00029		598.21478		64		100.03033		599.68334		64		100.04591		602.23556		64		100.02766

		562.10699		64.025		100.00046		100.03034		561.95203		64.025		99.99231		561.90399		64.025		99.99984		598.46522		64.025		100.03034		599.92601		64.025		100.04593		602.48734		64.025		100.02766

		562.38599		64.05		100.00235		100.03035		562.20697		64.05		99.99593		562.16998		64.05		100.00074		598.71911		64.05		100.03035		600.16912		64.05		100.04594		602.73845		64.05		100.02765

		562.64502		64.075		99.99931		100.03036		562.46899		64.075		99.99257		562.44202		64.075		99.99881		598.97155		64.075		100.03036		600.41179		64.075		100.04594		602.98356		64.075		100.02765

		562.91101		64.1		100.00114		100.03037		562.729		64.1		99.99493		562.70697		64.1		100.00004		599.22233		64.1		100.03037		600.65302		64.1		100.04594		603.22545		64.1		100.02765

		563.16901		64.125		100.00155		100.03038		562.99103		64.125		99.99209		562.95801		64.125		99.99938		599.47033		64.125		100.03038		600.90101		64.125		100.04594		603.46578		64.125		100.02764

		563.42902		64.15		100.0021		100.0304		563.25702		64.15		99.9928		563.23297		64.15		100.00026		599.71488		64.15		100.0304		601.15212		64.15		100.04594		603.70667		64.15		100.02764

		563.69202		64.175		100.00168		100.03042		563.534		64.175		99.99571		563.48901		64.175		100.00299		599.95533		64.175		100.03042		601.4029		64.175		100.04594		603.94545		64.175		100.02763

		563.95801		64.2		100.00212		100.03045		563.79303		64.2		99.99701		563.755		64.2		99.99929		600.19544		64.2		100.03045		601.65312		64.2		100.04594		604.19511		64.2		100.02763

		564.224		64.225		100.00309		100.03049		564.05298		64.225		99.99436		564.026		64.225		99.99927		600.43389		64.225		100.03049		601.90601		64.225		100.04594		604.44244		64.225		100.02762

		564.47803		64.25		99.99821		100.03053		564.315		64.25		99.99035		564.28198		64.25		99.99746		600.67322		64.25		100.03053		602.16256		64.25		100.04594		604.68822		64.25		100.02762

		564.75201		64.275		100.00075		100.03057		564.578		64.275		99.9944		564.54901		64.275		100.00098		600.91744		64.275		100.03057		602.41645		64.275		100.04594		604.93477		64.275		100.02762

		565.01501		64.3		100.00025		100.03063		564.84399		64.3		99.99329		564.80701		64.3		99.99913		601.164		64.3		100.03063		602.66745		64.3		100.04594		605.18555		64.3		100.02762

		565.27899		64.325		100.00097		100.03068		565.10602		64.325		99.99406		565.08099		64.325		99.99959		601.41111		64.325		100.03068		602.91822		64.325		100.04595		605.43644		64.325		100.02761

		565.54102		64.35		100.00047		100.03074		565.36603		64.35		99.99176		565.33801		64.35		100.00102		601.65712		64.35		100.03074		603.16144		64.35		100.04595		605.68789		64.35		100.02761

		565.80701		64.375		99.99896		100.03081		565.63098		64.375		99.9938		565.60602		64.375		99.99915		601.90123		64.375		100.03081		603.39988		64.375		100.04596		605.93755		64.375		100.02761

		566.07098		64.4		99.99864		100.03087		565.89203		64.4		99.99365		565.862		64.4		99.99975		602.1509		64.4		100.03087		603.63744		64.4		100.04597		606.18789		64.4		100.02761

		566.34003		64.425		99.99783		100.03093		566.15601		64.425		99.98985		566.13702		64.425		99.99818		602.39745		64.425		100.03093		603.87389		64.425		100.04598		606.431		64.425		100.02762

		566.599		64.45		100.00084		100.03098		566.41498		64.45		99.99531		566.39801		64.45		100.00242		602.64523		64.45		100.03098		604.11455		64.45		100.04599		606.67301		64.45		100.02762

		566.85901		64.475		99.9995		100.03103		566.68298		64.475		99.99163		566.65302		64.475		99.99816		602.89256		64.475		100.03103		604.35833		64.475		100.04601		606.91445		64.475		100.02762

		567.12402		64.5		99.99944		100.03107		566.94202		64.5		99.99374		566.92401		64.5		100.00022		603.13579		64.5		100.03107		604.60433		64.5		100.04602		607.15601		64.5		100.02763

		567.38599		64.525		100.0029		100.0311		567.21198		64.525		99.99469		567.18903		64.525		100.00151		603.37634		64.525		100.0311		604.85177		64.525		100.04604		607.39478		64.525		100.02763

		567.64801		64.55		99.99718		100.03112		567.47803		64.55		99.99241		567.45898		64.55		99.99909		603.61668		64.55		100.03112		605.10177		64.55		100.04607		607.63845		64.55		100.02764

		567.914		64.575		99.99967		100.03113		567.72998		64.575		99.994		567.72803		64.575		100.00017		603.85624		64.575		100.03113		605.35411		64.575		100.04609		607.883		64.575		100.02765

		568.17798		64.6		99.99948		100.03113		567.99597		64.6		99.99496		567.98901		64.6		99.99881		604.10246		64.6		100.03113		605.60889		64.6		100.04612		608.13144		64.6		100.02766

		568.435		64.625		100.00106		100.03112		568.27002		64.625		99.99515		568.25201		64.625		100.00081		604.35034		64.625		100.03112		605.86333		64.625		100.04614		608.38255		64.625		100.02767

		568.70502		64.65		100.00048		100.0311		568.547		64.65		99.99333		568.505		64.65		99.99942		604.60135		64.65		100.0311		606.11866		64.65		100.04617		608.632		64.65		100.02768

		568.96301		64.675		99.99733		100.03108		568.79102		64.675		99.99062		568.76501		64.675		99.99769		604.84901		64.675		100.03108		606.36888		64.675		100.0462		608.88289		64.675		100.02769

		569.229		64.7		100.0006		100.03105		569.05798		64.7		99.99504		569.026		64.7		100.00078		605.09734		64.7		100.03105		606.61377		64.7		100.04624		609.13489		64.7		100.02771

		569.50098		64.725		100.00001		100.03102		569.32397		64.725		99.99582		569.30603		64.725		99.99929		605.3479		64.725		100.03102		606.85643		64.725		100.04627		609.38733		64.725		100.02772

		569.76202		64.75		100.00048		100.031		569.586		64.75		99.99498		569.56897		64.75		100.00185		605.59834		64.75		100.031		607.09776		64.75		100.0463		609.637		64.75		100.02774

		570.02899		64.775		100.00314		100.03097		569.84998		64.775		99.99292		569.83002		64.775		99.99975		605.84789		64.775		100.03097		607.33921		64.775		100.04633		609.88144		64.775		100.02776

		570.29498		64.8		100.00519		100.03095		570.112		64.8		99.99263		570.09302		64.8		100.00156		606.09578		64.8		100.03095		607.58333		64.8		100.04636		610.12366		64.8		100.02777

		570.54999		64.825		99.99882		100.03095		570.37402		64.825		99.99449		570.35797		64.825		100.00114		606.34078		64.825		100.03095		607.82844		64.825		100.0464		610.362		64.825		100.02779

		570.80701		64.85		100.00079		100.03095		570.63599		64.85		99.99347		570.62201		64.85		100.00159		606.58122		64.85		100.03095		608.07377		64.85		100.04643		610.59933		64.85		100.02781

		571.07898		64.875		100.00191		100.03097		570.89301		64.875		99.99585		570.87201		64.875		100.00151		606.82022		64.875		100.03097		608.31989		64.875		100.04647		610.84011		64.875		100.02783

		571.349		64.9		100.00172		100.031		571.17102		64.9		99.99324		571.14099		64.9		99.99953		607.05967		64.9		100.031		608.56656		64.9		100.0465		611.084		64.9		100.02785

		571.59698		64.925		100.00025		100.03104		571.42499		64.925		99.99191		571.41498		64.925		100.00109		607.30012		64.925		100.03104		608.81255		64.925		100.04654		611.33189		64.925		100.02787

		571.86499		64.95		100.00275		100.03109		571.68903		64.95		99.99685		571.67902		64.95		100.00244		607.54178		64.95		100.03109		609.06234		64.95		100.04657		611.58078		64.95		100.02789

		572.12201		64.975		100.00156		100.03116		571.948		64.975		99.9929		571.935		64.975		100.00055		607.78623		64.975		100.03116		609.31301		64.975		100.04661		611.83411		64.975		100.0279

		572.38702		65		99.99961		100.03123		572.21301		65		99.99611		572.20099		65		99.99865		608.03412		65		100.03123		609.56367		65		100.04665		612.08845		65		100.02792

		572.66101		65.025		100.00144		100.0313		572.46698		65.025		99.99453		572.45898		65.025		99.99827		608.28534		65.025		100.0313		609.80912		65.025		100.04668		612.34523		65.025		100.02794

		572.91901		65.05		99.9992		100.03138		572.73999		65.05		99.99388		572.72601		65.05		99.99998		608.53267		65.05		100.03138		610.05034		65.05		100.04672		612.60167		65.05		100.02795

		573.18597		65.075		100.00273		100.03146		573		65.075		99.99322		572.992		65.075		99.99954		608.77911		65.075		100.03146		610.29156		65.075		100.04676		612.85667		65.075		100.02797

		573.45203		65.1		100.00159		100.03154		573.27002		65.1		99.99515		573.25201		65.1		99.99984		609.02789		65.1		100.03154		610.53379		65.1		100.04679		613.10778		65.1		100.02798

		573.69897		65.125		99.99992		100.03161		573.53198		65.125		99.99357		573.52802		65.125		99.99982		609.27866		65.125		100.03161		610.77656		65.125		100.04683		613.35389		65.125		100.02799

		573.97498		65.15		100.00052		100.03167		573.79303		65.15		99.99369		573.78302		65.15		99.99871		609.52711		65.15		100.03167		611.02734		65.15		100.04686		613.59844		65.15		100.028

		574.237		65.175		99.99891		100.03172		574.065		65.175		99.9942		574.04797		65.175		100.00011		609.77022		65.175		100.03172		611.28057		65.175		100.04689		613.84266		65.175		100.028

		574.49902		65.2		99.99885		100.03176		574.328		65.2		99.99199		574.30603		65.2		99.99956		610.00911		65.2		100.03176		611.53545		65.2		100.04692		614.08555		65.2		100.02801

		574.76801		65.225		99.9994		100.03179		574.58398		65.225		99.99125		574.58002		65.225		99.9992		610.24388		65.225		100.03179		611.79001		65.225		100.04694		614.3311		65.225		100.02801

		575.02899		65.25		100.00001		100.03181		574.84698		65.25		99.99371		574.85101		65.25		100.00014		610.48067		65.25		100.03181		612.04357		65.25		100.04697		614.57777		65.25		100.02801

		575.29401		65.275		99.99931		100.03181		575.11798		65.275		99.99344		575.10797		65.275		99.99987		610.71922		65.275		100.03181		612.30212		65.275		100.04699		614.82521		65.275		100.028

		575.56403		65.3		100.00004		100.03181		575.37598		65.3		99.99373		575.36401		65.3		99.99859		610.96322		65.3		100.03181		612.56045		65.3		100.04701		615.07454		65.3		100.028

		575.83197		65.325		99.99894		100.0318		575.64301		65.325		99.99214		575.64301		65.325		99.99728		611.21101		65.325		100.0318		612.81723		65.325		100.04704		615.32676		65.325		100.02799

		576.09698		65.35		99.99843		100.03179		575.90198		65.35		99.99475		575.89801		65.35		99.99752		611.45989		65.35		100.03179		613.07289		65.35		100.04706		615.58154		65.35		100.02799

		576.349		65.375		100.0006		100.03177		576.17603		65.375		99.99622		576.15698		65.375		99.99997		611.71067		65.375		100.03177		613.31978		65.375		100.04708		615.8351		65.375		100.02798

		576.61798		65.4		100.00139		100.03175		576.43701		65.4		99.99478		576.41803		65.4		99.99932		611.96222		65.4		100.03175		613.56411		65.4		100.0471		616.08732		65.4		100.02798

		576.87799		65.425		99.99961		100.03174		576.69897		65.425		99.99565		576.68597		65.425		100.00238		612.21422		65.425		100.03174		613.80778		65.425		100.04712		616.33654		65.425		100.02797

		577.146		65.45		99.99876		100.03172		576.96399		65.45		99.99515		576.94702		65.45		99.9989		612.46878		65.45		100.03172		614.04867		65.45		100.04714		616.5831		65.45		100.02797

		577.40802		65.475		99.99788		100.03172		577.23102		65.475		99.99211		577.20801		65.475		100.00154		612.72133		65.475		100.03172		614.29411		65.475		100.04717		616.82588		65.475		100.02797

		577.65997		65.5		99.99758		100.03172		577.50098		65.5		99.99274		577.47101		65.5		99.99653		612.973		65.5		100.03172		614.54055		65.5		100.0472		617.06833		65.5		100.02798

		577.927		65.525		99.99889		100.03172		577.763		65.525		99.9948		577.73798		65.525		100.0026		613.21833		65.525		100.03172		614.78711		65.525		100.04722		617.30855		65.525		100.02798

		578.18201		65.55		99.99832		100.03174		578.02698		65.55		99.99149		578.00702		65.55		99.99809		613.45766		65.55		100.03174		615.03422		65.55		100.04725		617.54721		65.55		100.02799

		578.45599		65.575		99.99965		100.03177		578.28101		65.575		99.9941		578.26599		65.575		100.00101		613.69744		65.575		100.03177		615.28244		65.575		100.04728		617.79154		65.575		100.028

		578.72803		65.6		99.99861		100.03181		578.55298		65.6		99.9939		578.53699		65.6		100.0008		613.93633		65.6		100.03181		615.53311		65.6		100.04731		618.03632		65.6		100.02802

		578.98499		65.625		100.00064		100.03186		578.80701		65.625		99.99593		578.79901		65.625		100.00155		614.17256		65.625		100.03186		615.78156		65.625		100.04733		618.28199		65.625		100.02803

		579.25		65.65		99.99923		100.03192		579.06702		65.65		99.99455		579.04999		65.65		99.99884		614.41956		65.65		100.03192		616.03056		65.65		100.04736		618.53355		65.65		100.02805

		579.49902		65.675		99.99957		100.03199		579.33698		65.675		99.99489		579.323		65.675		99.99997		614.66822		65.675		100.03199		616.27979		65.675		100.04739		618.78343		65.675		100.02807

		579.776		65.7		99.99898		100.03207		579.59802		65.7		99.99469		579.59601		65.7		99.99925		614.91822		65.7		100.03207		616.52623		65.7		100.04741		619.03166		65.7		100.02809

		580.039		65.725		100		100.03215		579.85999		65.725		99.99667		579.85498		65.725		100.0017		615.16856		65.725		100.03215		616.77045		65.725		100.04744		619.28021		65.725		100.02812

		580.29498		65.75		99.99874		100.03224		580.12799		65.75		99.99547		580.117		65.75		100.00107		615.423		65.75		100.03224		617.01256		65.75		100.04746		619.53299		65.75		100.02814

		580.57001		65.775		99.99944		100.03234		580.39099		65.775		99.99504		580.38202		65.775		99.99785		615.67922		65.775		100.03234		617.25245		65.775		100.04748		619.78499		65.775		100.02817

		580.82599		65.8		99.99921		100.03243		580.64001		65.8		99.99557		580.63898		65.8		99.99887		615.93167		65.8		100.03243		617.48912		65.8		100.04749		620.02944		65.8		100.02819

		581.09601		65.825		100.00151		100.03252		580.909		65.825		99.99609		580.90503		65.825		100.00187		616.18411		65.825		100.03252		617.73033		65.825		100.0475		620.27311		65.825		100.02821

		581.36102		65.85		99.99957		100.03261		581.17798		65.85		99.99584		581.17499		65.85		100.00111		616.44133		65.85		100.03261		617.97711		65.85		100.04751		620.51788		65.85		100.02823

		581.63202		65.875		99.99798		100.0327		581.43701		65.875		99.99652		581.422		65.875		99.99811		616.68911		65.875		100.0327		618.225		65.875		100.04751		620.75732		65.875		100.02825

		581.888		65.9		99.99793		100.03277		581.69897		65.9		99.99494		581.69702		65.9		99.99962		616.93478		65.9		100.03277		618.47367		65.9		100.0475		620.99677		65.9		100.02826

		582.15503		65.925		99.99822		100.03284		581.97198		65.925		99.99369		581.96002		65.925		99.99889		617.176		65.925		100.03284		618.72188		65.925		100.04749		621.24355		65.925		100.02827

		582.41901		65.95		99.99945		100.0329		582.23499		65.95		99.99412		582.22601		65.95		99.99749		617.41444		65.95		100.0329		618.96889		65.95		100.04748		621.49255		65.95		100.02827

		582.67999		65.975		99.99834		100.03294		582.49597		65.975		99.99611		582.49103		65.975		100.00294		617.65189		65.975		100.03294		619.21922		65.975		100.04746		621.74189		65.975		100.02827

		582.95001		66		100.00045		100.03298		582.75702		66		99.99366		582.75702		66		100.00005		617.89656		66		100.03298		619.47045		66		100.04744		621.99511		66		100.02827

		583.21198		66.025		99.99659		100.033		583.01801		66.025		99.99236		583.00299		66.025		99.99948		618.14423		66.025		100.033		619.72389		66.025		100.04741		622.249		66.025		100.02826

		583.47699		66.05		100.00003		100.03302		583.28302		66.05		99.99571		583.27502		66.05		99.99918		618.39145		66.05		100.03302		619.97178		66.05		100.04738		622.50356		66.05		100.02825

		583.737		66.075		99.9989		100.03302		583.54199		66.075		99.99513		583.54303		66.075		100.00055		618.63856		66.075		100.03302		620.21545		66.075		100.04736		622.75745		66.075		100.02823

		583.99799		66.1		100.00068		100.03301		583.81		66.1		99.99434		583.81799		66.1		99.99945		618.88356		66.1		100.03301		620.45744		66.1		100.04733		623.01378		66.1		100.02821

		584.26599		66.125		99.99818		100.033		584.07397		66.125		99.99511		584.07098		66.125		100.00021		619.13089		66.125		100.033		620.70189		66.125		100.0473		623.26923		66.125		100.0282

		584.51703		66.15		99.99817		100.03298		584.33502		66.15		99.99704		584.33502		66.15		99.99958		619.38078		66.15		100.03298		620.94534		66.15		100.04728		623.51767		66.15		100.02818

		584.79303		66.175		99.99967		100.03295		584.599		66.175		99.9946		584.59198		66.175		99.99977		619.63245		66.175		100.03295		621.19345		66.175		100.04726		623.7659		66.175		100.02816

		585.05298		66.2		100.00005		100.03292		584.86798		66.2		99.995		584.85797		66.2		100.00027		619.88344		66.2		100.03292		621.44311		66.2		100.04724		624.00956		66.2		100.02815

		585.31897		66.225		99.99785		100.03288		585.12701		66.225		99.9922		585.12201		66.225		99.99911		620.12711		66.225		100.03288		621.69522		66.225		100.04723		624.2499		66.225		100.02814

		585.58197		66.25		99.99925		100.03284		585.39502		66.25		99.99524		585.388		66.25		99.99796		620.36855		66.25		100.03284		621.94923		66.25		100.04722		624.48867		66.25		100.02813

		585.85101		66.275		99.99878		100.03281		585.65802		66.275		99.99617		585.64301		66.275		99.99989		620.61044		66.275		100.03281		622.20544		66.275		100.04722		624.73246		66.275		100.02813

		586.10999		66.3		99.99864		100.03277		585.91498		66.3		99.9956		585.90997		66.3		99.99913		620.84966		66.3		100.03277		622.46133		66.3		100.04722		624.97845		66.3		100.02813

		586.37701		66.325		99.99853		100.03273		586.17297		66.325		99.99396		586.17297		66.325		100.00117		621.09477		66.325		100.03273		622.71833		66.325		100.04723		625.22434		66.325		100.02814

		586.63098		66.35		99.99675		100.0327		586.43903		66.35		99.99197		586.43799		66.35		99.99808		621.34355		66.35		100.0327		622.975		66.35		100.04724		625.47112		66.35		100.02815

		586.89697		66.375		99.99801		100.03267		586.70398		66.375		99.99649		586.70502		66.375		99.99771		621.59455		66.375		100.03267		623.23222		66.375		100.04726		625.721		66.375		100.02817

		587.15802		66.4		99.99843		100.03264		586.96899		66.4		99.99432		586.96802		66.4		99.99991		621.84644		66.4		100.03264		623.48522		66.4		100.04729		625.96889		66.4		100.02819

		587.42603		66.425		99.99995		100.03262		587.237		66.425		99.99516		587.23199		66.425		100.00194		622.09833		66.425		100.03262		623.73711		66.425		100.04732		626.21944		66.425		100.02822

		587.69299		66.45		99.9994		100.03261		587.50299		66.45		99.99395		587.48999		66.45		100.00064		622.35111		66.45		100.03261		623.986		66.45		100.04735		626.47122		66.45		100.02825

		587.94598		66.475		99.99993		100.03259		587.758		66.475		99.99319		587.758		66.475		100.00267		622.60834		66.475		100.03259		624.23266		66.475		100.04739		626.72288		66.475		100.02829

		588.21698		66.5		100.00069		100.03259		588.026		66.5		99.99323		588.02197		66.5		99.99863		622.86523		66.5		100.03259		624.47733		66.5		100.04743		626.96888		66.5		100.02833

		588.48102		66.525		99.99944		100.03258		588.28198		66.525		99.99687		588.28497		66.525		100.00195		623.12389		66.525		100.03258		624.72733		66.525		100.04748		627.21166		66.525		100.02836

		588.73901		66.55		100.00164		100.03258		588.54498		66.55		99.99515		588.53998		66.55		100.00172		623.37912		66.55		100.03258		624.97889		66.55		100.04752		627.45433		66.55		100.0284

		589.01599		66.575		100.00013		100.03259		588.81097		66.575		99.99431		588.80103		66.575		100.00044		623.63267		66.575		100.03259		625.22877		66.575		100.04757		627.69567		66.575		100.02844

		589.27502		66.6		99.99903		100.03259		589.06702		66.6		99.99465		589.07202		66.6		99.99881		623.88234		66.6		100.03259		625.47888		66.6		100.04762		627.93978		66.6		100.02847

		589.54303		66.625		99.99835		100.03259		589.33899		66.625		99.99487		589.33197		66.625		99.99826		624.12945		66.625		100.03259		625.72666		66.625		100.04768		628.18845		66.625		100.0285

		589.797		66.65		99.99921		100.0326		589.59802		66.65		99.99619		589.60199		66.65		99.99809		624.37456		66.65		100.0326		625.97333		66.65		100.04773		628.43756		66.65		100.02852

		590.06299		66.675		100.00081		100.0326		589.85303		66.675		99.99301		589.85901		66.675		99.99929		624.62644		66.675		100.0326		626.22144		66.675		100.04778		628.68601		66.675		100.02854

		590.33099		66.7		100.00016		100.03259		590.13		66.7		99.9951		590.11902		66.7		100.00027		624.879		66.7		100.03259		626.47177		66.7		100.04783		628.93801		66.7		100.02855

		590.591		66.725		99.99868		100.03259		590.39001		66.725		99.99341		590.38501		66.725		99.99997		625.13155		66.725		100.03259		626.72232		66.725		100.04788		629.19001		66.725		100.02855

		590.85999		66.75		100.00003		100.03258		590.646		66.75		99.99524		590.65698		66.75		99.99969		625.38344		66.75		100.03258		626.96733		66.75		100.04792		629.44012		66.75		100.02855

		591.12598		66.775		100.00052		100.03256		590.914		66.775		99.99769		590.909		66.775		100.0019		625.63477		66.775		100.03256		627.21122		66.775		100.04796		629.69101		66.775		100.02853

		591.38202		66.8		99.99751		100.03254		591.17999		66.8		99.99372		591.177		66.8		99.99864		625.88222		66.8		100.03254		627.45244		66.8		100.04799		629.94812		66.8		100.02852

		591.646		66.825		99.99823		100.03251		591.44098		66.825		99.99656		591.435		66.825		100.00011		626.13166		66.825		100.03251		627.69366		66.825		100.04802		630.20034		66.825		100.02849

		591.91699		66.85		99.99879		100.03249		591.70203		66.85		99.99219		591.703		66.85		99.99864		626.38244		66.85		100.03249		627.94144		66.85		100.04804		630.44946		66.85		100.02846

		592.18298		66.875		99.99896		100.03245		591.96301		66.875		99.99372		591.96899		66.875		100.00119		626.63466		66.875		100.03245		628.19089		66.875		100.04806		630.69678		66.875		100.02843

		592.43903		66.9		99.99937		100.03242		592.23297		66.9		99.99345		592.22302		66.9		99.99954		626.87911		66.9		100.03242		628.44045		66.9		100.04807		630.94378		66.9		100.0284

		592.70697		66.925		99.99887		100.03238		592.5		66.925		99.99585		592.48999		66.925		99.99958		627.12022		66.925		100.03238		628.68867		66.925		100.04807		631.18789		66.925		100.02837

		592.96997		66.95		99.99857		100.03235		592.76001		66.95		99.99773		592.75201		66.95		100.00061		627.36244		66.95		100.03235		628.94123		66.95		100.04808		631.43678		66.95		100.02833

		593.23199		66.975		99.99928		100.03231		593.026		66.975		99.99467		593.021		66.975		100.0017		627.60278		66.975		100.03231		629.19456		66.975		100.04807		631.68955		66.975		100.0283

		593.49103		67		99.99585		100.03228		593.28198		67		99.99189		593.28302		67		100.00064		627.84334		67		100.03228		629.44756		67		100.04807		631.94278		67		100.02828

		593.75403		67.025		99.99765		100.03225		593.54199		67.025		99.99349		593.54999		67.025		99.99794		628.09278		67.025		100.03225		629.70334		67.025		100.04806		632.19322		67.025		100.02825

		594.01599		67.05		99.99809		100.03222		593.80603		67.05		99.99515		593.81299		67.05		100.00143		628.34378		67.05		100.03222		629.96089		67.05		100.04806		632.443		67.05		100.02824

		594.28302		67.075		99.99858		100.0322		594.08002		67.075		99.99394		594.07202		67.075		99.99869		628.59556		67.075		100.0322		630.21322		67.075		100.04806		632.692		67.075		100.02822

		594.54602		67.1		100.00021		100.03218		594.336		67.1		99.99679		594.34003		67.1		99.99988		628.848		67.1		100.03218		630.46411		67.1		100.04805		632.94278		67.1		100.02821

		594.81		67.125		99.99864		100.03217		594.59399		67.125		99.99363		594.60602		67.125		99.99903		629.10122		67.125		100.03217		630.71444		67.125		100.04806		633.196		67.125		100.0282

		595.08002		67.15		99.99945		100.03216		594.86298		67.15		99.99511		594.86401		67.15		100.00051		629.35356		67.15		100.03216		630.96489		67.15		100.04806		633.45022		67.15		100.0282

		595.336		67.175		99.99729		100.03215		595.12799		67.175		99.99559		595.13202		67.175		100.00101		629.60445		67.175		100.03215		631.21145		67.175		100.04807		633.69933		67.175		100.0282

		595.60199		67.2		99.99933		100.03215		595.38098		67.2		99.99671		595.40002		67.2		100.00122		629.85767		67.2		100.03215		631.462		67.2		100.04808		633.9439		67.2		100.02821

		595.86499		67.225		99.99602		100.03215		595.65802		67.225		99.9942		595.66199		67.225		99.99998		630.113		67.225		100.03215		631.71444		67.225		100.0481		634.18867		67.225		100.02822

		596.12701		67.25		100.00217		100.03216		595.914		67.25		99.99799		595.91699		67.25		100.00002		630.35934		67.25		100.03216		631.96722		67.25		100.04813		634.43067		67.25		100.02823

		596.39203		67.275		99.99991		100.03217		596.17603		67.275		99.99663		596.18402		67.275		99.99969		630.60412		67.275		100.03217		632.21878		67.275		100.04816		634.67178		67.275		100.02824

		596.64899		67.3		99.99751		100.03218		596.43799		67.3		99.99548		596.44098		67.3		99.99989		630.84923		67.3		100.03218		632.47111		67.3		100.04819		634.92034		67.3		100.02825

		596.90997		67.325		100.00028		100.0322		596.70001		67.325		99.99399		596.70502		67.325		100.00128		631.0939		67.325		100.0322		632.72233		67.325		100.04822		635.16867		67.325		100.02826

		597.17999		67.35		99.99794		100.03222		596.97101		67.35		99.99396		596.97101		67.35		99.99859		631.34123		67.35		100.03222		632.97211		67.35		100.04826		635.41334		67.35		100.02827

		597.43701		67.375		99.99966		100.03224		597.23798		67.375		99.99617		597.23102		67.375		99.99967		631.59235		67.375		100.03224		633.22344		67.375		100.0483		635.65811		67.375		100.02828

		597.71002		67.4		100.00101		100.03226		597.49298		67.4		99.99486		597.492		67.4		100.00025		631.84646		67.4		100.03226		633.47566		67.4		100.04834		635.90389		67.4		100.02828

		597.96899		67.425		99.99748		100.03229		597.758		67.425		99.9932		597.75897		67.425		99.99887		632.10012		67.425		100.03229		633.72433		67.425		100.04838		636.15245		67.425		100.02829

		598.23602		67.45		99.99962		100.03231		598.013		67.45		99.99467		598.02802		67.45		100.00097		632.35256		67.45		100.03231		633.97067		67.45		100.04841		636.39966		67.45		100.0283

		598.50403		67.475		99.99937		100.03234		598.28198		67.475		99.99444		598.28198		67.475		99.99878		632.60422		67.475		100.03234		634.21667		67.475		100.04844		636.64866		67.475		100.0283

		598.76398		67.5		99.99898		100.03236		598.54602		67.5		99.99229		598.55603		67.5		100.00056		632.85689		67.5		100.03236		634.46089		67.5		100.04847		636.90044		67.5		100.02831

		599.02301		67.525		99.99835		100.03239		598.80402		67.525		99.99578		598.81201		67.525		100.00004		633.11056		67.525		100.03239		634.70556		67.525		100.0485		637.14544		67.525		100.02831

		599.29303		67.55		99.99979		100.03242		599.06799		67.55		99.99717		599.07599		67.55		99.99985		633.36533		67.55		100.03242		634.95744		67.55		100.04852		637.38966		67.55		100.02832

		599.55499		67.575		100.00072		100.03245		599.34302		67.575		99.9964		599.34198		67.575		100.00247		633.61766		67.575		100.03245		635.212		67.575		100.04853		637.63378		67.575		100.02833

		599.81598		67.6		99.99813		100.03248		599.59698		67.6		99.99525		599.59601		67.6		99.99997		633.86521		67.6		100.03248		635.46478		67.6		100.04854		637.87755		67.6		100.02834

		600.073		67.625		100.00039		100.03251		599.86102		67.625		99.99635		599.862		67.625		100.00102		634.1121		67.625		100.03251		635.71489		67.625		100.04855		638.12311		67.625		100.02835

		600.34003		67.65		99.99866		100.03255		600.125		67.65		99.99183		600.133		67.65		99.99608		634.35766		67.65		100.03255		635.96644		67.65		100.04856		638.37588		67.65		100.02837

		600.60699		67.675		99.99828		100.03259		600.38501		67.675		99.99535		600.39899		67.675		100.00174		634.59989		67.675		100.03259		636.21833		67.675		100.04857		638.62955		67.675		100.02839

		600.862		67.7		99.99819		100.03263		600.64203		67.7		99.9956		600.66101		67.7		100.00088		634.84867		67.7		100.03263		636.47144		67.7		100.04858		638.88322		67.7		100.02841

		601.12201		67.725		99.99873		100.03267		600.91302		67.725		99.99657		600.91803		67.725		100.00045		635.09833		67.725		100.03267		636.72489		67.725		100.04858		639.13844		67.725		100.02844

		601.39398		67.75		99.99984		100.03272		601.17102		67.75		99.99627		601.18201		67.75		100.00171		635.348		67.75		100.03272		636.976		67.75		100.04859		639.39211		67.75		100.02847

		601.66101		67.775		99.99882		100.03277		601.42999		67.775		99.99453		601.45001		67.775		99.99823		635.59622		67.775		100.03277		637.22255		67.775		100.04861		639.64444		67.775		100.0285

		601.91998		67.8		100.00048		100.03282		601.69897		67.8		99.99448		601.71002		67.8		99.99937		635.843		67.8		100.03282		637.46756		67.8		100.04863		639.89977		67.8		100.02853

		602.17798		67.825		99.99838		100.03288		601.966		67.825		99.9938		601.97601		67.825		99.99918		636.09289		67.825		100.03288		637.70967		67.825		100.04865		640.15578		67.825		100.02857

		602.44598		67.85		100.00012		100.03293		602.22601		67.85		99.99521		602.23798		67.85		100.00174		636.34244		67.85		100.03293		637.94933		67.85		100.04867		640.40822		67.85		100.0286

		602.70898		67.875		99.99936		100.03298		602.49799		67.875		99.99496		602.49597		67.875		100.00034		636.59389		67.875		100.03298		638.19267		67.875		100.0487		640.654		67.875		100.02863

		602.97302		67.9		99.99843		100.03303		602.75299		67.9		99.99514		602.76801		67.9		99.99953		636.84833		67.9		100.03303		638.44011		67.9		100.04873		640.89966		67.9		100.02866

		603.22998		67.925		100.0008		100.03308		603.013		67.925		99.9938		603.03601		67.925		99.99927		637.09521		67.925		100.03308		638.68777		67.925		100.04876		641.14311		67.925		100.02868

		603.49902		67.95		100.00152		100.03312		603.27197		67.95		99.99601		603.29102		67.95		99.99973		637.3411		67.95		100.03312		638.93777		67.95		100.04879		641.383		67.95		100.0287

		603.75299		67.975		99.99941		100.03316		603.54797		67.975		99.99342		603.55902		67.975		99.99868		637.58655		67.975		100.03316		639.18977		67.975		100.04882		641.62933		67.975		100.02872

		604.026		68		100.00034		100.03319		603.80603		68		99.99585		603.815		68		100.00086		637.83055		68		100.03319		639.43911		68		100.04885		641.88077		68		100.02873

		604.28003		68.025		99.99898		100.0332		604.06598		68.025		99.9946		604.07501		68.025		99.99959		638.07366		68.025		100.0332		639.6901		68.025		100.04888		642.13244		68.025		100.02874

		604.54498		68.05		99.99944		100.03322		604.323		68.05		99.99318		604.34198		68.05		100.001		638.32043		68.05		100.03322		639.94288		68.05		100.0489		642.38599		68.05		100.02874

		604.79498		68.075		99.99992		100.03322		604.58002		68.075		99.99433		604.60999		68.075		99.99833		638.56877		68.075		100.03322		640.2011		68.075		100.04893		642.63833		68.075		100.02873

		605.065		68.1		99.99907		100.03321		604.84998		68.1		99.99545		604.87201		68.1		100.00087		638.81644		68.1		100.03321		640.45355		68.1		100.04895		642.89054		68.1		100.02873

		605.33801		68.125		99.99789		100.0332		605.11902		68.125		99.99279		605.125		68.125		100.00024		639.06611		68.125		100.0332		640.70232		68.125		100.04896		643.14443		68.125		100.02872

		605.59601		68.15		100.00104		100.03318		605.37598		68.15		99.99374		605.39502		68.15		100.00329		639.31889		68.15		100.03318		640.94877		68.15		100.04897		643.39865		68.15		100.0287

		605.862		68.175		99.99894		100.03315		605.63898		68.175		99.99482		605.65802		68.175		100.00006		639.569		68.175		100.03315		641.19155		68.175		100.04898		643.6551		68.175		100.02869

		606.117		68.2		99.99822		100.03311		605.90198		68.2		99.99383		605.91901		68.2		99.99956		639.81744		68.2		100.03311		641.43344		68.2		100.04899		643.905		68.2		100.02868

		606.383		68.225		99.99762		100.03308		606.17102		68.225		99.99287		606.18298		68.225		99.99848		640.07111		68.225		100.03308		641.67978		68.225		100.049		644.15266		68.225		100.02866

		606.65302		68.25		100.00038		100.03304		606.43402		68.25		99.99442		606.44202		68.25		99.99756		640.32745		68.25		100.03304		641.92744		68.25		100.049		644.39766		68.25		100.02865

		606.90503		68.275		100.00031		100.033		606.69299		68.275		99.99379		606.71002		68.275		99.99976		640.57611		68.275		100.033		642.17845		68.275		100.049		644.63888		68.275		100.02863

		607.17401		68.3		99.99793		100.03296		606.95203		68.3		99.99316		606.97601		68.3		99.9978		640.81944		68.3		100.03296		642.42944		68.3		100.049		644.88033		68.3		100.02862

		607.43298		68.325		99.99885		100.03292		607.224		68.325		99.99646		607.22998		68.325		100.00068		641.06322		68.325		100.03292		642.67834		68.325		100.04899		645.12944		68.325		100.02861

		607.69397		68.35		100.00118		100.03288		607.48297		68.35		99.99358		607.50098		68.35		100.00196		641.30644		68.35		100.03288		642.92623		68.35		100.04899		645.38033		68.35		100.0286

		607.95801		68.375		99.99881		100.03285		607.74701		68.375		99.99389		607.763		68.375		99.99978		641.54833		68.375		100.03285		643.17934		68.375		100.04899		645.633		68.375		100.0286

		608.21503		68.4		99.99877		100.03282		608.01398		68.4		99.99416		608.02502		68.4		99.99916		641.79921		68.4		100.03282		643.43578		68.4		100.04898		645.88288		68.4		100.02859

		608.487		68.425		99.99891		100.0328		608.26501		68.425		99.99547		608.29199		68.425		99.99979		642.05033		68.425		100.0328		643.69167		68.425		100.04898		646.13299		68.425		100.02859

		608.74902		68.45		99.99986		100.03278		608.53198		68.45		99.99603		608.55499		68.45		100.00016		642.29921		68.45		100.03278		643.94089		68.45		100.04898		646.38177		68.45		100.02859

		609.013		68.475		99.99657		100.03277		608.79498		68.475		99.99533		608.81299		68.475		99.99875		642.54544		68.475		100.03277		644.19134		68.475		100.04898		646.63211		68.475		100.0286

		609.26703		68.5		99.99945		100.03277		609.05902		68.5		99.99695		609.07599		68.5		99.99807		642.79566		68.5		100.03277		644.43889		68.5		100.04898		646.88255		68.5		100.0286

		609.53802		68.525		99.99784		100.03277		609.31097		68.525		99.9947		609.33502		68.525		99.99952		643.04955		68.525		100.03277		644.68456		68.525		100.04898		647.13555		68.525		100.02861

		609.79797		68.55		99.99941		100.03277		609.57599		68.55		99.99876		609.60101		68.55		100.00131		643.30422		68.55		100.03277		644.92866		68.55		100.04898		647.38022		68.55		100.02862

		610.06403		68.575		99.99699		100.03279		609.841		68.575		99.99412		609.86401		68.575		99.99799		643.55766		68.575		100.03279		645.18355		68.575		100.04899		647.61977		68.575		100.02863

		610.33197		68.6		99.99879		100.03281		610.10303		68.6		99.99356		610.125		68.6		100.00188		643.81111		68.6		100.03281		645.43644		68.6		100.049		647.85577		68.6		100.02864

		610.58301		68.625		99.9976		100.03283		610.35797		68.625		99.99744		610.38898		68.625		99.99941		644.05655		68.625		100.03283		645.68922		68.625		100.04901		648.09366		68.625		100.02866

		610.85303		68.65		99.99982		100.03285		610.63		68.65		99.99469		610.651		68.65		99.99984		644.302		68.65		100.03285		645.94244		68.65		100.04903		648.33366		68.65		100.02867

		611.104		68.675		99.99924		100.03288		610.888		68.675		99.9977		610.91803		68.675		99.99838		644.54489		68.675		100.03288		646.19833		68.675		100.04904		648.58255		68.675		100.02869

		611.37		68.7		99.99959		100.0329		611.14801		68.7		99.99616		611.18298		68.7		100.00085		644.78755		68.7		100.0329		646.45232		68.7		100.04906		648.83243		68.7		100.0287

		611.63702		68.725		99.99827		100.03293		611.414		68.725		99.99305		611.44702		68.725		100.00167		645.03255		68.725		100.03293		646.70721		68.725		100.04909		649.08366		68.725		100.02871

		611.896		68.75		99.99545		100.03296		611.67999		68.75		99.99336		611.716		68.75		99.99814		645.28311		68.75		100.03296		646.96288		68.75		100.04911		649.33499		68.75		100.02873

		612.15997		68.775		99.99844		100.033		611.93903		68.775		99.99361		611.97498		68.775		100.00034		645.53355		68.775		100.033		647.21933		68.775		100.04913		649.58655		68.775		100.02874

		612.42499		68.8		99.99948		100.03303		612.19202		68.8		99.99581		612.23199		68.8		100.00198		645.78411		68.8		100.03303		647.46489		68.8		100.04915		649.84055		68.8		100.02875

		612.685		68.825		99.99729		100.03306		612.46899		68.825		99.99406		612.508		68.825		100.00077		646.03488		68.825		100.03306		647.70856		68.825		100.04918		650.09711		68.825		100.02876

		612.94299		68.85		99.99993		100.03309		612.72601		68.85		99.99493		612.76398		68.85		99.9995		646.29033		68.85		100.03309		647.95133		68.85		100.0492		650.35278		68.85		100.02876

		613.211		68.875		99.99848		100.03313		612.992		68.875		99.99537		613.02301		68.875		99.99962		646.54722		68.875		100.03313		648.19156		68.875		100.04922		650.60789		68.875		100.02877

		613.47101		68.9		99.99898		100.03316		613.24902		68.9		99.99292		613.289		68.9		99.99868		646.80333		68.9		100.03316		648.43755		68.9		100.04925		650.85122		68.9		100.02877

		613.72998		68.925		99.99948		100.0332		613.51599		68.925		99.99607		613.54498		68.925		100.00088		647.06011		68.925		100.0332		648.68589		68.925		100.04927		651.09334		68.925		100.02878

		613.992		68.95		99.9973		100.03323		613.77899		68.95		99.99627		613.80603		68.95		100.00057		647.31411		68.95		100.03323		648.93234		68.95		100.04929		651.33378		68.95		100.02878

		614.25702		68.975		99.99759		100.03327		614.03302		68.975		99.99498		614.07501		68.975		99.99947		647.56045		68.975		100.03327		649.17834		68.975		100.0493		651.57334		68.975		100.02877

		614.52301		69		99.99869		100.03331		614.289		69		99.99437		614.33801		69		99.99822		647.80345		69		100.03331		649.42978		69		100.04932		651.81778		69		100.02877

		614.78699		69.025		99.99945		100.03335		614.56299		69.025		99.99507		614.60101		69.025		99.99871		648.04456		69.025		100.03335		649.67878		69.025		100.04934		652.06245		69.025		100.02876

		615.05902		69.05		99.997		100.03339		614.81799		69.05		99.99289		614.86401		69.05		99.99943		648.28878		69.05		100.03339		649.926		69.05		100.04935		652.31112		69.05		100.02875

		615.31702		69.075		100.0003		100.03343		615.08301		69.075		99.99503		615.12701		69.075		100.0038		648.53722		69.075		100.03343		650.17222		69.075		100.04936		652.56145		69.075		100.02874

		615.57397		69.1		99.99992		100.03346		615.33698		69.1		99.99591		615.39001		69.1		100.00021		648.78578		69.1		100.03346		650.42311		69.1		100.04937		652.81223		69.1		100.02873

		615.83197		69.125		99.9984		100.0335		615.60498		69.125		99.99765		615.64398		69.125		100.00113		649.03745		69.125		100.0335		650.66611		69.125		100.04937		653.06612		69.125		100.02871

		616.10303		69.15		100.00063		100.03353		615.87097		69.15		99.99759		615.909		69.15		100.00099		649.28745		69.15		100.03353		650.90444		69.15		100.04937		653.31901		69.15		100.02869

		616.36401		69.175		99.99946		100.03355		616.13898		69.175		99.99502		616.17102		69.175		100.00151		649.53923		69.175		100.03355		651.14277		69.175		100.04936		653.57545		69.175		100.02867

		616.625		69.2		99.99828		100.03358		616.38898		69.2		99.99451		616.43799		69.2		100.00129		649.79156		69.2		100.03358		651.38489		69.2		100.04935		653.8319		69.2		100.02865

		616.88098		69.225		99.99792		100.0336		616.65601		69.225		99.9936		616.703		69.225		100.00038		650.04189		69.225		100.0336		651.62122		69.225		100.04934		654.08101		69.225		100.02863

		617.138		69.25		99.99857		100.03362		616.92102		69.25		99.99366		616.961		69.25		99.99869		650.29367		69.25		100.03362		651.86599		69.25		100.04933		654.328		69.25		100.02861

		617.40503		69.275		100.0002		100.03364		617.17603		69.275		99.9942		617.22998		69.275		100.00042		650.54312		69.275		100.03364		652.11422		69.275		100.04931		654.57089		69.275		100.02859

		617.66302		69.3		100.00155		100.03367		617.43799		69.3		99.99649		617.47998		69.3		100.00216		650.78456		69.3		100.03367		652.36566		69.3		100.04929		654.81211		69.3		100.02857

		617.935		69.325		99.99927		100.03369		617.69397		69.325		99.99323		617.74597		69.325		99.99935		651.02412		69.325		100.03369		652.61578		69.325		100.04928		655.05111		69.325		100.02856

		618.19397		69.35		99.99965		100.03372		617.95398		69.35		99.99658		618.01202		69.35		100.00052		651.263		69.35		100.03372		652.86589		69.35		100.04927		655.29778		69.35		100.02855

		618.45502		69.375		100.00026		100.03376		618.229		69.375		99.99575		618.26898		69.375		100.00053		651.50555		69.375		100.03376		653.11645		69.375		100.04927		655.54644		69.375		100.02856

		618.72498		69.4		99.99949		100.0338		618.48297		69.4		99.99481		618.54199		69.4		99.99892		651.74788		69.4		100.0338		653.368		69.4		100.04927		655.79188		69.4		100.02857

		618.97498		69.425		99.99932		100.03385		618.74701		69.425		99.99513		618.80103		69.425		100.00184		651.99367		69.425		100.03385		653.61656		69.425		100.04929		656.03788		69.425		100.02859

		619.24103		69.45		99.99756		100.0339		619.01398		69.45		99.99354		619.06299		69.45		99.99916		652.24489		69.45		100.0339		653.86845		69.45		100.04931		656.28488		69.45		100.02861

		619.50403		69.475		99.99731		100.03396		619.27399		69.475		99.99275		619.31897		69.475		99.99802		652.49444		69.475		100.03396		654.11312		69.475		100.04935		656.53311		69.475		100.02865

		619.76801		69.5		99.99881		100.03402		619.54401		69.5		99.99587		619.59302		69.5		100.00026		652.74288		69.5		100.03402		654.35434		69.5		100.04939		656.78044		69.5		100.02869

		620.03998		69.525		100.00064		100.03409		619.80701		69.525		99.99711		619.849		69.525		99.99956		652.99188		69.525		100.03409		654.59345		69.525		100.04945		657.02722		69.525		100.02873

		620.29102		69.55		99.99915		100.03415		620.05798		69.55		99.99156		620.10901		69.55		99.99906		653.24077		69.55		100.03415		654.8319		69.55		100.04951		657.27433		69.55		100.02878

		620.56598		69.575		99.99801		100.03422		620.33002		69.575		99.99383		620.37799		69.575		99.9986		653.49233		69.575		100.03422		655.07323		69.575		100.04958		657.51145		69.575		100.02883

		620.81598		69.6		99.999		100.03429		620.59399		69.6		99.99601		620.64398		69.6		99.99906		653.742		69.6		100.03429		655.3239		69.6		100.04965		657.7459		69.6		100.02889

		621.07202		69.625		100.0005		100.03435		620.849		69.625		99.99459		620.90698		69.625		100.00045		653.98878		69.625		100.03435		655.57534		69.625		100.04972		657.98201		69.625		100.02893

		621.34998		69.65		99.999		100.0344		621.11798		69.65		99.99398		621.17603		69.65		100.00016		654.23255		69.65		100.0344		655.82534		69.65		100.04979		658.21701		69.65		100.02898

		621.60999		69.675		99.99851		100.03445		621.383		69.675		99.99769		621.435		69.675		100.00205		654.47755		69.675		100.03445		656.07401		69.675		100.04987		658.458		69.675		100.02902

		621.85901		69.7		100.00104		100.03448		621.64203		69.7		99.99732		621.69598		69.7		100.00295		654.72333		69.7		100.03448		656.32701		69.7		100.04993		658.70356		69.7		100.02906

		622.13		69.725		99.99945		100.03451		621.90198		69.725		99.99529		621.95599		69.725		99.99824		654.96611		69.725		100.03451		656.58056		69.725		100.04999		658.95045		69.725		100.02909

		622.39203		69.75		99.99882		100.03453		622.15997		69.75		99.995		622.21698		69.75		100.00029		655.21399		69.75		100.03453		656.83289		69.75		100.05005		659.19689		69.75		100.02911

		622.65698		69.775		99.99929		100.03453		622.42102		69.775		99.9944		622.46997		69.775		99.99833		655.46577		69.775		100.03453		657.08345		69.775		100.0501		659.44577		69.775		100.02912

		622.91498		69.8		99.99818		100.03453		622.68597		69.8		99.99589		622.742		69.8		99.99976		655.71476		69.8		100.03453		657.33345		69.8		100.05015		659.69688		69.8		100.02913

		623.17499		69.825		99.99835		100.03453		622.94397		69.825		99.99437		623.00201		69.825		99.99962		655.96554		69.825		100.03453		657.57711		69.825		100.05019		659.94954		69.825		100.02914

		623.44098		69.85		99.9999		100.03451		623.21002		69.85		99.99663		623.26599		69.85		99.99935		656.21643		69.85		100.03451		657.81923		69.85		100.05022		660.20043		69.85		100.02914

		623.70502		69.875		99.99788		100.0345		623.47302		69.875		99.9936		623.53198		69.875		99.99958		656.46821		69.875		100.0345		658.05956		69.875		100.05025		660.45188		69.875		100.02914

		623.95801		69.9		100.00194		100.03448		623.73102		69.9		99.99556		623.78699		69.9		100.00121		656.7161		69.9		100.03448		658.29878		69.9		100.05027		660.69899		69.9		100.02914

		624.21503		69.925		100.00031		100.03445		623.99298		69.925		99.99737		624.04199		69.925		100.00108		656.96099		69.925		100.03445		658.539		69.925		100.05029		660.94188		69.925		100.02915

		624.48102		69.95		100.0029		100.03443		624.25702		69.95		99.99682		624.32001		69.95		100.00242		657.20921		69.95		100.03443		658.78289		69.95		100.05031		661.18411		69.95		100.02915

		624.74298		69.975		100.00266		100.03441		624.505		69.975		99.9972		624.58099		69.975		100.00173		657.451		69.975		100.03441		659.02712		69.975		100.05032		661.42678		69.975		100.02915

		625.01099		70		100.00008		100.03438		624.77802		70		99.99503		624.84198		70		100.00049		657.69133		70		100.03438		659.27279		70		100.05033		661.66622		70		100.02916

		625.26898		70.025		100.00045		100.03437		625.03998		70.025		99.99414		625.09698		70.025		99.99826		657.92855		70.025		100.03437		659.51923		70.025		100.05035		661.91111		70.025		100.02917

		625.52698		70.05		99.999		100.03435		625.29901		70.05		99.99301		625.36298		70.05		99.99946		658.16355		70.05		100.03435		659.76145		70.05		100.05036		662.15744		70.05		100.02918

		625.79797		70.075		99.99838		100.03434		625.56097		70.075		99.99427		625.625		70.075		100.00112		658.39889		70.075		100.03434		660.00422		70.075		100.05036		662.40377		70.075		100.0292

		626.05603		70.1		99.99938		100.03433		625.82898		70.1		99.995		625.88501		70.1		100.00101		658.64234		70.1		100.03433		660.24978		70.1		100.05037		662.65133		70.1		100.02921

		626.32001		70.125		99.99979		100.03433		626.091		70.125		99.99464		626.15802		70.125		100.0014		658.8869		70.125		100.03433		660.49734		70.125		100.05037		662.89889		70.125		100.02923

		626.58002		70.15		100.00071		100.03433		626.34998		70.15		99.99633		626.42499		70.15		100.00011		659.13456		70.15		100.03433		660.74078		70.15		100.05038		663.14511		70.15		100.02925

		626.84302		70.175		99.99835		100.03434		626.60797		70.175		99.99469		626.67603		70.175		99.99905		659.38456		70.175		100.03434		660.98156		70.175		100.05038		663.39088		70.175		100.02928

		627.10303		70.2		99.99775		100.03436		626.86902		70.2		99.99536		626.94		70.2		99.99851		659.63411		70.2		100.03436		661.22189		70.2		100.05038		663.63733		70.2		100.0293

		627.37299		70.225		100.00101		100.03437		627.13397		70.225		99.99562		627.20203		70.225		99.99978		659.88167		70.225		100.03437		661.46255		70.225		100.05038		663.88544		70.225		100.02932

		627.63098		70.25		100.00026		100.03439		627.39899		70.25		99.99679		627.46899		70.25		100.00034		660.13267		70.25		100.03439		661.70378		70.25		100.05038		664.12756		70.25		100.02934

		627.90198		70.275		99.999		100.03441		627.65802		70.275		99.99438		627.72302		70.275		100.00053		660.38434		70.275		100.03441		661.95244		70.275		100.05038		664.36867		70.275		100.02936

		628.15698		70.3		99.99823		100.03443		627.92902		70.3		99.99656		627.98602		70.3		100.00008		660.63589		70.3		100.03443		662.20177		70.3		100.05037		664.61034		70.3		100.02937

		628.42102		70.325		100.00168		100.03446		628.185		70.325		99.99281		628.25299		70.325		99.99962		660.879		70.325		100.03446		662.45355		70.325		100.05037		664.85034		70.325		100.02938

		628.67999		70.35		100.00127		100.03448		628.44098		70.35		99.99349		628.513		70.35		100.00047		661.11978		70.35		100.03448		662.70443		70.35		100.05036		665.08911		70.35		100.02939

		628.93701		70.375		100.00267		100.0345		628.71399		70.375		99.99486		628.77002		70.375		100.00255		661.35978		70.375		100.0345		662.95699		70.375		100.05035		665.334		70.375		100.0294

		629.19897		70.4		99.99701		100.03452		628.96997		70.4		99.9911		629.03998		70.4		100.0012		661.60011		70.4		100.03452		663.20721		70.4		100.05034		665.58378		70.4		100.02939

		629.46802		70.425		100.00016		100.03453		629.23297		70.425		99.99434		629.29498		70.425		100.00265		661.84433		70.425		100.03453		663.46177		70.425		100.05033		665.83311		70.425		100.02939

		629.72803		70.45		99.99874		100.03453		629.48602		70.45		99.99598		629.56097		70.45		100.00066		662.09211		70.45		100.03453		663.71655		70.45		100.05031		666.08022		70.45		100.02938

		630.00098		70.475		100.0002		100.03453		629.74402		70.475		99.9975		629.82501		70.475		99.99997		662.34		70.475		100.03453		663.96922		70.475		100.0503		666.32622		70.475		100.02937

		630.24902		70.5		99.99771		100.03453		630.013		70.5		99.99562		630.09302		70.5		100.00042		662.59011		70.5		100.03453		664.21544		70.5		100.05029		666.57411		70.5		100.02935

		630.51202		70.525		100.00051		100.03451		630.27502		70.525		99.9959		630.36298		70.525		100.0005		662.83944		70.525		100.03451		664.45933		70.525		100.05028		666.82311		70.525		100.02933

		630.78497		70.55		99.99972		100.03449		630.53497		70.55		99.99429		630.62		70.55		99.9992		663.08689		70.55		100.03449		664.70066		70.55		100.05027		667.07311		70.55		100.02931

		631.04303		70.575		100.00183		100.03446		630.79303		70.575		99.99598		630.88202		70.575		99.99924		663.33622		70.575		100.03446		664.94166		70.575		100.05026		667.323		70.575		100.02928

		631.30298		70.6		100.00012		100.03443		631.06		70.6		99.99471		631.14001		70.6		99.99926		663.588		70.6		100.03443		665.18444		70.6		100.05025		667.56677		70.6		100.02926

		631.56097		70.625		99.99941		100.03439		631.32397		70.625		99.99383		631.40198		70.625		100.00135		663.83778		70.625		100.03439		665.43522		70.625		100.05025		667.80744		70.625		100.02924

		631.82898		70.65		100.00005		100.03434		631.58698		70.65		99.99483		631.67297		70.65		100.00076		664.083		70.65		100.03434		665.68322		70.65		100.05025		668.04678		70.65		100.02922

		632.091		70.675		99.99627		100.03429		631.849		70.675		99.99509		631.93298		70.675		99.9975		664.32611		70.675		100.03429		665.93066		70.675		100.05026		668.28822		70.675		100.0292

		632.35303		70.7		99.99868		100.03424		632.10602		70.7		99.99493		632.19		70.7		100.00082		664.56633		70.7		100.03424		666.18011		70.7		100.05026		668.53111		70.7		100.02918

		632.61298		70.725		99.99666		100.03419		632.37701		70.725		99.99314		632.461		70.725		99.99826		664.80622		70.725		100.03419		666.42689		70.725		100.05027		668.77789		70.725		100.02917

		632.87598		70.75		99.99682		100.03415		632.633		70.75		99.99439		632.72198		70.75		100.0001		665.04588		70.75		100.03415		666.67733		70.75		100.05028		669.02355		70.75		100.02916

		633.14001		70.775		99.99938		100.0341		632.901		70.775		99.99317		632.98297		70.775		99.99982		665.29256		70.775		100.0341		666.92756		70.775		100.0503		669.26922		70.775		100.02916

		633.40503		70.8		100.00193		100.03406		633.15802		70.8		99.99668		633.24103		70.8		99.99849		665.54333		70.8		100.03406		667.17744		70.8		100.05031		669.51522		70.8		100.02916

		633.65997		70.825		99.999		100.03402		633.41498		70.825		99.99498		633.50403		70.825		99.99973		665.79378		70.825		100.03402		667.42389		70.825		100.05033		669.762		70.825		100.02916

		633.91998		70.85		99.9989		100.03399		633.68103		70.85		99.99687		633.76599		70.85		99.99948		666.04189		70.85		100.03399		667.66477		70.85		100.05036		670.00944		70.85		100.02917

		634.17499		70.875		99.99815		100.03397		633.94202		70.875		99.99414		634.02698		70.875		99.99878		666.29034		70.875		100.03397		667.90533		70.875		100.05038		670.25899		70.875		100.02918

		634.44501		70.9		100.00048		100.03396		634.20898		70.9		99.99503		634.29602		70.9		99.99926		666.54123		70.9		100.03396		668.146		70.9		100.05041		670.5081		70.9		100.02919

		634.70801		70.925		100.00039		100.03395		634.46899		70.925		99.99432		634.54401		70.925		99.99928		666.79345		70.925		100.03395		668.38533		70.925		100.05044		670.75522		70.925		100.02921

		634.96198		70.95		99.99843		100.03396		634.724		70.95		99.99499		634.81097		70.95		99.9999		667.04578		70.95		100.03396		668.63566		70.95		100.05047		670.99588		70.95		100.02923

		635.22998		70.975		99.99735		100.03397		634.97998		70.975		99.9941		635.08197		70.975		100.00117		667.29967		70.975		100.03397		668.88333		70.975		100.05051		671.23733		70.975		100.02925

		635.495		71		99.99686		100.034		635.24701		71		99.99411		635.34497		71		99.99598		667.54778		71		100.034		669.13333		71		100.05055		671.47722		71		100.02927

		635.76099		71.025		99.99997		100.03403		635.51202		71.025		99.99478		635.60901		71.025		99.99881		667.79111		71.025		100.03403		669.38244		71.025		100.05059		671.71667		71.025		100.0293

		636.01898		71.05		99.9973		100.03407		635.771		71.05		99.99165		635.86902		71.05		99.9985		668.03333		71.05		100.03407		669.63355		71.05		100.05064		671.96367		71.05		100.02933

		636.27802		71.075		99.99794		100.03412		636.01898		71.075		99.99329		636.13599		71.075		99.99858		668.27544		71.075		100.03412		669.88522		71.075		100.05069		672.20945		71.075		100.02936

		636.53699		71.1		99.99912		100.03418		636.29303		71.1		99.99363		636.39398		71.1		99.99945		668.52121		71.1		100.03418		670.13466		71.1		100.05074		672.45633		71.1		100.02939

		636.79999		71.125		100.00056		100.03424		636.55798		71.125		99.99535		636.659		71.125		100.00028		668.77121		71.125		100.03424		670.38411		71.125		100.0508		672.70722		71.125		100.02942

		637.06598		71.15		99.99654		100.03431		636.82001		71.15		99.99308		636.91602		71.15		99.99906		669.02199		71.15		100.03431		670.63578		71.15		100.05086		672.96111		71.15		100.02946

		637.33099		71.175		99.99767		100.03439		637.08502		71.175		99.99585		637.177		71.175		100.00053		669.27177		71.175		100.03439		670.87855		71.175		100.05092		673.21411		71.175		100.0295

		637.58899		71.2		99.99883		100.03446		637.34497		71.2		99.99318		637.44299		71.2		99.9996		669.51999		71.2		100.03446		671.12233		71.2		100.05099		673.46789		71.2		100.02954

		637.85901		71.225		100.00151		100.03455		637.60303		71.225		99.99514		637.698		71.225		100.00171		669.76844		71.225		100.03455		671.36144		71.225		100.05105		673.72544		71.225		100.02958

		638.12		71.25		100.00018		100.03463		637.85901		71.25		99.99478		637.96002		71.25		100.00212		670.018		71.25		100.03463		671.60322		71.25		100.05111		673.98199		71.25		100.02963

		638.37701		71.275		100.00067		100.03472		638.12		71.275		99.99509		638.22601		71.275		100.00067		670.26777		71.275		100.03472		671.84366		71.275		100.05117		674.22877		71.275		100.02967

		638.638		71.3		99.99912		100.0348		638.38501		71.3		99.99661		638.49597		71.3		99.99829		670.51666		71.3		100.0348		672.09044		71.3		100.05123		674.47444		71.3		100.02972

		638.90399		71.325		99.99908		100.03487		638.64301		71.325		99.99226		638.75702		71.325		99.99858		670.76433		71.325		100.03487		672.33922		71.325		100.05128		674.71922		71.325		100.02976

		639.15802		71.35		100.00039		100.03494		638.91302		71.35		99.99213		639.01501		71.35		99.99888		671.00489		71.35		100.03494		672.58666		71.35		100.05133		674.95911		71.35		100.0298

		639.42102		71.375		99.99769		100.035		639.16199		71.375		99.99533		639.276		71.375		99.99961		671.24589		71.375		100.035		672.83299		71.375		100.05137		675.19977		71.375		100.02984

		639.68402		71.4		99.99921		100.03506		639.43103		71.4		99.99319		639.534		71.4		99.99866		671.48534		71.4		100.03506		673.07822		71.4		100.0514		675.44699		71.4		100.02988

		639.94501		71.425		99.99864		100.0351		639.68799		71.425		99.99401		639.79999		71.425		100.00065		671.72489		71.425		100.0351		673.32367		71.425		100.05143		675.69443		71.425		100.02991

		640.21997		71.45		99.99844		100.03513		639.94598		71.45		99.99563		640.06		71.45		99.99873		671.97189		71.45		100.03513		673.57145		71.45		100.05145		675.9391		71.45		100.02994

		640.47998		71.475		100.00014		100.03516		640.20801		71.475		99.99284		640.32001		71.475		100.00047		672.21911		71.475		100.03516		673.81845		71.475		100.05146		676.18621		71.475		100.02996

		640.73499		71.5		100.00176		100.03518		640.48102		71.5		99.996		640.586		71.5		100.00095		672.46489		71.5		100.03518		674.06411		71.5		100.05146		676.43477		71.5		100.02998

		640.99298		71.525		99.99864		100.03518		640.73297		71.525		99.99477		640.85101		71.525		99.99944		672.71589		71.525		100.03518		674.30322		71.525		100.05146		676.68221		71.525		100.02999

		641.26202		71.55		100.00021		100.03519		641.00598		71.55		99.99482		641.11798		71.55		100.00151		672.96745		71.55		100.03519		674.54156		71.55		100.05146		676.92877		71.55		100.03

		641.52197		71.575		100.00008		100.03518		641.25598		71.575		99.99811		641.37402		71.575		100.00137		673.21889		71.575		100.03518		674.78067		71.575		100.05145		677.17732		71.575		100.03001

		641.77899		71.6		99.99962		100.03518		641.51501		71.6		99.99631		641.63202		71.6		100.00041		673.46844		71.6		100.03518		675.01889		71.6		100.05145		677.42499		71.6		100.03002

		642.04797		71.625		100.00477		100.03517		641.79401		71.625		99.99917		641.89502		71.625		100.004		673.719		71.625		100.03517		675.262		71.625		100.05144		677.66999		71.625		100.03003

		642.30499		71.65		100.00046		100.03516		642.039		71.65		99.99325		642.15399		71.65		100.0006		673.96922		71.65		100.03516		675.51133		71.65		100.05144		677.91254		71.65		100.03004

		642.56299		71.675		99.99986		100.03516		642.29901		71.675		99.99405		642.414		71.675		100.00028		674.21167		71.675		100.03516		675.7601		71.675		100.05144		678.15521		71.675		100.03004

		642.836		71.7		99.99794		100.03515		642.56403		71.7		99.99434		642.677		71.7		100.00062		674.45256		71.7		100.03515		676.00866		71.7		100.05145		678.39477		71.7		100.03005

		643.09003		71.725		100.0002		100.03515		642.83002		71.725		99.99461		642.93799		71.725		100.00086		674.69667		71.725		100.03515		676.258		71.725		100.05145		678.64366		71.725		100.03006

		643.349		71.75		100.00029		100.03515		643.08899		71.75		99.99335		643.20697		71.75		99.99805		674.93734		71.75		100.03515		676.50766		71.75		100.05146		678.89644		71.75		100.03007

		643.60901		71.775		100.00094		100.03515		643.34802		71.775		99.99553		643.466		71.775		100.00102		675.17823		71.775		100.03515		676.75989		71.775		100.05148		679.15044		71.775		100.03008

		643.87701		71.8		99.99838		100.03515		643.60602		71.8		99.99355		643.72699		71.8		99.99683		675.42289		71.8		100.03515		677.01289		71.8		100.0515		679.40489		71.8		100.03009

		644.13501		71.825		100.0025		100.03516		643.87201		71.825		99.99704		643.98901		71.825		100.00081		675.67034		71.825		100.03516		677.26545		71.825		100.05152		679.65811		71.825		100.0301

		644.401		71.85		100.00434		100.03516		644.13202		71.85		99.99813		644.25299		71.85		100.00152		675.919		71.85		100.03516		677.51134		71.85		100.05154		679.90878		71.85		100.03011

		644.659		71.875		99.99797		100.03517		644.40002		71.875		99.99396		644.51703		71.875		99.99847		676.16944		71.875		100.03517		677.75467		71.875		100.05156		680.16078		71.875		100.03011

		644.927		71.9		99.99763		100.03517		644.66101		71.9		99.99389		644.78101		71.9		99.99838		676.42177		71.9		100.03517		677.99923		71.9		100.05159		680.41167		71.9		100.03012

		645.185		71.925		100.00041		100.03517		644.91901		71.925		99.99462		645.04303		71.925		99.9995		676.67477		71.925		100.03517		678.24123		71.925		100.05162		680.66423		71.925		100.03012

		645.45697		71.95		100.00123		100.03517		645.18402		71.95		99.99412		645.29999		71.95		100.00155		676.92489		71.95		100.03517		678.48045		71.95		100.05164		680.90934		71.95		100.03011

		645.70398		71.975		99.99903		100.03517		645.45203		71.975		99.99426		645.56		71.975		100.00097		677.17555		71.975		100.03517		678.72822		71.975		100.05167		681.15356		71.975		100.03011

		645.96997		72		99.99899		100.03516		645.70099		72		99.99498		645.828		72		100.00014		677.4251		72		100.03516		678.975		72		100.0517		681.39701		72		100.03009

		646.22101		72.025		99.99806		100.03516		645.96301		72.025		99.99221		646.09601		72.025		99.99751		677.66999		72.025		100.03516		679.21988		72.025		100.05172		681.63734		72.025		100.03007

		646.48602		72.05		99.99666		100.03515		646.22601		72.05		99.99041		646.35498		72.05		99.99833		677.91433		72.05		100.03515		679.4641		72.05		100.05175		681.88312		72.05		100.03005

		646.75201		72.075		100.00007		100.03514		646.48499		72.075		99.99336		646.61798		72.075		100.00069		678.159		72.075		100.03514		679.71377		72.075		100.05178		682.13289		72.075		100.03002

		647.013		72.1		99.99978		100.03514		646.74799		72.1		99.99625		646.88202		72.1		100.00368		678.40156		72.1		100.03514		679.96077		72.1		100.05181		682.38356		72.1		100.03

		647.276		72.125		99.99824		100.03513		647.021		72.125		99.99426		647.13702		72.125		100.00274		678.65045		72.125		100.03513		680.20666		72.125		100.05184		682.63978		72.125		100.02997

		647.53198		72.15		99.99773		100.03513		647.26801		72.15		99.99404		647.401		72.15		100.0037		678.90057		72.15		100.03513		680.45488		72.15		100.05187		682.89855		72.15		100.02994

		647.80499		72.175		100.00118		100.03513		647.53998		72.175		99.99819		647.664		72.175		100.00186		679.15201		72.175		100.03513		680.70511		72.175		100.0519		683.15477		72.175		100.02991

		648.05902		72.2		99.99832		100.03513		647.79199		72.2		99.99404		647.91998		72.2		100.00152		679.40301		72.2		100.03513		680.94699		72.2		100.05194		683.40999		72.2		100.02989

		648.328		72.225		99.99955		100.03513		648.05402		72.225		99.99693		648.17499		72.225		99.99821		679.65512		72.225		100.03513		681.18778		72.225		100.05198		683.6671		72.225		100.02987

		648.58698		72.25		99.99764		100.03514		648.31		72.25		99.99518		648.44897		72.25		100.0015		679.90868		72.25		100.03514		681.43022		72.25		100.05202		683.92444		72.25		100.02986

		648.85602		72.275		99.99912		100.03515		648.578		72.275		99.99276		648.70801		72.275		99.9996		680.16135		72.275		100.03515		681.67322		72.275		100.05207		684.17666		72.275		100.02985

		649.10999		72.3		99.99733		100.03517		648.82501		72.3		99.99426		648.96503		72.3		100.00168		680.41235		72.3		100.03517		681.92177		72.3		100.05212		684.42489		72.3		100.02985

		649.37		72.325		99.99865		100.0352		649.09601		72.325		99.9959		649.22601		72.325		100.00255		680.66412		72.325		100.0352		682.172		72.325		100.05217		684.671		72.325		100.02986

		649.638		72.35		99.99763		100.03523		649.35901		72.35		99.99395		649.487		72.35		99.99996		680.90779		72.35		100.03523		682.42278		72.35		100.05222		684.91356		72.35		100.02988

		649.89301		72.375		99.99817		100.03526		649.62299		72.375		99.99515		649.74701		72.375		100.00075		681.14834		72.375		100.03526		682.678		72.375		100.05227		685.15234		72.375		100.0299

		650.16699		72.4		99.9991		100.0353		649.89001		72.4		99.99575		650.01099		72.4		99.99979		681.38801		72.4		100.0353		682.93433		72.4		100.05233		685.39801		72.4		100.02993

		650.41602		72.425		100.00233		100.03534		650.14697		72.425		99.99743		650.26599		72.425		99.99972		681.62901		72.425		100.03534		683.18934		72.425		100.05238		685.6459		72.425		100.02996

		650.67499		72.45		100.0014		100.03539		650.40997		72.45		99.99617		650.53198		72.45		100.00304		681.86967		72.45		100.03539		683.44545		72.45		100.05244		685.89146		72.45		100.03

		650.93597		72.475		99.99975		100.03544		650.672		72.475		99.9944		650.802		72.475		100.0014		682.11534		72.475		100.03544		683.70234		72.475		100.05249		686.13923		72.475		100.03004

		651.19598		72.5		99.99934		100.03548		650.935		72.5		99.99311		651.06201		72.5		99.99891		682.36167		72.5		100.03548		683.959		72.5		100.05254		686.38701		72.5		100.03008

		651.45502		72.525		100.00165		100.03553		651.20203		72.525		99.99455		651.32599		72.525		100.00181		682.61156		72.525		100.03553		684.20879		72.525		100.05258		686.63445		72.525		100.03011

		651.72198		72.55		99.99958		100.03558		651.453		72.55		99.9956		651.586		72.55		99.99971		682.85911		72.55		100.03558		684.45512		72.55		100.05262		686.8839		72.55		100.03015

		651.96899		72.575		100.00317		100.03562		651.71997		72.575		99.99616		651.84302		72.575		100.00222		683.10633		72.575		100.03562		684.70178		72.575		100.05266		687.12978		72.575		100.03017

		652.24902		72.6		100.00031		100.03566		651.974		72.6		99.99219		652.10797		72.6		99.99963		683.35544		72.6		100.03566		684.94622		72.6		100.05269		687.37822		72.6		100.0302

		652.49701		72.625		100.00086		100.03569		652.24298		72.625		99.99396		652.36298		72.625		100.00013		683.60955		72.625		100.03569		685.19067		72.625		100.05271		687.62456		72.625		100.03021

		652.755		72.65		100.00055		100.03572		652.50702		72.65		99.99317		652.62701		72.65		99.99924		683.86511		72.65		100.03572		685.44		72.65		100.05273		687.86645		72.65		100.03023

		653.01898		72.675		100.00151		100.03575		652.75598		72.675		99.99804		652.89099		72.675		99.99929		684.11689		72.675		100.03575		685.692		72.675		100.05274		688.10945		72.675		100.03023

		653.27698		72.7		100.00214		100.03577		653.02002		72.7		99.99546		653.15302		72.7		99.99866		684.36289		72.7		100.03577		685.94567		72.7		100.05275		688.35056		72.7		100.03023

		653.54498		72.725		100.00117		100.03579		653.28198		72.725		99.99653		653.40997		72.725		99.99948		684.60489		72.725		100.03579		686.19756		72.725		100.05275		688.59722		72.725		100.03023

		653.802		72.75		100.00014		100.0358		653.547		72.75		99.99505		653.67401		72.75		100.00369		684.84456		72.75		100.0358		686.44711		72.75		100.05275		688.84878		72.75		100.03022

		654.06897		72.775		100.00208		100.03581		653.81201		72.775		99.99269		653.94202		72.775		100.00052		685.084		72.775		100.03581		686.70066		72.775		100.05275		689.10033		72.775		100.0302

		654.33099		72.8		100.0001		100.03582		654.07501		72.8		99.99625		654.20898		72.8		100.00262		685.33167		72.8		100.03582		686.95367		72.8		100.05275		689.35533		72.8		100.03019

		654.59802		72.825		99.99838		100.03583		654.33301		72.825		99.99524		654.46399		72.825		99.99835		685.58378		72.825		100.03583		687.20556		72.825		100.05274		689.60878		72.825		100.03017

		654.85999		72.85		100.00366		100.03583		654.59399		72.85		99.99737		654.72803		72.85		100.00251		685.83345		72.85		100.03583		687.4549		72.85		100.05273		689.859		72.85		100.03016

		655.12701		72.875		100.00168		100.03583		654.85303		72.875		99.99548		654.97699		72.875		100.00082		686.082		72.875		100.03583		687.70256		72.875		100.05272		690.11122		72.875		100.03014

		655.37903		72.9		100.00131		100.03583		655.11603		72.9		99.99488		655.24103		72.9		100.00013		686.33056		72.9		100.03583		687.94778		72.9		100.05271		690.36366		72.9		100.03013

		655.63501		72.925		100.00132		100.03583		655.37598		72.925		99.99723		655.51801		72.925		100.00081		686.57956		72.925		100.03583		688.18989		72.925		100.0527		690.61711		72.925		100.03011

		655.89697		72.95		100.0039		100.03583		655.63599		72.95		99.99765		655.76599		72.95		100.00333		686.83222		72.95		100.03583		688.43256		72.95		100.05269		690.86599		72.95		100.03009

		656.15198		72.975		100.00088		100.03583		655.896		72.975		99.99568		656.03699		72.975		99.99946		687.08478		72.975		100.03583		688.68222		72.975		100.05268		691.10877		72.975		100.03008

		656.41803		73		100.00305		100.03583		656.15698		73		99.99455		656.28998		73		100.00024		687.34144		73		100.03583		688.93222		73		100.05266		691.35022		73		100.03007

		656.68103		73.025		99.99938		100.03583		656.41101		73.025		99.995		656.56		73.025		99.99984		687.59033		73.025		100.03583		689.18334		73.025		100.05265		691.59077		73.025		100.03006

		656.94397		73.05		100.00221		100.03582		656.67297		73.05		99.9942		656.81403		73.05		100.00122		687.83544		73.05		100.03582		689.43233		73.05		100.05264		691.83277		73.05		100.03004

		657.20697		73.075		100.00111		100.03581		656.93597		73.075		99.9942		657.08301		73.075		99.99987		688.079		73.075		100.03581		689.68555		73.075		100.05263		692.08044		73.075		100.03003

		657.46198		73.1		100.00039		100.03581		657.20203		73.1		99.99427		657.33301		73.1		99.99818		688.32089		73.1		100.03581		689.93623		73.1		100.05262		692.33155		73.1		100.03002

		657.72699		73.125		100.00241		100.0358		657.46002		73.125		99.99508		657.59302		73.125		100.0009		688.56634		73.125		100.0358		690.18534		73.125		100.05261		692.58211		73.125		100.03001

		657.98199		73.15		100.00073		100.0358		657.72302		73.15		99.99383		657.85999		73.15		100.00096		688.81923		73.15		100.0358		690.43556		73.15		100.0526		692.83644		73.15		100.03

		658.24701		73.175		100.00223		100.03579		657.98499		73.175		99.99487		658.11902		73.175		99.99902		689.07289		73.175		100.03579		690.69134		73.175		100.05259		693.09044		73.175		100.02998

		658.50897		73.2		100.00162		100.03579		658.24402		73.2		99.99271		658.37598		73.2		100.00152		689.32555		73.2		100.03579		690.93956		73.2		100.05259		693.34655		73.2		100.02997

		658.77802		73.225		99.9989		100.0358		658.51099		73.225		99.99503		658.63898		73.225		99.99957		689.57789		73.225		100.0358		691.18312		73.225		100.05258		693.60211		73.225		100.02996

		659.04102		73.25		100.0002		100.0358		658.77002		73.25		99.99666		658.90399		73.25		99.99903		689.83267		73.25		100.0358		691.42489		73.25		100.05258		693.85788		73.25		100.02995

		659.29797		73.275		100.00109		100.03581		659.03601		73.275		99.99731		659.17499		73.275		100.00136		690.08634		73.275		100.03581		691.66845		73.275		100.05259		694.11366		73.275		100.02994

		659.55701		73.3		99.9987		100.03582		659.28601		73.3		99.99156		659.43402		73.3		99.99839		690.33778		73.3		100.03582		691.91045		73.3		100.05259		694.36333		73.3		100.02993

		659.82397		73.325		100.00083		100.03584		659.55402		73.325		99.99529		659.69098		73.325		99.99995		690.59056		73.325		100.03584		692.16022		73.325		100.0526		694.60721		73.325		100.02992

		660.08301		73.35		99.99988		100.03586		659.82501		73.35		99.99296		659.95801		73.35		99.99818		690.84222		73.35		100.03586		692.41245		73.35		100.05262		694.85188		73.35		100.02991

		660.34003		73.375		100.00166		100.03588		660.08502		73.375		99.99591		660.21698		73.375		99.99993		691.08577		73.375		100.03588		692.66656		73.375		100.05263		695.09366		73.375		100.0299

		660.604		73.4		99.99983		100.0359		660.33899		73.4		99.99374		660.48102		73.4		99.99584		691.32656		73.4		100.0359		692.91833		73.4		100.05266		695.33511		73.4		100.0299

		660.86603		73.425		99.99946		100.03593		660.604		73.425		99.99361		660.74701		73.425		99.9968		691.56834		73.425		100.03593		693.173		73.425		100.05269		695.58167		73.425		100.02989

		661.13098		73.45		100.00096		100.03597		660.85797		73.45		99.99696		661		73.45		100.00108		691.81068		73.45		100.03597		693.42855		73.45		100.05272		695.83078		73.45		100.02989

		661.39398		73.475		100.00104		100.036		661.133		73.475		99.99481		661.26599		73.475		99.99995		692.05656		73.475		100.036		693.68478		73.475		100.05276		696.08111		73.475		100.02989

		661.65601		73.5		99.99858		100.03605		661.39001		73.5		99.99716		661.53003		73.5		100.00076		692.30389		73.5		100.03605		693.94101		73.5		100.0528		696.331		73.5		100.0299

		661.90997		73.525		100.00062		100.03609		661.65198		73.525		99.9947		661.79602		73.525		100.00166		692.55367		73.525		100.03609		694.19678		73.525		100.05286		696.57978		73.525		100.02991

		662.16699		73.55		99.99801		100.03615		661.90399		73.55		99.99214		662.05103		73.55		99.99982		692.80467		73.55		100.03615		694.44423		73.55		100.05292		696.83122		73.55		100.02992

		662.43597		73.575		100.00115		100.0362		662.16901		73.575		99.99593		662.31097		73.575		100.0022		693.05712		73.575		100.0362		694.68922		73.575		100.05298		697.08266		73.575		100.02994

		662.703		73.6		99.9976		100.03627		662.43201		73.6		99.99383		662.57001		73.6		99.9978		693.3119		73.6		100.03627		694.93267		73.6		100.05306		697.33066		73.6		100.02997

		662.96198		73.625		100.00182		100.03634		662.68201		73.625		99.99765		662.83398		73.625		100.00335		693.56934		73.625		100.03634		695.174		73.625		100.05314		697.57833		73.625		100.03001

		663.21503		73.65		100.00371		100.03643		662.95398		73.65		99.99868		663.08698		73.65		100.00109		693.82657		73.65		100.03643		695.42234		73.65		100.05322		697.82133		73.65		100.03005

		663.48602		73.675		99.99984		100.03652		663.21002		73.675		99.9972		663.36298		73.675		100.00047		694.08123		73.675		100.03652		695.67145		73.675		100.05331		698.06222		73.675		100.0301

		663.745		73.7		100.00012		100.03661		663.47198		73.7		99.99499		663.61603		73.7		100.00108		694.32945		73.7		100.03661		695.92367		73.7		100.05341		698.30222		73.7		100.03016

		664.00403		73.725		100.00052		100.03672		663.73297		73.725		99.99518		663.87299		73.725		100.00091		694.57545		73.725		100.03672		696.17633		73.725		100.0535		698.54055		73.725		100.03022

		664.255		73.75		100.00242		100.03682		663.99902		73.75		99.99339		664.14001		73.75		100.0025		694.82267		73.75		100.03682		696.42722		73.75		100.0536		698.78866		73.75		100.03029

		664.51801		73.775		100.00161		100.03693		664.25702		73.775		99.99791		664.40601		73.775		100.00262		695.06822		73.775		100.03693		696.68066		73.775		100.05369		699.03878		73.775		100.03036

		664.77802		73.8		100.00064		100.03704		664.51202		73.8		99.99548		664.66498		73.8		100.00282		695.31734		73.8		100.03704		696.93555		73.8		100.05379		699.29011		73.8		100.03043

		665.03802		73.825		100.00204		100.03714		664.77899		73.825		99.9924		664.92999		73.825		100.002		695.56622		73.825		100.03714		697.19022		73.825		100.05387		699.54356		73.825		100.03051

		665.30103		73.85		99.9999		100.03724		665.03699		73.85		99.9933		665.18597		73.85		99.99929		695.81389		73.85		100.03724		697.44444		73.85		100.05395		699.79666		73.85		100.03058

		665.57501		73.875		100.00018		100.03733		665.29199		73.875		99.99284		665.44897		73.875		99.99961		696.06311		73.875		100.03733		697.69177		73.875		100.05402		700.04911		73.875		100.03064

		665.82703		73.9		99.99944		100.03742		665.56097		73.9		99.99502		665.716		73.9		99.99999		696.31444		73.9		100.03742		697.93989		73.9		100.05408		700.30067		73.9		100.0307

		666.09601		73.925		100.00168		100.03749		665.82898		73.925		99.99665		665.97601		73.925		100.00176		696.56755		73.925		100.03749		698.18411		73.925		100.05413		700.55345		73.925		100.03076

		666.35199		73.95		100.00022		100.03755		666.08002		73.95		99.99383		666.23798		73.95		99.99867		696.82255		73.95		100.03755		698.427		73.95		100.05417		700.80622		73.95		100.0308

		666.61902		73.975		99.99954		100.0376		666.34399		73.975		99.99198		666.49799		73.975		99.99824		697.07611		73.975		100.0376		698.67477		73.975		100.0542		701.05056		73.975		100.03084

		666.87598		74		99.99882		100.03764		666.60199		74		99.99274		666.755		74		99.9999		697.32667		74		100.03764		698.92622		74		100.05421		701.29311		74		100.03086

		667.14899		74.025		100.00088		100.03767		666.86401		74.025		99.99105		667.02301		74.025		99.99975		697.57411		74.025		100.03767		699.17666		74.025		100.05421		701.53333		74.025		100.03087

		667.401		74.05		99.99928		100.03768		667.13397		74.05		99.9936		667.289		74.05		100.0003		697.82345		74.05		100.03768		699.42855		74.05		100.0542		701.77255		74.05		100.03087

		667.67499		74.075		99.99924		100.03769		667.39203		74.075		99.99382		667.53601		74.075		99.99934		698.07322		74.075		100.03769		699.68233		74.075		100.05419		702.01744		74.075		100.03086

		667.92603		74.1		100.00039		100.03769		667.64899		74.1		99.99395		667.79797		74.1		100.0001		698.32311		74.1		100.03769		699.93621		74.1		100.05416		702.26533		74.1		100.03084

		668.19299		74.125		100.00283		100.03768		667.92102		74.125		99.99417		668.05798		74.125		100.00009		698.56911		74.125		100.03768		700.18766		74.125		100.05413		702.51288		74.125		100.03082

		668.44702		74.15		100.00043		100.03766		668.17999		74.15		99.99451		668.32898		74.15		99.99945		698.82134		74.15		100.03766		700.43744		74.15		100.05409		702.76155		74.15		100.03078

		668.71399		74.175		100.00073		100.03765		668.43597		74.175		99.99494		668.58398		74.175		100.00136		699.07323		74.175		100.03765		700.68722		74.175		100.05405		703.01299		74.175		100.03074

		668.97302		74.2		99.99938		100.03762		668.70502		74.2		99.99633		668.83899		74.2		100.00062		699.32645		74.2		100.03762		700.936		74.2		100.05401		703.26455		74.2		100.0307

		669.23401		74.225		99.99962		100.0376		668.96503		74.225		99.99237		669.10999		74.225		99.99971		699.5819		74.225		100.0376		701.17756		74.225		100.05398		703.51566		74.225		100.03066

		669.48798		74.25		100.00207		100.03758		669.22198		74.25		99.99482		669.36401		74.25		100.0003		699.83645		74.25		100.03758		701.41722		74.25		100.05394		703.76844		74.25		100.03062

		669.76099		74.275		100.00113		100.03756		669.492		74.275		99.99365		669.62299		74.275		99.99825		700.08811		74.275		100.03756		701.65478		74.275		100.05392		704.02277		74.275		100.03058

		670.01398		74.3		99.9984		100.03753		669.74298		74.3		99.99556		669.88202		74.3		100.00113		700.33778		74.3		100.03753		701.89334		74.3		100.0539		704.27066		74.3		100.03054

		670.27899		74.325		100.00149		100.03751		670.01202		74.325		99.99694		670.15601		74.325		99.999		700.584		74.325		100.03751		702.13912		74.325		100.05388		704.51466		74.325		100.03051

		670.54102		74.35		99.99992		100.03748		670.26898		74.35		99.99339		670.41498		74.35		100.00047		700.83312		74.35		100.03748		702.38634		74.35		100.05388		704.76033		74.35		100.03048

		670.80103		74.375		100.0002		100.03746		670.53003		74.375		99.99346		670.67297		74.375		100.00077		701.07645		74.375		100.03746		702.63612		74.375		100.05388		705.00344		74.375		100.03047

		671.06598		74.4		99.99996		100.03743		670.78802		74.4		99.9945		670.94202		74.4		100.00004		701.321		74.4		100.03743		702.88856		74.4		100.05389		705.2451		74.4		100.03045

		671.328		74.425		100.00085		100.0374		671.05298		74.425		99.9945		671.19299		74.425		100.00245		701.56178		74.425		100.0374		703.13822		74.425		100.05391		705.49099		74.425		100.03045

		671.58398		74.45		100.00384		100.03737		671.30902		74.45		99.99584		671.45898		74.45		100.00199		701.80045		74.45		100.03737		703.38767		74.45		100.05394		705.74089		74.45		100.03045

		671.85199		74.475		100.00185		100.03734		671.565		74.475		99.99371		671.70599		74.475		99.9986		702.04234		74.475		100.03734		703.63934		74.475		100.05397		705.98966		74.475		100.03045

		672.112		74.5		99.99937		100.03731		671.83002		74.5		99.99455		671.99103		74.5		99.99857		702.28701		74.5		100.03731		703.89056		74.5		100.054		706.23778		74.5		100.03046

		672.37402		74.525		100.00021		100.03727		672.08899		74.525		99.99436		672.245		74.525		100.00077		702.53323		74.525		100.03727		704.13867		74.525		100.05403		706.48745		74.525		100.03047

		672.64502		74.55		100.00034		100.03723		672.35101		74.55		99.99493		672.49902		74.55		99.99996		702.78423		74.55		100.03723		704.37878		74.55		100.05406		706.73945		74.55		100.03047

		672.89398		74.575		100.0011		100.03718		672.61401		74.575		99.99414		672.76202		74.575		100.00026		703.03567		74.575		100.03718		704.61911		74.575		100.05409		706.994		74.575		100.03048

		673.16498		74.6		100.0001		100.03713		672.87201		74.6		99.99284		673.02197		74.6		100.00145		703.285		74.6		100.03713		704.86067		74.6		100.05411		707.24834		74.6		100.03049

		673.41998		74.625		99.9984		100.03708		673.13501		74.625		99.99601		673.29102		74.625		99.9999		703.53333		74.625		100.03708		705.09922		74.625		100.05413		707.5029		74.625		100.03049

		673.67798		74.65		100.00001		100.03703		673.40601		74.65		99.99453		673.54797		74.65		99.99971		703.78166		74.65		100.03703		705.34367		74.65		100.05413		707.749		74.65		100.03049

		673.94397		74.675		100.00109		100.03697		673.66699		74.675		99.99471		673.81097		74.675		100.00066		704.03488		74.675		100.03697		705.59245		74.675		100.05413		707.99178		74.675		100.03048

		674.20001		74.7		99.99987		100.03692		673.92999		74.7		99.99437		674.07098		74.7		99.99882		704.28355		74.7		100.03692		705.84344		74.7		100.05412		708.23489		74.7		100.03047

		674.46802		74.725		99.99946		100.03686		674.18799		74.725		99.99513		674.328		74.725		100.00084		704.52911		74.725		100.03686		706.09323		74.725		100.0541		708.47756		74.725		100.03046

		674.72699		74.75		100.00228		100.03681		674.44702		74.75		99.9929		674.58398		74.75		100.00196		704.77256		74.75		100.03681		706.34434		74.75		100.05408		708.72534		74.75		100.03044

		674.995		74.775		99.99876		100.03676		674.70697		74.775		99.99309		674.85699		74.775		100.00011		705.01255		74.775		100.03676		706.59589		74.775		100.05406		708.97323		74.775		100.03043

		675.24902		74.8		100.00022		100.03672		674.97198		74.8		99.99433		675.11798		74.8		100.00064		705.25267		74.8		100.03672		706.84778		74.8		100.05404		709.21845		74.8		100.03041

		675.51801		74.825		99.99997		100.03668		675.23102		74.825		99.99311		675.37903		74.825		100.00103		705.50066		74.825		100.03668		707.09833		74.825		100.05402		709.46367		74.825		100.03039

		675.78003		74.85		100.00354		100.03665		675.48297		74.85		99.99603		675.63702		74.85		100.00177		705.75022		74.85		100.03665		707.34922		74.85		100.05401		709.7109		74.85		100.03038

		676.04102		74.875		100.00037		100.03663		675.74402		74.875		99.99099		675.90302		74.875		99.99983		706.00289		74.875		100.03663		707.59489		74.875		100.05401		709.96112		74.875		100.03037

		676.30298		74.9		99.99933		100.03661		676.00299		74.9		99.99383		676.16302		74.9		100.00026		706.254		74.9		100.03661		707.83633		74.9		100.05401		710.2109		74.9		100.03036

		676.56799		74.925		100.00072		100.0366		676.26703		74.925		99.99531		676.427		74.925		99.99933		706.50367		74.925		100.0366		708.07578		74.925		100.05403		710.46023		74.925		100.03036

		676.823		74.95		99.99853		100.0366		676.53101		74.95		99.99383		676.68298		74.95		100.0006		706.75589		74.95		100.0366		708.31822		74.95		100.05406		710.71467		74.95		100.03036

		677.09399		74.975		100.00176		100.0366		676.78699		74.975		99.99439		676.94897		74.975		100.0002		707.01077		74.975		100.0366		708.56256		74.975		100.0541		710.96101		74.975		100.03036

		677.34497		75		100.00214		100.03661		677.05603		75		99.99564		677.20697		75		100.00013		707.26644		75		100.03661		708.81278		75		100.05415		711.20479		75		100.03037

		677.60699		75.025		99.99999		100.03663		677.30902		75.025		99.99451		677.47101		75.025		99.99932		707.52199		75.025		100.03663		709.06245		75.025		100.05421		711.44634		75.025		100.03038

		677.87903		75.05		99.99984		100.03665		677.57703		75.05		99.99282		677.73401		75.05		100.00025		707.76955		75.05		100.03665		709.31445		75.05		100.05428		711.68745		75.05		100.03039

		678.13702		75.075		99.99886		100.03667		677.83801		75.075		99.99513		677.98999		75.075		100.00171		708.01599		75.075		100.03667		709.56445		75.075		100.05435		711.93233		75.075		100.0304

		678.401		75.1		99.99844		100.03669		678.099		75.1		99.99232		678.26202		75.1		100.0015		708.25888		75.1		100.03669		709.81545		75.1		100.05443		712.182		75.1		100.03042

		678.65198		75.125		99.99966		100.03671		678.35901		75.125		99.99665		678.51398		75.125		100.00064		708.50044		75.125		100.03671		710.06778		75.125		100.0545		712.42989		75.125		100.03044

		678.91901		75.15		100.00139		100.03674		678.62201		75.15		99.99592		678.77502		75.15		99.99997		708.75467		75.15		100.03674		710.32001		75.15		100.05458		712.67866		75.15		100.03045

		679.17401		75.175		99.99861		100.03676		678.88599		75.175		99.99502		679.04102		75.175		99.99918		709.00678		75.175		100.03676		710.57012		75.175		100.05465		712.92489		75.175		100.03047

		679.43597		75.2		100.00021		100.03678		679.14398		75.2		99.99418		679.30603		75.2		99.99869		709.25801		75.2		100.03678		710.82067		75.2		100.05472		713.17344		75.2		100.03049

		679.70099		75.225		100.00089		100.0368		679.409		75.225		99.99317		679.56403		75.225		100.00076		709.50945		75.225		100.0368		711.06445		75.225		100.05479		713.42177		75.225		100.0305

		679.96002		75.25		100.00083		100.03682		679.659		75.25		99.99498		679.82202		75.25		100.00223		709.7629		75.25		100.03682		711.30712		75.25		100.05484		713.67189		75.25		100.03052

		680.21997		75.275		99.99877		100.03684		679.92603		75.275		99.99394		680.08002		75.275		100.00133		710.01401		75.275		100.03684		711.54589		75.275		100.05489		713.92367		75.275		100.03053

		680.48499		75.3		100.00014		100.03686		680.18597		75.3		99.9966		680.34003		75.3		100.00211		710.2639		75.3		100.03686		711.78778		75.3		100.05494		714.17078		75.3		100.03054

		680.742		75.325		100.00168		100.03688		680.45099		75.325		99.9927		680.60797		75.325		100.00154		710.51712		75.325		100.03688		712.03634		75.325		100.05497		714.4129		75.325		100.03055

		681.00702		75.35		100.00093		100.03689		680.70502		75.35		99.99454		680.87598		75.35		99.99912		710.77412		75.35		100.03689		712.2859		75.35		100.055		714.65745		75.35		100.03056

		681.271		75.375		99.99914		100.03691		680.96899		75.375		99.99229		681.12799		75.375		100.00043		711.02112		75.375		100.03691		712.53745		75.375		100.05502		714.90201		75.375		100.03057

		681.534		75.4		100.00098		100.03693		681.229		75.4		99.99616		681.39099		75.4		100.00046		711.26589		75.4		100.03693		712.79156		75.4		100.05504		715.14623		75.4		100.03057

		681.789		75.425		99.99852		100.03695		681.49402		75.425		99.99543		681.65802		75.425		99.99805		711.512		75.425		100.03695		713.04489		75.425		100.05506		715.39545		75.425		100.03057

		682.05499		75.45		99.99961		100.03696		681.74799		75.45		99.99327		681.91498		75.45		100.00007		711.75433		75.45		100.03696		713.29656		75.45		100.05506		715.64512		75.45		100.03057

		682.31702		75.475		99.99978		100.03698		682.01801		75.475		99.99653		682.17401		75.475		100.00036		712.00012		75.475		100.03698		713.54822		75.475		100.05507		715.89812		75.475		100.03057

		682.58099		75.5		99.99865		100.037		682.27502		75.5		99.99379		682.43799		75.5		99.99935		712.25111		75.5		100.037		713.80288		75.5		100.05507		716.14901		75.5		100.03056

		682.84198		75.525		100.00022		100.03701		682.53601		75.525		99.99335		682.69598		75.525		99.99824		712.50189		75.525		100.03701		714.05533		75.525		100.05507		716.39878		75.525		100.03056

		683.10602		75.55		100.00069		100.03702		682.79999		75.55		99.99404		682.95898		75.55		100.00054		712.75578		75.55		100.03702		714.29867		75.55		100.05507		716.64922		75.55		100.03055

		683.36298		75.575		99.99946		100.03703		683.05603		75.575		99.99421		683.21997		75.575		100.00015		713.00655		75.575		100.03703		714.5411		75.575		100.05507		716.901		75.575		100.03054

		683.62201		75.6		100.00059		100.03704		683.31897		75.6		99.9954		683.48602		75.6		100		713.257		75.6		100.03704		714.78166		75.6		100.05506		717.15222		75.6		100.03053

		683.87598		75.625		100.00069		100.03705		683.58197		75.625		99.99718		683.73901		75.625		100.00061		713.50811		75.625		100.03705		715.02077		75.625		100.05506		717.40133		75.625		100.03051

		684.15198		75.65		99.99672		100.03705		683.84198		75.65		99.99416		684.01501		75.65		99.99991		713.76078		75.65		100.03705		715.26588		75.65		100.05505		717.64556		75.65		100.0305

		684.40997		75.675		100.00084		100.03704		684.10199		75.675		99.99553		684.27802		75.675		100.00001		714.01522		75.675		100.03704		715.516		75.675		100.05504		717.88789		75.675		100.03049

		684.66199		75.7		99.99919		100.03704		684.36102		75.7		99.9912		684.53802		75.7		99.99865		714.26377		75.7		100.03704		715.76711		75.7		100.05503		718.12678		75.7		100.03047

		684.92603		75.725		100.00076		100.03703		684.62299		75.725		99.99414		684.79199		75.725		99.99977		714.51067		75.725		100.03703		716.01955		75.725		100.05503		718.36555		75.725		100.03046

		685.18701		75.75		100.00046		100.03702		684.88098		75.75		99.99569		685.06		75.75		100.00056		714.75933		75.75		100.03702		716.27244		75.75		100.05502		718.61344		75.75		100.03045

		685.45001		75.775		99.9984		100.03701		685.14001		75.775		99.99567		685.31702		75.775		99.99783		715.00244		75.775		100.03701		716.52755		75.775		100.05501		718.86323		75.775		100.03044

		685.71301		75.8		99.99671		100.037		685.39697		75.8		99.99269		685.573		75.8		99.99761		715.25144		75.8		100.037		716.78556		75.8		100.055		719.10967		75.8		100.03044

		685.97803		75.825		99.99893		100.037		685.65997		75.825		99.99269		685.849		75.825		100.00161		715.50211		75.825		100.037		717.04323		75.825		100.055		719.35734		75.825		100.03043

		686.23999		75.85		100.00062		100.03701		685.91998		75.85		99.99706		686.10901		75.85		100.00044		715.75444		75.85		100.03701		717.30122		75.85		100.05499		719.60278		75.85		100.03043

		686.49902		75.875		99.99961		100.03702		686.18597		75.875		99.99328		686.35602		75.875		99.99942		716.00467		75.875		100.03702		717.55155		75.875		100.05499		719.84912		75.875		100.03044

		686.76202		75.9		99.9989		100.03703		686.44897		75.9		99.99395		686.62799		75.9		99.99984		716.25422		75.9		100.03703		717.79855		75.9		100.055		720.09924		75.9		100.03045

		687.02197		75.925		100.00004		100.03706		686.71301		75.925		99.99465		686.88		75.925		100.00054		716.506		75.925		100.03706		718.04489		75.925		100.05501		720.35012		75.925		100.03046

		687.27899		75.95		99.99988		100.0371		686.97699		75.95		99.99663		687.151		75.95		100.00093		716.76143		75.95		100.0371		718.28767		75.95		100.05502		720.60023		75.95		100.03048

		687.54401		75.975		100.00052		100.03715		687.24103		75.975		99.99396		687.41101		75.975		99.99855		717.01632		75.975		100.03715		718.53488		75.975		100.05504		720.84379		75.975		100.03051

		687.802		76		100.00051		100.0372		687.505		76		99.99639		687.66803		76		100.00094		717.27222		76		100.0372		718.78466		76		100.05507		721.08579		76		100.03054

		688.07098		76.025		100.00052		100.03727		687.76398		76.025		99.99603		687.92902		76.025		100.00153		717.51888		76.025		100.03727		719.03299		76.025		100.0551		721.32756		76.025		100.03058

		688.32501		76.05		99.99826		100.03734		688.01398		76.05		99.9932		688.198		76.05		99.99854		717.76554		76.05		100.03734		719.28054		76.05		100.05514		721.56834		76.05		100.03062

		688.586		76.075		99.99803		100.03742		688.27802		76.075		99.99354		688.44897		76.075		99.99879		718.0111		76.075		100.03742		719.52788		76.075		100.05518		721.81634		76.075		100.03067

		688.85498		76.1		99.99954		100.0375		688.539		76.1		99.99595		688.72498		76.1		100.00099		718.25566		76.1		100.0375		719.77732		76.1		100.05522		722.06812		76.1		100.03072

		689.11298		76.125		99.99899		100.03758		688.79401		76.125		99.99395		688.97803		76.125		99.99961		718.50366		76.125		100.03758		720.02588		76.125		100.05527		722.31967		76.125		100.03077

		689.37299		76.15		99.99993		100.03765		689.05798		76.15		99.99617		689.24103		76.15		100.00071		718.75554		76.15		100.03765		720.27388		76.15		100.05531		722.57233		76.15		100.03081

		689.63501		76.175		99.99612		100.03771		689.32202		76.175		99.99238		689.51599		76.175		99.99896		719.00444		76.175		100.03771		720.52266		76.175		100.05536		722.82567		76.175		100.03086

		689.89203		76.2		100.00062		100.03776		689.578		76.2		99.99396		689.76703		76.2		100.00029		719.25233		76.2		100.03776		720.7701		76.2		100.0554		723.07433		76.2		100.03089

		690.15698		76.225		100.00054		100.0378		689.841		76.225		99.99498		690.02899		76.225		100.00073		719.50043		76.225		100.0378		721.01288		76.225		100.05543		723.32244		76.225		100.03092

		690.41602		76.25		99.99831		100.03783		690.10797		76.25		99.99466		690.29199		76.25		99.99928		719.75222		76.25		100.03783		721.25299		76.25		100.05546		723.57277		76.25		100.03095

		690.69299		76.275		100.00025		100.03783		690.36298		76.275		99.99483		690.552		76.275		99.99875		720.00056		76.275		100.03783		721.49133		76.275		100.05548		723.825		76.275		100.03096

		690.93799		76.3		99.99796		100.03782		690.625		76.3		99.99156		690.81201		76.3		99.99811		720.25		76.3		100.03782		721.73355		76.3		100.05548		724.07367		76.3		100.03097

		691.20898		76.325		99.99852		100.03778		690.87903		76.325		99.99404		691.06897		76.325		100.0003		720.49834		76.325		100.03778		721.98166		76.325		100.05548		724.31589		76.325		100.03096

		691.46698		76.35		100.00114		100.03773		691.14899		76.35		99.99605		691.33801		76.35		100.00002		720.74779		76.35		100.03773		722.23222		76.35		100.05547		724.554		76.35		100.03095

		691.73199		76.375		99.99759		100.03766		691.41101		76.375		99.99465		691.59698		76.375		99.99864		720.99268		76.375		100.03766		722.48433		76.375		100.05545		724.79178		76.375		100.03092

		691.987		76.4		99.99733		100.03758		691.677		76.4		99.99103		691.85901		76.4		99.99829		721.23357		76.4		100.03758		722.73699		76.4		100.05542		725.033		76.4		100.03089

		692.24902		76.425		100.0011		100.03749		691.935		76.425		99.99605		692.117		76.425		99.99908		721.47412		76.425		100.03749		722.98622		76.425		100.05539		725.28333		76.425		100.03086

		692.51202		76.45		100.00055		100.0374		692.19702		76.45		99.99847		692.38397		76.45		99.99856		721.71601		76.45		100.0374		723.23778		76.45		100.05535		725.53589		76.45		100.03082

		692.776		76.475		99.99957		100.0373		692.44897		76.475		99.99571		692.63702		76.475		99.99987		721.96534		76.475		100.0373		723.49133		76.475		100.05531		725.78756		76.475		100.03078

		693.02899		76.5		99.99971		100.0372		692.716		76.5		99.99357		692.90302		76.5		100.00012		722.21611		76.5		100.0372		723.74911		76.5		100.05527		726.03577		76.5		100.03074

		693.28802		76.525		100.00051		100.03711		692.98199		76.525		99.99422		693.16498		76.525		100.00171		722.46522		76.525		100.03711		724.00433		76.525		100.05524		726.28555		76.525		100.0307

		693.55499		76.55		99.99971		100.03704		693.24103		76.55		99.99371		693.41998		76.55		100.00122		722.71722		76.55		100.03704		724.25078		76.55		100.05521		726.53888		76.55		100.03067

		693.82001		76.575		99.9994		100.03697		693.49799		76.575		99.99522		693.67902		76.575		100.00019		722.96678		76.575		100.03697		724.49533		76.575		100.05518		726.79544		76.575		100.03064

		694.078		76.6		100.0002		100.03692		693.76099		76.6		99.99432		693.94397		76.6		100.00114		723.21466		76.6		100.03692		724.74178		76.6		100.05517		727.05021		76.6		100.03062

		694.33002		76.625		99.99982		100.03689		694.021		76.625		99.99465		694.20398		76.625		100.00107		723.46544		76.625		100.03689		724.98556		76.625		100.05516		727.30122		76.625		100.03061

		694.60498		76.65		99.99786		100.03688		694.27301		76.65		99.99262		694.479		76.65		100.00084		723.71933		76.65		100.03688		725.23834		76.65		100.05517		727.54566		76.65		100.0306

		694.86499		76.675		99.99965		100.03689		694.534		76.675		99.99531		694.72699		76.675		100.00139		723.97155		76.675		100.03689		725.49333		76.675		100.05519		727.79155		76.675		100.03061

		695.133		76.7		100.00148		100.03692		694.79999		76.7		99.99693		694.98999		76.7		100.00319		724.21533		76.7		100.03692		725.75022		76.7		100.05521		728.03566		76.7		100.03062

		695.38898		76.725		99.9972		100.03696		695.06		76.725		99.99437		695.26202		76.725		100.00054		724.45889		76.725		100.03696		726.00411		76.725		100.05525		728.27767		76.725		100.03063

		695.65399		76.75		100.00025		100.03701		695.32397		76.75		99.99734		695.52002		76.75		100.00116		724.70378		76.75		100.03701		726.25622		76.75		100.0553		728.52433		76.75		100.03066

		695.92499		76.775		99.99849		100.03707		695.58801		76.775		99.99399		695.78101		76.775		99.99903		724.94588		76.775		100.03707		726.51122		76.775		100.05535		728.771		76.775		100.03068

		696.177		76.8		99.99969		100.03714		695.85901		76.8		99.99345		696.04498		76.8		100.00063		725.19533		76.8		100.03714		726.76733		76.8		100.05541		729.01756		76.8		100.0307

		696.43298		76.825		100.0016		100.0372		696.11499		76.825		99.9953		696.30603		76.825		100.00179		725.44689		76.825		100.0372		727.01999		76.825		100.05547		729.26656		76.825		100.03073

		696.70203		76.85		100.00115		100.03726		696.36603		76.85		99.99306		696.56598		76.85		99.99985		725.70211		76.85		100.03726		727.27532		76.85		100.05553		729.5159		76.85		100.03075

		696.95502		76.875		99.99716		100.03731		696.62903		76.875		99.99411		696.828		76.875		99.99835		725.95555		76.875		100.03731		727.52099		76.875		100.05558		729.7659		76.875		100.03078

		697.21399		76.9		100.00153		100.03735		696.89001		76.9		99.99384		697.08398		76.9		100.00044		726.20922		76.9		100.03735		727.76676		76.9		100.05564		730.01245		76.9		100.0308

		697.47998		76.925		100.00013		100.03738		697.15399		76.925		99.99614		697.35101		76.925		100.00149		726.46133		76.925		100.03738		728.00865		76.925		100.0557		730.26078		76.925		100.03081

		697.73999		76.95		99.99992		100.03739		697.41101		76.95		99.99302		697.60797		76.95		100.00174		726.71433		76.95		100.03739		728.24988		76.95		100.05574		730.51423		76.95		100.03082

		697.99799		76.975		99.99912		100.0374		697.67499		76.975		99.99317		697.86298		76.975		100.00126		726.96622		76.975		100.0374		728.50022		76.975		100.05579		730.76045		76.975		100.03083

		698.26398		77		99.99834		100.03739		697.94098		77		99.99472		698.13098		77		99.99916		727.21889		77		100.03739		728.751		77		100.05582		731.00401		77		100.03084

		698.52399		77.025		99.99889		100.03737		698.20001		77.025		99.99607		698.396		77.025		100.00154		727.464		77.025		100.03737		729.00056		77.025		100.05586		731.24467		77.025		100.03084

		698.776		77.05		99.99699		100.03735		698.45697		77.05		99.99396		698.65601		77.05		100.00034		727.70744		77.05		100.03735		729.25111		77.05		100.05588		731.48289		77.05		100.03085

		699.04199		77.075		99.99887		100.03732		698.716		77.075		99.99483		698.91901		77.075		99.99978		727.94889		77.075		100.03732		729.502		77.075		100.0559		731.72978		77.075		100.03085

		699.30701		77.1		99.99879		100.03729		698.97699		77.1		99.9957		699.185		77.1		99.99923		728.18877		77.1		100.03729		729.75534		77.1		100.05592		731.97833		77.1		100.03085

		699.57397		77.125		99.99725		100.03727		699.24298		77.125		99.9932		699.435		77.125		100.00053		728.43355		77.125		100.03727		730.00612		77.125		100.05593		732.22789		77.125		100.03086

		699.83398		77.15		99.99914		100.03725		699.49298		77.15		99.99434		699.69702		77.15		99.99907		728.68444		77.15		100.03725		730.25845		77.15		100.05594		732.47656		77.15		100.03087

		700.08698		77.175		100.00026		100.03724		699.76398		77.175		99.99536		699.96899		77.175		100.00026		728.93522		77.175		100.03724		730.51334		77.175		100.05594		732.72755		77.175		100.03088

		700.35101		77.2		100.0005		100.03725		700.01703		77.2		99.99536		700.216		77.2		99.99713		729.186		77.2		100.03725		730.76101		77.2		100.05594		732.97844		77.2		100.03089

		700.612		77.225		99.99945		100.03726		700.27698		77.225		99.99598		700.48901		77.225		100.00231		729.43922		77.225		100.03726		731.00478		77.225		100.05594		733.22977		77.225		100.0309

		700.88		77.25		99.99914		100.03728		700.54401		77.25		99.9921		700.73901		77.25		99.99849		729.69312		77.25		100.03728		731.24556		77.25		100.05594		733.484		77.25		100.03092

		701.14398		77.275		100.00083		100.03731		700.80902		77.275		99.99469		701.00403		77.275		100.00038		729.94856		77.275		100.03731		731.48545		77.275		100.05593		733.73977		77.275		100.03093

		701.40198		77.3		100.00056		100.03736		701.07202		77.3		99.99582		701.26202		77.3		100.00083		730.20201		77.3		100.03736		731.73467		77.3		100.05592		733.98866		77.3		100.03095

		701.65997		77.325		99.99573		100.03741		701.33002		77.325		99.99297		701.52197		77.325		100.00072		730.45645		77.325		100.03741		731.98556		77.325		100.05591		734.23288		77.325		100.03096

		701.92297		77.35		99.99931		100.03746		701.591		77.35		99.99565		701.78003		77.35		99.99969		730.70512		77.35		100.03746		732.23579		77.35		100.0559		734.47432		77.35		100.03098

		702.17499		77.375		99.99945		100.03752		701.854		77.375		99.99434		702.04602		77.375		100.00029		730.95079		77.375		100.03752		732.48745		77.375		100.05589		734.71566		77.375		100.03099

		702.43903		77.4		100.00136		100.03758		702.11102		77.4		99.99853		702.30499		77.4		99.99917		731.19423		77.4		100.03758		732.7409		77.4		100.05588		734.95899		77.4		100.031

		702.70203		77.425		100.00051		100.03764		702.37598		77.425		99.9971		702.58301		77.425		100.00051		731.43568		77.425		100.03764		732.99367		77.425		100.05587		735.20844		77.425		100.031

		702.96503		77.45		99.99891		100.03769		702.64001		77.45		99.9947		702.83099		77.45		100.00102		731.67801		77.45		100.03769		733.24856		77.45		100.05586		735.45899		77.45		100.03101

		703.22699		77.475		99.99803		100.03775		702.89697		77.475		99.99303		703.08899		77.475		99.99704		731.92712		77.475		100.03775		733.50745		77.475		100.05586		735.71144		77.475		100.03101

		703.48602		77.5		99.99611		100.0378		703.14801		77.5		99.99289		703.354		77.5		100.00056		732.17601		77.5		100.0378		733.76712		77.5		100.05585		735.96266		77.5		100.03101

		703.745		77.525		99.9998		100.03784		703.41498		77.525		99.9939		703.61102		77.525		99.99916		732.42423		77.525		100.03784		734.01656		77.525		100.05585		736.21355		77.525		100.031

		704.00702		77.55		100.0003		100.03788		703.67297		77.55		99.99814		703.86298		77.55		100.00265		732.67467		77.55		100.03788		734.26301		77.55		100.05585		736.46722		77.55		100.03099

		704.27197		77.575		100.00186		100.03792		703.935		77.575		99.99702		704.133		77.575		100.00025		732.92678		77.575		100.03792		734.50812		77.575		100.05586		736.72433		77.575		100.03099

		704.53101		77.6		100.00089		100.03795		704.19501		77.6		99.99723		704.388		77.6		100.00067		733.17634		77.6		100.03795		734.75012		77.6		100.05588		736.98189		77.6		100.03098

		704.79602		77.625		99.99735		100.03798		704.453		77.625		99.99504		704.65503		77.625		99.9999		733.42833		77.625		100.03798		734.99645		77.625		100.0559		737.23111		77.625		100.03098

		705.05798		77.65		99.99887		100.03801		704.71301		77.65		99.99454		704.91101		77.65		100.0001		733.68266		77.65		100.03801		735.247		77.65		100.05593		737.47456		77.65		100.03098

		705.31299		77.675		99.99674		100.03803		704.97198		77.675		99.9953		705.16699		77.675		99.99826		733.93444		77.675		100.03803		735.49767		77.675		100.05597		737.71545		77.675		100.03098

		705.586		77.7		99.99786		100.03805		705.23901		77.7		99.99496		705.44		77.7		99.9989		734.1771		77.7		100.03805		735.74889		77.7		100.05601		737.95266		77.7		100.03098

		705.83698		77.725		99.99739		100.03806		705.50598		77.725		99.9941		705.69501		77.725		100.00162		734.41855		77.725		100.03806		736.00211		77.725		100.05606		738.18945		77.725		100.03099

		706.09998		77.75		99.9962		100.03808		705.76599		77.75		99.99352		705.96002		77.75		99.99794		734.66189		77.75		100.03808		736.25255		77.75		100.05612		738.43467		77.75		100.031

		706.362		77.775		99.99955		100.03809		706.026		77.775		99.99352		706.21399		77.775		99.99993		734.90511		77.775		100.03809		736.50421		77.775		100.05618		738.67878		77.775		100.03102

		706.61902		77.8		99.99903		100.0381		706.28198		77.8		99.99354		706.47998		77.8		99.9998		735.15311		77.8		100.0381		736.75932		77.8		100.05623		738.92278		77.8		100.03104

		706.883		77.825		99.99836		100.0381		706.55298		77.825		99.99541		706.74402		77.825		99.99858		735.40211		77.825		100.0381		737.01588		77.825		100.0563		739.16833		77.825		100.03106

		707.14001		77.85		99.99776		100.0381		706.81598		77.85		99.99466		707.008		77.85		99.99888		735.651		77.85		100.0381		737.26532		77.85		100.05635		739.41567		77.85		100.03109

		707.39697		77.875		99.99915		100.0381		707.07501		77.875		99.99231		707.26398		77.875		99.99966		735.90089		77.875		100.0381		737.50888		77.875		100.05641		739.66589		77.875		100.03111

		707.65997		77.9		100.00024		100.0381		707.33301		77.9		99.99636		707.52301		77.9		100.00229		736.14834		77.9		100.0381		737.75177		77.9		100.05646		739.91778		77.9		100.03113

		707.92297		77.925		99.99821		100.0381		707.58698		77.925		99.99275		707.78497		77.925		100.00038		736.39634		77.925		100.0381		737.99266		77.925		100.0565		740.17		77.925		100.03115

		708.17999		77.95		100.00098		100.03809		707.854		77.95		99.99509		708.05798		77.95		100.00028		736.648		77.95		100.03809		738.23677		77.95		100.05654		740.42056		77.95		100.03117

		708.44299		77.975		100.0003		100.03807		708.117		77.975		99.99471		708.30902		77.975		99.99956		736.898		77.975		100.03807		738.4881		77.975		100.05656		740.66433		77.975		100.03118

		708.70398		78		99.99727		100.03806		708.37799		78		99.99178		708.57202		78		99.99862		737.14666		78		100.03806		738.74155		78		100.05657		740.90811		78		100.03119

		708.97302		78.025		99.99908		100.03803		708.62903		78.025		99.99645		708.83099		78.025		99.99922		737.39022		78.025		100.03803		738.99299		78.025		100.05657		741.14844		78.025		100.03119

		709.22699		78.05		99.99847		100.03801		708.88501		78.05		99.99433		709.09399		78.05		99.99771		737.63755		78.05		100.03801		739.24411		78.05		100.05656		741.38578		78.05		100.03119

		709.487		78.075		99.99911		100.03799		709.159		78.075		99.99447		709.35498		78.075		99.99988		737.88188		78.075		100.03799		739.49622		78.075		100.05654		741.62944		78.075		100.03118

		709.75		78.1		99.99952		100.03796		709.414		78.1		99.99742		709.61499		78.1		99.99951		738.12366		78.1		100.03796		739.75033		78.1		100.05651		741.87644		78.1		100.03117

		710.013		78.125		99.99966		100.03793		709.67798		78.125		99.99676		709.88		78.125		100.00095		738.37277		78.125		100.03793		740.00421		78.125		100.05647		742.12455		78.125		100.03115

		710.27399		78.15		99.99907		100.0379		709.94		78.15		99.99529		710.146		78.15		99.99891		738.62299		78.15		100.0379		740.25854		78.15		100.05643		742.37366		78.15		100.03113

		710.53198		78.175		99.9995		100.03786		710.18799		78.175		99.99482		710.396		78.175		99.99885		738.87055		78.175		100.03786		740.50665		78.175		100.05638		742.62577		78.175		100.03111

		710.79602		78.2		99.99817		100.03783		710.45099		78.2		99.99133		710.66498		78.2		99.99788		739.11977		78.2		100.03783		740.75077		78.2		100.05632		742.87689		78.2		100.03108

		711.05298		78.225		99.99921		100.0378		710.71698		78.225		99.99302		710.927		78.225		99.9984		739.3681		78.225		100.0378		740.99121		78.225		100.05627		743.12844		78.225		100.03106

		711.31201		78.25		100.00075		100.03778		710.97601		78.25		99.99462		711.177		78.25		100.0005		739.61732		78.25		100.03778		741.22777		78.25		100.05621		743.38155		78.25		100.03105

		711.565		78.275		99.99858		100.03776		711.23401		78.275		99.9962		711.44098		78.275		100.00014		739.86677		78.275		100.03776		741.46355		78.275		100.05616		743.639		78.275		100.03103

		711.83398		78.3		99.99965		100.03774		711.50403		78.3		99.99374		711.70502		78.3		100.0011		740.1181		78.3		100.03774		741.70722		78.3		100.05611		743.88911		78.3		100.03103

		712.09601		78.325		100.0001		100.03773		711.76202		78.325		99.99623		711.96503		78.325		99.99861		740.36988		78.325		100.03773		741.95222		78.325		100.05607		744.13189		78.325		100.03102

		712.35303		78.35		99.99895		100.03772		712.026		78.35		99.99383		712.23102		78.35		99.99773		740.61877		78.35		100.03772		742.19911		78.35		100.05604		744.37255		78.35		100.03103

		712.61401		78.375		99.99796		100.03772		712.27899		78.375		99.9935		712.49402		78.375		99.99916		740.86811		78.375		100.03772		742.44733		78.375		100.05601		744.61544		78.375		100.03104

		712.88098		78.4		99.99895		100.03772		712.54999		78.4		99.99678		712.76001		78.4		100.00263		741.11589		78.4		100.03772		742.69845		78.4		100.05599		744.86488		78.4		100.03105

		713.14502		78.425		99.99823		100.03773		712.80499		78.425		99.99313		713.01898		78.425		99.99927		741.36033		78.425		100.03773		742.94911		78.425		100.05597		745.11766		78.425		100.03107

		713.40503		78.45		99.99873		100.03774		713.07098		78.45		99.99565		713.28198		78.45		99.99972		741.61111		78.45		100.03774		743.20311		78.45		100.05597		745.371		78.45		100.03109

		713.66498		78.475		99.99768		100.03776		713.32599		78.475		99.99467		713.53302		78.475		99.99937		741.865		78.475		100.03776		743.45989		78.475		100.05597		745.627		78.475		100.03111

		713.92902		78.5		99.99813		100.03778		713.586		78.5		99.99529		713.79797		78.5		100.00014		742.11823		78.5		100.03778		743.71966		78.5		100.05598		745.88245		78.5		100.03113

		714.19		78.525		100.00056		100.0378		713.83899		78.525		99.99521		714.06403		78.525		100.00014		742.37089		78.525		100.0378		743.97032		78.525		100.05599		746.13856		78.525		100.03115

		714.45203		78.55		99.99848		100.03782		714.10699		78.55		99.99318		714.32001		78.55		99.99858		742.62223		78.55		100.03782		744.21721		78.55		100.05602		746.39644		78.55		100.03117

		714.71503		78.575		99.99572		100.03783		714.36798		78.575		99.99478		714.57898		78.575		99.99817		742.87333		78.575		100.03783		744.46244		78.575		100.05604		746.65822		78.575		100.03118

		714.96399		78.6		99.99823		100.03785		714.62903		78.6		99.99502		714.83698		78.6		99.99921		743.12311		78.6		100.03785		744.70877		78.6		100.05607		746.91745		78.6		100.0312

		715.22998		78.625		100.001		100.03787		714.888		78.625		99.99701		715.09497		78.625		99.99988		743.37377		78.625		100.03787		744.96033		78.625		100.05611		747.171		78.625		100.03121

		715.50201		78.65		99.99893		100.03787		715.151		78.65		99.99609		715.36401		78.65		99.99786		743.62522		78.65		100.03787		745.21389		78.65		100.05615		747.417		78.65		100.03121

		715.75598		78.675		100.00031		100.03788		715.414		78.675		99.99736		715.61902		78.675		99.99756		743.86989		78.675		100.03788		745.46944		78.675		100.05618		747.66333		78.675		100.03121

		716.01398		78.7		100.00252		100.03788		715.66498		78.7		99.9963		715.88501		78.7		100.00223		744.11066		78.7		100.03788		745.72544		78.7		100.05622		747.90622		78.7		100.03121

		716.27502		78.725		99.99844		100.03788		715.94		78.725		99.99614		716.146		78.725		100.00024		744.34878		78.725		100.03788		745.97956		78.725		100.05626		748.14311		78.725		100.03121

		716.53802		78.75		100.00052		100.03787		716.19397		78.75		99.99573		716.41302		78.75		100.00188		744.58999		78.75		100.03787		746.23212		78.75		100.0563		748.39033		78.75		100.03121

		716.79303		78.775		100.00102		100.03785		716.45502		78.775		99.99553		716.66699		78.775		99.99958		744.83844		78.775		100.03785		746.48634		78.775		100.05633		748.64044		78.775		100.0312

		717.052		78.8		100.00152		100.03784		716.71399		78.8		99.99608		716.92603		78.8		100.00239		745.09133		78.8		100.03784		746.7419		78.8		100.05636		748.88755		78.8		100.0312

		717.31799		78.825		99.99877		100.03782		716.98297		78.825		99.99549		717.185		78.825		100.00034		745.34633		78.825		100.03782		746.99601		78.825		100.05639		749.133		78.825		100.0312

		717.58099		78.85		99.99992		100.0378		717.23499		78.85		99.99461		717.45203		78.85		100.00206		745.60133		78.85		100.0378		747.24389		78.85		100.05642		749.37623		78.85		100.03119

		717.841		78.875		100.00012		100.03778		717.50598		78.875		99.99576		717.716		78.875		100.0011		745.85855		78.875		100.03778		747.49		78.875		100.05645		749.62322		78.875		100.03119

		718.10498		78.9		99.99927		100.03776		717.76001		78.9		99.99787		717.97601		78.9		99.99961		746.11599		78.9		100.03776		747.73278		78.9		100.05647		749.868		78.9		100.03118

		718.36102		78.925		99.99684		100.03775		718.02502		78.925		99.995		718.237		78.925		99.99954		746.37355		78.925		100.03775		747.975		78.925		100.05649		750.11445		78.925		100.03118

		718.62701		78.95		99.9999		100.03773		718.28101		78.95		99.99428		718.50098		78.95		100.00187		746.63333		78.95		100.03773		748.22067		78.95		100.05651		750.366		78.95		100.03118

		718.883		78.975		99.999		100.03772		718.52698		78.975		99.99627		718.76398		78.975		99.99876		746.88966		78.975		100.03772		748.47389		78.975		100.05653		750.60733		78.975		100.03118

		719.14502		79		99.99916		100.03772		718.797		79		99.99666		719.02197		79		99.9983		747.14044		79		100.03772		748.72722		79		100.05655		750.84456		79		100.03118

		719.40997		79.025		99.9987		100.03772		719.06598		79.025		99.99453		719.28497		79.025		100.00104		747.38277		79.025		100.03772		748.97856		79.025		100.05657		751.08145		79.025		100.03118

		719.66498		79.05		99.99883		100.03772		719.32098		79.05		99.9928		719.53802		79.05		99.99871		747.62577		79.05		100.03772		749.229		79.05		100.05659		751.31845		79.05		100.03118

		719.92499		79.075		99.99826		100.03773		719.57898		79.075		99.9942		719.80603		79.075		99.99796		747.86777		79.075		100.03773		749.48078		79.075		100.05661		751.56878		79.075		100.03118

		720.18597		79.1		99.99701		100.03774		719.83099		79.1		99.99498		720.06		79.1		99.99889		748.10799		79.1		100.03774		749.73267		79.1		100.05662		751.8189		79.1		100.03118

		720.45203		79.125		99.99941		100.03776		720.09802		79.125		99.99701		720.32703		79.125		100.00035		748.3571		79.125		100.03776		749.98423		79.125		100.05664		752.06912		79.125		100.03119

		720.71198		79.15		99.99948		100.03778		720.35699		79.15		99.99361		720.58099		79.15		100.00038		748.60921		79.15		100.03778		750.23501		79.15		100.05666		752.32012		79.15		100.03119

		720.97498		79.175		99.99928		100.03781		720.62201		79.175		99.99538		720.83301		79.175		99.99892		748.85944		79.175		100.03781		750.47989		79.175		100.05667		752.5699		79.175		100.0312

		721.22601		79.2		99.999		100.03783		720.883		79.2		99.99542		721.09698		79.2		99.999		749.11066		79.2		100.03783		750.72123		79.2		100.05669		752.82012		79.2		100.03121

		721.48798		79.225		99.99898		100.03787		721.14398		79.225		99.99418		721.35901		79.225		100.00171		749.36355		79.225		100.03787		750.96223		79.225		100.0567		753.07145		79.225		100.03122

		721.75201		79.25		99.99786		100.0379		721.40997		79.25		99.99275		721.625		79.25		99.99943		749.62		79.25		100.0379		751.20378		79.25		100.05672		753.32189		79.25		100.03124

		722.00897		79.275		99.99908		100.03795		721.67499		79.275		99.99247		721.88202		79.275		99.99971		749.874		79.275		100.03795		751.45378		79.275		100.05674		753.57489		79.275		100.03125

		722.27002		79.3		99.99768		100.03799		721.92102		79.3		99.99593		722.14099		79.3		99.99813		750.12878		79.3		100.03799		751.70334		79.3		100.05676		753.81556		79.3		100.03128

		722.52899		79.325		99.99972		100.03805		722.18903		79.325		99.9939		722.409		79.325		99.99977		750.38467		79.325		100.03805		751.95156		79.325		100.05678		754.054		79.325		100.03131

		722.79498		79.35		99.9989		100.0381		722.44702		79.35		99.99494		722.66498		79.35		100.0025		750.63267		79.35		100.0381		752.19956		79.35		100.05681		754.29211		79.35		100.03135

		723.05103		79.375		99.99822		100.03817		722.71503		79.375		99.9956		722.92401		79.375		99.99864		750.87745		79.375		100.03817		752.45245		79.375		100.05685		754.52711		79.375		100.03139

		723.31702		79.4		99.99793		100.03824		722.97699		79.4		99.99262		723.18298		79.4		99.99701		751.11778		79.4		100.03824		752.70744		79.4		100.05689		754.77056		79.4		100.03143

		723.565		79.425		99.99898		100.03831		723.23102		79.425		99.99249		723.44397		79.425		100.00026		751.359		79.425		100.03831		752.95811		79.425		100.05693		755.01556		79.425		100.03148

		723.82703		79.45		100.00042		100.03839		723.49298		79.45		99.99781		723.71899		79.45		100.00102		751.60978		79.45		100.03839		753.20789		79.45		100.05698		755.26023		79.45		100.03153

		724.09302		79.475		99.99912		100.03847		723.74298		79.475		99.9969		723.98499		79.475		99.99849		751.86033		79.475		100.03847		753.45888		79.475		100.05703		755.5069		79.475		100.03159

		724.349		79.5		99.99902		100.03855		724.005		79.5		99.9948		724.23401		79.5		99.99936		752.11089		79.5		100.03855		753.70044		79.5		100.05709		755.7529		79.5		100.03165

		724.61603		79.525		99.99734		100.03863		724.26898		79.525		99.9954		724.49103		79.525		99.99926		752.35978		79.525		100.03863		753.94022		79.525		100.05714		755.99845		79.525		100.0317

		724.87799		79.55		100.00031		100.03871		724.52301		79.55		99.99416		724.75299		79.55		99.99981		752.60933		79.55		100.03871		754.18122		79.55		100.0572		756.24478		79.55		100.03176

		725.14801		79.575		99.99991		100.03879		724.78302		79.575		99.99575		725.01599		79.575		99.9999		752.85911		79.575		100.03879		754.42177		79.575		100.05725		756.4939		79.575		100.03181

		725.39899		79.6		99.9978		100.03886		725.04602		79.6		99.99519		725.276		79.6		100.00009		753.10811		79.6		100.03886		754.66255		79.6		100.0573		756.74512		79.6		100.03186

		725.64801		79.625		99.99834		100.03892		725.315		79.625		99.99608		725.53601		79.625		99.9995		753.36467		79.625		100.03892		754.90833		79.625		100.05735		756.988		79.625		100.03191

		725.92499		79.65		99.99895		100.03898		725.56702		79.65		99.995		725.79498		79.65		100.00092		753.62201		79.65		100.03898		755.158		79.65		100.05739		757.23		79.65		100.03195

		726.17401		79.675		99.99865		100.03903		725.82703		79.675		99.9956		726.05499		79.675		100.0009		753.86501		79.675		100.03903		755.40944		79.675		100.05743		757.47033		79.675		100.03198

		726.43597		79.7		99.99912		100.03907		726.08899		79.7		99.99481		726.31799		79.7		100.00097		754.10512		79.7		100.03907		755.65666		79.7		100.05746		757.70955		79.7		100.032

		726.703		79.725		99.99707		100.0391		726.35199		79.725		99.99395		726.58398		79.725		99.99831		754.34357		79.725		100.0391		755.90567		79.725		100.05749		757.95311		79.725		100.03202

		726.95398		79.75		99.99832		100.03912		726.617		79.75		99.9945		726.841		79.75		100.00005		754.58501		79.75		100.03912		756.15389		79.75		100.05752		758.19989		79.75		100.03204

		727.22699		79.775		99.99703		100.03914		726.88		79.775		99.99363		727.10101		79.775		99.99896		754.83334		79.775		100.03914		756.40333		79.775		100.05755		758.44945		79.775		100.03204

		727.48499		79.8		99.99987		100.03915		727.125		79.8		99.99497		727.35797		79.8		99.99946		755.08134		79.8		100.03915		756.65311		79.8		100.05757		758.69889		79.8		100.03205

		727.75299		79.825		99.99898		100.03915		727.38599		79.825		99.99346		727.62701		79.825		99.99941		755.32878		79.825		100.03915		756.90067		79.825		100.0576		758.94878		79.825		100.03205

		728.00403		79.85		99.99934		100.03915		727.66101		79.85		99.99323		727.89099		79.85		99.99981		755.57423		79.85		100.03915		757.14322		79.85		100.05762		759.19545		79.85		100.03205

		728.26001		79.875		100.00021		100.03914		727.914		79.875		99.99238		728.14001		79.875		99.99945		755.81911		79.875		100.03914		757.38456		79.875		100.05765		759.44245		79.875		100.03204

		728.526		79.9		99.99726		100.03912		728.17798		79.9		99.99371		728.40302		79.9		99.99639		756.06722		79.9		100.03912		757.62333		79.9		100.05768		759.6899		79.9		100.03203

		728.78802		79.925		99.99746		100.0391		728.44202		79.925		99.99436		728.66699		79.925		100.00054		756.31811		79.925		100.0391		757.86245		79.925		100.05771		759.93812		79.925		100.03203

		729.04498		79.95		100		100.03908		728.69897		79.95		99.9951		728.92603		79.95		99.99875		756.56922		79.95		100.03908		758.10911		79.95		100.05774		760.18245		79.95		100.03202

		729.31299		79.975		99.99835		100.03904		728.953		79.975		99.99382		729.18402		79.975		99.99739		756.81778		79.975		100.03904		758.35811		79.975		100.05777		760.424		79.975		100.03201

		729.57098		80		99.99931		100.03901		729.211		80		99.99505		729.45099		80		100.00084		757.05745		80		100.03901		758.60544		80		100.0578		760.66233		80		100.03199

		729.823		80.025		99.99991		100.03897		729.46899		80.025		99.9972		729.70801		80.025		99.99954		757.29867		80.025		100.03897		758.85366		80.025		100.05783		760.89789		80.025		100.03198

		730.086		80.05		100.00001		100.03893		729.73999		80.05		99.99558		729.97302		80.05		99.99964		757.54122		80.05		100.03893		759.10022		80.05		100.05786		761.13122		80.05		100.03197

		730.34302		80.075		99.99645		100.03889		729.99597		80.075		99.99269		730.229		80.075		99.99688		757.78111		80.075		100.03889		759.34956		80.075		100.05788		761.37611		80.075		100.03196

		730.61401		80.1		99.99793		100.03885		730.258		80.1		99.99148		730.49298		80.1		99.99768		758.02799		80.1		100.03885		759.599		80.1		100.0579		761.62255		80.1		100.03195

		730.87701		80.125		99.99731		100.0388		730.52899		80.125		99.99309		730.75702		80.125		100.00024		758.27677		80.125		100.0388		759.84911		80.125		100.05792		761.87044		80.125		100.03194

		731.12903		80.15		99.99925		100.03876		730.776		80.15		99.99376		731.01099		80.15		100.00074		758.52522		80.15		100.03876		760.09956		80.15		100.05793		762.11677		80.15		100.03192

		731.39001		80.175		100.00003		100.03871		731.039		80.175		99.99248		731.26801		80.175		99.99882		758.77655		80.175		100.03871		760.343		80.175		100.05793		762.36578		80.175		100.03191

		731.65503		80.2		99.99707		100.03867		731.30298		80.2		99.99412		731.53101		80.2		99.99832		759.02955		80.2		100.03867		760.58523		80.2		100.05793		762.61355		80.2		100.03189

		731.91101		80.225		99.99581		100.03863		731.565		80.225		99.99472		731.797		80.225		99.99844		759.28244		80.225		100.03863		760.82745		80.225		100.05793		762.86188		80.225		100.03187

		732.18201		80.25		99.99898		100.03859		731.82202		80.25		99.99518		732.06		80.25		99.99915		759.53533		80.25		100.03859		761.06756		80.25		100.05793		763.11244		80.25		100.03186

		732.42902		80.275		100.00021		100.03856		732.08099		80.275		99.99737		732.31403		80.275		100.00077		759.78722		80.275		100.03856		761.31723		80.275		100.05793		763.36511		80.275		100.03184

		732.69		80.3		99.99674		100.03853		732.33502		80.3		99.99503		732.57703		80.3		99.99853		760.03689		80.3		100.03853		761.56511		80.3		100.05793		763.60866		80.3		100.03183

		732.95599		80.325		99.99999		100.03852		732.60101		80.325		99.99499		732.84003		80.325		100.0013		760.28189		80.325		100.03852		761.81445		80.325		100.05792		763.84966		80.325		100.03181

		733.20398		80.35		99.99917		100.03851		732.85797		80.35		99.99696		733.09302		80.35		99.99873		760.52567		80.35		100.03851		762.06156		80.35		100.05792		764.08888		80.35		100.0318

		733.47198		80.375		99.9968		100.0385		733.12201		80.375		99.99427		733.354		80.375		99.99792		760.76689		80.375		100.0385		762.31011		80.375		100.05792		764.32999		80.375		100.03179

		733.72998		80.4		100.00008		100.03851		733.37701		80.4		99.99596		733.63		80.4		100.00101		761.00567		80.4		100.03851		762.55722		80.4		100.05793		764.57366		80.4		100.03178

		733.98999		80.425		99.99969		100.03853		733.64697		80.425		99.99438		733.87903		80.425		99.99959		761.253		80.425		100.03853		762.80433		80.425		100.05795		764.82199		80.425		100.03177

		734.25403		80.45		99.99993		100.03855		733.89801		80.45		99.99608		734.14001		80.45		100.00126		761.50321		80.45		100.03855		763.05089		80.45		100.05797		765.07255		80.45		100.03177

		734.51801		80.475		99.9994		100.03858		734.15503		80.475		99.99579		734.40503		80.475		100.001		761.75144		80.475		100.03858		763.302		80.475		100.058		765.32555		80.475		100.03177

		734.776		80.5		99.99819		100.03862		734.41498		80.5		99.99383		734.66803		80.5		99.99827		761.99944		80.5		100.03862		763.54555		80.5		100.05803		765.57588		80.5		100.03178

		735.03601		80.525		99.99819		100.03867		734.68597		80.525		99.99433		734.92297		80.525		100.00071		762.25144		80.525		100.03867		763.78778		80.525		100.05807		765.82722		80.525		100.03179

		735.297		80.55		99.99781		100.03873		734.935		80.55		99.99333		735.185		80.55		99.9995		762.5001		80.55		100.03873		764.02745		80.55		100.05812		766.07822		80.55		100.03181

		735.56		80.575		100.0017		100.03879		735.19598		80.575		99.99551		735.44501		80.575		100.00084		762.74988		80.575		100.03879		764.27134		80.575		100.05818		766.33022		80.575		100.03183

		735.82397		80.6		99.99651		100.03885		735.45398		80.6		99.99262		735.70502		80.6		99.99769		763.00077		80.6		100.03885		764.52145		80.6		100.05824		766.58177		80.6		100.03186

		736.08502		80.625		99.99862		100.03892		735.71802		80.625		99.99655		735.97198		80.625		99.99948		763.25255		80.625		100.03892		764.77422		80.625		100.0583		766.82755		80.625		100.03189

		736.34302		80.65		99.99839		100.03899		735.97998		80.65		99.99642		736.22498		80.65		100.00127		763.49444		80.65		100.03899		765.02745		80.65		100.05837		767.0691		80.65		100.03193

		736.60498		80.675		99.99906		100.03905		736.242		80.675		99.99567		736.48102		80.675		99.99685		763.73622		80.675		100.03905		765.282		80.675		100.05844		767.30933		80.675		100.03197

		736.86902		80.7		99.99671		100.03912		736.49799		80.7		99.99465		736.74902		80.7		100.00078		763.97656		80.7		100.03912		765.53289		80.7		100.05851		767.54488		80.7		100.03201

		737.11603		80.725		99.99777		100.03918		736.75702		80.725		99.99275		737.00403		80.725		100.00129		764.21766		80.725		100.03918		765.78156		80.725		100.05858		767.78777		80.725		100.03205

		737.38098		80.75		99.99874		100.03923		737.01801		80.75		99.99384		737.27899		80.75		99.99741		764.46378		80.75		100.03923		766.03189		80.75		100.05864		768.03411		80.75		100.03208

		737.64301		80.775		100.00134		100.03928		737.276		80.775		99.99554		737.53003		80.775		100.00048		764.71434		80.775		100.03928		766.28423		80.775		100.0587		768.28099		80.775		100.03212

		737.90997		80.8		99.99874		100.03932		737.53802		80.8		99.99614		737.797		80.8		100.00239		764.96455		80.8		100.03932		766.53689		80.8		100.05874		768.52944		80.8		100.03215

		738.16998		80.825		99.99984		100.03936		737.79401		80.825		99.99493		738.05603		80.825		100.0016		765.21478		80.825		100.03936		766.783		80.825		100.05878		768.77633		80.825		100.03218

		738.42999		80.85		99.99801		100.0394		738.05499		80.85		99.99264		738.31897		80.85		100.00096		765.46589		80.85		100.0394		767.02456		80.85		100.05881		769.02323		80.85		100.03221

		738.68298		80.875		100.00024		100.03942		738.31897		80.875		100.00011		738.57501		80.875		100.00181		765.718		80.875		100.03942		767.26322		80.875		100.05884		769.27301		80.875		100.03223

		738.93903		80.9		99.99713		100.03945		738.58002		80.9		99.99251		738.83398		80.9		99.99898		765.96778		80.9		100.03945		767.50155		80.9		100.05885		769.52012		80.9		100.03225

		739.20801		80.925		99.99992		100.03948		738.84302		80.925		99.99434		739.10602		80.925		100.00287		766.22167		80.925		100.03948		767.74478		80.925		100.05885		769.76834		80.925		100.03226

		739.46399		80.95		99.99741		100.0395		739.09302		80.95		99.99705		739.36298		80.95		100.00219		766.47778		80.95		100.0395		767.99222		80.95		100.05885		770.01179		80.95		100.03227

		739.724		80.975		99.99987		100.03952		739.35999		80.975		99.99568		739.62402		80.975		99.99984		766.72622		80.975		100.03952		768.24011		80.975		100.05884		770.25435		80.975		100.03228

		739.974		81		99.99733		100.03955		739.625		81		99.99497		739.87701		81		99.99963		766.96855		81		100.03955		768.48688		81		100.05882		770.49568		81		100.03229

		740.23602		81.025		99.99751		100.03957		739.88098		81.025		99.99303		740.15198		81.025		100.00015		767.21211		81.025		100.03957		768.73166		81.025		100.0588		770.7349		81.025		100.0323

		740.49799		81.05		99.99927		100.0396		740.14301		81.05		99.99611		740.40997		81.05		100.00007		767.456		81.05		100.0396		768.979		81.05		100.05878		770.98023		81.05		100.03231

		740.763		81.075		99.998		100.03964		740.40302		81.075		99.99493		740.66199		81.075		100.00075		767.70422		81.075		100.03964		769.23144		81.075		100.05876		771.22923		81.075		100.03232

		741.026		81.1		99.99838		100.03967		740.65997		81.1		99.99298		740.92499		81.1		100.0028		767.95455		81.1		100.03967		769.48733		81.1		100.05874		771.47489		81.1		100.03233

		741.28497		81.125		99.99531		100.03971		740.92102		81.125		99.99264		741.185		81.125		99.99796		768.20744		81.125		100.03971		769.741		81.125		100.05872		771.72511		81.125		100.03235

		741.54602		81.15		99.9997		100.03976		741.18103		81.15		99.99515		741.44702		81.15		100.00376		768.45833		81.15		100.03976		769.99066		81.15		100.0587		771.977		81.15		100.03236

		741.80701		81.175		99.99971		100.0398		741.43799		81.175		99.99376		741.703		81.175		100.00249		768.707		81.175		100.0398		770.2361		81.175		100.05869		772.22856		81.175		100.03238

		742.065		81.2		99.99751		100.03985		741.70502		81.2		99.99109		741.966		81.2		100.00187		768.95722		81.2		100.03985		770.47989		81.2		100.05868		772.47588		81.2		100.03239

		742.32898		81.225		99.99865		100.03989		741.96399		81.225		99.99072		742.22601		81.225		100.00242		769.21022		81.225		100.03989		770.72266		81.225		100.05867		772.72466		81.225		100.03241

		742.58197		81.25		99.99907		100.03994		742.22101		81.25		99.99369		742.48602		81.25		100.00167		769.46122		81.25		100.03994		770.96988		81.25		100.05867		772.97478		81.25		100.03242

		742.84601		81.275		99.99796		100.03998		742.47601		81.275		99.99241		742.75098		81.275		100.0005		769.71211		81.275		100.03998		771.21999		81.275		100.05867		773.22144		81.275		100.03244

		743.10699		81.3		99.9954		100.04001		742.72998		81.3		99.99289		743.01202		81.3		100.0004		769.95489		81.3		100.04001		771.46766		81.3		100.05867		773.46244		81.3		100.03244

		743.36798		81.325		99.99624		100.04003		742.99902		81.325		99.99429		743.271		81.325		100.00158		770.19833		81.325		100.04003		771.71455		81.325		100.05867		773.702		81.325		100.03245

		743.62201		81.35		99.9991		100.04005		743.25897		81.35		99.99968		743.53699		81.35		100.00111		770.44022		81.35		100.04005		771.96677		81.35		100.05867		773.938		81.35		100.03245

		743.88202		81.375		99.9984		100.04006		743.51801		81.375		99.99499		743.79602		81.375		100.00048		770.68089		81.375		100.04006		772.21788		81.375		100.05868		774.17955		81.375		100.03246

		744.146		81.4		99.99828		100.04006		743.77899		81.4		99.99442		744.05603		81.4		100.00007		770.92511		81.4		100.04006		772.46966		81.4		100.05868		774.42645		81.4		100.03246

		744.409		81.425		100.00207		100.04006		744.03802		81.425		99.99474		744.30701		81.425		100.00168		771.17433		81.425		100.04006		772.71855		81.425		100.05869		774.67634		81.425		100.03246

		744.66101		81.45		99.99849		100.04004		744.29602		81.45		99.99374		744.56201		81.45		100.00617		771.42444		81.45		100.04004		772.96611		81.45		100.05869		774.92855		81.45		100.03246

		744.922		81.475		99.99416		100.04002		744.55701		81.475		99.99111		744.828		81.475		100.00101		771.67477		81.475		100.04002		773.21133		81.475		100.0587		775.17811		81.475		100.03247

		745.18903		81.5		99.99765		100.03999		744.82202		81.5		99.99087		745.08899		81.5		100.00133		771.92477		81.5		100.03999		773.452		81.5		100.05871		775.42633		81.5		100.03247

		745.44299		81.525		100.00168		100.03995		745.07898		81.525		99.99514		745.35199		81.525		100.00257		772.17833		81.525		100.03995		773.69078		81.525		100.05872		775.67655		81.525		100.03247

		745.711		81.55		99.99916		100.03991		745.34198		81.55		99.99398		745.60999		81.55		100.00162		772.42989		81.55		100.03991		773.92778		81.55		100.05873		775.93288		81.55		100.03248

		745.96698		81.575		100.00098		100.03987		745.59601		81.575		99.99758		745.87201		81.575		100.00278		772.68144		81.575		100.03987		774.16623		81.575		100.05875		776.19177		81.575		100.03249

		746.229		81.6		99.99858		100.03983		745.86902		81.6		99.99454		746.12903		81.6		100.00181		772.93378		81.6		100.03983		774.41123		81.6		100.05878		776.44222		81.6		100.0325

		746.49298		81.625		99.99872		100.03979		746.12598		81.625		99.9928		746.40198		81.625		100.002		773.184		81.625		100.03979		774.65689		81.625		100.05882		776.68577		81.625		100.03251

		746.742		81.65		99.99898		100.03975		746.38501		81.65		99.99425		746.66302		81.65		100.00372		773.42889		81.65		100.03975		774.90923		81.65		100.05886		776.92577		81.65		100.03253

		747.01001		81.675		99.99522		100.03971		746.65002		81.675		99.99189		746.922		81.675		100.00012		773.66901		81.675		100.03971		775.16345		81.675		100.05891		777.16433		81.675		100.03255

		747.27002		81.7		100.00105		100.03969		746.91101		81.7		99.99608		747.17999		81.7		100.00377		773.91056		81.7		100.03969		775.41522		81.7		100.05898		777.40678		81.7		100.03257

		747.53497		81.725		99.99952		100.03967		747.15399		81.725		99.99374		747.44299		81.725		100.00322		774.15612		81.725		100.03967		775.66623		81.725		100.05905		777.65645		81.725		100.03259

		747.78998		81.75		99.9953		100.03966		747.41199		81.75		99.99269		747.70599		81.75		99.99876		774.40701		81.75		100.03966		775.92344		81.75		100.05913		777.90734		81.75		100.03262

		748.04199		81.775		99.99752		100.03965		747.67798		81.775		99.99275		747.961		81.775		100.00111		774.65645		81.775		100.03965		776.1811		81.775		100.05923		778.15545		81.775		100.03264

		748.315		81.8		99.99769		100.03966		747.94		81.8		99.99387		748.22699		81.8		100.00298		774.90645		81.8		100.03966		776.43299		81.8		100.05933		778.401		81.8		100.03266

		748.58301		81.825		99.99848		100.03967		748.19202		81.825		99.9935		748.487		81.825		100.00481		775.15746		81.825		100.03967		776.67866		81.825		100.05944		778.64834		81.825		100.03269

		748.828		81.85		99.99929		100.03968		748.466		81.85		99.99431		748.74597		81.85		100.00174		775.40601		81.85		100.03968		776.92211		81.85		100.05956		778.89945		81.85		100.03271

		749.099		81.875		99.99775		100.0397		748.72498		81.875		99.9932		749.00897		81.875		100.0012		775.65601		81.875		100.0397		777.16288		81.875		100.05967		779.15234		81.875		100.03273

		749.35199		81.9		99.99933		100.03972		748.97498		81.9		99.99216		749.26501		81.9		100.00084		775.91057		81.9		100.03972		777.4051		81.9		100.05979		779.40434		81.9		100.03274

		749.62201		81.925		99.99865		100.03975		749.25201		81.925		99.99449		749.526		81.925		100.00189		776.16456		81.925		100.03975		777.65399		81.925		100.05991		779.65445		81.925		100.03276

		749.87299		81.95		99.99692		100.03977		749.50702		81.95		99.99297		749.79602		81.95		100.00038		776.41534		81.95		100.03977		777.9061		81.95		100.06002		779.89922		81.95		100.03277

		750.12598		81.975		99.99953		100.03979		749.77802		81.975		99.99183		750.04498		81.975		99.99916		776.65967		81.975		100.03979		778.15466		81.975		100.06012		780.14045		81.975		100.03278

		750.396		82		99.99959		100.03981		750.03003		82		99.99323		750.30402		82		100.00264		776.90289		82		100.03981		778.40455		82		100.06022		780.38034		82		100.03279

		750.651		82.025		99.99828		100.03983		750.28101		82.025		99.99373		750.56897		82.025		100.00199		777.14667		82.025		100.03983		778.655		82.025		100.06031		780.61968		82.025		100.0328

		750.91699		82.05		100.00178		100.03984		750.534		82.05		99.99401		750.828		82.05		99.99968		777.39089		82.05		100.03984		778.90645		82.05		100.06038		780.86745		82.05		100.0328

		751.17603		82.075		99.9975		100.03986		750.797		82.075		99.99455		751.09198		82.075		99.99998		777.64267		82.075		100.03986		779.15845		82.075		100.06045		781.11367		82.075		100.03281

		751.435		82.1		99.99637		100.03987		751.05603		82.1		99.99263		751.34302		82.1		100.00114		777.89478		82.1		100.03987		779.40834		82.1		100.0605		781.36067		82.1		100.03282

		751.70203		82.125		99.99709		100.03988		751.31897		82.125		99.99181		751.61401		82.125		99.99774		778.14544		82.125		100.03988		779.65757		82.125		100.06054		781.60723		82.125		100.03282

		751.95801		82.15		99.99891		100.03989		751.56403		82.15		99.99493		751.86298		82.15		100.00116		778.39544		82.15		100.03989		779.90101		82.15		100.06057		781.8559		82.15		100.03284

		752.21198		82.175		99.99929		100.0399		751.83899		82.175		99.9909		752.12299		82.175		100.00015		778.64644		82.175		100.0399		780.14379		82.175		100.06059		782.10312		82.175		100.03285

		752.47302		82.2		99.99658		100.03992		752.08899		82.2		99.9923		752.39001		82.2		100.00103		778.90067		82.2		100.03992		780.38523		82.2		100.0606		782.35189		82.2		100.03287

		752.73901		82.225		99.99669		100.03995		752.35901		82.225		99.99174		752.64301		82.225		100.00138		779.15634		82.225		100.03995		780.62623		82.225		100.0606		782.60055		82.225		100.03289

		752.99701		82.25		99.99709		100.03997		752.61902		82.25		99.99538		752.90997		82.25		99.99943		779.41222		82.25		100.03997		780.87412		82.25		100.06059		782.85433		82.25		100.03291

		753.25098		82.275		99.99971		100.04001		752.87402		82.275		99.99231		753.16901		82.275		99.99908		779.66589		82.275		100.04001		781.12467		82.275		100.06058		783.09922		82.275		100.03293

		753.51501		82.3		99.99822		100.04005		753.133		82.3		99.99481		753.42297		82.3		99.99972		779.91389		82.3		100.04005		781.37623		82.3		100.06056		783.34055		82.3		100.03296

		753.77899		82.325		99.99672		100.0401		753.39697		82.325		99.9933		753.69		82.325		99.99848		780.15855		82.325		100.0401		781.62912		82.325		100.06054		783.57977		82.325		100.03299

		754.03601		82.35		99.99764		100.04016		753.66803		82.35		99.99461		753.948		82.35		100.00114		780.40111		82.35		100.04016		781.88478		82.35		100.06051		783.82033		82.35		100.03303

		754.29797		82.375		99.99789		100.04023		753.91699		82.375		99.99131		754.21301		82.375		100.00179		780.64467		82.375		100.04023		782.14123		82.375		100.06049		784.06843		82.375		100.03306

		754.55798		82.4		99.99957		100.04029		754.177		82.4		99.99391		754.474		82.4		100.00297		780.89455		82.4		100.04029		782.39789		82.4		100.06047		784.31621		82.4		100.0331

		754.82098		82.425		99.99794		100.04037		754.43701		82.425		99.99493		754.737		82.425		100.00254		781.14422		82.425		100.04037		782.6519		82.425		100.06045		784.56532		82.425		100.03313

		755.08801		82.45		99.99934		100.04044		754.69598		82.45		99.99306		755.00201		82.45		100.00321		781.39511		82.45		100.04044		782.90679		82.45		100.06043		784.81721		82.45		100.03317

		755.336		82.475		99.99743		100.04052		754.961		82.475		99.99376		755.255		82.475		100.00802		781.64389		82.475		100.04052		783.15245		82.475		100.06042		785.06599		82.475		100.0332

		755.60101		82.5		99.99793		100.0406		755.21503		82.5		99.9941		755.51501		82.5		99.99851		781.89678		82.5		100.0406		783.39445		82.5		100.06042		785.31577		82.5		100.03324

		755.86102		82.525		99.99911		100.04067		755.48999		82.525		99.99428		755.77197		82.525		100.00375		782.14866		82.525		100.04067		783.63622		82.525		100.06042		785.56733		82.525		100.03327

		756.12097		82.55		99.9972		100.04074		755.74799		82.55		99.99158		756.03497		82.55		99.99581		782.40322		82.55		100.04074		783.87767		82.55		100.06043		785.82511		82.55		100.03329

		756.383		82.575		99.99687		100.0408		756.01099		82.575		99.99163		756.28998		82.575		99.99937		782.66044		82.575		100.0408		784.12489		82.575		100.06045		786.08167		82.575		100.03332

		756.64801		82.6		99.99835		100.04084		756.26703		82.6		99.99126		756.552		82.6		100.00028		782.91722		82.6		100.04084		784.37167		82.6		100.06048		786.32689		82.6		100.03334

		756.90198		82.625		99.99725		100.04088		756.52502		82.625		99.99391		756.81201		82.625		100.00414		783.16501		82.625		100.04088		784.61734		82.625		100.06051		786.57345		82.625		100.03336

		757.16199		82.65		99.99906		100.04091		756.79199		82.65		99.99376		757.073		82.65		99.99779		783.41212		82.65		100.04091		784.86789		82.65		100.06054		786.82001		82.65		100.03338

		757.42603		82.675		99.9981		100.04092		757.047		82.675		99.99366		757.33099		82.675		100.00361		783.65611		82.675		100.04092		785.11833		82.675		100.06058		787.06445		82.675		100.03339

		757.69		82.7		99.99625		100.04092		757.29401		82.7		99.99176		757.58899		82.7		100.00362		783.905		82.7		100.04092		785.37		82.7		100.06063		787.31579		82.7		100.0334

		757.93701		82.725		99.99856		100.0409		757.56299		82.725		99.99505		757.85498		82.725		99.99361		784.15689		82.725		100.0409		785.62344		82.725		100.06067		787.57034		82.725		100.03341

		758.203		82.75		99.99852		100.04088		757.81897		82.75		99.99536		758.11499		82.75		100.00589		784.4109		82.75		100.04088		785.878		82.75		100.06071		787.82633		82.75		100.03342

		758.46198		82.775		99.99638		100.04084		758.08899		82.775		99.99417		758.367		82.775		100.00341		784.66501		82.775		100.04084		786.13355		82.775		100.06075		788.078		82.775		100.03343

		758.71899		82.8		99.99995		100.04081		758.33899		82.8		99.99722		758.625		82.8		99.98422		784.91756		82.8		100.04081		786.3811		82.8		100.06078		788.32834		82.8		100.03343

		758.98102		82.825		99.99879		100.04076		758.604		82.825		99.99509		758.89801		82.825		99.99397		785.17055		82.825		100.04076		786.62688		82.825		100.06081		788.58089		82.825		100.03343

		759.25098		82.85		99.99865		100.04072		758.867		82.85		99.99532		759.15399		82.85		100.00035		785.42411		82.85		100.04072		786.87332		82.85		100.06083		788.83478		82.85		100.03343

		759.50098		82.875		99.99701		100.04069		759.12701		82.875		99.99349		759.40802		82.875		99.99132		785.67566		82.875		100.04069		787.12088		82.875		100.06085		789.08923		82.875		100.03344

		759.763		82.9		99.99873		100.04066		759.388		82.9		99.99294		759.66602		82.9		99.99501		785.931		82.9		100.04066		787.37554		82.9		100.06086		789.34311		82.9		100.03344

		760.02399		82.925		99.997		100.04064		759.651		82.925		99.99487		759.93799		82.925		99.99758		786.18277		82.925		100.04064		787.63432		82.925		100.06087		789.59089		82.925		100.03345

		760.284		82.95		99.99919		100.04064		759.91602		82.95		99.99485		760.203		82.95		99.99646		786.42811		82.95		100.04064		787.89233		82.95		100.06088		789.83655		82.95		100.03346

		760.54102		82.975		99.99727		100.04066		760.17297		82.975		99.99491		760.44702		82.975		99.99418		786.66966		82.975		100.04066		788.14866		82.975		100.06089		790.08056		82.975		100.03347

		760.80402		83		99.99703		100.0407		760.43201		83		99.99444		760.70898		83		99.99677		786.91033		83		100.0407		788.40544		83		100.06091		790.32355		83		100.03348

		761.06799		83.025		99.99745		100.04075		760.68597		83.025		99.9951		760.966		83.025		99.99213		787.15622		83.025		100.04075		788.66211		83.025		100.06093		790.57411		83.025		100.0335

		761.323		83.05		99.99931		100.04083		760.95001		83.05		99.99254		761.22699		83.05		100.00849		787.40645		83.05		100.04083		788.92078		83.05		100.06095		790.827		83.05		100.03353

		761.58502		83.075		99.99899		100.04092		761.20502		83.075		99.99493		761.48602		83.075		100.00094		787.66078		83.075		100.04092		789.178		83.075		100.06098		791.07678		83.075		100.03356

		761.84601		83.1		100.00081		100.04103		761.46698		83.1		99.99526		761.73999		83.1		99.99927		787.91722		83.1		100.04103		789.43245		83.1		100.06102		791.32444		83.1		100.03359

		762.10999		83.125		99.99809		100.04115		761.72998		83.125		99.99421		762.005		83.125		100.01824		788.17177		83.125		100.04115		789.67889		83.125		100.06106		791.575		83.125		100.03363

		762.36298		83.15		99.99953		100.04128		761.98798		83.15		99.99564		762.27197		83.15		100.00888		788.42644		83.15		100.04128		789.92122		83.15		100.06112		791.82589		83.15		100.03368

		762.625		83.175		99.9951		100.04141		762.26001		83.175		99.99247		762.526		83.175		99.989		788.68144		83.175		100.04141		790.16267		83.175		100.06118		792.07411		83.175		100.03372

		762.87903		83.2		99.99759		100.04154		762.51202		83.2		99.99018		762.79401		83.2		100.00575		788.93888		83.2		100.04154		790.41189		83.2		100.06124		792.32411		83.2		100.03377

		763.13898		83.225		100.00004		100.04167		762.76202		83.225		99.99215		763.05103		83.225		100.00473		789.19633		83.225		100.04167		790.66722		83.225		100.0613		792.57522		83.225		100.03381

		763.40302		83.25		100.00046		100.04179		763.03601		83.25		99.99514		763.315		83.25		100.00797		789.44967		83.25		100.04179		790.92122		83.25		100.06136		792.82167		83.25		100.03386

		763.66101		83.275		99.99726		100.0419		763.29401		83.275		99.99331		763.573		83.275		100.00431		789.69899		83.275		100.0419		791.17411		83.275		100.06142		793.06478		83.275		100.0339

		763.92798		83.3		99.99844		100.04199		763.55402		83.3		99.99027		763.84003		83.3		100.00008		789.94611		83.3		100.04199		791.42944		83.3		100.06147		793.307		83.3		100.03394

		764.185		83.325		99.99945		100.04206		763.81		83.325		99.99529		764.09198		83.325		99.99957		790.19122		83.325		100.04206		791.6861		83.325		100.06152		793.54933		83.325		100.03398

		764.44397		83.35		100.00113		100.04211		764.07397		83.35		99.99158		764.36102		83.35		100.00271		790.44233		83.35		100.04211		791.94333		83.35		100.06155		793.79867		83.35		100.03401

		764.70599		83.375		99.99595		100.04215		764.32898		83.375		99.99402		764.62402		83.375		100.00555		790.69633		83.375		100.04215		792.20177		83.375		100.06158		794.05178		83.375		100.03403

		764.966		83.4		100.00106		100.04216		764.60303		83.4		99.99344		764.87201		83.4		100.00142		790.95122		83.4		100.04216		792.45888		83.4		100.06159		794.30712		83.4		100.03405

		765.21997		83.425		100.00106		100.04216		764.84399		83.425		99.9934		765.14099		83.425		100.00213		791.20677		83.425		100.04216		792.71122		83.425		100.06159		794.56278		83.425		100.03407

		765.48297		83.45		99.99669		100.04214		765.11603		83.45		99.98964		765.39899		83.45		99.99737		791.46244		83.45		100.04214		792.95466		83.45		100.06159		794.81845		83.45		100.03408

		765.74298		83.475		99.99797		100.04211		765.37201		83.475		99.99278		765.66699		83.475		100.00027		791.71665		83.475		100.04211		793.19756		83.475		100.06157		795.07134		83.475		100.03408

		766.005		83.5		99.99845		100.04207		765.63202		83.5		99.99434		765.92102		83.5		99.99944		791.97266		83.5		100.04207		793.43867		83.5		100.06155		795.32567		83.5		100.03409

		766.26801		83.525		99.99894		100.04203		765.89099		83.525		99.98978		766.18799		83.525		100.00081		792.22765		83.525		100.04203		793.68411		83.525		100.06152		795.58178		83.525		100.03409

		766.52399		83.55		99.99735		100.04198		766.15399		83.55		99.9903		766.44501		83.55		99.99972		792.48099		83.55		100.04198		793.93399		83.55		100.0615		795.83756		83.55		100.03409

		766.784		83.575		99.99662		100.04194		766.40802		83.575		99.98985		766.68799		83.575		99.99994		792.73077		83.575		100.04194		794.18488		83.575		100.06147		796.08478		83.575		100.03409

		767.04199		83.6		99.99843		100.04189		766.67102		83.6		99.99273		766.94702		83.6		99.99877		792.97532		83.6		100.04189		794.43544		83.6		100.06144		796.32789		83.6		100.0341

		767.30798		83.625		99.99624		100.04185		766.93402		83.625		99.99203		767.21002		83.625		99.99945		793.21688		83.625		100.04185		794.68955		83.625		100.06143		796.56722		83.625		100.03411

		767.573		83.65		99.99944		100.04182		767.18701		83.65		99.99373		767.474		83.65		100.00159		793.45666		83.65		100.04182		794.93888		83.65		100.06141		796.80644		83.65		100.03412

		767.82501		83.675		99.99893		100.04179		767.44897		83.675		99.99376		767.73499		83.675		100.00274		793.70466		83.675		100.04179		795.19		83.675		100.06141		797.05389		83.675		100.03413

		768.08698		83.7		99.99917		100.04177		767.70697		83.7		99.99366		767.99902		83.7		100.00146		793.95734		83.7		100.04177		795.44522		83.7		100.06141		797.30333		83.7		100.03415

		768.34003		83.725		99.99949		100.04174		767.97498		83.725		99.99259		768.26001		83.725		99.99943		794.20767		83.725		100.04174		795.70344		83.725		100.06143		797.55444		83.725		100.03417

		768.60901		83.75		99.99746		100.04173		768.23401		83.75		99.99095		768.52197		83.75		100.00006		794.45767		83.75		100.04173		795.95234		83.75		100.06145		797.80478		83.75		100.0342

		768.86603		83.775		99.99856		100.04171		768.49298		83.775		99.99322		768.78101		83.775		99.99957		794.71289		83.775		100.04171		796.19478		83.775		100.06148		798.05589		83.775		100.03423

		769.125		83.8		99.99844		100.04169		768.74902		83.8		99.99316		769.04102		83.8		99.99962		794.96522		83.8		100.04169		796.43556		83.8		100.06151		798.30823		83.8		100.03427

		769.38898		83.825		99.99887		100.04167		769.008		83.825		99.99317		769.30902		83.825		100.00116		795.21967		83.825		100.04167		796.67845		83.825		100.06155		798.56245		83.825		100.0343

		769.65802		83.85		99.99747		100.04164		769.27698		83.85		99.99237		769.56598		83.85		100.0011		795.47711		83.85		100.04164		796.92212		83.85		100.0616		798.819		83.85		100.03433

		769.90601		83.875		99.99924		100.04162		769.54199		83.875		99.99486		769.828		83.875		99.99986		795.73533		83.875		100.04162		797.17301		83.875		100.06165		799.07612		83.875		100.03437

		770.16803		83.9		99.99741		100.04158		769.79303		83.9		99.99306		770.09198		83.9		99.99855		795.98511		83.9		100.04158		797.42523		83.9		100.06171		799.32478		83.9		100.0344

		770.42798		83.925		99.99661		100.04154		770.04401		83.925		99.99372		770.34998		83.925		100.00052		796.23144		83.925		100.04154		797.67567		83.925		100.06177		799.57067		83.925		100.03444

		770.70099		83.95		99.99822		100.04151		770.31299		83.95		99.99275		770.60901		83.95		100.00081		796.47322		83.95		100.04151		797.92611		83.95		100.06183		799.81378		83.95		100.03447

		770.95099		83.975		100.00132		100.04147		770.57397		83.975		99.99496		770.86401		83.975		100.00079		796.71589		83.975		100.04147		798.17933		83.975		100.06189		800.05556		83.975		100.0345

		771.21698		84		99.99743		100.04143		770.82501		84		99.99208		771.13098		84		100.00034		796.96133		84		100.04143		798.43666		84		100.06196		800.30411		84		100.03453

		771.47198		84.025		100.00093		100.04139		771.091		84.025		99.99671		771.39001		84.025		100.00219		797.21167		84.025		100.04139		798.69555		84.025		100.06203		800.55522		84.025		100.03456

		771.74103		84.05		99.99734		100.04136		771.35901		84.05		99.99404		771.65198		84.05		100.00259		797.46367		84.05		100.04136		798.95366		84.05		100.0621		800.80433		84.05		100.03459

		771.99402		84.075		99.99729		100.04133		771.61102		84.075		99.99069		771.90997		84.075		100.00007		797.71723		84.075		100.04133		799.20799		84.075		100.06217		801.05045		84.075		100.03462

		772.25702		84.1		99.9981		100.04132		771.87799		84.1		99.99398		772.172		84.1		100.00145		797.96878		84.1		100.04132		799.45578		84.1		100.06225		801.29656		84.1		100.03465

		772.51599		84.125		99.99959		100.04131		772.13397		84.125		99.99616		772.43201		84.125		100.00334		798.22011		84.125		100.04131		799.70144		84.125		100.06233		801.54256		84.125		100.03468

		772.77899		84.15		99.99969		100.04131		772.38599		84.15		99.99531		772.685		84.15		100.00098		798.47445		84.15		100.04131		799.94489		84.15		100.06241		801.79156		84.15		100.03472

		773.02002		84.175		99.99737		100.04132		772.64801		84.175		99.99252		772.94202		84.175		99.99851		798.732		84.175		100.04132		800.18944		84.175		100.06249		802.041		84.175		100.03475

		773.289		84.2		99.99927		100.04133		772.90503		84.2		99.99329		773.20599		84.2		100.00093		798.98878		84.2		100.04133		800.44		84.2		100.06257		802.291		84.2		100.03479

		773.55402		84.225		99.99638		100.04135		773.164		84.225		99.99264		773.47498		84.225		100.00121		799.23822		84.225		100.04135		800.68778		84.225		100.06264		802.53434		84.225		100.03482

		773.81201		84.25		99.9999		100.04138		773.43597		84.25		99.9953		773.72601		84.25		100.00256		799.48199		84.25		100.04138		800.93555		84.25		100.06272		802.772		84.25		100.03486

		774.07599		84.275		99.99828		100.0414		773.69501		84.275		99.99319		773.98499		84.275		99.99872		799.7251		84.275		100.0414		801.18233		84.275		100.06279		803.01067		84.275		100.0349

		774.32898		84.3		99.9965		100.04143		773.95801		84.3		99.99166		774.245		84.3		99.99945		799.96377		84.3		100.04143		801.43211		84.3		100.06286		803.25033		84.3		100.03494

		774.59003		84.325		99.9984		100.04145		774.21002		84.325		99.99449		774.50702		84.325		100.00077		800.209		84.325		100.04145		801.68488		84.325		100.06292		803.49989		84.325		100.03497

		774.849		84.35		99.99775		100.04147		774.47101		84.35		99.99502		774.76703		84.35		100.00223		800.46233		84.35		100.04147		801.93833		84.35		100.06298		803.75122		84.35		100.03501

		775.11401		84.375		100.00068		100.04148		774.72601		84.375		99.9957		775.03302		84.375		100.0016		800.71278		84.375		100.04148		802.19189		84.375		100.06303		804.00322		84.375		100.03504

		775.38		84.4		99.99848		100.04148		774.99402		84.4		99.99398		775.28497		84.4		100.00061		800.96478		84.4		100.04148		802.44366		84.4		100.06307		804.25456		84.4		100.03507

		775.63202		84.425		99.99849		100.04148		775.24701		84.425		99.99482		775.54797		84.425		100.00095		801.21711		84.425		100.04148		802.6881		84.425		100.06311		804.50522		84.425		100.0351

		775.89001		84.45		99.99967		100.04148		775.50702		84.45		99.99529		775.81097		84.45		100.00059		801.47289		84.45		100.04148		802.93022		84.45		100.06314		804.75677		84.45		100.03512

		776.15302		84.475		99.99501		100.04146		775.76099		84.475		99.99328		776.06598		84.475		100.00055		801.73011		84.475		100.04146		803.16977		84.475		100.06316		805.01		84.475		100.03513

		776.409		84.5		99.99606		100.04145		776.02301		84.5		99.99339		776.32898		84.5		100.0004		801.98511		84.5		100.04145		803.41821		84.5		100.06317		805.26367		84.5		100.03514

		776.66901		84.525		99.99881		100.04142		776.27698		84.525		99.99723		776.58899		84.525		100.00215		802.24055		84.525		100.04142		803.66899		84.525		100.06318		805.51867		84.525		100.03515

		776.927		84.55		99.99637		100.04139		776.539		84.55		99.99287		776.854		84.55		100.00018		802.4921		84.55		100.04139		803.91722		84.55		100.06318		805.76034		84.55		100.03515

		777.18298		84.575		99.99818		100.04136		776.80402		84.575		99.99453		777.10797		84.575		100.00112		802.7351		84.575		100.04136		804.16589		84.575		100.06318		805.99822		84.575		100.03514

		777.44397		84.6		99.99838		100.04133		777.07098		84.6		99.99655		777.37799		84.6		100.00074		802.97677		84.6		100.04133		804.41577		84.6		100.06317		806.23522		84.6		100.03512

		777.71002		84.625		99.99942		100.0413		777.31897		84.625		99.99448		777.63202		84.625		100.00137		803.21611		84.625		100.0413		804.66389		84.625		100.06315		806.47266		84.625		100.0351

		777.96802		84.65		99.997		100.04127		777.58698		84.65		99.99373		777.89301		84.65		100		803.46455		84.65		100.04127		804.91322		84.65		100.06314		806.71956		84.65		100.03507

		778.22803		84.675		99.99882		100.04125		777.84601		84.675		99.99394		778.15002		84.675		99.99943		803.71411		84.675		100.04125		805.165		84.675		100.06312		806.967		84.675		100.03504

		778.49103		84.7		99.99448		100.04124		778.11401		84.7		99.99349		778.41498		84.7		100.00084		803.96311		84.7		100.04124		805.41789		84.7		100.0631		807.21233		84.7		100.035

		778.74902		84.725		99.99844		100.04123		778.36902		84.725		99.99412		778.66602		84.725		100.00228		804.21334		84.725		100.04123		805.66322		84.725		100.06308		807.45533		84.725		100.03496

		779.01099		84.75		99.99742		100.04122		778.62799		84.75		99.99331		778.93201		84.75		100.00214		804.46534		84.75		100.04122		805.90311		84.75		100.06306		807.69933		84.75		100.03493

		779.26599		84.775		99.9989		100.04123		778.89203		84.775		99.99679		779.18799		84.775		100.00191		804.71723		84.775		100.04123		806.144		84.775		100.06304		807.94644		84.775		100.03489

		779.53302		84.8		99.99921		100.04124		779.146		84.8		99.9944		779.44598		84.8		100.00076		804.96901		84.8		100.04124		806.38344		84.8		100.06303		808.19722		84.8		100.03486

		779.784		84.825		99.99853		100.04127		779.40302		84.825		99.99502		779.70898		84.825		99.99909		805.22034		84.825		100.04127		806.62956		84.825		100.06302		808.44733		84.825		100.03483

		780.04199		84.85		99.99975		100.0413		779.66602		84.85		99.99551		779.979		84.85		99.99799		805.47401		84.85		100.0413		806.88011		84.85		100.06301		808.69611		84.85		100.03481

		780.30603		84.875		99.99862		100.04135		779.92902		84.875		99.99278		780.23901		84.875		100.00104		805.71878		84.875		100.04135		807.13245		84.875		100.06301		808.93955		84.875		100.03479

		780.56097		84.9		99.99824		100.0414		780.17902		84.9		99.99423		780.49597		84.9		100.00123		805.95989		84.9		100.0414		807.38578		84.9		100.06302		809.18334		84.9		100.03478

		780.823		84.925		99.99995		100.04145		780.44702		84.925		99.9956		780.75		84.925		100.00236		806.20222		84.925		100.04145		807.63822		84.925		100.06304		809.42912		84.925		100.03479

		781.08002		84.95		100.00008		100.04151		780.71198		84.95		99.9934		781.01099		84.95		100.00147		806.44156		84.95		100.04151		807.88967		84.95		100.06306		809.6739		84.95		100.03479

		781.341		84.975		100.00026		100.04158		780.961		84.975		99.99328		781.276		84.975		99.99986		806.68755		84.975		100.04158		808.141		84.975		100.06309		809.92501		84.975		100.03481

		781.60303		85		99.99679		100.04164		781.224		85		99.99465		781.539		85		100.00086		806.93433		85		100.04164		808.39367		85		100.06312		810.17556		85		100.03483

		781.85999		85.025		99.99899		100.0417		781.5		85.025		99.99437		781.79901		85.025		100.00097		807.18244		85.025		100.0417		808.64789		85.025		100.06316		810.4239		85.025		100.03486

		782.12299		85.05		99.99713		100.04175		781.73901		85.05		99.99393		782.05298		85.05		100.00086		807.433		85.05		100.04175		808.89412		85.05		100.0632		810.67167		85.05		100.0349

		782.383		85.075		99.99928		100.0418		782.008		85.075		99.99366		782.31097		85.075		100.00048		807.68311		85.075		100.0418		809.1409		85.075		100.06324		810.922		85.075		100.03494

		782.64502		85.1		99.9971		100.04184		782.27002		85.1		99.99467		782.56598		85.1		100.00064		807.93333		85.1		100.04184		809.38534		85.1		100.06329		811.16889		85.1		100.03498

		782.909		85.125		100.0008		100.04188		782.52899		85.125		99.99569		782.84198		85.125		100.00096		808.18511		85.125		100.04188		809.62657		85.125		100.06334		811.41245		85.125		100.03502

		783.16699		85.15		99.99755		100.0419		782.79303		85.15		99.99305		783.09802		85.15		100.00031		808.43444		85.15		100.0419		809.87756		85.15		100.06339		811.65745		85.15		100.03507

		783.42603		85.175		99.99995		100.04192		783.05103		85.175		99.99559		783.362		85.175		99.99868		808.68511		85.175		100.04192		810.13068		85.175		100.06343		811.90223		85.175		100.03512

		783.68201		85.2		99.99899		100.04192		783.30701		85.2		99.99425		783.617		85.2		100.00089		808.92788		85.2		100.04192		810.3839		85.2		100.06348		812.142		85.2		100.03516

		783.948		85.225		99.99879		100.04192		783.56897		85.225		99.99194		783.87701		85.225		99.99946		809.17188		85.225		100.04192		810.63612		85.225		100.06353		812.38078		85.225		100.03521

		784.20502		85.25		99.9994		100.04192		783.83099		85.25		99.99328		784.13397		85.25		99.99964		809.41488		85.25		100.04192		810.88956		85.25		100.06357		812.62023		85.25		100.03525

		784.47101		85.275		99.99613		100.04191		784.08698		85.275		99.99586		784.39697		85.275		100.00012		809.65455		85.275		100.04191		811.14734		85.275		100.06362		812.85945		85.275		100.0353

		784.72699		85.3		100.00092		100.0419		784.35101		85.3		99.99781		784.65503		85.3		100.00286		809.90044		85.3		100.0419		811.40122		85.3		100.06366		813.10578		85.3		100.03534

		784.98199		85.325		99.99902		100.0419		784.60699		85.325		99.99426		784.92102		85.325		100.00102		810.14943		85.325		100.0419		811.65523		85.325		100.0637		813.35478		85.325		100.03538

		785.24902		85.35		99.99776		100.04189		784.86499		85.35		99.99439		785.18799		85.35		99.99934		810.39921		85.35		100.04189		811.91022		85.35		100.06375		813.60512		85.35		100.03543

		785.51398		85.375		99.99742		100.04189		785.13098		85.375		99.99373		785.44299		85.375		99.99904		810.64832		85.375		100.04189		812.15723		85.375		100.06379		813.85733		85.375		100.03547

		785.76898		85.4		99.99803		100.0419		785.38		85.4		99.99513		785.70099		85.4		100.00005		810.89933		85.4		100.0419		812.402		85.4		100.06382		814.11278		85.4		100.0355

		786.03802		85.425		99.99938		100.04191		785.646		85.425		99.99557		785.96503		85.425		100.0004		811.15322		85.425		100.04191		812.64712		85.425		100.06386		814.36767		85.425		100.03554

		786.30103		85.45		99.99644		100.04192		785.90698		85.45		99.99096		786.22998		85.45		100.00043		811.405		85.45		100.04192		812.891		85.45		100.06389		814.62334		85.45		100.03558

		786.55298		85.475		100.00117		100.04194		786.16699		85.475		99.99542		786.48297		85.475		100.00282		811.658		85.475		100.04194		813.14311		85.475		100.06392		814.87778		85.475		100.03561

		786.81097		85.5		100.00018		100.04196		786.43799		85.5		99.99695		786.74701		85.5		100.00185		811.91245		85.5		100.04196		813.39444		85.5		100.06394		815.13266		85.5		100.03565

		787.07001		85.525		99.99954		100.04198		786.68903		85.525		99.99466		787.00702		85.525		100.00078		812.15878		85.525		100.04198		813.64722		85.525		100.06395		815.37989		85.525		100.03568

		787.33301		85.55		99.99835		100.04201		786.95001		85.55		99.99273		787.26898		85.55		100.00042		812.40367		85.55		100.04201		813.901		85.55		100.06396		815.62566		85.55		100.0357

		787.58801		85.575		99.99701		100.04203		787.21503		85.575		99.99423		787.52802		85.575		99.99969		812.6449		85.575		100.04203		814.15445		85.575		100.06397		815.86922		85.575		100.03573

		787.85101		85.6		100.00034		100.04204		787.46802		85.6		99.99527		787.789		85.6		100.00071		812.88734		85.6		100.04204		814.40622		85.6		100.06396		816.10923		85.6		100.03575

		788.11603		85.625		99.99831		100.04206		787.72498		85.625		99.99541		788.047		85.625		100.0041		813.1379		85.625		100.04206		814.65811		85.625		100.06395		816.35645		85.625		100.03577

		788.37701		85.65		99.99849		100.04207		787.987		85.65		99.99542		788.31299		85.65		100.00182		813.38623		85.65		100.04207		814.91055		85.65		100.06394		816.60478		85.65		100.03578

		788.64203		85.675		99.99773		100.04207		788.245		85.675		99.99221		788.57001		85.675		100.00086		813.63379		85.675		100.04207		815.16577		85.675		100.06392		816.85278		85.675		100.0358

		788.89801		85.7		99.99855		100.04207		788.505		85.7		99.99358		788.83398		85.7		100.0002		813.88379		85.7		100.04207		815.41066		85.7		100.0639		817.105		85.7		100.03581

		789.15698		85.725		99.99911		100.04207		788.76801		85.725		99.99487		789.10199		85.725		99.99961		814.13523		85.725		100.04207		815.65244		85.725		100.06387		817.35611		85.725		100.03582

		789.41901		85.75		99.9973		100.04207		789.03003		85.75		99.99533		789.34998		85.75		100.00098		814.3889		85.75		100.04207		815.89244		85.75		100.06385		817.60867		85.75		100.03584

		789.67999		85.775		99.99771		100.04207		789.29199		85.775		99.99323		789.62		85.775		99.99928		814.64046		85.775		100.04207		816.13443		85.775		100.06382		817.86001		85.775		100.03585

		789.93402		85.8		99.9983		100.04207		789.55701		85.8		99.99399		789.86902		85.8		99.99984		814.89345		85.8		100.04207		816.38499		85.8		100.06379		818.11378		85.8		100.03587

		790.19598		85.825		99.99509		100.04207		789.82098		85.825		99.99213		790.14203		85.825		99.99689		815.14756		85.825		100.04207		816.63854		85.825		100.06377		818.367		85.825		100.03588

		790.46399		85.85		99.99729		100.04208		790.08002		85.85		99.99453		790.39801		85.85		100.0011		815.39267		85.85		100.04208		816.89277		85.85		100.06375		818.61234		85.85		100.03591

		790.71002		85.875		99.99873		100.04209		790.336		85.875		99.99651		790.65302		85.875		100.00084		815.63801		85.875		100.04209		817.14821		85.875		100.06374		818.85746		85.875		100.03593

		790.97803		85.9		99.999		100.0421		790.59601		85.9		99.9936		790.91803		85.9		100.00107		815.88123		85.9		100.0421		817.40244		85.9		100.06372		819.1009		85.9		100.03596

		791.242		85.925		99.99982		100.04212		790.85602		85.925		99.99635		791.17499		85.925		100.00414		816.122		85.925		100.04212		817.65522		85.925		100.06372		819.34734		85.925		100.03598

		791.505		85.95		99.99966		100.04214		791.10999		85.95		99.99451		791.44202		85.95		100.00053		816.37111		85.95		100.04214		817.90866		85.95		100.06371		819.59989		85.95		100.03601

		791.76398		85.975		99.99745		100.04217		791.38202		85.975		99.9963		791.70398		85.975		99.99942		816.61967		85.975		100.04217		818.16267		85.975		100.06372		819.85211		85.975		100.03603

		792.021		86		99.99771		100.04219		791.63702		86		99.99436		791.95398		86		99.99944		816.87045		86		100.04219		818.41423		86		100.06372		820.10544		86		100.03606

		792.28998		86.025		99.99817		100.0422		791.89398		86.025		99.99449		792.23297		86.025		100.00063		817.12201		86.025		100.0422		818.65767		86.025		100.06373		820.35811		86.025		100.03608

		792.55402		86.05		99.99948		100.04222		792.15698		86.05		99.99609		792.48999		86.05		100.00117		817.37323		86.05		100.04222		818.90145		86.05		100.06374		820.61133		86.05		100.03609

		792.815		86.075		99.99765		100.04223		792.41901		86.075		99.99294		792.74402		86.075		100.00118		817.62423		86.075		100.04223		819.14433		86.075		100.06376		820.86422		86.075		100.0361

		793.07501		86.1		99.99772		100.04223		792.67102		86.1		99.99318		792.99799		86.1		99.99803		817.87412		86.1		100.04223		819.39178		86.1		100.06378		821.11388		86.1		100.0361

		793.33698		86.125		99.99695		100.04222		792.93903		86.125		99.99234		793.26898		86.125		100.0021		818.12657		86.125		100.04222		819.64089		86.125		100.0638		821.36666		86.125		100.0361

		793.58502		86.15		99.99881		100.04221		793.18903		86.15		99.99396		793.526		86.15		100.00338		818.37779		86.15		100.04221		819.89345		86.15		100.06382		821.61355		86.15		100.03609

		793.854		86.175		99.99683		100.04219		793.45801		86.175		99.99447		793.78601		86.175		99.99992		818.61912		86.175		100.04219		820.14656		86.175		100.06385		821.856		86.175		100.03609

		794.12		86.2		99.99613		100.04217		793.71198		86.2		99.99247		794.03699		86.2		99.99642		818.86179		86.2		100.04217		820.40011		86.2		100.06388		822.09611		86.2		100.03607

		794.37903		86.225		99.99992		100.04215		793.96802		86.225		99.99514		794.31		86.225		99.99911		819.10223		86.225		100.04215		820.65733		86.225		100.06392		822.33434		86.225		100.03606

		794.63898		86.25		99.99873		100.04213		794.22998		86.25		99.99537		794.57202		86.25		99.99859		819.34612		86.25		100.04213		820.91267		86.25		100.06396		822.57589		86.25		100.03605

		794.90399		86.275		99.99649		100.04211		794.48901		86.275		99.99301		794.83301		86.275		99.99685		819.59401		86.275		100.04211		821.16533		86.275		100.064		822.82356		86.275		100.03605

		795.15002		86.3		99.99864		100.0421		794.75702		86.3		99.99352		795.10303		86.3		99.9996		819.84368		86.3		100.0421		821.41745		86.3		100.06405		823.07212		86.3		100.03605

		795.42401		86.325		99.99879		100.0421		795.01703		86.325		99.99564		795.362		86.325		100.00147		820.09524		86.325		100.0421		821.66523		86.325		100.0641		823.3219		86.325		100.03606

		795.68103		86.35		99.99946		100.04211		795.26801		86.35		99.99281		795.61499		86.35		100.00258		820.34612		86.35		100.04211		821.91168		86.35		100.06416		823.5729		86.35		100.03607

		795.94098		86.375		99.99847		100.04212		795.52002		86.375		99.99341		795.88202		86.375		100.00003		820.59856		86.375		100.04212		822.15489		86.375		100.06422		823.82256		86.375		100.03609

		796.20502		86.4		99.99806		100.04215		795.78198		86.4		99.99331		796.14301		86.4		100.00201		820.8529		86.4		100.04215		822.39667		86.4		100.06429		824.07345		86.4		100.03612

		796.46301		86.425		99.99925		100.04218		796.04797		86.425		99.99762		796.401		86.425		100.00224		821.10379		86.425		100.04218		822.64589		86.425		100.06435		824.32523		86.425		100.03616

		796.71198		86.45		100.00001		100.04223		796.32202		86.45		99.9956		796.66101		86.45		100.00085		821.3559		86.45		100.04223		822.89545		86.45		100.06443		824.57967		86.45		100.0362

		796.97998		86.475		99.9983		100.04228		796.57703		86.475		99.99541		796.91998		86.475		100.0007		821.606		86.475		100.04228		823.14745		86.475		100.0645		824.83112		86.475		100.03625

		797.24103		86.5		99.99645		100.04233		796.83698		86.5		99.99389		797.17999		86.5		100.00024		821.85278		86.5		100.04233		823.39979		86.5		100.06458		825.07467		86.5		100.03631

		797.505		86.525		99.99882		100.04239		797.09497		86.525		99.99666		797.44397		86.525		100.00058		822.09867		86.525		100.04239		823.65356		86.525		100.06466		825.31545		86.525		100.03636

		797.75702		86.55		99.99731		100.04245		797.36102		86.55		99.99533		797.70801		86.55		99.99896		822.34245		86.55		100.04245		823.90557		86.55		100.06474		825.55856		86.55		100.03642

		798.01398		86.575		99.99851		100.04251		797.61603		86.575		99.99318		797.966		86.575		100.00128		822.58889		86.575		100.04251		824.15734		86.575		100.06482		825.80223		86.575		100.03649

		798.28003		86.6		99.99919		100.04256		797.87402		86.6		99.99942		798.224		86.6		100.00166		822.83911		86.6		100.04256		824.41079		86.6		100.06489		826.04989		86.6		100.03655

		798.53802		86.625		99.99803		100.04262		798.13702		86.625		99.99439		798.48798		86.625		99.99897		823.089		86.625		100.04262		824.66379		86.625		100.06497		826.29856		86.625		100.03661

		798.79498		86.65		99.99735		100.04267		798.39502		86.65		99.99298		798.742		86.65		99.99869		823.34199		86.65		100.04267		824.91001		86.65		100.06505		826.54889		86.65		100.03667

		799.06		86.675		99.99739		100.04272		798.659		86.675		99.99221		799.00299		86.675		100.0008		823.59722		86.675		100.04272		825.15124		86.675		100.06513		826.79878		86.675		100.03673

		799.32501		86.7		99.99944		100.04277		798.91699		86.7		99.99485		799.27002		86.7		100.00246		823.85088		86.7		100.04277		825.39179		86.7		100.0652		827.049		86.7		100.03679

		799.58398		86.725		99.99775		100.04281		799.17902		86.725		99.99224		799.53003		86.725		100.001		824.10522		86.725		100.04281		825.63246		86.725		100.06527		827.30111		86.725		100.03685

		799.84198		86.75		99.99684		100.04285		799.43402		86.75		99.99449		799.78998		86.75		99.99782		824.35866		86.75		100.04285		825.88046		86.75		100.06534		827.55589		86.75		100.0369

		800.10602		86.775		99.99642		100.04289		799.698		86.775		99.98997		800.05402		86.775		99.99827		824.61355		86.775		100.04289		826.13057		86.775		100.0654		827.80777		86.775		100.03695

		800.37299		86.8		99.99855		100.04293		799.95502		86.8		99.99402		800.30603		86.8		99.99985		824.86511		86.8		100.04293		826.38257		86.8		100.06546		828.05533		86.8		100.037

		800.63501		86.825		99.99737		100.04297		800.22601		86.825		99.99461		800.56897		86.825		99.99993		825.11144		86.825		100.04297		826.63568		86.825		100.06552		828.29933		86.825		100.03704

		800.88397		86.85		99.999		100.04301		800.48102		86.85		99.9958		800.83197		86.85		100.00206		825.35611		86.85		100.04301		826.89212		86.85		100.06557		828.54211		86.85		100.03708

		801.14301		86.875		99.99786		100.04304		800.742		86.875		99.99411		801.09003		86.875		100.0016		825.60044		86.875		100.04304		827.1479		86.875		100.06562		828.78345		86.875		100.03712

		801.41302		86.9		99.99928		100.04307		801		86.9		99.99387		801.35602		86.9		100.00186		825.84989		86.9		100.04307		827.4039		86.9		100.06566		829.02933		86.9		100.03715

		801.66803		86.925		99.99938		100.0431		801.26801		86.925		99.99526		801.604		86.925		100.00115		826.10189		86.925		100.0431		827.65934		86.925		100.06569		829.28022		86.925		100.03717

		801.93402		86.95		99.99817		100.04313		801.52197		86.95		99.99396		801.87598		86.95		100.0014		826.35222		86.95		100.04313		827.91501		86.95		100.06572		829.53222		86.95		100.03719

		802.19		86.975		99.99712		100.04315		801.78302		86.975		99.99426		802.14203		86.975		99.99901		826.60244		86.975		100.04315		828.16156		86.975		100.06574		829.78266		86.975		100.0372

		802.44897		87		99.99716		100.04317		802.04602		87		99.9928		802.40002		87		100.00013		826.85312		87		100.04317		828.40978		87		100.06575		830.03422		87		100.03721

		802.70898		87.025		100.00008		100.04318		802.29999		87.025		99.99571		802.66101		87.025		100.001		827.10434		87.025		100.04318		828.65456		87.025		100.06576		830.28633		87.025		100.03721

		802.96997		87.05		99.99921		100.04318		802.56201		87.05		99.99388		802.92297		87.05		100.00062		827.35678		87.05		100.04318		828.89812		87.05		100.06576		830.54066		87.05		100.03721

		803.22601		87.075		99.99876		100.04318		802.82397		87.075		99.99324		803.17999		87.075		100.00073		827.61112		87.075		100.04318		829.14667		87.075		100.06575		830.79422		87.075		100.03721

		803.49597		87.1		99.99612		100.04316		803.08002		87.1		99.99545		803.44397		87.1		99.99973		827.86468		87.1		100.04316		829.39645		87.1		100.06575		831.047		87.1		100.0372

		803.76398		87.125		99.9999		100.04314		803.33899		87.125		99.99613		803.70203		87.125		100.00057		828.10902		87.125		100.04314		829.64712		87.125		100.06573		831.29233		87.125		100.03719

		804.01001		87.15		99.9972		100.0431		803.60199		87.15		99.99416		803.96301		87.15		99.99927		828.35068		87.15		100.0431		829.90034		87.15		100.06572		831.53311		87.15		100.03718

		804.28198		87.175		99.9973		100.04306		803.875		87.175		99.99491		804.21802		87.175		99.99993		828.59224		87.175		100.04306		830.15201		87.175		100.0657		831.77256		87.175		100.03717

		804.53802		87.2		99.99756		100.043		804.12402		87.2		99.99549		804.48798		87.2		100.00137		828.8359		87.2		100.043		830.40701		87.2		100.06568		832.00956		87.2		100.03717

		804.79102		87.225		99.99641		100.04294		804.38397		87.225		99.99384		804.74701		87.225		99.99896		829.08824		87.225		100.04294		830.65901		87.225		100.06566		832.25322		87.225		100.03716

		805.065		87.25		99.9995		100.04287		804.64899		87.25		99.99538		805.01703		87.25		100.00139		829.34313		87.25		100.04287		830.91256		87.25		100.06563		832.502		87.25		100.03715

		805.31897		87.275		99.99916		100.0428		804.90997		87.275		99.99605		805.27802		87.275		100.00038		829.59802		87.275		100.0428		831.16612		87.275		100.06561		832.75033		87.275		100.03715

		805.57397		87.3		99.99784		100.04272		805.17102		87.3		99.99449		805.53802		87.3		99.99935		829.85246		87.3		100.04272		831.41178		87.3		100.06558		832.99856		87.3		100.03715

		805.83801		87.325		99.99641		100.04264		805.43402		87.325		99.99616		805.797		87.325		100.0004		830.10657		87.325		100.04264		831.65523		87.325		100.06556		833.24756		87.325		100.03716

		806.09399		87.35		100.00093		100.04256		805.69202		87.35		99.99262		806.06201		87.35		99.9996		830.36312		87.35		100.04256		831.899		87.35		100.06554		833.49934		87.35		100.03717

		806.36102		87.375		99.99659		100.04248		805.95502		87.375		99.99401		806.323		87.375		99.99906		830.61956		87.375		100.04248		832.14433		87.375		100.06551		833.75033		87.375		100.03718

		806.61298		87.4		99.99856		100.04241		806.20203		87.4		99.99352		806.58502		87.4		100.00044		830.87822		87.4		100.04241		832.39712		87.4		100.06549		834.00111		87.4		100.03719

		806.88		87.425		99.99624		100.04235		806.47302		87.425		99.99426		806.836		87.425		99.9986		831.13477		87.425		100.04235		832.64789		87.425		100.06546		834.25656		87.425		100.03721

		807.15002		87.45		99.99786		100.0423		806.72803		87.45		99.99335		807.10303		87.45		100.00093		831.38277		87.45		100.0423		832.89889		87.45		100.06544		834.50322		87.45		100.03723

		807.40698		87.475		99.99903		100.04226		806.99402		87.475		99.99504		807.36401		87.475		99.99942		831.62811		87.475		100.04226		833.15034		87.475		100.06541		834.74611		87.475		100.03725

		807.66699		87.5		99.99754		100.04223		807.25702		87.5		99.99507		807.61798		87.5		99.99926		831.87344		87.5		100.04223		833.40345		87.5		100.06539		834.98633		87.5		100.03727

		807.927		87.525		99.99759		100.04221		807.505		87.525		99.99256		807.87701		87.525		100.00069		832.11644		87.525		100.04221		833.65856		87.525		100.06536		835.22866		87.525		100.0373

		808.19397		87.55		99.9959		100.0422		807.76202		87.55		99.9903		808.14001		87.55		99.99908		832.36622		87.55		100.0422		833.91323		87.55		100.06534		835.48066		87.55		100.03732

		808.44501		87.575		99.99773		100.0422		808.02502		87.575		99.99383		808.40997		87.575		99.99961		832.61466		87.575		100.0422		834.16812		87.575		100.06531		835.73288		87.575		100.03735

		808.71399		87.6		99.99793		100.04222		808.289		87.6		99.99482		808.659		87.6		99.99991		832.866		87.6		100.04222		834.42056		87.6		100.06529		835.98511		87.6		100.03738

		808.97998		87.625		99.99891		100.04224		808.55103		87.625		99.99602		808.92297		87.625		100.00223		833.11422		87.625		100.04224		834.66711		87.625		100.06527		836.23833		87.625		100.0374

		809.23798		87.65		100.00012		100.04228		808.80402		87.65		99.9939		809.18597		87.65		99.99907		833.36545		87.65		100.04228		834.91233		87.65		100.06525		836.48878		87.65		100.03743

		809.49701		87.675		99.99649		100.04232		809.06897		87.675		99.99606		809.45502		87.675		99.99939		833.61723		87.675		100.04232		835.15611		87.675		100.06523		836.74089		87.675		100.03746

		809.745		87.7		99.99801		100.04237		809.32599		87.7		99.9938		809.716		87.7		100.00111		833.87		87.7		100.04237		835.40723		87.7		100.06522		836.99134		87.7		100.0375

		810.01398		87.725		100.00113		100.04243		809.59497		87.725		99.99494		809.96997		87.725		100.00219		834.12278		87.725		100.04243		835.66012		87.725		100.06521		837.24701		87.725		100.03753

		810.26898		87.75		99.99883		100.04248		809.84497		87.75		99.99896		810.22998		87.75		100.00028		834.37855		87.75		100.04248		835.91045		87.75		100.0652		837.50056		87.75		100.03756

		810.53497		87.775		99.99891		100.04254		810.10498		87.775		99.99541		810.48798		87.775		100.00127		834.627		87.775		100.04254		836.16256		87.775		100.0652		837.74467		87.775		100.03759

		810.79102		87.8		99.99881		100.04261		810.37097		87.8		99.99503		810.75098		87.8		100.00123		834.87455		87.8		100.04261		836.41412		87.8		100.06521		837.98734		87.8		100.03763

		811.05298		87.825		99.99531		100.04267		810.62402		87.825		99.99319		811.01001		87.825		99.99963		835.11655		87.825		100.04267		836.66679		87.825		100.06522		838.23123		87.825		100.03766

		811.31702		87.85		99.99836		100.04273		810.89301		87.85		99.99401		811.27502		87.85		100.00106		835.36599		87.85		100.04273		836.91768		87.85		100.06524		838.47289		87.85		100.0377

		811.57599		87.875		99.99637		100.04279		811.14398		87.875		99.99347		811.53998		87.875		99.99741		835.61866		87.875		100.04279		837.17124		87.875		100.06527		838.72267		87.875		100.03773

		811.84399		87.9		99.9984		100.04286		811.41699		87.9		99.99131		811.79498		87.9		100.00022		835.8711		87.9		100.04286		837.42524		87.9		100.0653		838.97722		87.9		100.03776

		812.10498		87.925		99.99727		100.04291		811.67297		87.925		99.99402		812.05701		87.925		100.00095		836.12499		87.925		100.04291		837.66935		87.925		100.06533		839.23355		87.925		100.0378

		812.37299		87.95		99.9983		100.04297		811.93597		87.95		99.9946		812.31097		87.95		100.00068		836.37855		87.95		100.04297		837.91001		87.95		100.06537		839.48733		87.95		100.03783

		812.63098		87.975		99.99848		100.04303		812.19501		87.975		99.99466		812.57098		87.975		99.99971		836.63189		87.975		100.04303		838.15523		87.975		100.06542		839.74056		87.975		100.03786

		812.89203		88		99.99659		100.04308		812.45203		88		99.99472		812.83197		88		99.99956		836.88466		88		100.04308		838.39989		88		100.06547		839.99411		88		100.03788

		813.15601		88.025		99.99627		100.04313		812.71503		88.025		99.9962		813.09497		88.025		100.0001		837.13511		88.025		100.04313		838.65333		88.025		100.06552		840.24789		88.025		100.03791

		813.414		88.05		99.99769		100.04318		812.966		88.05		99.99166		813.35101		88.05		99.99843		837.38955		88.05		100.04318		838.90788		88.05		100.06557		840.49955		88.05		100.03793

		813.68201		88.075		99.99889		100.04322		813.224		88.075		99.99486		813.612		88.075		100.00014		837.63845		88.075		100.04322		839.16333		88.075		100.06562		840.75489		88.075		100.03796

		813.93103		88.1		99.99916		100.04327		813.48602		88.1		99.9956		813.87		88.1		100.00261		837.88022		88.1		100.04327		839.41688		88.1		100.06568		841.003		88.1		100.03798

		814.20099		88.125		99.99815		100.04331		813.75		88.125		99.99355		814.14801		88.125		100.00072		838.12023		88.125		100.04331		839.67211		88.125		100.06573		841.24678		88.125		100.03801

		814.46002		88.15		99.99613		100.04336		814.01703		88.15		99.99139		814.40802		88.15		100.00061		838.35723		88.15		100.04336		839.93144		88.15		100.06578		841.48855		88.15		100.03804

		814.72101		88.175		99.99864		100.0434		814.27698		88.175		99.99416		814.66998		88.175		99.99951		838.60133		88.175		100.0434		840.19078		88.175		100.06584		841.72955		88.175		100.03807

		814.97803		88.2		99.99784		100.04345		814.53497		88.2		99.99631		814.927		88.2		99.99998		838.84955		88.2		100.04345		840.44722		88.2		100.06589		841.97999		88.2		100.0381

		815.23102		88.225		99.99941		100.0435		814.78998		88.225		99.99568		815.19299		88.225		100.00099		839.09911		88.225		100.0435		840.704		88.225		100.06595		842.23033		88.225		100.03814

		815.50403		88.25		99.99712		100.04355		815.052		88.25		99.9942		815.44598		88.25		100.00066		839.35233		88.25		100.04355		840.95089		88.25		100.06601		842.48155		88.25		100.03817

		815.76099		88.275		99.99712		100.0436		815.31702		88.275		99.99472		815.71802		88.275		99.9985		839.605		88.275		100.0436		841.1959		88.275		100.06606		842.73556		88.275		100.03822

		816.00897		88.3		100.00063		100.04366		815.57001		88.3		99.99557		815.96997		88.3		100.00052		839.85866		88.3		100.04366		841.44		88.3		100.06612		842.98855		88.3		100.03826

		816.27899		88.325		99.99756		100.04372		815.841		88.325		99.99248		816.22699		88.325		99.99853		840.11256		88.325		100.04372		841.68267		88.325		100.06618		843.24144		88.325		100.03831

		816.53802		88.35		99.99671		100.04378		816.10602		88.35		99.99323		816.48297		88.35		99.99958		840.36589		88.35		100.04378		841.93623		88.35		100.06624		843.49167		88.35		100.03835

		816.80603		88.375		99.9951		100.04384		816.36499		88.375		99.99116		816.74701		88.375		99.99794		840.62		88.375		100.04384		842.18933		88.375		100.0663		843.743		88.375		100.0384

		817.06		88.4		99.99904		100.0439		816.62701		88.4		99.99336		817.013		88.4		100.00114		840.86599		88.4		100.0439		842.44255		88.4		100.06637		843.99422		88.4		100.03846

		817.32001		88.425		99.99955		100.04396		816.87402		88.425		99.99374		817.276		88.425		100.0006		841.11044		88.425		100.04396		842.69611		88.425		100.06643		844.23611		88.425		100.03851

		817.586		88.45		99.99821		100.04403		817.13898		88.45		99.99358		817.52802		88.45		100.00053		841.35421		88.45		100.04403		842.95011		88.45		100.06649		844.47588		88.45		100.03856

		817.849		88.475		99.99938		100.04409		817.40002		88.475		99.99589		817.79498		88.475		100.00007		841.59732		88.475		100.04409		843.20544		88.475		100.06656		844.71478		88.475		100.03861

		818.11401		88.5		100.0013		100.04415		817.66803		88.5		99.99611		818.047		88.5		100.00028		841.84632		88.5		100.04415		843.45978		88.5		100.06662		844.95933		88.5		100.03865

		818.37299		88.525		100.00022		100.04421		817.91998		88.525		99.99618		818.31201		88.525		100.00084		842.09543		88.525		100.04421		843.71623		88.525		100.06667		845.20856		88.525		100.0387

		818.64001		88.55		99.99672		100.04426		818.18701		88.55		99.99207		818.57001		88.55		100.00028		842.34698		88.55		100.04426		843.97511		88.55		100.06673		845.45812		88.55		100.03874

		818.89502		88.575		99.99982		100.04431		818.44202		88.575		99.99297		818.83502		88.575		100.00013		842.59943		88.575		100.04431		844.221		88.575		100.06678		845.71178		88.575		100.03877

		819.15802		88.6		99.99789		100.04436		818.69897		88.6		99.99257		819.09399		88.6		99.99918		842.85566		88.6		100.04436		844.46389		88.6		100.06682		845.966		88.6		100.03881

		819.41302		88.625		100.00022		100.0444		818.96899		88.625		99.99567		819.35901		88.625		100.0007		843.11288		88.625		100.0444		844.70622		88.625		100.06687		846.22044		88.625		100.03883

		819.67902		88.65		99.99895		100.04443		819.22498		88.65		99.996		819.61499		88.65		100.00137		843.36766		88.65		100.04443		844.95278		88.65		100.0669		846.475		88.65		100.03886

		819.94		88.675		99.99724		100.04446		819.48999		88.675		99.99388		819.87799		88.675		99.99822		843.62255		88.675		100.04446		845.205		88.675		100.06694		846.73378		88.675		100.03888

		820.19702		88.7		99.99708		100.04449		819.75201		88.7		99.99442		820.14398		88.7		99.99827		843.87944		88.7		100.04449		845.45756		88.7		100.06697		846.99222		88.7		100.0389

		820.46002		88.725		99.99852		100.04452		820.013		88.725		99.99363		820.40198		88.725		99.99854		844.12811		88.725		100.04452		845.70911		88.725		100.067		847.24022		88.725		100.03891

		820.72803		88.75		99.99792		100.04454		820.27502		88.75		99.99253		820.66699		88.75		100.00046		844.37356		88.75		100.04454		845.96067		88.75		100.06703		847.48433		88.75		100.03893

		820.97198		88.775		99.99847		100.04457		820.53699		88.775		99.99462		820.92297		88.775		100.00126		844.61645		88.775		100.04457		846.21167		88.775		100.06706		847.72833		88.775		100.03894

		821.242		88.8		99.99834		100.04459		820.81299		88.8		99.99482		821.18799		88.8		99.9996		844.85822		88.8		100.04459		846.46389		88.8		100.06709		847.96988		88.8		100.03895

		821.50598		88.825		99.99972		100.04461		821.06		88.825		99.99587		821.44299		88.825		100.00168		845.10533		88.825		100.04461		846.72022		88.825		100.06713		848.21577		88.825		100.03897

		821.76703		88.85		100.00009		100.04463		821.31598		88.85		99.99547		821.703		88.85		100.00101		845.35778		88.85		100.04463		846.97833		88.85		100.06716		848.467		88.85		100.03898

		822.02301		88.875		99.99765		100.04465		821.57599		88.875		99.99232		821.96698		88.875		99.99946		845.611		88.875		100.04465		847.22944		88.875		100.0672		848.72344		88.875		100.039

		822.29199		88.9		99.99769		100.04468		821.84198		88.9		99.99242		822.24103		88.9		99.99916		845.86523		88.9		100.04468		847.47178		88.9		100.06724		848.97566		88.9		100.03902

		822.54901		88.925		99.99693		100.0447		822.10101		88.925		99.98896		822.49902		88.925		99.99829		846.11612		88.925		100.0447		847.71534		88.925		100.06729		849.22533		88.925		100.03904

		822.81201		88.95		99.99755		100.04472		822.362		88.95		99.99131		822.75098		88.95		99.99959		846.36789		88.95		100.04472		847.96056		88.95		100.06734		849.47844		88.95		100.03906

		823.07501		88.975		99.99969		100.04474		822.61902		88.975		99.99334		823.013		88.975		99.999		846.62156		88.975		100.04474		848.20856		88.975		100.06739		849.73244		88.975		100.03908

		823.33197		89		99.99813		100.04476		822.89001		89		99.99423		823.27802		89		99.99961		846.87823		89		100.04476		848.46067		89		100.06744		849.986		89		100.03911

		823.59497		89.025		99.99872		100.04477		823.15198		89.025		99.99426		823.53601		89.025		100.00088		847.13612		89.025		100.04477		848.71645		89.025		100.06748		850.23922		89.025		100.03913

		823.85999		89.05		99.99616		100.04478		823.40802		89.05		99.99265		823.79401		89.05		99.99716		847.38345		89.05		100.04478		848.96922		89.05		100.06753		850.48688		89.05		100.03916

		824.12097		89.075		99.99805		100.04478		823.66803		89.075		99.99414		824.05603		89.075		100.00036		847.62534		89.075		100.04478		849.22034		89.075		100.06757		850.72944		89.075		100.03918

		824.39099		89.1		99.99925		100.04478		823.92999		89.1		99.9965		824.31897		89.1		100.00142		847.8649		89.1		100.04478		849.47367		89.1		100.0676		850.96566		89.1		100.03921

		824.64502		89.125		99.99686		100.04477		824.19299		89.125		99.9928		824.58197		89.125		100.00193		848.10245		89.125		100.04477		849.72966		89.125		100.06763		851.20245		89.125		100.03923

		824.90503		89.15		99.99687		100.04475		824.44202		89.15		99.99156		824.849		89.15		99.99951		848.35023		89.15		100.04475		849.9831		89.15		100.06765		851.44977		89.15		100.03924

		825.16498		89.175		99.9964		100.04472		824.70801		89.175		99.99399		825.09601		89.175		100.00017		848.60045		89.175		100.04472		850.23443		89.175		100.06767		851.7		89.175		100.03926

		825.42603		89.2		99.99855		100.04469		824.97601		89.2		99.99567		825.35797		89.2		100.00048		848.8529		89.2		100.04469		850.48121		89.2		100.06768		851.94722		89.2		100.03927

		825.69702		89.225		99.99676		100.04466		825.24402		89.225		99.9918		825.61902		89.225		99.99927		849.10367		89.225		100.04466		850.72343		89.225		100.06768		852.19288		89.225		100.03928

		825.94397		89.25		99.99733		100.04462		825.50598		89.25		99.99216		825.88202		89.25		99.99962		849.35556		89.25		100.04462		850.96065		89.25		100.06768		852.44011		89.25		100.03928

		826.21503		89.275		99.99898		100.04458		825.76202		89.275		99.99442		826.14697		89.275		100.00026		849.61089		89.275		100.04458		851.19821		89.275		100.06768		852.688		89.275		100.03929

		826.46698		89.3		99.9972		100.04454		826.026		89.3		99.99449		826.41199		89.3		100.00082		849.866		89.3		100.04454		851.44354		89.3		100.06768		852.93633		89.3		100.0393

		826.73602		89.325		99.99819		100.04451		826.29102		89.325		99.99442		826.67499		89.325		100.00025		850.11966		89.325		100.04451		851.6921		89.325		100.06768		853.18589		89.325		100.0393

		827.00299		89.35		99.99873		100.04447		826.54401		89.35		99.9965		826.93298		89.35		100.00084		850.3741		89.35		100.04447		851.94132		89.35		100.06769		853.43644		89.35		100.03931

		827.26202		89.375		99.99582		100.04445		826.815		89.375		99.99411		827.19598		89.375		99.99919		850.62133		89.375		100.04445		852.19155		89.375		100.0677		853.67911		89.375		100.03932

		827.53101		89.4		99.9952		100.04443		827.07898		89.4		99.99584		827.46198		89.4		99.99801		850.865		89.4		100.04443		852.44222		89.4		100.06771		853.91844		89.4		100.03934

		827.784		89.425		99.9976		100.04441		827.336		89.425		99.99354		827.716		89.425		99.9989		851.10633		89.425		100.04441		852.69455		89.425		100.06773		854.15589		89.425		100.03935

		828.03998		89.45		99.99648		100.0444		827.599		89.45		99.98957		827.97302		89.45		99.99952		851.349		89.45		100.0444		852.94578		89.45		100.06775		854.39656		89.45		100.03937

		828.30103		89.475		99.99699		100.04439		827.849		89.475		99.98904		828.24597		89.475		99.99972		851.59667		89.475		100.04439		853.19889		89.475		100.06778		854.64478		89.475		100.03939

		828.56598		89.5		99.99752		100.04439		828.12299		89.5		99.99236		828.48901		89.5		100.00208		851.84244		89.5		100.04439		853.45345		89.5		100.06781		854.89423		89.5		100.03941

		828.828		89.525		99.99826		100.04439		828.38898		89.525		99.99043		828.76599		89.525		99.99965		852.08811		89.525		100.04439		853.69912		89.525		100.06784		855.142		89.525		100.03943

		829.09399		89.55		99.99682		100.04439		828.64801		89.55		99.99204		829.01898		89.55		100.00136		852.33655		89.55		100.04439		853.93867		89.55		100.06787		855.39145		89.55		100.03945

		829.34198		89.575		99.99944		100.0444		828.91302		89.575		99.99782		829.28699		89.575		100.00039		852.58756		89.575		100.0444		854.17423		89.575		100.0679		855.64189		89.575		100.03947

		829.59802		89.6		99.99764		100.0444		829.177		89.6		99.99758		829.53998		89.6		100.00042		852.83789		89.6		100.0444		854.41168		89.6		100.06793		855.89155		89.6		100.03948

		829.86401		89.625		99.99984		100.0444		829.42499		89.625		99.9982		829.79999		89.625		100.00204		853.09011		89.625		100.0444		854.65778		89.625		100.06795		856.14089		89.625		100.03949

		830.13		89.65		99.99885		100.04439		829.67798		89.65		99.99901		830.06		89.65		99.99797		853.34166		89.65		100.04439		854.903		89.65		100.06797		856.39423		89.65		100.03949

		830.39398		89.675		99.99807		100.04438		829.94501		89.675		99.9945		830.323		89.675		100.00307		853.59344		89.675		100.04438		855.15055		89.675		100.06798		856.64756		89.675		100.0395

		830.65302		89.7		99.99894		100.04437		830.20801		89.7		99.99546		830.586		89.7		99.99803		853.83888		89.7		100.04437		855.39889		89.7		100.06799		856.89078		89.7		100.0395

		830.909		89.725		99.99855		100.04436		830.45898		89.725		99.99351		830.84998		89.725		99.99846		854.08355		89.725		100.04436		855.64644		89.725		100.06799		857.13		89.725		100.03949

		831.17603		89.75		99.99868		100.04435		830.724		89.75		99.99467		831.12097		89.75		99.99846		854.32766		89.75		100.04435		855.89311		89.75		100.06799		857.36989		89.75		100.03949

		831.44		89.775		99.9973		100.04433		830.98901		89.775		99.99414		831.37701		89.775		99.99862		854.57722		89.775		100.04433		856.14022		89.775		100.06799		857.6059		89.775		100.03948

		831.69702		89.8		100.00007		100.04432		831.24597		89.8		99.99331		831.63397		89.8		100.00286		854.82722		89.8		100.04432		856.39233		89.8		100.06798		857.84989		89.8		100.03948

		831.95697		89.825		99.99915		100.04432		831.50299		89.825		99.99295		831.90399		89.825		100.00204		855.07711		89.825		100.04432		856.64177		89.825		100.06798		858.09767		89.825		100.03948

		832.21198		89.85		99.99929		100.04432		831.76099		89.85		99.99292		832.15601		89.85		99.99802		855.32867		89.85		100.04432		856.88222		89.85		100.06798		858.34467		89.85		100.03948

		832.48102		89.875		99.99501		100.04432		832.02899		89.875		99.98936		832.427		89.875		100.00007		855.58078		89.875		100.04432		857.1221		89.875		100.06799		858.59066		89.875		100.03949

		832.73499		89.9		99.99865		100.04434		832.289		89.9		99.99426		832.68201		89.9		99.9991		855.83		89.9		100.04434		857.35999		89.9		100.068		858.83466		89.9		100.0395

		832.992		89.925		99.99747		100.04436		832.56097		89.925		99.99503		832.93402		89.925		99.99834		856.08034		89.925		100.04436		857.59533		89.925		100.06801		859.08133		89.925		100.03951

		833.258		89.95		100.00004		100.04439		832.81702		89.95		99.99483		833.203		89.95		100.00134		856.33023		89.95		100.04439		857.8391		89.95		100.06803		859.33078		89.95		100.03953

		833.52802		89.975		99.99775		100.04443		833.078		89.975		99.99472		833.46399		89.975		99.99935		856.58322		89.975		100.04443		858.08856		89.975		100.06805		859.57989		89.975		100.03956

		833.78802		90		99.99904		100.04448		833.34601		90		99.99825		833.72601		90		100.00186		856.83		90		100.04448		858.33956		90		100.06808		859.83133		90		100.03958

		834.04401		90.025		99.99742		100.04454		833.60699		90.025		99.99235		833.98401		90.025		99.99786		857.072		90.025		100.04454		858.58678		90.025		100.06811		860.07178		90.025		100.03961

		834.30798		90.05		99.99949		100.0446		833.87		90.05		99.99409		834.255		90.05		100.00032		857.31389		90.05		100.0446		858.836		90.05		100.06815		860.311		90.05		100.03965

		834.56897		90.075		99.99938		100.04466		834.11902		90.075		99.99345		834.51703		90.075		100.00106		857.55311		90.075		100.04466		859.088		90.075		100.06818		860.5509		90.075		100.03968

		834.83502		90.1		99.99746		100.04474		834.38202		90.1		99.99545		834.77002		90.1		100.00141		857.80011		90.1		100.04474		859.34212		90.1		100.06822		860.79211		90.1		100.03971

		835.10699		90.125		99.99963		100.04481		834.64697		90.125		99.99402		835.03003		90.125		100.00031		858.04966		90.125		100.04481		859.59745		90.125		100.06826		861.04045		90.125		100.03975

		835.35101		90.15		100.0002		100.04488		834.90503		90.15		99.99509		835.29999		90.15		100.0006		858.29955		90.15		100.04488		859.85156		90.15		100.0683		861.28855		90.15		100.03978

		835.60901		90.175		99.99955		100.04495		835.15997		90.175		99.99322		835.55701		90.175		100.00018		858.55077		90.175		100.04495		860.09534		90.175		100.06833		861.53499		90.175		100.03981

		835.87299		90.2		99.99623		100.04502		835.42999		90.2		99.9944		835.815		90.2		100.00077		858.79833		90.2		100.04502		860.33501		90.2		100.06837		861.78288		90.2		100.03984

		836.13202		90.225		99.99747		100.04509		835.67902		90.225		99.99511		836.07397		90.225		100.00116		859.048		90.225		100.04509		860.57412		90.225		100.06841		862.0321		90.225		100.03986

		836.38702		90.25		99.99714		100.04515		835.94897		90.25		99.99497		836.34601		90.25		100.00031		859.29955		90.25		100.04515		860.81645		90.25		100.06845		862.28466		90.25		100.03989

		836.65698		90.275		100.00051		100.0452		836.20398		90.275		99.99507		836.604		90.275		100.00132		859.551		90.275		100.0452		861.0659		90.275		100.06848		862.53722		90.275		100.03991

		836.92102		90.3		99.99878		100.04525		836.47803		90.3		99.99165		836.86798		90.3		99.99983		859.80256		90.3		100.04525		861.31557		90.3		100.06852		862.78977		90.3		100.03994

		837.172		90.325		99.99831		100.04529		836.72803		90.325		99.99361		837.133		90.325		99.99918		860.04389		90.325		100.04529		861.56468		90.325		100.06856		863.03677		90.325		100.03997

		837.435		90.35		99.99772		100.04532		836.995		90.35		99.9953		837.39001		90.35		100.0005		860.28512		90.35		100.04532		861.8119		90.35		100.06859		863.27699		90.35		100.03999

		837.70203		90.375		99.99824		100.04534		837.26202		90.375		99.99642		837.65698		90.375		100.00164		860.52234		90.375		100.04534		862.06145		90.375		100.06863		863.51622		90.375		100.04002

		837.95398		90.4		99.99891		100.04535		837.51898		90.4		99.99331		837.91302		90.4		99.99922		860.76044		90.4		100.04535		862.31167		90.4		100.06867		863.75644		90.4		100.04005

		838.23199		90.425		99.99831		100.04536		837.784		90.425		99.99171		838.16901		90.425		100.00037		861.00922		90.425		100.04536		862.56289		90.425		100.06871		864.00267		90.425		100.04007

		838.48499		90.45		99.99849		100.04536		838.047		90.45		99.98956		838.42798		90.45		99.99848		861.25867		90.45		100.04536		862.81622		90.45		100.06875		864.25244		90.45		100.0401

		838.745		90.475		100.00048		100.04536		838.30499		90.475		99.99347		838.69598		90.475		99.99876		861.50911		90.475		100.04536		863.065		90.475		100.06879		864.50166		90.475		100.04013

		839.01501		90.5		99.99999		100.04535		838.57703		90.5		99.9935		838.961		90.5		100.00255		861.75922		90.5		100.04535		863.30533		90.5		100.06883		864.75088		90.5		100.04016

		839.27197		90.525		99.99938		100.04534		838.83301		90.525		99.99432		839.211		90.525		100.00041		862.00989		90.525		100.04534		863.54222		90.525		100.06887		864.99955		90.525		100.04019

		839.53802		90.55		99.99923		100.04533		839.086		90.55		99.99225		839.48297		90.55		99.99972		862.26267		90.55		100.04533		863.77745		90.55		100.0689		865.25255		90.55		100.04022

		839.79199		90.575		99.99996		100.04532		839.35999		90.575		99.9952		839.73901		90.575		99.999		862.51511		90.575		100.04532		864.02144		90.575		100.06894		865.50433		90.575		100.04025

		840.05103		90.6		99.99739		100.04531		839.61902		90.6		99.99383		840.008		90.6		99.99952		862.76955		90.6		100.04531		864.27011		90.6		100.06897		865.75655		90.6		100.04028

		840.32202		90.625		99.99834		100.0453		839.87701		90.625		99.99298		840.26801		90.625		99.99945		863.02367		90.625		100.0453		864.51923		90.625		100.069		866.01021		90.625		100.04031

		840.57501		90.65		99.99735		100.0453		840.13898		90.65		99.9904		840.53198		90.65		99.99821		863.26911		90.65		100.0453		864.76634		90.65		100.06902		866.25666		90.65		100.04033

		840.83801		90.675		100.00124		100.04529		840.39502		90.675		99.99579		840.78601		90.675		100.00042		863.51056		90.675		100.04529		865.01134		90.675		100.06905		866.49799		90.675		100.04036

		841.10797		90.7		99.99916		100.0453		840.64801		90.7		99.99352		841.05499		90.7		99.99976		863.75067		90.7		100.0453		865.26045		90.7		100.06907		866.73822		90.7		100.04038

		841.36298		90.725		100.00138		100.04531		840.91699		90.725		99.99702		841.31201		90.725		100.00319		863.99634		90.725		100.04531		865.51078		90.725		100.06908		866.978		90.725		100.04041

		841.62097		90.75		99.99879		100.04533		841.18402		90.75		99.99284		841.56598		90.75		100.00021		864.24534		90.75		100.04533		865.76456		90.75		100.0691		867.22355		90.75		100.04043

		841.88397		90.775		99.99738		100.04535		841.43799		90.775		99.99215		841.82599		90.775		99.99704		864.49667		90.775		100.04535		866.01944		90.775		100.06911		867.46956		90.775		100.04045

		842.15399		90.8		99.99704		100.04538		841.69897		90.8		99.99089		842.09601		90.8		100.00077		864.74689		90.8		100.04538		866.26478		90.8		100.06912		867.72111		90.8		100.04047

		842.41199		90.825		99.99741		100.04542		841.96997		90.825		99.99258		842.35901		90.825		99.99667		864.99901		90.825		100.04542		866.50399		90.825		100.06913		867.97378		90.825		100.0405

		842.67401		90.85		99.99824		100.04546		842.22498		90.85		99.99243		842.62402		90.85		99.99796		865.25112		90.85		100.04546		866.74089		90.85		100.06915		868.22356		90.85		100.04053

		842.93402		90.875		99.99721		100.04551		842.49103		90.875		99.99262		842.87799		90.875		99.99803		865.50356		90.875		100.04551		866.98022		90.875		100.06917		868.47434		90.875		100.04056

		843.19		90.9		99.99549		100.04557		842.75201		90.9		99.99178		843.14301		90.9		99.99871		865.75922		90.9		100.04557		867.22644		90.9		100.06919		868.72656		90.9		100.04059

		843.45599		90.925		99.99809		100.04563		843.021		90.925		99.99401		843.40601		90.925		100.00002		866.01455		90.925		100.04563		867.47466		90.925		100.06922		868.98056		90.925		100.04063

		843.72198		90.95		99.99769		100.0457		843.27698		90.95		99.9914		843.67102		90.95		99.99899		866.26266		90.95		100.0457		867.72577		90.95		100.06926		869.233		90.95		100.04067

		843.97302		90.975		99.99695		100.04577		843.53699		90.975		99.99429		843.92401		90.975		100.0006		866.506		90.975		100.04577		867.97388		90.975		100.0693		869.48322		90.975		100.04071

		844.24402		91		99.99889		100.04583		843.79901		91		99.99524		844.185		91		99.99994		866.74655		91		100.04583		868.22243		91		100.06935		869.72944		91		100.04075

		844.50201		91.025		99.99767		100.0459		844.06403		91.025		99.99253		844.44501		91.025		99.99981		866.98777		91.025		100.0459		868.47454		91.025		100.06941		869.97032		91.025		100.0408

		844.76898		91.05		99.99772		100.04597		844.31799		91.05		99.99433		844.716		91.05		99.99931		867.23111		91.05		100.04597		868.7291		91.05		100.06948		870.20976		91.05		100.04085

		845.02002		91.075		99.99896		100.04603		844.57397		91.075		99.99524		844.97699		91.075		99.99872		867.47622		91.075		100.04603		868.98532		91.075		100.06955		870.46065		91.075		100.0409

		845.29199		91.1		99.99906		100.04608		844.84198		91.1		99.99773		845.23297		91.1		100.00079		867.72433		91.1		100.04608		869.23965		91.1		100.06963		870.7141		91.1		100.04095

		845.53998		91.125		99.99955		100.04612		845.099		91.125		99.99733		845.492		91.125		100.00234		867.97245		91.125		100.04612		869.48687		91.125		100.06971		870.9661		91.125		100.041

		845.80499		91.15		99.99845		100.04616		845.36102		91.15		99.99775		845.75299		91.15		99.99957		868.22356		91.15		100.04616		869.73254		91.15		100.06978		871.21688		91.15		100.04105

		846.07001		91.175		99.99798		100.04619		845.61499		91.175		99.99356		846.01801		91.175		100.00086		868.47423		91.175		100.04619		869.97331		91.175		100.06986		871.46933		91.175		100.0411

		846.328		91.2		99.99847		100.0462		845.88		91.2		99.99775		846.27197		91.2		100.00152		868.72712		91.2		100.0462		870.21698		91.2		100.06993		871.71899		91.2		100.04114

		846.59802		91.225		99.99697		100.04621		846.138		91.225		99.99493		846.53497		91.225		99.99932		868.98134		91.225		100.04621		870.46665		91.225		100.07		871.96889		91.225		100.04118

		846.85101		91.25		99.99819		100.04621		846.40601		91.25		99.99188		846.79602		91.25		100.00084		869.23512		91.25		100.04621		870.71743		91.25		100.07007		872.21911		91.25		100.04122

		847.11603		91.275		99.99693		100.0462		846.66602		91.275		99.99552		847.05701		91.275		99.99891		869.48523		91.275		100.0462		870.96687		91.275		100.07013		872.47278		91.275		100.04125

		847.37402		91.3		100.00021		100.04619		846.92499		91.3		99.9918		847.32202		91.3		100.00443		869.73534		91.3		100.04619		871.21699		91.3		100.07018		872.71689		91.3		100.04128

		847.62903		91.325		99.99876		100.04618		847.19299		91.325		99.99504		847.58502		91.325		100.00005		869.98223		91.325		100.04618		871.4681		91.325		100.07023		872.95611		91.325		100.04131

		847.90002		91.35		99.99823		100.04615		847.44897		91.35		99.99325		847.84698		91.35		99.99994		870.22822		91.35		100.04615		871.71999		91.35		100.07027		873.19244		91.35		100.04133

		848.15399		91.375		99.99921		100.04613		847.71301		91.375		99.99221		848.10797		91.375		100.00133		870.47744		91.375		100.04613		871.97033		91.375		100.07031		873.43056		91.375		100.04135

		848.41998		91.4		100.00037		100.04611		847.96899		91.4		99.99667		848.37299		91.4		100.00162		870.73		91.4		100.04611		872.22122		91.4		100.07035		873.67367		91.4		100.04137

		848.685		91.425		99.99853		100.04609		848.229		91.425		99.99627		848.62903		91.425		100.00019		870.982		91.425		100.04609		872.47255		91.425		100.07038		873.91833		91.425		100.04139

		848.953		91.45		99.99801		100.04606		848.49597		91.45		99.99541		848.883		91.45		99.99942		871.235		91.45		100.04606		872.71689		91.45		100.07041		874.16511		91.45		100.04141

		849.20502		91.475		99.99735		100.04604		848.75702		91.475		99.99488		849.14301		91.475		99.9991		871.49167		91.475		100.04604		872.95756		91.475		100.07043		874.41623		91.475		100.04142

		849.46698		91.5		100.00005		100.04602		849.01898		91.5		99.99486		849.41101		91.5		100.00129		871.749		91.5		100.04602		873.19612		91.5		100.07046		874.66278		91.5		100.04143

		849.73102		91.525		99.99916		100.046		849.271		91.525		99.99464		849.66803		91.525		100.00162		872.00378		91.525		100.046		873.43956		91.525		100.07049		874.90834		91.525		100.04144

		849.98999		91.55		99.99819		100.04598		849.52899		91.55		99.99309		849.93103		91.55		100.00129		872.25511		91.55		100.04598		873.68678		91.55		100.07051		875.15289		91.55		100.04145

		850.25897		91.575		99.99793		100.04596		849.797		91.575		99.99499		850.20001		91.575		100.00206		872.50844		91.575		100.04596		873.93422		91.575		100.07053		875.40367		91.575		100.04146

		850.50702		91.6		99.99632		100.04595		850.05902		91.6		99.99497		850.461		91.6		99.99921		872.75545		91.6		100.04595		874.18033		91.6		100.07055		875.65078		91.6		100.04147

		850.77502		91.625		99.9976		100.04593		850.31702		91.625		99.99313		850.72302		91.625		100.00104		872.99967		91.625		100.04593		874.43033		91.625		100.07057		875.89277		91.625		100.04148

		851.03101		91.65		99.99699		100.04592		850.57501		91.65		99.99665		850.99103		91.65		99.99808		873.24333		91.65		100.04592		874.67833		91.65		100.07058		876.13411		91.65		100.04148

		851.29199		91.675		99.99893		100.0459		850.84399		91.675		99.99753		851.25403		91.675		99.99984		873.494		91.675		100.0459		874.92722		91.675		100.0706		876.37589		91.675		100.04149

		851.56097		91.7		99.99979		100.04589		851.09998		91.7		99.9953		851.50897		91.7		99.9997		873.74533		91.7		100.04589		875.17778		91.7		100.07061		876.62233		91.7		100.04149

		851.81403		91.725		99.99826		100.04588		851.35999		91.725		99.99338		851.76202		91.725		99.99867		873.99678		91.725		100.04588		875.433		91.725		100.07062		876.87467		91.725		100.04149

		852.07202		91.75		99.99902		100.04588		851.61603		91.75		99.99366		852.02899		91.75		100.00114		874.24889		91.75		100.04588		875.68333		91.75		100.07063		877.13055		91.75		100.04149

		852.33698		91.775		99.99691		100.04587		851.88599		91.775		99.99345		852.29401		91.775		99.99953		874.50433		91.775		100.04587		875.92978		91.775		100.07063		877.388		91.775		100.04149

		852.59802		91.8		99.99784		100.04588		852.14301		91.8		99.99323		852.55499		91.8		100.0003		874.75701		91.8		100.04588		876.17467		91.8		100.07064		877.64111		91.8		100.04148

		852.85999		91.825		99.99742		100.04588		852.40698		91.825		99.99432		852.81799		91.825		99.99896		875.012		91.825		100.04588		876.421		91.825		100.07064		877.89656		91.825		100.04148

		853.13098		91.85		99.99826		100.04589		852.66998		91.85		99.99516		853.07098		91.85		99.99982		875.26967		91.85		100.04589		876.67278		91.85		100.07064		878.15012		91.85		100.04147

		853.38599		91.875		99.99961		100.0459		852.93298		91.875		99.99421		853.33801		91.875		100.00098		875.529		91.875		100.0459		876.92756		91.875		100.07064		878.4019		91.875		100.04147

		853.64899		91.9		99.99674		100.04592		853.19897		91.9		99.99147		853.59399		91.9		99.99893		875.77966		91.9		100.04592		877.18278		91.9		100.07065		878.65512		91.9		100.04147

		853.914		91.925		99.99818		100.04594		853.44897		91.925		99.9954		853.85699		91.925		100.00126		876.02566		91.925		100.04594		877.43734		91.925		100.07065		878.90011		91.925		100.04147

		854.17401		91.95		99.99646		100.04596		853.71997		91.95		99.9939		854.125		91.95		100.00006		876.27233		91.95		100.04596		877.68978		91.95		100.07067		879.14355		91.95		100.04148

		854.435		91.975		99.9972		100.04599		853.98199		91.975		99.99312		854.388		91.975		100.00009		876.52334		91.975		100.04599		877.94178		91.975		100.07068		879.38411		91.975		100.04149

		854.70398		92		99.99843		100.04601		854.24402		92		99.99165		854.646		92		99.99962		876.78033		92		100.04601		878.19467		92		100.07071		879.62178		92		100.04151

		854.96301		92.025		99.998		100.04604		854.50098		92.025		99.99461		854.90601		92.025		99.99982		877.04011		92.025		100.04604		878.449		92.025		100.07074		879.86856		92.025		100.04153

		855.22198		92.05		99.99862		100.04608		854.763		92.05		99.99429		855.16498		92.05		99.99982		877.29989		92.05		100.04608		878.70378		92.05		100.07079		880.11745		92.05		100.04157

		855.48401		92.075		99.99952		100.04611		855.01703		92.075		99.99478		855.43298		92.075		100.00031		877.558		92.075		100.04611		878.94868		92.075		100.07084		880.36656		92.075		100.04161

		855.74103		92.1		99.99721		100.04615		855.28101		92.1		99.99558		855.69397		92.1		99.99983		877.81366		92.1		100.04615		879.19234		92.1		100.07091		880.61978		92.1		100.04167

		856.00098		92.125		100.00085		100.04619		855.54602		92.125		99.99758		855.95801		92.125		100.0014		878.06899		92.125		100.04619		879.43378		92.125		100.07099		880.87366		92.125		100.04173

		856.26398		92.15		99.99988		100.04623		855.80298		92.15		99.9935		856.21997		92.15		100.00002		878.32744		92.15		100.04623		879.67678		92.15		100.07108		881.12756		92.15		100.04181

		856.52197		92.175		99.99844		100.04628		856.07001		92.175		99.99554		856.48102		92.175		99.99723		878.58421		92.175		100.04628		879.92689		92.175		100.07117		881.379		92.175		100.04189

		856.79102		92.2		99.99739		100.04632		856.33197		92.2		99.99458		856.73602		92.2		99.99919		878.83788		92.2		100.04632		880.18155		92.2		100.07128		881.63		92.2		100.04198

		857.05103		92.225		99.99623		100.04637		856.58801		92.225		99.99079		857.005		92.225		99.99944		879.0841		92.225		100.04637		880.43545		92.225		100.07139		881.88356		92.225		100.04207

		857.31097		92.25		99.99984		100.04642		856.85303		92.25		99.9964		857.26501		92.25		100.00146		879.3251		92.25		100.04642		880.69022		92.25		100.0715		882.13034		92.25		100.04217

		857.58398		92.275		99.99758		100.04648		857.10901		92.275		99.99476		857.526		92.275		99.99961		879.56276		92.275		100.04648		880.94622		92.275		100.07161		882.37345		92.275		100.04227

		857.841		92.3		100.00134		100.04653		857.37299		92.3		99.99519		857.78699		92.3		100.00121		879.81043		92.3		100.04653		881.20155		92.3		100.07172		882.615		92.3		100.04236

		858.09998		92.325		100.00009		100.04659		857.633		92.325		99.99612		858.04999		92.325		99.99897		880.06366		92.325		100.04659		881.45321		92.325		100.07183		882.85866		92.325		100.04246

		858.35498		92.35		100.0001		100.04665		857.901		92.35		99.99631		858.315		92.35		99.99739		880.31788		92.35		100.04665		881.70477		92.35		100.07193		883.10689		92.35		100.04255

		858.62		92.375		99.99876		100.04671		858.16101		92.375		99.99701		858.56799		92.375		100.00035		880.56989		92.375		100.04671		881.95622		92.375		100.07202		883.35666		92.375		100.04263

		858.883		92.4		99.99824		100.04678		858.42401		92.4		99.99245		858.83301		92.4		100.00041		880.82277		92.4		100.04678		882.20133		92.4		100.0721		883.605		92.4		100.04271

		859.14001		92.425		99.99678		100.04684		858.67999		92.425		99.99237		859.09698		92.425		100.00121		881.07655		92.425		100.04684		882.44245		92.425		100.07217		883.85522		92.425		100.04277

		859.401		92.45		100.00131		100.04691		858.94702		92.45		99.99522		859.35999		92.45		99.99848		881.3331		92.45		100.04691		882.68267		92.45		100.07223		884.10633		92.45		100.04283

		859.66199		92.475		99.99785		100.04698		859.211		92.475		99.99328		859.617		92.475		99.99672		881.59066		92.475		100.04698		882.93067		92.475		100.07228		884.35444		92.475		100.04287

		859.91901		92.5		99.9975		100.04704		859.47699		92.5		99.99423		859.88702		92.5		99.99953		881.84877		92.5		100.04704		883.18067		92.5		100.07231		884.60411		92.5		100.04291

		860.18402		92.525		99.9992		100.04711		859.73297		92.525		99.99546		860.146		92.525		100.0004		882.09755		92.525		100.04711		883.43267		92.525		100.07234		884.85489		92.525		100.04294

		860.44501		92.55		99.99763		100.04717		859.99103		92.55		99.99372		860.40698		92.55		100.00019		882.34099		92.55		100.04717		883.68734		92.55		100.07236		885.10088		92.55		100.04296

		860.703		92.575		99.99575		100.04723		860.25702		92.575		99.99234		860.664		92.575		99.9992		882.58455		92.575		100.04723		883.94312		92.575		100.07237		885.33944		92.575		100.04297

		860.96198		92.6		99.99733		100.04729		860.51501		92.6		99.995		860.935		92.6		100.00008		882.83154		92.6		100.04729		884.19757		92.6		100.07238		885.57577		92.6		100.04298

		861.23499		92.625		99.99712		100.04734		860.78302		92.625		99.99109		861.19202		92.625		99.99823		883.0851		92.625		100.04734		884.44868		92.625		100.07238		885.81077		92.625		100.04298

		861.49103		92.65		99.99819		100.04738		861.047		92.65		99.99813		861.45001		92.65		99.99896		883.33689		92.65		100.04738		884.70334		92.65		100.07238		886.05254		92.65		100.04299

		861.75403		92.675		99.9983		100.04742		861.30298		92.675		99.99213		861.71899		92.675		100.00053		883.58845		92.675		100.04742		884.95867		92.675		100.07238		886.29932		92.675		100.04299

		862.02399		92.7		99.99742		100.04744		861.56702		92.7		99.9971		861.97699		92.7		99.99909		883.84267		92.7		100.04744		885.20601		92.7		100.07238		886.54855		92.7		100.04299

		862.28998		92.725		100.00092		100.04746		861.83398		92.725		99.9975		862.23401		92.725		100.00046		884.09834		92.725		100.04746		885.44934		92.725		100.07238		886.79744		92.725		100.04299

		862.54999		92.75		99.99805		100.04746		862.091		92.75		99.99232		862.49799		92.75		99.9986		884.35278		92.75		100.04746		885.69179		92.75		100.07238		887.04711		92.75		100.043

		862.80603		92.775		99.99629		100.04746		862.35498		92.775		99.9928		862.763		92.775		99.99683		884.60745		92.775		100.04746		885.93512		92.775		100.07238		887.29722		92.775		100.04301

		863.06702		92.8		99.99917		100.04745		862.612		92.8		99.9934		863.02399		92.8		100.00045		884.86222		92.8		100.04745		886.187		92.8		100.07239		887.55023		92.8		100.04303

		863.32703		92.825		99.99872		100.04743		862.87701		92.825		99.99406		863.28699		92.825		99.99978		885.11111		92.825		100.04743		886.43945		92.825		100.0724		887.80389		92.825		100.04305

		863.59302		92.85		99.99844		100.0474		863.14099		92.85		99.99454		863.552		92.85		100.00145		885.35355		92.85		100.0474		886.69767		92.85		100.07241		888.05889		92.85		100.04308

		863.84399		92.875		99.99865		100.04736		863.409		92.875		99.99378		863.81299		92.875		100.00067		885.59433		92.875		100.04736		886.94934		92.875		100.07243		888.30511		92.875		100.0431

		864.11499		92.9		99.99737		100.04732		863.67102		92.9		99.99545		864.06403		92.9		99.99675		885.83588		92.9		100.04732		887.20079		92.9		100.07244		888.54789		92.9		100.04314

		864.37201		92.925		99.99636		100.04728		863.92902		92.925		99.99581		864.336		92.925		99.99261		886.0831		92.925		100.04728		887.45178		92.925		100.07247		888.78933		92.925		100.04317

		864.63098		92.95		99.99733		100.04724		864.18597		92.95		99.99269		864.59601		92.95		99.99974		886.33399		92.95		100.04724		887.70412		92.95		100.07249		889.03		92.95		100.04321

		864.90198		92.975		100.00104		100.0472		864.44598		92.975		99.99809		864.85699		92.975		100.00621		886.58666		92.975		100.0472		887.95723		92.975		100.07252		889.27889		92.975		100.04324

		865.15802		93		99.99965		100.04716		864.71399		93		99.99582		865.11499		93		99.99983		886.83944		93		100.04716		888.20856		93		100.07255		889.53144		93		100.04328

		865.41998		93.025		99.99853		100.04713		864.97699		93.025		99.9951		865.375		93.025		100.00101		887.09044		93.025		100.04713		888.45434		93.025		100.07258		889.78099		93.025		100.04331

		865.685		93.05		99.99819		100.0471		865.237		93.05		99.99319		865.63501		93.05		99.9987		887.34289		93.05		100.0471		888.69901		93.05		100.07262		890.03166		93.05		100.04334

		865.94598		93.075		99.9972		100.04708		865.50201		93.075		99.99515		865.901		93.075		99.99718		887.59678		93.075		100.04708		888.93778		93.075		100.07265		890.28533		93.075		100.04337

		866.20502		93.1		99.99949		100.04705		865.75299		93.1		99.99466		866.17102		93.1		100.00004		887.85256		93.1		100.04705		889.18445		93.1		100.07269		890.54044		93.1		100.04338

		866.47198		93.125		99.99921		100.04703		866.02399		93.125		99.99268		866.43298		93.125		100.00007		888.10678		93.125		100.04703		889.43589		93.125		100.07272		890.794		93.125		100.04339

		866.73499		93.15		99.9987		100.04701		866.27502		93.15		99.99243		866.68903		93.15		100.0004		888.35434		93.15		100.04701		889.68989		93.15		100.07276		891.04744		93.15		100.0434

		866.99701		93.175		99.996		100.04699		866.53601		93.175		99.99393		866.95697		93.175		99.9982		888.59945		93.175		100.04699		889.94267		93.175		100.07279		891.29978		93.175		100.0434

		867.25598		93.2		99.99586		100.04697		866.80298		93.2		99.9918		867.22101		93.2		99.99735		888.843		93.2		100.04697		890.195		93.2		100.07282		891.54522		93.2		100.0434

		867.521		93.225		99.99689		100.04695		867.07098		93.225		99.99418		867.46997		93.225		99.99923		889.08689		93.225		100.04695		890.45078		93.225		100.07285		891.78489		93.225		100.04339

		867.77197		93.25		99.99755		100.04692		867.33099		93.25		99.99256		867.73499		93.25		99.9997		889.33845		93.25		100.04692		890.70544		93.25		100.07287		892.02445		93.25		100.04337

		868.03198		93.275		99.99952		100.04688		867.59802		93.275		99.9938		868.00201		93.275		100.00119		889.59266		93.275		100.04688		890.96044		93.275		100.07288		892.26378		93.275		100.04335

		868.297		93.3		99.99818		100.04684		867.86102		93.3		99.99616		868.26801		93.3		100.00037		889.84655		93.3		100.04684		891.21811		93.3		100.07289		892.50911		93.3		100.04333

		868.56		93.325		99.99895		100.0468		868.12201		93.325		99.99673		868.51898		93.325		100.0003		890.10133		93.325		100.0468		891.47156		93.325		100.0729		892.75633		93.325		100.0433

		868.82599		93.35		99.99691		100.04676		868.38098		93.35		99.99514		868.78198		93.35		100.00074		890.35477		93.35		100.04676		891.72011		93.35		100.07289		893.005		93.35		100.04328

		869.086		93.375		99.99545		100.04671		868.651		93.375		99.99486		869.039		93.375		99.99907		890.60766		93.375		100.04671		891.96501		93.375		100.07289		893.25389		93.375		100.04326

		869.34802		93.4		99.99784		100.04667		868.90802		93.4		99.99598		869.30701		93.4		99.99985		890.85966		93.4		100.04667		892.20757		93.4		100.07288		893.50444		93.4		100.04325

		869.61102		93.425		99.99714		100.04663		869.17798		93.425		99.99459		869.56702		93.425		99.99839		891.111		93.425		100.04663		892.46179		93.425		100.07287		893.75367		93.425		100.04324

		869.87201		93.45		99.99784		100.0466		869.435		93.45		99.99563		869.82501		93.45		99.99904		891.36544		93.45		100.0466		892.71279		93.45		100.07287		894.00367		93.45		100.04324

		870.13		93.475		99.99638		100.04657		869.69397		93.475		99.9917		870.091		93.475		99.99882		891.61521		93.475		100.04657		892.96368		93.475		100.07286		894.25878		93.475		100.04324

		870.388		93.5		99.9972		100.04656		869.95898		93.5		99.99472		870.35602		93.5		100.0015		891.86032		93.5		100.04656		893.21579		93.5		100.07286		894.51356		93.5		100.04326

		870.65002		93.525		99.99836		100.04656		870.21399		93.525		99.99709		870.61401		93.525		100.0017		892.10088		93.525		100.04656		893.46878		93.525		100.07287		894.75834		93.525		100.0433

		870.92102		93.55		99.99836		100.04658		870.47101		93.55		99.99562		870.87097		93.55		99.99899		892.34555		93.55		100.04658		893.72123		93.55		100.07289		894.99868		93.55		100.04335

		871.18298		93.575		99.99651		100.04661		870.73999		93.575		99.99325		871.14001		93.575		99.9995		892.59677		93.575		100.04661		893.97356		93.575		100.07293		895.23834		93.575		100.04341

		871.44702		93.6		99.99903		100.04667		870.99799		93.6		99.99727		871.39301		93.6		99.99937		892.84956		93.6		100.04667		894.226		93.6		100.07297		895.48323		93.6		100.04349

		871.70697		93.625		99.99903		100.04674		871.26001		93.625		99.99493		871.65997		93.625		100.00201		893.10156		93.625		100.04674		894.48344		93.625		100.07303		895.73389		93.625		100.04359

		871.966		93.65		99.99788		100.04682		871.53101		93.65		99.99402		871.92603		93.65		100.00113		893.35855		93.65		100.04682		894.72888		93.65		100.07311		895.98811		93.65		100.0437

		872.224		93.675		99.99722		100.04692		871.79199		93.675		99.9928		872.18799		93.675		99.99912		893.61355		93.675		100.04692		894.97488		93.675		100.0732		896.24177		93.675		100.04382

		872.48401		93.7		99.99813		100.04704		872.05103		93.7		99.9936		872.44598		93.7		99.99715		893.867		93.7		100.04704		895.22144		93.7		100.07329		896.49044		93.7		100.04396

		872.75403		93.725		99.99907		100.04716		872.31403		93.725		99.99585		872.71698		93.725		99.99959		894.12155		93.725		100.04716		895.47122		93.725		100.0734		896.73933		93.725		100.0441

		873.02502		93.75		99.9975		100.04729		872.57898		93.75		99.99778		872.97699		93.75		100.00099		894.37977		93.75		100.04729		895.72378		93.75		100.07352		896.99199		93.75		100.04424

		873.28699		93.775		99.99454		100.04742		872.84399		93.775		99.99769		873.23499		93.775		99.99756		894.63133		93.775		100.04742		895.98022		93.775		100.07363		897.24888		93.775		100.04439

		873.552		93.8		99.99738		100.04755		873.09802		93.8		99.99029		873.49902		93.8		99.99887		894.87777		93.8		100.04755		896.23812		93.8		100.07375		897.50589		93.8		100.04452

		873.80701		93.825		99.99742		100.04767		873.367		93.825		99.99342		873.76501		93.825		99.9999		895.12266		93.825		100.04767		896.49823		93.825		100.07386		897.75689		93.825		100.04465

		874.073		93.85		99.99834		100.04779		873.625		93.85		99.99265		874.02802		93.85		100.0003		895.36655		93.85		100.04779		896.75412		93.85		100.07396		898.002		93.85		100.04477

		874.33099		93.875		99.99945		100.04789		873.883		93.875		99.99606		874.28699		93.875		100.00134		895.61677		93.875		100.04789		897.00946		93.875		100.07406		898.24267		93.875		100.04487

		874.59497		93.9		99.997		100.04798		874.14301		93.9		99.9923		874.54901		93.9		99.99996		895.86844		93.9		100.04798		897.26557		93.9		100.07414		898.48423		93.9		100.04495

		874.84802		93.925		99.99602		100.04806		874.41101		93.925		99.99295		874.79999		93.925		99.99755		896.12155		93.925		100.04806		897.51946		93.925		100.0742		898.73634		93.925		100.04501

		875.12097		93.95		99.99649		100.04812		874.66803		93.95		99.99241		875.06799		93.95		99.99853		896.37566		93.95		100.04812		897.76856		93.95		100.07426		898.99078		93.95		100.04506

		875.38202		93.975		99.99924		100.04817		874.93402		93.975		99.99537		875.33698		93.975		99.99922		896.62989		93.975		100.04817		898.01534		93.975		100.07429		899.24467		93.975		100.04508

		875.64398		94		99.99821		100.0482		875.18701		94		99.99338		875.60699		94		100.00029		896.88356		94		100.0482		898.25723		94		100.07432		899.49545		94		100.04508

		875.90198		94.025		99.99899		100.04822		875.45398		94.025		99.99282		875.86298		94.025		99.99798		897.13734		94.025		100.04822		898.49645		94.025		100.07433		899.74667		94.025		100.04507

		876.16101		94.05		99.99813		100.04823		875.71399		94.05		99.9965		876.12097		94.05		99.99935		897.39122		94.05		100.04823		898.74367		94.05		100.07433		900.00034		94.05		100.04504

		876.42902		94.075		99.99729		100.04823		875.979		94.075		99.99537		876.38702		94.075		99.99907		897.64766		94.075		100.04823		898.99611		94.075		100.07432		900.25423		94.075		100.045

		876.68701		94.1		99.9997		100.04823		876.245		94.1		99.99289		876.64899		94.1		100.00093		897.89266		94.1		100.04823		899.25088		94.1		100.07431		900.50857		94.1		100.04495

		876.95203		94.125		99.99996		100.04822		876.50702		94.125		99.99458		876.90302		94.125		99.99933		898.13622		94.125		100.04822		899.50488		94.125		100.0743		900.76312		94.125		100.0449

		877.22198		94.15		99.99741		100.04821		876.77301		94.15		99.99782		877.17297		94.15		100.00051		898.378		94.15		100.04821		899.75933		94.15		100.07428		901.0089		94.15		100.04484

		877.47699		94.175		99.9987		100.04819		877.03699		94.175		99.99711		877.42999		94.175		99.99874		898.62345		94.175		100.04819		900.015		94.175		100.07426		901.25157		94.175		100.04479

		877.73499		94.2		99.99731		100.04818		877.29602		94.2		99.99465		877.70001		94.2		99.99931		898.87478		94.2		100.04818		900.26711		94.2		100.07425		901.49234		94.2		100.04474

		877.99597		94.225		99.99752		100.04817		877.55798		94.225		99.99758		877.96399		94.225		100.00041		899.12933		94.225		100.04817		900.51911		94.225		100.07425		901.73789		94.225		100.04469

		878.26599		94.25		99.997		100.04816		877.82202		94.25		99.99672		878.22601		94.25		99.99901		899.38445		94.25		100.04816		900.77289		94.25		100.07425		901.98767		94.25		100.04466

		878.52502		94.275		100.00092		100.04815		878.09003		94.275		99.99832		878.48602		94.275		100.00039		899.63878		94.275		100.04815		901.01778		94.275		100.07426		902.23589		94.275		100.04463

		878.78998		94.3		99.99995		100.04814		878.34998		94.3		99.99536		878.74402		94.3		100.00142		899.89045		94.3		100.04814		901.26		94.3		100.07427		902.48467		94.3		100.04462

		879.04602		94.325		99.99696		100.04814		878.60199		94.325		99.99213		879.00598		94.325		99.99986		900.14423		94.325		100.04814		901.49945		94.325		100.07429		902.73578		94.325		100.04461

		879.31299		94.35		99.99917		100.04814		878.87		94.35		99.99494		879.263		94.35		99.99995		900.39623		94.35		100.04814		901.74312		94.35		100.07433		902.98611		94.35		100.04462

		879.58099		94.375		99.99802		100.04815		879.12799		94.375		99.99439		879.52502		94.375		100.00073		900.64734		94.375		100.04815		901.99145		94.375		100.07437		903.23611		94.375		100.04464

		879.84003		94.4		99.99934		100.04815		879.38898		94.4		99.99425		879.79901		94.4		100.00061		900.89478		94.4		100.04815		902.23934		94.4		100.07442		903.48667		94.4		100.04467

		880.10498		94.425		100.00086		100.04815		879.65802		94.425		99.99546		880.06		94.425		100.00068		901.137		94.425		100.04815		902.48956		94.425		100.07447		903.73878		94.425		100.0447

		880.35999		94.45		99.99931		100.04816		879.91199		94.45		99.99482		880.32001		94.45		100.00087		901.37611		94.45		100.04816		902.7419		94.45		100.07453		903.98601		94.45		100.04474

		880.625		94.475		99.99642		100.04817		880.17603		94.475		99.99079		880.58301		94.475		99.997		901.61211		94.475		100.04817		902.99501		94.475		100.0746		904.22546		94.475		100.04479

		880.88702		94.5		99.99788		100.04818		880.44299		94.5		99.9924		880.83398		94.5		99.99869		901.85889		94.5		100.04818		903.24923		94.5		100.07467		904.46402		94.5		100.04485

		881.14301		94.525		99.99658		100.0482		880.70398		94.525		99.99334		881.10303		94.525		99.99893		902.10788		94.525		100.0482		903.50279		94.525		100.07474		904.70235		94.525		100.04491

		881.41498		94.55		99.99612		100.04821		880.96399		94.55		99.99368		881.37299		94.55		99.9983		902.35588		94.55		100.04821		903.7589		94.55		100.07481		904.94645		94.55		100.04497

		881.67499		94.575		99.99562		100.04823		881.23199		94.575		99.99334		881.62903		94.575		99.99643		902.60499		94.575		100.04823		904.00779		94.575		100.07488		905.19457		94.575		100.04503

		881.93903		94.6		100.00018		100.04825		881.49402		94.6		99.99713		881.896		94.6		100.00083		902.85577		94.6		100.04825		904.25067		94.6		100.07494		905.44046		94.6		100.04509

		882.20203		94.625		99.9972		100.04827		881.76099		94.625		99.99481		882.159		94.625		99.99741		903.10922		94.625		100.04827		904.49345		94.625		100.07499		905.68534		94.625		100.04515

		882.46802		94.65		100.0003		100.0483		882.01501		94.65		99.99709		882.414		94.65		99.99896		903.36256		94.65		100.0483		904.73722		94.65		100.07504		905.93079		94.65		100.04521

		882.72998		94.675		99.99675		100.04832		882.27802		94.675		99.99404		882.68201		94.675		99.99928		903.61555		94.675		100.04832		904.98855		94.675		100.07508		906.17745		94.675		100.04527

		882.99701		94.7		99.99967		100.04836		882.54901		94.7		99.99652		882.95203		94.7		100.00065		903.87145		94.7		100.04836		905.24111		94.7		100.07511		906.42967		94.7		100.04532

		883.258		94.725		99.99552		100.04839		882.80902		94.725		99.99438		883.20502		94.725		100.00054		904.11534		94.725		100.04839		905.49678		94.725		100.07513		906.68422		94.725		100.04538

		883.52301		94.75		99.9992		100.04843		883.06097		94.75		99.99696		883.46698		94.75		99.9982		904.35678		94.75		100.04843		905.75133		94.75		100.07514		906.94056		94.75		100.04543

		883.784		94.775		99.9979		100.04848		883.328		94.775		99.99137		883.72699		94.775		99.99859		904.59689		94.775		100.04848		906.00533		94.775		100.07515		907.18789		94.775		100.04549

		884.04602		94.8		99.99638		100.04853		883.58698		94.8		99.99241		883.995		94.8		99.99877		904.84166		94.8		100.04853		906.26155		94.8		100.07515		907.43178		94.8		100.04555

		884.30701		94.825		100.00102		100.04858		883.85602		94.825		99.99607		884.25403		94.825		100.00184		905.09033		94.825		100.04858		906.51911		94.825		100.07514		907.67722		94.825		100.04561

		884.565		94.85		100.00231		100.04862		884.11603		94.85		99.99563		884.52002		94.85		100.00119		905.337		94.85		100.04862		906.77677		94.85		100.07514		907.92622		94.85		100.04566

		884.83002		94.875		99.99999		100.04867		884.37701		94.875		99.99728		884.78302		94.875		100.00079		905.58566		94.875		100.04867		907.03144		94.875		100.07513		908.177		94.875		100.04572

		885.08698		94.9		99.99857		100.04872		884.64001		94.9		99.99354		885.04401		94.9		100.00115		905.83689		94.9		100.04872		907.27633		94.9		100.07512		908.43022		94.9		100.04578

		885.35498		94.925		99.99903		100.04876		884.90002		94.925		99.99398		885.30499		94.925		99.9997		906.08788		94.925		100.04876		907.51911		94.925		100.07511		908.68256		94.925		100.04584

		885.617		94.95		99.99887		100.0488		885.17102		94.95		99.99427		885.57501		94.95		100.00059		906.34311		94.95		100.0488		907.75744		94.95		100.07511		908.93444		94.95		100.0459

		885.883		94.975		99.99963		100.04883		885.42603		94.975		99.99653		885.82098		94.975		100.00101		906.6001		94.975		100.04883		908.00333		94.975		100.07511		909.18456		94.975		100.04595

		886.14398		95		99.99831		100.04885		885.68402		95		99.99548		886.09198		95		100.00068		906.85633		95		100.04885		908.24988		95		100.07512		909.43811		95		100.046

		886.40399		95.025		99.99959		100.04886		885.95697		95.025		99.99496		886.35602		95.025		99.99749		907.10667		95.025		100.04886		908.499		95.025		100.07514		909.69078		95.025		100.04605

		886.67297		95.05		99.9984		100.04887		886.20502		95.05		99.99238		886.61603		95.05		99.9986		907.35344		95.05		100.04887		908.74733		95.05		100.07517		909.94167		95.05		100.04609

		886.94202		95.075		99.99621		100.04888		886.47803		95.075		99.99171		886.87299		95.075		99.99839		907.60156		95.075		100.04888		908.99477		95.075		100.0752		910.19366		95.075		100.04613

		887.211		95.1		99.99944		100.04887		886.737		95.1		99.9962		887.13599		95.1		100.00195		907.84578		95.1		100.04887		909.24533		95.1		100.07525		910.44155		95.1		100.04616

		887.47101		95.125		99.99801		100.04887		887.01202		95.125		99.99548		887.39899		95.125		99.99946		908.09711		95.125		100.04887		909.49499		95.125		100.0753		910.68455		95.125		100.04619

		887.72302		95.15		99.9994		100.04886		887.27002		95.15		99.99791		887.68201		95.15		100.00145		908.35255		95.15		100.04886		909.74799		95.15		100.07537		910.92555		95.15		100.04622

		887.98199		95.175		99.99898		100.04886		887.52899		95.175		99.99678		887.93201		95.175		100.00059		908.607		95.175		100.04886		910.00155		95.175		100.07545		911.17289		95.175		100.04625

		888.24298		95.2		99.99651		100.04885		887.79498		95.2		99.99118		888.19598		95.2		99.99893		908.86078		95.2		100.04885		910.25111		95.2		100.07553		911.42211		95.2		100.04627

		888.508		95.225		99.99769		100.04886		888.04797		95.225		99.99483		888.45099		95.225		99.99826		909.11555		95.225		100.04886		910.49888		95.225		100.07562		911.66933		95.225		100.0463

		888.77698		95.25		99.9991		100.04887		888.31897		95.25		99.99639		888.71899		95.25		100.00026		909.37311		95.25		100.04887		910.74177		95.25		100.07572		911.91777		95.25		100.04633

		889.03101		95.275		99.99746		100.04889		888.58398		95.275		99.99414		888.979		95.275		99.99931		909.629		95.275		100.04889		910.98877		95.275		100.07583		912.17111		95.275		100.04636

		889.29797		95.3		99.99703		100.04893		888.84399		95.3		99.9932		889.23798		95.3		100.00139		909.884		95.3		100.04893		911.24433		95.3		100.07594		912.41978		95.3		100.04639

		889.55402		95.325		99.99712		100.04897		889.10699		95.325		99.99412		889.50403		95.325		99.9986		910.141		95.325		100.04897		911.49988		95.325		100.07605		912.67023		95.325		100.04643

		889.823		95.35		99.99877		100.04903		889.37402		95.35		99.99508		889.77197		95.35		99.99978		910.38734		95.35		100.04903		911.75766		95.35		100.07616		912.92256		95.35		100.04647

		890.09198		95.375		100.00119		100.0491		889.62903		95.375		99.9981		890.02802		95.375		100.00027		910.62678		95.375		100.0491		912.01189		95.375		100.07627		913.17667		95.375		100.04652

		890.35999		95.4		99.99869		100.04919		889.89001		95.4		99.99612		890.29199		95.4		100.00039		910.86355		95.4		100.04919		912.26567		95.4		100.07638		913.42312		95.4		100.04657

		890.61902		95.425		100.00109		100.04928		890.15601		95.425		99.99516		890.552		95.425		100.00243		911.10689		95.425		100.04928		912.51611		95.425		100.07648		913.66589		95.425		100.04662

		890.88501		95.45		99.99607		100.04938		890.41699		95.45		99.99274		890.80499		95.45		99.99995		911.35622		95.45		100.04938		912.76577		95.45		100.07658		913.90834		95.45		100.04667

		891.14697		95.475		100.00147		100.04949		890.68402		95.475		99.99642		891.06897		95.475		100.00248		911.60433		95.475		100.04949		913.01877		95.475		100.07667		914.15479		95.475		100.04673

		891.40997		95.5		100.00001		100.04961		890.94702		95.5		99.99587		891.33899		95.5		100.00035		911.85266		95.5		100.04961		913.27133		95.5		100.07675		914.40256		95.5		100.04678

		891.66901		95.525		99.99891		100.04972		891.21997		95.525		99.99736		891.604		95.525		99.99898		912.10111		95.525		100.04972		913.51555		95.525		100.07683		914.65034		95.525		100.04684

		891.935		95.55		99.99708		100.04984		891.48297		95.55		99.99585		891.86401		95.55		99.99876		912.34932		95.55		100.04984		913.75789		95.55		100.07691		914.89912		95.55		100.0469

		892.20203		95.575		99.99962		100.04996		891.75201		95.575		99.99541		892.12299		95.575		100.0006		912.60111		95.575		100.04996		914.001		95.575		100.07698		915.14978		95.575		100.04696

		892.46002		95.6		100.00041		100.05008		892.00598		95.6		99.99605		892.38898		95.6		100.00115		912.85467		95.6		100.05008		914.24988		95.6		100.07704		915.39867		95.6		100.04702

		892.71802		95.625		99.99665		100.05019		892.26801		95.625		99.99434		892.659		95.625		99.99814		913.11056		95.625		100.05019		914.50111		95.625		100.0771		915.64756		95.625		100.04708

		892.97998		95.65		99.99818		100.0503		892.52197		95.65		99.99238		892.914		95.65		99.99872		913.35922		95.65		100.0503		914.75355		95.65		100.07717		915.90056		95.65		100.04714

		893.24597		95.675		99.99672		100.0504		892.79602		95.675		99.99727		893.185		95.675		99.99873		913.60222		95.675		100.0504		915.00966		95.675		100.07723		916.15445		95.675		100.0472

		893.513		95.7		99.9979		100.05049		893.04797		95.7		99.99169		893.44397		95.7		100.00019		913.84256		95.7		100.05049		915.26511		95.7		100.07729		916.40445		95.7		100.04726

		893.77502		95.725		99.99788		100.05057		893.31702		95.725		99.99597		893.70099		95.725		99.99842		914.08811		95.725		100.05057		915.51878		95.725		100.07736		916.64978		95.725		100.04732

		894.034		95.75		99.99789		100.05064		893.57397		95.75		99.99829		893.96997		95.75		100.00025		914.33934		95.75		100.05064		915.77278		95.75		100.07743		916.89567		95.75		100.04738

		894.30298		95.775		100.0001		100.0507		893.83899		95.775		100.00058		894.22601		95.775		100.00063		914.59022		95.775		100.0507		916.02734		95.775		100.0775		917.13867		95.775		100.04744

		894.56799		95.8		99.99682		100.05075		894.10101		95.8		99.99432		894.49597		95.8		99.99948		914.84111		95.8		100.05075		916.28067		95.8		100.07757		917.38789		95.8		100.0475

		894.82703		95.825		99.99714		100.05079		894.36603		95.825		99.99336		894.76501		95.825		99.99865		915.09211		95.825		100.05079		916.52789		95.825		100.07765		917.64033		95.825		100.04755

		895.09003		95.85		99.99593		100.05082		894.62701		95.85		99.99058		895.01599		95.85		99.99702		915.34222		95.85		100.05082		916.77356		95.85		100.07772		917.89544		95.85		100.04761

		895.35303		95.875		99.99713		100.05083		894.88501		95.875		99.99284		895.28003		95.875		99.99934		915.59401		95.875		100.05083		917.01855		95.875		100.0778		918.14911		95.875		100.04766

		895.62097		95.9		99.99891		100.05083		895.151		95.9		99.99327		895.54602		95.9		99.99993		915.84989		95.9		100.05083		917.26489		95.9		100.07786		918.401		95.9		100.0477

		895.87799		95.925		99.99805		100.05083		895.422		95.925		99.99598		895.81403		95.925		99.99994		916.10978		95.925		100.05083		917.51789		95.925		100.07793		918.653		95.925		100.04774

		896.13702		95.95		100.00187		100.05081		895.67902		95.95		99.99598		896.07001		95.95		99.99972		916.36323		95.95		100.05081		917.77122		95.95		100.07799		918.90422		95.95		100.04778

		896.40698		95.975		99.99986		100.05079		895.94098		95.975		99.99638		896.33398		95.975		100.00117		916.60789		95.975		100.05079		918.02411		95.975		100.07805		919.15445		95.975		100.04781

		896.66803		96		99.99603		100.05075		896.211		96		99.99465		896.59802		96		100.00005		916.85345		96		100.05075		918.27511		96		100.0781		919.40423		96		100.04784

		896.91602		96.025		99.99984		100.05072		896.47101		96.025		99.99622		896.86102		96.025		100.00045		917.09567		96.025		100.05072		918.52422		96.025		100.07814		919.6499		96.025		100.04786

		897.18597		96.05		99.99806		100.05068		896.73199		96.05		99.99522		897.12598		96.05		99.99872		917.34623		96.05		100.05068		918.77555		96.05		100.07818		919.89278		96.05		100.04788

		897.45001		96.075		99.99817		100.05065		896.98999		96.075		99.99651		897.38202		96.075		99.99969		917.60166		96.075		100.05065		919.02578		96.075		100.0782		920.13445		96.075		100.0479

		897.71002		96.1		99.99937		100.05061		897.26001		96.1		99.99302		897.646		96.1		100.00035		917.856		96.1		100.05061		919.27745		96.1		100.07823		920.37946		96.1		100.04792

		897.98102		96.125		99.99796		100.05059		897.51398		96.125		99.99356		897.91199		96.125		99.99933		918.10589		96.125		100.05059		919.525		96.125		100.07824		920.62979		96.125		100.04793

		898.24701		96.15		99.99797		100.05056		897.78198		96.15		99.99365		898.17603		96.15		99.99926		918.35322		96.15		100.05056		919.76645		96.15		100.07825		920.88123		96.15		100.04795

		898.50201		96.175		100.00169		100.05055		898.04199		96.175		99.99503		898.43701		96.175		100.00072		918.60055		96.175		100.05055		920.00434		96.175		100.07825		921.13357		96.175		100.04796

		898.77698		96.2		100.00161		100.05054		898.30798		96.2		99.99704		898.70001		96.2		100.00078		918.85178		96.2		100.05054		920.24211		96.2		100.07824		921.38634		96.2		100.04798

		899.039		96.225		99.99967		100.05054		898.578		96.225		99.99538		898.95599		96.225		100.00028		919.10244		96.225		100.05054		920.49044		96.225		100.07823		921.641		96.225		100.048

		899.30298		96.25		99.99701		100.05055		898.828		96.25		99.99182		899.22699		96.25		99.99815		919.35567		96.25		100.05055		920.74367		96.25		100.07821		921.89212		96.25		100.04802

		899.56897		96.275		99.99957		100.05056		899.09302		96.275		99.99601		899.48999		96.275		100.00072		919.60067		96.275		100.05056		920.99678		96.275		100.07818		922.1429		96.275		100.04804

		899.83502		96.3		99.99785		100.05058		899.35699		96.3		99.99421		899.74902		96.3		99.99854		919.842		96.3		100.05058		921.25056		96.3		100.07815		922.39334		96.3		100.04807

		900.09497		96.325		99.99637		100.0506		899.62598		96.325		99.99366		900.013		96.325		99.9983		920.08255		96.325		100.0506		921.50134		96.325		100.07812		922.63911		96.325		100.04809

		900.362		96.35		99.99583		100.05062		899.883		96.35		99.99431		900.27502		96.35		99.99886		920.32733		96.35		100.05062		921.75267		96.35		100.07807		922.88178		96.35		100.04812

		900.62701		96.375		99.996		100.05064		900.151		96.375		99.99002		900.53998		96.375		99.99814		920.57833		96.375		100.05064		922.002		96.375		100.07803		923.12267		96.375		100.04815

		900.89099		96.4		99.99813		100.05066		900.40802		96.4		99.99882		900.789		96.4		99.9997		920.83044		96.4		100.05066		922.25522		96.4		100.07798		923.36367		96.4		100.04818

		901.14697		96.425		99.99818		100.05068		900.67297		96.425		99.99307		901.065		96.425		99.99907		921.08222		96.425		100.05068		922.51133		96.425		100.07792		923.61389		96.425		100.04821

		901.409		96.45		99.99865		100.05069		900.93103		96.45		99.99404		901.32599		96.45		100.00042		921.33578		96.45		100.05069		922.75667		96.45		100.07787		923.86511		96.45		100.04823

		901.664		96.475		99.99921		100.05069		901.19		96.475		99.99295		901.57898		96.475		99.99962		921.58956		96.475		100.05069		922.99744		96.475		100.07781		924.11766		96.475		100.04826

		901.94202		96.5		99.99862		100.05069		901.46802		96.5		99.99367		901.84497		96.5		99.99997		921.84344		96.5		100.05069		923.23566		96.5		100.07776		924.37088		96.5		100.04829

		902.20099		96.525		100.00094		100.05068		901.73297		96.525		99.99156		902.09998		96.525		99.99851		922.09545		96.525		100.05068		923.47955		96.525		100.07771		924.62455		96.525		100.04831

		902.45697		96.55		99.99717		100.05066		901.98999		96.55		99.99214		902.36102		96.55		99.99894		922.34956		96.55		100.05066		923.73211		96.55		100.07766		924.87811		96.55		100.04833

		902.72803		96.575		99.99992		100.05064		902.25299		96.575		99.99718		902.63		96.575		100.00001		922.59978		96.575		100.05064		923.983		96.575		100.07762		925.1311		96.575		100.04835

		902.98798		96.6		99.99642		100.05061		902.51898		96.6		99.99365		902.89301		96.6		99.9988		922.84189		96.6		100.05061		924.23789		96.6		100.07758		925.385		96.6		100.04837

		903.24902		96.625		99.99872		100.05058		902.78003		96.625		99.99263		903.15997		96.625		99.99681		923.08178		96.625		100.05058		924.48944		96.625		100.07756		925.63822		96.625		100.04839

		903.52301		96.65		99.99699		100.05055		903.04303		96.65		99.99334		903.41602		96.65		99.99867		923.319		96.65		100.05055		924.739		96.65		100.07754		925.88233		96.65		100.0484

		903.784		96.675		99.99858		100.05052		903.30902		96.675		99.99579		903.685		96.675		100.00105		923.56367		96.675		100.05052		924.99145		96.675		100.07753		926.123		96.675		100.04842

		904.04602		96.7		99.99948		100.05049		903.56299		96.7		99.99427		903.95203		96.7		99.99986		923.81133		96.7		100.05049		925.24689		96.7		100.07754		926.36334		96.7		100.04843

		904.30902		96.725		99.99962		100.05046		903.82703		96.725		99.99542		904.21899		96.725		100.00157		924.06011		96.725		100.05046		925.50178		96.725		100.07755		926.61001		96.725		100.04844

		904.578		96.75		99.99591		100.05044		904.09399		96.75		99.99485		904.479		96.75		100.00053		924.311		96.75		100.05044		925.74967		96.75		100.07758		926.86223		96.75		100.04846

		904.83698		96.775		99.99759		100.05042		904.35199		96.775		99.99802		904.73999		96.775		100.00134		924.56133		96.775		100.05042		925.98844		96.775		100.07761		927.11723		96.775		100.04848

		905.10199		96.8		99.99695		100.05041		904.61298		96.8		99.99369		905.00299		96.8		99.99734		924.81211		96.8		100.05041		926.22989		96.8		100.07766		927.37312		96.8		100.04849

		905.36298		96.825		99.99919		100.05042		904.88		96.825		99.99499		905.25201		96.825		100.00062		925.06655		96.825		100.05042		926.46766		96.825		100.07772		927.62823		96.825		100.04852

		905.63		96.85		99.99721		100.05043		905.13898		96.85		99.99378		905.51703		96.85		99.99928		925.32466		96.85		100.05043		926.71855		96.85		100.07779		927.88323		96.85		100.04854

		905.88898		96.875		99.99768		100.05046		905.40399		96.875		99.99537		905.78497		96.875		99.9993		925.58333		96.875		100.05046		926.96955		96.875		100.07787		928.1389		96.875		100.04858

		906.15302		96.9		99.99651		100.0505		905.67297		96.9		99.99436		906.052		96.9		99.99844		925.82911		96.9		100.0505		927.21966		96.9		100.07796		928.39579		96.9		100.04861

		906.41998		96.925		99.99615		100.05055		905.93402		96.925		99.99638		906.31201		96.925		99.99837		926.06933		96.925		100.05055		927.46832		96.925		100.07805		928.65223		96.925		100.04866

		906.67603		96.95		99.99691		100.05061		906.203		96.95		99.99285		906.57501		96.95		100.00006		926.31055		96.95		100.05061		927.71932		96.95		100.07816		928.90456		96.95		100.04871

		906.94202		96.975		99.99927		100.05068		906.46698		96.975		99.99646		906.83301		96.975		100.00122		926.55333		96.975		100.05068		927.97243		96.975		100.07827		929.14789		96.975		100.04877

		907.20801		97		99.99725		100.05077		906.72803		97		99.99502		907.09998		97		99.99955		926.80033		97		100.05077		928.22888		97		100.07839		929.38722		97		100.04883

		907.45801		97.025		99.99667		100.05086		906.98901		97.025		99.99634		907.36401		97.025		100.00089		927.052		97.025		100.05086		928.48376		97.025		100.07851		929.62444		97.025		100.04891

		907.72601		97.05		99.99934		100.05096		907.24103		97.05		99.99394		907.62402		97.05		99.99959		927.30233		97.05		100.05096		928.73676		97.05		100.07864		929.87177		97.05		100.04899

		907.995		97.075		99.99948		100.05107		907.51801		97.075		99.99423		907.88702		97.075		100.00001		927.55244		97.075		100.05107		928.97632		97.075		100.07877		930.122		97.075		100.04907

		908.25299		97.1		99.99991		100.05118		907.78101		97.1		99.99444		908.15601		97.1		100.00146		927.80366		97.1		100.05118		929.21455		97.1		100.07889		930.37411		97.1		100.04915

		908.521		97.125		99.99851		100.05129		908.03003		97.125		99.99556		908.41699		97.125		100.00153		928.05821		97.125		100.05129		929.45266		97.125		100.07901		930.62711		97.125		100.04924

		908.78497		97.15		99.99966		100.0514		908.29401		97.15		99.99485		908.67798		97.15		100.00083		928.31622		97.15		100.0514		929.69466		97.15		100.07913		930.87944		97.15		100.04932

		909.04602		97.175		99.99803		100.05151		908.55798		97.175		99.9921		908.94897		97.175		100.00139		928.57199		97.175		100.05151		929.94288		97.175		100.07924		931.12877		97.175		100.04941

		909.31201		97.2		99.99797		100.05161		908.82898		97.2		99.99486		909.20898		97.2		99.99924		928.82622		97.2		100.05161		930.19011		97.2		100.07934		931.38022		97.2		100.04948

		909.56799		97.225		100.00004		100.0517		909.08801		97.225		99.99137		909.47198		97.225		100.00251		929.07544		97.225		100.0517		930.43722		97.225		100.07943		931.63333		97.225		100.04955

		909.83099		97.25		99.99821		100.05179		909.35797		97.25		99.99209		909.72803		97.25		99.99749		929.32011		97.25		100.05179		930.68389		97.25		100.07951		931.88911		97.25		100.04962

		910.099		97.275		99.99938		100.05186		909.62097		97.275		99.99481		909.987		97.275		100.00302		929.56178		97.275		100.05186		930.93456		97.275		100.07958		932.13622		97.275		100.04967

		910.37		97.3		100.00052		100.05192		909.88599		97.3		99.99412		910.25201		97.3		100.002		929.81345		97.3		100.05192		931.18656		97.3		100.07963		932.37922		97.3		100.04971

		910.62598		97.325		99.99967		100.05197		910.151		97.325		99.99434		910.521		97.325		99.99992		930.06801		97.325		100.05197		931.43956		97.325		100.07968		932.61911		97.325		100.04975

		910.88702		97.35		99.99838		100.05201		910.41602		97.35		99.99402		910.78101		97.35		99.99757		930.32079		97.35		100.05201		931.69645		97.35		100.07972		932.86922		97.35		100.04979

		911.15399		97.375		99.99653		100.05205		910.67603		97.375		99.99363		911.04999		97.375		100.00012		930.573		97.375		100.05205		931.94889		97.375		100.07976		933.12244		97.375		100.04981

		911.41101		97.4		99.99948		100.05207		910.94299		97.4		99.9958		911.30701		97.4		99.9997		930.82689		97.4		100.05207		932.19501		97.4		100.07979		933.37488		97.4		100.04984

		911.677		97.425		99.99858		100.05209		911.20502		97.425		99.99671		911.57898		97.425		99.99961		931.07756		97.425		100.05209		932.43979		97.425		100.07982		933.62644		97.425		100.04986

		911.94299		97.45		100.00008		100.05211		911.466		97.45		99.99571		911.836		97.45		100.00032		931.32922		97.45		100.05211		932.68056		97.45		100.07986		933.87644		97.45		100.04989

		912.203		97.475		99.99621		100.05213		911.72302		97.475		99.99289		912.10797		97.475		99.99951		931.58122		97.475		100.05213		932.93256		97.475		100.0799		934.12667		97.475		100.04992

		912.47302		97.5		99.99781		100.05215		911.987		97.5		99.9959		912.35999		97.5		100.00176		931.83744		97.5		100.05215		933.18556		97.5		100.07994		934.376		97.5		100.04996

		912.73102		97.525		100.00052		100.05218		912.25201		97.525		99.99454		912.63202		97.525		100.0018		932.08189		97.525		100.05218		933.43823		97.525		100.08		934.62912		97.525		100.05

		912.99902		97.55		99.99649		100.05222		912.51599		97.55		99.99467		912.89801		97.55		100.00009		932.32255		97.55		100.05222		933.69334		97.55		100.08006		934.88511		97.55		100.05005

		913.26599		97.575		99.99948		100.05227		912.771		97.575		99.99778		913.16302		97.575		100.00092		932.56222		97.575		100.05227		933.94567		97.575		100.08013		935.13222		97.575		100.05011

		913.52301		97.6		99.99781		100.05232		913.03497		97.6		99.99342		913.42102		97.6		99.99952		932.81099		97.6		100.05232		934.19712		97.6		100.08021		935.37367		97.6		100.05018

		913.78497		97.625		100.00018		100.05239		913.30603		97.625		99.99755		913.67798		97.625		100.00221		933.06266		97.625		100.05239		934.44845		97.625		100.0803		935.61511		97.625		100.05026

		914.04999		97.65		99.99853		100.05247		913.56299		97.65		99.99407		913.94501		97.65		99.99901		933.31588		97.65		100.05247		934.70122		97.65		100.08039		935.862		97.65		100.05034

		914.31897		97.675		99.99754		100.05255		913.83002		97.675		99.99618		914.20099		97.675		99.99996		933.5671		97.675		100.05255		934.95711		97.675		100.08048		936.11511		97.675		100.05043

		914.57898		97.7		99.99917		100.05264		914.091		97.7		99.99431		914.46997		97.7		99.99997		933.82021		97.7		100.05264		935.20144		97.7		100.08058		936.3661		97.7		100.05052

		914.84998		97.725		99.99894		100.05274		914.36102		97.725		99.99535		914.72198		97.725		99.99875		934.07266		97.725		100.05274		935.44255		97.725		100.08067		936.61999		97.725		100.0506

		915.10498		97.75		100.00186		100.05283		914.62299		97.75		99.99711		914.98798		97.75		100.00173		934.32788		97.75		100.05283		935.68555		97.75		100.08075		936.87088		97.75		100.05069

		915.37701		97.775		99.99803		100.05292		914.888		97.775		99.9945		915.24799		97.775		99.99907		934.58499		97.775		100.05292		935.93355		97.775		100.08083		937.12021		97.775		100.05077

		915.63		97.8		99.99813		100.053		915.15302		97.8		99.99638		915.51801		97.8		100.00052		934.84389		97.8		100.053		936.18333		97.8		100.08089		937.3681		97.8		100.05085

		915.896		97.825		99.99476		100.05308		915.40997		97.825		99.99431		915.77399		97.825		99.99839		935.09244		97.825		100.05308		936.43433		97.825		100.08095		937.62066		97.825		100.05091

		916.164		97.85		99.9961		100.05315		915.672		97.85		99.99216		916.04401		97.85		99.99904		935.33633		97.85		100.05315		936.68656		97.85		100.081		937.87366		97.85		100.05098

		916.42798		97.875		99.99942		100.0532		915.94202		97.875		99.99439		916.31		97.875		100.00036		935.58167		97.875		100.0532		936.93889		97.875		100.08103		938.12377		97.875		100.05103

		916.69397		97.9		100.00038		100.05325		916.20099		97.9		99.99684		916.57501		97.9		99.99972		935.83289		97.9		100.05325		937.18933		97.9		100.08106		938.37033		97.9		100.05107

		916.948		97.925		99.9986		100.05328		916.45697		97.925		99.99508		916.84302		97.925		99.99911		936.08845		97.925		100.05328		937.44266		97.925		100.08107		938.61733		97.925		100.05111

		917.21997		97.95		99.99839		100.0533		916.72803		97.95		99.9941		917.104		97.95		100.00013		936.34489		97.95		100.0533		937.69655		97.95		100.08108		938.86022		97.95		100.05114

		917.48401		97.975		99.99813		100.05332		916.98499		97.975		99.99661		917.362		97.975		100.00095		936.603		97.975		100.05332		937.94878		97.975		100.08108		939.116		97.975		100.05117

		917.75299		98		100.00157		100.05332		917.24402		98		99.99671		917.62799		98		100.00169		936.86011		98		100.05332		938.19567		98		100.08109		939.37211		98		100.05119

		918.008		98.025		99.99699		100.05332		917.51001		98.025		99.99444		917.89801		98.025		100.00115		937.11744		98.025		100.05332		938.43966		98.025		100.08109		939.62845		98.025		100.0512

		918.28302		98.05		99.99806		100.05332		917.77502		98.05		99.99742		918.15802		98.05		99.9992		937.37699		98.05		100.05332		938.68311		98.05		100.08109		939.88289		98.05		100.05122

		918.53998		98.075		99.99866		100.05332		918.02802		98.075		99.99531		918.41803		98.075		100.00105		937.63633		98.075		100.05332		938.92544		98.075		100.0811		940.13877		98.075		100.05124

		918.79401		98.1		99.99937		100.05332		918.297		98.1		99.99581		918.67102		98.1		99.99976		937.89388		98.1		100.05332		939.17489		98.1		100.08112		940.39467		98.1		100.05125

		919.05902		98.125		99.9976		100.05332		918.55402		98.125		99.99295		918.935		98.125		100.00043		938.14699		98.125		100.05332		939.42889		98.125		100.08114		940.64934		98.125		100.05127

		919.32599		98.15		99.99659		100.05333		918.81403		98.15		99.99393		919.19897		98.15		100.00023		938.39477		98.15		100.05333		939.68056		98.15		100.08117		940.90323		98.15		100.05129

		919.58502		98.175		99.99853		100.05334		919.08698		98.175		99.99564		919.46301		98.175		100.00029		938.64054		98.175		100.05334		939.93333		98.175		100.08121		941.15956		98.175		100.05132

		919.86298		98.2		100.00012		100.05336		919.35101		98.2		99.99518		919.72198		98.2		100.00151		938.88354		98.2		100.05336		940.18433		98.2		100.08127		941.40578		98.2		100.05135

		920.11401		98.225		99.99679		100.0534		919.61499		98.225		99.99459		919.98297		98.225		99.99977		939.13777		98.225		100.0534		940.43488		98.225		100.08133		941.65112		98.225		100.05139

		920.38		98.25		99.99735		100.05343		919.87799		98.25		99.99273		920.25		98.25		99.99845		939.39266		98.25		100.05343		940.68733		98.25		100.0814		941.89578		98.25		100.05143

		920.64203		98.275		100.00153		100.05348		920.14001		98.275		99.99893		920.51099		98.275		100.00155		939.64588		98.275		100.05348		940.94022		98.275		100.08148		942.147		98.275		100.05147

		920.914		98.3		100.00185		100.05353		920.40997		98.3		99.99564		920.78101		98.3		100.00063		939.90011		98.3		100.05353		941.19477		98.3		100.08156		942.40044		98.3		100.05152

		921.17499		98.325		100.00142		100.05359		920.66699		98.325		99.99554		921.04498		98.325		99.9993		940.154		98.325		100.05359		941.43955		98.325		100.08165		942.65167		98.325		100.05157

		921.44098		98.35		99.99945		100.05365		920.92902		98.35		99.99608		921.31201		98.35		100.00052		940.40845		98.35		100.05365		941.68022		98.35		100.08174		942.90433		98.35		100.05163

		921.69897		98.375		99.99818		100.05371		921.20502		98.375		99.99407		921.56403		98.375		99.99872		940.66134		98.375		100.05371		941.91888		98.375		100.08184		943.15822		98.375		100.05169

		921.96301		98.4		99.99978		100.05378		921.46503		98.4		99.99335		921.82098		98.4		100.00061		940.91523		98.4		100.05378		942.165		98.4		100.08193		943.411		98.4		100.05176

		922.224		98.425		99.99788		100.05385		921.71899		98.425		99.99477		922.09698		98.425		100.00095		941.17134		98.425		100.05385		942.41844		98.425		100.08203		943.66255		98.425		100.05182

		922.492		98.45		100.00086		100.05392		921.98901		98.45		99.99826		922.36102		98.45		100.00182		941.41723		98.45		100.05392		942.67055		98.45		100.08212		943.91377		98.45		100.05188

		922.75702		98.475		100.0017		100.05399		922.25403		98.475		99.99607		922.63397		98.475		100.00087		941.6599		98.475		100.05399		942.92355		98.475		100.0822		944.16822		98.475		100.05195

		923.02197		98.5		99.9981		100.05406		922.51703		98.5		99.99658		922.89301		98.5		99.99943		941.90268		98.5		100.05406		943.17755		98.5		100.08228		944.41589		98.5		100.05201

		923.28302		98.525		99.99852		100.05413		922.77502		98.525		99.99532		923.15002		98.525		100.00045		942.15501		98.525		100.05413		943.42944		98.525		100.08236		944.65811		98.525		100.05207

		923.55298		98.55		99.99763		100.0542		923.03802		98.55		99.99586		923.42102		98.55		100.00066		942.41168		98.55		100.0542		943.68222		98.55		100.08244		944.90233		98.55		100.05212

		923.81799		98.575		100.00046		100.05426		923.30298		98.575		99.99734		923.68597		98.575		100.00002		942.668		98.575		100.05426		943.93578		98.575		100.0825		945.14722		98.575		100.05218

		924.08301		98.6		100.00013		100.05433		923.57202		98.6		99.99527		923.95502		98.6		100.00217		942.92533		98.6		100.05433		944.19189		98.6		100.08257		945.40088		98.6		100.05223

		924.33801		98.625		99.9994		100.05439		923.83398		98.625		99.99443		924.21301		98.625		100.00039		943.183		98.625		100.05439		944.44055		98.625		100.08263		945.65721		98.625		100.05228

		924.60498		98.65		99.99933		100.05445		924.08698		98.65		99.99667		924.47699		98.65		100.00142		943.438		98.65		100.05445		944.68389		98.65		100.08269		945.91099		98.65		100.05233

		924.87701		98.675		99.99908		100.05452		924.35699		98.675		99.99565		924.742		98.675		99.99972		943.69244		98.675		100.05452		944.92878		98.675		100.08275		946.16522		98.675		100.05238

		925.14203		98.7		99.99823		100.05458		924.61401		98.7		99.99453		924.99701		98.7		100.00161		943.9491		98.7		100.05458		945.17289		98.7		100.0828		946.4171		98.7		100.05243

		925.401		98.725		99.99864		100.05465		924.88		98.725		99.99732		925.258		98.725		100.00101		944.20555		98.725		100.05465		945.42189		98.725		100.08286		946.67177		98.725		100.05247

		925.65698		98.75		99.99887		100.05471		925.14301		98.75		99.9956		925.52399		98.75		100.00145		944.45188		98.75		100.05471		945.67111		98.75		100.08291		946.92899		98.75		100.05251

		925.92297		98.775		99.99967		100.05478		925.41302		98.775		99.99503		925.784		98.775		100.00103		

_1554468339.xls
Grafikon1

		670		670

		690		690

		710		710

		730		730

		750		750



FeCrAl

NiCr

Temperature [°C]

Coating thicknes [µm]

29.7

24.9

50.1

26.8

54.5

28.3

108.4

33.9

40.6



List1

		

				FeCrAl		NiCr

		670		29.7		24.9

		690		50.1		26.8

		710		54.5		28.3

		730		108.4		33.9

		750				40.6





List1

		



FeCrAl

NiCr

Temperature [°C]

Coating thicknes [µm]




