Dragi Stamenković, Mato Perić

_____________________________________________________________________________

Determination of residual stresses in tubular welded structural components
_____________________________________________________________________________


DETERMINATION OF RESIDUAL STRESSES IN TUBULAR WELDED STRUCTURAL COMPONENTS

Dragi Stamenković1, Mato Perić2
Summary: Numerical simulation of welding process with an example of two tubes of both same and different steel materials properties have been carried out in this paper. It is shown that the residual stress field and temperature field are symmetric in case of welding same materials, while in case of welding materials with different thermo-mechanical properties they are asymmetric. So, it can be concluded that beside thermo-mechanical properties of material, pipe diameter and pipe wall thickness can also influence the asymmetry of residual stress and temperature field.
Keywords: Welding process, Residual stress, Dissimilar butt-weld, Finite element methods, Abaqus
1.  INTRODUCTION

Residual stresses and distortion are common unavoidable adverse consequences of welding process that appear due to localized heating and subsequent rapid cooling material. High residual stresses  in regions near the weld  can cause fatigue, stress or fracture corrosion cracking. Therefore, estimating the magnitude and distribution of welding residual stresses is of great importance. 

In the early days of exploration of residual stresses and deformations in the welded structures, we relied on experimental methods: X-ray diffraction [1, 2], hole drilling [3], ultrasonic [4] and cracking [5]. In order to estimate residual stresses, in the last 30 years, finite element method has been used, by which is tried to substitute a rather expensive experiment [6-15]. Analytical methods remained limited to simpler problems. On the example of welding two tubes with the same material properties, Teng [6] proved that pipe diameter and wall thickness influence the size and distribution of residual stresses in welding of steel pipe. 
The welding of pipes and plates of steel with different thermo-mechanical properties is used in the case of constructing power plants and ships, which can be very well simulated using numerical methods. In the example of welding two tubes of size ø219 x 8.18 mm, and with the ‘’V’’ shape of weld groove, made from carbon and alloy steel, Akbari [7] showed that the temperature fields and residual stress fields are asymmetric. 

This paper presents two numerical simulations of welding two steel pipes of dimensions ø324.0 x 3.96 mm with the constant width of the weld of 3.84 mm throughout the whole tube wall, model A and model B. In the model A the welding of two pipes of the same carbonate steel was simulated, whilst in the model B the welding of tubes of carbon and stainless steel is stimulated. 

2.  FINITE ELEMENT ANALYSIS APPROACH 

The numerical simulations performed in this work use sequential thermal-stress solution procedure in which the transient heat transfer analysis is followed by the thermal stress analysis. Temperatures predicted by the heat transfer analysis are used as the loading for thermal stress analysis.
2.1.  Thermal model

The governing equation for transient non-linear heat transfer analysis is:


[image: image1.wmf]t

T

C

Q

z

T

k

z

y

T

k

y

x

T

k

x

z

y

x

¶

¶

=

+

÷

ø

ö

ç

è

æ

¶

¶

¶

¶

+

÷

÷

ø

ö

ç

ç

è

æ

¶

¶

¶

¶

+

÷

ø

ö

ç

è

æ

¶

¶

¶

¶

r

                                                (1)

where, 
[image: image2.wmf]x

k

, 
[image: image3.wmf],

y

k



 EMBED Equation.3  [image: image4.wmf]z

k

 thermal conductivity in the 
[image: image5.wmf]x

, 
[image: image6.wmf]y

 and 
[image: image7.wmf]z

 respectively, 
[image: image8.wmf]T

 is the current temperature, 
[image: image9.wmf]Q

 is the heat generation, 
[image: image10.wmf]r

 is the density, 
[image: image11.wmf]C

 is the specific heat capacity and 
[image: image12.wmf]t

 is the time, respectively. General solution of equation (1) is obtained introducing the initial and boundary conditions, as follows:

Initial condition:


[image: image13.wmf])

,

,

(

)

0

,

,

,

(

0

z

y

x

T

z

y

x

T

=

                                                                                                        (2)

Boundary conditions:


[image: image14.wmf]0

)

(

)

(

r

r

=

-

+

-

+

+

÷

÷

ø

ö

ç

ç

è

æ

¶

¶

+

¶

¶

+

¶

¶

¥

T

T

h

T

T

h

q

z

T

k

N

y

T

k

N

x

T

k

c

s

z

y

y

x

x

                          (3)

where, 
[image: image15.wmf]x

N

, 
[image: image16.wmf]y

N

, 
[image: image17.wmf]z

N

 are the direction cosine normal to the boundary, 
[image: image18.wmf]c

h

, 
[image: image19.wmf]r

h

 are the convection and radiation heat transfer coefficients respectively, 
[image: image20.wmf]s

q

 is the boundary heat flux and 
[image: image21.wmf]r

T

 is the temperature of radiation heat source and 
[image: image22.wmf]¥

T

 are the surrounding temperature. Radiation heat losses are dominant near the weld and can be expressed by equations:


[image: image23.wmf])

)(

(

r

2

r

2

r

T

T

T

T

F

h

+

+

=

se

                                                                                                  (4)
where, 
[image: image24.wmf]8

10

67

.

5

-

´

=

s

 J/(m2K4) is the Steffan-Boltzman constant, 
[image: image25.wmf]e

 is the effective emissivity and 
[image: image26.wmf]F

is the configuration factor.  Moving away from the weld zone radiation heat losses decrease and increase the share of convection heat loses 
[image: image27.wmf]c

h

. The total heat input is given by:


[image: image28.wmf]H

V

UI

q

h

=

                                                                                                                                   (5)
where, 
[image: image29.wmf]h

 the arc efficiency, 
[image: image30.wmf]V

is volume of the weld bead, 
[image: image31.wmf]I

 is current, 
[image: image32.wmf]U

 is the arc voltage and 
[image: image33.wmf]H

V

 is volume of the activated weld bead element. 

2.2. Mechanical model

The equilibrium equation can be expressed as:


[image: image34.wmf]0

=

+

i

ij

b

r

s

                                                                                                                            (6)

[image: image35.wmf]ji

ij

s

s

=

                                                                                                                                    (7)
In equations (6) and (7)  
[image: image36.wmf]ij

s

 is the stress tensor, 
[image: image37.wmf]r

 is density and 
[image: image38.wmf]i

b

 is the body force. In numerical simulation, it was used thermal-plastic constitutive equations:


[image: image39.wmf][

]

[

]

[

]

[

]

dT

C

d

D

d

th

ep

-

=

e

s

                                                                                                   (8)

[image: image40.wmf][

]

[

]

[

]

[

]

dT

C

d

D

d

th

ep

-

=

e

s

                                                                                                   (9)
where, 
[image: image41.wmf][

]

e

D

 is the elastic stiffness matrix, 
[image: image42.wmf][

]

p

D

 is the plastic stiffnes matrix, 
[image: image43.wmf]th

C

 is the thermal stiffness matrix, 
[image: image44.wmf][

]

e

d

 is the strain increment and 
[image: image45.wmf]dT

 is the temperature increment.

3.  BUTT-WELDED OF TWO PIPES  
Two numerical simulations of welding were performed, model A and model B.  In the model A the welding of two pipes of the same carbon steel, A 106-B, is simulated. In the model B the welding of tubes of carbon steel, A 106-B and stainless steel, A240 TP304, is stimulated. Diameter of tubes are ø324 mm, thickness of wall 3.96 mm and lenght of each tube 200 mm. Mechanical and thermal properties are given in Figure 1, 2, 3 and 4. The material is modelled as an elastic – ideally plastic. Welding parameters chosen for this analysis are as follows: tungsten inert gas welding, welding current I=110 A, welding voltage U=20 V and welding speed v=5 mm/s. The following values are assumed: the convective heat transfer hc=15 W/m2K, the arc efficiency 
[image: image46.wmf]h

 =70%  and the emissivity ε= 0.8. Welding of pipes is modelled in single 

pass. The specific heat flux input is 
[image: image47.wmf]10

10

076

.

2

´

=

q

 J/m3s. Width of welding bead is 3.84 mm and constant throughout the whole tube wall. The analyses are made with standard method for modelling of weld. Three-dimensional mesh consists of 14400 elements. The same mesh is used both for thermal and mechanical analysis. In thermal model DC3D8 elements are used, while for mechanical model C3D8 elements are used, according to ABAQUS code [15]. The smallest elements whose size is 5 x 1.92 x 1.32 mm are used at the root of the welded joint. Geometry of welded pipes and mechanical boundary conditions are shown in Figure 5.
[image: image48.emf]0

0,2

0,4

0,6

0,8

1

1,2

1,4

1,6

1,8

0 200 400 600 800 1000 1200 1400 1600

Temperature (°C)

Thermal Properties

Thermal conductivity

Density

Specific heat

r

 (10

-2

g/mm

3

)

C (J/g/°C)

l

 (10

-1

J/mm/s/°C)


Fig. 1 Thermal properties of steel A106-B
[image: image49.emf]0

50

100

150

200

250

300

0 200 400 600 800 1000 1200 1400 1600

Temperature (°C)

Mechanical Properties

Youngs Modulus (GPa)

Yield Stress (MPa)

Thermal Expansion Coefficient

Poisson ratio

a

(10

-7

m/m/K)

10

-3

n


Fig. 2  Mechanical properties of steel A106-B

[image: image50.emf]0

0,2

0,4

0,6

0,8

1

1,2

0 200 400 600 800 1000 1200 1400 1600

Temperature (°C)

Thermal Properties

Thermal conductivity

Specific heat

Density

r

 (10

-2

g/mm

3

)

l

 (10

-1

J/mm/s/°C)

C (J/g/°C)


Fig. 3  Thermal properties of steel A240 TP304
[image: image51.emf]0

50

100

150

200

250

300

0 200 400 600 800 1000 1200 1400 1600

Temperature (°C)

Mechanical Properties

Youngs Modulus (GPa)

Yield Stress (MPa)

Thermal Expansion Coefficient

Poisson ratio

a

(10

-7

m/m/K)

10

-3

n


Fig. 4  Mechanical properties of steel A240 TP304

[image: image52.emf]b


0°


90°


270°


180°


start of welding


20


0


20


0


40


0


O324 x 3.96


A106-B


A240 TP304


mechanical restraint in x, y and z direction


mechanical restraint in  y and z direction


mechanical restraint in  y  direction


weld


z


x


y






0°

90° 270°

180°

start of welding

200 200

400

O324 x 3.96

A106-B A240 TP304

mechanical restraint in x, y and z direction

mechanical restraint in  y and z direction

mechanical restraint in  y  direction

weld

z

x

y


Fig. 5  Geometry of welded pipes and mechanical boundary conditions

4.  RESULTS

Temperature field 50 s after welding for model A and model B are shown in Figures 6 and 7. Comparison of temperature profiles in  z direction for model A and model B, 50 s after welding is shown in Figures 8. Temperature profiles, shown in Figures 8,  are the same at inner and outer surface of tubes for Model A and Model B. In Figures 9 and 10 are shown residual stress field ,
[image: image53.wmf]z

σ

, in z direction for Model A i Model B. In Figures 11 and 12 are shown  comparison of residual stresses in z direction at inner and outer surfaces for 
[image: image54.wmf]b

=180°,  Model A and Model B.


[image: image55.png]AN
;/////////////////////

/////////

N

NMANIRER

N





Fig. 6  Temperature field 50 s after welding, Model A


[image: image56.png]



Fig. 7 Temperature field 50 s after welding, Model B
[image: image57.emf]-20

0

20

40

60

80

100

120

0 50 100 150 200 250 300 350 400

Z - Coordinate (mm)

Temperature (°C)

Model A

Model B

A240 

TP304

A106-B


Fig. 8  Comparison of temperature profiles in  z direction, 
[image: image58.wmf]b

=180°, Model A and  Model B


[image: image59.png]



Fig. 9  Residual stress in 
[image: image60.wmf]z

σ

in z direction, Model A


[image: image61.png]



Fig. 10 Residual stress in 
[image: image62.wmf]z

σ

 in z direction, Model B
[image: image63.emf]-100

-50

0

50

100

150

200

250

0 50 100 150 200 250 300 350 400

Z - Coordinate (mm)

Temperature (°C)

Model A

Model B

A240 

TP304

A106-B


Fig. 11 Comparison of residual stresses 
[image: image64.wmf]z

σ

 in z direction, at inner surface for
[image: image65.wmf]b

=180°,  Model A and Model B
[image: image66.emf]-200

-150

-100

-50

0

50

100

0 50 100 150 200 250 300 350 400

Z - Coordinate (mm)

Temperature (°C)

Model A

Model B

A240 

TP304

A106-B


Fig. 12  Comparison of residual stresses 
[image: image67.wmf]z

σ

in z direction, at outer surface for
[image: image68.wmf]b

=180°, Model A and Model B

5.  DISCUSSION AND CONCLUSION   

Numerical simulation of welding two tubes was conducted, carbon steel A-106B, A model, and after this the numerical simulation of welding two tubes made from two different materials carbon steel A106-B and stainless steel A-240 TP304, model B. The weld of the same width across the whole thickness of the tube wall was assumed. Weld of temperature field of such a form becomes uniform along the thickness of the tube at any point of time.

Model A: the symmetry of the temperature field was confirmed (Figures 6 and 8), after this stress fields (Figures 9, 11 and 12) which coincides with the results in Ref [7].

Model B: the asymmetry of the temperature field was confirmed (Figures 7 i 8), after this stress fields (Figures 10, 11 and 12). 

Maximum tensile and compressive strain in z direction in welded tubes made of carbon steel and stainless steel, at outer and inner surface of the tube are more balanced than in Ref [7], which could be attributed to the uniformity of temperature field along the thickness of the wall because of the constant width of the weld tube wall thickness.

LITERATURE

	[1]
	Norton JH, Rosenthal D. Stress measurement by X-ray diffraction. Proceedings of the Society for Experimental Stress Analysis 1944;1(2):73-76.

	[2]
	Norton JH, Rosental D. Recent contribitions to the X-ray method in the field of stress analysis. Proceedings of the Society for Experimental Stress Analysis 1947:5(1):71-77.

	[3]
	Pang HL, Pukas SR.Residual Stress Measurements in a crusi-form welded joint using hole drilling and strain gauges. Strain 1989; February:7-14.

	[4]
	Chu SL, Peukhrt H, Schnieder E. Residual stress in a welded steeel plate and their measurements using ultrasonic techniques. MRL Bull. Res. Dev., 1987;1(2):45-50.

	[5]
	Masubuchi K, Martin DC. Invesigation of residual stresses by use of hydrogen cracking. Welding J., 1961;40:553s-563s.

	[6]
	Teng TL, Chang PH. Three-dimensional thermomechanical analysis of circumferentiallly welded thin-waled pipes. International Journal of Pressure Vessels and Piping 75 (1998) 237-247.

	[7]
	Akbari D., Sattari-Far I. Effect of welding heat input on residual stresses in butt-weld of dissimilar pipe joints. International Journal of Pressure Vessels and Piping 86 (2009) 769-776.

	[8]
	Deng D. FEM prediction of welding residual stress and distortion in carbon steel considering phase transformation effects. Materials and Design 30 (2009) 359-366.

	[9]
	Deng D, Liang W, Murakawa H. Determination of welding deformation in fillet –welded joint by menas of numerical simulation and comparison with experimental measurements. Journal of Materials Processing Technology 183 (2007) 219-225.

	[10]
	Deng D, Murakawa H., Liang W., Numerical simulation of welding distortion in large structures. Computer methods in applied mechanics and engineering 196 (2007) 4613-4627.

	[11]
	Lee CH, Chang KH, Three-dimensional finite element simulation of residual stresses in circumferential welds of steel pipe diameter effects, Material Science and Engineering A (2008) 210-218

	[12]
	Peric M., Tonkovic Z., Karsaj I.: Numerical analysis ofresidual stresses using a shell/3D modeling technique, Proceedings of the International Conference on Advances in Welding Science and Technology for Construction, Energy and Transportation AWST-2010, pp.75-80

	[13]
	Stamenkovic D., Vasovic I.: Finite Element Analysis of Residual Stresses in Butt Welding Two Similar Plates, Scientific Technical Review, ISSN 1820-0206, 2009,Vol. LIX, No.1, pp.57-60.

	[14]
	Peric M., Stamenkovic D., Milkovic V.: Comparison of residual stresses in butt-welded plates using software packages abaqus and ansys, Scientific Technical Review , ISSN 1820-0206, 2010,Vol.60,No.3-4, pp.22-26

	[15]
	ABAQUS/Standard, User's guide and theoretical manual, Version 6.8, Hibbit, Karlsson & Serensen, Inc. (2008).



________________________________________________________________________________________________

MSc, Dragi Stamenković, Belgrade, Termoelektro d.o.o., dragi33@gmail.com
MSc, Mato Perić, Zagreb, Bureau of Energetics and Mechanical Engineering, mato.peric@bestprojekt.hr 

2
11

_1358527308.unknown

_1359021288.unknown

_1363165132.unknown

_1363257094.unknown

_1363257143.unknown

_1363257443.unknown

_1363208610.unknown

_1359024498.unknown

_1363165033.unknown

_1363165042.unknown

_1359052396.unknown

_1359021383.unknown

_1359022398.unknown

_1359022514.unknown

_1359021352.unknown

_1358528973.unknown

_1358617553.unknown

_1358617840.unknown

_1358618217.unknown

_1358617815.unknown

_1358617187.unknown

_1358617309.unknown

_1358529075.unknown

_1358527665.unknown

_1358528337.unknown

_1358528667.unknown

_1358527765.unknown

_1358527462.unknown

_1358527580.unknown

_1358527446.unknown

_1358525843.unknown

_1358526315.unknown

_1358527256.unknown

_1358527281.unknown

_1358527017.unknown

_1358525919.unknown

_1358525974.unknown

_1358525885.unknown

_1358525554.unknown

_1358525577.unknown

_1358525630.unknown

_1358525562.unknown

_1358525438.unknown

_1358525456.unknown

_1352095057.unknown

_1358525408.unknown

_1352095104.unknown

_1352094747.unknown

