Oпажање Fe3O4→α-Fe2O3 фазне трансформације на ниској температури

Виолета Н. Николић1

1Институт за нуклеарне науке "Винча", Универзитет у Београду, Мике Петровића Аласа 12-14, П. О. Бокc 522, 11001 Београд, Србија, violeta@vinca.rs

Магнетно понашање наночестица магнетита обложених олеинском киселином (Fe3O4/OA), синтетисаних хидротермалном методом, детаљно је истражено применом СКВИД мерења, која су урадили Николић и остали [1]. Да би се добио бољи увид у понашање припремљеног узорка који је подвргнут термичкој обради, извршена је детаљнија термо-гравиметријска анализа (термички анализатор ТА-СДТ 2090). Мерење ТГ и ДТА кривих је извршено стандардним протоколом. Такође су извршена додатна мерења узорка осушеног под сниженим притиском. Резултати су открили да процеси који се уочавају као последица термичког третмана имају изражeну егзотермну природу; најинтензивнији ДТА максимум је примећен на око Т = 289 °C. Имајући у виду резултате XRD и ТЕМ анализе [1], као и то да фазна трансформација магнетита у хематит представља егзотермни процес: Fe3O4+14 O2= 32α-Fe2O3+∆H, ∆H=115 kJmol-1 [2,3], уочени егзотермни процес приписaн је фазнoј трансформацији Fe3O4→α-Fe2O3 на ниским температурама (<300 °C). Уочено понашање се може приписати дефектима присутним у кристалној решетки магнетита.

Аутор захваљује др Н. Цвјетићанину на термогравиметријским мерењимa.

Кључне речи: магнетит, хематит, термо-гравиметријска анализа, фазна трансформација.

Observation of Fe3O4→α-Fe2O3 phase transformation at low temperature

Violeta N. Nikolić1

1Institute of Nuclear Sciences "Vinča", University of Belgrade, Mike Petrovića Alasa 12-14, P. O. Box 522, 11001

Belgrade, Serbia, violeta@vinca.rs

The magnetic behavior of nanoparticles of magnetite coated with oleic acid (Fe3O4/OA), synthesized by the hydrothermal method, was investigated in detail by SQUID measurements, performed by Nikolić et al. [1]. In order to get a better insight into the behavior of the prepared sample subjected to heat treatment, a more detailed thermo-gravimetric analysis was performed (thermal analyzer TA-SDT 2090). TG and DTA curves were measured by a standard protocol. Additional measurements of the sample dried under the lowered pressure were also performed. The results revealed that the processes, observed as a consequence of heat treatment, have a strong exothermic nature; the most intense DTA maximum is observed around T = 289 ° C. Having in mind the results of XRD and TEM analysis [1], as well as that the transformation of the magnetite phase into hematite represents an exothermic process: Fe3O4+14 O2= 32α-Fe2O3+∆H, ∆H=115 kJmol-1 [2,3], the observed exothermic process is attributed to Fe3O4→α-Fe2O3 phase transformation at low temperatures (<300 ℃). The observed behavior could be ascribed to the presence of cation deficiency in the magnetite crystal lattice.

The author is gratefully acknowledged Dr N. Cvjetićanin for thermogravimetric measurements.

Keywords: magnetite, hematite, thermo-gravimetric analysis, phase transformation.