Међународни научни скуп Савремени материјали –  Бања Лука.

International Scientific Conference Contemporary Materials – Banja Luka 

Empowering students in science: Phytosynthesis, characterization and biomedical application of metallic  (Ag, Si, Cu) and oxide  (ZnO, TiO2, CuO, Fe2O3) nanoparticles: microbiology, biokinetics and toxicology aspect

Nina Babić1, Dragana Žabić1, Zorica Jerković1, Stefan Četić1, Dragana Milisavić1, Dijana Jelić1
[image: image1.emf]Faculty of Natural Sciences and Mathematics, University of Banja Luka, Republic of Srpska, Bosnia and Herzegovina, nina.babic@student.pmf.unibl.org, dragana.zabic@student.pmf.unibl.org, zorica.jerkic@student.pmf.unibl.org, stefan.cetic@student.pmf.unibl.org, dragana.milisavic@pmf.unibl.org, dijana.jelic@med.unibl.org  
Abstract: Four students of Chemistry Department, Faculty of Natural Sciences and Mathematics, University of Banja Luka were involved in national research project ”Phytosynthesis, characterization and biomedical application of metallic  (Ag, Si, Cu) and oxide (ZnO, TiO2, CuO, Fe2O3) nanoparticles: microbiology, biokinetics and toxicology aspect” led by their professors. Students role was to independently synthesize metallic oxides: ZnO, TiO2, CuO, Fe2O3 using green chemistry approach and to evaluate metallic oxides physicochemical properties. All the metallic oxide sample were phytosynthesized using methanolic extract of flowers of Geranium robertianum L. (Geraniaceae). For characterization students used UV/VIS spectrophotometry, infrared spectroscopy and optical microscope. Additionaly, students evaluated photocatalytic properties of obtained samples, as well as, antimicrobial activity. All the samples were in nanorange, ZnO (530 nm), TiO2 (460 nm), CuO (710 nm), Fe2O3 (980 nm), showed good antimicrobial properties against gramm negative (E.coli) and gramm positive (S. Aureus) bacteria with average MIC value 0.312 mg/mL for S. Aureus and 0.156 mg/mL for E. coli. Photocatalytical efficiency was between 77 - 96% depending on the metallic oxide. The main focus of students involvement in research project was giving importance to scientific work and students’ empowering in scientific research.
Key words: phytosynthesis, photocatalysis, antimicrobial activity, nanoparticles... 
Authors are thankful to the Ministry for Scientific and Technological Development, Higher Education and Information Society of Republic of Srpska for supporting the study through the project No. 19/6-020/961-74/18.

