ЈОНСКА ТЕЧНОСТ НА БАЗИ НИКОТИНАМИДА КАО ПОТЕНЦИЈАЛНИ ИНХИБИТОР КОРОЗИЈЕ БАКРА

Ђенђи Ваштаг,1 Сузана Апостолов1, Милан Вранеш1,Слободан Гаџурић1

1 Универзитет у Новом Саду, Природно-математички факултет, Департман за хемију, биохемију и заштиту животне средине, Трг Д. Обрадовића 3, Нови Сад, Србија

djendji.vastag@dh.uns.ac.rs; suzana.apostolov@dh.uns.ac.rs

milan.vranes@dh.uns.ac.rs; slobodan.gadzuric@dh.uns.ac.rs

Сажетак: У овом раду испитивана је могућност примене новосинтетизоване јонске течности на бази никотинамида као потенцијалног инхибитора корозије бакра у киселој сулфатној средини. Анализирана је инхибиторска ефикасност бутил-никотинамида, [C4Nic]Br на корозију бакра у киселом (pH=3) раствору натријум-сулфата концентације 0,1 mol/dm3, применом поларизационих мерења и електрохемијске импедансне спектроскопије (EIS). Утврђено је да испитивана јонска течност поседује инхибиторске особине на корозију бакра у киселој средини. Инхибиторско дејство испитивано једињењe остварује брзом и спонтаном адсорпцијом [C4Nic]Br молекула на бакарну површину по механизму Лангмирове адсорпционе изотерме, при чему долази до смањења катодне густине струје као и до повећања поларизационог отпора система. Утрвђено је да инхибиторска ефикасност испитиванe јонске течности у великој мери зависи од примењене концентрације.

Кључне ријечи: корозија, бакар, инхибитори, јонске течности

NICOTINAMIDE-BASED IONIC LIQUID AS A POTENTIAL COPPER CORROSION INHIBITOR

Abstract: In this paper, the possibility of using newly synthesized ionic liquid based on nicotinamide as a potential inhibitor of copper corrosion in an acidic sulfate medium was investigated. Inhibition efficiency of butyl-nicotinamide, [C4Nic]Br  on copper corrosion in acidic (pH=3) 0.1 mol/dm3 sodium sulphate solution was analyzed using potentiostatic polarization measurements and electrochemical impedance spectroscopy (EIS). It was found that the investigated ionic liquid has inhibitory properties of the corrosion of copper in acidic media. The inhibitory effect of the test compound is manifested by rapid and spontaneous adsorption of  [C4Nic]Br molecules on the copper surface following the Langmuir’s adsorption isotherm. As a result, the cathodic corrosion current decreases as well as the polarization resistance of the system increases in relation to the basic solution. Inhibition efficiency of the investigated compound largely depends on the applied concentration.

Keywords: corrosion, copper, inhibitors, ionic liquid