KARAKTERIZACIJA SOLARNIH MODULA NA STANDARDNIM USLOVIMA

Darko Divnić1, Dragoljub Mirjanić1, Esad Jakupović1, Zoran Ž. Avramović2, Tomislav Pavlović3, Ivana Radonjić3

1Akademija nauka i umjetnosti Republike Srpske, Bana Lazarevića 1, 78000 Banja Luka, Republika Srpska, BiH, mirjanicd@gmail.com, divnic@gmail.com, dmirjanic@gmail, esadjakupovic50@gmail.com

2Univerzitet u Beogradu, Saobraćajni fakultet, Vojvode Stepe 305 11000 Beograd, Republika Srbija, zoran.avramovic@sf.bg.ac.rs

3 Univerzitet u Nišu, Prirodno-matematički fakultet, Departman za fiziku, Višegradska 33, 18000 Niš, Republika Srbija, pavlovic@pmf.ni.ac.rs, r_ivana_fizika@yahoo.com

Sažetak: Za pretvaranje Sunčevog zračenja u električnu energiju danas se u svijetu koriste solarne ćelije i solarni moduli od različitih materijala i to: monokristalnog, polikristalnog i amorfnog silicijuma na staklu ili plastičnoj osnovi, GaAs, CdTe, CIS i drugih. Eksperimentalna istraživanja i napredak u proizvodnji novih solarnih ćelija pokazuju da se efikasnost solarnih ćelija stalno povećava.

Za karakterizaciju solarnih ćelija i solarnih modula u idealnim standardnim uslovima, osim mjerne opreme, potrebno je zadovoljiti internacionalne standarde testnog okruženja gdje se koriste solarni simulatori sa različitim izvorima svjetlosti. Određivanje energetske efikasnosti solarnih ćelija i solarnih modula pomoću solarnih simulatora vrši se pri sledećim standardnim uslovima: temperaturi od 25oC, solarnom spektru AM1.5 i intenzitetu Sunčevog zračenja od 1000 W/m2, koje  solani simulator mora zadoviljiti po IEC standardu 60904.

U radu su dati rezultati ispitivanja fizickih karakteristika solarnog modula od monokristalnog silicijuma snage 50Wp u Laboratoriji za solarnu energetiku Akademije nauka i umjetnosti Republike Srpske u Banja Luci.

Ključne riječi: Sunčevo zračenje, solarne ćelije, solarni moduli, solarni simulatori, energetska efikasnost

CHARACTERIZATION OF SOLAR MODULES ON STANDARD CONDITIONS

Darko Divnić1, Dragoljub Mirjanić1, Esad Jakupović1, Zoran Ž. Avramović2, Tomislav Pavlović3, Ivana Radonjić3

1Academy of Sciences and Arts of the Republic of Srpska, Bana Lazarevića 1, 78000 Banja Luka, Republic of Srpska, mirjanicd@gmail.com, divnic@gmail.com, dmirjanic@gmail, esadjakupovic50@gmail.com

2University of Belgrade, Faculty of Transport and Traffic Engineering, Vojvode Stepe 305 11000 Belgrade, Republic of Serbia, zoran.avramovic@sf.bg.ac.rs

3University of Niš, Faculty of Sciences and Mathematics, Department of Physics, Višegradska 33, 18000 Niš, Republic of Serbia, pavlovic@pmf.ni.ac.rs, r_ivana_fizika@yahoo.com

Abstract: To convert solar radiation into electricity, solar cells and solar modules made of different materials are used in the world today: monocrystalline, polycrystalline and amorphous silicon on a glass or plastic base, GaAs, CdTe, CIS and others. Experimental research and progress in the production of new solar cells show that the efficiency of solar cells is constantly increasing.

For the characterization of solar cells and solar modules under ideal standard conditions, apart from the measuring equipment, it is necessary to meet the international standards of the test environment where solar simulators with different light sources are used. Determination of the energy efficiency of solar cells and solar modules using solar simulators is carried out under the following standard conditions: temperature of 25oC, solar spectrum AM1.5 and solar radiation intensity of 1000 W/m2, which the solar simulator must meet according to IEC standard 60904.

The paper presents the results of testing the physical characteristics of a 50Wp monocrystalline silicon solar module in the Solar Energy Laboratory of the Academy of Sciences and Arts of the Republic of Srpska in Banja Luka.

Keywords: Solar radiation, solar cells, solar modules, solar simulators, energy efficiency