Међународни научни скуп Савремени материјали –  Бања Лука.

International Scientific Conference Contemporary Materials – Banja Luka 

ANALYSIS OF TISSUE RESPONSE TO COLLAGEN MEMBRANE WITH AND WITHOUT ADDITION OF BLOOD IN A MOUSE SUBCUTANEOUS IMPLANTATION MODEL
Milena Radenković,1 Sanja Stojanović,1,2 Stevo Najman1,2
1Department for Cell and Tissue Engineering, Scientific Research Center for Biomedicine, Faculty of Medicine, University of Niš, 18000 Niš, Serbia,  milena1390nis@gmail.com
2Department of Biology and Human Genetics, Faculty of Medicine, University of Niš, 18000 Niš, Serbia, sanja.genetika.nis@gmail.com, stevo.najman@gmail.com
Abstract: Collagen membranes are widely used in the regeneration of soft and bone tissue when they can be applied alone, enriched with cells and certain physiological factors, or in combination with bone substitutes. As a natural polymer, collagen is a biocompatible material. Collagen can be isolated from various tissue compartments of different organisms, using different production procedures, which causes differences in the physico-chemical characteristics of collagen materials, but also tissue response after implantation. In addition, when placing biomaterials at the site of tissue injury, biomaterials come into contact with blood, which is another factor that can affect the dynamics of the interaction of tissues and implanted biomaterials. The aim of this study was to perform a comparative analysis of the tissue response to the collagen membrane with and without the addition of blood as a physiological factor, in order to predict the tissue response in realistic physiological conditions. The tissues response of to the collagen membrane of porcine origin with and without the addition of blood, as well as the changes in the membranes, were investigated in the mouse subcutaneous implantation model 3, 10 and 30 days after implantation. The explanted membranes and their interaction with the surrounding tissue were analyzed by histological method as well as the application of scanning electron microscopy. A difference was observed in the reaction of the surrounding tissue, which is reflected in the different number of cells and the presence of different cell populations, as well as the pattern of cellular infiltration, at all observed time points The obtained results indicate that the tissue response and the behavior of the implanted collagen membrane differ depending on whether blood is added to the membrane or not, which may have a great practical significance in the clinical application of collagen membranes.

Keywords: collagen  membranes, implantation, tissue response, blood 
АНАЛИЗА ОДГОВОРА ТКИВА НА КОЛАГЕНСКУ МЕМБРАНУ СА И БЕЗ ДОДАТКА КРВИ НА МОДЕЛУ ПОТКОЖНЕ ИМПЛАНТАЦИЈЕ МИШУ
Милена Раденковић, Сања Стојановић,Стево Најман
Сажетак: Колагенске мембране имају широку примену у регенерацији меког и костног ткива када се могу применити самостално, обогаћене ћелијама и одређеним физиолошким факторима, или у комбинацији са коштаним заменицима. Као природни полимер, колаген представља биокомпатибилни материјал. Колаген се може изоловати из разних ткивних компартмената различитих организама, различитим производним процедурама, што условљава разлике у физичко-хемијским карактеристикама колагенских материјала, али и одговор ткива после имплантације. Поред тога, приликом пласирања биоматеријала на место повреде ткива долази до контакта биоматеријала са крвљу, што је још један од фактора који може утицати на динамику интеракције ткива и имплантираног биоматеријала. Циљ ове студије је био да се уради упоредна анализа одговора ткива на колагенску мембрану са и без додатка крви као физиолошког фактора, како би се предвидео одговор ткива у реалним физиолошким условима. Одговор ткива на колагенску мембрану свињског порекла са и без додатка крви, као и промене у мембранама, испитивани су на моделу поткожне имплантације мишу 3, 10 и 30 дана након имплантације. Експлантиране мембране и њихова интеракција са околним ткивом анализирани су хистолошком методом као и применом скенинг електронске микроскопије. Уочена је разлика у реакцији околног ткива која се огледа у различитом броју ћелија и присуству различитих ћелијских популација, као и обрасцу ћелијске инфилтрације, на свим посматраним терминима. Добијени резултати указују на то да се одговор ткива и понашање имплантиране колагенске мембране разликују у зависности од тога да ли је мембрани додата крв или није, што може имати велики практични значај у клиничкој примени колагенских мембрана. 

Кључне ријечи: колагенске мембране, имплантација, одговор ткива, крв 
