Међународни научни скуп Савремени материјали –  Бања Лука.

International Scientific Conference Contemporary Materials – Banja Luka 

ДЕФИНИСАЊЕ БРОНЗАНЕ СТРУКТУРЕ ПРЕКО ФРАКТАЛНЕ ДИМЕНЗИЈЕ
Марина Симовић Павловић,1 Тијана Максимовић, 2 Јелена Максимовић, 3 Александра Радуловић, 4 Дарко Јанковић 5 и Маја Пањако6
[image: image1.emf]1 Nanophotonics Lab, Photonics Center, Institute of Physics, University
of Belgrade, Pregrevica 118, 11080 Belgrade, Serbia,
 simovicmarina99@gmail.com 

2University of Kragujevac, Faculty of science, Radoja Domanovića 12, Kragujevac, Serbia, tijana.maksimovic@pmf.kg.ac.rs 

3University of Belgrade, Faculty of physical chemistry, Studentski trg 12-16, Belgrade, Serbia, jelena.maksimovic@ffh.bg.ac.rs
4University of Belgrade, Institute of General and Physical Chemistry, Studentski trg 12/V, Belgrade, Serbia, aradulovic@iofh.bg.ac.rs 

5University of Defence, Military Academy, Veljka Lukića Kurjaka 33, Belgrade, Republic of Serbia, darkoojanko@gmail.com
6University of Belgrade, Institute of Chemistry, Technology and Metallurgy, Njegoseva 12, Belgrade, Serbia, maja.pagnacco@nanosys.ihtm.bg.ac.rs 

Сажетак: Представљено истраживање се бави слојевитим структурама које се називају Фосфат Волфрамове бронзе. То су материјали који садрже пентагоналне и хексагоналне тунеле у својој структури. Ово су уредно уређене структуре и посебно су интересантне због својих различитих хемијских, оптичких, електричних и механичких својстава. У овом раду су представљени резултати фракталне анализе рађене за наведене структуре. Ово је веома важно за дефинисање узорка испитиваних материјала, посебно понављања узорака унутар структуре.
Кључне ријечи: Бронза, Фрактална димензија, Структура материјала
DEFINING THE BRONZE STRUCTURE THROUGH THE FRACTAL DIMENSION
Abstract: The investigation of layered structures named Phosphate tungsten bronzes (PWBs) was done. Those are materials with pentagonal and hexagonal tunnels. These orderly-arranged structures are interesting for numerous applicаtions due to their different chemical, optical, electrical and mechanical features. Here, the results of fractal analysis of those structures were presented. This is important for defining the patterning in PWBs structures as well repeating these paterns whithin the structure.
Keywords: PWBs, Fractal dimension, Material structure

