Међународни научни скуп Савремени материјали –  Бања Лука.

International Scientific Conference Contemporary Materials – Banja Luka 

СТАТИСТИЧКА АНАЛИЗА ИНХИБИТОРСКОГ ДЕЈСТВА ЕКСТРАКТА МАЈЧИНЕ ДУШИЦЕ НА КОРОЗИЈУ ЧЕЛИКА У 3% РАСТВОРУ NaCl
Н. Васиљевић1, M. Митровић1, R. Fuchs-Godec2, Б. Горанчић1, М. Томић,1,3
[image: image1.emf] 1Универзитет у Источном Сарајеву, Технолошки факултет Зворник, 75400 Зворник, Република Српска, e-mail: nebojsa.vasiljevic@tfzv.ues.rs.ba, 
2Универзитет у Марибору, Факултет за хемију и хемијско инжењерство, 2000 Марибор, Словенија,
3Инжењерска академија Србије, Одељење за технологију и металургију, 11000 Београд, Србија
Сажетак: У овом раду испитивано је инхибиторско дејство екстракта мајчине душице на корозију две врсте челика у 3% раствору NaCl. Узорци челика потапани су у 3% раствор NaCl без инхибитора и растворе са 0,5, 1,0 i 1,5 g/L инхибитора (екстракта мајчине душице), а времена излагања корозиној средини била су 2, 4, 6, 8, 24, 48 и 168 часова. За оптимизацију и обраду експериментално добијених резултата кориштен је софтвер МINITAB 21, а анализирани параметри били су брзина корозије (Km-), дубински показатељ корозије (π) и ефикасност инхибитора (z). Установљено је да примјена инхибитора значајно смањује брзину корозије и повећава ефикасност заштите, а највиша ефикасност (z > 85 %) је при концентрацији инхибитора 1,5 g/L након 48 и 168 сати. Челик 2 је показао већу отпорност у одсуству инхибитора, док је додатак инхибитора значајно смањио брзину корозије код оба челика. 
Кључне ријечи: екстракт мајчине душице, зелени инхибитори, корозија челика, раствор NaCl, статистичка анализа.
STATISTICAL ANALYSIS OF THE INHIBITORY EFFECT OF THYME EXTRACT ON STEEL CORROSION IN A 3% NaCl SOLUTION
N. Vasiljević1, M. Mitrović1, R. Fuchs-Godec2, B. Gorančić1, M. Tomić1,3
 1University of East Sarajevo, Faculty of Technology, 75400 Zvornik, Republic of Srpska, e-mail: nebojsa.vasiljevic@tfzv.ues.rs.ba, 
2University of Maribor, Faculty of Chemistry and Chemical Engineering, 2000 Maribor, Slovenia,
3Engineering Academy of Serbia, Department of Technology and Metallurgy, 11000 Belgrade, Serbia 
 Abstract: In this paper, the inhibitory effect of thyme extract on the corrosion of two types of steel in 3% NaCl solution was investigated. Steel samples were immersed in 3% NaCl solution without inhibitor and solutions with 0.5, 1.0 and 1.5 g/L inhibitor (thyme extract), and the exposure times to the corrosive environment were 2, 4, 6, 8, 24, 48 and 168 hours. MINITAB 21 software was used to optimize and process the experimentally obtained results, and the analyzed parameters were corrosion rate (Km-), corrosion depth index (π) and inhibitor efficiency (z). It was found that the use of inhibitors significantly reduces the corrosion rate and increases the protection efficiency, and the highest efficiency (z>85%) is at an inhibitor concentration of 1.5 g/L after 48 and 168 hours. Steel 2 showed higher resistance in the absence of inhibitors, while the addition of inhibitors significantly reduced the corrosion rate of both steels.
Keywords: green inhibitors, NaCl solution, statistical analysis, steel corrosion, thyme extract.

