A study on the zeta potential of goethite, quartz and clay minerals depending on pH and the presence of inorganic dispersants

Ljiljana Tankosić1, Svjetlana Sredić1

Univerzitet u Banjoj Luci, Rudarski fakultet, Aleja kozarskog odreda 1, 79101 Prijedor1

Abstract

The knowledge of zeta potential is a very useful indicator of the stability of dispersed systems. This is especially important in many industrial processes, such as e.g. mineral processing, purification of water and many others. This article deals with the investigation of the electrokinetic behavior of goethite, quartz and clay minerals depending on pH and the presence of inorganic dispersants: sodiumhexamethaphosphate (SHMP), sodiumpyrophosphate (SPP) and sodium silicate (NS). All studies are conducted on natural samples, taken from Omarska iron mine (Bosnia and Herzegovina) by measuring the zeta potential. From the experimental results, it was found that the increase of the suspension pH resulted in an increase in the negative charge of all three tested samples. The clay did not show any isoelectric point (IEP). Quartz showed isoelectric points at pH about 2.6 and close to 2 in the absence and presence of sodium silicate in suspensions, respectively. Goethite showed isoelectric points at pH 6.7 and 4.95 in the absence and presence of sodium silicate in suspensions, respectively. An IEP could not be detected when the SHMP and SPP were used and the surface charge is negative from pH 2 to pH 12 in all tested samples. The addition of SHMP provided the highest negative zeta potential, i.e. the most stable dispersion, in all three tested samples.

Keywords: zeta potential, isoelectric point, goethite, quartz, clay, inorganic dispersants

Ispitivanje zeta potencijala mineral getita, kvarca i gline u zavisnosti od pH vrijednosti u prisustvu neorganiskih disperzanata

Apstrakt

Познавање зета потенцијала је веома користан индикатор стабилности дисперзних система. Ово је посебно важно у многим индустријским процесима, као што су нпр. Припрема минералних сировина, пречишћавање воде и многи други. Овај рад се бави истраживањем електрокинетичког понашања миерала гетита, кварца и глине у зависности од pH вриједности и присуства неорганских дисперзаната: натријум-хексаметафосфата (SHMP), натријум-пирофосфата (SPP) и натријум-силиката (NS). Сва истраживања су спроведена на природним узорцима, узетим из рудника руде гвожђа Омарска (Босна и Херцеговина) мјерењем зета потенцијала. Из експерименталних резултата утврђено је да повећање pH вредности суспензије доводи до повећања негативног наелектрисања сва три тестирана узорка. Глина није показала никакву изоелектричну тачку (IEP). Кварц је показао изоелектричне тачке на pH вредности око 2,6 и близу 2 у одсуству и присуству натријум-силиката у суспензијама, респективно. Гетит је показао изоелектричне тачке на pH вредности 6,7 и 4,95 у одсуству и присуству натријум-силиката у суспензијама, респективно. ИЕП није могао бити детектован када су коришћени SHMP и SPP, а површинско наелектрисање је негативно од pH 2 до pH 12 у свим тестираним узорцима. Додавање SHMP је обезбедило највећи негативни зета потенцијал, тј. најстабилнију дисперзију, у сва три тестирана узорка.

Кључне ријечи: зета потенцијал, изоелектрична тачка, гетит, кварц, глина, неоргански дисперзанти