PAGE  

MODELING OF SELF-HEALING MATERIALS USING NANOCONTAINERS
N. Filipovic1,2, D. Petrovic1,2, M. Obradovic1,2, A. Jovanovic3, S. Jovanovic3, D. Balos3 and M. Kojic2,4 
1Faculty of Mechanical Engineering, University of Kragujevac, Serbia
e-mail: fica@kg.ac.rs
2Research and Development Center for Bioengineering, BioIRC, Kragujevac, Serbia

e-mail: racanac@kg.ac.rs
3Risk-technologies, GmbH, Stuttgart, Germany

e-mail: jovanovic@risk-technologies.com
4Methodist Hospital Research Institute, Houston, USA

e-mail: mkojic@hsph.harvard.edu
Abstract. The surface defects of the material are difficult to detect and difficult to repair. A grand challenge in materials science is to design „smart“ synthetic system that can re-establishing the continuity and integrity of the damaged area. Recent research of the nanocontainers with process of self-healing materials promises a good avenue for new smart nanocoating interfaces. We use two different modeling approaches, discrete and continuum, to investigate coating substrates that contain nanoscale defects with healing agents. The discrete modeling uses the Dissipative Particle Dynamics (DPD) method with usual three forces: repulsive, dissipative and random forces, as well as additional forces which bound healing agents to metal substrate. The continuum modeling uses Finite Element Method (FEM) with different diffusivity and fluxes. The initial results show how much percentage of the inhibitors in the nanocontainers are necessary to protect the metal surface which is treated with these healing agents. Further application of modeling coupled with data mining technology could help faster development of new active multi-level protective systems for future materials.
Keywords: self-healing material process, dissipative particle dynamics (DPD), finite elеment methods (FEM), nanocoating
МОДЕЛИРАЊЕ САМОВЕЗУЈУЋИХ МАТЕРИЈАЛА КОРИШЋЕЊЕМ НАНОКОНТEЈНЕРА
Сажетак. Површинске дефекте у материјалу је тешко открити и санирати. Велики изазов у науци о материјалима је дизајн „паметних“ синтетичких система који могу да поново изграде континуитет и интегритет оштећене области. Недавна истраживања наноконтејнера са процесом самовезивања материјала обећавају нови пут за нове паметне нанопокривајуће заштите. Користимо две методе, дискретно и континуално моделирање, за истраживање покривања површина са самовезујућим материјалима које садрже оштећења на нивоу наноскале. Дискретна метода овде употребљена је „дискретна честична динамика“ у којој су коришћене уобичајене три силе: одбојна, вискозна и случајна, као и додатна сила везивања за металну површину. Континуум метода је метод коначних елемената са различитом дифузијом и флуксевима. Резултати показују колико је инхибитора у процентима потребно да буде у оквиру наноконтејнера да би могло доћи до потпуног покривања металне површине са овом методом самовезивања. Будућа примена моделирања ће укључити и data mining технологију која може убрзати развој нових вишеслојних заштитиних система за материјале у будућности.
Кључне речи: Самовезивни процеси у материјалу, дискретна честична динамика, метод коначних елемената, нанопокривање

1. Introduction

Corrosion degradation of materials and structures is one of important issues that lead to depreciation of investment goods. Two main approaches, an active and a passive one, are currently used for corrosion protection. The passive corrosion protection is achieved by deposition of а barrier layer preventing contact of the material with the corrosive environment [1].
Small size defects can appear on a material surface. Such defects have a substantial effect on the mechanical properties of material. To protect this material failure the coating systems are employed on a wide range of engineering structures, from cars to aircrafts, from chemical factories to household equipment. The “self-healing” or “inhibition” are a relatively new terms in material science which means a self-recovery of initial properties of the material after destructive actions of external environment. It is an urgent demand for industrial applications to initiate development of an active healing mechanism for polymer coatings and adhesives [2].
In this study we presented two different modeling approaches, DPD and FEM for self-healing materials. We begin by describing the details of the nanocontainers healing concept, DPD and FEM methodology. We then discuss the effect of varying the nanocontainers fillings, particle-particle interactions, diffusivity parameter and the localization of the particles into the scratch. These findings provide guidelines for formulating nanocomposite coatings that effectively heal the surfaces through the self-assembly of the particles into the defects. 
2. Methods

2.1 Nanocontainers healing concept

The initial process of nanocontainer breaking starts at а random position where a crack occurred. The nanocontainer membrane is approximated by one layer of particles and particles inside the nanocontainers represent healing agents – inhibitors. We consider that nanocontainers are fixed in the coating layer (pretreatment or primer layer) as can be seen in Fig. 1.
[image: image1.png]Corrosion protection investigated on artificial crack
(DIN EN ISO 11997-1; cycle B) in Mankiewicz Gebr. & Co.
industrial partner in MUST

Pretreatment

Metallic
substrate





Figure 1. Model with nanocontainers in primer layer

Nanocontainers release the “self – healing” agent particles which are filling the space inside a crack in order to bond it and to protect crack from further propagation. We modeled a process of self-healing using DPD method with additional spring force and surface wetting to attach healing agent particles to the damaged metal surface. The continuum model used the process of convective-diffusion for inhibitors binding to the substrate surface.
2.2 DPD Model
The coating layer with nanoscopic scratch can be modeled using molecular dynamics [2]. Another approach to this problem is a mesoscoping modeling using the DPD method [3], [4].  Motion of each DPD particle (further called “particle”) is described by the following Newton law equation: 


[image: image2.wmf](

)

i

ext

CDR

ijijij

ii

j

m

+++

=

å

FFF

vF

&


(1)

where 
[image: image3.wmf]i

m

 is the mass of particle “i”; 
[image: image4.wmf]i

v

&

 is the particle acceleration as the time derivative of velocity; 
[image: image5.wmf]C

ij

F

, 
[image: image6.wmf]D

ij

F

, and 
[image: image7.wmf]R

ij

F

 are the conservative (repulsive), dissipative and random (Brownian) interaction forces, that particle “j” exerts on particle “i”, respectively, provided that particle “j” is within the radius of influence 
[image: image8.wmf]c

r

 of particle “i”; and 
[image: image9.wmf]ext

i

F

 is the external force exerted on particle “i”, which usually represents gradient of pressure or gravity force as a driving force for the fluid domain [5]. The total interaction force 
[image: image10.wmf]ij

F

 (Fig. 2) between the two particles is 


[image: image11.wmf]CDR

ijijijij

=++

FFFF


(2)
[image: image12.jpg]oleleotelelele e e oo

ative

Disip

F;

j

Conservative
ij +

=F;




Figure 2. Interaction forces in the DPD method

The component forces can be expressed as [6]


[image: image13.wmf](

)

0

0

0

1

C

ij

ijij

j

c

D

ijij

ijDij

R

ijRij

j

r

r

a

i

w

w

i

g

sx

æö

-

ç÷

èø

×

=

=-

=

ve

Fr

Fr

Fr


(3)

In equation (3), aij is the maximum repulsion force per unit mass, rij is the distance between particles i and j, 
[image: image14.wmf]0

ij

ij

ij

r

=

r

r

 is the unit vector pointing in direction from j to i,   stands for the friction coefficient,  and σ is the amplitude of the random force. Also,  
[image: image15.wmf]D

w

 and 
[image: image16.wmf]R

w

 are the weight functions for dissipative and random forces, dependent on the distance r from the particle i; and ij is a random number with zero mean and unit variance. The interaction force is equal to zero outside the domain of influence, rc (cut radius), hence 
[image: image17.wmf]0

ij

F

=

 for rij>rc. 
Further, in order that a DPD fluid system possess a Gibbs–Boltzmann equilibrium state, the following relation between the amplitudes of the weight functions of dissipative and random forces, 
[image: image18.wmf]D

w

 and 
[image: image19.wmf]R

w

, must hold: 


[image: image20.wmf]2

DR

ww

=


(4)

Also the amplitude of the random force σ is related to the absolute temperature T,


[image: image21.wmf](

)

1/2

2

B

kT

sg

=


(5)
where 
[image: image22.wmf]B

k

is the Boltzmann constant. The weight functions can be expressed in a form given as [5]


[image: image23.wmf]2

1

ij

D

c

r

r

w

æö

-

ç÷

èø

=

,   
[image: image24.wmf]1

ij

R

c

r

r

w

=-


(6)
The particles used in this study represent both inhibition agents and surrounding coating material with different material characteristics. This was achieved by taking into account different repulsion force coefficient aij. The additional interaction forces between particles of inhibition agents, which are placed in the primer layer and metal substrate particles, are added similarly as it was done in a model of thrombosis in [7], [8].  These attractive forces are expressed as


[image: image25.wmf]max

1

sf

asf

sf

L

L

Fk

æö

ç÷

-

ç÷

èø

=


(7)

where Lsf is the distance of the inhibition particle from the substrate, ksf is the effective spring constant, and 
[image: image26.wmf]max

sf

L

 is the maximum length of inhibition particle attractive domain.
2.3 FEM model
The mass transport process for inhibition system of coating is governed by convection-diffusion equation,



[image: image27.wmf]222

222

wall

xyz

ccccccc

vvvDq

txyz

xyz

æö

¶¶¶¶¶¶¶

+++=+++

ç÷

¶¶¶¶

¶¶¶

èø


(8)

where c denotes the concentration of inhibitors; 
[image: image28.wmf]x

v

,
[image: image29.wmf]y

v

 and 
[image: image30.wmf]z

v

 are the velocity components in the coordinate system x,y,z; and D is the diffusion coefficient, assumed to be constant, of the transported material; and qwall is flux of the binding process for inhibitors which adhere on the substrate surface. Similar concept is using for calculation of the volume of inhibitors which are possible to diffuse on the scratch surface. Diffusivity coefficient and wall binding flux are the fitting parameters in FEM model. The drawback of continuum approach is that particle-particle interaction cannot be modeled but benefit is that a large substrate area is possible to be modeled.
3. Results
3.1 DPD model results
The primer layer is represented by green particles, while inhibitors are shown as red particles (see Fig. 3). The material is scratched and it should be protected; the scratched domain is represented by grey particles. Water which enters into the scratch is modeled by surrounding light blue particles. 
[image: image31.jpg]Scratch ()

Primer with Inhibitors (@)

HE
S
S
ST i T
o ﬁm HES ﬁm
BHiEHEHE R R R r
S

: S
HESS
HE
R R
i R
S
SRR R L SR p ]
R R R R n
i m i i
i G
o E

Inhibitors (@)



 
Figure 3. Model of material protection using inhibitors in the primer layer
A graphic interface for modeling by DPD method, with input parameters that can be changed using dialog window, is shown in Fig. 4.
[image: image32.png]efficient 2:

Ext. for . ntainers (%

Division U: 2 i o ainer diameter (um}: O Number of calculations

th (urm): i thickness (um):

jht (um) 0 o t (um)





Figure 4. Dialog of the input parameters interface for a DPD modeling. DeltaT is  time step for DPD simulation; Ext. force is the external force which acts in Y direction on all particles to produce motion; Division U is the total number of particles in X direction at initial time; Division V is the total number of particles in Y direction at initial time; Gamma is the viscosity friction coefficient used in DPD equations; Step average is the total number of steps for writing results for animation; Total steps is the total number of time steps for the entire modeling period; Rep. force. coefficient is the repulsive force coefficient used for repulsive force for simple DPD particles; Rep. force. coeff. 2 is the repulsive force coefficient used for the repulsive force between inhibition particles; Include random force checking button is used for including/excluding random force in a DPD calculation; Density of Nanocontainers means percent of inhibition particles in the primer layer; Calculation button starts the program execution; Run/Stop animation button is used for start/stop animation which is obtained from the DPD calculated results.

The external force is assumed to act on all particles. User can specify a DPD domain by defining a number of particles in X and Y directions. The basic material DPD constants: viscosity friction and repulsive force coefficient, are also prescribed. An additional repulsive force coefficient is given for inhibition particles in order to keep them close and direct them into the surrounding structural matrix which contains simple DPD particles, like primer and scratch particles.  
Geometrical parameters of the model are marked in Fig. 1. A scaled model was used for simulation due to a large number of particles in the real model.
[image: image33.png]il Cut = Layout ~ f} Text Direction E (@) Shape Fil ing
£ cut JJU t =l 4 Text Diecti BN NOOO qﬁ hape Fill A Fina
Copy BReset — Align T ALLDE G - "4 7 Shape Outline - || 85, Replace ~
P53 Fomat pinter || e sDeiete || B2 U abe & & Aa|[A Converttosmatart - || % AL 3 A= A B ) ropeeireas « || 3 selet~
e RESULIS ]
| resurs

Scratch width: 0.1 mm  Concentration of NCs: 10 %

Diameter of NCs : 100 nm

| Rresuurs

RESULTS

Metal substrate





Figure 5. Initial state and dimensions of a real model
In a process of primer protection when the scratch occurred, the inhibitors in the primer layer start to interact with the surrounding particles and slip through the scratch on the metal substrate. For pure protection of metal substrate it is necessary to cover surface with one layer of inhibitors whose diameter is about 1nm. During the process of protection, inhibitor particles interact with primer and fluid particles, but with different repulsive force coefficient (“Rep. force coefficient” and “Rep. force coefficient 2”, Fig. 4). Additional spring force was used (equation 7) to connect inhibition with metal substrate particles, so that the inhibitors particles are attached to the walls of the crack. 
The first DPD model, with inhibitors in the primer layer, consists of a 2D rectangle crack domain with depth of 0.1 mm. Total number of DPD particles was 24 000 (240x100) and the model is scaled four times. The total number of time steps for simulation was 100 000.
[image: image34.jpg]



Figure 6. The DPD model after 100 000 time steps (200s). Red particles represent the inhibition particles, green particles make primer layer, grey particles (substrate) are considered to be fixed in space domain. The surrounding particles are shown with light blue color and represent the fluid

A real scenario of realizing inhibition agents is to assume particle motion inside the crack domain and some surrounded area. 
We investigated substrate surface coverage and number of inhibitors in the primer needed to protect damaged material and repair it completely.
We tested metal coverage with different percent of inhibitors in the primer: 10%, 15% and 20%. The computed results for the current number of inhibitors in the crack and percentage of covered damaged surface after 200s are given in Fig. 7 and Fig. 8.

[image: image35.png]Current Number of Inhibitors in

Crack

Current Number of Inhibitors vs. 11me

—20%
——15%

——10%

50 100 150 200 250

Time (s)




Figure 7. Increase of number of inhibitors on the metal surface during time period obtained by a simple 2D analysis, for three percentage values of inhibitors in the primer: 10%, 15% and 20%. Total time steps for DPD calculation was 100 000

[image: image36.png]W 9~ e Petrovic et al [Compatibility Mode] - Microsoft Word
N T T
- HArna -
B Times NewRom =10~ AT & BT gaBhcel AaBb( AsBbCel [1] Amic AaBbCel ASM:DE AdBbCDe AdBHCeDE AwBbOeT AaBb( AsBeCel ianscel dapice damscel | PA cepince
P omatronter B 4 U e %, X - [v || Emphasis Headingl TNommal TSt-Ref  Strong  Stylel-A. TStylel-.. Stylel-Sh Sobttle  THe  TNoSpac. SwieEm.. ntemsef. Quote |- Change :mm,
Cipboara Font syes ating
| P i Fm— = - T — = fon T w 3 3 &
[l Figure 7. Increase of number of inhibitors on the metal surface during time period obtained by a simple 2D
analysis. Total time steps for DPD calculation was 100 000
Percent of Covered Surface vs.
N 140
P
s
& 10
] & 100
1
s 80
< 5
g 60
2z
EC w
el 20
€l
<
e 0
N z 0 50 100 150 200 250 E
4 )
[ Time (s)
Figure 8. Percentage of inhibitors particles on the metal surface during time period
For the second model, with nanocontainers in the primer layer, we also used a scaled
model, shown in Fig. 9.
W )
Page:7 0f9 | Words: 2125 | English (US) | P | EEE 0—@)

PP Comranie. | oo i) | 5




Figure 8. Percentage of inhibitors particles on the metal surface during time period, for three percentage values of inhibitors in the primer: 10%, 15% and 20%.
For the second DPD model, with nanocontainers in the primer layer, we also used a scaled model, shown in Fig. 9.
[image: image37.png]X

e
PRIILAY A L




Figure 9. Scaled model with nanocontainers in the primer layer

In the second model we investigated number of nanocontainers which are necessary to completely cover a certain specified surface, and the volume percentage of inhibitors in the nanocontainers. The production of nanocontainers and inhibitors is too expensive and it is needed to precisely establish minimum percentage of inhibitors in the nanocontainers for full protection of the treated material.
3.2 FEM results

The continuum model consists of mesh size of 30x30,000 = 900,000 3D finite elements where inhibitors are randomly prescribed as the influx boundary conditions. The scratch dimension is 0.1x100 mm, the primer layer is 4000 nm, nanocontainer diameter is 400 nm. The percentage of inhibitor inside nanocontainers is 20% and the percentage of nanocontainers in the primer or pre-treatment layers is 10%. The convection velocity is assumed to be zero due to dominant diffusion process. The binding flux was prescribed to be unit which depends on mechanical property of scratch, with no water inclusion on the surface. Computed results during time period of 20h of inhibition process are shown in Fig. 10. It can be seen that almost full 100% coverage is achieved for 10h.
[image: image38.jpg]120

100 -

[9%)] @bejUSDIad Bular0D

12 14 16 18 20 22

Time [h]

10




Figure 10. Cover percentage of the inhibitors on the substrate surface during time (FEM model).
Distribution of inhibitors on the scratch surface for time = 6h is presented in Fig. 11. The inhibitors fluxes are randomly distributed along the plate, which cause higher coverage near these plate sides. 
[image: image39.png]Contour plot. Nodal Temperature
Deformed (Scale factor=1)

1.56e+00

1.488+00

1.308+00

1.298+00

1188400

1.008+00

9.945-01

8.945-01

7.958-01

6.965-01

5.968-01

497601

398801

298801

1.998-01

9.948-02

0.008+00




Figure 11. Distribution of inhibitors on the scratch surface for t=6h. The width of the scratch is 0.1mm and the length is 100mm.
Space and time distribution of inhibitors on the scratch surface is shown in Fig. 12. 
[image: image40.jpg]I





Figure 12. Space and time distribution of inhibitors on the scratch surface. The width of the scratch is 0.1mm and the length is 100mm.
4. Conclusions
In this study we used DPD and FE computer modeling methods to provide guidelines for designing self-healing systems. Our study has been shown that it was sufficient to have 20% inhibitors in the primer layer with 10% of nanocontainers to completely protect the damaged material. Time for coverage can be fitted by employing real experimental data. By changing the input parameters it was possible to reduce this percentage, but not significantly. With these two methodologies we created new hybrid modeling methods that integrate fluid dynamics, structural mechanics, chemical reactivity, and phase transitions. 
Future work will include design of multiple nanocontainers with assumed “density” in the given regions. We also will analyze a coupling of this modeling and a data mining technology, which could help faster development of new active multi-level protective systems for future industrial materials. Progress in this field can greatly facilitate fabrication of the next generation of adaptive materials which can self-heal themselves before any catastrophic failure can occur.
Acknowledgement. This research was supported by Ministry of Science in Serbia, ON174028, III41007 and FP7 MUST project NMP3-LA-2008-214261.

References 

[1] Zheludkevich ML, Shchukin DG, Yasakau KA, Mohwald K, and Ferreira MGS, Anticorrosion Coatings with Self-Healing Effect Based on Nanocontainers Impregnated with Corrosion Inhibitor, Chem. Mater. 2007, 19, 402-411.
[2] Tyagi S, Lee J Y, Buxton G A, Balazs C A (2004) Using Nanocomposite Coatings To Heal Surface Defects, Macromolecules, 37, pp. 9160-9168.

Filipovic N, Ravnic D J, Kojic M, Mentzer S J, Haber S, Tsuda A (2008b) Interactions of Blood Cell Constituents: Experimental investigation and Computational Modeling by Discrete Particle Dynamics Algorithm, Microvascular Research, 75, pp. 279-284.

[3] Groot R D and Warren P B (1997) Dissipative particle dynamics: Bridging the gap between atomistic and mesoscopic simulation, J. Chem. Phys., 107(11), pp. 4423-4435.

[4] Boryczko K, Dzwinel W, Yuen D (2003) Dynamical clustering of red blood cells in capillary vessels, J. Mol . Model, 9, pp. 16-33.

[5] Filipovic N, Kojic M, Tsuda A (2008a) Мodeling thrombosis using dissipative particle dynamics method, Phil Trans Royal, 366, pp. 3265-3279.
[6] Hoogerbrugge P J and Koelman J M V A (1992) Simulating microscopic hydrodynamic phenomena with dissipative particle dynamics, Europhys. Lett., 19, pp. 155-160.

[7] Jovanovic A and Filipovic N (2006) Innovative modelling methods in damage assessment: application of dissipative particle dynamics to simulation of damage and self-healing of polymer coated surfaces, J. Theoretical and Applied Mechanics, 44, pp. 637-648. 

PAGE  
2

_1366093580.unknown

_1367066760.unknown

_1367066802.unknown

_1367066823.unknown

_1367066867.unknown

_1367070013.unknown

_1368179140.unknown

_1367066928.unknown

_1367066843.unknown

_1367066815.unknown

_1367066784.unknown

_1367066791.unknown

_1367066776.unknown

_1367066570.unknown

_1367066705.unknown

_1366095132.unknown

_1367066265.unknown

_1366095120.unknown

_1366093576.unknown

_1366093578.unknown

_1366093579.unknown

_1366093577.unknown

_1366093574.unknown

_1366093575.unknown

_1256726106.unknown

_1366093573.unknown

_1256726108.unknown

_1256726104.unknown

