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Сажетак: У овом раду наночестице хематита (α-Fe2O3) коцкастог и заобљеног облика синтетизоване су хидротермалном синтезом, уз варијациjу односа водe и етанола. Облик честица директно утиче на физичко-хемијске особине, магнетно понашање и оптичка својства. Морфологија и величина синтетизованих наночестица су проучаване помоћу скенирајуће електронске микроскопије (SEM) и трансмисионе електронске микроскопије (TEM). Магнетна својства наночестица хематита су испитивана у широком температурном опсегу (50-300 K) и под различитим примењеним магнетним пољима (до 3 T) коришћењем магнетометра са вибрирајућим узорком. Квадратне наночестице показују ултра-ниску јачину коерцитивног поља  (HC=21 Oe) због равних површина са минималним бројем дефеката, док заобљене хематитне наночестице показују већу јачину коерцитивног поља (HC=306 Oe) због закривљених површина богатих дефектима и атомским неуређеностима. Разумевање зависности магнетних својстава  од облика наночестица хематита од великог је значаја за унапређење њихових биомедицинских и нанотехнолошких примена. Уз ниску цитотоксичност и високу биокомпатибилност синтетизоване честице обећавају значајан потенцијал  у развоју магнетних наноуређаја и биомедицинској примени. 
Abstract:  In this study hematite nanoparticles (α-Fe2O3) of cube-like and rounded shape were synthesized via hydrothermal synthesis method by varying ethanol/water ratios. Particle shape directly influences physicochemical properties, magnetic behavior, and optical properties. The morphology and particle sizes of the synthesized samples were observed by scanning electron microscopy (SEM) and transmission electron microscopy (TEM). The magnetic properties of the hematite nanoparticles were investigated across a broad temperature range (50–300 K) and under various applied magnetic fields (up to 3 T) utilizing a vibrating-sample magnetometer. Cube-like hematite nanoparticles display ultra-low coercivity (HC = 21 Oe) due to defect-minimized planar surfaces, whereas rounded hematite nanoparticles exhibit higher coercivity (HC = 306 Oe) due to defect-rich curved surfaces and atomic misalignments. Understanding the shape-dependent magnetic properties of hematite (α-Fe2O3) nanoparticles is essential for advancing their biomedical and nanotechnological applications. With low cytotoxicity and high biocompatibility, the synthesized hematite nanoparticles show promise for magnetic nanodevice development and biomedical applications. 
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