ИН ВИТРО ЕВАЛУАЦИЈА СОРПЦИЈЕ И РАСТВОРЉИВОСТИ ТРИ ДЕНТАЛНА МАТРИЈАЛА

Рената Јосиповић1, Ирена Кузмановић Радман1, Тијана Адамовић1, Адриана Арбутина1, Марија Обрадовић1, Маријана Араповић Савић1, Мирјана Умићевић Давидовић1, Огњенка Јанковић1, Маријана Поповић Бајић2, Владан Мирјанић1

1Медицински факултет, Студијски програм Дентална медицина, Бања Лука, БиХ, Република Српска

2Стоматолошки факултет, Клиника за болести зуба, Београд, Србија

Сажетак: Увод: Растворљивост и сорпција су особине материјала које директно могу утицати на њихову стабилност, интегритет и трајност на мјесту апликације. Циљ: Циљ овог рада је да се испита растворљивост и сорпција новосинтетисаног наноматеријала на бази калцијум-алумината, калцијум-силиката и MTA. Материјал и методе рада: У истраживању је коришћен наноструктурни калцијум-алуминат синтетисан хидротермалном сол-гел методом од појединачних компонената калцијум-алумината (CaO·Al2O3), калцита (CaCO3) и баријум-сулфата (BaSO4) као рендгенског контрастног средства, и материјал на бази калцијум-силиката. Замијешани материјал је постављен у пластичне калупе пречника 5 ± 0,1 mm и висине 2 ± 0,1 mm. Након везивања, материјали су остављени у инкубатору на 37 °C током 24 h, а потом су извађени из калупа и анализирана је сорпција течности материјала. За сваки испитивани материјал направљено је по 8 узорака (n = 8). Као контролни материјал коришћен је MTA (Angelus, Londrina, Бразил). Резултати: Током 28 дана складиштења узорака у дестилованој и дејонизованој води, сорпција течности за MTA износила је 12,71%, сорпција за калцијум-силикате износила је 12,08%, док је за калцијум-алуминате забиљежена сорпција течности од 20,27%. Примјеном Студентовог т-теста уочена је разлика између калцијум-алумината и MTA (t = -7,094; p = 0,000005) и између калцијум-алумината и калцијум-силиката (t = -7,026; p = 0,000006), док између калцијум-силиката и MTA разлика није била статистички значајна. Растворљивост код MTA износила је 8,53%, растворљивост код калцијум-силиката 8,3%, док је код калцијум-алумината забиљежена растворљивост од 23,68%. Значајна разлика је забиљежена између калцијум-алумината и MTA (t = 4,828; p = 0,001308) и између калцијум-алумината и калцијум-силиката (t = 4,817; p = 0,000951), док између калцијум-силиката и MTA разлика није била статистички значајна. Закључак: Растворљивост материјала и апсорпција течности код наноструктурног материјала на бази калцијум-алумината била је значајно већа у поређењу са калцијум-силикатом и MTA.

Кључне ријечи: растворљивост; сорпција; калцијум-алуминат; калцијум-силикат; MTA; наноматеријали.

IN VITRO EVALUATION OF WATER SORPTION AND SOLUBILITY OF THREE DENTAL MATERIALS

Renata Josipovic1, Irena Kuzmanovic Radman1, Tijana Adamovic1, Adriana Arbutina1, Marija Obradovic1, Marijana Arapovic Savic1, Mirjana Umicevic Davidovic1, Ognjenka Janković1, Marijana Popovic Bajic2, Vladan Mirjanic1

1Faculty of Medicine, Study Programme of Dental Medicine, Banja Luka, Bosnia and Herzegovina, Republic of Srpska

2Faculty of Dentistry, Clinic for Dental Diseases, Belgrade, Serbia

Abstract: Introduction: Solubility and sorption are material properties that can directly affect their stability, integrity, and durability at the site of application. Aim: The aim of this study was to examine the solubility and sorption of a newly synthesised nanomaterial based on calcium aluminate, calcium silicate, and MTA. Materials and methods: The study used a nanostructured calcium aluminate synthesised by the hydrothermal sol-gel method from individual components of calcium aluminate (CaO·Al2O3), calcite (CaCO3), and barium sulphate (BaSO4) as a radiopacifier, and a calcium silicate-based material. The mixed material was placed into plastic moulds 5 ± 0.1 mm in diameter and 2 ± 0.1 mm in height. After setting, the materials were kept in an incubator at 37°C for 24 h, after which they were removed from the moulds and liquid sorption of the materials was analysed. Eight specimens were prepared for each tested material (n = 8). MTA (Angelus, Londrina, Brazil) was used as the control material. Results: During 28 days of specimen storage in distilled and deionised water, liquid sorption for MTA was 12.71%, sorption for calcium silicate was 12.08%, while calcium aluminate showed a liquid sorption of 20.27%. Using Student's t-test, a difference was observed between calcium aluminate and MTA (t = -7.094; p = 0.000005) and between calcium aluminate and calcium silicate (t = -7.026; p = 0.000006), while the difference between calcium silicate and MTA was not statistically significant. Solubility for MTA was 8.53%, solubility for calcium silicate was 8.3%, while calcium aluminate showed a solubility of 23.68%. A significant difference was observed between calcium aluminate and MTA (t = 4.828; p = 0.001308) and between calcium aluminate and calcium silicate (t = 4.817; p = 0.000951), while the difference between calcium silicate and MTA was not statistically significant. Conclusion: The solubility and liquid absorption of the nanostructured calcium aluminate-based material were significantly higher compared with calcium silicate and MTA.

Keywords: solubility; sorption; calcium aluminate; calcium silicate; MTA; nanomaterials.