TRIBOLOŠKA SVOJSTVA AUSTEMPEROVANOG NODULARNOG LIVA KAO FUNKCIJA NJIHOVESTRUKTURE

D. Ješić1, P. Kovač2, Lj. Soos3, B. Savković2, I. Mankova4

1International technology Management Academy, Trg D.Obradovića 7, 21000 Novi Sad, e-mail: dusanjesic@hotmail.com

2University of Novi Sad, Faculty of Technical Science, Trg D.Obradovića 6, 21000 Novi Sad, Serbia, e-mail: pkovac@uns.ac.rs, savkovic@uns.ac.rs

3Institute of Production Engineering and Quality, Faculty of Mechanical Engineering, Slovak University of Technology in Bratislava, Slovakia, e-mail: lubomir.soos@stuba.sk

4Technical University of Košice, Masiarska 74, 04001 Košice, Slovakia, e-mail: ildiko.mankova@tuke.sk

Apstrakt: Tribološka svojstva austemperovanog duktilnog čelika (ADI), kao i drugih materijala, mogu se odrediti merenjem sile trenja u tribo-mehaničkim sistemima (energetski aspekt) i merenjem izabranog parametra habanja (ekonomski aspekt) na kritičnim elementima tribo-mehaničkih sistema.

Tribološka svojstva nodularnog liva (ADI) EN-GJS-500-7 i EN-GJS-700-2, koja su tretirana izotermno i klasičnim postupcima, dugo se ispituju na tribometru „Pin i Disk“. Koeficijent trenja i PQ indeks se koriste za identifikaciju triboloških svojstava nodularnog liva u kontaktu sa karbidnim čelikom.

U ovom radu je predstavljen deo eksperimentalnih rezultata o uticaju dva parametra metalurške strukture nodularnog liva EN-GJS-500-7 na njegova tribološka svojstva.

Ključne reči: nodularni liv, termička obrada, trenje, habanje.

TRIBOLOGYPROPERTIES OF AUSTEMPERED DUCTILE IRON AS FUNCTION OF THEIR STRUCTURE

D. Ješić1, P. Kovač2, Lj. Soos3, B. Savković2, I. Mankova4

1International technology Management Academy, Trg D.Obradovića 7, 21000 Novi Sad, e-mail: dusanjesic@hotmail.com

2University of Novi Sad, Faculty of Technical Science, Trg D.Obradovića 6, 21000 Novi Sad, Serbia, e-mail: pkovac@uns.ac.rs, savkovic@uns.ac.rs

3Institute of Production Engineering and Quality, Faculty of Mechanical Engineering, Slovak University of Technology in Bratislava, Slovakia, e-mail: lubomir.soos@stuba.sk

4Technical University of Košice, Masiarska 74, 04001 Košice, Slovakia, e-mail: ildiko.mankova@tuke.sk

Abstract: Tribological properties of Austempered Ductile (ADI), as well as of the other materials, can be determinated by measuringthe friction force in the tribo-mechanical systems (energetic aspect) and by measuring the chosen parameter of wear (economic aspect) on critical elements of tribo-mechanical systems.

Tribological properties of nodular cast irons (ADI) EN-GJS-500-7 and EN-GJS-700-2, that are treated isothermally and classical procedures, are investigated a long time on tribometer "Pin and Disk". The friction coefficient and PQ index are used for identification tribological properties of nodular cast irons in contact with carbide steel.

In this paper is presented a part of experimental results about influence of two parameter of metalurgical structure of nodular cast iron EN-GJS-500-7 on its tribological properties.

Keywords: nodular cast iron, heat treatment, friction, wear.